MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A06656 | In-Flight Anomaly Number -- | Contractor Report Number T-032 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title SOFI TENSILE TESTING ERRORS |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A B (X) C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE TENSION TESTOR | PART# T34K230 | SER/LOT# N/A | MANUFACTURER MMA |
| Test/Operation L - FLD | Prevailing Condtion F - FUNCTIONAL | F / U UC | Fail Mode MSI - INSULATION | Cause ETT - EI-TEST-EQUP |
| System TPS | Defect -- | Material F - INSUL | Work Contact J. GUZMAN | Fail Date 05/01/1983 |
| Received at MSFC 06/07/1983 | Date Isolated -- | FMEA Reference 1.2 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location KSC | Symptom MI - INSULATION | Time Cycle -- |
| Effectivity Text LWT-5 & SUBS |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 05/16/1990 | CN RSLV SBMT 09/15/1983 | Defer Date -- | Add Date -- | R/C Codes 3 - F/TE -- -- |
| Assignee |
| Design B. DAVIS | Chief Engineer -- | S & MA D. NEWMAN | Project G. CAVALARIS | Project MGR -- |
| Approval |
| Design B. DAVIS | Chief Engineer -- | S & MA D. NEWMAN | Project P. BRIDWELL | Project MGR -- |
| PAC Assignee M. GLASS | PAC Review Complete MG | MSFC Closure Date 10/28/1983 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: TENSILE TEST FAILURES OF SOFI, WHICH WERE INITIALLY THOUGHT TO BE DUE TO MTRL PROPERTIES, PROVED TO BE DUE TO A COMBINATION OF FACTORS IN THE TEST ITSELF. THIS HAS RESULTED IN UNNECESSARY MRB ACTION & THE EXPENDITURE OF MANHRS TO INVESTIGATE THE CAUSES OF THE TEST FAILURES (REF F/A T-57792) |
| Contractor Investigation/Resolution CAUSE - (1) TOOLS ARE INADEQUARE, (2) PERSONNEL NOT USING CORRECT TECHNQIUES. 10/5/83 - RESOLUTION - THE PROBLEM OF POOR BOND TENSION TEST VALVES DUE TO TOOLING AND TECHNIQUE DIFFICIENCIES BECAME APPARENT DURING THE INVESTIGATION INTO CPR-488 FAILURE ON LWT-8 LH2 BARRELL CELL C IN THAT CASE, FALSE READINGS OF LOW STRENGTH FOAM INDICATED THE PROBLEM WAS MUCH MORE EX- TENSIVE THAN WAS ACTUALLY THE CASE, AND COMPLICATED FAILURE ANALYSIS. RECURRENCE CONTROL: (1) TOOLING USED TO OBTAIN TEST SAMPLES MODIFIED EXTENSIVELY TO ASSURE BETTER QUALITY TEST SPECIMENS. INSPECTION OF SAMPLE CUTTERS TO ASSURE QUALITY SAMPLES ARE ANALYZED. (2) TECHNIQUE FOR USE OF TPS MEASURING EQUIPMENT ASSURED BY CLASSES FOR PERSONNEL ON PROPER USE OF EQUIPMENT. 10/4/83 - CLOSURE DISTRIBUTED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A06656 | IFA# -- | Contractor RPT# T-032 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# T34K | Asmnt Part Name TENSION TESTER | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 3 | CAUSE CD ETT - EI-TEST-EQUP | FAIL MODE MI - INSULATION |
| Asmnt FMEA N/A | Asmnt FM N/A | FMEA CSE N/A | FMEA SCSE N/A |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |