MSFC PRACA : 2003-02-12 07:54

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A00012 | In-Flight Anomaly Number -- | Contractor Report Number P-025 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title FRACTURED PYRO BOLT |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (2) B (X) C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE LRU | NOMENCLATURE GND UMB CARR PLT | PART# 82629021000-029 | SER/LOT# N/A | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE PYRO BOLT | PART# PD5000020-029 | SER/LOT# 0000018&19 | MANUFACTURER HI-SHEAR |
| Test/Operation D - DEV | Prevailing Condtion -- | F / U F | Fail Mode -- | Cause -- |
| System PROPULSION | Defect -- | Material -- | Work Contact ALOST | Fail Date 10/25/1978 |
| Received at MSFC 06/27/1979 | Date Isolated -- | FMEA Reference 2.4.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location KSC | Symptom MW - INT LEAK | Time Cycle -- |
| Effectivity Text ET-1 AND SUBS |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 10/07/1987 | CN RSLV SBMT 10/02/1979 | Defer Date -- | Add Date -- | R/C Codes 1 - DES -- -- |
| Assignee |
| Design R. ZAGRODZKY | Chief Engineer -- | S & MA D. NEWMAN | Project C. CRANE | Project MGR -- |
| Approval |
| Design R. ZAGRODZKY | Chief Engineer -- | S & MA D. NEWMAN | Project J. ODOM | Project MGR -- |
| PAC Assignee C. NEWTON | PAC Review Complete CN | MSFC Closure Date 10/26/1979 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description DURING UMBILICAL CARRIER PLATE TESTING AT KSC, THE FOLLOWING FAILURES TO PYRO BOLTS OCCURRED: 1. DURING DROP TEST NO. 1 & NO. 4, BOLT S/N 000018 & S/N 000019 SHOWED EVIDENCE OF EXHAUSTING. MARS T19402 2 SUDDEN RELEASE OF PRESSURE 30 HOURS AFTER FIRING. MARS T19534 BOLT S/N 000024. 3. BOLT S/N 000025 WAS DISCOVERED IN A STORAGE LOCKER WITH A PRESSURE CARTRIDGE ASSEMBLY SEPARATED FROM BOLT. SIMILAR CIRCUMSTANCE FOR S/N 026 & S/N 027. MARS T19534 4. DURING GH2 VENT SYSTEM DROP TEST NO. 10, S/N 000022 BROKE PREMATURELY DURING RANDOM MOTION TESTS. MARS T16945 |
| Contractor Investigation/Resolution RESOLUTION: 1. ANALYSIS OF BOLTS FOR THE BLOW-BY CONDITION RESULTED IN A DETERMINATION THAT THE BOLT/STEM "O" RING WILL BE REPLACED WITH AN OMNI SEAL AND VERIFIED BY QUAL TEST. QUALIFICATION TEST COMPLETE (CLOSED). 2. S/N 0000018 AND S/N 0000019 BOLTS ANALYZED AND DETERMINED "O" RING SEAL LEAKED. REF. MARS T19402. (CLOSED). 3. A FAILURE ANALYSIS PLAN WAS IMPLEMENTED WITH THE EXCEPTION OF FIRING NOS. 4 THRU 7 WHICH NOT NECESSARY. THE CONCLUSIONS OF THE FAILURE ANALYSIS WERE: A. A PRESSURE CARTRIDGE FAILED AS THE RESULT OF SUSTAINED FLAW GROWTH IN THE PRESENCE OF AN AGGRESSIVE ATMOSPHERE & A STATIC LOAD. THE AGGRESSIVE ATMOSPHERE IS ATTRIBUTED TO COMBUS- TION PRODUCTS & THE STATIC LOAD IS DUE TO RESIDUAL PRESSURE IN THE CARTRIDGE. B. THE MODE OF FRACTURE WAS INTERGRANULAR. C. NO EVIDENCE OF PRE-EXISTING FLAWS WAS FOUND. CRACKS APPARENTLY WERE INITIATED DURING FIRING. D. THE PRESENCE OF A SHARP RADIUS ON THE MAIN CHARGE CAVITY OF THE PRESSURE CARTRIDGE MAY HAVE CONTRIBUTED TO THE FAILURE. IN EACH OF THE 5 CARTRIDGES WHICH WERE EXAMINED, CRACKS INITIATED IN THIS RADIUS & PROPAGATED THROUGH THE WALL THICKNESS. THE RESULTS HAVE CAUSED A REDESIGN TO ELIMINATE THE STRESS RISER AND INCREASED CARTRIDGE WALL THICKNESS. IN ADDITION, PROPER HEAT TREATMENT OF THE CARTRIDGE CLARIFIED ON DRAWING. REF. ETFA-29 (CLOSED) 4. S/N 0000022 FAILURE ANALYSIS INDICATED FAILURE WAS DUE TO MOTION SIMULATOR MISALIGNMENT MARS T16945. (CLOSED) 5. S/N 0000024 INITIATORS FORWARDED TO JSC FOR FAILURE ANALYSIS. NO ABNORMAL CHARACTERISTICS NOTED. REF. MARS T19534. DESIGN CHANGE TO INSTALL ORIFICE PLATE BETWEEN CARTRIDGE AND NSI. COMPLETE. QUALIFICATION TEST IS COMPLETE |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A00012 | IFA# -- | Contractor RPT# P-025 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# -- | Asmnt Part Name -- | Asmnt Serial/Lot# -- |
| HCRIT CD -- | FCRIT CD -- | CAUSE CD -- | FAIL MODE MW - INT LEAK |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |