OFFICIAL FAA HOLDOVER TIME TABLES

WINTER 2008-2009

NOTE:  These HOT tables will be published in the FAA-Approved Deicing Program Updates for Winter 2008 – 2009 Notice.  Operators may use these tables now in their ground deicing / anti-icing programs.  The FAA does not expect to make any changes to these tables for the Winter of 2008 – 2009.

## SUMMARY OF CHANGES FROM 2007-2008

### Type I Fluids.

### The Type I fluid holdover time table values are unchanged.

### TYPE II FLUIDS.

### One new Type II fluid, Kilfrost ABC-K Plus, has been added to the list of qualified Type II fluids.  The addition of this fluid did not cause any of the values to change in the Type II generic holdover time table, Table 2. A brand specific table has been added for this new fluid (Table 2G).

The FAA and Transport Canada have been notified that there were possible viscosity issues with the Aviation Xi’an High-Tech KHF II fluid which was first commercialized for use in winter 2007-08.

### Specifically, there may still be batches of this fluid in the field that were shipped or delivered with viscosities lower than the published Lowest On-Wing Viscosity (LOWV) for use with the holdover time guidelines.

### The FAA and Transport Canada have been advised that the fluid manufacturer is taking measures to correct this situation.

It is highly recommended that operators intending to use generic or fluid-specific holdover time guidelines associated with this fluid contact the vendor for further details, and carefully assess this fluid’s on-wing viscosity at time of use.

### 3.	TYPE III FLUIDS.

The Type III fluid holdover time table values are unchanged.

### TYPE IV FLUIDS.

In the Type IV generic holdover time tables, the values were increased in the Rain on Cold Soaked Wing cells due to the removal of obsolete data.

## TABLE OF CONTENTS FOR HOT GUIDELINES

## FOR WINTER 2008-2009

TABLE	PAGE

Table 1.	FAA Guidelines for Holdover Times SAE Type I Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	5

Table 1A.	FAA Guidelines for the Application of SAE Type I Fluid Mixture Minimum Concentrations as
a Function of Outside Air Temperature.	6

Table 1B.	Snowfall Intensities as a Function of Prevailing Visibility.	7

# Table 2.	FAA Guidelines for Holdover Times SAE Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	8

Table 2A.	FAA Guidelines for Holdover Times ABAX (SPCA) ECOWING 26 Type II Fluid Mixtures
as a Function of Weather Conditions and Outside Air Temperature.	9

Table 2B.	FAA Guidelines for Holdover Times AVIATION XI’AN HI-TECH KHF-II Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	10

Table 2C.	FAA Guidelines for Holdover Times CLARIANT SAFEWING MP II 2025 ECO Type II
Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	11

Table 2D.	FAA Guidelines for Holdover Times CLARIANT SAFEWING MP II FLIGHT Type II
Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	12

Table 2E.	FAA Guidelines for Holdover Times KILFROST ABC-2000 Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	13

Table 2F.	FAA Guidelines for Holdover Times KILFROST ABC-II PLUS  Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	14

Table 2G.	FAA Guidelines for Holdover Times KILFROST ABC-K PLUS  Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	15

Table 2H.	FAA Guidelines for Holdover Times NEWAVE AEROCHEMICAL FCY-2 Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	16

Table 2I.	FAA Guidelines for Holdover Times OCTAGON E-MAX Type-II Fluid Mixtures as a
Function of Weather Conditions and Outside Air Temperature……………………………...........17

Table 3.	FAA Guidelines for Holdover Times SAE Type III Fluid Mixture as a Function of Weather Conditions and Outside Air Temperature.	18

Table 4.	FAA Guidelines for Holdover Times SAE Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	19

Table 4A.	FAA Guidelines for Holdover Times ABAX (SPCA) AD-480  Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	20

Table 4B.	FAA Guidelines for Holdover Times  CLARIANT SAFEWING MP IV 2001 Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	21

TABLE	PAGE

Table 4C.	FAA Guidelines for Holdover Times CLARIANT SAFEWING MP IV 2012 PROTECT
Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature	22

Table 4D.	FAA Guidelines for Holdover Times CLARIANT SAFEWING MP IV LAUNCH Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	23

Table 4E.	FAA Guidelines for Holdover Times DOW UCAR™ ULTRA+ ADF/AAF Type IV
Fluid as a Function of Weather Conditions and Outside Air Temperature………….……………..24

Table 4F.	FAA Guidelines for Holdover Times DOW UCAR™ ENDURANCE EG106 Type IV Fluid as a Function of Weather Conditions and Outside Air Temperature……………………………….......25

Table 4G.	FAA Guidelines for Holdover Times DOW UCAR™ FLIGHTGUARD AD-480 Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature…………………....26

Table 4H.	FAA Guidelines for Holdover Times KILFROST ABC-S Type IV Fluid Mixtures as a
Function of Weather Conditions and Outside Air Temperature………………………..…….……27

Table 4I.	FAA Guidelines for Holdover Times KILFROST ABC-S PLUS Type IV Fluid Mixtures
as a Function of Weather Conditions and Outside Air Temperature.	28

Table 4J.	FAA Guidelines for Holdover Times LYONDELL ARCTIC SHIELD™ Type IV Fluid
Mixtures as a Function of Weather Conditions and Outside Air Temperature.	29

Table 4K.	FAA Guidelines for Holdover Times OCTAGON MAX-FLIGHT Type IV Fluid Mixtures
as a Function of Weather Conditions and Outside Air Temperature	30

Table 4L.	FAA Guidelines for Holdover Times OCTAGON MAX-FLIGHT 04 Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	31

Table 4M.	FAA Guidelines for Holdover Times OCTAGON MAXFLO Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature.	32

Table 5.	FAA Guidelines for the Application of SAE Type II, Type III, and Type IV Fluid Mixtures	33

Table 6.	Lowest On-wing Viscosity Values for Neat and Diluted SAE Type II and Type IV Fluids	34

Table 7.	List of Qualified Deicing/Anti-Icing Fluids – Winter 2008-2009	38

Table 8.	Ice Pellet Allowance Times Winter 2008 – 2009	43

### FAA TYPE I Holdover Time Guideline

### TABLE 1.  FAA GUIDELINES FOR HOLDOVER TIMES SAE TYPE I FLUID MIXTURES AS A FUNCTION OF WEATHER CONDITIONS AND OUTSIDE AIR TEMPERATURE

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- |
| DegreesCelsius | Degrees Fahren- heit | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
|  |  |  |  | Very Light(( | Light (( | Moderate(( |  |  |  |  |
| -3 and above | 27 and above | 0:45 | 0:11-0:17 | 0:18-0:22 | 0:11-0:18 | 0:06-0:11 | 0:09-0:13 | 0:02-0:05 | 0:02-0:05 |  |
| below -3 to -6 | below 27 to 21 | 0:45 | 0:08-0:13 | 0:14-0:17 | 0:08-0:14 | 0:05-0:08 | 0:05-0:09 | 0:02-0:05 | CAUTION: No holdover time guidelines exist |
| below -6 to -10 | below 21 to 14 | 0:45 | 0:06-0:10 | 0:11-0:13 | 0:06-0:11 | 0:04-0:06 | 0:04-0:07 | 0:02-0:05 |  |
| below -10 | below 14 | 0:45 | 0:05-0:09 | 0:07-0:08 | 0:04-0:07 | 0:02-0:04 |  |  |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

‡ Heavy snow, snow pellets, ice pellets, moderate and heavy freezing rain, hail

(( TO USE THESE TIMES, THE FLUID MUST BE HEATED TO A MINIMUM TEMPERATURE OF 60 (C (140 (F) AT THE   NOZZLE AND AT LEAST 1

LITER/M2 (( 2 GALS/100FT2) MUST BE APPLIED TO DEICED SURFACES

SAE Type I fluid/water mixture is selected so that the freezing point of the mixture is at least 10 (C (18 (F) below OAT.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME 
BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- SAE TYPE I FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.																
																	           August 2008

TABLE  1A.  FAA Guidelines for the Application of SAE Type I Fluid Mixture

Minimum Concentrations as a Function of OUTSIDE AIR TEMPERATURE

Concentrations in % volume

| Outside Air Temperature (OAT) | One-step Procedure Deicing/Anti-icing1 | Two-step Procedure |
| --- | --- | --- |
|  |  | First step: Deicing | Second step: Anti-icing 1, 2 |
| -3 (C (27 (F) and above | Mix of fluid and water heated to 60 (C (140 (F) minimum at the nozzle, with a freezing point of at least 10 (C (18 (F) below OAT | Heated water or a mix of fluid and water heated to 60 (C (140 (F) minimum at the nozzle | Mix of fluid and water heated to 60 (C (140 (F) minimum at the nozzle, with a freezing point of at least 10 (C (18 (F) below OAT |
| Below -3 (C (27 (F) |  | Freezing point of heated fluid mixture shall not be more than 3 (C (5 (F) above OAT |  |
| Fluids must only be used at temperatures above their lowest operational use temperature (LOUT). To be applied before first-step fluid freezes, typically within 3 minutes. |
| Notes: Upper temperature limit shall not exceed fluid and aircraft manufacturers’ recommendations. To use Type I holdover time guidelines in snow conditions, at least 1 liter per square meter (2 gal. Per 100 square feet) fluid must be applied to the deiced surfaces. This table is applicable for the use of Type I Holdover Time Guidelines. If holdover times are not required, a temperature of 60 (C (140 (F) at the nozzle is desirable. The lowest operational use temperature (LOUT) for a given fluid is the higher of: The lowest temperature at which the fluid meets the aerodynamic acceptance test for a given aircraft type, or The actual freezing point of the fluid plus a freezing point buffer of 10°C (18°F). Caution: Wing skin temperatures may differ and, in some cases, be lower than OAT. A stronger mix (more glycol) can be used under these conditions. |

August 2008

Table 1B.  Snowfall INTENSITIES as a Function of prevailing Visibility

| Time of Day | Temp. | Visibility (Statute Mile) |  |
| --- | --- | --- | --- |
|  | Degrees Celsius | Degrees Fahrenheit | ( 2 1/2 | 2 | 1 1/2 | 1 | 3/4 | 1/2 | ( 1/4 |  |
| Day | colder/equal -1 | colder/equal 30 | Very Light | Very Light | Light | Light | Moderate | Moderate | Heavy | Snowfall Intensity |
|  | warmer than -1 | warmer than 30 | Very Light | Light | Light | Moderate | Moderate | Heavy | Heavy |  |
| Night | colder/equal -1 | colder/equal 30 | Very Light | Light | Moderate | Moderate | Heavy | Heavy | Heavy |  |
|  | warmer than -1 | warmer than 30 | Very Light | Light | Moderate | Heavy | Heavy | Heavy | Heavy |  |
| NOTE 1: This table is for estimating snowfall intensity. It is based upon the technical report, “The Estimation of Snowfall Rate Using Visibility,” Rasmussen, et al., Journal of Applied Meteorology, October 1999 and additional in situ data. NOTE 2: This table is to be used with Type I fluid guidelines. It may also be used with Type II, III, or IV fluid guidelines. |
| HEAVY = Caution—No Holdover Time Guidelines Exist |

August 2008

FAA TYPE II Holdover Time Guideline

### TABLE 2.  FAA Guidelines for Holdover Times SAE Type II Fluid Mixtures as a Function of Weather Conditions and OUTSIDE AIR TEMPERATURE

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 0:35-1:30 | 0:20-0:45 | 0:30-0:55 | 0:15-0:30 | 0:05-0:40 |  |
|  |  | 75/25 | 5:00 | 0:25-1:00 | 0:15-0:30 | 0:20-0:45 | 0:10-0:25 | 0:05-0:25 |  |
|  |  | 50/50 | 3:00† | 0:15-0:30 | 0:05-0:15 | 0:05-0:15 | 0:05-0:10 |  |  |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:20-1:05 | 0:15-0:30 | ***0:15-0:45 | ***0:10-0:20 | CAUTION: No holdover time guidelines exist |
|  |  | 75/25 | 5:00† | 0:20-0:55 | 0:10-0:20 | ***0:15-0:30 | ***0: 05-0: 15 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:15-0:20 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | SAE Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 (C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when SAE Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below  -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air              temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- SAE TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 2A.  FAA Guidelines for Holdover Times ABAX (SPCA) ECOWING 26 Type II  Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 1:25-2:35 | 0:40-1:00 | 0:50-1:35 | 0:40-0:50 | 0:20-1:25 |  |
|  |  | 75/25 | 5:00 | 1:05-1:55 | 0:25-0:45 | 0:45-1:05 | 0:25-0:35 | 0:10-1:00 |  |
|  |  | 50/50 | 3:00† | 0:30-0:45 | 0:10-0:20 | 0:15-0:25 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:45-2:15 | 0:35-0:55 | ***0:30-1:10 | ***0:15-0:35 |  |
|  |  | 75/25 | 5:00† | 0:35-1:15 | 0:25-0:40 | ***0:20-0:50 | ***0:15-0:25 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:25-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | ABAX Ecowing 26 Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when ABAX Ecowing 26 Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below  -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
             range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- ABAX ECOWING 26 TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 2B.  FAA Guidelines for Holdover Times AVIATION XI’AN HI-TECH KHF-II TYPE II Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 1:15-2:15 | 0:45-1:20 | 0:50-1:30 | 0:30-0:45 | 0:10-1:15 |  |
|  |  | 75/25 | 5:00 | 0:45-1:00 | 0:25-0:40 | 0:25-0:45 | 0:15-0:25 | 0:05-0:45 |  |
|  |  | 50/50 | 3:00† | 0:20-0:30 | 015-0:25 | 0:10-0:15 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 1:10-2:40 | 0:35-1:00 | ***0:20-1:35 | ***0:25-0:40 |  |
|  |  | 75/25 | 5:00† | 0:45-1:20 | 0:15-0:30 | ***0:20-0:45 | ***0:15-0:20 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:35-0:50 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | AVIATION XI’AN HIGH-TECH KHF-II Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when AVIATION XI’AN HIGH-TECH KHF-II Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
              range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- AVIATION XI’AN HIGH-TECH KHF-II TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.																																																			August 2008

## TABLE 2C.  FAA Guidelines for Holdover Times CLARIANT SAFEWING MP II 2025 ECO Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 1:30-2:05 | 0:40-1:10 | 0:40-1:00 | 0:25-0:35 | 0:10-1:15 |  |
|  |  | 75/25 | 5:00 | 0:55-1:45 | 0:25-0:45 | 0:25-0:45 | 0:20-0:25 | 0:05-0:50 |  |
|  |  | 50/50 | 3:00† | 0:20-0:35 | 0:05-0:15 | 0:10-0:15 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:45-1:50 | 0:35-1:00 | ***0:35-1:05 | ***0:20-0:35 |  |
|  |  | 75/25 | 5:00† | 0:40-1:20 | 0:25-0:45 | ***0:30-0:40 | ***0:15-0:25 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:25-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | CLARIANT Safewing mpii 2025 ECO Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when CLARIANT Safewing mpii 2025 ECO Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

†  Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
              range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- CLARIANT SAFEWING MP II 2025 ECO TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

                                                                                                                                                                                                                                             August 2008

## TABLE 2D.  FAA Guidelines for Holdover Times CLARIANT SAFEWING MP II Flight Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 3:30-4:00 | 1:00-1:35 | 1:20-2:00 | 0:45-1:25 | 0:10-1:30 |  |
|  |  | 75/25 | 5:00 | 2:30-4:00 | 0:40-1:20 | 1:15-2:00 | 0:30-0:55 | 0:05-1:20 |  |
|  |  | 50/50 | 3:00† | 0:55-1:45 | 0:10-0:25 | 0:20-0:30 | 0:10-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:55-1:45 | 0:40-1:05 | ***0:35-1:30 | ***0:25-0:45 |  |
|  |  | 75/25 | 5:00† | 0:40-1:10 | 0:20-0:40 | ***0:25-1:10 | ***0:30-0:40 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:30-0:50 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | CLARIANT Safewing mp ii Flight Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when CLARIANT Safewing mp ii Flight Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail
            † Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
              range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- CLARIANT SAFEWING MP II FLIGHT TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

TABLE 2E.  FAA Guidelines for Holdover Times KILFROST ABC-2000 Type II Fluid Mixtures as a    Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 1:30-3:05 | 0:30-1:00 | 0:55-1:35 | 0:40-0:50 | 0:15-1:10 |  |
|  |  | 75/25 | 5:00 | 1:40-3:30 | 0:30-1:05 | 0:45-1:15 | 0:40-0:50 | 0:15-1:40 |  |
|  |  | 50/50 | 3:00† | 1:00-2:10 | 0:15-0:30 | 0:15-0:25 | 0:05-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:35-1:25 | 0:25-0:45 | ***0:25-0:50 | ***0:10-0:30 |  |
|  |  | 75/25 | 5:00† | 0:35-1:15 | 0:25-0:50 | ***0:25-0:55 | ***0:15-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:20-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | KILFROST ABC-2000 Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when KILFROST ABC-2000 Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below  -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
            range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- KILFROST ABC-2000 TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 2F.  FAA Guidelines for Holdover Times KILFROST ABC-II PLUS Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other ‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 1:10-2:25 | 0:25-0:55 | 0:35-1:10 | 0:30-0:40 | 0:05-1:00 |  |
|  |  | 75/25 | 5:00 | 1:10-2:25 | 0:25-0:50 | 0:30-1:00 | 0:20-0:40 | 0:05-0:50 |  |
|  |  | 50/50 | 3:00† | 0:15-0:45 | 0:15-0:35 | 0:05-0:25 | 0:05-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:30-1:05 | 0:15-0:35 | ***0:15-0:45 | ***0:10-0:30 |  |
|  |  | 75/25 | 5:00† | 0:20-0:55 | 0:15-0:35 | ***0:15-0:30 | ***0:10-0:20 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:15-0:20 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | KILFROST ABC-II PLUS Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when KILFROST ABC-II PLUS Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below  -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

†Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
          range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- KILFROST ABC-II PLUS TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 2G.  FAA Guidelines for Holdover Times KILFROST ABC-K PLUS Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other ‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 2:15-3:45 | 1:00-1:40 | 1:50-2:00 | 1:00-1:25 | 0:20-2:00 |  |
|  |  | 75/25 | 5:00 | 1:40-2:30 | 0:35-1:10 | 1:25-2:00 | 0:50-1:10 | 0:15-2:00 |  |
|  |  | 50/50 | 3:00† | 0:35-1:05 | 0:05-0:15 | 0:20-0:30 | 0:10-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:30-1:05 | 0:50-1:25 | ***0:25-1:00 | ***0:15-0:35 |  |
|  |  | 75/25 | 5:00† | 0:25-1:25 | 0:35-1:05 | ***0:25-0:55 | ***0:05-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:30-0:55 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | KILFROST ABC-K PLUS Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when KILFROST ABC-K PLUS Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below  -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
          range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- KILFROST ABC-K PLUS TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 2H.  FAA Guidelines for Holdover Times NEWAVE AEROCHEMICAL FCY-2 TYPE II Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 1:15-2:25 | 0:30-0:55 | 0:35-1:05 | 0:25-0:35 | 0:05-0:45 |  |
|  |  | 75/25 | 5:00 | 0:50-1:30 | 0:20-0:40 | 0:25-0:45 | 0:15-0:25 | 0:05-0:25 |  |
|  |  | 50/50 | 3:00† | 0:25-0:35 | 0:15-0:25 | 0:10-0:20 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:45-1:30 | 0:15-0:30 | ***0:20-0:45 | ***0:15-0:20 |  |
|  |  | 75/25 | 5:00† | 0:30-1:05 | 0:10-0:20 | ***0:15-0:30 | ***0:05-0:15 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:25-0:35 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | NEWAvE AEROCHEMICAL FCY-2 Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when NEWAYE AEROCHEMICAL FCY-2 Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
               range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- NEWAVE AEROCHEMICAL FCY-2 TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

August 2008

TABLE 2I.  FAA Guidelines for Holdover Times OCTAGON E-MAX Type II Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type II Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 8:00 | 2:05-3:45 | 0:40-1:20 | 0:45-1:35 | 0:30-0:40 | 0:15-1:30 |  |
|  |  | 75/25 | 5:00 | 1:25-2:50 | 0:25-0:55 | 0:40-1:10 | 0:20-0:30 | 0:10-1:05 |  |
|  |  | 50/50 | 3:00† | 0:30-0:55 | 0:10-0:25 | 0:15-0:30 | 0:10-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 8:00† | 0:50-1:45 | 0:35-1:10 | ***0:35-1:00 | ***0:20-0:30 |  |
|  |  | 75/25 | 5:00† | 0:30-1:20 | 0:25-0:50 | ***0:35-1:05 | ***0:15-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 8:00† | 0:20-0:35 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | OCTAGON E-MAX Type II fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when OCTAGON E-MAX Type II fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below  -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature
             range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- OCTAGON E-MAX TYPE II FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

FAA TYPE III Holdover Time Guideline

### Table 3.  FAA Guidelines for Holdover Times SAE Type III Fluid Mixture as a Function of Weather Conditions and OUTSIDE AIR TEMPERATURE.

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRETAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- |
| Degrees Celsius | Degrees Fahrenheit | Type III Fluid Concentration Neat Fluid/Water (Volume %/Volume %) | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
|  |  |  |  |  | Very Light | Light | Moderate |  |  |  |  |
| -3 and above | 27 and above | 100/0 | 2:00 | 0:20 - 0:40 | 0:35 - 0:40 | 0:20 - 0:35 | 0:10 - 0:20 | 0:10 - 0:20 | 0:08 - 0:10 | 0:06 - 0:20 |  |
|  |  | 75/25 | 1:00 | 0:15 - 0:30 | 0:25 - 0:35 | 0:15 - 0:25 | 0:08 - 0:15 | 0:08 - 0:15 | 0:06 - 0:10 | 0:02 - 0:10 |  |
|  |  | 50/50 | 0:30 | 0:10 - 0:20 | 0:15 - 0:20 | 0:08 - 0:15 | 0:04 - 0:08 | 0:05 - 0:09 | 0:04 - 0:06 |  |  |
| below -3 to -10 | below 27 to 14 | 100/0 | 2:00 | 0:20 - 0:40 | 0:30 - 0:35 | 0:15 - 0:30 | 0:09 - 0:15 | 0:10 - 0:20 | 0:08 - 0:10 |  |
|  |  | 75/25 | 1:00 | 0:15 - 0:30 | 0:25 - 0:30 | 0:10 - 0:25 | 0:07 - 0:10 | 0:09 - 0:12 | 0:06 - 0:09 |  |
| below -10 | below 14 | 100/0 | 2:00 | 0:20 - 0:40 | 0:30 - 0:35 | 0:15 - 0:30 | 0:08 - 0:15 | CAUTION: No holdover time guidelines exist |
| SAE Type III fluid may be used below -10 (C (14 (F), provided the freezing point of the fluid is at least 7 (C (13 (F) below OAT and aerodynamic acceptance criteria are met. Consider the use of SAE Type I when Type III fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

*Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

**This column is for use at temperatures above 0 °C (32 °F) only

‡Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST WILL REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- SAE TYPE III FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR - AND DOES NOT PROVIDE - PROTECTION DURING FLIGHT.

August 2008

FAA TYPE IV Holdover Time GuidelineS

## TABLE 4.  FAA Guidelines for Holdover Times SAE Type IV Fluid Mixtures as a Function of
Weather Conditions and OUTSIDE AIR TEMPERATURE

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 1:15-2:30 | 0:35-1:15 | 0:40-1:10 | 0:25-0:40 | 0:10-1:05 |  |
|  |  | 75/25 | 5:00 | 1:05-1:45 | 0:20-0:55 | 0:35-0:50 | 0:15-0:30 | 0:05-0:40 |  |
|  |  | 50/50 | 3:00† | 0:15-0:35 | 0:05-0:15 | 0:10-0:20 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:20-1:20 | 0:20-0:40 | ***0:20-0:45 | ***0:10-0:25 |  |
|  |  | 75/25 | 5:00† | 0:25-0:50 | 0:15-0:35 | ***0:15-0:30 | ***0:10-0:20 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:15-0:40 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | SAE Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when SAE Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

*  Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- SAE TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

TABLE 4A.  FAA Guidelines for Holdover Times ABAX (SPCA) AD-480 Type IV Fluid Mixtures as a function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:00-3:30 | 0:40-1:20 | 0:50-1:30 | 0:35-0:55 | 0:15-1:35 |  |
|  |  | 75/25 | 5:00 | 1:30-2:45 | 0:30-1:05 | 0:50-1:15 | 0:30-0:45 | 0:10-1:15 |  |
|  |  | 50/50 | 3:00† | 0:30-0:45 | 0:10-0:20 | 0:15-0:25 | 0:05-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:20-1:20 | 0:30-0:55 | ***0:25-1:20 | ***0:15-0:30 |  |
|  |  | 75/25 | 5:00† | 0:25-0:50 | 0:20-0:45 | ***0:25-1:05 | ***0:15-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:15-0:40 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | ABAX AD-480 Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when ABAX AD-480 Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air     temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- ABAX AD-480 TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.  

                                                                                                                                                                                                                                                          August 2008

## TABLE 4B.  FAA Guidelines for Holdover Times CLARIANT SAFEWING MP IV 2001 Type IV Fluid 
 Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 1:20-3:20 | 1:00-1:55 | 0:55-1:55 | 0:40-1:00 | 0:15-2:00 |  |
|  |  | 75/25 | 5:00 | 1:20-2:00 | 0:35-1:00 | 0:35-1:10 | 0:25-0:35 | 0:10-1:25 |  |
|  |  | 50/50 | 3:00† | 0:15-0:40 | 0:10-0:20 | 0:10-0:20 | 0:05-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:45-1:35 | 0:30-0:50 | ***0:55-1:35 | ***0:30-0:45 |  |
|  |  | 75/25 | 5:00† | 0:30-1:00 | 0:20-0:35 | ***0:40-1:10 | ***0:20-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:20-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | CLARIANT SAFEWING MP IV 2001 Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when CLARIANT SAFEWING MP IV 2001 Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- CLARIANT SAFEWING MP IV 2001 TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.
	                                                                                                                                                                                                                                            August 2008

## TABLE 4C.  FAA Guidelines for Holdover Times CLARIANT SAFEWING MP IV 2012 PROTECT Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 1:15-2:30 | 0:40-1:15 | 0:40-1:10 | 0:25-0:45 | 0:10-1:05 |  |
|  |  | 75/25 | 5:00 | 1:10-2:05 | 0:25-0:55 | 0:35-0:50 | 0:15-0:30 | 0:05-0:40 |  |
|  |  | 50/50 | 3:00† | 0:25-0:45 | 0:15-0:25 | 0:15-0:20 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:45-1:45 | 0:20-0:40 | ***0:25-0:45 | ***0:15-0:25 |  |
|  |  | 75/25 | 5:00† | 0:25-1:05 | 0:20-0:40 | ***0:15-0:30 | ***0:10-0:20 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:20-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | CLARIANT SAFEWING MP IV 2012 PROTECT Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when CLARIANT SAFEWING MP IV 2012 PROTECT Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- CLARIANT SAFEWING MP IV 2012 PROTECT TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 4D.  FAA Guidelines for Holdover Times CLARIANT SAFEWING MP IV LAUNCH Type IV Fluid Mixtures as a function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 4:00-4:00 | 1:05-1:45 | 1:30-2:00 | 1:00-1:40 | 0:15-1:40 |  |
|  |  | 75/25 | 5:00 | 3:40-4:00 | 1:00-1:45 | 1:40-2:00 | 0:45-1:15 | 0:10-1:45 |  |
|  |  | 50/50 | 3:00† | 1:25-2:45 | 0:25-0:45 | 0:30-0:50 | 0:20-0:25 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 1:00-1:55 | 0:50-1:20 | ***0:35-1:40 | ***0:25-0:45 |  |
|  |  | 75/25 | 5:00† | 0:40-1:20 | 0:45-1:25 | ***0:25-1:10 | ***0:25-0:45 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:30-0:50 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | CLARIANT SAFEWING MPIV LAUNCH Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when CLARIANT SAFEWING MPIV LAUNCH Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- CLARIANT SAFEWING MP IV LAUNCH TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT

August 2008

## TABLE 4E.  FAA Guidelines for Holdover Times DOW UCAR™ ULTRA+ ADF/AAF Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 1:35-3:35 | 0:35-1:15 | 0:45-1:35 | 0:25-0:40 | 0:10-1:20 |  |
|  |  | 75/25 |  |  |  |  |  | CAUTION: No holdover time guidelines exist |
|  |  | 50/50 |  |  |  |  |  |  |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 1:25-3:00 | 0:25-0:55 | ***0:45-1:25 | ***0:30-0:45 |  |
|  |  | 75/25 |  |  |  |  |  |  |
| below -14 to -24 | below 7 to -12 | 100/0 | 12:00† | 0:40-2:10 | 0:20-0:45 |  |
| below -24 | below -12 | 100/0 | DOW UCAR ULTRA+ Type IV fluid may be used below -24 °C (-12 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when DOW UCAR ULTRA+ Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- DOW UCAR ULTRA+ TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 4F.  FAA Guidelines for Holdover Times DOW UCAR™ ENDURANCE EG106 Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:05-3:10 | 0:40-1:20 | 1:10-2:00 | 0:50-1:15 | 0:20-2:00 |  |
|  |  | 75/25 |  |  |  |  |  | CAUTION: No holdover time guidelines exist |
|  |  | 50/50 |  |  |  |  |  |  |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 1:50-3:20 | 0:30-1:05 | ***0:55-1:50 | ***0:45-1:10 |  |
|  |  | 75/25 |  |  |  |  |  |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:30-1:05 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | DOW UCAR ENDURANCE EG 106 Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when DOW UCAR ENDURANCE EG 106 Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- DOW UCAR ENDURANCE EG 106 TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

TABLE 4G.  FAA Guidelines for Holdover Times DOW UCARTM FLIGHTGUARD AD-480 Type IV Fluid
Mixtures as a function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:00-3:30 | 0:40-1:20 | 0:50-1:30 | 0:35-0:55 | 0:15-1:35 |  |
|  |  | 75/25 | 5:00 | 1:30-2:45 | 0:30-1:05 | 0:50-1:15 | 0:30-0:45 | 0:10-1:15 |  |
|  |  | 50/50 | 3:00† | 0:30-0:45 | 0:10-0:20 | 0:15-0:25 | 0:05-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:20-1:20 | 0:30-0:55 | ***0:25-1:20 | ***0:15-0:30 |  |
|  |  | 75/25 | 5:00† | 0:25-0:50 | 0:20-0:45 | ***0:25-1:05 | ***0:15-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:15-0:40 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | DOW UCAR FLIGHTGUARD AD-480 Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when DOW UCAR FLIGHTGUARD AD-480 Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- DOW UCAR FLIGHTGUARD AD-480 TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 4H.  FAA Guidelines for Holdover Times KILFROST ABC-S Type IV Fluid Mixtures 
as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:35-4:00 | 1:00-1:40 | 1:20-1:50 | 1:00-1:25 | 0:20-1:15 |  |
|  |  | 75/25 | 5:00 | 1:05-1:45 | 0:30-0:55 | 0:45-1:10 | 0:35-0:50 | 0:10-0:50 |  |
|  |  | 50/50 | 3:00† | 0:20-0:35 | 0:05-0:15 | 0:15-0:20 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:45-2:05 | 0:45-1:20 | ***0:20-1:00 | ***0:10-0:30 |  |
|  |  | 75/25 | 5:00† | 0:25-1:00 | 0:25-0:50 | ***0:20-1:10 | ***0:10-0:35 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:20-0:40 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | KILFROST ABC-S Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when KILFROST ABC-S Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- KILFROST ABC-S TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 4I.  FAA Guidelines for Holdover Times KILFROST ABC-S PLUS Type IV Fluid Mixtures
 as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:10-4:00 | 1:15-2:00 | 1:50-2:00 | 1:05-2:00 | 0:25-2:00 |  |
|  |  | 75/25 | 5:00 | 1:25-2:40 | 0:45-1:15 | 1:00-1:20 | 0:30-0:50 | 0:10-1:20 |  |
|  |  | 50/50 | 3:00† | 0:30-0:55 | 0:15-0:30 | 0:15-0:40 | 0:15-0:20 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:55-3:30 | 1:00-1:45 | ***0:25-1:35 | ***0:20-0:30 |  |
|  |  | 75/25 | 5:00† | 0:45-1:50 | 0:35-1:00 | ***0:20-1:10 | ***0:15-0:25 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:40-1:00 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | KILFROST ABC-S PLUS Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when KILFROST ABC-S PLUS Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- KILFROST ABC-S PLUS TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

                                                                                                                                                                                                                                                          August 2008

## TABLE 4J.  FAA Guidelines for Holdover Times LYONDELL ARCTIC SHIELDTM Type IV Fluid Mixtures as a function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/ Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 1:55-3:10 | 0:50-1:25 | 0:55-1:40 | 0:45-1:05 | 0:15-1:25 |  |
|  |  | 75/25 | 5:00 | 1:20-2:15 | 0:40-1:05 | 0:55-1:25 | 0:30-0:45 | 0:05-1:20 |  |
|  |  | 50/50 | 3:00† | 0:35-0:45 | 0:20-0:35 | 0:20-0:30 | 0:10-0:15 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 1:00-2:25 | 0:45-1:15 | ***0:25-1:30 | ***0:25-0:30 |  |
|  |  | 75/25 | 5:00† | 0:50-1:45 | 0:35-0:55 | ***0:30-1:15 | ***0:25-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:25-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | LYONDELL ARCTIC SHIELD Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when LYONDELL ARCTIC SHIELD Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 degrees Celsius (32 degrees Fahrenheit) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- LYONDELL ARCTIC SHIELD TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 4K.  FAA Guidelines for Holdover Times OCTAGON MAX-FLIGHT Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:40-4:00 | 0:50-1:35 | 0:55-2:00 | 0:35-1:00 | 0:15-1:15 |  |
|  |  | 75/25 | 5:00 | 2:05-3:15 | 0:45-1:45 | 1:15-2:00 | 0:35-1:10 | 0:10-0:40 |  |
|  |  | 50/50 | 3:00† | 0:55-1:45 | 0:25-1:15 | 0:35-1:00 | 0:15-0:30 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:50-2:30 | 0:25-0:50 | ***0:25-1:10 | ***0:20-0:40 |  |
|  |  | 75/25 | 5:00† | 0:30-1:05 | 0:20-0:50 | ***0:20-1:00 | ***0:15-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:20-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | OCTAGON MAX-FLIGHT Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when OCTAGON MAX-FLIGHT Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- OCTAGON MAX-FLIGHT TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

## TABLE 4L.  FAA Guidelines for Holdover Times OCTAGON MAX-FLIGHT 04 Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Active Frost | Freezing Fog | Snow/Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:40-4:00 | 1:25-2:00 | 2:00-2:00 | 1:10-1:30 | 0:20-2:00 |  |
|  |  | 75/25 | 5:00 | 2:05-3:15 | 1:05-2:00 | 1:50-2:00 | 1:00-1:20 | 0:20-2:00 |  |
|  |  | 50/50 | 3:00† | 0:55-1:45 | 0:25-1:15 | 0:35-1:10 | 0:25-0:35 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 0:50-2:30 | 0:35-1:10 | ***0:25-1:30 | ***0:20-0:40 |  |
|  |  | 75/25 | 5:00† | 0:30-1:05 | 0:40-1:20 | ***0:20-1:00 | ***0:15-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:20-0:45 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | OCTAGON MAX-FLIGHT 04 Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when OCTAGON MAX-FLIGHT 04 Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- OCTAGON MAX-FLIGHT 04 TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.
															           August 2008

## TABLE 4M.  FAA Guidelines for Holdover Times OCTAGON MAXFLO Type IV Fluid Mixtures as a Function of Weather Conditions and Outside Air Temperature

CAUTION:  THIS TABLE IS FOR DEPARTURE PLANNING ONLY AND SHOULD BE USED IN CONJUNCTION WITH PRE-TAKEOFF CHECK PROCEDURES.

| Outside Air Temperature | Manufacturer Specific Type IV Fluid Concentration Neat-Fluid/Water (Volume %/Volume %) | Approximate Holdover Times Under Various Weather Conditions (hours: minutes) |
| --- | --- | --- |
| Degrees Celsius | Degrees Fahrenheit |  | Frost | Freezing Fog | Snow /Snow Grains | Freezing Drizzle* | Light Freezing Rain | Rain on Cold Soaked Wing** | Other‡ |
| -3 and above | 27 and above | 100/0 | 12:00 | 2:20-3:35 | 0:40-1:30 | 1:20-2:00 | 0:30-1:00 | 0:10-2:00 |  |
|  |  | 75/25 | 5:00 | 1:25-2:00 | 0:20-0:55 | 0:40-1:05 | 0:20-0:35 | 0:05-1:15 |  |
|  |  | 50/50 | 3:00† | 0:20-0:40 | 0:05-0:15 | 0:10-0:20 | 0:05-0:10 | CAUTION: No holdover time guidelines exist |
| below -3 to -14 | below 27 to 7 | 100/0 | 12:00† | 1:10-2:20 | 0:25-1:00 | ***0:35-1:45 | ***0:30-0:50 |  |
|  |  | 75/25 | 5:00† | 0:40-1:25 | 0:15-0:40 | ***0:35-1:15 | ***0:15-0:30 |  |
| below -14 to -25 | below 7 to -13 | 100/0 | 12:00† | 0:30-1:00 | 0:15-0:30 |  |
| below -25 | below -13 | 100/0 | OCTAGON MAXFLO Type IV fluid may be used below -25 °C (-13 °F) provided the freezing point of the fluid is at least 7 °C (13 °F) below the OAT and the aerodynamic acceptance criteria are met. Consider use of SAE Type I when OCTAGON MAXFLO Type IV fluid cannot be used. |

THE RESPONSIBILITY FOR THE APPLICATION OF THESE DATA REMAINS WITH THE USER.

* Use light freezing rain holdover times if positive identification of freezing drizzle is not possible

** This column is for use at temperatures above 0 °C (32 °F) only

*** No holdover time guidelines exist for this condition below -10 (C (14 (F)

‡ Snow pellets, ice pellets, heavy snow, moderate and heavy freezing rain, and hail

† Radiational cooling during active frost conditions may reduce holdover times when operating close to the lower end of the outside air temperature range.

CAUTIONS:

- THE TIME OF PROTECTION WILL BE SHORTENED IN HEAVY WEATHER CONDITIONS.  HEAVY PRECIPITATION RATES OR HIGH MOISTURE CONTENT, HIGH WIND VELOCITY, OR JET BLAST MAY REDUCE HOLDOVER TIME BELOW THE LOWEST TIME STATED IN THE RANGE.  HOLDOVER TIME MAY BE REDUCED WHEN AIRCRAFT SKIN TEMPERATURE IS LOWER THAN OAT.

- OCTAGON MAXFLO TYPE IV FLUID USED DURING GROUND DEICING/ANTI-ICING IS NOT INTENDED FOR AND DOES NOT PROVIDE PROTECTION DURING FLIGHT.

August 2008

TABLE 5.  FAA Guidelines for the Application of SAE Type II, Type III, and Type IV Fluid Mixtures Minimum Concentrations as a Function of Outside Air Temperature

Concentrations in % Volume

| Outside Air Temperature (OAT) | One-step Procedure Deicing/Anti-icing1 | Two-step Procedure |
| --- | --- | --- |
|  |  | First step: Deicing | Second step: Anti-icing1, 2, |
| -3 (C (27 (F) and above | 50/50 Heated3 Types II, III or IV | Heated water or a heated mix of Types I, II, III or IV and water | 50/50 Type II, III, or IV |
| Below -3 (C (27 (F) to -14 (C (7 (F) | 75/25 Heated3 Types II, III or IV | Heated suitable mix of Types I, II, III or IV, and water with a freezing point not more than 3 (C (5 (F) above actual OAT | 75/25 Type II, III, or IV |
| below -14 (C (7 (F) to -25 (C (-13 (F) | 100/0 Heated3 Types II, III or IV | Heated suitable mix of Types I, II, III or IV, and water with a freezing point not more than 3 (C (5 (F) above actual OAT | 100/0 Type II, III, or IV |
| Below -25 (C (-13 (F) | SAE Type II/IV fluid may be used below -25 (C (-13 (F) provided that the OAT is at or above the LOUT. SAE Type III fluid may be used below -10°C (14°F) provided that the OAT is at or above the LOUT Consider the use of SAE Type I when Type II, III, or IV fluid cannot be used. |
| 1) Fluids must only be used at temperatures above their lowest operational use temperature (LOUT). 2) To be applied before first step fluid freezes, typically within 3 minutes. 3) Clean aircraft may be anti-iced with unheated Types II, III, or IV fluid. |
| NOTES: For heated fluids, a fluid temperature not less than 60 (C (140 (F) at the nozzle is desirable. Upper temperature limit shall not exceed fluid and aircraft manufacturers’ recommendations. The lowest operational use temperature (LOUT) for a given fluid is the higher of: The lowest temperature at which the fluid meets the aerodynamic acceptance test for a given aircraft type, or The actual freezing point of the fluid plus a freezing point buffer of 7°C (13°F). |
| CAUTIONS: Wing skin temperatures may differ and in some cases may be lower than OAT. A stronger mix (more glycol) can be used under these conditions. As fluid freezing may occur, 50/50 Types II, III, or IV fluid shall not be used for the anti-icing step of a cold-soaked wing as indicated by frost or ice on the lower surface of the wing in the area of the fuel tank. An insufficient amount of anti-icing fluid, especially in the second step of a two-step procedure, may cause a substantial loss of holdover time, particularly when using a Type I fluid mixture for the first step (deicing) of a two-step procedure. |

TABLE 6

LOWEST ON-WING VISCOSITY VALUES FOR ANTI-ICING FLUIDS

(See Page 36 for Table 6 Notes)

| Table 6-1: Type II Anti-Icing Fluids |
| --- |
| Fluid Name | Fluid Dilution | Lowest On-Wing Viscosity a (mPa.s) |
|  |  | Manufacturer Method | AIR 9968 revision a method |
| ABAX (SPCA) Ecowing 26 | 100/0 | 4,900 e | 4,600 g |
|  | 75/25 | 2,200 g | 2,200 g |
|  | 50/50 | 50 g | 50 g |
| Aviation Xi’An Hi-Tech KHF-II | 100/0 | 8,750 c | 7,690 g |
|  | 75/25 | 6,400 c | 6,890 g |
|  | 50/50 | 2,950 c | 3,150 g |
| Clariant Safewing MP II 2025 ECO | 100/0 | 5,500 b | 5,750 g |
|  | 75/25 | 10,000 b | 10,000 g |
|  | 50/50 | 3,000 b | 3,250 g |
| Clariant Safewing MP II Flight | 100/0 | 3,340 g | 3,340 g |
|  | 75/25 | 17,500 g | 17,500 g |
|  | 50/50 | 11,500 g | 11,500 g |
| Clariant Safewing MP II 1951 | 100/0 | 2,500 b | 2,750 g |
|  | 75/25 | 2,900 b | 3,000 g |
|  | 50/50 | 50 b | 50 g |
| Kilfrost ABC-3 | 100/0 | 2,500 c | 2,500 j |
|  | 75/25 | 2,000 c | 2,000 j |
|  | 50/50 | 400 c | 400 j |
| Kilfrost ABC-2000 | 100/0 | 2,350 c | 2,350 g |
|  | 75/25 | 3,000 c | 3,000 j |
|  | 50/50 | 1,000 c | 1,000 j |
| Kilfrost ABC-II Plus | 100/0 | 3,600 c | 3,600 g |
|  | 75/25 | 4,000 c | 4,000 j |
|  | 50/50 | 1,000 c | 1,000 j |
| Kilfrost ABC-K Plus | 100/0 | 2,850 c | 2,640 g |
|  | 75/25 | 12,650 c | 12,650 c |
|  | 50/50 | 4,200 c | 5,260 g |
| Newave Aerochemical FCY-2 | 100/0 | 7,000 c | 8,920 g |
|  | 75/25 | 18,550 c | 18,550 c |
|  | 50/50 | 6,750 c | 7,030 g |
| Octagon E Max II | 100/0 | 13,520 d | 13,520 g |
|  | 75/25 | 11,400 g | 11,400 g |
|  | 50/50 | 2,820 g | 2,820 g |

| Table 6-2: Type III Anti-Icing Fluids |
| --- |
| Fluid Name | Fluid Dilution | Lowest On-Wing Viscosity a (mPa.s) |
|  |  | Manufacturer Method | AIR 9968 revision a method |
| Clariant Safewing MP III 2031 ECO | 100/0 | 30 h | Not Applicable |
|  | 75/25 | 55 h | Not Applicable |
|  | 50/50 | 10 h | Not Applicable |

| Table 6.3 Type IV Anti-Icing Fluids |
| --- |
| Fluid Name | Fluid Dilution | Lowest On-Wing Viscosity a (mPa.s) |
|  |  | Manufacturer Method | SAE AIR 9968 revision a method |
| ABAX (SPCA) AD-480 | 100/0 | 15,200 e | 12,800 c |
|  | 75/25 | 16,000 e | 12,400 c |
|  | 50/50 | 4,000 e | 3,800 g |
| Clariant Safewing MP IV 2001 | 100/0 | 18,000 b | 18,000 c |
|  | 75/25 | 8,000 b | 11,500 g |
|  | 50/50 | 1,200 b | 1,750 g |
| Clariant Safewing MP IV 2012 Protect | 100/0 | 7,800 b | 7,250 g |
|  | 75/25 | 17,800 b | 17,700 c |
|  | 50/50 | 4,500 b | 4,250 g |
| Clariant Safewing MP IV Launch | 100/0 | 7,550 g | 7,550 g |
|  | 75/25 | 18,000 g | 18,000 g |
|  | 50/50 | 17,800 g | 17,800 g |
| Dow UCAR ADF/AAF ULTRA+ | 100/0 | 36,000 f | 28,000 c |
|  | 75/25 | Dilution Not Applicable | Dilution Not Applicable |
|  | 50/50 | Dilution Not Applicable | Dilution Not Applicable |
| Dow UCAR Endurance EG106 | 100/0 | 24,850 f | 2,230 g |
|  | 75/25 | Dilution Not Applicable | Dilution Not Applicable |
|  | 50/50 | Dilution Not Applicable | Dilution Not Applicable |
| Dow UCAR FlightGuard AD-480 | 100/0 | 15,200 e | 12,800 c |
|  | 75/25 | 16,000 e | 12,400 c |
|  | 50/50 | 4,000 e | 3,800 g |
| Kilfrost ABC-S | 100/0 | 17,000 c | 17,000 c |
|  | 75/25 | 12,000 c | 12,000 c |
|  | 50/50 | 2,000 c | 2,000 j |
| Kilfrost ABC-S PLUS | 100/0 | 17,900 c | 17,900 c |
|  | 75/25 | 18,300 c | 18,300 c |
|  | 50/50 | 7,500 c | 7,500 j |
| Lyondell Arctic Shield | 100/0 | 23,150 i | 28,000 c |
|  | 75/25 | 21,700 i | 22,100 c |
|  | 50/50 | 6,400 i | 7,640 g |
| Octagon Max-Flight | 100/0 | 5,540 d | 5,540 g |
|  | 75/25 | 15,000 g | 15,000 g |
|  | 50/50 | 5,200 g | 5,200 g |
| Octagon Max-Flight 04 | 100/0 | 5,540 d | 5,540 g |
|  | 75/25 | 15,000 g | 15,000 g |
|  | 50/50 | 5,200 g | 5,200 g |
| Octagon MaxFlo | 100/0 | 8,670 g | 8,670 g |
|  | 75/25 | 8,200 g | 8,200 g |
|  | 50/50 | 2,200 g | 2,200 g |

NOTES

a	The SAE Aerospace Information Report (AIR) 9968 Revision A (December 2004) viscosity method should only be used for field verification and auditing purposes; when in doubt as to which method is appropriate, use the manufacturer method.

b	Brookfield Spindle SC4-34/13R, small sample adapter, 10 mL of fluid, at 20°C, 0.3 rpm, for 15 minutes 0 seconds.

c	Brookfield Spindle LV2-disc with guard leg, 150 mL of fluid, at 20°C, 0.3 rpm, for 10 minutes 0 seconds.

d	Brookfield Spindle LV1 with guard leg, 500 mL of fluid, at 20°C, 0.3 rpm, for 33 minutes 20 seconds.

e	Brookfield Spindle SC4-34/13R, small sample adapter, 10 mL of fluid, at 20°C, 0.3 rpm, for 30 minutes 0 seconds.

f 	Brookfield Spindle SC4-31/13R, small sample adapter, 10 mL of fluid, at 0°C, 0.3 rpm, for 10 minutes 0 seconds.

g	Brookfield Spindle LV1 with guard leg, 500 mL of fluid, at 20ºC, 0.3 rpm, for 10 minutes 0 seconds.

h	Brookfield Spindle LV0, UL-Adapter, 16 mL of fluid, at 20ºC, 0.3 rpm, for 10 minutes 0 seconds.

i	Brookfield Spindle SC4-31/13R, small sample adapter, 9 mL of fluid, at 20°C, 0.3 rpm, for 33 minutes 0 seconds.

j	Brookfield Spindle LV1 with guard leg, 150 mL of fluid, at 20ºC, 0.3 rpm, for 10 minutes 0 seconds.

August 2008

### SIGNIFICANCE OF TABLE 6.  The viscosity values of the fluids in Table 6 are those provided by the fluid manufacturers for holdover time testing. For the holdover time guidelines to be valid, the viscosity of the fluid on the wing shall not be lower than that listed in this table. The user should periodically ensure that the viscosity of a fluid sample taken from the wing is not lower than the value listed here.

Table 7.  List of Qualified (1) Deicing/Anti-Icing Fluids-Winter 2008-2009

###### Qualified Type I Deicing/Anti-Icing Fluids

| Company Name | Fluid Name |
| --- | --- |
| ABAX Industries (formerly SPCA) | ABAX DE-950 |
| ABAX Industries (formerly SPCA) | ABAX DE-950 Colorless |
| Arkton Ltd. | Artica DG |
| Aviation Xi’an High-Tech | KHF-1 |
| Battelle | D3: Degradable by Design Deicer™ ADF 1006A |
| Beijing Wangye Aviation Chem. Prod. Co. | KLA-1 |
| Beijing Wangye Aviation Chem. Prod. Co | YJF-1 |
| Chemical Specialists and Development | Prist Wing Deicer |
| Clariant GmbH | Safewing MPI 1938 TF |
| Clariant GmbH | Safewing MPI 1938 TF Pre-mix |
| Clariant GmbH | Safewing MP I 1938 ECO (80) |
| Clariant GmbH | Safewing MP I 1938 ECO (80) Pre-mix |
| Clariant GmbH | Safewing MP I 1938 ECO |
| Clariant GmbH | Safewing EG I 1996 |
| Dow Chemical Company | UCAR™ ADF Concentrate |
| Dow Chemical Company | UCAR™ ADF XL-54 |
| Dow Chemical Company | UCAR™ PG ADF Concentrate |
| Dow Chemical Company | UCAR™ PG ADF Dilute 55/45 |
| HOC Industries | SafeTemp I ES |
| HOC Industries | SafeTemp I ES Plus |
| Inland Technologies | Duragly - P ready to use |
| Inland Technologies | Duragly - E ready to use |
| Kilfrost | Kilfrost DF PLUS |
| Kilfrost | Kilfrost DF PLUS (80) |
| Kilfrost | Kilfrost DF PLUS (88)® |
| Kilfrost | Kilfrost DFSUSTAIN ™ |
| Lyondell Chemical Company | ARCOPlus® |
| Lyondell Chemical Company | ARCTIC Plus® |
| Newave Aerochemical Company | FCY-1A |
| Octagon Process | EcoFlo |
| Octagon Process | Octaflo EF |
| Octagon Process | Octaflo EG |
| Viterbo S.A. | Jarkleer SAE Type I |

###### Table 7.  List of Qualified (1) Deicing/Anti-Icing Fluids-Winter 2008-2009 (Continued)

###### Qualified Type II Deicing/Anti-Icing Fluids

| Company Name | Fluid Name |
| --- | --- |
| ABAX Industries (formerly SPCA) | ABAX Ecowing 26 |
| Aviation Xi’an High-Tech | KHF-II |
| Clariant GmbH | Safewing MP II 1951 |
| Clariant GmbH | Safewing MP II 2025 ECO |
| Clariant GmbH | Safewing MP II Flight |
| Kilfrost | Kilfrost ABC-II PLUS |
| Kilfrost | Kilfrost ABC-3 |
| Kilfrost | Kilfrost ABC-2000 |
| Kilfrost | Kilfrost ABC-K PLUS |
| Newave Aerochemical Technology | FCY-2 |
| Octagon Process | E-Max |

###### Qualified Type III Deicing/Anti-Icing Fluids

| Company Name | Fluid Name |
| --- | --- |
| Clariant GmbH | Safewing MP III 2031 ECO |

###### Qualified Type IV Deicing/Anti-Icing Fluids

| Company Name | Fluid Name |
| --- | --- |
| ABAX (formerly SPCA) | ABAX AD-480 |
| Clariant GmbH | Safewing MP IV 2001 |
| Clariant GmbH | Safewing MP IV 2012 Protect |
| Clariant GmbH | Safewing MP IV Launch |
| Dow Chemical Company | UCAR™ ADF/AAF ULTRA+ |
| Dow Chemical Company | UCAR™ Endurance EG106 |
| Dow Chemical Company | UCAR™ FlightGuard AD-480 |
| Kilfrost | Kilfrost ABC-S |
| Kilfrost | Kilfrost ABC-S Plus |
| Lyondell Chemical Company | ARCTIC Shield™ |
| Octagon Process | Max-Flight |
| Octagon Process | Max-Flight 04 |

Table 7.  List of Qualified (1) Deicing/Anti-Icing Fluids–Winter 2008-2009 (Continued)

| Octagon Process | MaxFlo |
| --- | --- |

¹ Qualified indicates that the fluid has been qualified solely to the requirements of the applicable SAE anti-icing and aerodynamic performance specifications in effect at the time of certification, as conducted by the Anti-Icing Materials International Laboratory at the University of Quebec at Chicoutimi, Canada, Web site: http://www.uqac.ca/amil/index.htm.  For other specification requirements for Type I fluids, see SAE AMS 1424 (latest version) and for SAE Types II, III, and IV fluids, see SAE AMS 1428 (latest version). Fluids that qualify after the issuance of this list will appear in a later update.

ICE PELLET ALLOWANCE TIMES WINTER 2008-2009

The values for the Ice Pellet Allowance Times Winter 2008 – 2009 table remain unchanged from the Winter 2007 – 2008 table.  Limited testing was accomplished during the 2007 – 2008 icing season with inconclusive results.

Operations in Light and Moderate Ice Pellets and Light Ice Pellets mixed with other forms of precipitation.

(1)  Tests have shown that ice pellets generally remain in the frozen state imbedded in Type IV anti-icing fluid, and are not absorbed by the fluid in the same manner as other forms of precipitation.  Using current guidelines for determining anti-icing fluid failure, the presence of a contaminant not absorbed by the fluid (remaining imbedded) would be an indication that the fluid has failed.  These imbedded ice pellets are generally not readily detectable by the human eye during pre-takeoff contamination check procedures.  Therefore, a visual pre-takeoff contamination check in ice pellet conditions may not be of value and is not required.

(2)  The research data have also shown that after proper deicing and anti-icing, the accumulation of light ice pellets, moderate ice pellets, and ice pellets mixed with other forms of precipitation in Type IV fluid will not prevent the fluid from flowing off the aerodynamic surfaces during takeoff.  This flow due to shearing occurs with rotation speeds consistent with Type IV anti-icing fluid recommended applications for up to the applicable allowance time listed in  Table-1.  These allowance times are from the start of the Type IV anti-icing fluid application.  Additionally, if the ice pellet condition stops, and the allowance time has not been exceeded, and the OAT has remained constant or increased from the temperature on which the allowance time was based, the operator is permitted to consider the Type IV anti-icing fluid effective without any further action up to 90 minutes after the start of the application time of the Type IV anti-icing fluid.

Examples: 	a) Type IV anti-icing fluid is applied with a start of application time of 10:00, OAT is 00C, light ice pellets fall until 10:20 and stop and do not restart.  The allowance time stops at 10:50; however, provided that the OAT remains constant or increases and that no precipitation restarts after the allowance time of 10:50  the aircraft may takeoff without any further action up to 11:30.

b) Type IV anti-icing fluid is applied with a start of application time of 10:00, OAT is 00C, light ice pellets mixed with freezing drizzle falls until 10:10 and stops and restarts at 10:15 and stops at 10:20.  The allowance time stops at 10:25, however provided that the OAT remains constant or increases and that no precipitation restarts after the allowance time of 10:25, the aircraft may takeoff without any further action up to 11:30.

c) On the other hand, if Type IV anti-icing fluid is applied with a start of application time of 10:00, OAT is 00C, light ice pellets mixed with freezing drizzle falls until 10:10 and stops and restarts at 10:30 with the allowance time stopping at 10:25 the aircraft may not takeoff, no matter how short the time or type of precipitation after 10:25, without being deiced and anti-iced if precipitation is present.

(3)  Operators with a deicing program approved in accordance with Title 14 of the Code of Federal Regulations (14 CFR) part 121, section 121.629, will be allowed, in the specified ice pellet conditions and corresponding outside air temperatures (OAT) listed in Table-1 “Ice Pellet Allowance Times Winter 2008-2009”, up to the specific allowance time listed in Table-1 after the start of the anti-icing fluid application to commence the takeoff with the following restrictions:

(a)  The aircraft critical surfaces must be free of contaminants before applying Type IV anti-icing fluid.  If not, the aircraft must be properly deiced and checked to be free of contaminants before the application of Type IV anti-icing fluid.

(b)  The allowance time is valid only if the aircraft is anti-iced with undiluted Type IV fluid.

(c)  Due to the shearing qualities of Type IV fluids with imbedded ice pellets, this allowance is limited to aircraft with a rotation speed of 100 knots or greater.

(d)  If the takeoff is not accomplished within the applicable allowance time in Table-1, the aircraft must be completely deiced, and if precipitation is still present, anti-iced again prior to a subsequent takeoff.  If the precipitation stops at or before the time limits of the applicable allowance time in Table-1 and does not restart the aircraft may takeoff up to 90 minutes after the start of the application of the Type IV anti-icing fluid provided the temperature on which the allowance time was based remains constant or increases.

(e)  A pre-takeoff contamination check is not required.  The allowance time cannot be extended by an internal or external check of the aircraft critical surfaces.

(f)  If ice pellet precipitation becomes heavier than moderate or if the light ice pellets mixed with other forms of allowable precipitation exceeds the listed intensities or temperature range, the allowance time cannot be used.

(g)  If the temperature decreases below the temperature on which the allowance time was based,

1.  And the new lower temperature has an associated allowance time for the precipitation condition and the present time is within the new allowance time, then that new time must be used as the allowance time limit.

2.  And the allowance time has expired (within the 90 minute post anti-icing window if the precipitation has stopped within the allowance time), the aircraft may not takeoff and must be completely deiced and, if applicable, anti-iced before a subsequent takeoff.

Table 8.  Ice Pellet Allowance Times Winter 2008-2009

|  | OAT -50 C or Warmer | OAT Colder Than -50 C |
| --- | --- | --- |
| Light Ice Pellets | 50 Minutes | 30 Minutes |
| Moderate Ice Pellets | 25 Minutes | 10 Minutes |
| Light Ice Pellets Mixed with Light or Moderate Snow | 25 Minutes | Operations Not Authorized |
| Light Ice Pellets Mixed with Light or Moderate Freezing Drizzle, or Light Freezing Rain (Operations not authorized below -10o C OAT) | 25 Minutes | 10 Minutes (Operations Not Authorized below -10o C OAT) |
| Light Ice Pellets Mixed with Light Rain (Operations not authorized below 0o C OAT) | 25 Minutes (Operations Not Authorized below 0o C OAT) | (Operations Not Authorized below 0o C OAT |

# Text boxes

Page 5

Page 6

Page 7

Page 8

Page 10

Page 14

Page 13

Page 17

Page 9

Page 11

Page 12

Page 18

Page 19

Page 24

Page 25

Page 26

Page 30

Page 31

Page 32

Page 27

Page 28

Page 21

Page 22

Page 15

Page 16

Page 23

Page 20

Page 33

Page 15

Page 29