MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A09681 | In-Flight Anomaly Number -- | Contractor Report Number T-052 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title NUMEROUS PIN HOLES IN PRIMER OVER ENTIRE SURFACE OF TANK |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (1) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE EXTERNAL TANK | PART# 82601000000 | SER/LOT# LWT-34 | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE EPOXY PRIMER | PART# MMS-K-719 | SER/LOT# 17-0218 | MANUFACTURER DESOTO |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode MSI - INSULATION | Cause MP - MFG-PRC |
| System TPS | Defect DD - DETACH | Material F - INSUL | Work Contact F. RAMSEY | Fail Date 10/28/1985 |
| Received at MSFC 11/19/1985 | Date Isolated -- | FMEA Reference 1.2.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text LWT-35 AND SUBS |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 01/03/1992 | CN RSLV SBMT 07/01/1986 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design B. DAVIS | Chief Engineer -- | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |
| Approval |
| Design B. DAVIS | Chief Engineer -- | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |
| PAC Assignee G. MILLER | PAC Review Complete GM | MSFC Closure Date 08/08/1986 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: MARS T-83805 PRIMER APPLIED TO LH2 TANK OF LWT-34 EXHIBITED A NUMEROUS AMOUNT OF PIN HOLES OVER THE ENTIRE SURFACE OF THE TANK. THE PRIMER MANUFACTURING LOT NUMBERS ARE 17-0218 (BASE) AND 17-0219 (CURING AGENT) |
| Contractor Investigation/Resolution R/A - BARE METAL IS TOUCHEDUP AS A STANDARD REPAIR. 11/19/85 GENERAL - THE PIN HOLES IN THE EPOXY PRIMER WAS FIRST REPORTED ON LH2 TANK, LWT-34, IN CELL "P." THE SAME PROBLEM (TO A LESSER EXTENT) WAS THEN OBSERVED ON LO2 AND LH2, LWT-33. IT WAS FURTHER NOTED THAT A SIMILAR PROBLEM HAD OCCURRED ON AN LO2 FEEDLINE WHICH WAS PRIMED IN THE COMMODITIES SHOP, BUILDING 103. ALL OF THE ABOVE OCCURRENCES WERE RELATED TO THE EPOXY PRIMER MANUFACTURING LOT NUMBERS 17-0218 (BASE) AND 17-0219 (CURING AGENT). A TEST OF THE RETAINED SAMPLE AT DESOTO DID NOT REVEAL THE SAME CHARACTERISTICS (PIN HOLES). HOWEVER, PARTICULATES IN EXCESS OF 25 MICRONS WERE NOTICED BY DESOTO; REQUIREMENT IS 12 MICRONS MAXIMUM. UPON NOTIFICATION BY DESOTO, MMC SUSPENDED THE USE OF THIS LOT OF MATERIAL AT ALL LOCATIONS, INCLUDING THE SUBCONTRACTOR LEVEL. A STUDY OF USAGE OF THE MATERIAL SHOWED THAT AT TANK LEVEL APPLICATION, LO2 AND LH2 TANK, LWT'S 29 AND UP, WERE AFFECTED AND AT THE COMPONENT LEVEL, LWT'S 28 AND UP WERE AFFECTED. INVESTIGATION - THIS CAPS WILL DETERMINE THE CAUSE AND/OR RELATIONSHIP BETWEEN THE PIN HOLES FOUND AT MICHOUD AND THE PARTICULATES NOTED AT DESOTO AND SUBSEQUENTLY AT MAF. VARIOUS TASKS HAVE BEEN ASSIGNED TO INVESTIGATE SPECIFIC AREAS AS FOLLOWS: TASK I THE QUALITY ENGINEERING LABS TO TEST LOTS 0218 AND 0219 AND IDENTIFY ANY CHANGES OR UNUSUAL CHARACTERISTICS IN THE BASE, CURE, AND SOLVENT COMPONENTS.. TASK II MARTIN MARIETTA LABS (BALTIMORE) TO ANALYZE LOTS 0218 AND 0219 USING VARIOUS ANALYTICAL TECHNIQUES AND COMPARE TO PRIMER DATA HISTORY AT MML. TASK III MATERIAL AND TPS ENGINEERING TO PERFORM TESTS TO DEVELOP ACCEPTANCE RATIONALE FOR AS-BUILT HARDWARE USING PRIMER LOT 17-0218 AND 0219. TESTS TO BE CONDUCTED AT CYROGENIC CONDITIONS AND TO INCLUDE A STUDY ON CORROSION IMPACTS. TASK IV QUALITY ENGINEERNG LAB AND MATERIALS ENGINEERING TO DEVELOP A TEST SCHEDULE WHICH WILL ASSESS THE CHEMICAL STABILITY OF LOTS 0218 AND 0219 WITH TIME. THE TEST SCHEDULE SHOULD INCLUDE THE NEW LOT OF EPOXY PRIMER WITH MANUFACTURING LOTS 17-4107 AND 4108. TASK V MATERIALS ENGINEERING, QUALITY ENGINEERING, QUALITY ENGINEERING LAB, AND RELIABILITY ASSURANCE TO REVIEW SHELF LIFE REQUIREMENTS FOR MMS-Y-719 PRIMER, AND INCLUDE ALL TPS MATERIALS. TAKS VI MATERIALS ENGINEERING TO MONITOR AND REPORT TESTS CONDUCTED BY DESOTO ON LOTS 0218 AND 0219 TO EXPLAIN DIFFERENCE AND/OR CORRELATION OF PIN HOLES AND PARTICLE EFFECTS NOTICED. 5/15/86 PRB STATUS - CAPS IS BEING PUBLISHED FOR CLOSURE. 7/8/86 PROBLEM CAUSE - THE MOST PROBABLE CAUSE FOR PINHOLES IN THE PRIMER IS A TRACE AMOUNT OF ORGANIC SILICONE INADVERTENTLY INTRODUCED TO THE BASE COMPONENT DURING NORMAL MANUFACTURING OPERATIONS AT DESOTO. THE CONTAMINANT MAY HAVE CONTRIBUTED TO PIGMENT AGGLOMERATION UPON AGING, AS NOTED BY OVERSIZED PARTICLES IN THE CURED FILM. FAILURE INVESTIGATION - THE LH2 TANK IS CLEANED AND EPOXY PRIMED IN CELL "P", BUILDING 131. AFTER THE PRIMING OPERATION, THE TANK IS VISUALLY INSPECTED FOR CONFORMANCE TO PI 3004 THE PINHOLES IN THE EPOXY PRIMER WERE FIRST NOTICED ON THE LH2 TANK, LWT-34. SIMILAR PROBLEMS WERE REPORTED ON THE LO2 AND LH2, LWT-33 AND AN LO2 FEEDLINE PRIMED IN THE COMMODITIES SHOP. ALL OF THE ABOVE DEFECTS WERE FOUND TO BE RELATED TO ONE LOT OF PRIMER WHICH WAS MANUFACTURING NUMBERS 17-0218 (BASE) AND 17-0219 (CURING AGENT). AN IN-DEPTH STUDY, COORDINATED BY RELIABILITY ASSURANCE AND CONDUCTED BY THREE LABORATORIES (MMC, MML, DESOTO), WAS PERFORMED ON THE SUSPECT PRIMER TO DETERMINE THE CAUSE AND EFFECT OF THE PINHOLES AND OVERSIZED PARTICULATES. RESULTS FROM DESOTO, INCORPORATED, SUGGESTS PIGMENT AGGLOMERATION WAS MOST PROBABLY DUE TO UNDISPERSED BETONE THICKENER EVEN THOUGH REGRINDING THE SUSPECT BASE MATERIAL SATISFACTORILY REDISPERSED THE PIGMENT AND THE BETONE. USING VARIOUS ANALYTICAL TECHNIQUES (SEM, ESCA, SRF, GS/MS), DESOTO FOUND NO SUBSTANTIAL DIFFERENCES BETWEEN THE STANDARD AND SUSPECT PRIMER COMPOSI- TIONS THEY COULD NOT ACCOUNT FOR THE PINHOLE PHENOMENON WHICH WAS OBSERVED EVEN IN THE REDISPERSEDSUSPECT BASE. MARTIN MARIETTA QUALITY EVALUATION LABS, USING SMALL AREA ELECTRON SPECTROSCOPY FOR CHEMICAL ANALY- SIS (ESCA), REPORTED FINDING SILICONE IN THE BOTTOM OF SEVERAL PINHOLES THIS WAS THOUGHT INSIGNI- FICANT IN CAUSING PINHOLING AS THE CURING AGENT CONTAINS AN AMINO-SILANE COUPLING AGENT, WHICH ALSO FORMS ORGANOSILANE BONDS TO THE SUBSTRATE. AT MMC'S REQUEST, DESOTO PROVIDED A DIFFERENT CURING AGENT WITHOUT THE AMINOSILANE COUPLER TO MIX WITH THE SUSPECT BASE. ONCE MIXED, THE RESULTANT FILM STILL DISPLAYED PINHOLES, AND VIA SMALL AREA ESCA, AGAIN INDICATED THE PRESENCE OF AN ORGANIC SILICONE WITHIN THE PINHOLE. EXTENSIVE TESTING BY MML SHOWED DIFFERENCES IN PARTICLE MORPHOLOGY AND A MUCH LOWER SOLUTION VISCOSITY FOR THE SUSPECT MIXED COMPONENTS, BUT DID NOT FIND CHEMICAL VARIATIONS IN COMPOSITION VERSUS THE STANDARD PRIMER. MML DETERMINED THAT, AT THE BOTTOM OF EACH PINHOLE, A THIN LAYER OF PRIMER RESIN CONTAINING DISPERSED CORROSION RETARDING PIGMENTS COVERED THE ALUMINUM SUBSTRATE A THOROUGH REVIEW OF THE DESOTO PROCESS AND RAW MATERIAL INSPECTION TESTING WAS CONDUCTED BY MMC MATERIALS ENGINEERING AND DESOTO PERSONNEL, WITH NO CONCLUSIVE INDICATIONS AS TO WHERE OR HOW THE CONTAMINATION WAS INTRODUCED. THE PRIMER APPLIED TO THE LH2 TANK, LWT-34, WAS EXTENSIVELY TESTED BY MATERIALS ENGINEERING ON THE FLIGHT HARDWARE AND TEST PANELS, WITH ACCEPTABLE RESULTS AS INDICATED BELOW: - FLIGHT HARDWARE TESTS WERE: - WET ADHESION TAPE TEST (REF MARS T-83805) - ELCOMETER TEST (REF MARS T-83805) - TEST PANELS TEST WERE: - WET ADHESION TAPE TEST - ELCOMETER TEST - LAP SHEAR - CRYOFLEX - BOND TENSION - FINGER FLEX - CORROSION TESTING THE SUSPECT EPOXY PRIMER BASE AND CURING AGENT AND RAW MATERIALS UNDERWENT THE FOLLOWING ANALYSES: - SCANNING ELECTRON MICROSCOPY (SEM) - ENERGY DISPERSIVE X-RAY SPECTROSCOPY (EDX) - X-RAY FLUORESENCE SPECTROSCOPY (XRF) - GAS CHROMATOGRAPHY/MASS SPECTROSCOPY (GS/MS) - SECONDARY ION MASS SPECTROSCOPY (SIMS) - ELECTRON SPECTROSCOPY FOR CHEMICAL ANALYSIS (ESCA) - CONVENTIONAL AND SMALL SPOT THE ONLY SIGNIFICANT RESULTS, USING SMALL SPOT ESCA, REVEALED A HIGH LEVEL OF SILICONE IN THE OF THE PINHOLE. SMALL SPOT ESCA. THIS ORGANIC SILICONE COULD NOT BE DETECTED BY OTHER TECHNIQUES AS IT IS PRESENT IN THE BASE, ONLY IN TRACE AMOUNTS. THIS CONTAMINATION IS BELIEVED TO HAVE BEEN INADVERTENTLY INTRODUCED DURING NORMAL MANUFACTURING OPERATIONS AT DESOTO AND MOST PROBABLY CONTRI- BUTED TO THE AGGLOMERATION OF PIGMENTS. CORRECTIVE ACTIONS - THE PRIMER SPECIFICATION, STM K-719, HAS BEEN UPDATED TO REFLECT THE FOLLOWING CHANGES: 1. ADD FINENESS OF GRIND CHECK AT VENDOR AND ON MMC INSPECTION TESTS. THIS TEST INDICATES THE ULTIMATE PARTICLE SIZE IN THE PRIMER. ACCEPTANCE CRITERIA IS 6 OR BETTER ON HEGMAN GAUGE. 2. ADD STABILITY ON AGING TEST AT VENDOR ONLY THIS IS AN ACCELERATED AGING TEST WHICH WILL HASTEN THE FORMATION OF PIGMENT AGGLOMERATION IF THE PRIMER SYSTEM IS UNSTABLE. ON SPRAYOUT AFTER TEST, THE CURED FILM SHALL NOT EXHIBIT DEFECTS OR OVERSIZED PARTICULATES. THE ABOVE CORRECTIVE ACTIONS HAVE BEEN IMPLEMENTED BY DESOTO, INCORPORATED, AND DEEMED ADEQUATE BY RELIABILITY ASSURANCE TO PRECLUDE THIS PROBLEM. ALL BARE METAL (PINHOLES) ARE TOUCHED UP AS A STANDARD REPAIR. CLEARANCE OF EFFECTIVITIES - BASED ON THE ACCEPTABLE TEST RESULTS FOR BOND TENSION AND CRYOGLEX, THE CONSTRAINTS ON AFFECTED ET'S (LWT'S 28 THROUGH 34) ARE LIFTED (REFERENCE INTEROFFICE MEMORANDUM 3571-86-02.) BASED ON THE CORRECTIVE ACTION IMPLEMENTED AT DESOTO TO PERFORM STABILITY (AGING) TESTS, RELIABILITY ASSURANCE DEEMS THESE ACTIONS ACCEPTABLE TO CLOSE THIS CAPS. RECOMMEND THIS PROBLEM REPORT BE CLOSED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A09681 | IFA# -- | Contractor RPT# T-052 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80974018409 | Asmnt Part Name LH2 TANK BARREL SOFI | Asmnt Serial/Lot# LWT-34 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MP - MFG-PRC | FAIL MODE MI - INSULATION |
| Asmnt FMEA 5.2.2.1 | Asmnt FM 1 | FMEA CSE B | FMEA SCSE 5 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |