Homework Assignment ---A

Superpave PG Grading Systems

Name:___________________________

Date:____________________________

- Use the Superpave software provided to determine the average 7 day high and 1-day minimum low pavement temperature and standard deviations for the following locations.

- Anchorage, Alaska

- Phoenix, Arizona

- Orlando, Florida

- Cincinnati, Ohio

- Boston, Massachusetts

- Select a PG grade to use in each of the above locations.  Use the maximum and minimum temperatures plus 2 standard deviations.

- What is the PG grade of the asphalt whose results are shown in Table 1?

TABLE 1.  Asphalt Cement Test Results.

| Properties | Asphalt No. 1 |
| --- | --- |
| Original Properties |  |
| Flash point temperature, oC | 257 |
| Viscosity at 135oC | 0.259 Poise |
| Dynamic shear G*/ sin  at 58oC G*/ sin  at 64oC G*/ sin  at 70oC | 0.74 1.05 1.90 |
| Rolling Thin Film Oven Aged Binder |  |
| Dynamic shear G*/ sin  at 58oC G*/ sin  at 64oC G*/ sin  at 70oC | 1.68 2.34 3.98 |
| Rolling Thin Film Oven and PAV Aged Binder |  |
| Dynamic shear G* sin  at 22oC G* sin  at 25oC G* sin  at 28oC | 2258 2987 3879 |
| Creep Stiffness Stiffness and m-value at -6oC Stiffness and m-value at -12oC Stiffness and m-value at -18oC | S m-value 225 0.359 259 0.310 289 0.287 |