| CABLE No. | LHC-4-F-B0792 |
| --- | --- |
| MFG. | 1/29/01 |
| OPERATOR: | Hugh Higley Evan Palmerston |

CABLE LOG SHEET

LBNL-SUPERCON-AFRD

# SUPERCONDUCTING MAGNET MATERIALS

OBJECTIVE: Mfg. LHC-HGQ Outer cable 46 st. Dwg.# 5525-MA-344389A

- STRAND INFORMATION -

| MANUFACTURER : | Furukawa LBNL SSC inventory |
| --- | --- |
| BILLET & Spool #: | See Respool Notes. |
| BNL avg. strand Ic@7T |  |
| COMPOSITION : | NbTi |
| STRAND Dia.. NOMINAL : | .648mm +/- .0025 | INSP. DIA..: | .6500mm avg. See respool notes. |
| Cu/SC RATIO NOMINAL : |  | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : | 1/13mm | DIRECTION : | RIGHT |
| SHARP BEND TEST : | Fail 2of5 to 5of5 See respool Notes. |
| LENGTH PER SPOOL : | 2,120m |

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | LHC-HGQ-OUTER FNAL Dwg.# 5525-MA-344389A |
| --- | --- |
| No. of STRANDS: | 46 |
| PITCH DIRECTION: | LEFT | PITCH LENGTH: | 109.5mm |
| PLANETARY RATIO: | -.57:1 |
| ROLLER ID #: | P25 & P26 | WIDTH: | 15.336 | ANGLE:: | .895 deg. |
| MANDREL ID #: | 20 | WIDTH: | 15.02mm | THICKNESS:: | .702 mm | Tip Ang.: | 4 deg. |
| LUBRICATION : | 4BR 100% drip. |
| STRAND TENSION: | 2.0kg. +/-.1kg | TURKS HEAD LOAD "SGM": | -68 kgm. |
| Nom. THICKNESS: | 1.146 mm +/- .006mm |
| Nom. WIDTH: | 15.400 mm +/- .025mm |
| Nom. ANGLE: | .707 deg. +/- 0.1deg. |

- FINISHED CABLE -

| FINISHED LENGTH: | 805m delivered as one length + 4m sample from each end 813m total. |
| --- | --- |
| Avg. THICKNESS: | 1.1464 mm |
| Avg. WIDTH: | 15.3979 mm |
| Avg. ANGLE: | 0.752 deg. Note entire run was at upper limit for angle many points were slightly over tolerance |

| RESIDUAL TWIST/Mtr.: | ~ Nearly flat < 10 deg. |
| --- | --- |
| ETCH for FILAMENT DAMAGE: | Some random single filaments damaged over entire surface of cable, with bundles of 30-80 filaments broken at both edges of the cable. 14” etched sample had 3 broken bundles at the minor edge and 1 broken bundle at the major edge. |

Notes:

This strand appeared to be much harder than the Alsthom strand with severe breaks in the filaments during sharp bend tests.

-4m samples from point and tail ends shipped to Arup Ghosh BNL 1/29/01.

- The balance of this run ~ 5-6 units or 1200m will be reserved pending test results from Arup Ghosh.

STRAND MAP							LBNL S/C #  L4F-B0792 & future cable?

Date : 1/16/01   H. Higley

| Strand Mfg. | Strand ID# | Length m | RESPOOL # | RESPOOL Length m | Insp. Dia. mm | Sharp Bend Failures | NOTES: |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Furukawa | 2-F-11008-A-05 | 2339 | 1 | 2120 | .6551 | 5 of 5 | Over Dia. Nom= .648 |
|  | 2-F-11003-F-03 | 7835 | 2 | 2120 | .6500 | 4 of 5 |  |
|  | “” |  | 3 | 2120 | .6500 |  |  |
|  | “” |  | 4 | 2120 | .6501 |  |  |
|  | 2-F-11001-A-06 | 13987 | 5 | 2120 | .6492 | 3 of 5 |  |
|  | “” |  | 6 | 2120 | .6490 |  |  |
|  | “” |  | 7 | 2120 | .6492 |  |  |
|  | “” |  | 8 | 2120 | .6493 |  |  |
|  | “” |  | 9 | 2120 | .6491 |  |  |
|  | “” |  | 10 | 2120 | .6492 |  |  |
|  | 2-F-11002-F-02 | 16779 | 11 | 2120 | .6505 | 4 of 5 |  |
|  | “” |  | 12 | 2120 | .6504 |  |  |
|  | “” |  | 13 | 2120 | .6505 |  |  |
|  | “” |  | 14 | 2120 | .6507 |  |  |
|  | “” |  | 15 | 2120 | .6506 |  |  |
|  | “” |  | 16 | 2120 | .6506 |  |  |
|  | “” |  | 17 | 2120 | .6506 |  |  |
|  | 2-F-11008-A-06 | 15864 | 18 | 2120 | .6490 | 5 of 5 |  |
|  | “” |  | 19 | 2120 | .6487 |  |  |
|  | “” |  | 20 | 2120 | .6489 |  |  |
|  | “” |  | 21 | 2120 | .6488 |  |  |
|  | “” |  | 22 | 2120 | .6489 |  |  |
|  | “” |  | 23 | 2120 | .6486 |  |  |
|  | “” |  | 24 | 2120 | .6487 |  |  |
|  | 2-F-11006-F-03 | 16565 | 25 | 2120 | .6503 | 2 of 5 |  |
|  | “” |  | 26 | 2120 | .6506 |  |  |
|  | “” |  | 27 | 2120 | .6504 |  |  |
|  | “” |  | 28 | 2120 | .6503 |  |  |
|  | “” |  | 29 | 2120 | .6509 |  |  |
|  | “” |  | 30 | 2120 | .6509 |  |  |
|  | “” |  | 31 | 2120 | .6503 |  |  |
|  | 2-F-11006-A-01 | 18484 | 32 | 2120 | .6558 | 5 of 5 | Over Dia. Nom= .648 |
|  | “” |  | 33 | 2120 | .6556 |  | Over Dia. Nom= .648 |
|  | “” |  | 34 | 2120 | .6558 |  | Over Dia. Nom= .648 |
|  | “” |  | 35 | 2120 | .6557 |  | Over Dia. Nom= .648 |
|  | 2-F-11011-A-03 | 28570 | 36 | 2120 | .6472 | 2 of 5 |  |
|  | “” |  | 37 | 2120 | .6481 |  |  |
|  | “” |  | 38 | 2120 | .6479 |  |  |
|  | “” |  | 39 | 2120 | .6479 |  |  |
|  | “” |  | 40 | 2120 | .6480 |  |  |
|  | “” |  | 41 | 2120 | .6484 |  |  |
|  | “” |  | 42 | 2120 | .6475 |  |  |
|  | “” |  | 43 | 2120 | .6479 |  |  |
|  | “” |  | 44 | 2120 | .6481 |  |  |
|  | “” |  | 45 | 2120 | .6478 |  |  |
|  | “” |  | 46 | 2120 | .6472 |  |  |
|  |  |  |  | Avg. Dia. = | .6500mm |  |  |