03E03/29/06

S303-03E.doc

Use on projects when specifying Pulverization as the method of road reconditioning. This also allows for additional Crushed Aggregate to be used to fulfill quantities.

Section 303. - ROAD RECONDITIONING

Material

303.02  Add the following:

Crushed aggregate	703.06

Construction Requirements

303.08  Pulverizing.  Delete the text and substitute the following:

Pulverize the existing asphalt pavement and/or base to the width and depth shown in the plans with an approved rotary milling machine to meet the following size requirements according to AASHTO T27:

| Sieve Designation | Percent Passing |
| --- | --- |
| 1 inch | 100 |
| ¾ inch | 85 – 100 |

Place and compact the pulverized material according to Subsection 301.05.  Compact each layer to at least 95 percent of maximum density.  Determine the inplace density and moisture content according to AASHTO T 310 or ASTM D2950.

Remove and dispose of unsuitable material prior to pulverizing as directed by the CO.  Replace unsuitable material with minor crushed aggregate.  Perform work according to Section 308.

Clean the compacted surface of all loose material, dirt, or other deleterious substances by approved methods.  Correct surface irregularities by scarifying the defective area and reworking the pulverized material.  Finish the pulverized surface according to Subsection 301.06.