96M06/12/06

S704-96M.doc

When select granular backfill is required, or when MSE walls are specified, include the following:

Section 704. – SOIL

When select granular backfill is required, include the following:

704.10  Select Granular Backfill.  Delete the text but retain Table 704-4, and substitute the following:

Furnish sound, durable, granular material free from organic matter or other deleterious material.  Conform to the following:

(a) Quality requirements.

(1) Gradation	Table 704-4

(2) Shear maximum angle of internal friction	34o min.

on the portion passing the 4.75 mm sieve,

AASHTO T 236

Note:  Compact samples for AASHTO T 236 to 95 percent of the maximum density determined according to AASHTO T 99 method C or D and corrected for oversized material according to AASHTO T 99, Note 7.

(3) Sodium sulfate soundness loss (5 cycles),	15% max.

AASHTO T 104

(4) Liquid limit, AASHTO T 89	30 max.

(b) Electrochemical requirements for MSE walls.

(1) Resistivity, AASHTO T 288	3000 Ω·cm min.

(2) pH, AASHTO T 289	5.0 to 10.0

(3) Sulfate content, AASHTO T 290	200 ppm max.

(4) Chloride content, AASHTO T 291	100 ppm max.

Note:  Tests for sulfate and chloride content are not required when resistivity is greater than 5000 ohm centimeters.

Use on all projects with MSE walls

Add the following Subsection:

704.13  Wall fill soils.

(a) Select wall backfill.  Furnish sound, durable, granular soil free from organic matter or other deleterious material (such as shale or other soft particles with poor durability).  Conform to the following:

(1) Quality requirements.

(a) Gradation	Table 704-6

(b) Shear maximum angle of internal friction	34o min.

on the portion passing the 4.75 mm sieve,

AASHTO T 236

Note:  Compact samples for AASHTO T 236 to 95 percent of the maximum density determined according to AASHTO T 99 method C.

(c) Sodium sulfate soundness loss (5 cycles)	15% max.

(d) Los Angeles abrasion, AASHTO T 96	50% max.

(e) Liquid limit, AASHTO T 89	30 max.

(f) Plastic index, AASHTO T 90	6 max.

(2) Electrochemical requirements

(a) Resistivity, AASHTO T 288	3000 (-cm min.

(b) pH, AASHTO T 289	5.0 to 10.0

(c) Sulfate content, AASHTO T 290	200 ppm max.

(d) Chloride content, AASHTO T 291	100 ppm max.

Notes:

(1) Tests for sulfate and chloride content are not required when pH is between 6.0 and 8.0 and the resistivity is greater than 5000 ohm centimeters.

(2) Electrochemical requirements are not applicable to geogrid-reinforced walls.  Refer to Subsection 720.01(k) for durability design requirements.

# Table 704-6

# Select Wall Backfill Gradation

| Sieve Size | Percent by Mass Passing Designated Sieve (AASHTO T 27 and T 11) |
| --- | --- |
| 100 mm | 100 |
| 75 mm | 75 – 100 |
| 4.75 mm | 30 – 75 |
| 0.075 mm | 0 – 15 |

(b) Wall backfill.  Furnish granular soil free from organic matter or other deleterious material (such as shale or other soft particles with poor durability) conforming to AASHTO soil classifications A-1, A-3, or A-2-4.  Remove all rock particles and hard earth clods larger than 300 millimeters in the longest dimension.

(c) Wall facing fill.  Furnish sound, durable, and pervious granular soil free from organic matter or other deleterious material (such as shale or other soft particles with poor durability) conforming to the following:

(1) Quality requirements.

(a) Gradation	Table 704-7

(b) Sodium sulfate soundness loss (5 cycles)	15% max.

(c) Los Angeles abrasion, AASHTO T 96	50% max.

Table 704-7

Wall Facing Fill

| Sieve Size | Percent by Mass Passing Designated Sieve (AASHTO T 27 and T 11) |
| --- | --- |
| 100 mm | 100 |
| 50 mm | 0 – 5 |