CONTROL OF STATIC AND DYNAMIC FIELD-ERROR (AC LOSS)

IN COS-( DIPOLES

E.W. Collings and M.D. Sumption

Laboratory for Applied Superconductivity and Magnetism

Department of Materials Science and Engineering

The Ohio State University

Columbus, OH 43210

U.S.A.

Supported

by

The U.S. Department of Energy

Division of High Energy Physics

under contract number

DE-FG02-95ER 40900

CONTROL OF STATIC AND DYNAMIC

FIELD-ERROR (AC LOSS) IN COS-( DIPOLES

INTRODUCTION

Copper-wound, DC-excited, cos-( dipoles can, in principal, be designed to deliver a very uniform transverse bore field (i.e. with small or negligible harmonic or multipolar field distortion).

But if the Cu is replaced by (a) superconducting strand that is (b) present in the form of Rutherford cable the extra magnetizations present within the windings cause distortions of the otherwise uniform bore field.

The magnetizations take two forms:

- static or persistent-current magnetization of the

superconducting filaments.

(b) dynamic magnetizations due to dB/dt-generated coupling currents between the strands of the cable, currents that also give rise to AC loss.

We discuss these effects and go on to show how they can be compensated and suppressed.

THE STATIC MAGNETIZATION

Referred to here is the intrinsic diamagnetism of the super-conductors shielding critical state.  The strand magnetization, Mstr, is proportional to the filament's critical current density, Jc, and effective diameter, deff. It is negligible at the magnet's maximum operating field.  But as the operating field decreases, Mstr increases and hence becomes disproportionately large at injection field.

Over the years Msat has been minimized by reducing deff.  As for the residue, several active and passive compensation schemes (involving the ferromagnetic elements Fe or Ni) have been devised.

DYNAMIC MAGNETIZATION

During field ramping circulating B-dot-generating coupling currents are another source of field error. As "AC loss" they contribute to the system's cryogenic loading, and by augmenting the transport current they reduce the stability of the magnet.

Both the "normal interstrand coupling currents" and widely-circulating, long-time-constant "Boundary Induced Coupling Currents" can be suppressed by increasing the interstrand contact resistance, an upper limit to which is imposed by stability (current-sharing) constraints.

The desired interstrand contact resistance is achieved by applying strand coatings or the introduction of an "insulating" core.

STATIC MAGNETIZATION

The half-height of the filament magnetization loop, or the magnetization in the shielding critical state, say, is

1

With the SSC strand it was found that with decreasing d, Mstr minimized at a d = 6 (m.  Proximity effect coupling then took over to produce deffs > 6 (m until the introduction of the dilute Cu-Mn matrix.

As an interesting aside, the Mn idea would not have surfaced had the filaments not been clad in a protective barrier film of Nb.  Niobium helps to launch NbTi's superelectrons into the surrounding Cu matrix.

As a second interesting aside, the apparent PE-suppressing action of Si additions to the Cu matrix is probably due to the absence of the Nb barrier in the NbTi/Cu-Si test strands.

The fine-filament NbTi/Cu strands still needed to be magnetically compensated, for which purpose various schemes have been suggested including:

(i) The placing of small pieces of ferromagnetic material within the bore of the magnet or in one of the coil wedges.

(ii) The inclusion of ferromagnetic material, in particular Ni, within the strand itself.

MAGNETIC COMPENSATION

The goal off magnetic compensation is to cancel out the shielding (i.e. field-increasing) magnetic moment resident in the superconducting windings.  On a per-unit-length basis this is achieved by setting:

2

where (s is the saturation magnetization of the ferromagnetic element and MSC is the magnetization of the SC. The As represent cross sectional areas.

Taking for pure Ni a (s of 507-521 emu/cm3 we found that SSC-type NbTi/Cu strand could be compensated at fields of 0.5-0.7 T by:

(1) applying an electroplated Ni coating of thickness 2.4-1.9 (m, or

(2) replacing some of the NbTi filaments with Ni ones, NbTi/Ni ratios 47/1-57/1.

Calculations of sextupole ratio at R = 1 cm by M. Green predicted substantial reductions in both cases.

MAGNETIZATIONS OF NbTi AND Nb3Sn

For NbTi we might expect a Jc of about 8,500 A/mm2 at 0.5 T, yielding for d = 6 (m a Jcd product of 5.10 in the units "A/mm2cm".

For a Nb3Sn strand we find a non-Cu Jc by taking some recently published Jc(B) data, scaling it to 2200 A/mm2 at 12 T and using a Kramer plot to extrapolate to 0.5 T.  The result was 46,300 A/mm2.  Taking a deff of 20 (m we obtain a Jcdeff product in the above units of 93.

Based on a Jcdeff 18X larger than that of NbTi, the magnetization of Nb3Sn, and its effect on injection field quality, becomes a serious problem.  Even so, ferromagnetic compensation of the Rutherford cable through the insertion of a Ni ribbon may be worth serious consideration.  For compensation we require

3

where

ANi is the c/s area of the Ni ribbon

fc is the packing factor of the standard cable

w and t are the width and thickness of the original cable

( is the nonCu/(Cu+nonCu) ratio for the strand

STRIP THICKNESS

Picture a cable of dimensions 1.5 cm x 0.2 cm wound with the above Nb3Sn strand; assume nonCu/(Cu+nonCu) = 0.5, and a packing factor of 90%.  Then the thickness, tNi cm, of a 1.3-cm wide strip of Ni (assume (s = 510 emu/cm3) that would provide magnetic compensation at 0.5 T is given by

4

which yields a tNi of 0.400 mm (i.e. "15.7 mils").

DEPLOYMENT AND PROPERTIES

OF THE STRIP

At half the thickness of a typical strand, the strip is fairly thick.  It may be preferable to employ three strips each of thickness 5 mils., sandwiching the cable between two of them and employing the other as a core.

Stabrite cables with stainless steel cores of thicknesses 0.5, 1, and 2 mils have already been successfully produced.

Such cores increase the effective interstrand contact resistance and by so doing suppress dynamic field error.

USE OF IRON INSTEAD OF NICKEL

With an Ms of 1745 emu/cm3 compared to Ni's 510 emu/cm3 the core thickness could be reduced by a factor 0.29 down to a value of 0.117 mm or 5 mils.

Such a core would not be unreasonable from the standpoints of fabrication and space utilization.

However, demagnetization considerations would require the field to be directed parallel to the surface of the cable rather than normal to it.

SUPPRESSION OF DYNAMIC MAGNETIZATION

-- CORE-TYPE CABLES

During excitation of the magnet the induced interstrand coupling currents (ICRs) cause both energy losses and distortions of the field at the beam line.  They are moderated by the magnitude of the interstrand contact resistance (ICR).  There are both "normal" ICRs that can be envisioned as looping around a half pitch of the cable, and "supercurrents" (Schmidt) otherwise known as Boundary Induced Coupling Currents (BICCs, Verweij) that can flow over a whole cable length and induce field errors that vary with the period of the twist pitch.  The latter are caused by a dB/dt or an ICR that varies sharply with distance along the cable (hence the term "boundary").

Coupling currents are suppressed by increasing the crossover and side-by-side ICRs -- Rc and Ra, respectively.  For a standard uncored LHC-type cable, it is generally agreed that Rc should be not less than 15±5 (( and Ra not less than 0.2 ((.

In the case of a cored cable, we have replaced Rc by a numerically equivalent Reff.

Rc (or Reff) is upper limited by a need to preserve interstrand current sharing and hence cable stability.

CHANGING THE ICR

Over the years various groups have modified ICR by:

(1) applying metallic or insulating coatings to the individual strands of the cable.

(2) inserting a metallic or insulating ribbon between the two layers of the cable

We ourselves have applied almost a dozen coatings and have measured AC loss in cables with cores of titanium, kapton, stainless steel, and nichrome-80.  The latter was used as a core for HTSC-2212/Ag cables, and we have settled on AISI 316 stainless steel ribbon as a core for cables wound with:

bare NbTi/Cu

stabrite-coated NbTi/Cu

Cu-stabilized Nb3Al

Nb3Sn.

The core can increase Rc by two orders of magnitude.

For Nb3Sn cables the effect of a core on AC loss is illustrated by the following pair of curves:

AC loss in uncored and cored Rutherford cables

wound with Nb3Sn strand and heat treated under

uniaxial compactions of 5, 10, and 20 MPa

CONTROL OF ICR AND STABILITY

The ICR of a fully cored cable will vary with processing conditions -- heat treatment temperature and level of uniaxial pressure and its application cycle.  For example:

Cable Type			HT Temp,	Reff,LHC,

deg.C		  ((

(1) stabrite NbTi		170			75

(2) Nb3Sn				660			36

(3) Nb3Al				750		 	 5

With cables (1) and (2) the Reffs were too high to ensure stability; however we have shown that they can easily be reduced (fine-tuned, in fact) by reducing the width of the core.

CONCLUDING DISCUSSION

I  MAGNETIZATION

High-Jc Nb3Sn strands will have correspondingly higher Jcs at injection field.  Assuming a Jc,4K,12T of 2200 A/mm2 and a Kim Jc(B) model, the Jc at 0.5 T is expected to be a factor of 22 higher, or 48.4 kA/mm2

Associated with this is critical-state magnetization proportional to Jc x deff. This magnetization has two consequences that have to be borne in mind during the development of strands with higher and higher Jc.

(1) Field Error

There is the magnetization itself which contributes multipolar field distortion of the dipole magnet.  Already at 2200 A/mm2 (12 T) and deff = 20 (m the calculated magnetization, viz. (M  = 3.93 x 102 emu/cm3, is equivalent to that contributed by 346 mT/s-generated coupling currents.

The question of compensation becomes very important. For passive ferromagnetic compensation the volume of added Ni would need to be 20% of the strand volume.

Line of equal dynamic and static 0.5 tesla magnetizations, the latter calculated on the basis of a 12 tesla Jc of 2200 A/mm2

Influence of effective filament diameter on a Sytnikov-calculated LHC-type cable equivalent ramp rate

(2) Flux-Jump Instability

The strand tends to become adiabatically flux-jump unstable.  It has been shown, in terms of the full hysteresis-loop height, (M, that the flux-jump threshold for adiabatic flux-jump instability can be expressed in the form

5

where t = T/Tc and the heat capacity of the SC is represented by (cT3.

At (M = 2.67 x 102 emu/cm3 this is already smaller than the above-mentioned loop height of 3.93 x 102 emu/cm3.

Clearly some extra dynamic or cryostabilization is playing a role, nevertheless the strand must be approaching its flux-jump stability limit.

The Significance of deff

As indicated above, the controlling low-field parameter is the MAGNETIZATION.

deff is just a secondary parameter associated with magnetization; furthermore it cannot be derived at low fields where Jc is immeasurably large in most laboratories.

Nevertheless its high-field-measured value is still a useful number from a processing standpoint, since it indicates very clearly the extent to which interfilament bridging has taken place.

II COUPLING CURRENTS IN CABLES

To suppress coupling in Nb3Sn Rutherford cable a core is needed.

In case the full width core produces too much Reff a fine tuning can be achieved by varying the width of the core.  This has already been demonstrated with stabrite cables.

By selecting Ni for the core partial magnetic compensation can be achieved.

BIBLIOGRAPHY

ENHANCEMENT AND CONTROL OF PROXIMITY EFFECT COUPLING BETWEEN FILAMENTS IN A NbTi MULTIFILAMENTARY COMPOSITE

PROXIMITY EFFECT SUPPRESSION

BY MEANS OF A Cu-Mn ALLOY MATRIX

100.	STABILIZER DESIGN CONSIDERATIONS IN FINE FILAMENT Cu/NbTi COMPOSITES,

E. W. COLLINGS, Adv. Cryo. Eng. (Materials) 34, 867 (1988).

111.	A CONDUCTOR WITH UNCOUPLED 2.5 (m DIAMETER FILAMENTS DESIGNED FOR THE OUTER CABLE OF SSC DIPOLE MAGNETS,

E. GREGORY, T. S. KREILICK, J. WONG, E. W. COLLINGS, K. R. MARKEN, Jr., R. M. SCANLAN, AND C. E. TAYLOR, IEEE Trans. Magn. 25, 1926-1929 (1989).

PROXIMITY EFFECT ENHANCEMENT

FOLLOWING THE NIOBIUM COATING OF THE FILAMENTS

182.	ENHANCED PROXIMITY EFFECT COUPLING DUE TO THE PRESENCE OF A Nb BARRIER IN FINE NbTi MULTIFILAMENTARY COMPOSITES

M. D. SUMPTION, H. LIU, E. GREGORY, AND E. W. COLLINGS, Adv. Cryo. Eng. (Materials) 42, 1175-1182 (1997).

198.	PROXIMITY EFFECT CURRENT STRENGTHS IN NbTi MULTIFILAMENTARY SAMPLES WITH AND WITHOUT Nb BARRIERS AND PROCESSED UNDER VARIOUS CONDITIONS

M. D. SUMPTION AND E. W. COLLINGS, IEEE Trans. Appl. Supercond. 7, 1117-1121 (1997).

209.	CRITICAL CURRENTS AND SUPERCONDUCTING BOUNDARY EFFECTS IN S-N-S MULTIFILAMENTARY COMPOSITES

M.D. SUMPTION, S. TAKÁCS, AND E.W. COLLINGS, Adv. Cryo. Eng. (Materials) 44, 843-850 (1998).

COMPENSATION OF "PERSISTENT-CURRENT"

(STRAND) MAGNETIZATION

117.	DESIGN OF COUPLED OR UNCOUPLED MULTIFILAMENTARY SSC-TYPE STRANDS WITH ALMOST ZERO RETAINED MAGNETIZATION AT FIELDS NEAR 0.3 T,

E. W. COLLINGS, K. R. MARKEN, Jr., AND M. D. SUMPTION, Adv. Cryo. Eng. (Materials) 36, 247-254 (1990).

123.	INTERFILAMENT AND INTRAFILAMENT MAGNETIZATIONS IN FINE-FILAMENT COMPOSITE STRANDS FOR PRECISION-DIPOLE MAGNET APPLICATIONS

E. W. COLLINGS, K. R. MARKEN, Jr., AND M. D. SUMPTION, Cryogenics 30, 48-55, (1990).

124.	DESIGN, FABRICATION, AND PROPERTIES OF MAGNETICALLY COMPENSATED SSC STRANDS

E. W. COLLINGS, K. R. MARKEN, Jr., M. D. SUMPTION, G. IWAKI, AND S. SAKAI, IEEE Trans. Magn. 27, 1787-1790 (1991).

128.	FERROMAGNETIC MATERIAL IN THE SUPERCONDUCTOR AND ITS EFFECT ON THE MAGNETIZATION SEXTUPOLE AND DECAPOLE IN THE SSC DIPOLES AT INJECTION

M. A. GREEN, E. W. COLLINGS, K. R. MARKEN, M. D. SUMPTION, in Supercollider 3, Plenum Press, 1991, pp. 365-373.

172.	MATERIALS SELECTION FOR FERROMAGNETIC COMPENSATION IN ACCELERATOR MAGNETS

E. W. COLLINGS AND M. D. SUMPTION, IEEE Trans. Appl. Supercond. 5, 408-411 (1995).

FLUX-JUMP STABILITY

218.	LOW FIELD FLUX JUMPING IN HIGH PERFORMANCE MULTIFILAMENTARY Nb3Al AND Nb3Sn COMPOSITE STRANDS

M.D. SUMPTION AND E.W. COLLINGS, IEEE Trans. Appl. Supercond. 9, 1455-1458 (1999).

# CONTACT RESISTANCE AND AC LOSS

175.	CONTACT RESISTANCE AND CABLE LOSS MEASUREMENT OF COATED STRANDS AND CABLES WOUND FROM THEM

M. D. SUMPTION, H. H. J. TEN KATE, R. M. SCANLAN, AND E. W. COLLINGS, IEEE Trans. Appl. Supercond. 5, 692-696 (1995).

216.	INFLUENCE OF STRAND SURFACE CONDITION ON INTERSTRAND CONTACT RESISTANCE AND COUPLING LOSS IN NbTi-WOUND RUTHERFORD CABLES

M.D. SUMPTION, E.W. COLLINGS, R.M. SCANLAN, A. NIJHUIS, H.H.J. ten KATE, S.W. KIM, M. WAKE, AND T. SHINTOMI, Cryogenics 39, 197-208 (1999).

AC LOSS IN NbTi CABLES

183.	MAGNETIC STUDIES OF AC LOSS IN PRESSURIZED RUTHERFORD CABLES WITH COATED STRANDS AND RESISTIVE CORES

E. W. COLLINGS, M. D. SUMPTION, R. M. SCANLAN, S. W. KIM, M. WAKE, AND T. SHINTOMI, Adv. Cryo. Eng. (Materials) 42, 1225-1232 (1997).

184.	CALORIMETRIC MEASUREMENTS OF THE EFFECT OF NICKEL AND STABRITE COATINGS AND RESISTIVE CORES ON AC LOSS IN ACCELERATOR CABLES UNDER FIXED PRESSURE

M. D. SUMPTION, R. M. SCANLAN, A. NIJHUIS, H. H. J. ten KATE AND E. W. COLLINGS, Adv. Cryo. Eng. (Materials) 42, 1303-1311 (1997).

193.	SUPPRESSION OF EDDY CURRENT LOSS IN BARE-COPPER RUTHERFORD CABLES USING STAINLESS STEEL CORES OF VARIOUS THICKNESSES

E.W. COLLINGS, M. D. SUMPTION, S. W. KIM, M. WAKE, AND T. SHINTOMI, Proc. 16thICEC/ICMC Conference, ed. by T. Haruyama, T. Mitsui, and K. Yamafuji, (Elsevier Science Japan, 1997) pp. 1767-1770.

200.	SUPPRESSION AND CONTROL OF COUPLING CURRENTS IN STABRITE-COATED RUTHERFORD CABLE WITH CORES OF VARIOUS MATERIALS AND THICKNESSES

E. W. COLLINGS, M. D. SUMPTION, S. W. KIM, M. WAKE, T. SHINTOMI, A. NIJHUIS, H. H. J. ten KATE, AND R. M. SCANLAN, IEEE Trans. Appl. Supercond. 7, 962-966 (1997)

226.	COUPLING CRRENT CONTROL IN STABRITE-COATED NbTi RUTHERFORD CABLE BY VARYING THE WIDTH OF A STAINLESS STEEL CORE

M.D. SUMPTION, E.W. COLLINGS, A. NIJHUIS, AND R.M. SCANLAN, Adv. Cryo. Eng. (Materials) 46 -- to be published

AC LOSS IN Nb3Sn AND Nb3Al CABLES

207.	AC LOSS AND CONTACT RESISTANCE IN Nb3Sn RUTHERFORD CABLES WITH AND WITHOUT A STAINLESS STEEL CORE

M.D. SUMPTION, E.W. COLLINGS, R.M. SCANLAN, A. NIJHUIS, AND H.H.J. ten KATE, Adv. Cryo. Eng. (Materials) 44, 1077-1084 (1998).

217.	CORE-SUPPRESSED AC LOSS AND STRAND-MODERATED CONTACT RESISTANCE IN A Nb3Sn RUTHERFORD CABLE

M.D. SUMPTION, E.W. COLLINGS, R.M. SCANLAN, A. NIJHUIS, AND H.H.J. ten Kate, Cryogenics 39, 1-12 (1999).

221.	AC LOSSES IN Nb3Sn RUTHERFORD CABLES WITH A STAINLESS STEEL CORE

F. SUMIYOSHI, S. KAWABATA, T. GOHDA, A. KAWAGOE, T. SHINTOMI, E.W. COLLINGS, M.D. SUMPTION AND R.M. SCANLAN, IEEE Trans. Appl. Supercond. 9, 731-734 (1999).

227.	AC LOSS AND CONTACT RESISTANCE IN COPPER-STABILIZED Nb3Al RUTHERFORD CABLES WITH AND WITHOUT A STAINLESS STEEL CORE

M.D. SUMPTION, R.M. SCANLAN, A. NIJHUIS, AND E.W. COLLINGS, EUCAS-99, Inst. of Physics, Ser. -- to be published

AC LOSS IN Bi:2212/Ag CABLES

212.	COUPLING CURRENT CONTROL IN RUTHERFORD CABLES WOUND WITH NbTi, Nb3Sn, AND Bi:2212/Ag

M.D. SUMPTION, R.M. SCANLAN, AND E.W COLLINGS, Proc. ICMC'98,  Topical Conference on AC Loss and Stability of Low and High-Tc Superconductors, Physica C 310, 291-295 (1998).

213.	AC LOSS PROPERTIES OF SOME Bi:2212/Ag RUTHERFORD CABLES AND A COMPARISON WITH THOSE OF CABLES WOUND WITH NbTi AND Nb3Sn

M.D. SUMPTION, R.M. SCANLAN, AND E.W. COLLINGS, Cryogenics 38, 1225-1232 (1998).

214.	LOW COUPLING LOSS CORE-STRENGTHENED Bi:2212/Ag RUTHERFORD CABLES

E..W. COLLINGS, M.D. SUMPTION, R.M. SCANLAN, L.R. MOTOWIDLO,  IEEE Trans. Appl. Supercond. 9, 758-761 (1999)

215.	Bi:2212/Ag-BASED RUTHERFORD CABLES: PRODUCTION, PROCESSING, AND PROPERTIES

R.M. SCANLAN, D.R. DIETERICH, E.W. COLLINGS, M.D. SUMPTION, L.R. MOTOWIDLO, Y. AOKI, AND T. HASEGAWA, Supercond. Sci. and Tech. 12, 87-96 (1999).

223.	DESIGN, PROCESSING, AND PROPERTIES OF Bi:2212/Ag RUTHERFORD CABLES

E.W. COLLINGS, M.D. SUMPTION, R.M. SCANLAN, D.R. DIETDERICH, L.R. MOTOWIDLO, R.S. SOKOLOWSKI, Y. AOKI, AND T. HASEGAWA, Advances in Superconductivity-XI, N. Koshizuka and S. Tajima, eds. (Springer-Verlag Tokyo 1999) pp. 1369-1372.