# Clay Mineral Identification Flow Diagram

## X-Rays of Oriented Aggregates

## Treated with	Electron Micrograph	X-rays of randomly

## Air Dried	ethylene glycol	Heated to 400o C	Heated to 550o C	if required	oriented powders	RESULT

~29Å	Expands to 31-32Å with	May disappear or give 24Å spacing.	Increase in intensity of 24Å spacing			Regularly interstratified

rational sequence of						chlorite-montmorillonite or

higher orders					cholorite-vermiculite (corrensite)

Expands but gives irrational sequence.	May give irrational sequence.	May give irrational sequences.  May show			Randomly interstratified

Peaks may be broad.		increase in intensity of 12-14Å peak			chlorite-montmorillonite

~14Å	No change	No change	Increase in intensity		060 near 1.54Å	Chlorite

060 near 1.50Å	Dioctahedral chlorite

No change or slight increase	Collapses to ~10Å	No change or slight additional collapse		060 near 1.54Å	Vermiculite

Slight collapse ~12Å	Additional collapse ~11Å		060 near 1.50Å	Dioctahedral vermiculite

Expands to 17Å	Collapses to ~10Å	No change or slight additional collapse		060 near 1.50Å	Montmorillonite

Collapses to ~10Å with	No change or slight additional collapse		060 near 1.52Å	Nontronite

very weak 5Å peak			060 near 1.54Å	Trioctahedral montmorillonite

or vermiculite

>10 - 14Å	No change - rational sequence	Collapses to ~10Å	Collapses to 10Å		060 near 1.54Å	Regularly interstratified

of higher orders					illite-vermiculite

No change	No change or slight increase in intensity		060 near 1.54Å	Regularly interstratified

illite-chlorite

No change - irrational sequence	Collapses to ~10Å	Collapses to 10Å		060 near 1.54Å	Randomly interstratified

illite-vermiculite

No change	No change or slight increase in intensity		060 near 1.54Å	Randomly interstratified

illite-chlorite

Expands to higher spacing	Collapses to ~10Å	Collapses to 10Å		060 near 1.50Å	Interstratified

illite-montmorillonite

060 near 1.54Å	Interstratified trioctahedral

illite-montmorillonite

No change	Slight collapse	Further collapse		060 near 1.50Å	Interstratified dioctahedral

illite-vermiculite

12 - 12.5Å	No change	Destroyed or reduced in intensity	Destroyed	Fibrous morphology	Check hkl's against standard	Sepiolite

10.5Å	No change	Destroyed - - may survive slightly	Destroyed	Fibrous morphology	Check hkl's against standard	Palygorskite

lower temperature

~10Å	Symmetrical - no change	No change	No change		060 near 1.50Å;	Illite (and/or mica),

check hkl's against	muscovitic,

standards for polymorphs	various polymorphs

060 between 1.51Å - 1.52Å	Glauconite or celadonite

5Å peak very weak	(Roscoelite if V bearing)

060 near 1.54Å	Bictite, various polymorphs

Unsymmetrical or slight shift either way	No change or slight sharpening			060 variable	Interstratified illite-montmorillonite

or illite-vermiculite

Expands to ~11Å	Collapses to ~7Å	Destroyed	Tubular morphology	060 near 1.49Å	Endellite

7Å	Increases in spacing or no change	Collapses to 7Å	Destroyed	Tubular morphology	060 near 1.49Å;	Halloysite

hk bands present

No change	No change	No change	Fibrous morphology	Check hkl's against standard	Chrysotile

Platy morphology	Check hkl's against standard	Antigorite

Destroyed	Platy morphology	060 near 1.49Å;	Disordered kaolinite

hk bands present;	(fireclay)

moderately broad 001's

060 near 1.54Å	Chlorite

(Check increase in intensity

of 14Å spacing)

060 near 1.50Å	Dioctahedral chlorite

(Check increase in intensity

of 14Å spacing)

Hexagonal  morphology	hkl's resolved	Kaolinite

Dickite

Nacrite

(Check against standard patterns)