MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A08606 | In-Flight Anomaly Number -- | Contractor Report Number P-049 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title PROPELLANT FEEDLINE FLANGE WAVINESS |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (5) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE EXTERNAL TANK | PART# 82601000000 | SER/LOT# LWT-16 | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE PROPELLANT FEED INST | PART# 80921011009-019 | SER/LOT# 0000045 | MANUFACTURER MMC |
| Test/Operation A - ATP | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode MV - EXT LEAK | Cause MP - MFG-PRC |
| System PROPULSION | Defect DA - ROUGH | Material P - SEAL | Work Contact C. CAMPBELL | Fail Date 07/09/1984 |
| Received at MSFC 09/10/1984 | Date Isolated -- | FMEA Reference 2.2.2 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom MV - EXT LEAK | Time Cycle -- |
| Effectivity Text NONE |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 12/02/1991 | CN RSLV SBMT 09/17/1985 | Defer Date -- | Add Date -- | R/C Codes 1 - DES -- -- |
| Assignee |
| Design W. COBB | Chief Engineer -- | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| Approval |
| Design W. COBB | Chief Engineer -- | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| PAC Assignee L. CUNNINGHM | PAC Review Complete -- | MSFC Closure Date 10/29/1985 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: DURING ATP, THE LH2 RECIR. LINE/UMBILICAL CONNECTION ON LWT-16 INDICATED A LEAK RATE EXCEEDING 4.0 SCIM. MAX ALLOWABLE IS .025 SCIM THIS WAS THE FIRST ATP USING THE SEAL CAVITY LEAK TEST. HOWEVER, THIS IS THE ELEVENTH SUCH FAILURE SINCE INTRODUCTION OF THIS METHOD AS A CONFIDENCE TEST BEGINNING WITH LWT-8 WITH ON,E EXCEPTION ALL LEAKS WERE ATTRIBUTED TO SECONDARY SEAL SEEPAGE |
| Contractor Investigation/Resolution 9/11/84 - FAILURE INVESTIGATION REVEALED A SCRATCH ON THE UMBILICAL FLANGE IN THE SECONDARY SEALING SURFACE. SUBSEQUENT LAPPING REVEALED A WAVINESS VIOLATION CONSISTING OF A RAISED RIDGE FROM .001 INCH TO .004 INCH. AFTER REWORK, THE JOINT WAS RETESTED SUCCESSFULLY. CAUSE: IS ATTRIBUTED TO UMBILICAL FLANGE WAVINESS. ADDITIONAL TESTING & INVESTIGATION IS CONTINUING.THIS FAILURE IS NOT CONSIDERED A LAUNCH CONSTRAINT TO LWT-8 BECAUSE THE LH2 RECIR LINE/UMBILICAL CONNECTION WAS TESTED SUCCESSFULLY BY THE OLD METHOD IN BUILDING 420 PRIOR TO THE INTRODUCTION OF THE ATP SEAL CAVITY LEAK TEST. THIS DECISION HAS BEEN COORDINATED WITH THE ET PROJECT OFFICE - ___G. P. BRIDWELL____ 12/17/84 - THIS PROBLEM IS NOT A CONSTRAINT TO FUTURE LAUNCHES SINCE THESE TESTS ARE RUN DURING ASSY & PRIOR TO APPLICATION OF INSULATION ALL LEAKS ASSOCIATED WITH THE LH2 RECIRCULATION LINE/ UMBILICAL CONNECTION ARE REPAIRED & RETESTED. ALL LEAKS ARE RESOLVED PRIOR TO APPLYING INSULATION & ACCEPTANCE TESTING - ___G. P. BRIDWELL 12-11-84___. 3/5/85 UPDATE FROM PRB DATED 2-25-85 - ENGR'G TESTS NEED TO BE COMPLETED. WILL ALSO DETERMINE IF PRACTICE OF USING SECONDARY SEALS WITH SCRATCHES (BY MRD) NEEDS TO BE REVIEWED. ECD FOR CAPS CLOSURE IS END OF MAY, 1985 (AFTER LWT-23). 4/30/85 UPDATE FROM PRB DATED 4-16-85 - TWO LEAKS ON LWT-23 WILL EXTEND COMPLETION APPROX 2 MONTHS. CURRENTLY THE SILVER COATED SEALS IN STOCK ARE BEING CHECKED FOR FLATNESS. WILL EVALUATE THE USE OF A TEFLON COATED SEAL. 6/5/85 UPDATE FROM PRB DATED 5-9-85 - THREE LEAKS ON LWT-23. TAPER PROBLEM WITH NAFLEX SECONDARY SEALS. WORKING WITH VENDOR TO TIGHTEN TOLERANCE ON SEALS. WILL REQUIRE SPEC CHANGE. ALSO, WILL CHANGE TO TEFLON COATED SEALS. ECD FOR CAPS CLOSURE EXTENDED 30 DAYS TO 7-17-85. 7/2/85 UPDATED FROM PRB DATED 6-20-85 - ALL CLOSURE ACTION TASKS HAVE BEEN COMPLETED EXCEPT ONE, WHICH IS AWAITING ECP APPROVAL. MMC EXPECTS TO HAVE CLOSURE TO MSFC BY 7-17-85. 8/15/85 PRB STATUS - ACTION TO GENERATE ECP TO TIGHTEN SEAL TOLERANCE REMAINS OPEN. ECD FOR CLOSURE HAS BEEN SLIPPED TO 8-31-85. 9/20/85 - SINCE THE INTRODUCTION OF THE SEAL CAVITY LEAK TEST FAILURE, OTHER RELATED PROBLEMS WERE DISCOVERED & IDENTIFIED THESE PROBLEMS WERE: SEAL DAMAGE; FLANGE WAVINESS DUE TO MACHINING; BOLT SHANKING; & NAFLEX SEAL TAPER. DISASSY OF THE AFFECTED JOINT ON LWT-16 REVEALED A SCRATCH ON THE UMBILICAL FLANGE IN THE SECONDARY SEALING SURFACE. IT IS NOT KNOWN DURING WHAT OPERATION THE SCRATCH WAS INFLICTED. SUBSEQUENT LAPPING OF THE FLANGE TO REMOVE THE SCRATCH REVEALED A WAVINESS VIOLATION CONSISTING OF A RAISED RIDGE FROM .001" TO .004" RUNNING ALONG THE INNER CIRCUMFERENCE OF THE FLANGE. THE UMBILICAL WAS LAPPED UNTIL ALL EVIDENCE OF THIS RIDGE WAS ELIMINATED CONSIDERING SUCCESSFUL REWORK & RETEST, THE CAUSE OF THE LEAK IS ATTRIBUTED TO THE UMBILICAL WAVINESS VIOLATION. THIS ISSUE HAS BEEN A TOPIC OF DISCUSSION WITH JSC, MSFC, ROCKWELL & MMC & HAS BEEN ADDRESSED ON CAPS P-046. IT HAS BEEN DETERMINED THAT MSRMNT TECHNIQUES AT MAF & PROPULSION LINE VENDORS HAVE NOT BEEN ADEQUATE; THEREFORE, A SATISFACTORY MSRMNT TECHNIQUE WILL BE ESTABLISHED BY MAF METROLOGY. AS AN INTERIM TECHNIQUE, THE METHOD ESTABLISHED BY ARROWHEAD PRODUCTS WILL BE UTILIZED UNTIL SUCH TIME AS METROLOGY MAKES RECOMMENDATIONS & MSRMNT EQUIPMENT IS PROCURED. MAF METROLOGY PROPOSED THE USE OF A MODIFIED GRANITE SURFACE PLATE WITH A PRECISION DIAL INDICATOR & HOLDING DEVICE A PROTOTYPE UNIT WAS FABRICATED & SUCCESSFULLY TESTED. AFTER MINOR MODIFICA- TIONS, PROCUREMENT WAS INITIATED FOR PRODUCTION UNITS PRESENTLY, THE TOOL IS IN USE BY MAF REC'G INSPECTION & ARROWHEAD PRODUCTS FOR FLANGE INSPECTION. FIVE RECIRCULATION LINES WERE INSPECTED FOR FLANGE WAVINESS VIOLATIONS. ALL FIVE PARTS FAILED WAVINESS CHECKS VIOLATIONS WERE MEASURABLE FROM .001" TO .003" (SPEC REQMNT IS +/- .0003"). THE PARTS WERE THEN LEAKED CHECKED USING A BLANK-OFF PLATE WHICH PRODUCED SECONDARY LEAKAGE ON FOUR OF THE FIVE UNITS. THE LINES WERE REWORKED BY LAPPING & A SCAR WAS ISSUED TO THE VENDOR. FAILURE HISTORY FOR THE CAVITY SEAL LEAK CHECK INDICATES THAT MOST PROBLEMS ARE TRACEABLE TO A WAVINESS NONCONFORMANCE. C/A FOR THE VENDOR (SCAR 3761-84-082) STATES THAT EQUIPMENT & PROCESSES USED ARE ADEQUATE TO PRODUCE REQ'D RESULTS, & PERSONNEL WILL BE REINSTRUCTED IN PROPER PROCEDURE. THIS IS EFFECTIVE AS OF 4-19-84. PROPULSION ENGR'G WILL IMPLEMENT A DWG CHANGE TO REQUIRE A SPECIFIC NUMBER OF WASHERS BE USED ON THROUGH-BOLT APPLICATIONS & ALLOW A REDUCTION OF WASHERS AS NECESSARY, TO ACHIEVE THE MINIMUM TWO THREAD PROTRUSION REQMNTS OF PI 2014. IN ADDITION, AN ANALYSIS WILL BE CONDUCTED ON BLIND-HOLE INSTALLATIONS TO DETERMINE WHICH CONNECTIONS WILL EXPERIENCE BOLT SHANKING DURING A WORST CASE TOLERANCE BUILD UP. IN THESE AREAS, ADDITIONAL WASHERS WILL BE ADDED TO AVOID SHANKING. THIS ACTION WILL ALSO BE ACCOMPLISHED BY DWG CHANGE. THREE LEAKS WERE EXPERIENCED AT THE ECO SENSOR BLANK-OFF PLATES. THESE LEAKS WERE ALSO ATTRIBUTED TO BOLT SHANKING. THIS PARTICULAR INSTALLATION WAS NOT A SUBJECT OF THE TOLERANCE ANALYSIS CONDUCTED BY ENGR'G. AS THE ECO SENSOR MOUNTING BOSS IS DELETED AT LWT-23, A DWG CHANGE WAS NOT IMPLEMENTED DUE TO THE LIMITED NUMBER OF EFFECTIVITIES A DCN WOULD SERVE &, THAT SHANKING COULD BE DETECTED DURING LEAK TESTING. FIVE LEAKS HAVE BEEN ATTRIBUTED TO NAFLEX SEALS WHICH EXHIBIT A TAPERED CONDITION IN THE SECONDARY SEALING SURFACE. SEALS ARE THICKER AT THE OUTER EDGE OF THE SECONDARY THAN AT THE INBOARD EDGE. THICKNESS VARIA- TIONS OF .001" TO .002" HAVE BEEN RECORDED (SPEC IS .001 MAX.). ONE GFP SEAL WAS WITHIN TOLERANCE, BUT ALLOWED SECONDARY LEAKAGE. THE SEALS EXHIBIT A POLISHED AREA AT THE OUTER PERIPHERY, OUTSIDE THE BOLT CIRCLE, INDICATIVE OF THE POINT AT WHICH SEATING OCCURS. THIS CONDITION PROVIDES VENTING AT ATMOSPHERE THROUGH THE BOLT HOLES. AT THIS TIME, THE VENDOR HAS NOT ISOLATED THIS DEFECT TO A PARTICULAR LOT OR DATE OF MFR. AT VENDOR REQUEST, TWO NAFLEX CONSUMERS WERE INFORMED OF THIS CONDITION (ROCKWELL/ROCKETDYNE) DISSECTION OF A DEFECTIVE SEAL REVEALED THE PROBLEM TO BE A VARIATION OF SUBSTRATE THICKNESS, NOT PLATING OR COATING THICKNESS. ALL FIVE SEALS WHICH FAILED LEAK TESTS ARE SILVER PLATED. IT IS THE OPINION OF RELIABILITY ASSURANCE THAT TEFLON COATED SEALS ARE MORE FORGIVING OF THE TAPERED CONDITION DUE TO THE TEFLONS THICKNESS & ABILITY TO COLD FLOW. IT IS ALSO BELIEVED THAT THE MAN- HOLE COVER LEAKS MAY HAVE BEEN THE RESULT OF SECONDARY TAPER. THE INCREASED TENSION PLACED ON THE SEAL BY REMOVAL & REINSTALLATION OF THE BOLTS MAY HAVE CAUSED SUFFICIENT YIELD IN THE TEFLON COATING TO STOP THE LEAKAGE. ADDITIONALLY, IT HAS BEEN DEMONSTRATED THAT RELATIVELY LOW TORQUE VALUES USED AT THE UMBILICALS WILL INCREASE THE AMOUNT OF LEAKAGE THROUGH THE BOLT PATTERN. RESOLUTION - SEAL CAVITY LEAK TESTING RESULTED IN NUMEROUS LEAKS ON LWT'S 16-23. THESE LEAKS WERE ATTRIBUTED TO SECONDARY SEALING PROBLEMS RELATED TO FLANGE WAVINESS, BOLT SHANKING & SEAL TAPER. FLANGE WAVINESS WAS RESPONSIBLE FOR LEAKAGE ON VEHICLES PRIOR TO LWT-18. THE VENDOR'S NEW PROCESS- ING HAS BEEN EFFECTIVE IN REDUCING MAF REJECTIONS FOR WAVINESS TO |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A08606 | IFA# -- | Contractor RPT# P-049 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80921011009-019 | Asmnt Part Name LH2 RECIR. LINE | Asmnt Serial/Lot# 45 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MP - MFG-PRC | FAIL MODE MV - EXT LEAK |
| Asmnt FMEA 2.6.1.1 | Asmnt FM 1 | FMEA CSE C | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |