Project Number:  AW 2226

Contract Number:  TW 0681

Date:  March 29, 1995

SPECIAL SPECIFICATION

SECTION 07160

BITUMINOUS DAMPPROOFING

Page

PART 1 - GENERAL

1.01	Description of Work

1.02	References

1.03	Submittals

1.04	Quality Assurance

1.05	Delivery, Storage, and Handling

1.06	Project conditions

PART 2 - PRODUCTS

2.01 	Manufacturers	4

2.02	Materials

2.03	Miscellaneous Materials

PART 3 - EXECUTION

3.01	Preparation

3.02	Application

3.03	Protection and Cleaning	6

3.04	Installation of Dampproof Protection Course	6

SPECIAL SPECIFICATION

SECTION 07160

BITUMINOUS DAMPPROOFING

PART 1 - GENERAL

1.01	DESCRIPTION OF WORK

This Section includes liquid, cold-applied asphalt emulsion dampproofing membrane.

1.02	REFERENCES

American Society of Testing and Materials (ASTM)

D41	Specification for Asphalt Primer Used in Roofing, Dampproofing, and Waterproofing

D412	Test Methods for Rubber Properties in Tension

D1227	Specification for Emulsified Asphalt Used as a Protective Coating for Roofing

D1621	Test Method for Compressive Properties of Rigid Cellular Plastics

D2240	Test Method for Rubber Property - Durometer Hardness

D2842	Test Method for Water Absorption of Rigid Cellular Plastics

E84	Test Method for Surface Burning Characteristics of Building Materials

E96	Test Methods for Water Vapor Transmission of Materials

1.03	SUBMITTALS

Submit the following in accordance with Conditions of Contract and Division 1, Section “Descriptive Submittals".

A.	Product Data: Include data substantiating that materials comply with specified requirements for each dampproofing material specified.

B.	Certification:  Provide certification of Contractor to perform work as specified in Section 1.04 B Quality Assurance.

C.	Provide certification stating that all products used are asbestos-free and lead paint-free.

1.04	QUALITY ASSURANCE

A.	Manufacturer Qualifications:  The manufacturer of the specified product shall have had in existence, for a minimum of 10 years, a program of training, certifying, and technically supporting a nationally organized Approved Contractor Program with annual re-certification of its participants.

B.	Installer Qualifications:  Engage an experienced Installer who is a Certified and Approved Installer to the manufacturer of the specified product and has completed a program of instruction in the use of a water-based elastomeric membrane for dampproofing a substrate.  Provide a certification from the manufacturer attesting to their Approved Installer status.

1.	At the discretion of the Sandia Delegated Representative (SDR), bids shall be accepted from Contractors other than a Certified and Approved Installer of the specified product.

2.	Said Installer shall provide the SDR with five job references where they have successfully coated a substrate with the specified product.

C.	Single-Source Responsibility:  Obtain primary dampproofing materials and primers from one source and by a single manufacturer.  Provide secondary materials only as recommended by manufacturer of primary materials.

1.05	DELIVERY, STORAGE, AND HANDLING

A.	Deliver the specified product in original, unopened containers with the manufacturer’s name, labels, product identification and batch numbers.

B.	Store the specified product as recommended by the manufacturer.

1.06	PROJECT CONDITIONS

A.	Substrate:  Proceed with dampproofing work only after substrate construction and penetrating work have been completed.

B.	Weather:  Proceed with dampproofing work only when existing and forecasted weather conditions will permit work to be performed in accordance with manufacturer's recommendations.

C.	Protection:  Precautions should be taken to avoid damage to any surface near the work zone due to the mixing and handling of the water-based elastomeric membrane.

PART 2 - PRODUCTS

2.01	MANUFACTURERS

A.	Dampproofing Membrane:  Provide HLM 5000 membrane, as manufactured by Sonneborn Building Products Division/ChemRex, Inc. or approved equal.

B.	Protection Board:  Provide DOW High Performance Underlayment Board or approved equal.

C.	Substitutions:  The use of other than the specified product will be considered providing the Contractor requests its use in writing to the SDR.  This request shall be accompanied by the following:

1.	Certificate of compliance from an approved independent testing laboratory that the proposed substitute product meets or exceeds the specified performance criteria, tested in accordance with the specified test standards

2.	Documented proof that the proposed substitute product has a five year proven record of sealing absorptive surfaces, confirmed by actual field tests and five successful installations that the SDR can verify.

2.02	MATERIALS

Cold-Applied, Asphalt Emulsion Dampproofing:  Non-combustible, single-component asphalt and water emulsion coating, compounded to penetrate substrate and build to moisture-resistant coating.  Membrane shall be capable of being applied to vertical and horizontal surfaces.

Provide emulsified asphalt semimastic, containing fibers other than asbestos, complying with ASTM D1227, Type II or IV, and the following performance criteria:

1.	Tensile Properties:  ASTM D412

a.	Tensile Strength:  125 psi (862 kPa) min.

b.	Average Elongation:  600%

2.	Hardness: Shore A - 35 max., ASTM D2240

3.	Moisture Vapor Transmission:  0.15 perm inches, ASTM E96

2.03	MISCELLANEOUS MATERIALS

A.	Primer:  Asphalt primer complying with ASTM D41, for asphalt-based dampproofing.

B.	Protection Boards: Minimum 1/2 inch (13 mm) thick extruded polystyrene foam insulation boards for backfilling operations that comply with the following requirements:

1.	Water Absorption:  1.7 % by volume, ASTM D2842.

2.	Compressive Strength:  15 psi (103 kPa), ASTM D1621.

3.	Permeance:  2 Perms, ASTM E96.

4.	Flame Spread:  Maximum 25, ASTM E84.

PART 3 - EXECUTION

3.01	PREPARATION

A.	Surface Preparation:  Clean substrate of projections and substances detrimental to work to provide smooth substrate to receive dampproofing.  Comply with manufacturer’s recommendations.

B.	Fill voids, seal joints, and repair all cracks in the substrate to achieve a smooth, level surface as required by the SDR.

C.	Install separate flashings and corner protection stripping as recommended by prime materials manufacturer, where indicated to precede application of dampproofing.  Comply with details shown and manufacturer's recommendations.  Give particular attention to requirements at building expansion joints, if any.

D.	Prime substrate as recommended by manufacturer.

E.	Protection of Other Work:  Do not allow liquid and mastic compounds to enter and clog drains and conductors.  Prevent spillage and migration onto other surfaces of work, by masking or otherwise protecting adjoining work.

3.02	APPLICATION

A.	Comply with manufacturer's recommendations, except where more stringent requirements are indicated or specified and where Project conditions require extra precautions or provisions to ensure satisfactory performance of work.

B.	Apply dampproofing to all exterior below-grade surfaces of exterior underground walls in contact with earth or other backfill and where space is enclosed on opposite side.

C.	Apply vertical dampproofing down walls from finished grade line to top of footing, extend over top of footing, and down a minimum of 6 inches (150mm) over outside face of footing.  Extend 12 inches (300mm) onto intersecting walls and footings, but do not extend onto surfaces that will be exposed to view when project is completed.

D.	Semimastic Grade:  Brush or spray apply a coat of dampproofing membrane at a rate of 5 gal/100 sq. Ft (2 L/sq. m), to produce a uniform, dry thickness.  Application thickness shall be between 75-90 wet mil thickness (45-55 dry mil thickness) on horizontal surfaces or approximately 40 wet mil thickness (25 dry mil thickness) to vertical surfaces.

Care must be taken to obtain a pin-hole free continuous film.  Multiple coats are acceptable to achieve the required thickness.

3.03	PROTECTION AND CLEANING

Protect exterior, below-grade dampproofing membrane from damage until backfill is completed.  Remove overspray and spilled materials from surfaces not intended to receive dampproofing.

3.04	INSTALLATION OF DAMPPROOF PROTECTION COURSE

Install protection course of type indicated over completed-and-cured dampproofing treatment.  Comply with dampproofing materials manufacturer's recommendations for method of support or attachment of protection materials. Support with spot application of plastic cement where not otherwise indicated.

END OF SECTION