# X-Ray Reflectivity as a Probe of the Structure of Thin Lubricating Films

Sunil K. Sinha

University of California San Diego La Jolla, CA 92093-0319  and Los Alamos Natl. Laboratory, Los Alamos, NM 87105

and

J. Johnson and A.Erdemir

## Energy Technology Divn., Argonne Natl. Laboratory, Argonne, IL 60439

ABSTRACT:

X-Ray specular reflectivity can be used to probe the electron density profile of a liquid or solid film on a surface as well as films confined between two solid surfaces. Information can thus be obtained regarding layering, roughness and changes induced by pressure or temperature. Off-specular scattering can be used to study the topology of the roughness and in-plane structure which might develop. We shall illustrate with applications we have made to two systems, namely ultra-low friction Carbon films developed at Argonne Natl. Laboratory, and liquid films confined between silicon plates.