Fractional Factorial Technique to Predict Welding Current in Gas Metal Arc Welding

# Masood Aghakhani

Abstract

During research on Gas Metal Arc Welding (GMAW) of aluminum, it was observed that the welding current was affected by any change in wire feed rate, arc voltage, nozzle-to-plate distance, torch angle, and welding speed. To determine accurately the welding current for any set of these parameters, a mathematical model has been presented. The model was developed using a two-level fractional factorial design and its adequacy was tested by the analysis of variance technique. The estimated and observed values of the welding current have been shown on a scatter diagram and the interaction effects of different parameters involved have been presented in graphical forms. These results can be utilized for determining accurately the heat input into the workpiece from which reliable predictions can be made about the mechanical and the metallurgical properties of welded joints.

Keywords: Fractional Factorial Technique; Welding Current; Gas Metal Arc Welding; and Aluminum.

Introduction

Gas Metal Arc (GMA) also known as Metal Inert Gas (MIG) is the most often used welding process for welding aluminum and it’s alloys (Ref. 1). In MIG welding, the wire electrode used is thin (0.5-1.6 mm diameter) and consequently the wire feed speed is high. To achieve self-adjustment of arc at high-speed rates, it is essential to use power sources with flat or nearly flat V-I (volt-ampere) characteristics. For welding with such a power source, the wire feed rate has been given by Halmoy (Ref. 2) by the following equation:

Where

| W | = wire feed rate |
| --- | --- |
| I | = welding current |
| l | = electrode stick-out |
| a | = area of cross section of the wire |

--------------------------------------------------------------------------------------------------------

Masood Aghakhani, Assistant Professor in Production Engineering (Welding Technology), College of Engineering, University of Razi, Kermanshah-67149, Iran.

E-Mail: aghakhani@razi.ac.ir & aghakhanim@yahoo.com

| ( | = constant of proportionality for anode or cathode heating |
| --- | --- |
| ( | = constant of proportionality for electrical resistance heating |

It is reported that for aluminum ( = 0.75 mm/A-sec and ( is negligible (Ref. 3), thus reducing Halmoy's equation for GMAW of aluminum to:

or, in other words, the welding current (I) is directly proportional to the wire feed rate (W). However, during prolonged investigations on GMAW of aluminum, it was observed that the welding current (I) was not only affected by the changes made in wire feed rate (W), but arc voltage (V), nozzle-to-plate distance (N), torch angle ((), and welding speed (S) also affected the welding current accordingly. Welding current affects the metal transfer (pinch effect α ) and the amount of heat input into the weld pool and consequently it affects the bead shape as well as the metallurgical and mechanical properties. To avoid any serious effects on the analysis of results of erroneous assumption that the welding current is only proportional directly to wire feed rate, it was found imperative to determine accurately the welding current as affected by different welding parameters.

This paper reports the development of a mathematical model, based on practical observations, made during gas metal arc welding of aluminum to estimate accurately the welding current as affected by welding parameters.

Plan of Investigation

To achieve the desired aim, the planning for investigations were carried out in the following steps:

| 1. | Selection of a mathematical model; |
| --- | --- |
| 2. | Design of experiments; |
| 3. | Selection of useful limits of the welding parameters viz.; wire feed rate (W), arc voltage (V), nozzle-to-plate distance (N), torch angle (() and welding speed (S); |
| 4. | Developing a design matrix; |
| 5. | Conducting experiments as per designed matrix; |
| 6. | Estimation of the coefficients of the equation; |
| 8. | Checking the adequacy of the model; |
| 9. | Testing the significance of the regression coefficients and arriving at the final form of the mathematical model; |
| 10. | Presenting the estimated and observed data on a scatter diagram; |
| 11. | Presenting the significant interactions between different parameters in graphical form; |
| 12. | Analysis of results; and |
| 13. | Conclusions. |

Selection of the Mathematical Model

It was observed from the preliminary experiments that the welding current (I) was affected by wire feed rate, arc voltage, nozzle-to-plate distance, torch angle, and welding speed within the limits employed for the study. Under these conditions, the response function could be expressed as

Assuming a linear relationship and taking into account all possible two-factor interactions, it could be written as:

Where I is the estimated welding current and  are the coefficients of the polynomial to be determined.

Design of Experiments

The design of experiment, that is, the decision to use different values of different parameters for conducting a particular experiment was based on the fractional factorial design, which is a standard statistical tool to investigate the effects of a number of parameters on the required response. In addition, interactions between two or more parameters can be evaluated, which is not possible with the conventional experimental approach since in that approach all parameters other than being studied are held constant.

For calculating the main and interaction effects of five variables W, V, N, (, S at two levels, a half fractional factorial design was selected. This design gave  weld runs to fit an equation and was sufficient for the evaluation of coefficients.

Selection of Useful Limits of Welding Parameters

On the basis of preliminary experiments conducted using 1.6 mm diameter wire with argon shielding, it was found that for proper bead configurations the wire feed rate, arc voltage, nozzle-to-plate distance, torch angle, and welding speed were required to be kept between 6.1 m/min and 7.6 m/min, 24 V to 29 V, 15 mm to 20 mm, 80 deg to 100 deg and 25 cm/min to 40 cm/min respectively. These limits were adhered to throughout the investigations reported here.

For the ease of recording and processing of the observed data, upper and lower levels of welding parameters were coded as + 1 and -1, respectively by using the following relationship:

Two levels of welding parameters, their levels, units, and coded values are given in Table 1.

# Table 1-Welding parameters and their limits.

| Parameter | Unit | Symbol | Coded Value | Coded Value |
| --- | --- | --- | --- | --- |
|  |  |  | Low (-1) | High (+1) |
| Wire Feed Rate | m/min | W | 6.1 | 7.6 |
| Arc Voltage | volts | V | 24.0 | 29.0 |
| Nozzle-to-Plate Distance | mm | N | 15.0 | 20.0 |
| Torch Angle | deg |  | 80.0 | 100.0 |
| Welding Speed | cm/min | S | 25.0 | 40.0 |

Design Matrix

The design matrix evolved to conduct sixteen experiments is given in Table 2 and is based on the method suggested elsewhere (Refs. 4, 5).

# Table 2-Design Matrix

| S. # | W | V | N |  | S (-WVN) |
| --- | --- | --- | --- | --- | --- |
| 1 | + | + | + | + | - |
| 2 | - | + | + | + | + |
| 3 | + | - | + | + | + |
| 4 | - | - | + | + | - |
| 5 | + | + | - | + | + |
| 6 | - | + | - | + | - |
| 7 | + | - | - | + | - |
| 8 | - | - | - | + | + |
| 9 | + | + | + | - | + |
| 10 | - | + | + | - | - |
| 11 | + | - | + | - | - |
| 12 | - | - | + | - | + |
| 13 | + | + | - | - | - |
| 14 | - | + | - | - | + |
| 15 | + | - | - | - | + |
| 16 | - | - | - | - | - |

Experimentation

Employing a mechanized welding system, experiments were conducted as per the conditions set in the design matrix of Table 2. Welding current observations were made by making weld runs of 25 cm length on 13 mm thick plates of aluminum. The power source used was a three-phase transformer cum full-wave rectifier unit having a flat V-I (volt-ampere) characteristics with a current capacity of 425 A at 60% duty cycle and an infinitely variable OCV (open circuit voltage) of 12-48 V in two ranges. A 1.6 mm diameter NG-6 filler wire (Al-5%Mg) with argon as shielding gas at a flow rate of 30 l/mm was used.

Sixteen weld runs were made using the conditions set in the design matrix but to avoid any systematic error in experimentation, the sets of conditions were chosen at random. The recorded values of welding current (I) for two sets of experiments are given in Table 3.

Table 3-Recorded values of welding current

| S.# | Trial No. | W | V | N | ( | S | Welding Current ------------------------ I1 I2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1 | + | + | + | + | - | 260 270 |
| 2 | 2 | - | + | + | + | + | 240 240 |
| 3 | 3 | + | - | + | + | + | 260 260 |
| 4 | 4 | - | - | + | + | - | 220 220 |
| 5 | 9 | + | + | + | - | + | 280 290 |
| 6 | 10 | - | + | + | - | - | 245 245 |
| 7 | 11 | + | - | + | - | - | 270 270 |
| 8 | 12 | - | - | + | - | + | 240 240 |
| 9 | 13 | + | + | - | - | - | 290 290 |
| 10 | 14 | - | + | - | - | + | 240 240 |
| 11 | 15 | + | - | - | - | + | 280 280 |
| 12 | 16 | - | - | - | - | - | 240 240 |
| 13 | 5 | + | + | - | + | + | 290 290 |
| 14 | 6 | - | + | - | + | - | 240 250 |
| 15 | 7 | + | - | - | + | - | 260 260 |
| 16 | 8 | - | - | - | + | + | 245 245 |

Evaluation of Coefficients of the Model

To determine the regression coefficients of the selected model, following formula (Ref. 4, 5) based on the method of least squares was used:

where:

| Xji | = value of a factor or interaction in coded form. |
| --- | --- |
| Yi | = average value of the response parameter, that is, the welding current in this case |
| N | = number of the observations. |
| k | = number of the coefficients of the model. |

A matrix designed to apply this formula to calculate different coefficients is given in Table 4.

# Table 4-Design matrix to calculate different coefficients

| S.# | Trial No. | b0 | b1 | b2 | b3 | b4 | b5 | b6 | b7 | b8 | b9 | b10 | b11 | b12 | b13 | b14 | b15 | Yavg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1 | + | + | + | + | + | - | + | + | + | - | + | + | - | + | - | - | 265 |
| 2 | 2 | + | - | + | + | + | + | - | - | - | - | + | + | + | + | + | + | 240 |
| 3 | 3 | + | + | - | + | + | + | - | + | + | + | - | - | - | + | + | + | 260 |
| 4 | 4 | + | - | - | + | + | - | + | - | - | + | - | - | + | + | - | - | 220 |
| 5 | 9 | + | + | + | + | - | + | + | + | - | + | + | - | + | - | + | - | 285 |
| 6 | 10 | + | - | + | + | - | - | - | - | + | + | + | - | - | - | - | + | 245 |
| 7 | 11 | + | + | - | + | - | - | - | + | - | - | - | + | + | - | - | - | 270 |
| 8 | 12 | + | - | - | + | - | + | + | - | + | - | - | + | - | - | + | - | 240 |
| 9 | 13 | + | + | + | - | - | - | + | - | - | - | - | - | - | + | + | + | 290 |
| 10 | 14 | + | - | + | - | - | + | - | + | + | - | - | - | + | + | - | - | 240 |
| 11 | 15 | + | + | - | - | - | + | - | - | - | + | + | + | - | + | - | - | 280 |
| 12 | 16 | + | - | - | - | - | - | + | + | + | + | + | + | + | + | + | + | 240 |
| 13 | 5 | + | + | + | - | + | + | + | - | + | + | - | + | + | - | - | + | 290 |
| 14 | 6 | + | - | + | - | + | - | - | + | - | + | - | + | - | - | + | - | 245 |
| 15 | 7 | + | + | - | - | + | - | - | - | + | - | + | - | + | - | + | - | 260 |
| 16 | 8 | + | - | - | - | + | + | + | + | - | - | + | - | - | - | - | + | 245 |

The estimated coefficients of the variables and their interactions computed using the above relationship are given in Table 5.

# Table 5-Coefficients of the model

| b0 | b1 W | b2 V | b3 N | b4 ( | b5 S | b6 WV | b7 WN | b8 W( | b9 WS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 257.2 | 17.8 | 5.3 | -4.1 | -4.1 | 2.8 | 2.2 | -0.9 | -2.2 | 0.9 |

| b10 VN | b11 V( | b12 VS | b13 N( | b14 NS | b15 (S |
| --- | --- | --- | --- | --- | --- |
| 0.3 | 1.6 | -1.6 | -2.8 | 0.3 | 2.8 |

Using these coefficients, the complete model, in coded form, can be expressed as follows:

### Checking the Adequacy of the Model

The adequacy of the model was determined by the analysis of variance technique. The regression coefficients were determined by the method of least squares, from which the F-ratio for the polynomial was found. The F-ratio of the model was compared with the corresponding F-ratio from the standard tables and it was found that the model was adequate within 95% level of confidence, thus justifying the use of assumed polynomial. Details of analysis of variance are given in Table 6.

# Table 6-Details of analysis of variance

| Response | Degrees of Freedom for | Variance of Response | Standard Deviation of Coefficients | Variance of Adequacy | `F' Ratio Model | `F' Ratio Table | Adequacy of Model |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | at (10,16,0.05) | Whether |
| Welding Current | 16 10 | 9.375 | 0.765 | 7.50 | 0.80 | 2.49 | Yes |

Checking the Significance of the Coefficients of the Model

To eliminate the statistical insignificant terms of the model, if any, it is essential to check the significance of each of the coefficient and to do that Student's `t'-test was employed. It was found that the coefficients of all the main effects and WV, W(, N(, and (S interactions were significant. The rest of the coefficients could be dropped conveniently. Thus the final model with only the statistically significant coefficients in the coded form is given as:

Results

A large number of observations were taken under different sets of parameters within the limits investigated and the corresponding estimated values of welding current were determined from the model. The observed and the estimated values were then represented in a graphical form as a scatter diagram shown in Fig. 1.

The significant interactions viz. WV, W(, N( and (S as deduced from the model are shown in Figs. 2-5.

Analysis of Results

Fig. 1 shows that the estimated and the observed values of the welding current are scattered close to 45( lines, passing though the origin, indicating an almost perfect fit of the developed empirical model. Furthermore, the analysis of results show that the increase in the levels of W, V, and S resulted in the corresponding increase in welding current whereas, the increase in the levels of N, and ( proved to be otherwise.

Effect of Wire Feed Rate (W)

Wire feed rate is the most important parameter affecting the welding current. An increase in welding current from 6.1 to 7.6 m/min resulted in the increase in welding current by a magnitude of 34.36 amperes. This increase in welding current with the increase in wire feed rate is to keep the wire feed rate and burn off rate in equilibrium.

Effect of Arc Voltage (V)

The second largest increase in welding current is caused by arc voltage by a magnitude of 10.6 amperes when it is varied from 24 to 29 volts. The increase in welding current with the increase in arc voltage indicates the rising characteristics of the welding arc.

Effect of Nozzle-to-Plate Distance (N)

The welding current decreased by approximately eight amperes with the increase in nozzle-to-plate distance from 15 to 20 mm. This is due to the fact that as the value of ‘N’ is increased, the arc length also increases momentarily thereby increasing the arc voltage but the same is restored to its original value due to the self-adjustment of the welding arc. This increases the stick-out and hence the amount of I2R heating. Increase in the preheating of the stick-out reduces the welding current slightly so that the equilibrium between wire feed rate and the burn off rate is maintained.

Effect of Electrode/Torch Angle (()

The increase in the torch angle from 80( to 100( resulted in the decrease of welding current by approximately 8 amperes. The reason for this could be explained due to the fact that as the electrode angle increases the effective arc length increases, and hence a decrease in welding current is observed.

Effect of Welding Speed (S)

The increase in welding speed from 25 to 40 cm/min resulted in the increase in welding current by approximately 6 amperes. This could be due to the fact that at low welding speed the arc is very close to the deposited metal and since the melting point of the filler wire is quite low, the current required to maintain the burn off rate equilibrium, is less and when the welding speed is increased, the heat content of the arc is reduced and hence to maintain the burn off rate equilibrium, the welding current requirement increases.

Effect of Interactions

Fig. 2 shows that welding current increased with the increase in wire feed rate. The increase in welding current was 6 and 12 amperes for low and high values of wire feed rate when, arc voltage was varied from 24 to 29 volts. This shows that the interaction of W&V is highly significant at higher levels.

Fig. 3 shows that welding current increased with the change in the torch angle from 80( to 100(, backhand to forehand. The increase in the welding current was just 3 amperes compared to 12 amperes for low and high values of wire feed rate.

Fig. 4 shows that welding current decreased with the change in torch angle from backhand to forehand position. Effect of torch angle on welding current at low levels of wire feed rate is quite insignificant compared to the variation of 14 amperes at the high level of nozzle-to-plate distance.

Fig. 5 shows that welding current decreased with the increase in torch angle from 80( to 100(. There is no effect of welding speed on the welding current at low level of torch angle however; it became quite significant at the high level of torch angle. The figure also shows that there is hardly any effect of torch angle of 80( on welding current. The welding current decreased by 12 amperes at 40 cm/min & forehand angle of 100(.

Conclusions

| 1. | In GMAW, the welding current is affected not only by the wire feed rate but also by the arc voltage, the nozzle-to-plate distance, the electrode/torch angle and the welding speed. |
| --- | --- |
| 2. | An empirical model was developed to estimate the welding current by correlating these parameters for GMAW of aluminum. |
| 3. | At low wire feed rates, the effect of arc voltage on welding current was negligible. However, it increased enormously at higher feed rates. |
| 4. | Increase in nozzle-to-plate distance resulted in the decrease in welding current possibly due to the increase in arc length. |
| 5. | The increase in arc voltage resulted in the increase in welding current indicating a rising volt-ampere characteristic of the welding arc. |
| 6. | The increase in electrode/torch angle resulted in the decrease in welding current. |
| 7. | The increase in welding speed resulted in the increase in welding current. |

### Acknowledgement

The author wishes to thank the research vice-chancellor of the University of Razi, for granting permission to publish this paper.

### References

| 1. | Walser, H.; and Zehnder, M. 1981. Practical and technological aspects of inert gas welding of aluminum and its alloys. Colloquium on Aluminum and Its Alloys. Porto (Portugal): IIW, Paper I-8. |
| --- | --- |
| 2. | Halmoy, E. 1979. Wire melting rate, droplet temperature and effective anode melting potential. Proc. of International Conference on Arc Physics and Weld Pool Behavior--Paper 44. Welding Institute, London, pp. 241-249. |
| 3. | Trindade, H. 1982. M.Sc. thesis. School of Industrial Science, Cranfield, Cranfield Institute of Technology. |
| 4. | Adler, Yu.P.; Markova, E.V.; and Granovsky, Yu.P. 1975. The design of experiments to find optimal conditions, Moscow: Mir Publishers. |
| 5. | Box, G. E. P.; Hunter, W.G.; and Hunter J. S. 1978. Statistics for experimenters: An introduction to design data analysis and model building, New York: John Wiley & Sons. |
| 6. | Montgomery, D.C. 1991. Design and analysis of experiments, Third Edition, New York: John Wiley & Sons. |