##### DEPARTMENT OF TRANSPORTATION

PERFORMANCE ORIENTED PACKAGE TESTING

CERTIFICATION

Performed by:

Good Results Testing

1 PHIMSA Ave

Nowhere, Maryland 20590

555-555-5555

Testing Performed for:

Big Guy Chemical Company

2 Old RSPA Way

Anyplace, Maryland 20590

555-555-1234

Design Qualification Testing of a

##### UN 5M2 Water Resistant Multiwall Paper Bag

###### 5M2/Y25.5/S/**

USA/+QQ2350

** Is to be replaced by the

year of manufacture

Signature of Certifying Individual

(Must be listed on the Laboratory’s Approval)

Section 2

Package Description

# Multiwall Bag: See Appendix A for drawing

| Manufacturer: | Big Bag Company, Springfield, MD |
| --- | --- |
| Bag Style: | Sewn Open Mouth Flat Tube Sack |
| Part Number: | UN Bag 12345 |
| Outer dimensions cm (in): | 61.6 x 30.8 (24.0 x 12.0) |
| Number of Plies | 5 plies 3 paper, 2 plastic |
| Tensile Strength – Machine Direction |  |
| Tensile Strength – Cross Direction |  |
| Burst strength | 257 lb |
| Tare Weight | 230 grams |

Basis Weights and Thicknesses of Plies:

| Ply | Material | Location | Thickness | Basis Weight |
| --- | --- | --- | --- | --- |
| 1 | Natural kraft | Outer most | 1.1 mm | 50.1 |
| 2 | Natural kraft | 2nd from outside | 0.7 mm | 51.2 |
| 3 | HDPE | Outer plastic | 0.05 mm |  |
| 4 | Natural kraft | Inner most paper | 0.8 mm | 49.9 |
| 5 | HDPE | Inner most | 0.05 mm |  |

# Closing Methods:

| Sealing Method for the bag | Top: Heat sealed (11 mm) plastic inner liner and folded over and sewed outer paper closure Bottom: Factory heat sealed, folded over and sewn. |
| --- | --- |
| Stitches per inch | 4 stitches per inch top and bottom |
| Filler cord type | None |

# Additional Test Information

| Overall Tare Weight of Package | 0.23 kg |
| --- | --- |
| Thread material | Polyester |
| Thread strength | 50 lb tensile |
| Test Contents: | Clay granules, 6mm average particle diameter |
| Weight of Package as Tested: | 25.65 kg |

Section 3 - TESTING

Test Descriptions and Results

Package Preparation – For All Testing

The packages were filled to their maximum gross mass.

Drop Test –

Test Method: 49 CFR 178.603

Number of Packages Tested – 3

Drop Height – 1.2 meters

Conditioning

The packages were conditioned to 50% +/-2 percent relative humidity, and at a temperature of 23 degrees C+/-2 degrees C for 24 hours in accordance with 49 CFR 178.603(c).  Drop testing was conducted approximately 2 minutes after removing the test package from the conditioning chamber.

# Results

| Bag Number | Package Weight | Orientation | Result |
| --- | --- | --- | --- |
| 1 | 25.65 | Flat on wide face | Pass – No damage |
| 2 | 25.66 | Flat on wide face | Pass – No damage |
| 3 | 25.64 | Flat on wide face | Pass – No damage |
| 1 | 25.65 | Flat on end | Pass – No damage |
| 2 | 25.66 | Flat on end | Pass – No damage |
| 3 | 26.64 | Flat on End | Pass – no damage |

Pass/Fail Criteria -

A package is considered to successfully pass the drop tests if for each sample tested: There is no damage to the outer most ply likely to adversely affect safety during transport, there is no leakage of the filling substance from the inner packaging and any discharge from a closure is slight and ceases immediately after impact.

# Vibration Standard

Packages Tested – 3

Test Method: 49 CFR 178.608 on a rotary vibration table.

Duration: 1 Hour

Frequency: 3.6 Hz (216 rpm)

Results

| Package 1 | No damage |
| --- | --- |
| Package 2 | No damage |
| Package 3 | No damage |

Pass/Fail Criteria -

A packaging passes the vibration test if there is no rupture or leakage from any of the packages. No test sample should show any deterioration which could adversely affect transportation safety or any distortion liable to reduce packaging strength.

Section 4

Drawings of Packaging Components

Paper Bag

APPENDIX

Test Equipment and Instrumentation

| Instrument or Equipment | Manufacturer | Model Number | Serial Number | Calibration Date |
| --- | --- | --- | --- | --- |
| Drop Tester |  |  |  |  |
| Gram Scale |  |  |  |  |
| Electronic Scale |  |  |  |  |
| Pressure Gauge |  |  |  |  |
| Vibration Table |  |  |  |  |
| Add other equipment as needed. |  |  |  |  |

# Text boxes

u

n

30.8 cm

61.6 cm