### Guidelines cabling of first 66 meter PIT-504 NbSn wires

## General

- Applicable cable log sheet			LHC-5-P-00767,a,b,c

# Mandril tip					#39 C (the very same I hope)

- Recommended connection scheme
  1. preferred Cu leader : a few meters ????? 
  2. PIT-504 scrap wires from R-labelled spools, to be cut to 11 meter long pieces
      (see table 2)
  3. PIT-504 good wire from A-labelled spools, each 66-67 meter long 
      (see table 1), preferably positioned on the planetary wheel in the logical order
       A1, A2,……, A35.
  4. Cu tailer

- The ends that are tape-marked ‘punt’ on the A-spools must be connected to the (PIT-504-scrap) leader wires.

- Please mark the first 20 cm of 2 good PIT-504 wires with black and red ink and report their respective spool number. This enables us to trace the wires and their respective manufacturing origin.

Proposed program.

- start cabling Cu leader

- if OK, continue with about 5-6 meters of the PIT-504-scrap leader

- stop cabling at this point, cut the cable for microscopic inspection of the cross-section. Points for inspection:
1. core: position and no folds, eventually correct core tension
2. symmetric deformation of both layers
3. no cross-over or other problems
At this point please call me by phone (+31 53 4778584) and send me pictures of the cross section by e-mail. We’ll discuss the results on-line.

- if OK, continue and complete the cabling run

## Return shipment

- e-mail mrs. D. van der Vegte-Morsink (see attached shipping letter on the box) who will arrange the return shipment

use the same box for the cable spool and all the wire spools with or without remaining wire pieces.

- Table 1. Spool labelling of the good PIT-504 NbSn wires

| spool number: | measured length |
| --- | --- |
|  | [m] |
| A1 | 66.9 |
| A2 | 67.1 |
| A3 | 67.0 |
| A4 | 67.1 |
| A5 | 66.8 |
| A6 | 67.0 |
| A7 | 66.7 |
| A8 | 66.5 |
| A9 | 66.7 |
| A10 | 66.6 |
| A11 | 66.6 |
| A12 | 66.9 |
| A13 | 66.8 |
| A14 | 66.8 |
| A15 | 66.8 |
| A16 | 67.1 |
| A17 | 67.1 |
| A18 | 66.5 |
| A19 | 66.5 |
| A20 | 66.8 |
| A21 | 67.2 |
| A22 | 66.8 |
| A23 | 66.8 |
| A24 | 66.6 |
| A25 | 66.7 |
| A26 | 66.7 |
| A27 | 66.7 |
| A28 | 66.8 |
| A29 | 66.8 |
| A30 | 66.7 |
| A31 | 66.9 |
| A32 | 66.6 |
| A33 | 66.7 |
| A34 | 66.7 |
| A35 | 66.6 |

# The wire ends are taped to the spools. The end with the tape-label ‘punt’ must be connected to the leader.

# Table 2. Spool labelling of the scrap PIT-504 NbSn wires

| spool label | piece label | piece length | units of 11 meter |
| --- | --- | --- | --- |
|  |  | [m] | [-] |
| R1 | A | 21 | 1 |
|  | B | 8.5 | 0 |
|  | C | 35 | 3 |
| R2 | A | 53 | 4 |
|  | B | 11 | 1 |
| R3 | A | 13 | 1 |
|  | B | 16 | 1 |
|  | C | 11.5 | 1 |
| R4 | A | 11.5 | 1 |
|  | B | 16.3 | 1 |
|  | C | 18.7 | 1 |
| R5 | A | 19 | 1 |
|  | B | 15.7 | 1 |
|  | C | 13 | 1 |
| R6 | A | 22 | 2 |
|  | B | 5.5 | 0 |
|  | C | 8 | 0 |
| R7 |  | 64 | 5 |
| R8 |  | 61 | 5 |
| R9 |  | 51 | 4 |
| R10 |  | 35 | 3 |
| Total |  |  | 37 |