HIGH PERFORMANCE CONCRETE QUESTIONNAIRE

Version: 7-15-03

State: _Utah________________

1.	Which of the following changes have been made to your concrete specifications                    in the last 10 years?

Check those that apply:

|  | Changes Made in Last 10 Years | Included in Current Specifications |
| --- | --- | --- |
| Use HPC-low permeability concrete | Allowed by special |  |
| Use HPC-high strength concrete | Allowed by special |  |
| Allow admixtures | Yes | Yes |
| Concrete strengths | Yes | Yes |
| Bridge deck curing |  |  |
| Deck finishing requirements |  |  |
| Limit cement/alkali content |  |  |
| Testing and acceptance requirements | Yes | Yes |
| Heat of Hydration required for cement |  |  |
| Chloride testing of hardened concrete |  |  |
| Lightweight concrete |  |  |
| Self-consolidating concrete (SCC) in use | Yes | No |
| Flowing concrete in use | Same as SCC |  |
| Epoxy coated reinforcing steel used | Yes | Yes |
| Stainless Steel reinforcing steel used | Allowed by special | No |
| Stainless clad reinforcing steel used | “ | “ |
| Specify air void parameters (spacing factor and/or specific surface) | No | No |

2.	Current Concrete Specifications:

| Class of Concrete | Air Content % | Max. W/C Ratio | Slump (in.) | Cement Type | Min. Cement Content (lb/cy) | Max. Cement Content (lb/cy) | Maximum Aggregate Size (in.) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Prestressed | 5 – 7.5 | 0.44 | 7 | I,II,III | 611 |  | No 4 |
| Decks | “ | “ | 1-3.5 | II | “ |  | 1 |
| Parapets | “ | “ | “ | II | “ |  | “ |
| Substr./General | “ | “ | “ | II | “ |  | “ |
| Paving | “ | “ | .5-3.5 | II | “ |  | 1.5-#4 |
| Latex Hydraulic Cement Concrete | By Special | By Spec. | By Spec. | By Spec. | By Spec. | By Spec. | By Spec. |
| Silica Fume Concrete | By Special | By Spec. | By Spec. | By Spec. | By Spec. | By Special | By Spec |

Highest compressive strength used for prestressed concrete girders: 8500 psi_________

Compressive concrete strength used for decks: _3650-4000 psi__________________

- All states have experienced some of the below concrete distresses.  To what extent has your State experienced these (Rank from 1 to 5 with 1=rare and 5=often):

| Type of Distress | 1 | 2 | 3 | 4 | 5 |
| --- | --- | --- | --- | --- | --- |
| Corrosion of Reinforcing Steel |  |  | x |  |  |
| Sulfate Attack | x |  |  |  |  |
| Alkali-silica Reactivity |  | x |  |  |  |
| Freezing and Thawing |  |  | x |  |  |
| Cracking (girders, substructure, pvmt) |  |  | x |  |  |
| Deck Cracking (Early age < 5 years) |  |  |  | x |  |
| Overload |  | x |  |  |  |
| Poor Construction Quality |  | x |  |  |  |

- Construction Requirements:

Workability Requirements:

| ADMIXTURES AND SLAG USAGE |  |  |
| --- | --- | --- |
| ADMIXTURE/SLAG | Non-Aggressive Environment | Aggressive Environment | ELEMENTS WHERE USED All, D, G, P, F, CP, DS* |
|  | YES | NO | YES | NO |  |
| Air-Entraining | x |  | x |  | All |
| Retarding | x |  | x |  | G |
| Accelerating |  |  |  |  |  |
| Water Reducing (Normal) | x |  | x |  | All |
| Water Reducing (High Range) | x |  | x |  | G |
| Water Reducer + Retarder | x |  | x |  | G |
| Water Reducer + Accelerator |  |  |  |  |  |
| Viscosity Modifying Admixture | x |  | x |  | G, Posssible all |
| Silica Fume |  |  |  |  |  |
| Fly Ash, Class F | x |  | x |  | All |
| Fly Ash, Class C |  |  |  |  |  |
| Fly Ash, Class N |  |  |  |  |  |
| Metakaolin |  |  |  |  |  |
| Rice Hull Ash |  |  |  |  |  |
| Other Ash Materials |  |  |  |  |  |
| Bark Ash |  |  |  |  |  |
| Bottom Ash |  |  |  |  |  |
| Pet Coke Ash |  |  |  |  |  |
| Slag |  |  |  |  |  |
| Latex |  |  |  |  |  |
| Corrosion Inhibitors |  |  |  |  | D |

*Key: Deck(D); Girder(G); Pier(P); Footing(F); Concrete Pile(CP); Drilled Shaft(DS)

| ADMIXTURE TYPE & SLAG | RANGE % (Wt. Of Cement Replaced) |
| --- | --- |
| Fly Ash | 20 |
| Slag |  |
| Silica Fume | Allowed if included in mix design |
| Metakaolin |  |
| Rice Hull Ash |  |
| Other Ash Materials |  |

Yes			No

Is water allowed to be added at the job site?		___x____		______

Are air-entraining admixtures allowed to be

added at the job site?				__x_____		______

Are accelerators added at the job site?		_______		______

Are there any special finishing requirements?	_______		__x___

Explain: ____________________________________________________

___________________________________________________________

Are there any time constraints between finishing

and applying curing?				______		___x__

Explain: (Minimum and Maximum Times)_________________________

___________________________________________________________

| CURING REQUIREMENTS |
| --- |
| Structural Element | Exist. Spec. Y/N | Curing Comp. Y/N | Fog Mist Y/N | Wet Burlap Duration | ERL LB/SF/HR | Cure Time (Days) |
| Deck | Y | Y | Y | 7 days |  |  |
| SF Overlay |  |  |  |  |  |  |
| Latex Conc. Overlay |  |  |  |  |  |  |
| Dense Conc. Overlay |  |  |  |  |  |  |
| Paving | Y | Y | Y |  |  |  |
| Shotcrete |  |  |  |  |  |  |
| Shotcrete With SF |  |  |  |  |  |  |
| Massive Element |  |  |  |  |  |  |

Key :  ERL= Evaporation Rate Limit (LBS/SF/HR)

Any construction requirements for reducing evaporation?

Yes __Y____			No ______

How and how often is evaporation rate measured?

According to ACI charts, contractor responsible for frequencies.

- Has fiber-reinforced concrete been specified for bridge decks or overlays and paving (either steel or plastic fibers)(Indicate R = Regular and E = Experimental.)

Bridge decks:  Yes ___x___	No ______   	Fiber Type ___Steel_________

Overlays:	Yes ___x___	No ______	Fiber Type ___Steel_________

Paving:	Yes ______	No ______	Fiber Type _________________

- Identify concrete cover requirements:

| MINIMUM CONCRETE COVER REQUIREMENTS |
| --- |
| STRUCTURAL ELEMENT | COVER (in.) |
|  | Non-Aggressive Environment | Aggressive Environment |
| Decks – Top | 2” | 2” |
| Decks – Bottom | 1” | 1” |
| Reinforced Concrete Beams | 2” | 2” |
| Prestressed Concrete Beams - CIP | 2” | 2” |
| Prestressed Concrete Beams - Precast | 1.5” | 1.5” |
| Substructure – Piers | 2” | 2” |
| Substructure – Abutments | 2” | 2” |
| Substructure - Footings | 2” | 2” |

| REQUIRED REINFORCING STEEL |
| --- |
| STRUCTURAL ELEMENT | TYPE REINFORCING STEEL BS, ECS, GS, SS, SCD, MMFX |
|  | Non-Aggressive Environment | Aggressive Environment | Experimental Use Only |
| Decks – Top | Ecs,gs | Ecs,gs | Ss,scd, mmfx |
| Decks – Bottom | Ecs,gs | Ecs,gs | Ss,scd, mmfx |
| Reinforced Concrete Beams | Ecs,gs | Ecs,gs | Ss,scd, mmfx |
| Prestressed Concrete Beams, CIP | Ecs,gs | Ecs,gs | Ss,scd, mmfx |
| Prestressed Concrete Beams, Precast | Ecs,gs | Ecs,gs | Ss,scd, mmfx |
| Substructure – Piers | Ecs,gs | Ecs,gs | Ss,scd, mmfx |
| Substructure – Abutments | Ecs,gs | Ecs,gs | Ss,scd, mmfx |
| Substructure - Footings | Ecs,gs | Ecs,gs | Ss,scd, mmfx |

Key:  BS = Black Reinforcing Steel; ECS = Epoxy Coated Reinforcing Steel; GS = Galvanized Reinforcing Steel; SS = Stainless Reinforcing Steel; SCD = Stainless Clad Reinforcing Steel; MMFX = MMFX Microcomposite Steel Rebar

7.	Is there a limit on the percent of alkali allowed in the cement?

Yes __X____			No ______

8.	Are aggregates tested for reactivity?

Yes __X____		No ______

Pit Acceptance

How many sources of aggregates?

9.	Indicate specification permeability requirement limits for: by Special Provision

| Structural Element | Coulombs |
| --- | --- |
|  | Non-Aggressive Environment | Aggressive Environment |
| Bridge Decks | 100-1000 | 100-1000 |
| Prestressed Concrete Members |  |  |
| Substructure Elements |  |  |
| Pavements |  |  |

10 (a):  What QC/QA tests do you specify?

| Fresh Concrete | Hardened Concrete |
| --- | --- |
|  | Tests |  | Tests |
| Slump | X | Compressive Strength | X |
| Spread |  | Air/Void System |  |
| Unit Weight |  | Chloride Permeability |  |
| Air Content | X | Maturity |  |
| Water Content |  | Freeze/Thaw |  |
| W/CM | x | Shrinkage |  |
|  |  | ASR |  |

10 (b): What are your acceptance criteria for cracks?

Depends on the item.

10 (c): Do you specify pre-construction mock-ups?  		If yes, provide details.

Yes, for new mixes or special items.  Has been required for all HPC work.

10 (d): Do you specify design properties at 28 days or 56 days or some other duration?

Yes, 28 day

10 (e): Do you allow 4x8 cylinders for compressive strength tests?

Yes

10 (f): What types of end-caps do you specify/allow – Sulfur, Neoprene, Ground Ends?

Neoprene

10 (g): Do you specify match-cured cylinders?

No

10 (h): How do you enforce/monitor wet-water curing?

Field Inspecitoin

10 (i): Do you require warrantees against defects – e.g. bridge deck cracking?  	No If yes, provide details.

10 (j):  What is your experience/evaluation/specification regarding the Microwave Test for w/cm?

None

11.	How often are the following types of concrete overlays used?  (Rank from 1 to 5 with 1=rare and 5=often)

| Type of Overlay | 1 | 2 | 3 | 4 | 5 | Comment on Performance E, G, or P** |
| --- | --- | --- | --- | --- | --- | --- |
| Latex-modified Concrete | X |  |  |  |  |  |
| Silica Fume Concrete |  | X |  |  |  | G |
| Dense Concrete |  | X |  |  |  | G |
| Fly Ash Concrete |  |  |  |  |  |  |
| Slag Concrete |  |  |  |  |  |  |
| Epoxy (Thin Bonded) | X |  |  |  |  | G |
| Polymer (Thin Bonded) |  |  |  | X |  | E |
| Other |  |  |  |  |  |  |

**Key: Excellent(E); Good(G); Poor(P)

12.	Rank the need or interest for your State to learn more about the following from 1 to 5 (1=low; 5=very high)

| BENEFICIAL ATTRIBUTES | 1 | 2 | 3 | 4 | 5 | Overall Ranking (1-11) |
| --- | --- | --- | --- | --- | --- | --- |
| Low Permeability (Dense Concrete) | X |  |  |  |  | 6 |
| High Durability | X |  |  |  |  | 1 |
| High Corrosion Resistance |  | X |  |  |  | 7 |
| Alkali-silica Reactivity Resistance |  | X |  |  |  | 8 |
| Higher Concrete Strengths |  |  | X |  |  | 11 |
| Highly Flowable Concrete |  |  | X |  |  | 13 |
| Crack Control |  | X |  |  |  | 9 |
| Skid Resistance |  | X |  |  |  | 10 |
| Rideability | X |  |  |  |  | 5 |
| Toughness of Concrete* |  |  |  | X |  | 12 |
| Minimum Maintenance | X |  |  |  |  | 4 |
| Longer Service Life | X |  |  |  |  | 3 |
| Savings (Life Cycle Costs) | X |  |  |  |  | 2 |

*Add fibers:  steel, glass, plastic, polypropolene, etc.

13.	Who at State and Division levels i.e., Materials, Construction, Pavement, Research, Structures, would be involved in examining concrete specifications and procedures and learning about High Performance Concrete?

Check those that apply:

Materials ___x___________

Construction ___________

Pavement ___x___________

Structures ____x__________

Research _____x_________

14.	Have you considered  adopting/implementing the following SHRP products?

2005	A Guide to Determining the Optimal Gradation of Concrete Aggregates?

Yes ______	No ______	Unknown __x____	    Implemented ______

- Specifications for High Performance Concrete?

Yes __x____	No ______	Unknown ______	    Implemented ______

- Designing ASR-Safe concrete Mix?

Yes __x____	No ______	Unknown ______	    Implemented ______

- Manual for Bridge Rehabilitation and Protection

Yes ______	No ______	Unknown __x____	    Implemented ______

Contact Person: Boyd Wheeler

UDOT Structures

Address: Box 148470

4501 South 2700 West

Salt Lake City, Utah 84114-8470

Telephone No.:801-+964-4456

Email Address:bwheeler@utah.gov

Contact Person: Bill Lawrence

UDOT Materials

Address: 4501 South 2700 West

Salt Lake City, Utah 84114

Telephone No.: 965-4560

Email Address: billlawrence@utah.gov

Thank you for completing the questionnaire.   A summary of compiled results will be made available upon completion.