$$717.00A

Section 717.—STRUCTURAL METAL

Revised 18 May 2005

INCLUDE THE FOLLOWING FOR BRIDGE EXPANSION JOINTS

$$717.01A

717.01  Add the following after 717.01(e):

(f) Anchor bolts, nuts, and washers for expansion joints.  Stainless steel conforming to ASTM A 276, Type 304.

INCLUDE THE FOLLOWING FOR ELASTOMERIC EXPANSION JOINT SEALS

$$717.17A

Add the following after Subsection 717.16:

717.17.  Elastomeric Expansion Joint Seals.  Furnish synthetic, non-wicking, fabric-reinforced, neoprene elastomeric expansion joint seals.  Furnish neoprene elastomer conforming to ASTM D 2000 and to Table 717-4.

Table 717-4 - Neoprene

| Physical Property | ASTM Test Method | Requirement |
| --- | --- | --- |
|  | Hardness, Durometer A |  | D 2240 |  | 60±5 |
|  | Tensile Strength |  | D 412 |  | 2000 psi (13.8 MegaPascals) min |
|  | Elongation at Break |  | D 412 |  | 250% min |
|  | Low Temperature |  | D 746 |  | Not Brittle at -67 oF (-55 oC) |
|  | Weather Resistant |  | D 1171 |  | No Cracks |
|  | Ozone Cracking |  | D 1149 |  | No Cracks |
|  | 100 PPHM 70 hours |  |  |  |  |
|  | @ 100 oF (38 oC), 20% strain |  |  |  |  |
|  | Water Resistance |  | D 471 |  | 3% max. volume swell |
|  | Compression Set |  | D 395, Method B |  | 25% max |
|  | 22 hours @ 158 oF (70 oC) |  |  |  |  |

INCLUDE THE FOLLOWING FOR GRANITE BRIDGE CURB.

$$717.18A

Add the following after Subsection 717.16:

717.18.  Masonry Anchors for Granite Bridge Curb.  Stainless steel conforming to

ASTM A 276, Type 304.