MSFC PRACA : 2003-02-12 07:54

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A10330 | In-Flight Anomaly Number -- | Contractor Report Number T-055 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title PDL LIFTOFF AT EPOXY PRIMER/POFI BONDLINE |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A B C D E (X) F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE ET COMPLETE | PART# 80901010000 | SER/LOT# N/A | MANUFACTURER PDL |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE ET COMPLETE | PART# 80901010000 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation L - FLD | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode UC - UNSAT | Cause MP - MFG-PRC |
| System TPS | Defect DD - DETACH | Material F - INSUL | Work Contact W. JOHNSON | Fail Date 05/05/1986 |
| Received at MSFC 10/08/1986 | Date Isolated -- | FMEA Reference 1.2.3 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location VAFB | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text LWT 16 AND UP |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 01/15/1992 | CN RSLV SBMT 07/21/1987 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design B. DAVIS | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |
| Approval |
| Design B. DAVIS | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete -- | MSFC Closure Date 08/06/1987 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: 1. AFTER TRIMMING TO REMOVE CRUSHED FOAM (LO2 FEEDLINE FLANGE; STATION 1360), IT WAS NOTED THAT PDL "LIFTOFF" HAD OCCURRED AT THE EPOXY PRIMER/POFI BONDLINE. 2. REIVEW OF EXTERNAL TANK FLIGHT SEPARATION PHOTOS INDICATE LO2 FEEDLINE FLANGE PDL DEBOND DURING FLIGHT (POSSIBLE DEBRIS ISSUED) |
| Contractor Investigation/Resolution R/C: NEW PROCESS HAS BEEN DEVELOPED BY AMT WHICH REQUIRES THE REDESIGN OF THE POFI MOLD TOOLS FOR THE L02 FEED LINE AND THE THRUST STRUT FLANGE CLOSE OUTS. 10/9/86 - FAILURE ANALYSIS DETERMINED THE CAUSE OF DEBOND IS THE RESULT OF AN INEFFECTIVE PDL POUR MOLD PROCESS/TOOLING 1/29/87 PRB STATUS - ALL ACTIONS TO BE CLOSED BY APPROXIMATELY 3-1-87 MMC IS REVIEWING PROCESS TO ILLUMINATE DEBRIS. 2/3/87 - UPDATED CRITICALITY TO 1 THIS PROBLEM IS CONSTRAINT TO 61M. THIS CONSTRAINT WAS COORDINATED WITH ET PROJECT MANAGER G. P. BRIDWELL. 5/28/87 - PRB STATUS - MMC IS REVIEWING POFI MOLD TOOL PROCESS FOR IMPROVEMENT AND MOD KITS TO BE ISSUED TO REPAIR THE FLEET. ECD 7/16/87. 7/22/87 - UPDATE GENERAL (REF T-055C) A. AN ACTION REQUEST (V-6126) WAS RECEIVED AT MAF FROM VAFB FOR LATENT DEFECT RECURRENCE CONTROL PER PR-ET-34-TS-0022. LOCATION: STATION 1360 - 4TH LEVEL - LWT-27 ANOMALY: CRUSHED FOAM ON L02 FEEDLINE - 30 DEGREES AFTER TRIMMING TO REMOVED CRUSHED FOAM, IT WAS NOTED THAT PDL "LIFT OFF" HAD OCCURRED AT THE EPOXY PRIMER/POFI BONDLINE. B. EXTERNAL TANK SEPARATION FLIGHT PHOTOS DEPICT A LOSS OF PDL FOAM FROM THE L02 FEEDLINE FLANGE CLOSEOUTS. C. AS A RESULT OF AR V-6126, AMELIORATION OF THE EXISTING POFI MOLD PROCESS WAS EXPEDITED TO SUP- PORT THE VALIDATION OF A NEW POFI MOLD TOOL/PROCESS FOR LWTS 37 AND UP; TO AFFECT THE VALIDA- TION OF PROCESSES FOR PREVIOUS BUILT VEHICLES (LWTS 16 THROUGH 36). D. TASKS I THROUGH IV OF THIS CAPS, ADDRESSES THE FAILURE ANALYSIS OF THE L02 POFI FEEDLINE CLOSE- OUT FLANGE, PROCESS AMELIORATION, CORRECTIVE ACTION FOR PREVIOUS BUILT VEHICLES, AND CONTROL TO PREVENT RECURRENCE. TASK I - CORRECTIVE ACTION A. THE L02 FEEDLINE AND THRUST STRUT FLANGE POFI MOLD CLOSEOUT PROCESSES ARE VALIDATED BY A COMMIT- TEE OF MMC AND AMT PERSONNEL. AMELIORATION OF THE PROCESSES INCLUDED FABRICATION OF NEW POFI MOLD TOOLS. TWO SUCCESSIVE, SUCCESSFUL RUNS WERE PERFORMED ON EACH FLANGE WITH SUBSTRATE BOND TENSION, SHORE "A" HARDNESS, SOFI FOAM DUROMETER, AND INTERNAL VOIDS MEETING THE PROCESS RE- QUIREMENTS (REFERENCE INTEROFFICE MEMORANDUM 3693-87-MK-017, MK-006, MK-011; 3693-86-DB-364; 3693-86-MK-398 AND 3693-87-TW-206). LWT -37 WAS THE PATH FINDER VEHICLE USED FOR FIRST PART VERIFICATION. B. A DEBRIS ASSESSMENT TEAM REVIEWED FLIGHT SEPARATION PHOTOS, ENGINEERING (DRAWING/STP) REQUIRE- MENTS, PROCESSING PLANS (MPP/PI), DEVELOPMENT/VERIFICATION/VALIDATION HISTORY, THERMAL AND AEROLOADING CONCERNS, AND THE IMPACTS OF REWORK TO DETERMINE L02 FEEDLINE PDL DEBOND SIMILAR DEBRIS/PROCESS CONCERNS. EXTERNAL TANK FLEET REWORK OF THE L02 FEEDLINE AND THRUST STRUT FLANGES WAS THE TEAM RECOMMENDATION (REFERENCE INTEROFFICE MEMORANDUM 3571-86-46). SUBSEQUENT- LY, THE THRUST STRUT FLANGE CLOSEOUT WAS INCLUDED AS A CORRECTIVE ACTION, HEREIN. - CLOSURE SUMMARY - A LATENT DEFECT (DEBONDED PDL L02 FLANGE CLOSEOUT) DISCOVERED AT VAFB, LWT-27, AND EXTERNAL TANK FLIGHT SEPARATION PHOTOS (DEPICTING A LOSS OF PDL FOAM MATERIAL DURING FLIGHT) VERIFIED AN EXISTING INADEQUATE POFI MOLD PROCESS. AN INVESTIGATION INTO THIS PHENOMENA SHOWED THAT THE INCUMBENT POFI MOLD TOOLING WAS NOT SECURED SUFFICIENTLY TO PRECLUDE FOAM VOIDS DURING MATERIAL RISE. IN ADDITION,THE METHOD UTILIZED IN THE FOAM CHARGING OF THE MOLD CREATED IRREGULAR BOND LINES. THIS LED TO FOAM RUNOVER AND SEPARATION OF MATERIAL FROM SUBSTRATE. SIMULATION OF THE INCUMBENT POFI MOLD PROCESS WAS PERFORMED IN THE ADVANCED MANUFACTURING TECHNOLOGYLABORATORIES. AN IMPROVED PROCESS WAS THEN DEVELOPED BY AMT (REF. ATTACHMENT 1). TENSILE TESTS ANDTHE DISSECTION OF THE FOAM MATERIAL (DETERMINATION OF VOID ANOMALIES), WERE THE PHYSICAL PARAMETERS USED TO INDICATE AN IMPROVED PROCESS. SUBSEQUENT RESULTS SHOWED A SIGNIFICANT PROCESS IMPROVEMENT (REF. ATTACHMENT 2). THE NEW PROCESS REQURIED THE REDESIGN OF THE POFI MOLD TOOLS FOR THE L02 FEEDLINE AND THE THRUST STRUT CLOSEOUTS. THE PDL FOAM WAS POURED INTO THE NEW MOLD CONFIGURATION IN TWO STEPS. AFTER THE FIRST POUR, THE POFI INTERFACES WERE SANDED SMOOTH, ADHESIVE APPLIED, AND THE SECOND POUR WAS PERFORMED, CREATING A RELIABLE MATERIAL-SUBSTRATE BOND. THE AMT DEVELOPED PROCESS WAS VALIDATED FOR EACH NEW POFI MOLD TOOL USED. THE FIRST PART VERIFICA- TION WAS WITNESSED TWICE BY THE VALIDATION COMMITTEE (MMC AND MAT PERSONNEL) DURING THE LWT-37 BUILDCYCLE. SUBSEQUENT MOLD VALIDATIONS WERE PERFORMED (SIMULATED IN THE AMT LABORATORY) ON THE POFI MOLD TOOLS WHICH WILL BE UTILIZED (FOR FLANGE CLOSEOUT) WHEN THE EXTERNAL TANK IS IN THE VERITICAL POSITION (KSC). REWORK/REPAIR OF THE FLEET CLOSEOUT FLANGES (AS DETAILED, HEREIN) WILL BE ACCOMPLISHED PER MODIFI- CATION KITS (REFERENCE B01777). THIS PROBLEM IS SUBMITTED TO MSFC FOR REVIEW AND APPROVAL |
| MSFC Response/Concurrence |

| ASSESSMENT ADDENDUM REPORT |
| --- |
| MSFC Report# A10330 | IFA# -- | Contractor RPT# T-055 | JSC# -- | KSC# -- | EICN# -- |
| Asmnt Part# 80901010000 | Asmnt Part Name ET COMPLETE | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MP - MFG-PRC | FAIL MODE UC - UNSAT |
| Asmnt FMEA 5.8.1.1 | Asmnt FM 1 | FMEA CSE B | FMEA SCSE 3 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |