03M03/29/06

S614-03M.doc

Use on projects when lean concrete backfill is specified:

Section 614. - LEAN CONCRETE BACKFILL

Construction Requirements

614.03  Composition of Mix.  Delete Table 614-1 and substitute the following:

Table 614-1

Composition of Lean Concrete Backfill

| Property | Specification |
| --- | --- |
| Cement content | 56 kg/m3 min. |
| Aggregate particle size | 25 mm max. |
| Aggregate passing 75-(m sieve | 10% max. |
| 7-day compressive strength | 1.5 MPa max. |