LHC Q1 – Q2 Interconnect Procedure

Reference Drawings:

Q1 - Q2 Bus and Splice Assembly (ME-430179)

Q1 - Q2 Piping Connections Installation (ME-390866)

Q1 - Q2 Main Assembly (ME-390867)

Q1 - Q2 Bellows Protectors Installation (ME-390871)

By: Jamie Blowers, Rodger Bossert, Tom Page, Jim Rife Technical Division, Fermilab

|  | Description | Dwg Size | Number | Rev | Unit | Quantity Required |
| --- | --- | --- | --- | --- | --- | --- |
|  | KAPTON | MA | 292722 |  |  | A/R |
|  | Q2 COLDMASS PREPARATION Q2A BUS HOUSING-EXTENSION | ME | 369872 | B | REF | 0 |
|  | Q2 COLDMASS PREPARATION Q2A BUS HSG-EXTENSION-BS | MC | 369873 | A | REF | 0 |
|  | SOLDER STRIP 96/4 | MA | 369904 |  |  | A/R |
|  | FLUX – KESTER 135 | MA | 369911 |  |  | A/R |
|  | DRIFT TUBE ASSEMBLY | ME | 390190 | A | EA | 1 |
|  | VACUUM VESSEL LEFT HAND SLEEVE ASSEMBLY | ME | 390322 | A | EA | 1 |
|  | HEAT EXCHANGER / COLD MASS CONNECTOR | MD | 390334 | A | EA | 1 |
|  | SHIELD LINE CONNECTOR | MD | 390343 | A | EA | 2 |
|  | COOLDOWN LINE CONNECTOR | MD | 390344 | A | EA | 1 |
|  | PUMPING LINE CONNECTOR | MD | 390345 | A | EA | 1 |
|  | COLD MASS INSTRUMENTATION CONNECTOR | MD | 390346 | A | EA | 1 |
|  | COLD MASS CONNECTOR | MD | 390347 | A | EA | 1 |
|  | SHIELD ASSEMBLY ALUMINUM SPACER, 4.6 LONG | MA | 390373 | * | EA | 32 |
|  | RETAINING WASHER | MA | 390378 | * | EA | 32 |
|  | INTERCONNECTION COLD MASS PIPES SUPPORT | ME | 390450 | B | EA | 1 |
|  | COLD MASS PIPE SUPPORT CLAMP | MC | 390451 | A | EA | 3 |
|  | COLD MASS/Hx PIPE SUPPORT CLAMP | MC | 390453 | * | EA | 1 |
|  | Hx PIPE SUPPORT CLAMP | MC | 390454 | * | EA | 1 |
|  | COOLDOWN PIPE SUPPORT CLAMP | MB | 390455 | * | EA | 1 |
|  | UPPER PIPE SUPPORT | ME | 390456 | A | EA | 1 |
|  | THERMAL SHIELD Q1-Q2 LEFT HAND SECTION | ME | 390505 | A | EA | 2 |
|  | THERMAL SHIELD Q1-Q2 LEFT HAND INSTRUMENTATION SECTION | ME | 390506 | A | EA | 1 |
|  | THERMAL SHIELD Q1-Q2 LEFT HAND VENT SECTION | ME | 390510 | A | EA | 1 |
|  | THERMAL SHIELD Q2 CONNECTOR | ME | 390515 | * | EA | 2 |
|  | THERMAL SHIELD - SHIELD CONNECTOR | ME | 390516 | * | EA | 2 |
|  | THERMAL SHIELD DEFLECTOR | MB | 390517 | * | EA | 1 |
|  | THERMAL SHIELD CENTER BAND CONNECTOR | MC | 390518 | * | EA | 1 |
|  | THERMAL SHIELD FILLER | MB | 390519 | * | EA | 4 |
|  | THERMAL SHIELD CENTER BAND | ME | 390520 | * | EA | 2 |
|  | SHIELD MLI INSULATION - INNER BLANKET | ME | 390546 | * | EA | 1 |
|  | SHIELD MLI INSULATION - OUTER BLANKET | ME | 390547 | * | EA | 1 |
|  | THERMAL SHIELD ALUMINUM SPACER, 12.4 LONG | MA | 390553 | * | EA | 4 |
|  | 1/4-20 U-BOLT | MB | 390554 | * | EA | 4 |
|  | COOLDOWN / SHIELD LINE BELLOWS PROTECTOR | MC | 390578 | * | EA | 6 |
|  | Hx OUTER SHELL BELLOWS PROTECTOR | ME | 390579 | * | EA | 4 |
|  | PUMPING LINE BELLOWS PROTECTOR | MD | 390580 | * | EA | 2 |
|  | PIPING INSULATION MLI BLANKET | ME | 390594 | * | EA | 1 |
|  | Hx OUTER TUBE END FLANGE SPACER RING | MC | 390600 | * | EA | 2 |
|  | COLD MASS SINGLE - BELLOWS OPEN PROTECTOR | MD | 390603 | A | EA | 4 |
|  | COLD MASS DOUBLE - BELLOWS OPEN PROTECTOR | ME | 390607 | * | EA | 2 |
|  | PUMPING LINE & COLD MASS END FLANGE SPACER RING | MB | 390617 | * | EA | 5 |
|  | COOLDOWN & SHIELD LINE END FLANGE SPACER RING | MB | 390618 | * | EA | 6 |
|  | BEAMLINE DRIFT TUBE COOLING JACKET FLEX HOSE | MA | 390625 | * | EA | 1 |
|  | 3.5” PIPE PERSISTENT RING | MC | 390640 |  | EA | 1 |
|  | INTERCONNECTION BEAM TUBE SUPPORT ASSEMBLY | ME | 390779 | * | EA | 1 |
|  | 4.5K CC SUPPLY FLEX HOSE | MB | 390806 | * | EA | 1 |
|  | 4.5K INTERCEPT CC SUPPLY FLEX HOSE RETAINER PLATE | MA | 390807 | * | EA | 1 |
|  | 4.5K INTERCEPT TUBE BRACE BAR | MB | 390816 | * | EA | 2 |
|  | BEAM SCREEN COOLING SPOOL | MD | 390819 | * | EA | 1 |
|  | 3.5” Pipe Coldmass Weld Ring | MC | 390875 |  | EA | 2 |
|  | SCREW, M8 x 25 | MA | 393018 | * | EA | 4 |
|  | M6 LOCK WASHER | MA | 393026 | * | EA | 22 |
|  | M8 LOCK WASHER | MA | 393027 | * | EA | 4 |
|  | M5 x 16 CAP SCREW | MA | 393028 | * | EA | 128 |
|  | SCREW, M6 x 20 | MA | 393037 | * | EA | 38 |
|  | M30 x 3.5 x 2.0m LONG THREADED ROD | MA | 393041 | * | EA | 4 |
|  | M30 SPHERICAL WASHER | MA | 393043 | * | EA | 16 |
|  | M30 HEX NUT | MA | 393044 | * | EA | 16 |
|  | M5 x 25 CAP SCREW | MA | 393053 | * | EA | 4 |
|  | 1/4-20 HEX NUT | MA | 393054 | * | EA | 16 |
|  | M5 LOCK WASHER | MA | 393056 | * | EA | 96 |
|  | M5 FLAT WASHER | MA | 393057 | * | EA | 76 |
|  | COMMON FASTENERS-#6-32 X .75 LG. (SST) | MA | 393237 | A | EA | 12 |
|  | Q1 CORRECTION COIL SPLICE SUPPORT | MD | 430023 |  | EA | 1 |
|  | Q2 MOD.ASSY/Q2 BUS SPIDER ASSEMBLY | MD | 430044 | C | EA | 1 |
|  | BUS SPLICE SEPARATOR | MB | 430084 |  | EA | 1 |
|  | Bus Housing Transition Cover - Q2 | ME | 430153 | * | EA | 1 |
|  | Bus Housing Transition Base – Q2 | ME | 430154 |  | EA | 1 |
|  | GLASS TAPE (item #7 on ME-430179) |  |  |  |  | A/R |
|  | Hypertronics Tie-Down Link | MA | 418109 |  | EA | 4 |
|  | M3 Nut | MA | 418111 |  | EA | 8 |
|  | Kevlar string | MA | 369912 |  |  | A/R |
|  | Kapton sleeves (PROVIDED BY CERN) |  |  |  |  | 4 |
|  | TOOLING: |  |  |  |  |  |
|  | Corrector Wire Bus Splice Soldering Fixture | MD | 430016 |  |  | 1 |
|  | Bus Cable Splice Fixture | MC | 430138 |  |  | 1 |
|  | Compression Collar |  | 390444 |  |  | 16 |
|  | M12 Threaded Rod |  | 390449 |  |  | 24 |
|  | M12 Flat Washer |  | 393331 |  |  | 96 |
|  | M12 Hex Nut |  | 393039 |  |  | 96 |
|  | Collar Screws, M8 X 50mm |  | 393020 |  |  | 16 |
|  | Compression Collar |  | 390442 |  |  | 24 |
|  | M10 Threaded Rod |  | 390448 |  |  | 48 |
|  | M10 Flat Washer |  | 364306 |  |  | 192 |
|  | M10 Hex Nut |  | 393038 |  |  | 192 |
|  | Collar Screws, M6 X 40mm |  | 393047 |  |  | 48 |
|  | Compression Collar |  | 390440 |  |  | 1 |
|  | Splice Fixture Controllers |  | N/A |  |  |  |
|  | Bellows Restraints | MB | 418232 |  |  | 9 per IR set |
|  | Lead position tool | MB | 430191 |  |  |  |

GENERAL NOTES:

- All screws installed in the vacuum and cryogenic space must have some form of additional protection from working themselves loose during thermal cycling. The use of Loctite 242 or 245, or Stycast is recommended for this purpose.

(Complete Above Ground)

- Carefully remove all shrink tubing from cable leads.

- If cable labels are place where they will interfere with the splicing operation (e.g. at the end of the leads), then additional labels should be applied at a position on the cable where they will not interfere with the splicing operation. In order to apply new labels, it may be necessary to remove ground wrap which is holding the wire bundles together. If this is the case, be sure to remove only what is necessary. The labels at the ends can be removed in the tunnel, after the length of the lead is correctly determined.

- All leads should be dressed to remove solder/weld excess.

- Verify that the bus leads coming out of the IP-end of the Q2 magnet are correctly wrapped together. You may find them ground-wrapped separately, instead of together. If this is the case, remove the individual ground wraps, and then wrap the two together with one layer 2/3 lapped of Kapton (MA-292722, or equivalent).

- Install Vacuum Outer Shell Sleeve (ME-390322) and Vacuum Vessel Bellows Assembly (Provided by CERN) as per Q1 to Q2 Main Assembly (ME-390867). Position them so that they do not interfere with subsequent work.

##### Parts list

- VACUUM OUTER SHELL SLEEVE (ME-390322)

- VACUUM VESSEL BELLOWS ASSEMBLY (PROVIDED BY CERN)

- Install Bus Housing (Item Numbers called out below refer to Drawing No.		 ME-430155) (also refer to ME-430179).

  - Inspect Q1-Q2 bus housing assembly (ME-430155) to ensure all parts exist.

  - Place bus housing parts items 5 (ME-430153) and 6 (ME-430154) around lead and correction coil busses.

  - Attach item 5 (ME-430153) to item 2 (MC-369873) with four screws item 3 (MA-393237) as shown on Bus Housing Assembly drawing (ME-430155) and Q1-Q2 Bus and Splice Assembly drawing (ME-430179). Be sure to apply Loctite (or equivalent) to the screws.

  - Attach Bus Housing Transition base item 6 (ME-430154) to bus housing transition cover item 5 (ME-430155) with screws item 3 (MA-393237) as shown on Bus Housing Assembly drawing (ME-430155). Be sure to apply Loctite (or equivalent) to the screws.

  - Attach item 4 Bus Spider Assembly (MD-430044) to bus housing assembly as shown on Bus Housing Assembly (ME-430155) and Q1-Q2 Bus and Splice Assembly (ME-430179).

  - Slide the 3.5” Pipe Coldmass Weld Ring (MC-390875), and the Cold Mass Instrumentation Connector (MD-390346) over the Bus Housing Assembly.

  - Weld the Cold Mass Instrumentation Connector (MD-390346) to Q2.  Refer to the Q1 to Q2 Piping Connections Installation (ME-390866), View M-M for details. NOTE: instrumentation wires need to be protected from the weld heat (e.g. pull them tight enough so that they are not resting on the tube during welding, apply protection which can be removed after welding, etc.).

##### Parts list

- #6-32 X .75 LG. (SST) (MA-393237)

- Q2 MOD.ASSY/Q2 BUS SPIDER ASSEMBLY (MD-430044)

- Bus Housing Transition Cover - Q2 (ME-430153)

- Bus Housing Transition Base - Q2 (ME-430154)

- 3.5” PIPE COLDMASS WELD RING (MC-390875)

- COLD MASS INSTRUMENTATION CONNECTOR (MD-390346)

- Install Drift Tube

  - Install Drift Tube (ME-390190) on the Q1 magnet as per Q1 to Q2 Piping Connections Installation (ME-390866), View K-K.

##### Parts list

- DRIFT TUBE (ME-390190)

- Install the CERN-supplied Beam Screen and BPMS assemblies per the CERN drawings listed below.

##### CERN Drawings

- Cold Beam Vacuum Interconnects Type QQ1 (LHCLVI GG0002 - Right side, IRs 1, 2, 5 and 8)

- Beam Vacuum Interconnects Assembly Type IT 1 IR Right (LHCLVIGG0002)

- Beam Vacuum Interconnects Assembly Type IT 4 IR Right (LHCLVIGG0007)

- Beam Vacuum Interconnects Assembly Type IT 1 IR Left (LHCLVIGG0009)

- Beam Vacuum Interconnects Assembly Type IT 4 IR Left (LHCLVIGG0010)

(Complete Below Ground)

- Perform Lead Splices

  - Install End Flange Spacer Ring (ME-390617) as per Q1 to Q2 Piping Connections Installation (ME-390866).

  - Compress cold mass bellows.

  - Set the Q1 lead longitudinal position using the supplied tool (MB-430191), as per Q1-Q2 Bus and Splice Assembly (ME-430179).

  - Mark position of end of Q1 lead cable at position at end of Q2 lead.

  - Perform main bus splices.

    - Place main bus leads in configuration needed for splicing, as per Q1-Q2 Bus and Splice Assembly (ME-430179), sections B-B and D-D, and on Figure 9.5.1-A below, making sure end of Q1 lead is at mark on Q2 lead from previous step.

Figure 9.5.1-A

    - Clean all leads with Tech spray and Scotch Brite, or equivalent. Wipe down with Kay-dry or equivalent.

    - Paint flux (Kester 135, MA-369911 or equivalent) on all surfaces to be soldered.

    - Add solder strips (MA-369904 or equivalent, 0.2 mm thick) to areas to be spliced, between each main lead.

    - Place solder fixture (MD-430138) around both lead splices.

    - Screw solder fixture together around splices.

    - If desired, add an additional temperature measuring device (e.g. handheld thermocouple).

    - Turn on resistive heaters, and wait for the solder to melt, while monitoring the temperature. Tighten screws as the solder is softening, so that the fixture is completely closed when the solder is completely melted. When the solder has melted, turn off the heater controller. The solder typically melts at about 220°C, but the temperature should be held at 235°C for one minute. Do not allow the temperature to exceed 240°C.

    - Monitor the temperature during cool-down, and let splice cool to ~ 40°C. To monitor the temperature, unplug the heating element, and then turn the controller back on.

    - After cooling (to ~ 40°C), remove the splices from the fixture. NOTE: It is easiest to remove the splices while the fixture is a little warm, so it is best not to let it cool to room temperature before removing the leads from the fixture.

    - Clean exterior of splices with Tech spray and Scotch Brite or equivalent.  Wipe down with Kay-dry or equivalent.

  - Using the tool provided (MB-430191), verify that the Q1 lead longitudinal position is correct.

  - Insulate Main Bus Splices.

    - There are two main bus splices, positioned vertically, as shown in section B-B of the Q1-Q2 Bus and Splice Assembly (ME-430179).  Wrap each splice separately, using one wrap of 50 um thick by 9.5mm wide Kapton (MA-292722) with 50% overlap as shown in detail E.

    - Place one G-11 splice separator (MB-430084) between the two splices as shown in section B-B.

    - Wrap entire splice bundle with one wrap of 50 um thick by 9.5mm wide Kapton (MA-292722) with 75% overlap surrounded by one layer of glass tape (item #7 on ME-430179) with 50% overlap as shown in detail E.

    - Fuse the ends of the glass tape to prevent the tape from unraveling. Use soldering iron to burn line over the last couple of wraps.

    - Wrap entire splice bundle with Kevlar string (MA-369912, or equivalent) in a similar fashion to cartoon below (figure 9.7.5-A). The spacing between each loop should be ~ 1.5 cm, and the string should be pulled tightly around the splice bundle. Apply Loctite to each cross-over to hold the string in place. The colors of the string in the cartoon below (figure 9.7.5-A) show the way in which the string is wrapped, but the string should be one continuous piece, as much as is possible.

Figure 9.7.5-A

  - Perform Corrector lead splices

    - Cut corrector wires at an appropriate length to provide for a splice 60mm long as shown in Q1-Q2 Bus and Splice Assembly	 (ME-430179).

    - Cut back “spare” corrector (shown on section A-A of ME-430179) wire 100mm back from center of splice.

    - Using appropriate means, remove the varnish from the corrector leads only in the areas to be soldered. See figure 9.8.3-A below.

Figure 9.8.3-A

    - Pre-tin all corrector leads to be spliced with solder made of 96% tin/4% silver.

    - Slide Kapton sleeves over each corrector lead on the Q2 magnet (CERN part # XXX).

    - Place corrector wires in configuration needed for splicing, as per Q1-Q2 Bus and Splice Assembly (ME-430179), section B-B and detail D, and on Figure 9.8.6-A below.

Figure 9.8.6-A

    - Place Solder Fixture (MD-430016) under the four corrector leads at area to be spliced according to Figure 9.8.3-A above. NOTE: The main bus splices should be protected from the heat applied for the corrector lead soldering. If necessary, place insulation between the soldering fixture and the main bus.

    - Paint flux (Kester 135, MA-369911 or equivalent) on all surfaces to be soldered.

    - Screw solder fixture together.

    - If desired, add an additional temperature measuring device (e.g. handheld thermocouple).

    - Turn on resistive heaters, and wait for the solder to melt, while monitoring the temperature. Tighten screws as the solder is softening, so that the fixture is completely closed when the solder is completely melted. When the solder has melted, turn off the heater controller. The solder typically melts at about 220° C, but the temperature should be held at 235°C for one minute. Do not allow the temperature to exceed 240°C.

    - Monitor the temperature during cool-down, and let splice cool to ~ 40°C. To monitor the temperature, unplug the heating element, and then turn the controller back on.

    - After cooling (to ~ 40°C), remove the splices from the fixture. NOTE: It is easiest to remove the splices while the fixture is a little warm, so it is best not to let it cool to room temperature before removing the leads from the fixture.

    - Clean exterior of splices with Tech spray and Scotch Brite or equivalent.  Wipe down with Kay-dry or equivalent.

    - Slide the Kapton sleeves over the splices.

    - Install corrector bus housing splice support (MD-430023) as shown on drawing. Be sure to apply Loctite (or equivalent) to the screws.

  - Release and connect Cold Mass Bellows.

###### Parts list

- Glass tape (item #7 on ME-430179)

- Kapton (MA-292722)

- Bus Splice Separator (MB-430084)

- Flux, Kester 135 (MA-369911)

- Solder Strip 96/4 (MA-369904) or CERN equivalent

- Q1 Correction Coil Splice Support (MD-430023):

    - Threaded Tray (MC-430001)

    - Single Cover (MC-430003)

    - 3mm/.5 X 8 Screw (MA-393246)

  - Kapton sleeves (provided by CERN)

###### Tooling

- Corrector Wire Bus Splice Soldering Fixture (MD-430016)

- Bus Cable Splice Soldering Fixture (MC-430138)

- Lead position tool (MB-430191)

- Install Cold Mass Connector (MD-390347) on the M2 pipe.

  - Slide the 3.5” Pipe Coldmass Weld Ring (MC-390875) over the wires and connector.

  - Wrap a welding blanket around the cables. The blanket should have a cord attached so that it can be pulled out after the welding operation.

  - Slide the Cold Mass Connector (MD-390347) over instrumentation wire and Hypertronics connector, making sure to have the weld blanket cord coming out of the end of the pipe.

  - Weld per Q1 to Q2 Piping Connections Installation (ME-390866), View M-M.

  - Pull out the welding blanket.

##### Parts list

- COLD MASS CONNECTOR (MD-390347)

- 3.5” PIPE COLDMASS WELD RING (MC-3906875)

- Connect Hypertronics Connectors (Q1 - MB-418119 & Q2 – MB-418133; Assembly drawing MD-430182)

  - Compress the M2 pipe Bellows.

  - Install the End Flange Spacer Ring (MB-390617).

  - Connect the connectors.

  - Using the M3 nuts (MA-418111) install the G11 Tie-Down Links (MA-418109) per MD-430182. The nuts should have Loctite, or equivalent, applied prior to installation.

  - Release the Bellows.

  - Weld per Q1 to Q2 Piping Connections Installation (ME-390866), View C–C.

##### Parts list

- END FLANGE SPACER RING (MB-390617)

- HYPERTRONICS TIE-DOWN LINKS (MA-418109)

- M3 Nuts (MA-418111)

Tools

- Bellows Tools.

##### Inspection

- Electrical checkout?

- Install Heat Exchanger / Cold Mass Connector (MD-390334).

  - Compress the Hx Outer Bellows, both sides.

  - Compress the Cold Mass Bellows.

  - Install the End Flange Spacer Rings (MB-390600) for the Hx bellows.

  - Install the Persistent Ring (MB-390640) for the M4 pipe (Q2 side).

  - Install the End Flange Spacer Ring (MB-390617) for the M4 pipe (Q1 side).

  - Position Heat Exchanger/Cold Mass Connector Pipe Assembly (MD-390334).

  - Position the Hx inner Tube (XB on ME-390866).

  - Weld inner Hx Tube (XB on ME-390866) both sides per Q1 to Q2 Piping Connections Installation (ME-390866), View B–B.

  - Release the Hx outer bellows.

  - Weld outer Hx Tube (L on ME-390866) both sides per Q1 to Q2 Piping Connections Installation (ME-390866), View A–A.

  - Weld M4 Line (M4 on ME-390866) both sides per Q1 to Q2 Piping Connections Installation (ME-390866), View H–H and C–C.

##### Parts list

- END FLANGE SPACER RINGS (MB-390600)

- PERSISTENT RING (MB-390640)

- END FLANGE SPACER RINGS (MB-390617)

- HEAT EXCHANGER/COLD MASS CONNECTOR (MD-390334)

##### Weld Details

- View H–H, Upper Cold Mass Q2 side.

- View C–C, Upper Cold Mass Q1 side.

- View A–A, Hx Outer Shell both sides.

- View B–B, Hx Inner Shell both sides.

- Install the CERN-supplied Plug-in Module per the CERN drawings listed below.

##### CERN Drawings

- Cold Beam Vacuum Interconnects Type QQ1 (LHCLVI GG0002 - Right side, IRs 1, 2, 5 and 8)

- Beam Vacuum Interconnects Assembly Type IT 1 IR Right (LHCLVIGG0002)

- Beam Vacuum Interconnects Assembly Type IT 4 IR Right (LHCLVIGG0007)

- Beam Vacuum Interconnects Assembly Type IT 1 IR Left (LHCLVIGG0009)

- Beam Vacuum Interconnects Assembly Type IT 4 IR Left (LHCLVIGG0010)

- Install Pumping Line Connector (MD-390345).

  - Compress the Bellows.

  - Install the End Flange Spacer Ring (MB-390617).

  - Position the Pumping Line Connector (MD-390345, XBt on ME-390866).

  - Release the Bellows.

  - Weld Pumping Line Connector (MD-390345, XBt on ME-390866) per Q1 to Q2 Piping Connections Installation (ME-390866), View C–C and E–E.

##### Parts list

- PUMPING LINE CONNECTOR (MD-390345)

- END FLANGE SPACER RING (MB-390617)

##### Weld Details

- View C–C

- View E–E

- Install Cooldown Line Connector (MD-390344).

  - Compress the Bellows.

  - Install the End Flange Spacer Rings (MB-390618).

  - Position the Cooldown Line Connector (MD-390344).

  - Release the Bellows.

  - Weld Cooldown Line Connector (MD-390344) both ends, per Q1 to Q2 Piping Connections Installation (ME-390866), View D–D.

##### Parts list

- COOLDOWN LINE CONNECTOR (MD-390344)

- END FLANGE SPACER RING (MB-390618)

- Install Cooling Jacket Flex Hose (MA-390625).

  - Install the Cooling Jacket Flex Hose (MA-390625) between the port on the Drift Tube (ME-390190) and the port on the M4 pipe, as per Q1-Q2 Piping Connections Installation (ME-390866).

  - Weld Cooling Jacket Flex Hose (MA-390625) per Q1-Q2 Piping Connections Installation (ME-390866), View L–L for both welds.

##### Parts list

- COOLING JACKET FLEX HOSE (MA-390625)

- Install Cooling Spool (MD-390819).

  - Install and weld the Cooling Spool (MD-390819) onto the Beam Screen Assembly, as per Q1 to Q2 Piping Connections Installation (ME-390866), View J–J.

##### Parts list

- BEAM SCREEN COOLING SPOOL (MD-390819)

- Install 4.5K CC Supply Flex - Hose (MB-390806).

  - Install 4.5K CC Supply Flex - Hose (MB-390806).

  - Position 4.5K CC Supply Flex - Hose (MB-390806).

  - Weld 4.5K CC Supply Flex - Hose (MB-390806) per Q1 to Q2 Piping Connections Installation (ME-390866), View G–G.

##### Parts list

- 4.5K CC SUPPLY FLEX - HOSE (MB-390806)

- Install 4.5K Intercept Tube Brace Bar (MB-390816).

  - Install 4.5K Intercept Tube Brace Bar (MB-390816), if necessary.

##### Parts list

- 4.5K INTERCEPT TUBE BRACE BAR (MB-390816)

- Install Cold Mass Pipe Support Assembly (ME-390820).

  - Install Cold Mass Pipe Support Assembly (ME-390820) as per Q1 to Q2 Bellows Protectors Installation (ME-390871). Be sure to apply Loctite (or equivalent) to the screws.

##### Parts list

- COLDMASS PIPE SUPPORT (MC-390450)

- COLDMASS PIPE SUPPORT CLAMP (MC-390451)

- Hx PIPE SUPPORT CLAMP (MC-390453)

- FLEX HOSE RETAINER PLATE (MA-390807)

- SCREW M6 X 20 (MA-393037)

- M6 LOCK WASHER (MA-393026)

- Install Beam Tube Support Assembly (ME-390779).

  - Using the Flex Hose Retainer Plate (MA-390807), position Flex - Hose (MB-390806) in Pipe Support Assembly shown in “Opposite Side View” on Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Beam Tube Support Assembly (ME-390779) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

##### Parts list

- BEAM TUBE SUPPORT ASSEMBLY (ME-390779)

- FLEX HOSE RETAINER PLATE (MA-390807)

- Install Upper Pipe Support Assembly (ME-390821).

  - Install Upper Pipe Support Assembly (ME-390821) as per Q1 to Q2 Bellows Protectors Installation (ME-390871). Be sure to apply Loctite (or equivalent) to the screws.

##### Parts list

- COLDMASS PIPE SUPPORT CLAMP (MC-390451)

- HEAT EXCHANGER PIPE SUPPORT (MC-390454)

- COOLDOWN PIPE SUPPORT CLAMP (MB-390455)

- HEAT EXCH. COOLDOWN-PUMPING PIPES SUPPORT (ME-390456)

- SHCS M8 X 25.0 (MA-393018) [NOTE: for the first magnet we sent MA-393040 M8 X 20]

- M6 LOCK WASHER (MA-393026)

- M8 LOCK WASHER (MA-393027)

- SCREW M6 X 20 (MA-393037)

- Install Shield Line Connectors (FF & EE) (MD-390343).

  - Compress the Bellows.

  - Install the End Flange Spacer Rings (MB-390618).

  - Position the Shield Line Connectors (FF & EE) (MD-390343) (See Q1 to Q2 Piping Connections Installation ME-390866 for pipe orientation.)

  - Release the Bellows.

  - Weld Shield Line Connectors per Q1 to Q2 Piping Connections Installation (ME-390866), View D–D for all connections.

##### Parts list

- SHIELD LINE CONNECTORS (FF & EE) (MD-390343)

- END FLANGE SPACER RINGS (MB-390618)

- Leak Check

  - When all assemblies have been installed, perform a Leak Check on the entire Assembly.

- Install Bellows Protectors.

NOTE: Be sure to apply Loctite (or equivalent) to the screws.

  - Install Cold Mass Electrical Bus (M1) Bellows Protectors (ME-390607) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Cold Mass Instrumentation (M2) Bellows Protectors (ME-390603) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Cold Mass Heat Exchanger (M4) Bellows Protectors (ME-390603) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Heat Exchanger (L) Bellows Protectors (ME-390579) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Pumping Line (XBt) Bellows Protectors (MD-390580) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Cooldown Line (LD1) Bellows Protectors (MC-390578) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Shield Line (FF) Bellows Protectors (MC-390578) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

  - Install Shield Line (EE) Bellows Protectors (MC-390578) as per Q1 to Q2 Bellows Protectors Installation (ME-390871).

##### Parts list

- COLD MASS ELECTRICAL BUS (M1) BELLOWS PROTECTORS (ME-390607)

- COLD MASS INSTRUMENTATION (M2) BELLOWS PROTECTORS (ME-390603)

- COLD MASS HEAT EXCHANGER (M4) BELLOWS PROTECTORS (ME-390603)

- HEAT EXCHANGER (L) BELLOWS PROTECTORS (ME-390579)

- PUMPING LINE (XBT) BELLOWS PROTECTORS (MD-390580)

- COOLDOWN LINE (LD1) BELLOWS PROTECTORS (MC-390578)

- SHIELD LINE (FF) BELLOWS PROTECTORS (MC-390578)

- SHIELD LINE (EE) BELLOWS PROTECTORS (MC-390578)

- SCREW, M6 X 20 (MA-393037)

- Install eight BPM steel jacket cables (CERN supplied).

- Pipe Insulation

  - Wrap piping with MLI blankets as per Q1 to Q2 Main Assembly (ME-390867).

##### Parts list

- PIPING INSULATION MLI BLANKET (ME-390594)

- Install Thermal Shield (ME-390503)

  - Install parts listed below as per Q1 to Q2 Main Assembly (ME-390867). Be sure to apply Loctite (or equivalent) to all screws.

##### Parts list

- THERMAL SHIELD Q1-Q2 LEFT HAND SECTION (ME-390505)

- THERMAL SHIELD Q1-Q2 LEFT HAND INSTRUMENTATION SECTION (ME-390506)

- THERMAL SHIELD Q1-Q2 LEFT HAND VENT SECTION (ME-390510)

- THERMAL SHIELD Q2 CONNECTOR (ME-390515)

- THERMAL SHIELD - SHIELD CONNECTOR (ME-390516)

- THERMAL SHIELD DEFLECTOR (MB-390517)

- THERMAL SHIELD CENTER BAND CONNECTOR (MC-390518)

- THERMAL SHIELD FILLER (MB-390519)

- THERMAL SHIELD CENTER BAND (ME-390520)

- THERMAL SHIELD ALUMINUM SPACER, 12.4 LONG (MA-390553)

- SHIELD ASSEMBLY ALUM SPACER (MA-390373)

- SHIELD ASSEMBLY RETAINING WASHER (MA-390378)

- Q1-Q2 INTERCONNECT SHIELD INNER BLANKET (ME-390546)

- Q1-Q2 INTERCONNECT SHIELD OUTER BLANKET (ME-390547)

- INTERCONNECT THERMAL SHIELD, U- BOLT (MB-390554)

- M5 X 16 CAP SCREW (MA-393028)

- M5 X 25 CAP SCREW (MA-393053)

- 1/4-20 HEX JAM NUT (MA-393054)

- M5 LOCK WASHER (MA-393056)

- M5 FLAT WASHER (MA-393057)

- Shield Insulation

  - Wrap thermal shielding with MLI blankets as per Q1 to Q2 Main Assembly (ME-390867).

##### Parts list

- SHIELD MLI INSULATION – OUTER BLANKET (ME-390547)

- SHIELD MLI INSULATION – INNER BLANKET (ME-390546)

- Connect the vacuum shell sleeve and bellows

  - Reposition the outer vacuum shell and vacuum bellows over the interconnect region, and attach per Q1 to Q2 Main Assembly (ME-390867).

##### Parts list

- Claw Clamps (MA-393337, PROVIDED BY CERN)

- Install Threaded Rods

  - Install Threaded Rods (Qty. 4) (MA-393041) as per Q1 to Q2 Main Assembly (ME-390867).

##### Parts list

- THREADED RODS (MA-393041)

- M30 X 3.5 HEX NUT (MA-393044)

- M30 SPHERICAL WASHER (MA-393043)

# Text boxes

(Side View)

(Top View)

Apply Loctite.

Spacing between loops should be ~ 1.5 cm.