WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A13245 | In-Flight Anomaly Number -- | Contractor Report Number P-068 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LH2 FEEDLINE UMBILICAL FLANGE DOES NOT MEET DESIGN REQUIREMENTS |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (1) B (X) C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE LH2 FEEDLINE | PART# PD4800184 | SER/LOT# ET-59 | MANUFACTURER ARROWHEAD |
| Test/Operation L - FLD | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode UC - UNSAT | Cause MA - MFG-ASY |
| System PROPULSION | Defect MC - MISFIT | Material N - HOLE | Work Contact S. PARIKH | Fail Date 07/08/1990 |
| Received at MSFC 10/15/1990 | Date Isolated 09/25/1990 | FMEA Reference 2.5.8.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom EV - NOT-TO-SPEC | Time Cycle -- |
| Effectivity Text ETS-35, 41-58, 60-63 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date 01/31/1991 | Contractor Req Defer Until Date 07/15/1992 | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary REFERENCE: MARS T100571 AND T100581 |
| Last MSFC Update 02/13/1995 | CN RSLV SBMT 04/28/1993 | Defer Date 11/20/1992 | Add Date 10/19/1990 | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design W. PATTERSON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR P. COUNTS |
| Approval |
| Design W. PATTERSON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR P. COUNTS |
| PAC Assignee B. HURST | PAC Review Complete BH | MSFC Closure Date 05/18/1993 | Status C - CLOSED | F/A Completion 01/17/1991 |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary OPEN, REV. A RECEIVED 1/31/91 CLOSURE SUBMITTED TO MSFC BY REV.B CLOSURE REJECTED BY MSFC CRITICALITY UPGRADED AND DEFERRAL RATIONALE SUBMITTED BY REV. F, 11/12/91 |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description PROBLEM DESCRIPTION: AS A RESULT OF THE HYDROGEN LEAK DETECTED ON ET-37 DURING TANKING, MMC MANAGEMENT DIRECTED INSPECTION OF TWO EACH LH2 FEEDLINE AND RECIRCULATION LINE UMBILICAL FLANGES AT MAF FOR COMPLIANCE WITH DESIGN REQUIREMENTS. THE INSPECTION REVEALED THAT THE LH2 FEEDLINE UMBILICAL FLANGE DID NOT MEET DESIGN REQUIREMENTS. (REF. MARS T100571 AND T100581). ADDITIONALLY, FOUR MORE LH2 FEEDLINE UMBILICAL FLANGES WERE INSPECTED AT KSC AND TWO MORE LH2 FEEDLINE UMBILICAL FLANGES WERE INSPECTED AT THE VENDOR (ARROWHEAD). THESE FEEDLINES ALSO VIOLATED ENGINEERING REQUIREMENTS. FURTHER MORE, INSPECTION OF ONE EACH LO2 FEEDLINE ELBOW, GH2 AND GO2 PRESSLINE WAS DIRECTED BY MMC MANAGEMENT TO ASSURE THAT THE OUT-OF TOLERANCE CONDITION(S) WITNESSED ON LH2 FEEDLINE DOES NOT EXIST ON OTHER INTERFACING PROPULSION LINES THE LH2 RECIRCULATION LINES, GO2 AND GH2 PRESSLINES AND LO2 FEEDLINE ELBOW INSPECTED AT MAF WERE WITHIN ENGINEERING REQUIREMENTS GENERAL: DURING TANKING OF ET-37, A HYDROGEN LEAK WAS DETECTED IN THE SURROUNDING AREA OF ET/ORBITER QUICK DISCONNECT AND LH2 FEEDLINE. THIS UNUSUAL CIRCUMSTANCE PROMPTED AN INVESTIGATION WHICH INCLUDED DIMENSIONAL INSPECTION OF TWO HYDROGEN FEEDLINE UMBILICAL FLANGES FOR COMPLIANCE WITH DESIGN REQUIREMENTS. THE INSPECTION DATA INDICATED THAT THE LH2 FEEDLINE UMBILICAL FLANGE DID NOT MEET THE DESIGN REQUIREMENTS FOR INSIDE DIAMETER, OUTSIDE DIAMETER, BOLT HOLE COORDINATE MEASUREMENTS, HOLE DIAMETER, BOLT CIRCLE DIAMETER, AND WAVINESS. THE FLANGE FLATNESS WAS WITHIN THE PD REQUIREMENTS BUT DID NOT MEET THE ICD REQUIREMENTS TO FURTHER UNDERSTAND THE CONDITION EXPERIENCED ON THE ET-59 AND 60 LH2 FEEDLINES, A DECISION WAS MADE TO DIMENSIONALLY INSPECT TWO LH2 FEEDLINE UMBILICAL FLANGES IN-PROCESS AT ARROWHEAD (ONE AT SUB-ASSEMBLY LEVEL AND ONE POST ATP), AND FOUR LH2 FEEDLINE UMBILICAL FLANGES FOR INSIDE/OUTSIDE DIAMETER AND FLANGE THICKNESS AT KSC. INSPECTION DATA INDICATED THAT ALL THE ABOVE CAPTIONED LH2 FEEDLINES DID NOT MEET THE DESIGN REQUIREMENTS. IN ADDITION TO ABOVE, EVALUATION OF ARROWHEAD'S MANUFACTURING PROCESS FLOW INDICATED IN-PROCESS AND POST ATP MANUFACTURING AND INSPECTION DEFICIENCIES THE CAPS IS ISSUED TO INVESTIGATE THESE OCCURRENCES AND TO IMPLEMENT CORRECTIVE ACTIONS AS REQUIRED MMC NOTE: SINCE THE ANOMALIES WERE NOT IDENTIFIED AS A RESULT OF LEAKAGE, THIS CAPS IS DESIGNATED AS CRITICALITY 3 11/13/91 PAC NOTE: CRITICALITY UPGRADED TO CRITICALITY 1 BY REV. F |
| Contractor Investigation/Resolution |
| MSFC Response/Concurrence CAUSE MOST PROBABLE CAUSE FOR OUT OF TOLERANCE CONDITION IS RESIDUAL STRESSES FROM WELD PROCESS COUPLED WITH IN-PROCESS INSPECTION POINT DEFICIENCIES TASK I PROBLEM/FAILURE INVESTIGATION 1. PROCUREMENT QUALITY AND ENGINEERING EVALUATE ARROWHEAD'S MANUFACTURING FLOW TO DETERMINE POSSIBLE CONTRIBUTORS TO THE OUT-OF-TOLERANCE CONDITIONS AND IMPLEMENT CORRECTIVE ACTION COMPLETED: 11/13/90 CLOSURE STATEMENT PROCUREMENT QUALITY AND ENGINEERING HAS REVIEWED THE MANUFACTURING FLOW AT ARROWHEAD PRODUCTS IN ORDER TO DETERMINE IF ANY DEFICIENCIES EXIST THIS REVIEW INCLUDED THE FLANGE DETAIL, ELBOW CONSTRUCTION AND TOP ASSEMBLY PLANNING. SINCE NO CONCLUSIVE DEFICIENCIES WERE FOUND, ARROWHEAD HAS BEEN DIRECTED VIA CHANGE ORDER TO IMPLEMENT ADDITIONAL INSPECTIONS. THESE INSPECTIONS ARE REQUIRED ON THE NEXT FIVE PRODUCTION UNITS. INSPECTION RESULTS FROM THE FIRST TWO UNITS WILL BE UTILIZED TO DETERMINE THE CAUSE OF THE DISCREPANCIES. INSPECTION RESULTS FROM THE THREE SUBSEQUENT UNITS WILL BE UTILIZED TO VERIFY THE EFFECTIVENESS OF THE CORRECTIVE ACTIONS. TO ENHANCE ARROWHEADS MANUFACTURING PROCESS, THE DRILL FIXTURE T12A6012 HAS BEEN MODIFIED FOR TOOLING HOLES AS DEPICTED IN THE REVISED PD DRAWING. ALSO THE INSPECTION PROCESS/TOOLS FOR FLANGE FLATNESS HAS BEEN IMPROVED. (REF. I.O.M. 3761-90-159 AND CONTRACT #M60020 CHANGE ORDER 24) 2. ENGINEERING PROVIDE RATIONALE FOR ACCEPTANCE OF THE LH2 FEEDLINES WITH ABOVE CAPTIONED DISCREPANCIES ECD: 10/26/90 SECOND ECD: 1/11/91 COMPLETED: 1/17/91 CLOSURE STATEMENT THE HARDWARE MEETS THE INTENT OF THE ICD AS THE LH2 FEEDLINE FLANGES, SEAL AND UMBILICAL DISCONNECT HAVE MATED WITHOUT DIFFICULTY. ALSO VISUAL OBSERVATION OF SEAL LOCATION ON FLANGE DURING ASSEMBLY HAS APPEARED NORMAL (AS VERIFIED BY RELIABILITY ASSURANCE REVIEW OF THE COMPLETED BUILD RECORDS), AND THE SUCCESSFUL LEAK CHECKS PERFORMED AT MAF AND KSC (OMRSD AND DURING ROSAN INSERT VERIFICATION) ASSURES THE SEALING CAPABILITY OF FLANGE TO THE SEAL. BASED ON THE ABOVE, FLEET LH2 FEEDLINE/DISCONNECT JOINT ASSEMBLIES ARE PROPERLY MATED AND FUNCTIONALLY CAPABLE FOR FLIGHT. (REF: IOM 3515-90-002) 3. ENGINEERING REVIEW THE ICD REQUIREMENTS TO PD AND VENDOR DRAWINGS TO ASSURE COMPATIBILITY OF DRAWINGS ECD: 10/19/90 SECOND ECD: 1/11/91 COMPLETED: 1/17/91 CLOSURE STATEMENT AN ENGINEERING REVIEW OF ICD REQUIREMENTS TO PD AND VENDOR DRAWINGS IDENTIFIED THAT THE DESIGN IS ADEQUATE BUT NOT IN TOTAL COMPLIANCE WITH THE ICD. A REVISION TO THE ICD FOR OUTSIDE DIAMETER, INSIDE DIAMETER, AND BOLT HOLE TRUE POSITION HAS BEEN INITIATED. (REF. PIRN #TC-0512 TO ICD-2-12001 AND IOM 3515-90-002) 4. ENGINEERING REVIEW AND CLARIFY THE FLANGE WAVINESS REQUIREMENTS TO IDENTIFY WHETHER MEASUREMENT SHOULD BE RADIALLY, CIRCUMFERENTIALLY OR BOTH ECD: 10/19/90 SECOND ECD: 1/11/91 COMPLETED: 1/17/91 CLOSURE STATEMENT ENGINEERING EVALUATION OF FLANGE FLATNESS AND WAVINESS HAS RESULTED IN CLARIFICATION OF THE ICD REQUIREMENTS. (REF. IOM 3515-90-002) 5. RELIABILITY ASSURANCE ISSUE DC&R TO VERIFY DIMENSIONS ON LH2 FEEDLINE UMBILICAL FLANGES FOR ETS THAT REQUIRE UMBILICAL REPLACEMENT COMPLETED: 10/8/90 CLOSURE STATEMENT DC&R P-90-002 ISSUED TO DIMENSIONALLY INSPECT THE LH2 FEEDLINE UMBILICAL FLANGES ON ETS 42, 44, 45, 48, 49, 51, AND 55 6. PROCUREMENT QUALITY MATERIEL AND ENGINEERING EVALUATE DATA FROM THE FIRST TWO PRODUCTION UNITS (PER ITEM 1) TO SPECIFICALLY DETERMINE THE CAUSE FOR THE OUT-OF-TOLERANCE CONDITIONS EXPERIENCED ON THE LH2 FEEDLINE COMPLETED: 10/15/91 CLOSURE STATEMENT THE INPROCESS DIMENSIONAL INSPECTION DATA FROM S/N 146, 147 AND 148 REVEALED THAT STRESSES ARE INDUCED DURING THE WELDING OPERATION. THE POSSIBLE CAUSE OF THE OUT OF TOLERANCE CONDITION CAN BE ATTRIBUTED TO THE RESIDUAL STRESS 7. PRELIMINARY EVALUATION OF THE DATA OBTAINED FROM TASK I ITEM 6 INDICATED THAT THE OUT OF TOLERANCE CONDITION MAY BE ATTRIBUTED TO THE RESIDUAL STRESSES AFTER WELDING. FLANGE SUB-ASSEMBLY FOR S/N 152 HAS BEEN SUBJECTED TO A STRESS RELIEVING OPERATION. INCREMENTAL INSPECTION DATA FROM PRE-WELD THROUGH ATP WILL BE RECEIVED AND ANALYZED. PRO- CUREMENT QUALITY, MATERIEL, AND ENGINEERING DEPARTMENTS WILL EVALUATE THE DATA FROM INCREMENTAL INSPECTIONS TO ACCESS THE EFFECTS OF THE STRESS RELIEVING OPERATION ECD: 6/28/92 SECOND ECD: 11/6/92 COMPLETED: 4/21/93 CLOSURE STATEMENT TO VERIFY THAT THE STRESS RELIEF OPERATION WOULD ELIMINATE THE CAUSE OF THE DIMENSIONAL ERRORS IN THE INSIDE AND OUTSIDE DIAMETER, THE FLANGE SUB ASSEMBLY OF S/N 152 WAS STRESS RELIEVED AFTER THE WELDING OPERATION AND DIMENSIONALLY MEASURED AT SEVERAL MILESTONES IN THE PRODUCTION FLOW THE DATA RECEIVED AND EVALUATED BY ENGINEERING AND RELIABILITY ASSURANCE INDICATES THAT THE STRESS RELIEF OPERATION AFTER WELDING STABILIZED THE FLANGE AND THE DIMENSIONS STAYED WITHIN THE DRAWING REQUIREMENTS TASK II CORRECTIVE ACTIONS CORRECTIVE ACTIONS AS A RESULT OF TASK I, THE FOLLOWING CORRECTIVE ACTIONS HAVE BEEN IMPLEMENTED BOLT HOLE DIAMETER VENDOR IMPLEMENTED A REAMING OPERATION AFTER DRILLING AND ALSO ADDED ADDITIONAL IN PROCESS INSPECTION FLANGE FLATNESS VENDOR REVISED POST ATP LAPPING PROCESS AND FLANGE FLATNESS INSPECT- TION METHOD; MMMSS PROVIDED SUPPLIER WITH A FLATNESS MEASURING TOOL IN ADDITION, MMMSS DRAWING (PD4800184) HAS BEEN REVISED TO REFLECT FLATNESS REQUIREMENT PER ICD FLANGE WAVINESS VENDOR REVISED THE POST ATP LAPPING PROCESS INSIDE DIAMETER ICD REVISED TO RELAX THE REQUIREMENT FROM 16.875+/-0.010 TO 16.880+/-0.030 (REF IRN0461) OUTSIDE DIAMETER ICD REVISED TO RELAX REQUIREMENT FROM 19.062+/-0.010 TO 19.042 MINIMUM (REF. IRN0461) BOLT HOLE COORDINATE MEASUREMENT (TRUE POSITION) - VENDOR REVISED MANUFACTURING PROCESS FOR SHIMS - VENDOR ADDED CLAMPING REQUIREMENT FOR STABILITY DURING DRILLING (REF. IOM MTO-0792-SMG-016 AND 4114-92-019) - TOOLING HOLES WERE ADDED TO MINIMIZE DEFLECTION BETWEEN ELBOW AND DRILL JIG - MMMSS PROVIDED DRILL FIXTURE T2A6196 (REF. IOM 4120-93-018) - ICD REVISED TO RELAX REQUIREMENT FOR THE TRUE POSITION FROM 0.010 INCH TO 0.020 INCH (REF. IRN0461) 2. PROCUREMENT QUALITY, ENGINEERING AND MATERIEL OBTAIN CORRECTIVE ACTION TO RESOLVE THE CAUSE DETERMINED BY TASK I ITEM 7 ECD: 7/15/92 SECOND ECD: 11/16/92 COMPLETED: 4/21/93 CLOSURE STATEMENT THROUGH EVALUATION OF DATA RECEIVED FROM THE SUPPLIER, THE STRESS RELIEF OPERATION WAS FOUND TO HAVE STABILIZED THE FLANGE ASSEMBLY THROUGHOUT THE BUILD PROCESS. THE MANUFACTURING PROCESS PLANS HAVE BEEN REDLINED TO STRESS RELIEVE TWO ADDITIONAL LINES. THE DATA FROM ALL THREE LINES WILL BE EVALUATED TO DETERMINE WHETHER THE STRESS RELIEVING OPERATION IS A COST EFFECTIVE ENHANCEMENT AND SHOULD BE PERMANENTLY INCLUDED IN THE PROCESS. (REF. IOM 4114-92-022) TASK III CLEARANCE OF EFFECTIVITIES ALL ETS CLEARED BASED ON SUCCESSFUL INSTALLATION AND LEAK TEST OF THE LH2 FEEDLINES AT MAF AND KSC. THIS SATISFIES THE FINAL CIL RETENTION RATIONALE NOTE: THIS IS ALSO THE DEFERRAL RATIONALE TASK IV CAPS CLOSURE SUMMARY THE LH2 FEED LINES INSPECTED AT MAF WERE FOUND TO HAVE SEVERAL DIMENSIONAL ANOMALIES ASSOCIATED WITH THE ICD REQUIREMENTS. AN INVESTIGATION AT THE SUPPLIER WAS CONDUCTED AND CAUSE AND CORRECTIVE ACTIONS FOR THESE ANOMALIES WERE ESTABLISHED. THE FEED LINE ASSEMBLY FOR S/N 152 WAS INSPECTED THROUGH PRE-ATP WHICH INCORPORATED ALL THE CORRECTIVE ACTIONS AND A POST WELD STRESS RELIEVING OPERATION ON THE ELBOW. (SEE TASK II). THE FEED LINE FLANGE MET ALL DRAWING DIMENSIONAL REQUIREMENTS. BASED ON THE MEASUREMENTS OBTAINED FROM S/N 152, THE RELAXED ICD REQUIREMENTS, AND THE REVISED MMMSS DRAWING REQUIREMENTS, NO FURTHER CORRECTIVE ACTION IS REQUIRED ALTHOUGH THE ICD CHANGE RESOLVED THE OVALITY PROBLEM, THE SUPPLIER AND ENGINEERING ARE CONTINUING TO EVALUATE THE STRESS RELIEVING OPERATION AND WILL PERMANENTLY IMPLEMENT IT AS AN ENHANCEMENT IF IT PROVES TO BE COST EFFECTIVE ************************************************************************ 2/15/91 - PAC NOTE: CLOSURE SUBMITTAL REJECTED ************************************************************************ CLOSURE SUBMITTED BY MMMSS TO MSFC ON 2/4/91. CLOSURE WAS REJECTED ON 2/15/91 ********************************************************************* PAC NOTE: DEFERRAL RATIONALE SUBMITTED FOR MSFC REVIEW 11/14/91 ********************************************************************* 11/14/91 - DEFERRAL RATIONALE: THIS PROBLEM HAS BEEN DEFERRED FOR THE NEXT SIX MONTHS PER NSTS 08126, REVISION D, PARAGRAPH 3.3.10.1, ITEM D WHICH STATES "THE PROBLEM CONDITION IS CLEARLY SCREENED BY PREFLIGHT CHECKOUT OR SPECIAL TESTS (I.E., FAILURE MODE SHOULD NOT OCCUR FOLLOWING THE TEST)." APPROVAL: _____CRAIG E. SUMNER (SIGNED)___________ DATE: __11/14/91____ FOR GERALD C. LADNER ET PROJECT MANAGER ************************************************************************ 5/6/92 - DEFERRAL RATIONALE ************************************************************************ THIS PROBLEM HAS BEEN DEFERRED FOR THE NEXT SIX (6) MONTHS PER NSTS 08126, REVISION D, PARAGRAPH 3.3.10.1, ITEM D WHICH STATES "THE PROBLEM CONDITION IS CLEARLY SCREENED BY PREFLIGHT CHECKOUT OR SPECIAL TESTS (I.E. FAILURE MODE SHOULD NOT OCCUR FOLLOWING THE TEST)." APPROVAL:____GERALD C. LADNER(SIGNED)__ DATE:___5/22/92______ GERALD C. LADNER ET PROJECT MANAGER ************************************************************************ 11/19/92 - DEFERRAL RATIONALE: ************************************************************************ THIS PROBLEM HAS BEEN DEFERRED FOR THE NEXT SIX (6) MONTHS PER NSTS 08126, REVISION D, PARAGRAPH 3.3.10.1, ITEM D WHICH STATES "THE PROBLEM CONDITION IS CLEARLY SCREENED BY PREFLIGHT CHECKOUT OR SPECIAL TESTS (I.E. FAILURE MODE SHOULD NOT OCCUR FOLLOWING THE TEST)." APPROVAL:PARKER COUNTS (SIGNED) DATE:__11/20/92______ PARKER COUNTS ET PROJECT MANAGER |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A13245 | IFA# -- | Contractor RPT# P-068 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD4800184 | Asmnt Part Name LH2 FEEDLINE | Asmnt Serial/Lot# ET-59 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MA - MFG-ASY | FAIL MODE UC - UNSAT |
| Asmnt FMEA 2.5.8.1 | Asmnt FM 1 | FMEA CSE C | FMEA SCSE 2 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |