July 22, 1994

Contract #TW0592

SPECIAL STANDARD SPECIFICATION

SECTION 10160-S

TOILET PARTITIONS

Page

PART 1 - GENERAL

1.01	Description Of Work	2

1.02	Submittals	2

1.03	Quality Assurance	2

1.04	Produce Delivery, Storage And Handling	2

PART 2 - PRODUCTS

2.01	Manufacturers	3

2.02	Materials	3

2.03	Fabrication	4

2.04	Finishes	5

PART 3 - EXECUTION

3.01	Installation	5

3.02	Adjust And Clean	65

SPECIAL STANDARD SPECIFICATION

SECTION 10160-S

TOILET PARTITIONS

PART 1 - GENERAL

1.01	DESCRIPTION OF WORK

A.	Extent of toilet partitions is indicated on drawings.

B.	Types of Toilet Compartments and Screens Include:  Metal -- baked enamel finish

C.	Styles of Toilet Compartments Include:  Floor anchored, overhead braced

D.	Styles of Screens Include:  Floor anchored

E.	Toilet accessories are specified elsewhere in Division 10.

1.02	SUBMITTALS

A.	Product Data:  Submit manufacturer's detailed technical data for materials, fabrication, and installation, including catalog cuts of anchors, hardware, fastenings, and accessories.

B.	Shop Drawings:  Submit shop drawings for fabrication and erection of toilet partition assemblies not fully described by product drawings, templates, and instructions for installation of anchorage devices built into other work.

C.	Samples:  Submit full range of color samples for comparison to colors of other products.

1.03	QUALITY ASSURANCE

A.	Field Measurements:  Take field measurements prior to preparation of shop drawings and fabrication where possible, to ensure proper fitting of work.  Allow for adjustments within specified tolerances wherever taking of field measurements before fabrication might delay work.

B.	Coordination:  Furnish inserts and anchorages which must be built into other work for installation of toilet partitions and related work; coordinate delivery with other work to avoid delay.

1.04	PRODUCE DELIVERY, STORAGE AND HANDLING

A.	Delivery:  Deliver materials in manufacturer's original unopened and undamaged packages.  Clearly identify manufacturer, brand name, contents, color, stock number, and order number on each package.

B.	Storage:  Store in original packaging under protective cover and protect from damage.  Stack containers in accordance with manufacturer's recommendations.

C.	Handling:  Handle materials in accordance with manufacturer's instructions to prevent damage to products and finishes.

PART 2 - PRODUCTS

2.01	MANUFACTURERS

A.	Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products which may be incorporated in the work, but are not limited to, the following:

1.	Accurate Partitions Div., United States Gypsum Co.

2.	Bobrick Washroom Equipment, Inc.

3.	General Partitions Mfg. Corp.

4.	Global Steel Products Corp.

5.	Knickerbocker Partition Corp.

6.	Metpar Steel Products Corp.

7.	Sanymetal Products Co.

2.02	MATERIALS

A.	General:  Provide materials which have been selected for surface flatness and smoothness.  Exposed surfaces which exhibit pitting, seam marks, roller marks, stains, discolorations, telegraphing of core material, or other imperfections on finished units are not acceptable.

B.	Steel Sheets for Baked Enamel Finish:  ASTM A591, Class C, galvanized-bonderized, of following minimum thicknesses:

1.	Pilasters (Overhead Braced):  20 gage

2.	Pilasters (Unbraced):  16 gage

3.	Panels and Screens:  20 gage

4.	Doors:  22 gage

C.	Concealed Anchorage Reinforcement:  Minimum 12 gage galvanized steel sheet.

D.	Concealed Tapping Reinforcement:  Minimum 14 gage galvanized steel sheet.

E.	Core Material for Metal Partitions:  Manufacturer's standard sound-deadening honeycomb of impregnated Kraft paper, in thickness to provide finished dimension of 1" minimum for doors, panels, and screens, 1-1/4" minimum for pilasters.

F.	Pilaster Shoes:  ASTM A167, Type 302/304 stainless steel, not less than 3" high, 20 gage, finished to match hardware.

G.	Stirrup Brackets:  Manufacturer's standard design for attaching panels to walls and pilasters, either chromium-plated non-ferrous cast alloy ("Zamac") or anodized aluminum.

H	Hardware and Accessories:  Manufacturer's standard design, heavy-duty operating hardware and accessories of chromium-plated non-ferrous cast alloy ("Zamac").

I.	Overhead Bracing:  Continuous extruded aluminum, anti-grip profile, with clear anodized finish.

J.	Anchorages and Fasteners:  Manufacturer's standard exposed fasteners of stainless steel, chromium-plated steel, or brass finished to match hardware, with theft-resistant type heads and nuts. For concealed anchors, use hot-dip galvanized, cadmium-plated, or other rust-resistant protective-coated steel.

2.03	FABRICATION

A.	General:  Furnish standard doors, panels, screens, and pilasters fabricated for partition system, unless otherwise indicated.  Furnish units with cutouts, drilled holes, and internal reinforcement to receive partition-mounted hardware, accessories, and grab bars, as indicated.

B.	Door Dimensions:  Unless otherwise indicated, furnish 24" wide in-swinging doors for ordinary toilet stalls and 32" wide (clean opening) out-swinging doors at stalls equipped for use by handicapped.

C.	Metal Toilet Partitions and Screens:  Pressure laminate seamless face sheets to core material and seal edges with continuous interlocking strip or with lapped and formed edges.  Weld edges and corners, with exposed welds ground smooth.

D.	Overhead-Braced Partitions:  Furnish galvanized steel supports and leveling bolts at pilasters, as recommended by manufacturer, to suit floor conditions.  Make provisions for setting and securing continuous extruded aluminum anti-grip overhead bracing at top of each pilaster.  Furnish shoe at each pilaster to conceal supports and leveling mechanism.

E.	Floor-Supported Screens:  Furnish pilasters not less than 1" in thickness, panels and pilasters of same construction and finish as toilet partitions.  Furnish galvanized steel anchorage devices, complete with threaded rods, lock washers, and leveling adjusting nuts at pilasters, to permit structural connection to floor.  Furnish shoe at pilaster to conceal anchorage.

F.	Hardware:  Furnish hardware for each compartment in partition system, as follows:

1.	Hinges:  Cutout inset type, adjustable to hold door open at any angle up to 90 degrees.  Provide gravity type, spring-action cam type, or concealed torsion rod type, to suit manufacturer's standards.

2.	Latch and Keeper:  Recessed  latch unit, designed for emergency access, with combination rubber-faced door strike and keeper.

3.	Coat Hook:  Manufacturer's standard unit, combination hook and rubber-tipped bumper, sized to prevent door hitting mounted accessories.

4.	Door Pull:  Manufacturer's standard unit for out-swing doors.

2.04	FINISHES

A.	Baked Enamel Finish

1.	Clean galvanized steel surfaces after fabrication and before application of enamel coating system, to remove processing compounds, oils, and other contaminants.

2.	Prime metal with baked-on rust-inhibitive primer.

3.	Apply two coats of thermostating enamel finish, applied by electrostatic process, and baked in accordance with paint manufacturer's instructions.

4.	Color:  WhiteManufacturer's standard colors in each room as selected by SDR.

PART 3 - EXECUTION

3.01	INSTALLATION

A.	General:  Comply with manufacturer's recommended procedures and installation sequence.  Install partitions rigid, straight, plumb, and level.  Provide clearances of not more than 1/2" between pilasters and panels, and not more  than 1" between panels and walls.  Secure panels to walls with not less than two stirrup brackets attached near top and bottom of panel.  Locate wall brackets so that holes for wall anchorages occur in masonry or tile joints.  Secure panels to pilasters with not less than two stirrup brackets located to align with stirrup brackets at wall.  Secure panels in position with manufacturer's recommended anchoring devices.  Repair wall surfaces damaged during installation.

B.	Overhead-Braced Partitions:  Secure pilasters to floor and level, plumb, and tighten installation with devices furnished.  Secure overhead brace to each pilaster with not less than two fasteners.  Hang doors and adjust so that tops of doors are parallel with overhead brace when doors are in closed position.

C.	Screens:  Attach with concealed anchoring devices, as recommended by manufacturer, to suit supporting structure.  Set units to provide support and to resist lateral impact.

3.02	ADJUST AND CLEAN

A.	Hardware Adjustment:  Adjust and lubricate hardware for proper operation.  Set hinges on in-swinging doors to hold open approximately 30 degrees from closed position when unlatched.  Set hinges on out-swinging doors (and entrance swing doors) to return to fully closed position.

B.	Clean exposed surfaces of partition systems using materials and methods recommended by manufacturer, and provide protection as necessary to prevent damage during remainder of construction period.

END OF SECTION