Table 1

Uses of Fatty Acid Dimers and Trimer

| Substance | CAS # | Primary Function | Use Category | Major End Use Application | % |
| --- | --- | --- | --- | --- | --- |
| Dimer | 61788-89-4 | Chemical intermediate (feed for polyamide resins) | Industrial | Printing inks Coatings Adhesives | 30 40 30 |
| Trimer | 68937-90-6 | Chemical intermediate | Industrial | Oil drilling Lubes | 85 15 |
| Hydrogenated dimer | 68783-41-5 | Chemical intermediate (feed for polyamide resins) | Industrial | Adhesives Coatings | 80 20 |
| Crude dimer | 71803-39-4 | Chemical intermediate | Industrial | Monomer, dimer & trimer Oil drilling | 90 10 |