## Database for Solder Properties with Emphasis on New Lead-free Solders

## National Institute of Standards and Technology

&

Colorado School of Mines

## Properties of Lead-Free Solders

Release 3.0

## Dr. Thomas Siewert

National Institute of Standards and Technology

Dr. Stephen Liu

Colorado School of Mines

Dr. David R. Smith

National Institute of Standards and Technology

Mr. Juan Carlos Madeni

Colorado School of Mines

Colorado, May 31, 2001

## Properties of Lead-Free Solders

Disclaimer: In the following database, companies and products are sometimes mentioned, but solely to identify materials and sources of data. Such identification neither constitutes nor implies endorsement by NIST of the companies or of the products. Other commercial materials or suppliers may be found as useful as those identified here.

Note: Alloy compositions are given in the form “Sn-2.5Ag-0.8Cu-0.5Sb,” which means: 2.5 % Ag, 0.8 % Cu, and 0.5 % Sb (percent by mass), with the leading element (in this case, Sn) making up the balance to 100 %.

Abbreviations for metallic elements appearing in this database:

| Ag: silver | Cu: copper | Pt: platinum |
| --- | --- | --- |
| Al: aluminum | In: indium | Sb: antimony |
| Au: gold | Mo: molybdenum | Sn: tin |
| Bi: bismuth | Ni: nickel | W: tungsten |
| Cd: cadmium | Pb: lead | Zn: zinc |
| Cr: chromium | Pd: palladium |  |

Table of Contents:

- Mechanical Properties: creep, ductility, activation energy, elastic modulus, elongation, strain rate, stress relaxation, tensile strength, yield strength

Table 1.1. Strength and Ductility of Low-Lead Alloys Compared with Alloy Sn-37Pb (NCMS Alloy A1), Ranked by Yield Strength (15 Alloys) and by Total Elongation (19 Alloys)

Table 1.2. Tensile Properties of Lead-Free Solders (two parts)

Table 1.3. Elastic Properties of Sn-37Pb (eutectic) and Sn-3.5Ag

###### Table 1.4. Elastic Properties of Sn-2.5Ag-0.8Cu-0.5Sb (Castin™) and Sn-37Pb Eutectic-A

###### Table 1.5. Elastic Properties of Sn-2.5Ag-0.8Cu-0.5Sb (Castin™) and Sn-37Pb Eutectic-B

Table 1.6. Parameters for Strain Rate: Norton Equation, dε/dt = A·σn·exp(-Q/(RT)); Dorn Equation, dε/dt = A·(σn/T)·exp(-Q/(RT)); Stress-relaxation Rate, dσ/dt = A·(σ-σt)n ·exp(-Q/(RT)); and Strain-Rate Sensitivity, σ = C·(dε/dt)m; for Two Lead-Free Solder Alloys, Sn-3.5Ag and Sn-9Zn.

Table 1.7. Steady-state Creep Properties and Associated Mechanisms for Three Lead-Free Solders and Sn-37Pb Eutectic

Table 1.8. Stress Exponents and Activation Energies for Dorn Equation for Tin and Four Lead-Free Solder Alloys

Table 1.9. Activation Energy versus Strain Rate for Two Lead-Free Eutectic Solders (Sn-3.5Ag and Sn-9Zn)

Table 1.10. Elastic Properties of Metallic Elements Used In Electronic Packaging

Table 1.11. Material Properties of a Via-in-Pad Chip-Scale Package Printed Circuit Board (PCB) Assembly

###### Table 1.12. Elastic Properties and Thermal Expansion Coefficient of Electronic-Packaging Materials and Lead Solder Alloys

Table 1.13. Lead-free Solder Alloys: Tensile and Shear Strengths

Table 1.14. Lead-containing Solder Alloys: Tensile and Shear Strengths

Table 1.15. Shear Strengths of Three Lead-Free Solders and Tin-Lead Eutectic (by Ring-and-Plug Test)

Table 1.16. Mechanical Properties of Tin, Tin-Lead, and Four Lead-Free Solder Alloys (by Ring-and-Plug Tests)

Table 1.17. Shear Strengths, Solidus and Liquidus Temperatures, and Wetting Angles of Experimental Sn-Ag-Cu Solder Alloys

Table 1.18. Physical and Mechanical Properties of Lead-Free Alloys and Sn-Pb37 (eutectic)

Table 1.19. Pure Copper, Tin and Nickel, and Their Intermetallics:  Room-Temperature Physical and Thermal Properties

Table 1.20. Effects of Transition Metals on Vickers Hardness and Ultimate Tensile Strength of Sn-4.7Ag-1.7Cu Solder Alloys

Figure 1.1. Creep data at 75oC for Sn-Ag-Cu, Sn-Ag-Bi, Sn-Ag, Sn-Bi, and Sn-Pb solder alloys

2. Thermal Properties

2.1. Solidus, Liquidus, and Melting-Point Temperatures

    - Liquidus and Reflow Temperatures of Candidate Lead-Free Solder Alloys for Replacing Eutectic Tin-Lead Solder

    - Melting Temperatures of Lead-Free Solders (two parts)

2.2. Thermal Properties: Miscellaneous

    - Thickness (μm) of Intermetallics in Solder Alloys Aged at 150 ºC

    - Thermal and Electrical Properties of Castin™ (Sn-2.5Ag-0.8Cu-0.5Sb)

    - Physical and Mechanical Properties of Sn-2.8Ag-20.0In and Sn-37Pb Eutectic Solders

    - Some Physical Properties of Materials Used as Electronic Packaging Conductors

    - Thermophysical Properties of Metallic Elements Used In Electronic Packaging

    - Some Properties of Materials Commonly Used In Electronics – A

    - Some Properties of Materials Commonly Used In Electronics – B

    - Electrical Resistivity and Temperature Coefficient of Resistance (TCR) of Pure Metallic Elements Used in Electronic Packaging

    - Wetting Properties of Sn-2.8Ag-20.0In and Sn-37Pb Eutectic Solders

    - Wetting Times and Forces (at 300 ºC): Lead-Free Solder Alloys, and Eutectic Tin-Lead

    - Wetting Times (at 250 ºC) of Lead-free Solder Alloys

    - Onset of Melting Temperatures for Five Sn-Ag-Cu Lead-Free Solder Alloys

    - Solidus Temperatures and Wetting Contact Angles of Selected Lead-Free Solder Alloys with Use of RMA (GF-1235) Flux

    - Solidus and Liquidus Temperatures and Wetting Angles of Some Lead-Free Alloys on Copper

    - Melting Properties, Resistivity, Wettability and Hardness of Lead-Free Solders

    - Wetting Contact Angles of Sn-Ag, Sn-Bi, and Sn-Zn Alloys on Copper: Eutectic, and With 1% Addition of Ternary Elements

    - Wetting Contact Angles on Copper of Sn-Bi Alloys: Eutectic, and With 1% Addition of Ternary Elements

    - Wetting Properties of Pure Tin, Four Lead-Free Tin Alloys and Three Lead-Tin Alloys

    - Lead-Free Solder Alloys: Solidus and Liquidus Temperatures, Coefficient of Thermal Expansion, Surface Tension, and Electrical Resistivity

    - Fluid Properties of Some Molten Lead-Free Solders

    - Densities and Costs of Popular Solder Metals and Alloys – A

    - Densities and Costs of Popular Solder Metals and Alloys – B

    - Cost of Lead-Free Solder Alloys Relative to That of Sn-37Pb Eutectic

A. Solder Alloys for Plated-Through Holes

- Candidate Alloys for Replacing Lead-Alloy Solders

###### Criteria for Down-Selection of Lead-Free Alloys

  - Chemical Compositions of 79 Lead-Free Solder Alloys Down-Selected for Preliminary Testing by the National Center for Manufacturing Sciences (NCMS).

##### Miscellaneous

- Major Considerations for Replacement Lead-Free Solders

  - Designation and Composition of Lead-Free Solders.

- Useful References

  - References to Tabular Data

  - Reference Books

  - Useful URLs

Key words: Alloys, aluminum, antimony, atomic weight, bibliography, bismuth, Castin, chemical, chromium, coefficient, composition, conductivity, copper, costs, creep, ductility, elastic, electrical, electronic, elements, elongation, eutectic, expansion, gold, hardness, indium, intermetallic, lead, lead-free, liquidus, material, mechanical, melting, metallic, modulus, molybdenum, nickel, packaging, palladium, physical, platinum, Poisson ratio, PCB, printed circuit board, properties, replacement, resistivity, silver, solders, solidus, strength, surface tension, temperature, tensile, thermal, thermophysical, tin, tungsten, viscosity, wetting, Young’s modulus, zinc

Useful Conversion Factors

Standard Acceleration of Gravity, g:

g = 32.174 f/s2 = 9.80665 m/ s2  (not to be confused with “gram”, g)

Electrical Conductivity:

1 S (siemens) = 1 Ω–1  (reciprocal ohm)

Density:

1 g/cm3 =  0.036127 lbm/in3  =  62.428 lbm/ft3

Energy:

1 cal = 4.187 J  (joule)

1 Btu = 1055.056 J = 252 cal = 0.252 kcal (kilocalories)

Force:

1 lbf  = 4.4482 N  (newton)

1 kgf = 9.80665 N

1 dyne = 10–5 N

Length:

1 in = 2.54 cm = 0.0254 m (exact)

1 f  = 30.48 cm = 0.3048 m (exact)

Mass:

1 lbm = 0.45359 kg;   1kg = 2.20463 lbm

Pressure (or Tensile stress):

1 Pa (pascal) = 1 N/m2

1 psi = 6894.76 Pa = 6.89476 kPa

1 kps = 6.89476 MPa

Specific Heat (Capacity):

1 cal/(g∙K) = 1 Btu/(lbm ∙F) = 4.187 J/(kg ∙K)

# Temperature; temperature intervals:

Fahrenheit temperature  F = 1.8∙C + 32, where C is Celsius temperature

Kelvin temperature K = C + 273.15

1 K (1 kelvin) = 1 ºC (1 Celsius degree) = 1.8 ºF (1 Fahrenheit degree = temperature interval)

Thermal Conductivity:

1 W/(m∙K) = 0.5778 Btu/(ft∙hr ∙˚F)

Explanatory Note:

This version (31 May 2001) represents our present collection of information on properties of lead-free solders. We are just now beginning to have enough properties data to begin consolidating duplicate data, to better organize the tables into a more useful order, and to begin some evaluation of uncertainties. Also, no systematic mining of resources from journals that publish articles on relevant properties of lead-free solders has yet been done by us, but is a planned next step. However these next steps await further funding. We hope to greatly extend the work beyond this present state into a larger and more useful one. Your patience is appreciated. – the authors

1. Mechanical Properties: creep, ductility, activation energy, elastic modulus, elongation, strain rate, stress relaxation, tensile strength, yield strength

Table 1.1. Strength and Ductility of Low-Lead Alloys Compared with Alloy Sn-37Pb (NCMS Alloy Code A1), Ranked by Yield Strength (15 Alloys) and by Total Elongation (19 Alloys)

| Alloy Code | Alloy Composition | Yield Strength (psi) | Alloy Code | Alloy Composition | Total Elongation (%) |
| --- | --- | --- | --- | --- | --- |
| C5 | Sn-2Ag-9.8Bi-9.8In | 14,560 | B6 | Sn-56Bi-2In | 116 |
| F1 | Sn-2Ag-7.5Bi-0.5Cu | 12,370 | F15 | Sn-57Bi | 77 |
| F11 | Sn-2.5Ag-19.5Bi | 12,070 | D2 | Sn-57Bi-2In | 72 |
| D10 | Sn-3Ag-54Bi-2Cu-2Sb | 11,440 | D5 | Sn-57Bi-1Sb | 60 |
| F7 | Sn-31.5Bi-3Zn | 10,500 | B2 | Sn-52Bi | 57 |
| D9 | Sn-3Ag-54Bi-2In-2Sb | 5,055 | B1 | Sn-50Bi | 53 |
| F8 | Sn-3.5Ag-1.5In | 4,616 | A8 | Sn-75Pb | 53 |
| A1 | Sn-37Pb | 3,950 | F7 | Sn-31.5Bi-3Zn | 53 |
| F10 | Sn-0.2Ag-2Cu-0.8Sb | 3,758 | A1 | Sn-37Pb | 48 |
| F3 | Sn-0.5Ag-4Cu | 3,724 | D4 | Sn-57Bi-2Sb | 47 |
| A5 | Sn-5Sb | 3,720 | A6 | Sn-58Bi | 46 |
| A8 | Sn-75Pb | 3,426 | D7 | Sn-3Ag-55.5Bi-1.5Sb | 45 |
| F2 | Sn-2.6Ag-0.8Cu-0.5Sb | 3,311 | D8 | Sn-3Ag-55Bi-2Sb | 44 |
| A4 | Sn-3.5Ag | 3,256 | F13 | Sn-55Bi-2Cu | 41 |
| A3 | Sn-97Pb | 1,126 | F2 | Sn-2.6Ag-0.8Cu-0.5Sb | 9 |
|  |  |  | C5 | Sn-2Ag-9.8Bi-9.8In | 7 |
|  |  |  | D10 | Sn-3Ag-54Bi-2Cu-2Sb | 4 |
|  |  |  | E9 | Sn-10Bi-20In | 4 |
|  |  |  | B5 | Sn-2Ag-46Bi-4Cu | 3 |

Source: Technical Reports for the Lead Free Solder Project: Properties Reports: "Room Temperature Tensile Properties of Lead-Free Solder Alloys;" Lead Free Solder Project CD-ROM, National Center for Manufacturing Sciences (NCMS), 1998

##### Table 1.2. Tensile Properties of Lead-Free Solders

(A.C.: Alloy Code (NCMS); Blank cells: no values reported)

| A.C. | Chemical Composition | Elastic Modulus | Yield Strength (0.2 % offset) | Tensile Strength | Relative Elongation (%) | Strength Coefficient | Hard-ening Expo-nent |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | % by Mass | (ksi) | GPa | (psi) | MPa | (psi) | MPa | Uni- form | Total | (psi) | MPa |  |
| A1 | Sn-37Pb | 2,273 | 15.7 | 3,950 | 27.2 | 4,442 | 30.6 | 3 | 48 | 4,917 | 33.9 | 0.033 |
| A2 | Sn-2Ag-36Pb | 2,617 | 18.0 | 6,287 | 43.3 | 6,904 | 47.6 | 1 | 31 | 7,223 | 49.8 | 0.011 |
| A3 | Sn-97Pb | 2,753 | 19.0 | 1,126 | 7.8 | 2,383 | 16.4 | 27 | 38 | 3,934 | 27.1 | 0.235 |
| A4 | Sn-3.5Ag | 3,793 | 26.2 | 3,256 | 22.5 | 3,873 | 26.7 | 3 | 24 | 4,226 | 29.1 | 0.026 |
| A5 | Sn-5Sb | 6,460 | 44.5 | 3,720 | 25.7 | 5,110 | 35.2 | 3 | 22 | 4,177 | 28.8 | 0.031 |
| A6 | Sn-58Bi | 1,720 | 11.9 | 7,119 | 49.1 | 8,766 | 60.4 | 3 | 46 | 9,829 | 67,8 | 0.029 |
| A7 | Sn-3.5Ag-0.5Sb-1Cd |  |  | 7,545 | 52.0 |  |  |  | 15 |  |  |  |
| A8 | Sn-75Pb |  |  | 3,426 | 23.6 |  |  |  | 53 |  |  |  |
| B1 | Sn-50Bi |  |  | 8,263 | 57.0 | 8,965 | 61,8 |  | 53 |  |  |  |
| B2 | Sn-52Bi |  |  | 6,414 | 44.2 | 8,834 | 60.9 |  | 57 |  |  |  |
| B5 | Sn-2Ag-46Bi-4Cu |  |  | 9,806 | 67.6 | 10,070 | 69.4 |  | 3 |  |  |  |
| B6 | Sn-56Bi-2In |  |  | 7,224 | 49.8 | 8,429 | 58.1 |  | 116 |  |  |  |
| C1 | Sn-2Ag-1.5Sb-29Pb |  |  | 6,489 | 44.7 | 6,865 | 47.3 |  | 25 |  |  |  |
| C2 | Sn-3Ag-4Cu |  |  | 6,276 | 43.3 | 7,006 | 48.3 |  | 22 |  |  |  |
| C3 | Sn-2.5Ag-2Bi-1.5Sb |  |  | 7,070 | 48.7 | 8,117 | 56.0 |  | 21 |  |  |  |
| C4 | Sn-3Ag-1Bi-1Cu-1.5Sb |  |  | 8,361 | 57.6 | 9,256 | 63.8 |  | 21 |  |  |  |
| C5 | Sn-2Ag-9.8Bi-9.8In |  |  | 14,560 | 100.4 | 15,380 | 106.0 |  | 7 |  |  |  |
| D2 | Sn-57Bi-2In |  |  | 7,304 | 50.4 | 8,436 | 58.2 |  | 72 |  |  |  |
| D3 | Sn-2Ag-57Bi |  |  | 9,487 | 65.4 | 10,390 | 71.6 |  | 31 |  |  |  |
| D4 | Sn-57Bi-2Sb |  |  | 8,521 | 58.8 | 9,586 | 66.1 |  | 47 |  |  |  |
| D5 | Sn-57Bi-1Sb |  |  | 8,285 | 57.1 | 8,944 | 61.7 |  | 60 |  |  |  |
| D6 | Sn-2Ag-56Bi-1.5Sb |  |  | 9,063 | 62.5 | 9,946 | 68.6 |  | 27 |  |  |  |
| D7 | Sn-3Ag-55.5Bi-1.5Sb |  |  | 8,665 | 59.7 | 9,379 | 64.7 |  | 45 |  |  |  |
| D8 | Sn-3Ag-55Bi-2Sb |  |  | 8,984 | 61.9 | 9,807 | 67.6 |  | 44 |  |  |  |
| D9 | Sn-3Ag-54Bi-2In-2Sb |  |  | 5,055 | 34.9 | 11,640 | 80.3 |  | 13 |  |  |  |
| D10 | Sn-3Ag-54Bi-2Cu-2Sb |  |  | 11,440 | 78.9 | 12,280 | 84.7 |  | 4 |  |  |  |

##### Tensile Properties of Lead-Free Solders (cont.)

(A.C.: Alloy Code (NCMS); Blank cells: no values reported)

| A.C. | Chemical Composition | Elastic Modulus | 0.2% Yield Strength | Tensile Strength | Relative Elongation (%) | Strength Coefficient | Hard-ening Expo-nent |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | % by Mass | (ksi) | GPa | (psi) | MPa | (psi) | Mpa | Uni- form | Total | (psi) | MPa |  |
| E1 | Sn-3Ag-2Sb |  |  | 5,749 | 39.6 | 6,124 | 42.2 |  | 25 |  |  |  |
| E2 | Sn-3Ag-2Cu-2Sb |  |  | 6,684 | 46.1 | 7,655 | 52.8 |  | 32 |  |  |  |
| E3 | Sn-3Ag-2Bi-2Sb |  |  | 6,918 | 47.7 | 9,212 | 63.5 |  | 36 |  |  |  |
| E4 | Sn-3Ag-2Bi |  |  | 5,463 | 37.7 | 7,930 | 54.7 | 6 | 30 | 8,946 | 61.7 | 0.041 |
| E5 | Sn-2.5Ag-2Bi |  |  | 6,592 | 45.5 | 7,564 | 52.2 |  | 26 |  |  |  |
| E6 | Sn-2Bi-1.5Cu-3Sb |  |  | 7,343 | 50.6 | 9,350 | 64.5 |  | 28 |  |  |  |
| E7 | Sn-2Bi-8In |  |  | 7,160 | 49.4 | 7,970 | 55.0 |  | 25 |  |  |  |
| E9 | Sn-10Bi-20In |  |  | -- | -- | 6,938 | 47.8 |  | 4 |  |  |  |
| E10 | Sn-9Zn |  |  | 7,478 | 51.6 | 7,708 | 53.1 |  | 27 |  |  |  |
| F1 | Sn-2Ag-7.5Bi-0.5Cu |  |  | 12,370 | 85.3 | 13,440 | 92.7 |  | 12 |  |  |  |
| F2 | Sn-2.6Ag-0.8Cu-0.5Sb |  |  | 3,311 | 22.8 | 3,749 | 25.8 | 2 | 9 | 4,536 | 31.3 | 0.049 |
| F3 | Sn-0.5Ag-4Cu |  |  | 3,724 | 25.7 | 4,312 | 29.7 |  | 27 |  |  |  |
| F4 | Sn-8.8In-7.6Zn |  |  | 6,033 | 41.6 | 6,445 | 44.4 |  | 14 |  |  |  |
| F5 | Sn-20In-2.8Zn |  |  | 5,095 | 35.1 | 5,381 | 37.1 |  | 31 |  |  |  |
| F7 | Sn-31.5Bi-3Zn |  |  | 10,500 | 72.4 | 11,210 | 77.3 |  | 53 |  |  |  |
| F8 | Sn-3.5Ag-1.5In |  |  | 4,616 | 31.8 | 4,987 | 34.4 |  | 26 |  |  |  |
| F9 | Sn-2Ag-0.5Bi-7.5Sb |  |  | 8,230 | 56.7 | 8,773 | 60.5 |  | 19 |  |  |  |
| F10 | Sn-0.2Ag-2Cu-0.8Sb |  |  | 3,758 | 25.9 | 4,323 | 29.8 |  | 27 |  |  |  |
| F11 | Sn-2.5Ag-19.5Bi |  |  | 12,070 | 83.2 | 13,450 | 92.7 |  | 17 |  |  |  |
| F12 | Sn-3Ag-41Bi |  |  | 9,287 | 64.0 | 10,130 | 69.8 |  | 39 |  |  |  |
| F13 | Sn-55Bi-2Cu |  |  | 8,985 | 62.0 | 9,478 | 65.4 |  | 41 |  |  |  |
| F14 | Sn-48Bi-2Cu |  |  | 8,899 | 61.4 | 9,495 | 65.5 |  | 19 |  |  |  |
| F15 | Sn-57Bi |  |  | 7,972 | 55.0 | 8,540 | 58.9 |  | 77 |  |  |  |
| F16 | Sn-56.7Bi-0.3Cu-1In |  |  | 8,359 | 57.6 | 8,985 | 62.0 |  | 38 |  |  |  |
| F17 | Sn-3.4Ag-4.8Bi |  |  | 6,712 | 46.3 | 10,349 | 71.4 | 5 | 16 | 17,795 | 122.7 | 0.153 |

Source: Technical Reports for the Lead Free Solder Project: Properties Reports: "Room Temperature Tensile Properties of Lead-Free Solder Alloys;" Lead Free Solder Project CD-ROM, National Center for Manufacturing Sciences  (NCMS), 1998

### Table 1.3. Elastic Properties of Sn-37Pb (eutectic) and Sn-3.5Ag

| Property | Sn-37Pb | Sn-3.5Ag | Sn-5Sb |
| --- | --- | --- | --- |
| Melting Point, ºC | 183 | 221 |  |
| UTS* MPa | 31 – 46 | 55 |  |
| Elongation, % | 35 – 176 | 35 |  |
| Shear Strength, MPa | 28.4 | 32.1 |  |
| Young’s Modulus§, GPa | 35§ | 56§ | 58§ |

*Ultimate Tensile Strength

Jeff D. Sigelko and K.N. Subramanian, “Overview of lead-free solders,” Adv. Mat. & Proc., pp. 47-48 (March 2000)

§ Rodney J. McCabe and Morris E. Fine, “Athermal and Thermally Activated Plastic Flow in Low Melting Temperature Solders at Small Stresses,” Scripta Materialia 39(2), 189 (1998)

Table 1.4. Elastic Properties of Sn-2.5Ag-0.8Cu-0.5Sb (Castin™) and Sn-37Pb

Eutectic - A

| Tensile Properties (1 ksi = 6.895 MPa) |
| --- |
|  | Castin™ | Sn-37Pb |
|  | (ksi) | (MPa) | (ksi) | (MPa) |
| Young’s Modulus | 7420 | 51.16 (GPa) | 4870 | 33.58 (GPa) |
| Yield Strength | 4.86 | 33.5 | 4.38 | 30.2 |
| UTS* | 5.73 | 39.5 | 4.92 | 33.92 |
| Elongation (%) | 50.00 | 52.87 |
| Compressive Properties |
|  | (ksi) | (MPa) | (ksi) | (MPa) |
| Elastic Modulus | 4260 | 29.37 (GPa) | 3990 | 27.51 (GPa) |
| Yield Strength | 4.33 | 29.85 | 4.52 | 31.16 |
| Stress (25 (/u) | 8.54 | 58.88 | 7.17 | 49.44 |
| Rockwell Hardness (15 W scale hardness) | 18.28 | 10.08 |

### *Ultimate Tensile Strength

Karl Seelig and David Suraski, “The Status of Lead-Free Solder Alloys,” Proc. 50th IEEE 2000 Electronic Components and Technology Conference (May 21-24, 2000), Las Vegas, NV

### Table 1.5. Elastic Properties of Sn-2.5Ag-0.8Cu-0.5Sb (Castin™) and Sn-37Pb

Eutectic – B

| Tensile Properties (1 ksi = 6.895 MPa) |
| --- |
|  | Castin™ | Sn-37Pb |
|  | (ksi) | (MPa) | (ksi) | (MPa) |
| Young’s Modulus | 4300 | 29.65 (GPa) | 5740 | 39.58 (GPa) |
| Yield Strength | 4.03 | 27.8 | 4.07 | 28.1 |
| UTS* | 5.56 | 38.3 | 5.91 | 40.7 |
| Elongation (%) | 50.00 | 43.66 |
| Compressive Properties |
|  | (ksi) | (MPa) | (ksi) | (MPa) |
| Young’s Modulus | 10890 | 75.08 (GPa) | 16600 | 11.45 (GPa) |
| Yield Strength (0.2% strain) | 4.53 | 31.2 | 4.84 | 33.4 |
| Stress (25 ( strain) | 10.07 | 69.4 | 9.88 | 68.1 |
| Rockwell Hardness (16 W scale hardness) | 13.5 | 12.2 |

### *Ultimate Tensile Strength

Note: It is not stated explicitly, but accompanying textual description suggests that the measured specimens of these alloys may have been first soaked at 125 (C before the properties listed in this table were measured. This may explain the differences in measured properties between this table and the previous one (A) comparing Castin™  with Sn-37Pb.

Karl Seelig and David Suraski, “The Status of Lead-Free Solder Alloys,” Proc. 50th IEEE 2000 Electronic Components and Technology Conference (May 21-24, 2000), Las Vegas, NV

Table 1.6. Parameters for Strain Rate (Norton Equation, dε/dt = A·σn·exp(-Q/RT); and Dorn Equation, dε/dt = A·(σn/T)·exp(-Q/(RT))); Stress-relaxation Rate, dσ/dt = A·(σ-σt)n ·exp(-Q/(RT)); and Strain-rate Sensitivity, σ = C·(dε/dt)m; for Two Lead-Free Solder Alloys, Sn-3.5Ag and Sn-9Zn.

Here ε is strain, t is the time variable, dε/dt is strain rate (s–1), A and C are con-stants, σ is stress (MPa), σt is a threshold stress for stress relaxation, n is the stress exponent, Q is an activation energy (kJ/mol), R is the universal gas constant, T is absolute temperature, and m is the strain-rate sensitivity.

| Alloy | Norton | Dorn | Stress Relax-ation | Tempera- ture (ºC) |
| --- | --- | --- | --- | --- |
|  | Tensile | Creep | Tensile | Creep |  | 25 | 80 |
| Sn-3.5Ag | A | 6.62·10-3 | 1.50·10-3 | 5.83 | 1.36·10-3 |  |  |  |
|  | n | 12 | 11.3 | 12 | 11.3 | 6 |  |  |
|  | Q | 108.5 | 79.5 | 111.2 | 82.3 | 33.5 |  |  |
|  | m |  |  |  |  |  | 0.080 | 0.083 |
|  | σt |  |  |  |  | 9.8 |  |  |
| Sn-9Zn | A | 9.27 | 0.0217 | 8220 | 19.1 |  |  |  |
|  | n | 8.1 | 5.7 | 8.1 | 5.7 | 4.2 |  |  |
|  | Q | 99.9 | 65.2 | 102.6 | 68.0 | 106.9 |  |  |
|  | m |  |  |  |  |  | 0.122 | 0.124 |
|  | σt |  |  |  |  | 3 |  |  |
| Sn-37Pb | n |  | 6.2* |  |  |  |  |  |
|  | Q |  | 64* |  |  |  |  |  |

*E.W. Hare and R.G. Stang, J. Electronic Mater. 21, 599 (1992)

H. Mavoori, J. Chin, S. Vaynman, B. Moran, L. Keer and M. Fine, “Creep, Stress Relaxation, and Plastic Deformation in Sn-Ag and Sn-Zn Eutectic Solders,” J. Electronic Materials, 26(7), 783 (1997)

Table 1.7. Steady-state Creep Properties and Associated Mechanisms for Three Lead-free Solders and Sn-37Pb Eutectic

| Alloy | Deformation Mechanism | B* (Mpa-n∙s-1) | ΔH (eV) | n (40 ºC) | n (140 ºC) |
| --- | --- | --- | --- | --- | --- |
| Sn-4Cu-0.5Ag | Athermal, short-range Cu clustering | 4.229×10-12 | 0.062 | 8.36 | 8.36 |
| Sn-2Cu-0.8Sb-0.2Ag | Dislocation glide / climb | 3.031 | 0.85 | 8.91 | 7.37 |
| Sn-36Pb-2Ag | Dislocation glide / climb | 0.04423 | 0.50 | 5.25 | 5.25 |
| Sn-37Pb | Dislocation glide / climb | 0.205 | 0.49 | 5.25 | 5.25 |

Y.-H. Pao, S. Badgley, R. Govila and E. Jih, “An Experimental and Modeling Study of Thermal Cyclic Behavior of Sn-Cu and Sn-Pb Solder Joints,” Mat. Res. Soc. Symp. Proc. Vol. 323, p. 128 (MRS, 1994)

[Here the steady-state creep behavior was assumed to be described by  (Norton’s Law; see previous table, “Parameters for Strain Rate”), dγcrp/dt=B*τn exp(-ΔH/(kT)), with dγcrp/dt as the rate of shear creep strain, τ the shear stress,  n a stress exponent, ΔH an activation energy, kT the product of Boltzmann’s constant and absolute temperature, and B* a material constant.]

Table 1.8. Stress Exponents and Activation Energies for Dorn Equation for Tin and Four Lead-Free Solder Alloys

| Alloy | Region 1 | Region 2 | Region 3 |
| --- | --- | --- | --- |
|  | Activation Energy, Q (kJ/mol) | Stress Exponent, n | Activation Energy, Q (kJ/mol) | Stress Exponent, n | Activation Energy, Q (kJ/mol) | Stress Exponent, n |
| Sn |  |  |  |  | 66 | 8.4 |
| Sn-2.6Sb |  |  | 115 | 5.9 | 87 | 9.0 |
| Sn-5Sb |  |  | 103 | 5.7 | 85 | 11.6 |
| Sn-7.8Sb | 68 | 0.9 | 52 | 6.2 | 49 | 9.8 |
| Sn-2Sb-2In |  |  | 71 | 5.9 | 96 | 9.3 |

Rodney J. McCabe and Morris E. Fine, “The Creep Properties of Precipitation-Strengthened Tin-Based Alloys,” JOM, p. 33 (June 2000)

Table 1.9. Activation Energy versus Strain Rate for Two Lead-Free Eutectic Solders (Sn-3.5Ag and Sn-9Zn)

| Strain Rate (s-1) | Activation energy (J/mol) |
| --- | --- |
|  | Sn-3.5Ag | Sn-9Zn |
| 10–2 | 8.56 | 12.3 |
| 10–3 | 9.97 | 12.5 |
| 10–4 | 7.90 | 12.1 |
| 10–5 | 9.70 | 12.6 |

H. Mavoori, Semyon Vaynman, Jason Chin, Brian Moran, Leon M. Keer and Morris E. Fine, “Mechanical Behavior of Eutectic Sn-Ag and Sn-Zn Solders,” Mat. Res. Soc. Symp. Proc. Vol. 390, p. 161 (MRS, 1995)

### Table 1.10. Elastic Properties of Metallic Elements Used In Electronic Packaging

| Metal | Condition | E (Elastic) (GPa) | G (Shear) (GPa) | Tensile Strength (MPa) | Yield Strength* (MPa) |
| --- | --- | --- | --- | --- | --- |
| Aluminum 99.996 | Annealed | 68.9 | 26.5 | 47.4 | 12.2 |
| Antimony |  | 77.8 |  | 11 |  |
| Copper 99.997 | Rod, cold-drawn | 127.7 | 46.8 | 351 | 340 |
| Gold 99.99 | Cast | 74.4 |  | 124 |  |
| Lead 99.90 | Rolled, aged |  |  |  | 9.5 (0.5 %) |
| Molybdenum | Pressed, sintered sheet | 340 |  | 690 |  |
| Nickel >99.0 | Wrought, annealed | 210 |  | 482 | 138 |
| Platinum 99.99 | Annealed | 147 |  | 120-130 |  |
| Silver | Strained 5 %, heated 5 hr at 350 C | 71 – 78 |  |  |  |
| Tin | Pure, cast | 41 – 45 |  | 21.4 |  |
| Tin-5Ag | Sheet, aged at room temp. |  |  | 31.7 | 24.8 |
| Tungsten |  | 340 | 135 |  |  |
| Zinc <0.10 Pb | Hot-rolled strip |  |  | 134-160 |  |

*(0.2 % offset)

D.E. Gray, ed., American Institute of Physics Handbook, pp. 2-61 ff. (McGraw-Hill, New York, 1957) [Note: original units were in dyn/cm2; 10 dyn/cm2 = 1 N/m2 = 1 Pa]

[FOLLOWING TABLE STILL NEEDS A COMPLETE DOCUMENTATION OF SOURCE]:

Table 1.11. Material Properties of a Via-in-Pad Chip-Scale Package Printed Circuit Board Assembly

| Material | Young’s Modulus, E (GPa) | Poisson’s Ratio (() | Thermal Exp. Coefficient (10-6/K) |
| --- | --- | --- | --- |
| FR-4 epoxy-glass PCB substrate | 22 | 0.28 | 18.5 |
| Copper VIP (via-in-pad) | 76 | 0.35 | 17 |
| Sn-37Pb (eutectic) solder | E=32.0-0.088·t (0 ≤ t ≤ 100, t is Celsius temp.) | 0.4 | 21 |
| Underfill | 6 | 0.35 | 30 |
| Silicon chip | 131 | 0.3 | 2.8 |
| Solder mask | 6.9 | 0.35 | 19 |
| *AL | 69 | 0.33 | 22.8 |
| *Si3Ni4 | 314 | 0.33 | 3 |
| Micro-via filler | 7 | 0.3 | 35 |
| Bismaleimide Triazene (BT) | 26 | 0.39 | 15 |

J. Lau, C. Chang, R. Lee, T.-Y. Chen, D. Cheng, T.J. Tseng, D. Lin, “Thermal-Fatigue Life of Solder Bumped Flip Chip on Micro Via-In-Pad (VIP) Low Cost Substrates”

*J.H. Lau and S.-W. Ricky Lee, “Fracture Mechanics Analysis of Low Cost Solder Bumped Flip Chip Assemblies with Imperfect Underfills,” Proceedings: NEPCON West Conference (February 28 – March 2, 1995), Anaheim, CA

Table 1.12. Elastic Properties and Thermal Expansion Coefficient of Electronic-Packaging Materials and Lead Solder Alloys

| Material | Temp. (ºC) | Young’s Modulus, (GPa) | Poisson’s Ratio (() | Thermal Exp. Coefficient (10-6/K) |
| --- | --- | --- | --- | --- |
| Sn-37Pb (eutectic) solder | -70 20 140 | 38.1 30.2 19.7 | 0.4 0.4 0.4 | 24.0 24.0 24.0 |
| Pb-10Sn | -55 22 100 | 13.4 9.78 4.91 | 0.4 0.4 0.4 | 27.8 28.9 30.5 |
| Alumina (substrate) | -55 22 100 | 303 303 303 | 0.21 0.21 0.21 | 3.9 4.5 6.7 |
| Silicon chip | -73 27 127 | 162 162 162 | 0.22 0.22 0.22 | 1.40 2.62 3.23 |
| Polyimide PWB | -55 to 125 | 14.5 | 0.16 | 13.0 |
| Hysol FP4526 Underfill | -73 25 52 77 102 127 | 9.78 9.51 9.23 8.82 7.72 5.37 | 0.3 0.3 0.3 0.3 0.3 0.3 | 33.0 33.0 33.0 33.0 33.0 33.0 |

Tim Wong and A.H. Matsunaga, “Ceramic Ball Grid Array Solder Joint Thermal Fatigue Life Enhancement,” Proceedings: NEPCON West Conference (February 28 – March 2, 1995), Anaheim, CA

### Table 1.13. Lead-free Solder Alloys: Tensile and Shear Strengths

| Lead-free Solder Alloy | Temperature (ºF) | Tensile Strength (psi) | Shear Strength (psi) | Density (g/cm3) |
| --- | --- | --- | --- | --- |
|  | Solidus | Liquidus |  |  |  |
| Sn (pure) | 450 | 450 | 1800 | 2560 | 7.31 |
| Sn-3.5Ag | 430 | 430 | 8900 | 4600 | 7.36 |
| Sn-5Ag | 430 | 473 | 10100 | 8400 | 7.45 |
| Sn-3Cu | 441 | 635 | 6420 | NA | 7.34 |
| Sn-5Sb | 450 | 464 | 5900 | 6200 | 7.26 |

Solder Data Sheet, Welco Castings, 2 Hillyard Street, Hamilton, Ontario, Canada

### Table 1.14. Lead-containing Solder Alloys: Tensile and Shear Strengths

| Solder (Lead) Alloy | Temperature (ºF) | Tensile Strength (psi) | Shear Strength (psi) | Density (g/cm3) |
| --- | --- | --- | --- | --- |
|  | Solidus | Liquidus |  |  |  |
| Pb (pure) | 621 | 621 | 1780 | 1800 | 11.34 |
| Pb-1Sn-1.5Ag |  |  | 3600 |  |  |
| Pb-5Sn | 518 | 596 | 4190 | 3000 | 11.13 |
| Pb-10Sn | 514 | 576 | 4400 | 3780 | 10.94 |
| Pb-15Sn | 437 | 553 | 4700 | 4470 | 10.7 |
| Pb-20Sn | 362 | 533 |  | 4740 | 10.5 |
| Pb-25Sn | 362 | 514 | 5770 | 5310 | 10.3 |
| Pb-30Sn | 362 | 490 | 6140 | 5500 | 9.8 |
| Pb-35Sn | 362 | 475 | 6230 | 5590 | 9.6 |
| Pb-38Sn | 362 | 465 | 6285 | 5640 | 9.81 |
| Pb-40Sn | 362 | 460 | 6320 | 5680 | 9.34 |
| Pb-45Sn | 362 | 440 | 6400 | 5780 | 9.13 |
| Pb-50Sn | 362 | 420 | 6450 | 5870 | 8.91 |
| Pb-60Sn | 362 | 375 | 6400 | 5700 | 8.67 |
| Pb-62Sn | 362 | 363 | 6700 | 6060 | 8.50 |
| Pb-63Sn (eutectic) | 362 | 362 | 6700 | 6060 | 8.42 |
| Pb-95Sn |  |  | 5900 |  |  |
| Sn-36Pb-4Ag | 350 | 378 | 8500 | 7000 | 8.88 |

Solder Data Sheet, Welco Castings, 2 Hillyard Street, Hamilton, Ontario, Canada

Table 1.15. Shear Strengths of Three Lead-Free Solders and Tin-Lead Eutectic (by Ring-and-Plug Test)

| Solder | Load | Stress (area = 0.046 in2) |
| --- | --- | --- |
|  | (lbs) | (N) | (psi) | (MPa) |
| Sn-37Pb (eutectic) | 269 + 11 | 1197 + 49 | 5840 + 240 | 40.27 + 1.65 |
| Sn-3.5Ag | 367 + 24 | 1632 + 107 | 7970 + 530 | 54.95 + 3.65 |
| Sn-3.33Ag-4.83Bi | 540 + 80 | 2402 + 356 | 11,800 + 1700 | 81.36 + 11.7 |
| Sn-3.15Ag-5.0Bi-5.0Au | 560 + 15 | 2491 + 67 | 12,170 + 330 | 83.91 + 2.28 |

Cynthia L. Hernandez, Paul T. Vianco, Jerome A. Rejent, “Effect of Interface Microstructure on the Mechanical Properties of Pb-Free Hybrid Microcircuit Solder Joints,” IPC/SMTA Electronics Assembly Expo (1998), p. S19-2-1

Table 1.16. Mechanical Properties of Tin, Tin-Lead, and Four Lead-Free Solder Alloys (by Ring-and-Plug Tests)

|  | Shear Strength at 1mm/min (MPa) | Stress to Rupture in 1000 hr (MPa) | Fatigue Strength in 1000 cycles (MPa) |
| --- | --- | --- | --- |
| Alloy | Temperature | Temperature | Temperature |
|  | Room | 100 ºC | Room | 100 ºC | Room | 100 ºC |
| Sn (pure) | 22.6 | 19.3 | 8.4 | 2.2 | 13.7 | 9.0 |
| Sn-1Cu | 28.5 | 21.2 | 7.8 | 2.2 | 14.9 | 8.3 |
| Sn-3.5Ag | 39.0 | 23.5 | 14.0 | 5.5 | 18.6 | 10.5 |
| Sn-5Sb | 38.7 | 21.3 | 11.0 | 3.6 | 20.9 | 14.1 |
| Sn-58Bi | 48.0 | 15.6 | 3.3 | 0.9 | 16.0 | 7.9 |
| Sn-40Pb | 34.5 | 21.6 | 3.5 | 1.1 | 16.2 | 10.2 |

International Tin Research Institute, Publ. No. 656; through: William B. Hampshire, “The Search for Lead-Free Solders,” Proc. Surface Mount International Conference (Sept. 1992) San Jose, CA, p. 729

Table 1.17. Shear Strengths, Solidus and Liquidus Temperatures, and Wetting Angles of Experimental Sn-Ag-Cu Solder Alloys

| Alloy | Shear Strength (MPa) (Cross-head speed: 0.1 mm/min; gap thickness: 76.2 μm) | Tsol/Tliq (ºC) | Wetting Angle (deg) |
| --- | --- | --- | --- |
|  | Test temperature |  |  |
|  | 22 ºC | 170 ºC |  |  |
|  | A* | B* | C* | # D | B* |  |  |
| Sn-3.5Ag | 20.9 | 61.2 |  | 27 32 | 20.5 | 221 | 33 |
| Sn-0.7Cu | -- | 29.8 |  | 23 | 10.1 | 227 |  |
| Sn-3.60Ag-1.00Cu (gap thickness: 152.4 μm) | 54.0 | 67.0 +2.4 | 70.8 + 2.3 (59.4 + 4.4) |  | 24.4 | 217/217.9 |  |
| Sn-3.59Ag-0.99Cu-0.15Co | 65.4 | 65.5 |  |  | 22.8 | 217/218.5 |  |
| Sn-3.59Ag-0.99Cu-0.30Co | 53.5 | 56.1 |  |  | 17.5 | 217/219.3 |  |
| Sn-3.58Ag-0.99Cu-0.45Co | 56.7 | 65.7 +3.8 | 56.2 + 6.2 |  | 21.2 | 217/218.9 |  |
| Sn-4.70Ag-1.70Cu | 47.0 | 58.0 |  |  | 21.6 | 217 | 21 |
| Sn-4.68Ag-1.69Cu-0.30Co | 54.5 | 57.8 |  |  | 22.9 | 217/218.1 | 18 |
| Sn-4.68Ag-1.69Cu-0.30Ni | 50.2 | 65.5 |  |  | 23.2 | 217/218.1 | 24 |
| Sn-3.8Ag-0.7Cu | -- | 63.8 |  | 27 | 25.1 | 217 |  |
| Sn-3.8Ag-0.7Cu-0.5Sb | -- | 64.1 |  |  | 28.9 |  | 44 |
| Sn-40Pb | 37.4 | 36.5 |  | 26 | 4.5 | 183/188 | 17 |

*A:  Cooling rate in soldering (test) butt joints=1.5 º/s

*B:  Cooling rate=10 º/s

*C: “Refined” test, (solderability and microstructure)

Measurements A, B and C by Asymmetric Four-Point Bend [AFPB] method

# D: Values from technical literature (four different sources); by ring-and-plug method

# Iver E. Anderson, Tamara E. Bloomer, Robert L. Terpstra, James C. Foley, Bruce A. Cook  and Joel Harringa, “Development of Eutectic and Near-Eutectic Tin-Silver-Copper Solder Alloys for Lead-Free Electronic Assemblies,” IPCWorks ’99: An International Summit on Lead-Free Electronics Assemblies,” (October 25-28, 1999), Minneapolis, MN

Iver E. Anderson, Tamara E. Bloomer, Robert L. Terpstra, James C. Foley, Bruce A. Cook  and Joel Harringa, “Development of Eutectic and Near-Eutectic Tin-Silver-Copper Solder Alloys for Lead-Free Joining Applications,” p. 575

Table 1.18. Physical and Mechanical Properties of  Lead-free Alloys and Sn-Pb37 (eutectic)

| Property | Sn-3.5Ag | Sn-3.5Ag-0.7Cu | Sn-3.8Ag-0.7Cu@ | Sn-0.7Cu (“Alloy 99C”*) | Sn-37Pb (eutectic) |
| --- | --- | --- | --- | --- | --- |
| Density, g/cm3 | 7.5 |  | 7.5 | 7.3 | 8.4 |
| Melting Point (ºC) | 221 |  | 217 | 227-240* | 183 |
| Electrical Conductivity, %IACS# | 14 | 13* | 13 | 13* | 11.9 |
| Electrical Resistivity, μΩ·cm | 12.3 |  | 13 |  | 14.5 |
| Brinell Hardness, HB | 15 |  | 15 |  | 17 |
| Tensile Strength (20 ºC), N/mm2 at Strain Rate: 0.004 s–1 | 58 | 48* | 48 |  | 40 |
| Stress to Rupture | +/- 5 N/mm2 |  |  |  | 4300* |  |
|  | +/- 10 N/mm2 |  |  |  | 1460* |  |
| Joint Shear Strength, N/mm2 at 0.1 mm/min | 20 ºC | 27 |  | 27 | 23 20* | 23 |
|  | 100 ºC | 17 |  | 17 | 16 21* | 14 |
| Creep Strength, N/mm2 at 0.1 mm/min | 20 ºC | 13.7 | 13* | 13.0 | 8.6 | 3.3 |
|  | 100 ºC | 5.0 | 5* | 5.0 | 2.1 | 1.0 |

@Proprietary (patented) alloy (“Ecosol TSC”) of Multicore Solders

*Peter Biocca, “Global Update on Lead-free Solders,” Proc. Surface Mount International (San Jose, CA, 1998), pp. 705-709

#100 %IACS = 58.00 MS/m

Table 1.19. Pure Copper, Tin and Nickel, and Their Intermetallics:  Room-Temperature Physical and Thermal Properties

| Property | Cu | Sn | Ni | Cu6Sn5 | Cu3Sn | Ni3Sn4 |
| --- | --- | --- | --- | --- | --- | --- |
| Density (g/cm3) | 8.9 | 7.3 | 8.9 | 8.28 | 8.9 | 8.65 |
| Young’s Modulus (GPa) | 117 | 41 | 213 | 85.56 | 108.3 | 133.3 |
| Shear Modulus (GPa) |  |  |  | 50.21 | 42.41 | 45.0 |
| Toughness (MPa·m-1/2) |  |  |  | 1.4 | 1.7 | 1.2 |
| Vickers Hardness (kg/mm2) | 30 | 100 | 15 | 378 | 343 | 365 |
| Electrical Resistivity (μΩ·cm) | 1.7 | 11.5 | 7.8 | 17.5 | 8.93 | 28.5 |
| Thermal Conductivity (W/(m·K)) | 3.98 | 0.67 | 0.905 | 34.1 | 70.4 | 19.6 |
| Thermal Diffusivity (cm2/s) |  |  |  | 0.145 | 0.24 | 0.083 |
| Specific Heat (J/(kg·K)) | 0.385 | 0.227 | 0.439 | 286 | 326 | 272 |
| Thermal Expansion (10–6/K) | 17.1 | 23 | 12.9 | 16.3 | 19.0 | 13.7 |

D.R. Frear, S.N. Burchett, H.S. Morgan, and J.H. Lau, eds., The Mechanics of Solder Alloy Interconnects, p. 60 (Van Nostrand Reinhold, New York, 1994)

Table 1.20. Effects of Transition Metals on Vickers Hardness and UTS of Sn-4.7Ag-1.7Cu Solder Alloys

| Alloy | Designation | As Drawn | Annealed |
| --- | --- | --- | --- |
|  |  | VHN | Std. Dev. | UTS (MPa) | Ratio, VHN:UTS | VHN | Std. Dev. | Est. UTS (MPa) |
| Sn-3.5Ag | eutectic | 13.25 | 0.35 | 52 | 0.255 | 13.90 | 0.46 | 54.6 |
| Sn-4.7Ag-1.7Cu | eutectic | 10.25 | 0.35 | 44 | 0.233 | 12.45 | 0.14 | 53 |
| Sn-4.69Ag-1.69Cu-0.3Fe | eutectic+Fe | 6.25 | 0.07 |  |  | 15.05 | 0.35 |  |
| Sn-4.68Ag-1.69Cu-0.5Co | Eutectic+Co | 17.95 | 0.21 | 76 | 0.236 | 15.20 | 0.14 | 64 |
| Sn-4.69Ag-1.69Cu-0.3Ni | eutectic+Ni | 16.55 | 0.35 | 70 | 0.236 | 13.75 | 0.35 | 58 |
| Sn-3.59Ag-1.00Cu-0.3Ni | lean eutectic+Ni | 15.70 | 0.42 | 61.5 | 0.255 | 13.55 | 0.49 | 53 |

VHN: Vickers Hardness Number

UTS: Ultimate Tensile Strength

Iver E. Anderson, Özer Ünal, Tamara E. Bloomer and James C. Foley, “Effects of Transition Metal Alloying on Microstructural Stability and Mechanical Properties of Tin-Silver-Copper Solder Alloys,” Proc. Third Pacific Rim International Conference on Advanced Materials and Processing (PRICM 3) (The Minerals, Metals and Materials Society, 1998)

Figure 1.1. Creep properties at 75oC for Sn-Ag-Cu, Sn-Ag-Bi, Sn-Ag, Sn-Bi, and Sn-Pb solder alloys.

Alan Woosley, Geoff Swan, T.S.Chong, Linda Matsushita, Thomas Koschmieder and Kennon Simmons, "Development of

Lead (Pb) and Halogen Free Peripheral Leaded and PBGA Components to Meet MSL3 260C Peak Reflow", Work

presented by the research team from Motorola at EGG, 2001

2. Thermal Properties: Solidus, Liquidus, and Melting-point Temperatures

2.1. Solidus, Liquidus and Melting Temperatures

Table 2.1.1. Liquidus and Reflow Temperatures of Candidate Lead-Free Solder Alloys for Replacing Eutectic Tin-Lead Solder

| Alloy Composition | Liquidus Temp. (ºC) | Reflow Temp. (ºC) | Melting Range# (ºC) |
| --- | --- | --- | --- |
| Sn-2Ag |  |  | 221-226 |
| Sn-3.5Ag | 221 | 240 – 250 | 221 |
| Sn-0.7Cu | 227 | 245 – 255 | 227 |
| Sn-3.0Ag-0.5Cu* | 220 | 238 – 248 |  |
| Sn-3.2Ag-0.5Cu | 218 | 238 – 248 | 217-218 |
| Sn-3.5Ag-0.75Cu* | 218 | 238 – 248 |  |
| Sn-3.8Ag-0.7Cu | 210 | 238 – 248 | 217-210 |
| Sn-4.0Ag-0.5Cu |  |  | 217-219 |
| Sn-4.0Ag-1.0Cu* | 220 | 238 – 248 | 217-220 |
| Sn-4.7Ag-1.7Cu* | 244 | 237 – 247 | 217-220 |
| Sn-5Sb |  |  | 232-240 |
| Sn-0.2Ag-2Cu-0.8Sb* | 285 | 246 - 256 | 226-228% |
| Sn-2.5Ag-0.8Cu-0.5Sb* | 225 | 233 – 243 |  |
| Sn-2Ag-7.5Bi* | 216 | 220 – 230 |  |
| Sn-3Ag-3Bi* | 218 | 233 – 243 |  |
| Sn-3Ag-5Bi* | 216 | 230 – 240 |  |
| Sn-3.4Ag-4.8Bi* | 215 | 225 – 235 | 200-216 |
| Sn-3.5Ag-3Bi* | 217 | 230 – 240 |  |
| Sn-58Bi |  |  | 138 |
| Sn-3.2Ag-1.1Cu-3Bi* | 240 | 230 – 240 |  |
| Sn-3.5Ag-3In-0.5Bi* | 215 | 230 – 240 |  |
| Sn-3Bi-8Zn |  |  | 189-199 |

V. Solberg, “No-Lead Solder for CSP: The Impact of Higher Temperature SMT Assembly Processing,” Proc. NEPCON West 2000 Conf. (Feb. 28 - Mar. 2, 2000) Anaheim, CA  (Source: Indium Corp.)

#N.-C. Lee, “Lead-Free Chip-Scale Soldering of Packages,” Chip Scale Review, March-April 2000

*Patented compositions; may require licensing or royalty agreements before use.

%Kester, SAF-ALLOY

### Table 2.1.2. Melting Temperatures of Lead-Free Solders

| Alloy | Melting Temperature Range (ºC) | Comments# |
| --- | --- | --- |
| Sn-25Ag-10Sb | 233 (m.p.) | High strength; patented by Motorola (“Alloy J”) |
| Sn-0.7Cu | 227@ |  |
| Sn-3.5Ag | 221@ | Excellent strength and wetting |
| Sn-2Ag | 221 – 226 |  |
| Sn-2.8Ag-20In | 175 – 186 |  |
| Sn-5Sb* | 232 – 240 | Good high-temperature shear strength |
| Sn-58Bi | 138@ | Well established history; Inexpensive |
| Sn-9Zn | 199* | Corrosion; high dross |
| Sn-0.5Ag-4Cu | 217 – 350 | Very wide and high melting range; Engelhard’s lead-free plumbing solder |
| Sn-2Ag-0.75Cu | 217 – 219 |  |
| Sn-3.2Ag-0.5Cu | 217 – 218 |  |
| Sn-3.8Ag-0.7Cu | 217 – 220 |  |
| Sn-4Ag-0.5Cu | 217 – 225 |  |
| Sn-4Ag-1Cu | 217 – 220 |  |
| Sn-4.7Ag-1.7Cu | 217 – 244 |  |
| Sn-8Zn-3Bi | 192 – 197 |  |
| Sn-0.2Ag-2Cu-0.8Sb | 287 – 218 | High melting range; Kester Solder Co.’s Aquabond |
| Sn-2.5Ag-0.8Cu-0.5Sb (Castin) | 217 – 225 |  |
| Sn-2Ag-7.5Bi | 190 – 216 |  |
| Sn-3.4Ag-4.8Bi | 201 – 205 | (205 – 210)% |
| Sn-3.5Ag-3Bi | 208 – 217 | (m.p.: 220 ºC)% |
| Sn-2Ag-3Bi-0.75Cu% | 205 – 217 |  |
| Sn-3.5Ag-5Bi-0.7Cu% | 198 – 213 |  |
| Sn-2Ag-4Bi-0.5Cu-0.1Ge% | 202 – 217 |  |
| Sn-57Bi-0.1Ag% | 138 – 140 |  |
| Sn-52In | 118* | Lowest melt. pt.: expensive |

*Eutectic

N.-C. Lee and W. Casey, “Soldering Technology for Area Array Packages,” Proceedings: NEPCON WEST 2000 (February 27 – March 2, 2000), Anaheim, CA

#N.-C. Lee, J.A. Slattery, J.R. Sovinsky, I. Artaki, P.T. Vianco, “A Drop-In Lead-Free Solder Replacement,” Proceedings: NEPCON West Conference (February 28 – March 2, 1995), Anaheim, CA

*Ning-Cheng Lee, “Lead-Free Soldering of Chip-Scale Packages,” Chip Scale Review, p. 42 (March-April 2000)

%Rao Mahidhara, “A Primer on Lead-Free Solder,” Chip Scale Review (March-April 2000)

2.2. Thermal Properties: Miscellaneous

### Table 2.2.1. Thickness (μm) of Intermetallics in Solder Alloys Aged at 150 ºC

| Alloy: | Sn-3.5Ag | Sn-4Ag-.5Cu |
| --- | --- | --- |
| Inter-metallics: | Cu3Sn | Cu6Sn5 | Cu3Sn | Cu6Sn5 |
| Time (h) |  |  |  |  |
| 0 | 0.25 | 2 | 0.25 | 2 |
| 48 | 0.5 | 3.25 | 0.5 | 2.5 |
| 96 | 0.75 | 2.5 | 0.75 | 2.5 |
| 264 | 1.0 | 2.5 | 1.0 | 3 |
| 480 | 1.5 | 3 | 1.5 | 4.5 |
| 984 | 2.5 | 4 | 2.5 | (nonuniform morphology) |

Angela Grusd, “Lead Free Solders in Electronics,” SMI97, p. 648

Table 2.2.2. Thermal and Electrical Properties of Castin™ (Sn-2.5Ag-0.8Cu-0.5Sb)

| Melting Point | 215 – 217 (C |
| --- | --- |
| Thermal Diffusivity | 35.82 +/- 0.18 mm2/s |
| Specific Heat | 218.99 J/(kg.K) |
| Thermal Conductivity | 57.26 W/(m.K) |
| Electrical Resistivity | 1.21(10-7 ohm.m |
| Electrical Conductivity | 8.25 MS/m |

Karl Seelig and David Suraski, “The Status of Lead-Free Solder Alloys,” Proc. 50th IEEE 2000 Electronic Components and Technology Conference (May 21-24, 2000), Las Vegas, NV

Table 2.2.3. Physical and Mechanical Properties of Sn-2.8Ag-20.0In and Sn-37Pb Eutectic

| Property (measured at 20 (C, except where otherwise noted) | Alloys |
| --- | --- |
|  | Sn-2.8Ag-20.0In | Sn-37Pb (eutectic) |
| Density (g/cm3) | 7.25 | 8.36 |
| Electrical Resistivity (10-6ohm.m) | 0.170 | 0.146 |
| Thermal Conductivity (W/(m.K)) (30 (C) | 53.5 | 50.9 |
| Thermal Expansion (10-6.K-1) | 28 | 25 |
| Tensile Strength (psi) | 6800 | 3900 |
| Tensile Elongation (%) | 47 | 35 |
| Shear Strength (psi) | 4800 | 3450 |
| Poisson’s Ratio | 0.40 | 0.40 |
| Young’s Modulus (kpsi) | 5600 | 4500 |

N.-C. Lee, J.A. Slattery, J.R. Sovinsky, I. Artaki, P.T. Vianco, “A Drop-In Lead-Free Solder Replacement,” Proceedings: NEPCON West Conference (February 28 – March 2, 1995), Anaheim, CA

### Table 2.2.4. Some Physical Properties of Materials Used as Electronic Packaging Conductors

| Metal | Melting Point ((C) | Electrical Resistivity (μohm.cm) | Thermal Expansion Coeff. (10-6/(C) | Thermal Conductivity (W/(m.K)) | #Surface Tension, σ |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | (dyn/ cm) | ((C) |
| Aluminum | 660.1 | 4.3 | 23.0 | 240 | 520 | 750 |
| Antimony | 630.5 |  | 11.0* | 24.0* | 383 | 635 |
| Bismuth | 271.0 |  | 13.4* | 8.0* | 376 | 300 |
| Chromium | 1900 | 20 | 8.2 | 66 |  |  |
| Copper | 1083 | 1.7 | 16.6 | 393; 401* |  |  |
| Gold | 1063 | 2.2 | 14.2 | 297 |  |  |
| Indium | 156.4 |  | 32.1* | 82.0* | 340 | 170 |
| Lead | 327.3 |  |  |  | 431 | 500 |
| Molybdenum | 2625 | 5.2 | 5.0 | 146 |  |  |
| Nickel | 1455 | 6.8 | 12.8 | 92; 91* |  |  |
| Palladium | 1552 | 10.8 | 11.8 | 70 |  |  |
| Platinum | 1774 | 10.6 | 9.0 | 71 |  |  |
| Silver | 960.8 | 1.6 | 18.9 | 418; 429* | 923 | 995 |
| Tin | 231.9 |  | 22.0* | 73.0* | 550% 526 510 | 232% 300 500 |
| Tungsten | 3415 | 5.5 | 4.5 | 200 |  |  |
| Zinc | 419.5 |  |  |  | 785 761 | 510 640 |
| Invar | 1500 | 46 | 1.5 | 11 |  |  |
| Kovar | 1450 | 50 | 5.3 | 17 |  |  |
| Silver-palladium | 1145 | 20 | 14.0 | 150 |  |  |
| Gold-platinum | 1350 | 30 | 10.0 | 130 |  |  |
| Au-20Sn | 280 | 16 | 15.9 | 57 |  |  |
| Sn-37Pb | 183 |  |  |  | 470% | 280% |
| Pb-5Sn | 310 | 19 | 29.0 | 63 |  |  |
| Cu-W(20%Cu) | 1083 | 2.5 | 7.0 | 248 |  |  |
| Cu-Mo(20%Cu) | 1083 | 2.4 | 7.2 | 197 |  |  |

Microelectronics Packaging Handbook, R.R. Tummala and E.J. Rymaszewski, eds. (Van Nostrand Reinhold, 1989, NY)

# N.A. Lange, Handbook of Chemistry, p. 100  (Handbook Publishers, Sandusky, Ohio, 1956)

%M. Abtew, “Wetting Characteristics of Lead Free Solders for High Volume Surface Mount Application,” Proc. NEPCON West 2000 Conf. (Feb. 28 - Mar. 2, 2000) Anaheim, CA

*J.S. Hwang, “Overview of Lead-Free Solders for Electronics & Microelectronics,” Proc. SMI Conf. , p. 405

### Table 2.2.5. Thermophysical Properties of Metallic Elements Used In Electronic Packaging

| Metal | At. Wt. | Density (20(C) | Melt. Point | Lat. Ht. Fusion | Heat capacity (25(C) | Thermal Exp. coef. (20(C) | Electrical Resistivity (20(C) | #Thermal conducti-vity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | (g/cm3) | ((C) | (kg-cal/ g.atom) | (g-cal/ g-at.K) | J/ (kg.K) | (10-6 K-1) | (10-6 (.cm) | (W/(m.K)) |
| Aluminum | 26.98 | 2.702 | *660.46 | 2.6 | 5.817 | 902.1 | 23.03 | 2.62; 2.828# | 238. |
| Antimony | 121.76 | 6.684 (25( C) | *630.75 | 4.8 | 6.08 | 209.0 | 11.4 | 39; 39.1# | 24.5; 23.8§ |
| Bismuth | 208.98 | 9.8 | *271.44 | 2.63 | 6.1 | 122.1 | 13.4§ | 115; 119.0# | 11.2; 9§ |
| Chromium | 51.996 | 7.1 | 1860§ | 3.5 | 5.58 | 449.0 | 8.2 | 2.6 (0(C) | 91.3§ |
| Copper | 63.54 | 8.92 | *1084.9 | 3.11 | 5.85 | 385.2 | 16.6 | 1.69 | 416; 397§ |
| Gold | 196.97 | 19.3 | *1064.4 | 3.03 | 6.0 | 127.5 | 14.2 | 2.4; 2.44# | 311;315.5§ |
| Indium | 114.82 | 7.3 | *156.63 | 0.78 | 6.55 | 238.7 | 33; 24.8§ | 9; 8.37# | 80.0§ |
| Lead | 207.2 | 11.34 | *327.50 | 1.22 | 6.41 | 129.4 | 29.1 | 21.9; 19.8# | 35.0 |
| Molybdenum | 95.94 | 10.2 | *2623 | 6.66 | 5.61 | 244.8 | 4. | 4.77; 5.14# | 138. |
| Nickel | 58.69 | 8.90; 8.8# | *1455 | 4.2 | 6.21 | 442.6 | 12.8 | 6.9; 7.24# | 76.; 88.5§ |
| Palladium | 106.42 | 12. | *1554 | 4.12 | 6.3 | 247.7 | 11.8 | 10.8; 10.21# | 75.2 |
| Platinum | 195.08 | 21.45 | *1769 | 5.2 | 6.35 | 136.2 | 8.9 | 10.5; 9.83# | 69.9; 73.4§ |
| Silver | 107.87 | 10.5 | *961.93 | 2.70 | 6.092 | 236.3 | 18.9 | 1.62; 1.47# | 417.; 425§ |
| Tin | 118.71 | 7.31 | *231.97 | 1.69 | 6.30 | 222.1 | 20.; 23.5§ | 11.4; 11.5# | 66.6; 73.2§ |
| Tungsten | 184.83 | 19.3 | *3387 | 8.42 | 5.97 | 135.9 | 4. | 5.48; 5.51# | 169.; 174§ |
| Zinc | 65.39 | 7.14;7.04# | *419.58 | 1.595 | 5.99 | 383.3 | 33. | 6; 5.75# | 125.;119.5§ |

N.A. Lange, Handbook of Chemistry pp. 100-107  (pp. 854-861)  (Handbook Publishers, Sandusky, Ohio, 1956)

*Thermometric fixed point; E.A. Brandes, Smithells Metals Reference Book, 6th ed., p. 16-2 (Butterworths, London, 1983)

#D.E. Gray, ed., American Institute of Physics Handbook, pp. 2-17 (density), 4-40 (ht. cap.), 5-204 (resistivity), 4-78 (th. cond.) (McGraw-Hill, New York, 1957)

§E.A. Brandes, Smithells Metals Reference Book, 6th ed., p. 14-1 (th. cond.: 0-100(C) (Butterworths, London, 1983)

Table 2.2.6. Some Properties of Materials Commonly Used In Electronics - A

| Metal | CTE (10-6/(C) | Thermal Cond. (W/(m.K)) | Elastic Mod. (GPa) | Density (g/cm3) | Poisson’s Ratio (ν) |
| --- | --- | --- | --- | --- | --- |
| Aluminum | 22.3 | 237 | 69 | 2.7 |  |
| Copper | 16.5 16.9# 17.3* | 398 | 124 125# 117* | 8.9 | 0.31 |
| Molybdenum | 5.0 | 140 | 324 | 10.2 |  |
| Cu/ Invar/Cu | 5.2 | 167% | -- | 8.4 |  |
| Kovar | 5.9 | 17 | 138 | 8.3 |  |
| Silicon Carbide | 2.6 | -- | 412 | 3.17 |  |
| Solder (95/5) | 28 | 36 | 23.5 | 11. |  |
| Diamond | 1.7 | 2300 | 785 | 3.51 |  |
| Silicon | 2.8 3.2# | 150 | 190 110# | 2.3 | 0.27 |
| Alumina | 6.7 7.0# | 21 | 306 375# | 3.9 | 0.23 |
| Aluminum Nitride | 4.5 4.03# | 250 | 327 320# | 3.2 | 0.25 |
| Beryllia | 8.0 | 275 | 345 | 2.9 |  |
| Epoxy / Glass (FR4; T<Tg) (FR4; T>Tg) | 12 / 70 x,y: 15.8* z: 80-90* x,y: 20* z: 400* | 1.7 | 17.2 x,y: 7.0* z: 7.5* x,y:17.0* z: 0.6* | 1.9 |  |
| Polyimides | 45 | 8 | 4.2 | 1.6 |  |

(CTE: Coefficient of thermal expansion)

%In plane

Walter L. Winterbottom, “Converting to Lead-Free Solders: An Automotive Industry Perspective,” JOM, 20-24 (July 1993)

*M.A. Korhonen, D.D. Brown and C.-Y. Li, “Mechanical Properties of Plated Copper,” Mat. Res. Soc. Symp. Proc. Vol. 323, p. 104 (MRS, 1994) (“plated [thin foil] copper”)

#S.M. Spearing, M.A. Tenhover, D.B. Lukco, L. Viswanathan and D.K. Hollen, “Models for the Thermomechanical Behavior of Metal/Ceramic Laminates,” Mat. Res. Soc. Symp. Proc. Vol. 323, p. 128 (MRS, 1994)

Table 2.2.7. Some Properties of Materials Commonly Used In Electronics – B

| Material | Melt. Pt. ((C) | Density (g/cm3) | CTE (10-6/(C) | Young’s Modulus E (GPa) | Tensile Strength (MPa) |
| --- | --- | --- | --- | --- | --- |
| Alumina (Al2O3) | 2050 | 3.985 | 5.8 | 380 | 620 |
| Beryllia (BeO) | 2530 | 3.01 | 8.4 – 9.0 | 311 | 172 - 275 |
| Silica (SiO2) (vitreous) | 1710 | 2.19 | 0.54 | 69 | 110 |
| Zirconia (ZrO2) / (Yttria: Y2O3) | 2960 | 5.56 | 10. | 138 | >300 |
| AlN | 2400 | 3.25 | 5.3 | 350 | 270 |
| Si3N4 | >1750 | 3.19 | 3.3 | 304 | >400 |
| Al | 660 | 2.70 | 23.5 | 69 | 50 -195 |
| Cu | 1083 | 8.96 | 17.0 | 180 |  |
| Ni | 1453 | 8.9 | 13.3 | 199 | 660 |
| Mo | 2617 | 10.22 | 5.1 | 324.8 | 458-690 |
| W | 3410 | 19.3 | 4.5 | 411. | 550-620 |

S.D. Brandi, S. Liu, J.E. Indacochea and  R. Xu, “Brazeability and Solderability of Engineering Materials,” ASM Handbook, Vol. 6: Welding, Brazing and Soldering (ASM International, 1993)

Table 2.2.8. Electrical Resistivity and Temperature Coefficient (TCR) of Pure Metallic Elements Used in Electronic Packaging

| Metal | Temp. (K) | Resistivity (ohm.cm) | TCR (10–3 K-1) |
| --- | --- | --- | --- |
| Aluminum | 293 | 2.61 | 4.2 |
| Antimony | 293 | 37.6 | 5.1 |
| Bismuth | 293 | 115 | 4.6 |
| Chromium | 300 | 12.9 | 5.9 |
| Copper | 293 | 1.58 | 4.3 |
| Gold | 293 | 2.01 | 4.0 |
| Indium | 293 | 8.0 | 5.2 |
| Lead | 293 | 19.3 | 4.2 |
| Molybdenum | 300 | 5.3 | 4.35 |
| Nickel | 293 | 6.2 | 6.8 |
| Palladium | 300 | 10.5 | 4.2 |
| Platinum | 300 | 10.4 | 3.0 |
| Silver | 300 | 1.47 | 4.1 |
| Tin | 293 | 10.1 | 4.6 |
| Tungsten | 300 | 5.3 | 4.8 |
| Zinc | 293 | 5.45 | 4.2 |

E.A. Brandes, Smithells Metals Reference Book, 6th ed., p. 16-2 (Butterworths, London, 1983)

Table 2.2.9. Wetting Properties of Sn-2.8Ag-20.0In and Sn-37Pb Eutectic Solders

| Fluxes | Sn-2.8Ag-20.0In* |
| --- | --- |
|  | Wetting Time (seconds) | Wetting Force (mN/mm) |
|  | 200 ºC | 240 ºC | 200 ºC | 240 ºC |
| A | 10.60 | 4.60 | 0.70 | 0.71 |
| B | 1.53 | 0.42 | 0.72 | 0.56 |
| C | 5.08 | 2.40 | 0.72 | 0.64 |
| D | 5.73 | 2.09 | 0.67 | 0.67 |
| Geometric Mean | 4.66 | 1.76 | 0.70 | 0.64 |
| A | Sn-37Pb |
|  | 2.87 | 1.48 | 0.73 | 0.72 |
| B | 1.03 | 0.50 | 0.71 | 0.61 |
| C | 1.65 | 1.00 | 0.75 | 0.72 |
| D | 2.50 | 1.44 | 0.73 | 0.73 |
| Geometric Mean | 1.87 | 1.02 | 0.73 | 0.69 |

N.-C. Lee, J.A. Slattery, J.R. Sovinsky, I. Artaki, P.T. Vianco, “A Drop-In

Lead-Free Solder Replacement,” Proceedings: NEPCON West Conference

(February 28 – March 2, 1995), Anaheim, CA

*J.A. Slattery and C.E.T. White, U.S. Patent 5,256,370 (Oct. 26, 1993)

Table 2.2.10. Wetting Times and Forces (at 300 ºC): Lead-Free Solder Alloys, and Eutectic Tin-Lead

| Alloy | T0 Mean + σ | T2/3 Mean + σ | Force (2 s) Mean + σ | Forcemax Mean + σ |
| --- | --- | --- | --- | --- |
|  | (s) | (s) | (μN/mm) | (μN/mm) |
| Sn-3.5Ag | 0.0 + 0.0 | 1.23 + 0.01 | 549 + 42 | 579 + 47 |
| Sn-5Sb | 0.11 + 0.08 | 0.74 + 0.07 | 403 + 14 | 413 + 15 |
| Sn-2.8Ag-20In | 0.0 + 0.0 | 1.28 + 0.04 | 250 + 24 | 290 + 31 |
| Sn-37Pb | 0.0 + 0.0 | 1.00 + 0.06 | 470 + 24 | 485 + 19 |

M.A. Kwoka and D.M. Foster, “Lead Finish Comparison of Lead-Free Solders versus Eutectic Solder,” Proc. Surface Mount International Conference (1994), p. 433

### Table 2.2.11. Wetting Times (seconds; at 250 ºC) of Lead-free Solder Alloys

| Alloy | Pure Rosin | Actiec 5 Flux |
| --- | --- | --- |
|  | Tb | T2/3 | Tb | T2/3 |
| Sn-40Pb | 0.6 | 1.0 | 0.4 | 0.5 |
| Sn-3.6Ag | 0.9 | 1.4 | 0.6 | 0.8 |
| Sn-3.6Ag-0.7Cu | 0.6 | 1.0 | 0.5 | 0.7 |
| Sn-0.7Cu | 1.0 | 1.4 | 0.7 | 1.0 |

%Rao Mahidhara, “A Primer on Lead-Free Solder,” Chip Scale Review (March-April 2000)

Table 2.2.12. Onset of Melting Temperatures for Five Sn-Ag-Cu Lead-Free Solder Alloys

| Alloy | Spec. No. | Temperature, Onset of Melting (ºC) |
| --- | --- | --- |
|  |  | This Work | Other (Ref.) |
| Sn-3.6Ag-1.5Cu | 1 | 217.0 | 225 (1) |
| Sn-4.7Ag-1.7Cu | 2a | 216.7 |  |
| Sn-4.7Ag-1.7Cu | 2b | 216.8 |  |
| Sn-4.1Ag-0.9Cu | 3 | 216.5 |  |
| Ave. onset temp., specimens 1-3 |  | 216.8 |  |
| Reference Samples: |  |  |  |
| Sn-3.8Ag-2.3Cu | -- |  | 217.4 (3) |
| Sn-3.5Ag-0.0Cu | 4 | 220.8 | 221 (2) |
| Sn (pure) | 5 | 231.2 | 231.97 (2) |

Chad M. Miller, Iver E. Anderson and Jack F. Smith, “A Viable Tin-Lead Solder Substitute: Sn-Ag-Cu,” J. Electronic Matls. 23(7) 595-601 (1994)

- E.Gebhardt and G. Petzow, Z. Metallkde. 50, 597 (1950)

- T.B. Massalski, Binary Phase Diagrams, 2nd ed. (Amer. Soc. Metals, 1990)

(3) Miller, Anderson and Smith, Note added in proof, J. Electronic Matls. 23(7) 601 (1994)

Table 2.2.13. Solidus Temperatures and Wetting Contact Angles of Selected Lead-Free Solder Alloys with Use of RMA (GF-1235) Flux

| Alloy | Solidus (ºC) | Contact Angle (degrees) |
| --- | --- | --- |
| Sn-4.7Ag-1.7Cu | 217 (eutectic) | 32 |
| Sn-3.33Ag-4.83Bi | 212 | n.a. |
| Sn-5Ag-2Bi | 214.5 | 30 |
| Sn-8Ag-3Sb | 224 | 39 |
| Sn-4.5Ag-6Bi-5.4Sb-4In | 214 | 36 |
| Sn-4.4Ag-6Bi-5.3Sb-6In | 217 | 34 |
| Sn-37Pb (control) | 183 (eutectic) | 16 |

Iver E. Anderson, “Tin-Silver-Copper: A Lead-Free Solder for Capacitor Interconnects,” p. 16, Proc. 16th Capacitor and Resistor Technology Symposium (CARTS 96), 11-15 March, 1996;

Table 2.2.14. Solidus and Liquidus Temperatures and Wetting Angles of Some Lead-free Alloys on Copper (Note opposing effects on wetting angle of increasing temperature for alloys with or without zinc)

| Alloy | Solidus (ºC) | Liquidus (ºC) | Wetting Angle (deg) (with Kester Flux No. 197) |
| --- | --- | --- | --- |
|  | Calc. | Exptl. | Calc. | Exptl. | 250 ºC | 295 ºC | 340 ºC |
| Sn-1Ag-1Sb | 222 | 222 | 232 | 232 | 38 |  | 43 |
| Sn-1Ag-1Sb-1Zn |  |  |  |  | 41 | 41 | 42 |
| Sn-4Ag-7Sb | 229 | 230 | 230 | 230 | 35 |  | 39 |
| Sn-4Ag-7Sb-1Zn |  |  |  |  | 48 | 46 | 36 |
| Sn-2Ag-0.8Cu-6Zn | 190 | 217 | 195 | 217 | 77 | 67 | 62 |
| Sn-2Ag-0.8Cu-8Zn | 191 | 215 | 200 | 215 | 86 | 70 | 52 |
| Sn-10Bi-0.8Cu | 178 | 185 | 218 | 217 | 32 |  | 42 |
| Sn-10Bi-0.8Cu-1Zn |  |  |  |  | 33 | 38 | 27 |
| Sn-10Bi-5Sb | 186 | 193 | 228 | 232 | 39 |  | 48 |
| Sn-10Bi-5Sb-1Zn |  |  |  |  | 50 | 42 | 29 |
| Sn-45Bi-3Sb | 147 | 145 | 168 | 178 |  |  | 37 |
| Sn-45Bi-3Sb-1Zn |  |  |  |  | 98 | 46 | 27 |
| Sn-37Pb (eutectic) |  |  |  |  |  |  | 14 |

M.E. Loomans, S. Vaynman, G.Ghosh and M.E. Fine, “Investigation of Multi-component Lead-free Solders,” J. Elect. Matls. 23(8), 741 (1994)

### Table 2.2.15. Melting Properties, Resistivity, Wettability and Hardness of Lead-Free Solders

| Alloy | Tex (ºC) | Tp (ºC) | Tob (ºC) | Electrical Resistivity* (μΩ-cm) | Wetta-bility Ratio | Hard-ness (VHN)Ha |
| --- | --- | --- | --- | --- | --- | --- |
| Sn-3.5Ag | 221.5 | 226.5 | 220.0 | 7.7 | 97, 95 | 17.9 |
| Sn-5Bi | 219.4 | 228.7 | 196.0 | 11.0 | 97, 97 | 25.6 |
| Sn-10Bi | 209.1 | 221.2 | 165.0 | 17.7 | 98, 97 | 33.0 |
| Sn-5In | 219.7 | 223.4 | 211.5 | 8.3 | 99, 97 | 20.8 |
| Sn-5Sb | 236.8 | 244.9 | 231.6 | 17.1 | 96, 96 | 17.2 |
| Sn-3Ag -5Bi | 214.4 | 218.1 | 191.6 | 11.6 | 98, 98 | 29.9 |
| Sn-3Ag-10Bi | 201.5 | 214.3 | 164.4 | 8.8 | --- | --- |
| Sn-3Ag-3In | 210.7 | 214.7 | 193.3 | 7.7 | 99, 99 | 21.3 |
| Sn-3Ag-5Sb | 225.0 | 235.9 | 216.3 | 10.5 | 99, 99 | 25.4 |
| Sn-3Ag-1Zn | 215.9 | 220.9 | 210.0 | 10.4 | 98, 97 | 18.2 |
| Sn-3Ag-3Zn | 217.8 | 222.5 | 206.8 | 4.8 | 97, 97 | 21.9 |
| Sn-5Bi-5In | 205.5 | 218.4 | 177.0 | 19.1 | 98, 95 | 28.0 |
| Sn-5Sb-3In | 226.7 | 240.3 | 211.7 | 9.8 | 98, 97 | 31.9 |
| Sn-1Cu-5Bi | 216.7 | 226.7 | 184.8 | 10.5 | 96, 95 | 31.9 |
| Sn-1Cu-5Bi-5In | 204.9 | 211.0 | 167.5 | 14.1 | 96, 95 | 40.6 |
| Sn-1.5Cu-2Bi-3Sb | 224.1 | 234.5 | 207.0 | 8.0 | 98, 96 | 32.9 |
| Sn-3Ag-2Cu -2Sb | 218.6 | 230.1 | 212.8 | 11.2 | 98, 98 | 28.6 |
| Sn-3Ag-3Cu -2Bi | 211.1 | 222.2 | 195.7 | 10.6 | 97, 96 | 34.5 |
| Sn-3Ag-5Bi-5In | 195.7 | 209.0 | 158.9 | 12.1 | --- | --- |
| Sn (pure) |  |  |  | 11.2 | --- | 10.5 |
| Sn-37Pb (eutectic) |  |  |  | 17.0 | 95, 91 | 12.9 |

Tex is the extrapolated onset melting temperature by differential scanning calorimetry (DSC)

Tp is the peak melting temperature by DSC

Tob is the observed onset melting temperature

*Method of Van der Pauw

S.K. Kang et al., “Pb-Free Solder Alloys for Flip Chip Applications,” 49th Electronic Components Technology Conf. (1999), June 1-4, San Diego CA

Table 2.2.16. Wetting Contact Angles of Sn-Ag, Sn-Bi, and Sn-Zn Alloys on Copper: Eutectic, and With 1% Addition of Ternary Elements

| Solder Alloy | SnCl2, Saturated Solution | Kester Rosin Flux No. 197 | 20 % Rosin in Isopropyl Alcohol |
| --- | --- | --- | --- |
|  | 165 ºC | 200 ºC | 165 ºC | 200 ºC | 250 ºC | 165 ºC | 200 ºC | 250 ºC |
| Sn-3.5Ag |  |  |  |  | 38 |  |  | 45 |
| Sn-3.5Ag-1Cu |  |  |  |  | 36 |  |  | 44 |
| Sn-3.5Ag-1In |  |  |  |  | 35 |  |  | 39 |
| Sn-3.5Ag-1Sb |  |  |  |  | 35 |  |  | 35 |
| Sn-3.5Ag-1Bi |  |  |  |  | 28 |  |  | 38 |
| Sn-3.5Ag-5Bi |  |  |  |  | 31 |  |  | 42 |
| Sn-58Bi | 10 | 15 | 27 | 28 |  | 40 | 32 |  |
| Sn-58Bi-1Ag | 14 | 17 | 35 | 44 |  | 43 | 39 |  |
| Sn-58Bi-1Cu | 9 | 12 | 36 | 38 |  | 40 | 30 |  |
| Sn-58Bi-1In | 7 | 12 | 40 | 35 |  | 56 | 43 |  |
| Sn-58Bi-1Sb | 20 | 15 | 31 | 35 |  | 38 | 42 |  |
| Sn-58Bi-1Zn | 18 | 12 | 58 | 54 |  | 50 | -- |  |
| Sn-8.9Zn |  |  |  |  | 59 |  |  | 58 |
| Sn-8.9Zn-1In |  |  |  |  | 63 |  |  | 53 |

M.E. Loomans, S. Vaynman, G.Ghosh and M.E. Fine, “Investigation of Multi-component Lead-free Solders,” J. Elect. Matls. 23(8), 741 (1994)

Table 2.2.17. Wetting Contact Angles on Copper of Sn-Bi Alloys: Eutectic, and With Addition of Ternary Elements

| Solder Alloy | SnCl2, Saturated Solution | Kester Flux No. 197 | 20 % Rosin in Isopropyl Alcohol (IPA) | 20 % Rosin in IPA + 1% SnCl2 |
| --- | --- | --- | --- | --- |
|  | 165 ºC | 200 ºC | 165 ºC | 200 ºC | 165 ºC | 200 ºC | 165 ºC | 200 ºC |
| Sn-58Bi | 10 | 15 | 27 | 28 | 40 | 32 | 43 | 35 |
| Sn-58Bi-1Ag | 14 | 17 | 35 | 44 | 43 | 39 | 93 | 45 |
| Sn-58Bi-1Cu | 9 | 12 | 36 | 38 | 40 | 30 | 46 | 31 |
| Sn-58Bi-1In | 7 | 12 | 40 | 35 | 56 | 43 |  |  |
| Sn-58Bi-1Sb | 20 | 15 | 31 | 35 | 38 | 42 |  |  |
| Sn-58Bi-1Zn | 18 | 12 | 58 | 54 | 50 | -- |  |  |

M.E. Loomans, S. Vaynman, G.Ghosh and M.E. Fine, “Investigation of Multi-component Lead-free Solders,” J. Elect. Matls. 23(8), 741 (1994)

Table 2.2.18. Wetting Properties of Pure Tin, Four Lead-Free Tin Alloys and Three Lead-Tin Alloys

| Solder Alloy | Temp. (ºC) | Wetting Time, Mean (std.dev.) (s) | Max. Wetting Force, mean (std.dev.) (mg) | Wetting Rate | Area of Spread (cm2) |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | mean (std.dev.) (mV/s) | Normal- Ized (Sn = 1) | Fluxite | Power flow Flux |
| Sn (pure) | 282 | 0.68 (0.10) | 607 ( 84) | 138 ( 43) | 1.00 | 0.5 | 0.55 |
| Sn-1Cu | 300 | 0.60 (0.11) | 565 ( 82) | 120 ( 43) | 0.87 | 0.5 | 0.5 |
| Sn-3Cu | 365 | 0.19 (0.08) | 648 ( 61) | 365 (122) | 2.64 | 0.7 | 0.8 |
| Sn-3.5Ag | 260 | 0.60 (0.12) | 533 (109) | 124 ( 30) | 0.90 | 0.5 | 0.6 |
| Sn-5Sb | 280 | 0.83 (0.12) | 393 (117) | 97 ( 24) | 0.70 | 0.5 | 0.55 |
| Sn-40Pb | 234 | 0.45 (0.14) | 602 (114) | 146 ( 43) | 1.06 | 2.2 | -- |
| Sn-50Pb | 265 | 0.37 (0.09) | 523 (115) | 191 (119) | 1.38 | 2.5 | 2.6 |
| Sn-60Pb | 285 | 0.55 (0.09) | 623 ( 68) | 100 ( 17) | 0.72 | 1.7 | 1.9 |

M.E. Warwick, “The Wetting and Mechanical Properties of Lead-Free Capillary Plumbing Solders,” ATB Metallurgie XXV, No. 1, 43-50 (1985)

Table 2.2.19. Lead-Free Solder Alloys: Solidus and Liquidus Temperatures, Coefficient of Thermal Expansion, Surface Tension, and Electrical Resistivity

| Alloy | Tsol* (ºC) | Tliq (ºC) | CTE (20 ºC) (x 10+5/ºC) | Surface Tension (at Tliq + 50 ºC) (mN/mm) | Intermetallic Phases | Electrical Resistivity (μΩ-cm) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Air | Nitrogen |  |  |
| Sn (pure) | 232 |  | 2.6 |  |  |  | 11.5 |
| Sn-37Pb | 183 |  | 2.5 | 417 | 464 |  | 14.5 |
| Sn-3.5Ag | 221 |  |  | 431 | 493 | Ag3Sn | 10 – 15 |
| Sn-4Cu-0.5Ag | 216 | 222 |  |  |  | Ag3Sn, Cu6Sn5 | 10 – 15 |
| Sn-0.7Cu | 227 |  |  | 491 | 461 | Cu6Sn5 | 10 – 15 |
| Sn-58Bi | 138 |  | 1.5 | 319 | 349 |  | 30 – 35 |
| Sn-52In § | 120 |  | 2.0 |  |  |  | 10 – 15 |
| Sn-9Zn | 199 |  |  | 518 | 487 |  | 10 – 15 |

*Where no liquidus temperature is given, the alloy is eutectic and has a single, definite fusion temperature. (For pure tin the melting point is given.)

§ (Eutectic: Sn-50.9In)

Judith Glazer, “Microstructure and Mechanical Properties of Pb-free Solder Alloys for Low-Cost Electronic Assembly: A Review,” J. Electronic Materials 23(8), 693 (1994)

### Table 2.2.20. Fluid Properties of Some Molten Lead-Free Solders

| Solder Alloy | Liquidus temperature | Contact angle | Wetting rate | Surface tension |
| --- | --- | --- | --- | --- |
|  | (ºC) | (deg) | (dyne/ sec) | (dyne/ cm) |
| Sn-58Bi | 138 | 43 | 350 | 300 |
| Sn-2.8Ag-20In | 114 (low-temp. peak); 178 (primary peak) | 44 | 650 | 390 |
| Sn-3.5Ag-4.8Bi | 212 | 31 | 2420 | 420 |
| Sn-2.5Ag-0.8Cu-0.5Sb | 217 | 44 | 4280 | 510 |
| Sn-37Pb (eutectic) | 183 | 17 | 2030 | 380 |

I. Artaki, D.W. Finley, A.M. Jackson, U. Ray and P.T. Vianco, “Wave Soldering with Pb-Free Solders,” Proc. Surface Mount International  (San Jose, CA, August 27-31, 1995), p. 495.

Table 2.2.21. Densities and Costs of Popular Solder Metals and Alloys – A

| Metal | Price per kg (2nd Q. 1999) | Density (g/cm3) | Price per cm3 (2nd Q. 1999) |
| --- | --- | --- | --- |
|  | ($) | Normalized (Pb = 1) |  | ($) | Normalized (Pb = 1) |
| Pb | 0.55 | 1.00 | 11.36 | 0.00625 | 1.00 |
| Sb | 2.00* | 2.5* | 6.684 | 0.0134 | 2.14 |
| Cu | 1.50 | 2.73 | 8.92 | 0.0134 | 2.14 |
| Bi | 6.60* | 8.25* | 9.8 | 0.0647 | 10.35 |
| Sn | 5.70 | 10.36 | 7.31 | 0.0416 | 6.57 |
| Ag | 170. | 309.1 | 10.5 | 1.78 | 285. |
| In | 242.50* | 303.1* | 7.3 | 1.77 | 283. |
| Sn-37Pb | 3.80 | 6.91 | 8.4 | 0.0319 | 5.10 |
| Sn-Pb (solder paste) | 90.00 | 163.6 | 8.4 | 0.756 | 121. |
| Sn-0.7Cu | 5.66 | 10.29 | 7.30 | 0.0413 | 6.61 |
| Sn-4Ag-0.5Cu | 12.25 | 22.27 | 7.39 | 0.0905 | 14.5 |

Adapted from Alan Rae and Ronald C. Lasky, “Economics and Implications of Moving to Lead-Free Assembly,” Proc. NEPCON WEST 2000 (February 27 – March 2, 2000), Anaheim, CA

*(1992 prices; Pb: $0.80/kg) Paul T. Vianco, “General Soldering,” ASM Handbook, Vol. 6, Welding, Brazing, and Soldering (ASM International, 9639 Kinsman Road, Materials Park, Ohio 44073 USA, 1993)

Table 2.2.22. Densities and Costs of Popular Solder Metals and Alloys – B

| Element | Cost/(unit mass) [2/3/99] | Density (25 ºC) | Cost/(unit volume) | Comment |
| --- | --- | --- | --- | --- |
|  | $/lb | $/kg | lb/in3 | g/cm3 | $/in3 | $/cm3 | Availability |
| Lead | 0.45 | 0.99 | 0.41 | 11.35 | 0.18 | 0.011 |  |
| Zinc | 0.50 | 1.10 | 0.258 | 7.14 | 0.13 | 0.008 |  |
| Copper | 0.65 | 1.43 | 0.324 | 8.97 | 0.21 | 0.013 |  |
| Antimony | 0.80 | 1.76 | 0.239 | 6.61 | 0.19 | 0.012 |  |
| Bismuth | 3.40 | 7.48 | 0.354 | 9.80 | 1.20 | 0.073 | limited |
| Tin | 3.50 | 7.70 | 0.264 | 7.31 | 0.92 | 0.056 |  |
| Silver | 84.20 | 185.24 | 0.379 | 10.50 | 31.91 | 1.947 | limited |
| Indium | 125.00 | 275.00 | 0.264 | 7.31 | 33.00 | 2.014 | scarce |
| Alloy | Melt. Range (ºC) |  |  |  |  |  |  | Patented |
| Sn-37Pb | 183 | 2.37 | 5.21 | 0.318 | 8.80 | 0.75 | 0.046 |  |
| Sn-3.5Ag | 221 | 6.32 | 13.90 | 0.268 | 7.42 | 2.33 | 0.142 |  |
| Sn-0.7Cu | 227 | 3.48 | 7.66 | 0.264 | 7.31 | 0.92 | 0.056 |  |
| Sn-58Bi | 139 | 3.44 | 7.57 | 0.316 | 8.75 | 1.09 | 0.067 |  |
| Sn-5Sb | 232-240 | 3.37 | 7.41 | 0.263 | 7.28 | 0.88 | 0.054 |  |
| Sn-9Zn | 199 | 3.23 | 7.11 | 0.263 | 7.28 | 0.85 | 0.052 |  |
| Sn-4Ag-0.5Cu | 217-218 | 6.55 | 14.41 | 0.269 | 7.44 | 1.76 | 0.107 |  |
| Sn-3.4Ag-4.8Bi | 208-215 | 6.24 | 13.73 | 0.272 | 7.53 | 1.70 | 0.104 | Y |
| Sn-3.5Ag-3Bi | 216-220 | 5.92 | 13.02 | 0.269 | 7.44 | 1.59 | 0.097 |  |
| Sn-2.8Ag-20In | 179-189 | 30.06 | 66.13 | 0.267 | 7.39 | 8.02 | 0.489 | Y |
| Sn-3.5Ag-1.5In | 218 | 8.15 | 17.93 | 0.268 | 7.42 | 2.18 | 0.133 |  |
| Sn-2Ag-0.5Cu-7.5Bi | 186-212 | 5.09 | 11.20 | 0.273 | 7.56 | 1.39 | 0.085 |  |
| Sn-2.5Ag-0.8Cu-0.5Sb | 213-219 | 5.48 | 12.06 | 0.267 | 7.39 | 1.46 | 0.089 | Y (Castin™) |

Authors not listed; “Lead-Free Alloy Trends for the Assembly of Mixed Technology PWBs”, Proc. NEPCON-West 2000 (Feb. 27-Mar. 2) Anaheim, CA

Table 2.2.23. Cost of Lead-Free Solder Alloys Relative to That of Sn-37Pb Eutectic

| Alloy | Relative Cost |
| --- | --- |
|  | Bar | Paste |
| Sn-37Pb | 1.000 | 1.000 |
| Sn-3.5Ag | 2.29 | 1.07 |
| Sn-3Ag-2Bi | 2.17 | 1.06 |
| Sn-3.4Ag-4.8Bi | 2.26 | 1.06 |
| Sn-3.2Ag-0.7Cu | 2.21 | 1.06 |
| Sn-3.5Ag-1.3Cu | 2.28 | 1.06 |
| Sn-4.7Ag-1.7Cu | 2.56 | 1.08 |
| Sn-2.6Ag-0.8Cu-0.5Sb | 2.06 | 1.05 |
| Sn-3.5Ag-0.5Cu-1Zn | 2.27 | 1.06 |
| Costs of pure metals (relative to Pb=1): Zn: 1.7; Cu: 3.0; Sb: 3.9; Bi: 8.6; Sn: 11; Ag: 260; Au: 15000 |

Ning-Cheng Lee, “Lead-Free Soldering of Chip-Scale Packages,” Chip Scale Review, p. 42 (March/April 2000)

# A. Solder Alloy for Plated Through Holes

A series of investigations to reduce the solidus temperature and strength of lead-free solders (by adding indium, which is very ductile) was carried out by NCMS. Beginning with three alloys: (1) Sn-3.5Ag (Tmelt=221 ºC), (2) Sn-3Ag-2Bi (Tonset = 216 ºC), and (3) Sn-3.33Ag-4.83Bi (Tonset = 212 ºC).  A solder alloy with composition Sn-3.5Ag-5.0In, with addition of either 1 % or 2 % (by mass) Cu was found to reduce the alloy's melting temperature by 5 ºC and also desirably decreased the alloy's strength, reducing the probability of its cracking due to buildup of residual stress during thermal cycling (cooling after a soldering operation).

Source: Technical Reports for the Lead Free Solder Project: Properties Reports: "Solder Alloy Development for Plated Through-Hole Applications: DSC Analyses and Ring-in-Plug Mechanical Tests;" Lead Free Solder Project CD-ROM, National Center for Manufacturing Sciences (NCMS), 1998

3. Candidate Alloys for Replacing Lead-Alloy Solders

### Table 3.1. Criteria for Down-Selection of Lead-Free Alloys

| Property | Definition | Minimum Acceptance Level |
| --- | --- | --- |
| Liquidus temperature | Temperature at which solder alloy is completely molten |  |
| Pasty Range | Range of temperature between solidus and liquidus, where alloy is part solid and part liquid. | < 30 (ºC) |
| Wettability | Assessed by force required to wet a copper wire with molten solder. A large force indicates good wetting, as does short duration t0 at zero wetting force and time t2/3 to reach two thirds of maximum wetting force. | Fmax > 300 (N t0 < 0.6 s t2/3 < 1 s |
| Area of Coverage | Measures coverage of copper test piece by solder | > 85 % |
| Drossing | Measured by amount of oxide formed in air on surface of molten solder after a fix duration at soldering temperature | Qualitative |
| TMF | Lifetime at a given failure rate compared to that of (eutectic) Sn/37Pb, for a specific configuration of board and solder joint | > 75 % |
| Thermal Mismatch | Difference in coefficients of thermal expansion that causes unacceptable thermal stress | < 29 ppm/ºC |
| Creep | Stress load to failure at room temperature, in 10,000 minutes (~167 hours) | > 500 psi |
| Yield Strength |  | >2000 psi |
| Elongation | Relative elongation of material under uniaxial tension at room temperature | > 10 % |

Source: Technical Reports for the Lead Free Solder Project: Properties Reports: "Down Selection;" on Lead Free Solder Project CD-ROM, National Center for Manufacturing Sciences  (NCMS), 1998

Table 3.2. Chemical compositions of 79 lead-free solder alloys down-selected for preliminary testing by the National Center for Manufacturing Sciences (NCMS). The seven lead-free alloys in bold type are those down-selected for extensive testing and measurement from the initial pool of 79. Selection process is detailed in Technical Reports for the Lead Free Solder Project: Properties Reports: "Down Selection," on Lead Free Solder Project CD-ROM, National Center for Manufacturing Sciences (1998).

| NCMS Alloy Code | Chemical Composition (% by mass) |  | Alloy Code | Chemical Composition (% by mass) |  | Alloy Code | Chemical Composition (% by mass) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A1* | Sn-37Pb |  | D8 | Sn-3Ag-55Bi-2Sb |  | F5 | Sn-20In-2.8Zn |
| A2 | Sn-2Ag-36Pb |  | D9 | Sn-3Ag-54Bi-2In-2Sb |  | F6 | Sn-5Bi-7Zn |
| A3 | Sn-97Pb |  | D10 | Sn-3Ag-54Bi-2Cu-2Sb |  | F7 | Sn-31.5Bi-3Zn |
| A4* | Sn-3.5Ag |  |  |  |  | F8 | Sn-3.5Ag-1.5In |
| A5 | Sn-5Sb |  | E1 | Sn-3Ag-2Sb |  | F9 | Sn-2Ag-7.5Bi-0.5Cu |
| A6* | Sn-58Bi |  | E2 | Sn-3Ag-2Cu-2Sb |  | F10 | Sn-0.2Ag-2Cu-0.8Sb |
| A7 | Sn-3.5Ag-0.5Sb-1Cd |  | E3 | Sn-3Ag-2Bi-2Sb |  |  |  |
| A8 | Sn-75Pb |  | E4 | Sn-3Ag-2Bi |  | F11 | Sn-2.5Ag-19.5Bi |
|  |  |  | E5 | Sn-2.5Ag-2Bi |  | F12 | Sn-3Ag-41Bi |
| B1 | Sn-50Bi |  | E6 | Sn-2Bi-1.5Cu-3Sb |  | F13 | Sn-55Bi-2Cu |
| B2 | Sn-52Bi |  | E7 | Sn-2Bi-8In |  | F14 | Sn-48Bi-2Cu |
| B3 | Sn-55Bi-3Cu |  | E8 | Sn-10Bi-10In |  | F15 | Sn-57Bi |
| B4 | Sn-48Bi-4Cu |  | E9 | Sn-10Bi-20In |  | F16 | Sn-56.7Bi-0.3Cu-1In |
| B5 | Sn-2Ag-46Bi-4Cu |  | E10 | Sn-9Zn |  | F17 | Sn-3.4Ag-4.8Bi |
| B6 | Sn-56Bi-2In |  |  |  |  | F18 | Sn-3Ag-15In |
|  |  |  | EN1 | Sn-5Ag-8.6In |  | F19 | Sn-3Ag-5Bi-10In |
| C1 | Sn-2Ag-1.5Sb-29Pb |  | EN2 | Sn-5.6Ag-14.4In |  | F20 | Sn-5Bi-10In |
| C2 | Sn-3Ag-4Cu |  | EN3 | Sn-6.8Ag-20In |  |  |  |
| C3 | Sn-2.5Ag-2Bi-1.5Sb |  | EN4 | Sn-3.1Ag-6.1Bi |  | F21 | Sn-2.8Ag-20In |
| C4 | Sn-3Ag-1Bi-1Cu-1.5Sb |  | EN5 | Sn-3.5Ag-10Bi |  | F22 | Sn-0.1Ag-1Bi-3.9Sb |
| C5 | Sn-2Ag-9.8Bi-9.8In |  | EN6 | Sn-3.3Ag-15Bi |  | F23 | Sn-0.5Ag-1.5Bi-3Sb |
|  |  |  | EN7 | Sn-6.8Ag-30Bi |  | F24 | Sn-55Bi-2Zn |
| D1 | Sn-45Bi |  | EN8 | Sn-3.3Ag-11.2Bi-5.5In |  | F25 | Sn-0.5Ag-56Bi |
| D2 | Sn-57Bi-2In |  | EN9 | Sn-2.5Ag-11.2Bi-5.5In |  | F26 | Sn-4.5Ag-1.6Cu-5Sb |
| D3 | Sn-2Ag-57Bi |  |  |  |  | F27 | Sn-3.5Ag-0.5Cu-1Zn |
| D4 | Sn-57Bi-2Sb |  | F1 | Sn-2Ag-7.5Bi-0.5Cu |  | F28 | Sn-3Ag-10.9In-0.4Sb |
| D5 | Sn-57Bi-1Sb |  | F2# | Sn-2.6Ag-0.8Cu-0.5Sb |  | F29 | Sn-4.7Ag-1.7Cu |
| D6 | Sn-2Ag-56Bi-1.5Sb |  | F3 | Sn-0.5Ag-4Cu |  | F30 | Sn-3.2Ag-0.7Cu |
| D7 | Sn-3Ag-55.5Bi-1.5Sb |  | F4 | Sn-8.8In-7.6Zn |  | F31 | Sn-3.5Ag-1.3Cu |

*Eutectic composition

#Composition F2 is a proprietary composition, Castin®

4. Miscellaneous

- Major considerations for replacement of lead-free solders:

- Melting (or solidus) temperature similar to that of Sn-37Pb solder

- Other physical properties (such as ductility, tensile strength, thermal conductivity and expansion, electrical conductivity) as good as, or better than, those of Sn-37Pb solder

- Narrow plastic range

- Capability of being fabricated into contemporary physical forms of solder, such as wire, preforms, ribbon, spheres, powder, and paste

- Adequate wetting properties and viscosity

- Acceptably low dross formation when used in wave soldering

- Compatibility with existing systems of liquid flux

- For paste, adequate shelf life and performance

- No toxicity problems

Table 4.1. Designation and Composition of Lead-Free Solders.

A.C. = "Alloy Code"; L = liquidus; S = solidus; P.R. = pasty range; CTE = coefficient of thermal expansion.  Blank cells indicate either zero composition or no available data.

[Due to space limitations, source is documented at end of this series of tables.]

| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| A0 | 100 |  |  |  |  |  |  |  | Reference: pure Sn |  |  |  | 7.31 | 7.30 |  |  |
| A1* | 63 |  |  |  |  |  |  | 37 | Baseline (eutectic) alloy, properties used as reference. | 183 | 183 | 0 | 8.39 | 8.42 | 45. | 18.74 |
| A2 | 62 | 2 |  |  |  |  |  | 36 | Popular surface- mount alloy | 180 | 179 | 1 | 8.44 | 8.44 | 47. | 25.70 |
| A3 | 3 |  |  |  |  |  |  | 97 | Low-usage, low-lead con- tent, very-high-temp, C4 alloy used by IBM; very good in thermal fatigue. | 318 | 318 | 0 | 11.13 | 11.21 | 22. | 29.72 |
| A4* | 96.5 | 3.5 |  |  |  |  |  |  | Baseline (eutectic) alloy, properties used as reference. | 221 | 221 | 0 | 7.37 | 7.38 | 64. | 20.04 |
| A5 | 95 |  |  |  |  | 5 |  |  | Popular high-temp. alloy. | 241 | 234 | 7 | 7.25 | 7.27 | 57. | 20.09 |
| A6* | 42 |  | 58 |  |  |  |  |  | Baseline (eutectic) alloy, properties used as reference. | 138 | 138 | 0 | 8.57 | 8.57 | 46. | 14.26 |
| A7 | 95 | 3.5 |  |  |  | 0.5 | Cd: 1.0 |  | Alpha alloy #38, low usage; contains cadmium. | 223 | 221 | 2 | 7.39 | 7.39 | 64. | 20.54 |
| A8 | 25 |  |  |  |  |  |  | 75 |  | 264 | 183 | 81 | 9.68 | 10.00 | 17. |  |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- Ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| B1 | 50 |  | 50 |  |  |  |  |  | Similar to B2, wider pasty range and lower elongation (21%) | 152 | 138 | 14 | 8.37 | 8.37 | 43. |  |
| B2 | 48 |  | 52 |  |  |  |  |  | Compare solderability results with B1, choose one. High Bi content | 151 | 138 | 13 | 8.42 | 8.42 | 40. | 12.13 |
| B3 | 42 |  | 55 | 3 |  |  |  |  | High Cu, wide pasty range, high liquidus, low elongation | >400 | - |  |  | 8.55 |  |  |
| B4 | 48 |  | 48 | 4 |  |  |  |  | High Cu, wide pasty range, high liquidus, low elongation | >400 | - |  |  | 8.39 |  |  |
| B5 | 48 | 2 | 46 | 4 |  |  |  |  | Poor ductility (2.7% elongation) | 146 | 137 | 9 | 8.44 | 8.4 | 36. | 14.38 |
| B6 | 42 |  | 56 |  | 2 |  |  |  | Quenched alloy shows ternary melting (99°C solidus),116% total elongation. | 140 | 126 | 14 | 8.52 | 8.52 | 45. | 16.01 |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| C1 | 67.5 | 2 |  |  |  | 1.5 |  | 29 | IBM patent alloy, low usage and lead content; not commercially available. | 198 | 183 | 15 | 8.1 | 8.19 | 52. | 20.45 |
| C2 | 93. | 3 |  | 4 |  |  |  |  | 95 ºC pasty range, liquidus > 300 ºC. | 221 | 221 | 0 | 7.42 | 7.42 | 61. | 14.83 |
| C3 | 94. | 2.5 | 2 |  |  | 1.5 |  |  | Similar to E3, same pasty range and YS but lower % elongation. | 226 | 219 | 7 | 7.4 | 7.38 | 59. |  |
| C4 | 93.5 | 3 | 1 | 1 |  | 1.5 |  |  | A complex system, but meets acceptance criteria. | 224 | 220 | 4 | 7.34 | 7.39 | 65. | 19.9 |
| C5 | 78.4 | 2 | 9.8 |  | 9.8 |  |  |  | 32 C pasty range, 7.1% total elongation, high indium content ($12.8 / lb). | 195 | 163 | 32 | 7.48 | 7.54 | 46. | 11.86 |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| D1 | 55. |  | 45. |  |  |  |  |  | Similar to B1, 29 ºC (26 ºC) pasty range, lower pasty range | 164 | 138 | 26 |  | 8.25 |  |  |
| D2 | 41. |  | 57. |  | 2. |  |  |  | Similar to B6, lower % elongation (71.8%) | 140 | 127 | 13 | 8.55 | 8.54 | 44. | 15.85 |
| D3 | 41. | 2. | 57. |  |  |  |  |  | Meets acceptance criteria but questionable value over A6 | 147 | 140 | 7 | 8.61 | 8.60 | 44. | 14.39 |
| D4 | 41. |  | 57. |  |  | 2. |  |  | Similar to D5, lower elongation, wider (sic) pasty range | 150 | 141 | 9 | 8.53 | 8.52 | 45. | 15.8 |
| D5 | 42. |  | 57. |  |  | 1. |  |  | Meets acceptance criteria, high Bi | 149 | 138 | 11 |  | 8.53 |  |  |
| D6 | 40.5 | 2. | 56. |  |  | 1.5 |  |  | Similar to D7, lower % elongation (26.8%) | 145 | 137 | 8 | 8.59 | 8.56 | 44. | 13.15 |
| D7 | 40. | 3. | 55.5 |  |  | 1.5 |  |  | Meets acceptance criteria but questionable value over D5 | 147 | 137 | 10 |  | 8.58 |  |  |
| D8 | 40. | 3. | 55. |  |  | 2. |  |  | Similar to D7, same % elongation, wider pasty range (12 ºC) | 150 | 138 | 12 |  | 8.56 |  |  |
| D9 | 39. | 3. | 54. |  | 2. | 2. |  |  | 99 ºC solidus, wide pasty range (39 ºC) | 138 | 99 | 39 | 8.56 | 8.54 | 40. | 15.25 |
| D10 | 39. | 3. | 54. |  |  | 2. |  |  | 3.7 % elongation | 154 | 138 | 16 | 8.61 | 8.58 | 40. | 15.24 |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| E1 | 95 | 3 |  |  |  | 2 |  |  | Meets acceptance criteria; other alloys more promising | 228 | 225 | 3 | 7.35 | 7.35 | 62. | 13.44 |
| E2 | 93 | 3 |  | 2 |  | 2 |  |  | Meets acceptance criteria; other alloys more promising | 224 | 221 | 3 | 7.36 | 7.38 | 62. | 13.44 |
| E3 | 93 | 3 | 2 |  |  | 2 |  |  | Meets acceptance criteria; good yield strength and elongation | 226 | 219 | 7 | 7.39 | 7.39 | 60. |  |
| E4 | 95 | 3 | 2 |  |  |  |  |  | Meets acceptance criteria; similar to F17, good candidate | 220 | 216 | 4 | 7.39 | 7.41 | 59. | 14.84 |
| E5 | 95.5 | 2.5 | 2 |  |  |  |  |  | Similar to E4; lower % elongation, wider pasty range | 221 | 215 | 6 |  | 7.39 |  |  |
| E6 | 93.5 |  | 2 | 1.5 |  | 3 |  |  | Quaternary alloy; high Cu content | 231 | 225 | 6 | 7.34 | 7.34 | 57. | 16.81 |
| E7 | 90 |  | 2 |  | 8 |  |  |  | Meets acceptance criteria; high In content, lower elongation | 215 | 206 | 9 | 7.33 | 7.34 | 49. | 20.73 |
| E8 | 80 |  | 10 |  | 10 |  |  |  | 30-degree pasty range | 200 | 170 | 30 | 7.47 | 7.49 | 38. | 19.68 |
| E9 | 70 |  | 10 |  | 20 |  |  |  | Potentially expensive (high In content) and 3.6% elongation |  |  |  |  | 7.49 |  | 15.69 |
| E10 | 91 |  |  |  |  |  | 9 |  | High dross; low Fmax | 198 | 198 | 0 | 7.26 | 7.29 | 69. | 31.77 |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| EN1 | 86.4 | 5 |  | - | 8.6 | 2 |  |  | Meets acceptance criteria; midrange melting temperature | 205 | 200 | 5 | 7.44 | 7.41 | 54. | . |
| EN2 | 80 | 5.6 |  |  | 14.4 |  |  |  | High liquidus, high In; similar to EN1 and F18 | 199 | 189 | 10 | 7.45 | 7.43 |  |  |
| EN3 | 73.2 | 6.8 |  |  | 20 |  |  |  | Low solidus, very wide pasty range | 242 | 113 | 129 | 7.49 | 7.46 |  |  |
| EN4 | 90.8 | 3.1 | 6.1 |  | - | - |  |  | From quench, 78 degree pasty range, 137 ºC solidus | 215 | 202 | 13 | 7.49 | 7.49 | 56. |  |
| EN5 | 86.5 | 3.5 | 10 |  | - | - |  |  | Wide pasty range | 208 | 137 | 71 | 7.6 | 7.57 |  |  |
| EN6 | 81.7 | 3.3 | 15 |  |  |  |  |  | Wide pasty range | 200 | 137 | 63 | 7.7 | 7.67 |  |  |
| EN7 | 63.2 | 6.8 | 30 |  |  |  |  |  | Very wide pasty range | 282 | 137 | 145 | 8.12 | 8.10 |  |  |
| EN8 | 80 | 3.3 | 11.2 |  | 5.5 |  |  |  | Wide pasty range | 221 | 170 | 51 | 7.66 | 7.59 |  |  |
| EN9 | 80.8 | 2.5 | 11.2 |  | 5.5 |  |  |  | Wide pasty range | 200 | 169 | 31 | 7.61 | 7.57 | 46. |  |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F1 | 90 | 2 | 7.5 | 0.5 |  |  |  |  | ITRI alloy, meets acceptance criteria; lower elongation | 213 | 193 | 20 |  | 7.50 |  |  |
| F2 | 96.1 | 2.6 |  | 0.8 |  | 0.5 |  |  | AIM "Castin" alloy. Meets acceptance criteria, good results in mfg. Trials | 226 | 211 | 15 |  | 7.37 |  | 26.2 |
| F3 | 95.5 | 0.5 |  | 4 |  |  |  |  | Englehart alloy. Meets acceptance criteria; high liquidus | 226 | 218 | 8 |  | 7.37 |  |  |
| F4 | 83.6 |  |  |  | 8.8 | - | 7.6 |  | Midrange, Indium alloy. Low elongation. Zinc drossing | 195 | 178 | 17 |  | 7.29 |  |  |
| F5 | 77.2 |  |  |  | 20 |  | 2.8 |  | Indium alloy; wide pasty range | 180 | 106 | 74 |  | 7.30 |  |  |
| F6 | 88 |  | 5 |  |  |  | 7 |  | Alpha midrange alloy; Zinc drossing | 194 | 185 | 9 |  | 7.38 |  | 20.5 |
| F7 | 65.5 |  | 31.5 |  |  |  | 3 |  | Alpha alloy, wide pasty range | 171 | 133 | 38 |  | 7.93 |  |  |
| F8 | 95 | 3.5 |  |  | 1.5 |  |  |  | Alpha high-indium alloy; meets acceptance criter- ia; lower yield strength may be beneficial | 220 | 214 | 6 |  | 7.38 |  | 20.4 |
| F9 | 90 | 2 | 0.5 |  |  | 7.5 |  |  | Alpha quaternary alloy | 238 | 229 | 9 |  | 7.30 |  |  |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F10 | 97 | 0.2 |  | 2 |  | 0.8 |  |  | Kester alloy, meets acceptance criteria; lower yield strength may be beneficial | 230 | 219 | 11 |  | 7.33 |  | 21.8 |
| F11 | 78 | 2.5 | 19.5 |  |  |  |  |  | Kester alloy; wide pasty range | 196 | 138 | 58 |  | 7.74 |  |  |
| F12 | 56 | 3 | 41 |  |  |  |  |  | IBM Endicott alloy; low elongation (38.9%) | 166 | 138 | 28 |  | 8.24 |  |  |
| F13 | 43 |  | 55 | 2 |  |  |  |  | High Cu, similar to A6; lower elongation, wider pasty range | 140 | 138 | 2 |  | 8.53 |  |  |
| F14 | 50 |  | 48 | 2 |  |  |  |  | Similar to F13 and A6; lower elongation (18.5%), wider pasty range | 153 | 138 | 15 |  | 8.35 |  |  |
| F15 | 42 |  | 57 |  | 1 |  |  |  | IBM alloy; high Bi content, improved elongation over A6, meets acceptance criteria; poor wetting | 138 | 132 | 6 |  | 8.54 |  | 16.5 |
| F16 | 42 |  | 56.7 | 0.3 | 1 |  |  |  | IBM alloy; similar to F15, lower elongation | 138 | 132 | 6 |  | 8.54 |  |  |
| F17 | 91.8 | 3.4 | 4.8 |  |  |  |  |  | SNL alloy #1. Similar to E4; small peak at 137 ºC from quench. | 215.9 | 211 | 4.9 |  | 7.47 |  | 22.3 |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Sb | Zn | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F18 | 82 |  | 3 |  | 15 |  |  |  | NIST Sn-Bi-In system, similary to EN1; 113 ºC solidus |  | 113 |  |  | 7.37 |  |  |
| F19 | 82 | 3 | 5 |  | 10 |  |  |  | Midrange high-In alloy, composition adjusted to reduce pasty range |  |  |  |  | 7.46 |  |  |
| F20 | 85 |  | 5 |  | 10 |  |  |  | Midrange high-In alloy, composition adjusted to reduce pasty range |  |  |  |  | 7.40 |  | 20.3 |
| F21 | 77.2 | 2.8 |  |  | 20 |  |  |  | INDALLOY 227 | 187 | 175 | 12 |  | 7.36 |  | 23.1 |
| F22 | 95 | 0.1 | 1 |  |  | 3.9 |  |  | Plumbing solder |  |  |  |  | 7.29 |  |  |
| F23 | 95 | 0.5 | 1.5 |  |  | 3 |  |  | Plumbing solder |  |  |  |  | 7.32 |  |  |
| F24 | 43 |  | 55 |  |  |  | 2 |  | Ternary Sn-Bi-Zn eutectic |  |  |  |  | 8.49 |  |  |
| F25 | 43.5 | 0.5 | 56 |  |  |  |  |  | Ternary Sn-Bi-Ag eutectic |  |  |  |  | 8.53 |  |  |
| F26 | 88.9 | 4.5 |  | 1.6 |  | 5 |  |  | SNL alloy #2 |  |  |  |  | 7.39 |  |  |
| F27 | 95.5 | 3.5 |  | 0.5 |  |  | 1 |  | AT&T alloy [check total composition, 100.5%] | 221 | 219 | 2 |  | 7.38 |  |  |
| F28 | 85.7 | 3 |  |  | 10.9 | 0.4 |  |  | Qualitek alloy | 217.6 | 201 | 16.6 |  | 7.37 |  |  |
| F29 | 93.6 | 4.7 |  | 1.7 |  |  |  |  | SNL alloy #3 |  |  |  |  | 7.43 |  |  |
| F30 | 96.1 | 3.2 |  | 0.7 |  |  |  |  | NIST alloy |  |  |  |  | 7.38 |  |  |
| F31 | 95.2 | 3.5 |  | 1.3 |  |  |  |  | NIST alloy |  |  |  |  | 7.40 |  |  |

Note: Following alloys F32 to F65 and A0 were experimental or reference alloys prepared to investigate failures due

to fillet-lifting observed in through-hole joints when soldered with certain lead-free solder alloys.  Because these alloys

were not intended to replace tin-lead solder, their property values were not systematically collected.

| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Sn | Ag | Bi | Cu | In | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F32 | 95.54 | 3.47 |  |  | 0.99 |  | Alloy A4, plus 1% In; Sn/Ag ratio preserved | 223 | 218.8 | 4.2 |  | 7.38 |  |  |
| F33 | 93.69 | 3.40 |  |  | 2.91 |  | Alloy A4, plus 3% In; Sn/Ag ratio preserved | 216 | 214.1 | 1.9 |  | 7.38 |  |  |
| F34 | 91.90 | 3.33 |  |  | 4.76 |  | Alloy A4, plus 5% In; Sn/Ag ratio preserved | 214.7 | 210.4 | 4.3 |  | 7.38 |  |  |
| F35 | 94.06 | 2.97 | 1.98 |  | 0.99 |  | Alloy E4, plus 1% In; Sn/Ag ratio preserved | 221.1 | 215.2 | 5.9 |  | 7.40 |  |  |
| F36 | 92.23 | 2.91 | 1.94 |  | 2.91 |  | Alloy E4, plus 3% In; Sn/Ag ratio preserved | 215.1 | 208.9 | 6.2 |  | 7.40 |  |  |
| F37 | 90.48 | 2.86 | 1.90 |  | 4.76 |  | Alloy E4, plus 5% In; Sn/Ag ratio preserved | 210.1 | 202.8 | 7.3 |  | 7.40 |  |  |
| F38 | 90.89 | 3.37 | 4.75 |  | 0.99 |  | Alloy E4, plus 1% In; Sn/Ag ratio preserved | 215.9 | 210.4 | 5.5 |  | 7.47 |  |  |
| F39 | 89.13 | 3.30 | 4.66 |  | 2.91 |  | Alloy E4, plus 3% In; Sn/Ag ratio preserved | 212.6 | 206.1 | 6.5 |  | 7.46 |  |  |
| F40 | 87.43 | 3.24 | 4.57 |  | 4.76 |  | Alloy E4, plus 5% In; Sn/Ag ratio preserved | 208.0 | 199.1 | 8.9 |  | 7.46 |  |  |
| F41 | 89.5 | 3.5 | 7 |  |  |  |  | 202.0 | 185 | 17 |  | 7.51 |  |  |
| F42 | 86.5 | 3.5 | 10 |  |  |  |  | 213.3 | 205.5 | 7.8 |  | 7.57 |  |  |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F43 | 91.5 | 2.5 |  | 1 | 5 |  | Ag reduced to increase ductility; Cu added to improve wetting. Same room-temperature strength as for F2. | 205 | 140 |  |  | 7.37 |  |  |
| F44 | 91.5 | 1.5 |  | 2 | 5 |  | Ag reduced to increase ductility; Cu added to improve wetting. Same room-temperature strength as for F2. | 205 | 140 |  |  | 7.36 |  |  |
| F45 | 91.5 | 0.5 |  | 3 | 5 |  | Ag reduced to increase ductility; Cu added to improve wetting. Same room-temperature strength as for F2. | 212 |  |  |  | 7.35 |  |  |
| F46 | 95 |  | 5 |  |  |  | Ag replaced by 5% Bi to lower melting point. | 222 |  |  |  | 7.39 |  |  |
| F47 | 94 |  | 5 |  | 1 |  | Ag replaced by 5% Bi to lower melting point; 1% In added to increase ductility, lower melting pt. | 221 |  |  |  | 7.39 |  |  |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F48 | 92 |  | 5 |  | 3 |  | Ag replaced by 5% Bi to lower melting point; 3% In added to increase ductility, lower melting pt. | 215 |  |  |  | 7.39 |  |  |
| F49 | 90 |  | 5 |  | 5 |  | Ag replaced by 5% Bi to lower melting point; 3% In added to increase ductility, lower melting pt. | 210 |  |  |  | 7.39 |  |  |
| F50 | 95 |  |  |  | 5 |  | Sn only, with 5% In added to increase ductility, lower melting pt | 221 |  |  |  | 7.30 |  |  |
| F51 | 93.5 | 0.5 |  | 1 | 5 |  | Reintroduce Ag; add Cu at eutectic composition; complements F43-F45. |  |  |  |  | 7.33 |  |  |
| F52 | 92.5 | 1.5 |  | 1 | 5 |  | Add more Ag; add Cu at eutectic composition; complements F43-F45. |  |  |  |  | 7.35 |  |  |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F53 | 94 |  | 1 |  | 5 |  | Reintroduce 1% Bi to lower melting point; keep In at 5%. |  |  |  |  | 7.32 |  |  |
| F54 | 92 |  | 3 |  | 5 |  | Increase Bi; keep In at 5%. |  |  |  |  | 7.36 |  |  |
| F55 | 94.5 | 0.5 |  |  | 5 |  | Remove Bi, reintroduce Ag; keep In at 5%. |  |  |  |  | 7.31 |  |  |
| F56 | 93.5 | 1.5 |  |  | 5 |  | Increase Ag; keep In at 5%. |  |  |  |  | 7.33 |  |  |
| F57 | 94.15 | 3.41 |  |  |  | 2.44 | 2.5% Pb added to A4; Sn/Ag ratio maintained same as in A4 |  |  |  |  | 7.44 |  |  |
| F58 | 91.90 | 3.33 |  |  |  | 4.76 | 5% Pb added to A4; Sn/Ag ratio maintained same as in A4 |  |  |  |  | 7.50 |  |  |
| F59 | 89.56 | 3.32 | 4.68 |  |  | 2.44 | 2.5% Pb added to F17; Sn/Ag ratio maintained same as in F17 |  |  |  |  | 7.53 |  |  |
| F60 | 87.43 | 3.24 | 4.57 |  |  | 4.76 | 5% Pb added to F17; Sn/Ag ratio maintained same as in F17 |  |  |  |  | 7.59 |  |  |

| Designation and Composition of Lead-Free Solders (cont.) |
| --- |
| A. C. | Composition (% by Mass) | Comments | Melting Temperature (ºC) | Density (g/cm3) | Spec- ific Heat (J/g) | CTE (µm per m.ºC) |
|  | Sn | Ag | Bi | Cu | In | Pb |  |  |  |  |  |
|  |  |  |  |  |  |  |  | L | S | P. R. | Meas. | Calc. |  |  |
| F61 | 92.68 |  |  |  | 4.88 | 2.44 | 2.5% Pb added to F50; Sn/In ratio maintained same as in F50 |  |  |  |  | 7.37 |  |  |
| F62 | 90.48 |  |  |  | 4.76 | 4.76 | 5% Pb added to F50; Sn/In ratio maintained same as in F50 |  |  |  |  | 7.43 |  |  |
| F63 | 97.5 | 2.5 |  |  |  |  |  |  |  |  |  | 7.36 |  |  |
| F64 | 95.12 | 2.44 |  |  |  | 2.44 | 2.5% Pb added to F63; Sn/Ag ratio maintained same as in F63 |  |  |  |  | 7.42 |  |  |
| F65 | 92.86 | 2.38 |  |  |  | 4.76 | 5% Pb added to F63; Sn/Ag ratio maintained same as in F63 |  |  |  |  | 7.48 |  |  |

Source: Technical Reports for the Lead Free Solder Project: Alloy Descriptions: "Lead-Free Solder Alloy Designation and Composition;" Lead Free Solder Project CD-ROM, National Center for Manufacturing Sciences  (NCMS), 1998

5. Useful References:

5.1. References to Tabular Data:

- Authors not listed; “Lead-Free Alloy Trends for the Assembly of Mixed Technology PWBs”, Proc. NEPCON-West 2000 (Feb. 27-Mar. 2) Anaheim, CA

- M. Abtew, “Wetting Characteristics of Lead Free Solders for High Volume Surface Mount Application,” Proc. NEPCON West 2000 Conf. (Feb. 28 - Mar. 2, 2000) Anaheim, CA

- Chad M. Miller, Iver E. Anderson and Jack F. Smith, “A Viable Tin-Lead Solder Substitute: Sn-Ag-Cu,” J. Electronic Mater. 23(7) 595-601 (1994)

- Iver E. Anderson, “Tin-Silver-Copper: A Lead-Free Solder for Capacitor Interconnects,” p. 16, Proc. 16th Capacitor and Resistor Technology Symposium (CARTS 96), 11-15 March, 1996

- Iver E. Anderson, Özer Ünal, Tamara E. Bloomer and James C. Foley, “Effects of Transition Metal Alloying on Microstructural Stability and Mechanical Properties of Tin-Silver-Copper Solder Alloys,” Proc. Third Pacific Rim International Conference on Advanced Materials and Processing (PRICM 3) (The Minerals, Metals and Materials Society, 1998)

- Iver E. Anderson, Tamara E. Bloomer, Robert L. Terpstra, James C. Foley, Bruce A. Cook  and Joel Harringa, “Development of Eutectic and Near-Eutectic Tin-Silver-Copper Solder Alloys for Lead-Free Electronic Assemblies,” IPCWorks ’99: An International Summit on Lead-Free Electronics Assemblies,” (October 25-28, 1999), Minneapolis, MN

- Iver E. Anderson, Tamara E. Bloomer, Robert L. Terpstra, James C. Foley, Bruce A. Cook  and Joel Harringa, “Development of Eutectic and Near-Eutectic Tin-Silver-Copper Solder Alloys for Lead-Free Joining Applications,” p. 575 (complete citation not available)

- Artaki, D.W. Finley, A.M. Jackson, U. Ray and P.T. Vianco, “Wave Soldering with Pb-Free Solders,” Proc. Surface Mount International  (San Jose, CA, August 27-31, 1995), p. 495.

- Peter Biocca, “Global Update on Lead-free Solders,” Proc. Surface Mount International (San Jose, CA, 1998), pp. 705-709

- E.A. Brandes, Smithells Metals Reference Book, 6th ed. (Butterworths, London, 1983)

- S.D. Brandi, S. Liu, J.E. Indacochea and  R. Xu, “Brazeability and Solderability of Engineering Materials,” ASM Handbook, Vol. 6: Welding, Brazing and Soldering (ASM International, 1993)

- D.R. Frear, S.N. Burchett, H.S. Morgan, and J.H. Lau, eds., The Mechanics of Solder Alloy Interconnects, p. 60 (Van Nostrand Reinhold, New York, 1994)

- E.Gebhardt and G. Petzow, Z. Metallkde. 50, 597 (1950)

- Judith Glazer, “Microstructure and Mechanical Properties of Pb-free Solder Alloys for Low-Cost Electronic Assembly: A Review,” J. Electronic Materials 23(8), 693 (1994)

- D.E. Gray, ed., American Institute of Physics Handbook, (McGraw-Hill, New York, 1957)

- Angela Grusd, “Lead Free Solders in Electronics,” SMI97, p. 648

- William B. Hampshire, “The Search for Lead-Free Solders,” Proc. Surface Mount International Conference (Sept. 1992) San Jose, CA, p. 729

- E.W. Hare and R.G. Stang, J. Electronic Mater. 21, 599 (1992)

- Cynthia L. Hernandez, Paul T. Vianco, Jerome A. Rejent, “Effect of Interface Microstructure on the Mechanical Properties of Pb-Free Hybrid Microcircuit Solder Joints,” IPC/SMTA Electronics Assembly Expo (1998), p. S19-2-1

- J.S. Hwang, “Overview of Lead-Free Solders for Electronics & Microelectronics,” Proc. SMI Conf. , p. 405

- S.K. Kang, J. Horkans, P.C. Andricacos, R.A. Carruthers, J. Cotte, M. Datta, P. Gruber, J.M.E. Harper, K. Kwietniak, S. Sambucetti, L. Shi, G. Brouillette and D. Danovitch, “Pb-Free Solder Alloys for Flip Chip Applications,” 49th Electronic Components Technology Conf. (1999), June 1-4, San Diego CA

- M.A. Korhonen, D.D. Brown and C.-Y. Li, “Mechanical Properties of Plated Copper,” Mat. Res. Soc. Symp. Proc. Vol. 323, p. 104 (MRS, 1994) (“plated [thin foil] copper”)

- M.A. Kwoka and D.M. Foster, “Lead Finish Comparison of Lead-Free Solders versus Eutectic Solder,” Proc. Surface Mount International Conference (1994), p. 433

- N.A. Lange, Handbook of Chemistry, p. 100  (Handbook Publishers, Sandusky, Ohio, 1956)

- J. Lau, C. Chang, R. Lee, T.-Y. Chen, D. Cheng, T.J. Tseng, D. Lin, “Thermal-Fatigue Life of Solder Bumped Flip Chip on Micro Via-In-Pad (VIP) Low Cost Substrates”

- J.H. Lau and S.-W. Ricky Lee, “Fracture Mechanics Analysis of Low Cost Solder Bumped Flip Chip Assemblies with Imperfect Underfills,” Proceedings: NEPCON West Conference (February 28 – March 2, 1995), Anaheim, CA

- N.-C. Lee, J.A. Slattery, J.R. Sovinsky, I. Artaki, P.T. Vianco, “A Drop-In Lead-Free Solder Replacement,” Proceedings: NEPCON West Conference (February 28 – March 2, 1995), Anaheim, CA

- N.-C. Lee and W. Casey, “Soldering Technology for Area Array Packages,” Proceedings: NEPCON WEST 2000 (February 27 – March 2, 2000), Anaheim, CA

- Ning-Cheng Lee, “Lead-Free Soldering of Chip-Scale Packages,” Chip Scale Review, p. 42 (March/April 2000)

- M.E. Loomans, S. Vaynman, G.Ghosh and M.E. Fine, “Investigation of Multi-component Lead-free Solders,” J. Elect. Matls. 23(8), 741 (1994)

- Rao Mahidhara, “A Primer on Lead-Free Solder,” Chip Scale Review (March-April 2000)

- T.B. Massalski, Binary Phase Diagrams, 2nd ed. (Amer. Soc. Metals, 1990)

- H. Mavoori, Semyon Vaynman, Jason Chin, Brian Moran, Leon M. Keer and Morris E. Fine, “Mechanical Behavior of Eutectic Sn-Ag and Sn-Zn Solders,” Mat. Res. Soc. Symp. Proc. Vol. 390, p. 161 (MRS, 1995)

- H. Mavoori, J. Chin, S. Vaynman, B. Moran, L. Keer and M. Fine, “Creep, Stress Relaxation, and Plastic Deformation in Sn-Ag and Sn-Zn Eutectic Solders,” J. Electronic Materials, 26(7), 783 (1997)

- Rodney J. McCabe and Morris E. Fine, “Athermal and Thermally Activated Plastic Flow in Low Melting Temperature Solders at Small Stresses,” Scripta Materialia 39(2), 189 (1998)

- Rodney J. McCabe and Morris E. Fine, “The Creep Properties of Precipitation-Strengthened Tin-Based Alloys,” JOM, p. 33 (June 2000)

- NCMS, Technical Reports for the Lead Free Solder Project: Properties Reports: "Room Temperature Tensile Properties of Lead-Free Solder Alloys;" Lead Free Solder Project CD-ROM, National Center for Manufacturing Sciences  (NCMS), 1998

- Y.-H. Pao, S. Badgley, R. Govila and E. Jih, “An Experimental and Modeling Study of Thermal Cyclic Behavior of Sn-Cu and Sn-Pb Solder Joints,” Mat. Res. Soc. Symp. Proc. Vol. 323, p. 128 (MRS, 1994)

- Alan Rae and Ronald C. Lasky, “Economics and Implications of Moving to Lead-Free Assembly,” Proc. NEPCON WEST 2000 (February 27 – March 2, 2000), Anaheim, CA

- Karl Seelig and David Suraski, “The Status of Lead-Free Solder Alloys,” Proc. 50th IEEE 2000 Electronic Components and Technology Conference (May 21-24, 2000), Las Vegas, NV

- Jeff D. Sigelko and K.N. Subramanian, “Overview of lead-free solders,” Adv. Mat. & Proc., pp. 47-48 (March 2000)

- J.A. Slattery and C.E.T. White, U.S. Patent 5,256,370 (Oct. 26, 1993)

- V. Solberg, “No-Lead Solder for CSP: The Impact of Higher Temperature SMT Assembly Processing,” Proc. NEPCON West 2000 Conf. (Feb. 28 - Mar. 2, 2000) Anaheim, CA  (Source: Indium Corp.)

- S.M. Spearing, M.A. Tenhover, D.B. Lukco, L. Viswanathan and D.K. Hollen, “Models for the Thermomechanical Behavior of Metal/Ceramic Laminates,” Mat. Res. Soc. Symp. Proc. Vol. 323, p. 128 (MRS, 1994)

- R.R. Tummala and E.J. Rymaszewski, eds. Microelectronics Packaging Handbook,  (Van Nostrand Reinhold, 1989, NY)

- Paul T. Vianco, “General Soldering,” ASM Handbook, Vol. 6, Welding, Brazing, and Soldering (ASM International, 9639 Kinsman Road, Materials Park, Ohio 44073 USA, 1993)

- M.E. Warwick, “The Wetting and Mechanical Properties of Lead-Free Capillary Plumbing Solders,” ATB Metallurgie XXV, No. 1, 43-50 (1985)

- Welco Castings, Solder Data Sheet, 2 Hillyard Street, Hamilton, Ontario, Canada

- Walter L. Winterbottom, “Converting to Lead-Free Solders: An Automotive Industry Perspective,” JOM, 20-24 (July 1993)

- Tim Wong and A.H. Matsunaga, “Ceramic Ball Grid Array Solder Joint Thermal Fatigue Life Enhancement,” Proceedings: NEPCON West Conference (February 28 – March 2, 1995), Anaheim, CA

5.2. Reference Books:

- ASM Handbook, Vol. 6, Welding, Brazing, and Soldering (ASM International, 9639 Kinsman Road, Materials Park, Ohio 44073 USA, 1993)

- P. Borgesen, K.F. Jensen and R.A. Pollak, eds., “Electronic Packaging Materials Science VII,” Matls. Res. Soc. Symp. Proc. Vol. 323, (MRS, Pittsburgh, 1994

- E.A. Brandes, Smithells Metals Reference Book, 6th ed. (Butterworths, London, 1983)

- J.R. Davis, ed., Metals Handbook, Desk Edition (2nd ed.), (ASM International, Materials Park, Ohio 44073-0002 USA, 1998)

- D.R. Frear, W.B. Jones and K.R. Kinsman, eds., Solder Mechanics (TMS, 1991)

- D.R. Frear, H.S. Morgan, S.N. Burchett, and J.H. Lau, eds., The Mechanics of Solder Alloy Interconnects  (Van Nostrand Reinhold. New York, 1994)

- D.E. Gray, ed., American Institute of Physics Handbook, (McGraw-Hill, New York, 1957)

- R.J. Klein Wassink, Soldering in Electronics (Electrochemical Publications, Ltd., 1989)

- N.A. Lange, Handbook of Chemistry, p. 100  (Handbook Publishers, Sandusky, Ohio, 1956)

- Lieberman, Modern Soldering and Brazing Techniques (Business News Publishing Co., 1988)

- H.H. Manko, Solders and Soldering, 3nd ed. (McGraw-Hill, 1992)

- R. Skipp, Soldering Handbook (McGraw-Hill, 1964)

- R.R. Tummala and E.J. Rymaszewski, eds. Microelectronics Packaging Handbook,  (Van Nostrand Reinhold, 1989, NY)

- Paul T. Vianco, “General Soldering,” ASM Handbook, Vol. 6, Welding, Brazing, and Soldering (ASM International, 9639 Kinsman Road, Materials Park, Ohio 44073 USA, 1993)

- R.W. Woodgate, The Handbook of Machine Soldering, 2nd ed. (John Wiley & Sons, 1988)

5.3. Useful URLs

Organizations Involved in Lead-Free Solder Issues:

Japan Electronic Industry Development Association (JEIDA): “Challenges and Efforts Toward Commercialization of Lead-free Solder – Road Map 2000 for Commercialization of Lead-free Solder” – Ver 1.2

Lead Free Soldering Technology Centre (Soldertec)

( www.lead-free.org/  and  http://www.solderworld.com/ )

IPC: Association Connecting Electronics Industries  (“Get the Lead OUT!)

( http://www.leadfree.org/ )

Materials Properties and Data, Materials Science and Engineering Laboratory (MSEL), NIST