TD-04-013

May 12, 2004

RESULTS OF Nb3Sn CABLE TESTS AT SELF-FIELD USING THE UPGRADED SC TRANSFORMER

E. Barzi, D. Turrioni

Abstract:

A 28 kA SC transformer [1] was used to measure the quench current of PIT and MJR SC cables at self-field under various cooling conditions. Using the existing SSTF and strand power supply makes this an efficient way to a fast turn-around and reliable data. A fast DAQ system [2] allows a real-time acquisition of the secondary current, as well as recording each quench pattern by means of voltage taps placed along the sample. The results obtained in the first systematic run of thirteen Nb3Sn cable tests are herein described.

- INTRODUCTION

To investigate cable instability, which is a phenomenon that shows itself at low fields, cable tests at self-field using the existing SSTF and strand power supply is an economic way to a fast turn-around and reliable data. To make this also an efficient and useful system for magnet R&D, the upgraded transformer was designed to provide a maximum current in the secondary winding close to 28 kA, which is a typical short sample limit for Small Racetracks with strand Jc’s of 2000 A/mm2. The short sample limits of Cos-theta models are typically close to 25 kA for the same strand critical current densities. The upgraded transformer is being extensively used to test impregnated and non-impregnated cables, enabling investigation of the various effects that have been tied to cable instability, such as deff, matrix resistivity, RRR and cooling. This note reports in detail the results obtained in a first systematic run of thirteen cable tests, including impregnated 28 x 1 mm rectangular PIT, impregnated and non-impregnated 28 x 1 mm keystoned MJR, and impregnated and non-impregnated 41 x 0.7 mm rectangular MJR cables of the react & wind type.

- STRAND AND CABLE DESCRIPTION

The parameters of the thirteen cable samples that were tested are shown in Table I. The PIT and MJR2 cables were fabricated at FNAL, whereas the MJR1 and MJR3 cables were fabricated at LBNL. All cables had the same pitch length of about 110 mm, corresponding to a transposition angle of 14.5(0.1 degree for the 28-strand cables and of 15.4(0.1 degree for the 41-strand cables. The “R” and “KS” under “Cable Geometry” in Table I denote rectangular and keystoned cables respectively. For the keystoned cables, the keystone angle was 0.9(0.1 degree. The SS core material is 9.52 mm by 0.025 mm, 316-L annealed. The heat treatment (HT) cycles are shown in Table III. Three different multifilamentary Modified Jelly Roll (MJR) Nb3Sn strands by Oxford Superconducting Technology (OST), and one Powder-in-Tube strand by ShapeMetal Innovation (SMI) were used to manufacture the cables. The strands parameters are shown in Table II. Close-ups of cross sections of the rectangular PIT and the keystoned MJR2 cables after reaction are shown in Figs. 1 and 2 respectively.

The SC transformer and test facility, sample preparation, instrumentation and mounting, and data acquisition and test procedure are described in [1, 2].

Table I. Parameters of tested cable samples.

| Sample No. | Strand Type | Strand Size, mm | Strand No. | HT | RRR | PF, % | Cable Geometry | SS Core | Impregnation | Test Date (2004) | Special Notes |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | PIT | 1.0 | 28 | A | ~ 90 | 88.6 | R | N | Y | 03/24 | Ceramic Insulation & Binder |
| 2 | PIT | 1.0 | 28 | A | ~ 90 | 88.6 | R | N | Y | 03/29,30 | “ |
| 3 | MJR1 | 1.0 | 28 | B | ~ 5 | 88.6 | KS | N | Y | 01/09 | Ceramic Insulation & Binder |
| 4 | MJR1 | 1.0 | 28 | B | ~ 5 | 88.6 | KS | N | Y | 04/01 | “ |
| 5 | MJR2 | 1.0 | 28 | C | ~ 50 | 88.4 | KS | Y | N | 03/25 | Ceramic Insulation & Binder |
| 6 | MJR2 | 1.0 | 28 | C | ~ 50 | 88.4 | KS | Y | Y | 04/15 | “ |
| 7 | MJR2 | 1.0 | 28 | C | ~ 50 | 88.4 | KS | Y | Y | 04/23 | “ |
| 5a | MJR2 | 1.0 | 28 | C | ~ 50 | 88.4 | KS | Y | Y | 05/03 | Is Sample 5 impregnated |
| 8 | MJR3 | 0.7 | 41 | B | ~ 5 | 85.6 | R | N | N | 04/21 | React & Wind |
| 9 | MJR3 | 0.7 | 41 | B | ~ 5 | 85.6 | R | N | N | 05/12 | “ |
| 10 | MJR3 | 0.7 | 41 | B | ~ 5 | 85.6 | R | N | Y | 04/19 | R&W, E-glass sleeve |
| 11 | MJR3 | 0.7 | 41 | B | ~ 5 | 85.6 | R | N | Y | 04/22 | “ , “ |
| 8a | MJR3 | 0.7 | 41 | B | ~ 5 | 85.6 | R | N | Y | 04/27 | Is Sample 8 impregnated |

Table II. Parameters of the strands used in the cables.

| Strand Parameter | MJR1 | MJR2 | MJR3 | PIT |
| --- | --- | --- | --- | --- |
| Strand diameter, mm | 1.000(0.001 | 1.000(0.001 | 0.7(0.001 | 1.000(0.001 |
| Ic(12T), A | ~ 700 | ~ 730 | ~ 400 | ~ 700 |
| deff, (m | ~ 110 | ~ 110 | ~ 80 | ~ 50 |
| Cu, % | 47.8 ( 0.3 | 46.7 ( 0.3 | 47 ( 0.3 | 53.6 ( 0.3 |
| Twist pitch, mm/turn | 23 ( 3 | 23 ( 3 | 15( 3 | 20 ( 3 |

Table III. Heat treatment cycles.

| Heat Treatment | Step 1 | Step 2 | Step 3 |
| --- | --- | --- | --- |
|  |  | Ramp rate, oC/h | 25 |  |  |
| A | SMI_NOMINAL | Temperature, oC | 655 |  |  |
|  |  | Duration, h | 170 |  |  |
|  |  | Ramp rate, oC/h | 25 | 50 | 75 |
| B | OST_NOMINAL | Temperature, oC | 210 | 340 | 650 |
|  |  | Duration, h | 100 | 48 | 180 |
|  |  | Ramp rate, oC/h | 25 | 50 | 75 |
| C | OST_SHORT | Temperature, oC | 210 | 340 | 650 |
|  |  | Duration, h | 100 | 48 | 72 |

Fig. 1.  Close-up of cross section of rectangular PIT cable after reaction (Ryuji Yamada courtesy).

Fig. 2.  Close-up of cross section of keystoned MJR2 cable after reaction (Ryuji Yamada courtesy).

- RESULTS AND DISCUSSION

In the following, a summary of the test results at self-field is shown for every family of cables, i.e. the PIT, MJR1, MJR2 and MJR3 cables. To evaluate the self-field of each test, the load line of the secondary winding is given for convenience in Fig. 10 in Appendix. Details on each cable test run can also be found in Appendix, including the voltage tap schematic (Figs. 11 to 14) that was used for the fast DAQ, a table with comprehensive information on the transformer parameters and splice resistance (Tables IV to XVI) for each test number, a plot of the maximum currents or of the quench history where primary ramp rates are also specified (Figs. 15 to 27), and in the case of quench, typical patterns that were found for the voltage signals (Figs. 28 to XX).

  - 28 x 1 mm Rectangular PIT Cables

Results

Test results for Samples 1 and 2, which are impregnated rectangular cables made of 28 x 1 mm PIT strands, heat treated using the SMI nominal cycle (HT A, RRR ~ 90), are shown in Figs. 3 and 4. Closed markers denote reaching maximum current without quenching, open markers represent quenches. Sample 1, which is the only sample that was tested without operating at all the fast DAQ, reached a maximum current of 23,332A +30A-0A without quenching, as obtained with the 0.8 Hz standard system, and using a primary ramp rate of 20 A/s. Details of the tests are reported in Table IV and Fig. 15. To account for the inaccuracy of the slow DAQ system, error bars are shown in Figure below for all data points associated to tests performed without fast DAQ.

In the case of a sample that does not quench up to maximum secondary currents, the higher the ramp rate with which the primary coil is ramped down, the larger the current induced in the secondary, as the time for the secondary current to decay is shorter. Sample 2 was therefore tested at increasing ramp rates to push the secondary current as high as possible. Details of the tests are reported in Table V and Fig. 16. In a first test run encompassing Test Nos. 1 to 18, the sample showed some training, with a first quench at 24,120A +2,200A-0A before reaching a maximum current of 26,708 A without quenching, with a primary current of 724 A and a ramp rate of 100 A/s. However, the sample quenched again at 26,600 A using a ramp rate of 120 A/s. After such quench, some damage occurred to the splices as confirmed by two subsequent quenches at around 20 kA, and by monitoring the splices resistance during the run. Splices resistance is measured from the decay of the secondary winding using an inductance L2 of 0.23 (H. As detailed in Table V, at the start of the test run, the splices resistance was 1.55 n( at about 24 kA. After the first quench it was 1.72 n( at about 25 kA, but after the second quench it peaked to 5.29 n( at 15 kA. The corresponding resistances at a current level of 5 kA were 1.15 n(, 1.15 n(, and 4.35 n(. The test run was then stopped, the transformer extracted from the cryostat and the sample properly re-spliced. In the second test run, which included Test Nos. 19 to 34, Sample 2 showed again some training by quenching at 25,627 A with a ramp rate of 80 A/s. After such quench, the splices resistance went up by only 0.6 n( at about 26 kA from 1.6 n( at 25.5 kA and the sample reached a maximum current of 26,623 A without quenching anymore, with a primary current of 756 A and a ramp rate of 150 A/s.

Discussion

The good consistency between the results of Sample 1 and Sample 2, and the excellent reproducibility of Sample 2 behavior after a thermal cycle, especially the values of the maximum quench currents in each run, indicate that these PIT cables are close to their stability limits at levels of current of about 26 kA. This would be consistent with SR01 test results at 2.2 K [3], where a quench current cut-off was observed at about 24.2 kA, albeit the expected short sample limit that had been calculated from strand data at 2.2K was 26.1 kA. As in that case the cable was subject to a transverse load that caused at that field a critical current degradation of about 10%, whereas in the transformer setup no substantial load is applied to the sample, such cut-off could have been predicted to be between 23.6 kA and 24.5 kA by reducing the quench current range observed in the cable test (i.e. 25,627 A to 26,600 A) by about 10%.

Fig. 3.  Test results for an impregnated rectangular cable (Sample 1) made of 28 x 1 mm PIT strands, heat treated using the SMI nominal cycle (HT A, RRR ~ 90).

Fig. 4.  Test results for an impregnated rectangular cables (Sample 2) made of 28 x 1 mm PIT strands, heat treated using the SMI nominal cycle (HT A, RRR ~ 90). Closed markers denote reaching maximum current without quenching, open markers represent quenches.

  - 28 x 1 mm Keystoned MJR1 Cables

Results

The quench history results for Samples 3 and 4, which are impregnated keystoned cables made of 28 x 1 mm MJR1 strands, heat treated using the OST nominal cycle (HT B, RRR ~ 5), are plotted in Fig. 5. Two identical cables were simultaneously measured at various magnetic fields at the cable test facility at BNL [4]. In all cases, the cable samples quenched at around some average current. For Sample 3 such current was 14,686 A with a width (stdev) of (608 A. For Sample 4 it was 10,194 A (432 A. The average quench current including both tests would be 12,248 A with a width (stdev) of (2,306 A. Details of the tests are reported in Table VI and VII and Figs. 17 and 18.

Discussion

In both cases, the quench current width is about 4%, as in [4] where the average quench current was 15,040 A ( 588 A. Including all ramp rates, for Sample 3 the 2,547 A difference between maximum and minimum quench currents is 17.3% of the average current, for Sample 4 such difference is 1,657, i.e. 16.3% of the average current, and for [4] it is 2,967 A, i.e. 19.7% of the average current. The standard deviation obtained including data from both cable samples 3 and 4 is on a similar level at 18.8% of the overall average quench current. The difference between Sample 3 and Sample 4 average currents is about 50% larger than the difference between maximum and minimum quench currents in [4]. Consistently with [4], there appears to be a flat ramp rate dependency on the quench current.

It is interesting to notice that the difference between maximum and minimum quench currents in the cos-theta dipole models were on the same level as in Samples 3 and 4. Considering for the sake of homogeneity only coil ramp rates of 20 A/s, at 4.5 K HFDA02 had a quench current difference of 2,350 A, HFDA03 of 1,450 A, and HFDA04 of 1,850 A. Fig. 6 shows a comparison of quench currents at 4.5 K as a function of cable ramp rate between Samples 3 and 4, and HFDA03b [5] and HFDA04 [6], which were fabricated out of cable made of the same MJR1 strand (OST billets 131, and 132) and heat treated with the same thermal cycle. A transformer ratio of 35 was used to calculate current ramp rate in the sample. One can see how the performance of the two cable samples correlates well with that of HFDA03b and HFDA04. This is as more relevant as unstable cables performance does not appear to depend on background field [4]. The widths of the quench current distributions shown in Fig. 6 cannot be compared at all ramp rates as for some ramp rates the number of data points available is insufficient.

Fig. 5.  Quench history results for two impregnated keystoned cables (Samples 3 and 4) made of 28 x 1 mm MJR1 strands, heat treated using the OST nominal cycle (HT B, RRR ~ 5).

Fig. 6.  Comparison of quench currents at 4.5 K as function of cable ramp rate between tests of Samples 3 and 4, and tests of HFDA03b [5] and HFDA04 [6].

3.3   28 x 1 mm Keystoned MJR2 Cables

Results

A summary of test results for Samples 5 to 7, which are keystoned cables made of 28 x 1 mm MJR2 strands and featuring a SS core, heat treated using the short OST cycle (HT C, RRR ~ 50), is shown in Fig. 7. Two of these cables were tested after impregnation, one was tested both before and after impregnation (Sample 5). Closed markers denote reaching maximum current without quenching, open markers represent quenches. In the case of the non-impregnated cable (Sample 5), the sample reached maximum current without quenching. The maximum current reached by the sample as measured with the fast DAQ system was 27,539 A with a current in the primary of 704 A, and a primary ramp rate of 70 A/s. However, in the case of the impregnated cables, Samples 6 and 7, they started quenching above currents of about 24 kA for Sample 6 and of 26 kA for Sample 7. Sample 6 also reached a maximum current of 26,026 A without quenching in Test No. 10 using a ramp rate of 100 A/s, and Sample 7 was able to reach 27,859 A without quenching with a ramp rate of 186 A/s. As the quenches occurred close to the transformer maximum current, such high primary ramp rates had to be used to push the limits of the transformer. Therefore from these data, information of ramp rate dependency on the quench current cannot be inferred. Of the four quench events of Sample 7 (open triangles in Fig. 7), all using a ramp rate of 186 A/s, three occurred during secondary current decay, after the sample had reached its maximum current without quenching. However, Sample 5 after impregnation (Sample 5a) always showed quench, with an average quench current of 21,029 A and a width (stdev) of ( 771 A. The average quench current including all tests of the three impregnated samples would be 23,104 A with a width (stdev) of (2,565 A. Details of these tests are reported in Tables VIII to XI and Figs. 19 to 22.

Discussion

The first observation to be made is that these MJR2 cables, which are made of strands very similar to those used in the MJR1 cables, show a lot better quench current performance. This was first observed for the non-impregnated Sample 5 on March 25, 2004, and confirmed for the impregnated Sample 6 on April 15, 2004. Even cos-theta dipole mirror HFDM02, which was fabricated out of cable made of the same MJR2 strand (OST billets 187, and 190), featured an average quench current at 4.5 K of only 11,485 A ( 507 A, including all ramp rates. A major difference between the MJR1 samples and HFDM02 on one side, and these MJR2 samples on the other is the RRR, which was measured to be 5 in the MJR1 samples, 6 in HFDM02, and about 50 in the MJR2 samples. These data represent a strong experimental evidence of the very important effect of the RRR in the instability phenomenon.

These data show also that the current stability range of the MJR2 samples is smaller than for the PIT samples. In a set of three impregnated cables, there was one (Sample 5a) that featured quench currents as measured with the fast DAQ between 20,146 A and 22,613 A. This was useful to predict SR02 performance, which was limited at 20,200 A despite a 25,500 A short sample limit as calculated from the critical current of witness samples. For Sample 5a, the quench current spread is 3.7%. Including all ramp rates, for this sample the 2,467 A difference between maximum and minimum quench currents is 11.7% of the average current. For Sample 5a, quench currents do not depend on ramp rate. The standard deviation obtained including data from all tests of the three impregnated samples is 11.1% of the overall average quench current. More PIT samples need to be tested to confirm their better performance, but this would certainly be consistent with these strands having both a lower deff and a larger RRR. A lot more statistics is necessary to try and quantifying their separate effects.

Fig. 7.  Summary of test results for three keystoned cables (Samples 5 to 7) made of 28 x 1 mm MJR2 strands and featuring a SS core, heat treated using the OST short cycle (HT C, RRR ~ 50). Two of these cables were tested impregnated, one was tested both before (Sample 5) and after (Sample 5a) impregnation. Closed markers denote reaching maximum current without quenching, open markers represent quenches.

3.4   41 x 0.7 mm Rectangular MJR3 Cables

Results

A summary of test results for Samples 8 to 11, which are rectangular cables made of 41 x 0.7 mm MJR3 strands, heat treated using the nominal OST cycle (HT B, RRR ~ 5), is shown in Fig. 8. One of these cables was tested only non-impregnated, two after impregnation, and one before and after impregnation (Sample 8). As the cables were heat treated on a spool, to be used in the React & Wind technique, they are more prone to damage. In the case of the non-impregnated cables (Samples 8 and 9), after some training the samples reached currents between ~12.5 kA and ~18.9 kA before quenching. The maximum quench current for Sample 8 was 18,862 A, which was obtained with a primary ramp rate of 120 A/s. After a training phase of about 16 quenches, there was no apparent ramp rate dependency on the quench current as can be seen in Fig. 9, where the ramp rate dependency of the quench current is shown for all samples. In the case of the impregnated cables (Samples 10, 11, and 8a), they quenched at lower currents, between ~7.1 kA and ~14.6 kA. Details of these tests are reported in Tables XII to XVI and Figs. 24 to 28.

Discussion

Typical widths of React & Wind quench current distributions appear to be larger than in the Wind & React case. Aside from Sample 10, for which there is very little statistics, the quench current width of the MJR3 cable samples goes from a minimum of 3.7% of the average quench current for Sample 8a to 5.6% of the average quench current for Sample 9, to 7.6% of the average quench current for Sample 11 to a maximum of 10.6% of the average quench current for Sample 8.

Fig. 8 compares the quench current performance of racetrack models HFDB02 [7] and HFDB03 [8], which were made of the same cables as the MJR3 samples, with the quench current performance of the latter. The band delimited by the two red lines envelopes the quench currents of racetrack models HFDB02 and HFDB03 obtained at 4.5K at all ramp rates. It can be seen as there is some consistency between the racetracks test results and the results associated to the impregnated cable samples.

Fig. 8.  Quench history results for four rectangular cables (Samples 8 to 11, and 8a) made of 41 x 0.7 mm MJR3 strands, heat treated using the OST nominal cycle (HT B, RRR ~ 5). One of these cables was tested only non-impregnated, two after impregnation, and one was tested both before (Sample 8) and after (Sample 8a) impregnation. The band delimited by the two red lines envelopes the quench currents of racetrack models HFDB02 [7] and HFDB03 [8] obtained at 4.5K at all ramp rates.

Fig. 9.  Ramp rate dependency of quench current for four rectangular cables (Samples 8 to 11, and 8a) made of 41 x 0.7 mm MJR3 strands, heat treated using the OST nominal cycle (HT B, RRR ~ 5). One of these cables was tested only non-impregnated, two after impregnation, and one was tested both before (Sample 8) and after (Sample 8a) impregnation.

- SUMMARY

Since there are indications that cable instability might have a flat dependence on field, at least in the lower field range, cable tests at self-field using a SC transformer are proving to be extremely useful to gather large statistics at very low costs. With this first run of thirteen tested cables, substantial insight has been collected on the effect of various parameters on the instability phenomenon. First of all, that a RRR of 50 can improve average quench current by nearly a factor of 2 with respect to a RRR of 5. Then that the insulation effect of impregnation could also depend on RRR, as for instance average quench current degradation was about double for a set of impregnated cables having a RRR of 5 than for a set having a RRR of 50, with respect to the average quench current of their non-impregnated versions. More statistics is needed to confirm these first observations, and to quantify the effect of RRR for the various Nb3Sn technologies.

APPENDIX

Fig. 10.  Load line of the transformer secondary winding to evaluate self-field for each test.

Fig. 11.  Voltage tap schematic used for Samples 1, 3, and 5.

Fig. 12.  Voltage tap schematic used for a first run on Samples 2.

Fig. 13.  Voltage tap schematic used for the second run on Sample 2, and for Samples 4, and 6 to 11.

Fig. 14.  Voltage tap schematic used for Sample 5a.

Table IV. Transformer parameters and splice resistance during Sample 1 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Primary Quench | 630 | - | - | - | - |  |
| 2 | NO QUENCH | 645 | 21767 |  | 21767 +30 | 20 | 1.446 |
| 3 | NO QUENCH | 679 | 22159 |  | 22061+400 | 20 | 1.467 |
| 4 | Primary Quench | 707 | - | - | - | - |  |
| 5 | Primary Quench | 704 | - | - | - | - |  |
| 6 | NO QUENCH | 701 | 23332 |  | 23332 +30 | 20 | 1.401 |
| 7 | Primary Quench | 711 | - | - | - | - |  |
| 8 | NO QUENCH | 701 | 22129 |  | 2219+30 | 20 | 1.387 |
| 9 | Primary Quench | 633 | - | - | - | - |  |
| 10 | Primary Quench | 600 | - | - | - | - |  |
| 11 | Primary Quench | 705 | - | - | - | - |  |
| 12 | Primary Quench | 629 | - | - | - | - |  |
| 13 | NO QUENCH | 641 | 20144 |  | 20144+30 | 20 | 1.428 |
| 14 | Primary Quench | 692 | - | - | - | - |  |

NOTE: The column “I2 drift” is I2 as measured by the slow acquisition system after drift correction. The column “I2 Fast DAQ” is I2 as acquired by the fast DAQ system. The column “I2 Fast DAQ drift” is I2 as acquired by the fast DAQ system and corrected for the drift.

Table V. Transformer parameters and splice resistance during Sample 2 test runs.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n | R Splices (I2=5000), n |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FIRST RUN |
| 1 | NO QUENCH | 682 | 22463 |  | 22463+100 | 20 |  |  |
| 2 | NO QUENCH | 700 | 24105 |  | 24105+400 | 40 | 1.55 | 1.15 |
| 3 | Primary Quench | 740 | - | - | - | - |  |  |
| 4 | Primary Quench | 780 | - | - | - | 5 |  |  |
| 5 | Primary Quench | 722 | - | - | - | - |  |  |
| 6 | QUENCH | 722 | 24120 | - | 24120+2200 | 60 |  |  |
| 7 | NO QUENCH | 722 | 24450 | 24500 | 24824 | 30 | 1.72 | 1.15 |
| 8 | NO QUENCH | 723 | 25129 | 25410 | 25571 | 40 |  |  |
| 9 | NO QUENCH | 723 | 25740 | 26370 | 26130 | 60 |  |  |
| 10 | Primary Quench | 735 | - | - | - | - |  |  |
| 11 | NO QUENCH | 724 | 25531 | 26711 | 26708 | 100 |  |  |
| 12 | NO QUENCH | 723 | 25596 | 25911 | 26019 | 60 | 1.83 | 1.24 |
| 13 | QUENCH | 726 | 22184 | 26450 | 26600 | 120 |  |  |
| 14 | QUENCH | 726 | 19145 | 20234 | 20384 | 120 |  |  |
| 15 | Primary or Secondary Quench | 665 | - | - | - | 120 |  |  |
| 16 | Primary Quench | 725 | - | - | - | 1 |  |  |
| 17 | QUENCH | 725 | 17503 | 19370 | 19370 | 60 |  |  |
| 18 | NO QUENCH | 725 | 14383 | 15211 | 15205 | 20 | 5.29 | 4.35 |
| SECOND RUN |
| 19 | Primary Quench | 724 | - | - | - | - |  |  |
| 20 | NO QUENCH | 703 | 23625 | 23810 | 24039 | 35 | 1.71 |  |
| 21 | NO QUENCH | 708 | 24765 | 25156 | 25408 | 70 | 1.56 |  |
| 22 | NO QUENCH | 721 | 25276 | 25045 | 25562 | 60 | 1.63 |  |
| 23 | QUENCH | 723 | 22974 | 25565 | 25627 | 80 |  |  |
| 24 | NO QUENCH | 747 | 25048 |  |  | 80 | 2.21 |  |
| 25 | NO QUENCH | 768 | 25687 | 26457 | 26243 | 78 | 2.23 |  |
| 26 | Primary Quench | 720 | - | - | - | - |  |  |
| 27 | Primary Quench | 764 | - | - | - | - |  |  |
| 28 | NO QUENCH | 730 | 25086 | 25570 | 25671 | 120 |  |  |
| 29 | NO QUENCH | 756 | 26153 | 26332 | 26623 | 150 |  |  |
| 30 | Primary Quench | 720 | - | - | - | - |  |  |
| 31 | NO QUENCH | 725 | 23930 | 24611 | 24510 | 60 |  |  |
| 32 | NO QUENCH | 700 | 24369 |  | 24369+400 | 230 |  |  |
| 33 | Primary Quench | 730 | - | - | - | - |  |  |
| 34 | NO QUENCH | 726 | 25437 | 25646 | 25881 | 240 | 2.39 |  |

Table VI. Transformer parameters and splice resistance during Sample 3 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 700 | 13925 |  | 13925 + 600 | 20 |  |
| 2 | NO DATA | - | - | - | - | - |  |
| 3 | Primary or Secondary Quench | 519 | - | - | - | - |  |
| 4 | NO DATA | - | - | - | - | - |  |
| 5 | QUENCH | 680 | 14389 | 14330 | 15049 | 20 |  |
| 6 | QUENCH | 700 | 13822 | 13815 | 14361 | 20 |  |
| 7 | QUENCH | 660 | 14340 | 14550 | 15069 | 20 |  |
| 8 | QUENCH | 680 | 14892 | 14670 | 15414 | 20 |  |
| 9 | QUENCH | 660 | 12854 | 12744 | 13281 | 20 |  |
| 10 | QUENCH | 640 | 13909 | 14220 | 14805 | 20 |  |
| 11 | QUENCH | 680 | 14400 | 14504 | 15083 | 20 |  |
| 12 | QUENCH | 660 | 14511 | 14433 | 14952 | 20 |  |
| 13 | QUENCH | 800 | 13023 | 13276 | 13904 | 20 |  |
| 14 | QUENCH | 660 | 14000 | 14200 | 14857 | 20 |  |
| 15 | QUENCH | 660 | 13577 | 13800 | 14409 | 20 |  |
| 16 | QUENCH | 600 | 14928 | 15221 | 15828 | 20 |  |
| 17 | QUENCH | 600 | 13497 | 13180 | 13988 | 20 |  |
| 18 | QUENCH | 680 | 14452 | 14210 | 14864 | 20 |  |
| 19 | QUENCH | 560 | 14430 | 14440 | 14975 | 20 |  |
| 21 | QUENCH | 700 | 13924 | 14100 | 14495 | 40 |  |
| 22 | QUENCH | 660 | 12838 | 13960 | 14326 | 40 |  |

Table VII. Transformer parameters and splice resistance during Sample 4 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 571 | 9726 |  | 9726 + 800 | 20 |  |
| 2 | QUENCH | 532 | 9747 | 10220 | 10559 | 20 |  |
| 3 | QUENCH | 467 | 8835 | 9500 | 9589 | 15 |  |
| 4 | QUENCH | 348 | 9868 | 10295 | 10466 | 15 |  |
| 5 | QUENCH | 406 | 8899 | 9450 | 9572 | 15 |  |
| 6 | QUENCH | 424 | 8912 | 9661 | 9914 | 15 |  |
| 7 | QUENCH | 401 | 9285 | - | 9285 + 400 | 10 |  |
| 8 | QUENCH | 360 | 8935 | 9100 | 10042 | 15 |  |
| 9 | QUENCH | 410 | 10255 | 10955 | 11157 | 15 |  |
| 10 | QUENCH | 394 | 9371 | 10210 | 10372 | 15 |  |
| 11 | QUENCH | 378 | 8927 | 9240 | 9500 | 15 |  |
| 12 | QUENCH | 360 | 9406 | 9970 | 10207 | 15 |  |
| 13 | QUENCH | 391 | 10271 | 10850 | 11085 | 15 |  |
| 14 | QUENCH | 365 | 9386 | 10288 | 10405 | 15 |  |
| 15 | QUENCH | 407 | 9411 | 10060 | 10200 | 15 |  |
| 16 | QUENCH | 395 | 9816 | 9893 | 10095 | 15 |  |
| 17 | QUENCH | 352 | 9110 | 9477 | 9765 | 15 |  |
| 18 | QUENCH | 362 | 8676 | 9850 | 10051 | 30 |  |
| 19 | QUENCH | 346 | 9767 | 10323 | 10531 | 30 |  |
| 20 | QUENCH | 361 | 8845 | 9750 | 10017 | 60 |  |
| 21 | QUENCH | 361 | 6554 | 9981 | 10225 | 60 |  |
| 22 | QUENCH | 391 | 4482 | 10103 | 10300 | 120 |  |
| 23 | QUENCH | 400 | 4169 | 9854 | 10032 | 120 |  |

Table VIII. Transformer parameters and splice resistance during Sample 5 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Primary Quench | 640 | - | - | - | - |  |
| 2 | Primary Quench | 630 | - | - | - | - |  |
| 3 | File not saved | 612 |  |  |  | 10 |  |
| 4 | Primary Quench | 621 | - | - | - | - |  |
| 5 | NO QUENCH | 613 | 21812 | 22576 | 22474 | 20 |  |
| 6 | NO QUENCH | 641 | 23333 | 23407 | 23607 | 20 |  |
| 7 | NO QUENCH | 665 | 23867 | 24100 | 24350 | 20 |  |
| 8 | Primary Quench | 685 | - | - | - | - |  |
| 9 | NO QUENCH | 680 | 25853 | 25970 | 26131 | 40 |  |
| 10 | NO QUENCH | 683 | 25511 | 26766 | 26866 | 60 |  |
| 11 | NO QUENCH | 690 | 25318 | 25643 | 26341 | 50 |  |
| 12 | Primary Quench | 712 | - | - | - | - |  |
| 13 | NO QUENCH | 704 | 27048 | 27207 | 27539 | 70 |  |
| 14 | NO QUENCH | 703 | 27155 | 27205 | 27520 | 100 |  |
| 15 | Primary or Secondary Natural Quench | 587 |  |  |  | 100 |  |
| 16 | Primary Quench | 594 | - | - | - | - |  |
| 17 | Primary Quench | 649 | - | - | - | - |  |
| 18 | Primary Quench | 693 | - | - | - | - |  |
| 19 | NO QUENCH | 704 | 24951 | 25040 | 25259 | 100 |  |
| 20 | NO QUENCH | 705 | 24600 | 24680 | 24983 | 70 |  |

Table IX. Transformer parameters and splice resistance during Sample 5a test run.

| Test No. | EVENT | I1, A | I2, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splice nL2=0.23H |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 706 | 19130 | 18112 |  | 18112 +1750 | 50 |  |
| 2 | QUENCH | 706 | 19235 | 19647 | 21370 | 21782 | 50 |  |
| 3 | QUENCH | 617 | 18161 | 18690 | 20173 | 20702 | 30 |  |
| 4 | Standard test Splice | 560 | 17313 | 17680 |  |  |  | 1.58 |
| 5 | Primary Quench | 690 | 3000 | - | - | - | - |  |
| 6 | Primary Quench | 689 | 3588 | - | - | - | - |  |
| 7 | Primary Quench | 687 | 800 | - | - | - | - |  |
| 8 | QUENCH | 633 | 19378 | 19782 | 20769 | 21173 | 30 |  |
| 9 | QUENCH | 662 | 17952 | 19507 | 18592 | 20146 | 15 |  |
| 10 | QUENCH | 690 | 20011 | 20227 | 20011 | 20227 | 15 |  |
| 11 | QUENCH | 694 | 19531 | 19579 | 20126 | 20174 | 15 |  |
| 12 | QUENCH | 701 | 19637 | 19895 | 20345 | 20604 | 15 |  |
| 13 | Primary Quench | 705 | 647 |  |  |  |  |  |
| 14 | QUENCH | 699 | 19347 | 19843 | 19786 | 20282 | 15 |  |
| 15 | Primary Quench | 645 | 5739 |  |  |  |  |  |
| 16 | Standard test Splice | 695 | 20663 | 20742 |  |  |  | 1.74 |
| 17 | QUENCH | 697 | 18588 | 18732 | 20380 | 20524 | 30 |  |
| 18 | QUENCH | 695 | 19312 | 19512 | 21530 | 21730 | 60 |  |
| 19 | QUENCH | 681 | 19748 | 19549 | 21965 | 21766 | 60 |  |
| 20 | QUENCH | 707 | 18399 | 18618 | 22000 | 22219 | 100 |  |
| 21 | Primary Quench | 660 | 1013 |  |  |  |  |  |
| 22 | NO Quench | 706 | 22063 | 22271 | 22822 | 23030 | 100 |  |
|  | QUENCH |  | 22063 | 22271 | 22405 | 22613 | 100 |  |
| 23 | QUENCH | 707 | 20135 | 20262 | 20764 | 20891 | 20 |  |
| 24 | QUENCH | 701 | 19926 | 20189 | 20558 | 20821 | 20 |  |
| 25 | QUENCH | 701 | 18416 | 18645 | 20583 | 20812 | 100 |  |
| 26 | QUENCH | 601 | 18612 | 18804 |  | 18804 + 3500 | 100 |  |
| 27 | Standard test Splice | 620 | 19235 | 19442 |  |  |  | 1.61 |

Table X. Transformer parameters and splice resistance during Sample 6 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | NO QUENCH | 500 | 16880 | 16950 | 17630 | 15 | 1.484 |
| 2 | NO QUENCH | 629 | 20892 |  |  | 15 | 1.556 |
| 3 | Primary Quench | 670 | - | - | - | - |  |
| 4 | NO QUENCH | 637 | 22226 | 22395 | 22746 | 30 | 1.617 |
| 5 | NO QUENCH | 680 | 24256 | 24790 | 24813 | 40 | 1.612 |
| 6 | Primary Quench | 700 | - | - | - | - |  |
| 7 | QUENCH | 685 | 22579 | 24140 | 23899 | 85 |  |
| 8 | Primary Quench | 680 | - | - | - | - |  |
| 9 | NO QUENCH | 689 | 25051 | 25290 | 25510 | 85 | 1.641 |
| 10 | NO QUENCH | 702 | 25757 | 25491 | 26026 | 100 | 1.620 |
| 11 | QUENCH | 725 | 22857 | 25654 | 25916 | 120 |  |
| 12 | QUENCH | 725 | 22795 |  | 22794+4000 | 120 |  |
| 13 | Primary Quench | 755 | - | - | - | - |  |
| 14 | Primary Quench | 780 | - | - | - | - |  |
| 15 | QUENCH | 729 | 22786 | 26237 | 26304 | 120 |  |
| 16 | Primary Quench | 620 | - | - | - | - |  |
| 17 | QUENCH | 720 | 22791 |  | 22791+4000 | 120 |  |
| 18 | Primary Quench | 725 | - | - | - | - |  |
| 19 | QUENCH | 725 | 22722 | 25092 | 25192 | 120 |  |
| 20 | Primary Quench | 709 | - | - | - | - |  |
| 21 | QUENCH | 720 | 22811 | 26000 | 26016 | 120 |  |
| 22 | Primary Quench | 689 | - | - | - | - |  |
| 23 | QUENCH | 729 | 22797 | 25950 | 25792 | 120 |  |
| 24 | QUENCH | 725 | 23583 | 25182 | 25171 | 90 |  |
| 25 | Primary Quench | 690 | - | - | - | - |  |
| 26 | QUENCH | 725 | 23621 | 25979 | 25720 | 90 |  |
| 27 | Primary Quench | 680 | - | - | - | - |  |

Table XI. Transformer parameters and splice resistance during Sample 7 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Primary Quench | 637 | - | - | - | - |  |
| 2 | NO QUENCH | 676 | 20800 |  |  | 15 |  |
| 3 | Primary Quench | 709 | - | - | - | - |  |
| 4 | Primary Quench | 700 | - | - | - | - |  |
| 5 | NO QUENCH | 695 | 23553 | 23746 | 23864 | 30 | 1.70 |
| 6 | Primary Quench | 700 | - | - | - | - |  |
| 7 | NO QUENCH | 685 | 23808 | 24278 | 24278 | 40 | 1.79 |
| 8 | NO QUENCH | 685 | 23269 | 24330 | 24670 | 80 |  |
| 9 | NO QUENCH | 705 | 25214 | 25122 | 25494 | 70 |  |
| 10 | NO QUENCH | 711 | 25597 | 25828 | 26272 | 100 |  |
| 11 | NO QUENCH | 724 | 26442 | 26601 | 26875 | 120 |  |
| 12 | NO QUENCH | 722 | 26785 | 26895 | 27119 | 180 |  |
| 13 | Primary Quench | 720 | - | - | - | - |  |
| 14 | NO QUENCH | 739 | 27274 | 27419 | 27619 | 184 | 1.90 |
| 15 | QUENCH | 744 | 21544 | 26240 | 26420 | 186 |  |
| 16 | Primary Quench | 670 | - | - | - | - |  |
| 17 | Primary Quench | 710 | - | - | - | - |  |
| 18 | NO QUENCH | 746 | 27498 | 27831 | 27859 | 186 | 1.94 |
| 19 | Primary Quench | 706 | - | - | - | - |  |
| 20 | Primary Quench | 700 | - | - | - | - |  |
| 21 | Primary Quench | 763 | - | - | - | - |  |
| 22 | Low Helium |  | - | - | - | - |  |
| 23 | NO QUENCH | 744 | 27439 | 27660 | 27720 | 186 |  |
|  | QUENCH |  | 27008 | 26811 | 26871 | 186 |  |
| 24 | Primary Quench | 700 | - | - | - | - |  |
| 25 | Primary Quench | 710 | - | - | - | - |  |
| 26 | NO QUENCH | 708 | 25454 | 25900 | 26007 | 100 |  |
| 27 | Primary Quench | 722 | - | - | - | - |  |
| 28 | Primary Quench | 725 | - | - | - | - |  |
| 29 | NO QUENCH | 716 | 25922 | 26070 | 26238 | 102 |  |
| 30 | NO QUENCH | 746 | 27402 | 27630 | 27771 | 186 |  |
|  | QUENCH |  | 27402 | 27000 | 27141 | 186 |  |
| 31 | Primary Quench | 710 | - | - | - | - |  |
| 32 | Primary Quench | 702 | - | - | - | - |  |
| 33 | Primary Quench | 746 | - | - | - | - |  |
| 34 | NO QUENCH | 722 | 26543 | 26934 | 26876 | 120 |  |
| 35 | Primary Quench | 744 | - | - | - | - |  |
| 36 | Primary Quench | 728 | - | - | - | - |  |
| 37 | NO QUENCH | 745 | 27185 | 27228 | 27510 | 186 |  |
|  | QUENCH |  | 26031 | 25720 | 26004 | 186 |  |
| 38 | NO QUENCH | 700 | 24741 | 24646 | 25073 | 100 | 1.77 |

Table XII. Transformer parameters and splice resistance during Sample 8 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 626 | 10294 | 11180 | 10879 | 15 |  |
| 2 | QUENCH | 352 | 11591 | 12267 | 12536 | 15 |  |
| 3 | NO QUENCH | 333 | 12649 |  |  |  | 1.353 |
| 4 | NO QUENCH | 372 | 13491 |  |  |  | 1.596 |
| 5 | QUENCH | 457 | 14610 | 14938 | 15093 | 15 |  |
| 6 | NO QUENCH | 432 | 15426 |  |  |  | 1.536 |
| 7 | QUENCH | 512 | 15961 | 16270 | 16594 | 15 |  |
| 8 | QUENCH | 533 | 16446 | 16900 | 17208 | 15 |  |
| 9 | QUENCH | 543 | 15931 | 16600 | 17008 | 15 |  |
| 10 | QUENCH | 516 | 15999 | 16490 | 16690 | 15 |  |
| 11 | QUENCH | 511 | 16054 | 16490 | 16715 | 15 |  |
| 12 | QUENCH | 577 | 16977 | 17681 | 18050 | 15 |  |
| 13 | NO QUENCH | 436 | 15475 |  |  |  | 1.533 |
| 14 | QUENCH | 526 | 13996 |  |  | 5 |  |
| 15 | QUENCH | 589 | 14819 | 14624 | 15144 | 5 |  |
| 16 | Primary Quench | 630 | - | - | - | - |  |
| 17 | QUENCH | 626 | 15150 | 15250 | 15382 | 5 |  |
| 18 | QUENCH | 647 | 15528 | 15208 | 15727 | 5 |  |
| 19 | QUENCH | 560 | 16472 | 17190 | 17495 | 15 |  |
| 20 | QUENCH | 571 | 12808 | 14255 | 14561 | 30 |  |
| 21 | QUENCH | 563 | 10551 | 12332 | 12687 | 30 |  |
| 22 | QUENCH | 473 | 13976 | 16545 | 16746 | 50 |  |
| 23 | QUENCH | 541 | 15853 |  |  | 50 |  |
| 24 | QUENCH | 525 | 13930 | 17707 | 17887 | 50 |  |
| 25 | QUENCH | 561 | 16181 | 18181 | 18357 | 80 |  |
| 26 | QUENCH | 582 | 16028 | 18500 | 18752 | 80 |  |
| 27 | QUENCH | 520 | 15059 | 18500 | 18749 | 120 |  |
| 28 | QUENCH | 527 | 14870 | 18028 | 18200 | 120 |  |
| 29 | QUENCH | 580 | 14537 | 18700 | 18862 | 120 |  |
| 30 | QUENCH | 600 | 17405 | 17789 | 18148 | 15 |  |
| 31 | QUENCH | 513 | 16062 | 16632 | 16952 | 15 |  |
| 32 | QUENCH | 525 | 16380 | 18083 | 18307 | 30 |  |
| 33 | QUENCH | 451 | 13659 |  |  | 15 |  |
| 34 | NO QUENCH | 431 | 14629 |  |  |  | 1.501 |

Table XIII. Transformer parameters and splice resistance during Sample 8a test run.

| Test No. | EVENT | I1, A | I2,A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splice nL2=0.23H |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 722 | 13032 | 13135 |  | 13135 + 500 | 15 |  |
| 2 | QUENCH | 427 | 13577 | 13634 | 14500 | 14557 | 15 |  |
| 3 | QUENCH | 473 | 12877 | 12760 | 13660 | 13543 | 15 |  |
| 4 | QUENCH | 551 | 12890 | 12749 | 13630 | 13489 | 15 |  |
| 5 | QUENCH | 465 | 12248 | 12782 | 12900 | 13433 | 15 |  |
| 6 | QUENCH | 545 | 13616 | 13671 | 14285 | 14340 | 15 |  |
| 7 | QUENCH | 481 | 12819 | 12819 | 13580 | 13580 | 15 |  |
| 8 | Standard test Splice | 317 | 10738 | 10890 |  |  |  | 1.21 |
| 9 | QUENCH | 512 | 12815 | 12815 | 13430 | 13430 | 10 |  |
| 10 | QUENCH | 555 | 12732 | 13010 | 13260 | 13537 | 10 |  |
| 11 | QUENCH | 472 | 11276 | 11085 | 13490 | 13299 | 30 |  |
| 12 | QUENCH | 460 | 11044 | 11010 | 13000 | 12965 | 30 | 1.44 |
| 13 | QUENCH | 421 | 9232 | 8968 | 13050 | 12787 | 60 |  |
| 14 | QUENCH | 436 | 12813 | 12868 |  | 12868 + 350 | 10 |  |
| 15 | QUENCH | 512 | 12871 | 13059 | 13557 | 13745 | 10 |  |
| 16 | QUENCH | 504 | 7436 | 7601 | 12645 | 12810 | 100 |  |
| 17 | QUENCH | 466 | 12728 | 12785 | 13320 | 13377 | 15 |  |
| 18 | Standard test Splice | 320 | 10626 | 10825 |  |  |  | 1.19 |

Table XIV. Transformer parameters and splice resistance during Sample 9 test run.

| Test No. | EVENT | I1, A | I2,A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splice nL2=0.23H |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 662 | 13376 | 12720 | 14500 | 13844 | 15 |  |
| 2 | QUENCH | 424 | 13012 | 12944 | 14000 | 13932 | 15 |  |
| 3 | QUENCH | 437 | 12759 | 12411 | 13700 | 13352 | 15 | 1.57 |
| 4 | Primary or Secondary Quench | 400 | 9326 |  |  |  | 15 |  |
| 5 | NO Quench | 378 | 13800 | 13973 |  |  | 15 | 1.77 |
| 6 | QUENCH | 444 | 12836 | 12863 |  | 12863 + 650 | 15 |  |
| 7 | QUENCH | 423 | 13968 | 13777 | 14770 | 14579 | 15 |  |
| 8 | QUENCH | 405 | 13525 | 13340 | 14540 | 14355 | 15 |  |
| 9 | QUENCH | 422 | 13186 | 13048 | 14200 | 14062 | 15 |  |
| 10 | QUENCH | 406 | 13535 | 13389 | 14470 | 14324 | 15 |  |
| 11 | QUENCH | 408 | 13115 | 12999 | 14050 | 13934 | 15 |  |
| 12 | QUENCH | 416 | 13039 | 12880 | 13840 | 13681 | 15 |  |
| 13 | Primary or Secondary Quench | 309 | 11450 |  |  |  |  |  |
| 14 | QUENCH | 423 | 12201 | 12340 | 12970 | 13109 | 15 | 1.52 |
| 15 | QUENCH | 426 | 11870 | 11874 | 13740 | 13744 | 30 |  |
| 16 | QUENCH | 434 | 12952 | 12913 | 14855 | 14817 | 30 |  |
| 17 | QUENCH | 453 | 12658 | 12114 | 16190 | 15646 | 60 |  |
| 18 | QUENCH | 435 | 12017 | 11934 | 15700 | 15618 | 60 |  |
| 19 | Primary or Secondary Quench | 423 | 9643 |  |  |  |  |  |
| 20 | QUENCH | 423 | 12259 | 12094 | 14500 | 14335 | 100 |  |
| 21 | QUENCH | 402 | 12037 | 12037 | 15240 | 15240 | 100 |  |
| 22 | QUENCH | 443 | 12439 | 12482 | 13190 | 13234 | 15 |  |
| 23 | Primary or Secondary Quench | 316 | 10498 |  |  |  |  |  |
| 24 | QUENCH | 487 | 13301 | 13411 | 14145 | 14254 | 15 | 1.54 |

Table XV. Transformer parameters and splice resistance during Sample 10 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 650 | 6796 |  | 6796 + 600 | 15 |  |
| 2 | QUENCH | 414 | 6637 | 7343 | 7467 | 15 |  |
| 3 | QUENCH | 245 | 6844 | 7415 | 7483 | 15 |  |
| 4 | NO QUENCH | 202 | 6875 |  |  |  | 1.679 |
| 5 | NO QUENCH | 227 | 6811 |  |  |  |  |
| 6 | QUENCH | 235 | 6827 | 7478 | 7531 | 15 |  |
| 7 | NO QUENCH | 221 | 7116 |  |  | 15 | 1.955 |
| 8 | QUENCH | 270 | 6822 | 7367 | 7502 | 15 |  |
| 9 | QUENCH | 311 | 6979 | 7060 | 7263 | 5 |  |
| 10 | NO QUENCH | 341 | 6096 |  |  | 2 |  |
| 11 | NO QUENCH | 450 | 6696 |  |  | 2 |  |
| 12 | QUENCH | 390 | 6901 |  | 6901+200 | 5 |  |
| 13 | QUENCH | 320 | 6826 | 6850 | 7142 | 5 |  |
| 14 | QUENCH | 311 | 6774 | 6780 | 7098 | 5 |  |

Table XVI. Transformer parameters and splice resistance during Sample 11 test run.

| Test No. | EVENT | I1, A | I2 drift, A | I2 Fast DAQ, A | I2 Fast DAQ drift, A | I1 ramp rate, A/s | R Splices, n |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | QUENCH | 482 | 7302 | 8082 | 8255 | 15 |  |
| 2 | QUENCH | 305 | 7362 | 8272 | 8443 | 15 |  |
| 3 | QUENCH | 332 | 7891 | 8520 | 8642 | 15 |  |
| 4 | QUENCH | 256 | 7317 | 8180 | 8274 | 15 |  |
| 5 | NO QUENCH | 230 | 7430 |  |  |  | 1.364 |
| 6 | QUENCH | 287 | 7365 |  |  | 15 |  |
| 7 | QUENCH | 257 | 7349 | 8090 | 8220 | 15 |  |
| 8 | QUENCH | 259 | 7841 | 8512 | 8648 | 15 |  |
| 9 | QUENCH | 242 | 7863 | 8447 | 8576 | 15 |  |
| 10 | QUENCH | 257 | 7313 | 8260 | 8396 | 15 |  |
| 11 | QUENCH | 241 | 7854 | 8709 | 8844 | 15 |  |
| 12 | QUENCH | 321 | 8804 | 9200 | 9101 | 5 |  |
| 13 | QUENCH | 335 | 9232 | 9340 | 9521 | 5 |  |
| 14 | QUENCH | 326 | 8768 | 8800 | 9031 | 5 |  |
| 15 | QUENCH | 306 | 5721 | 7470 | 7611 | 30 |  |
| 16 | QUENCH | 362 | 5766 | 7617 | 7567 | 30 |  |
| 17 | File Not Saved |  |  | 7499 |  |  |  |
| 18 | QUENCH | 302 | 5694 | 7665 | 7794 | 30 |  |
| 19 | QUENCH | 251 | 4680 | 7300 | 7407 | 60 |  |
| 20 | QUENCH | 288 | 4462 | 7330 | 7420 | 60 |  |
| 21 | QUENCH | 247 | 4566 | 7800 | 7640 | 120 |  |
| 22 | QUENCH | 256 | 4629 | 7317 | 7343 | 120 |  |
| 23 | QUENCH | 252 | 7173 | 8168 | 8203 | 15 |  |
| 24 | QUENCH | 347 | 8695 | 8855 | 9004 | 5 |  |
| 25 | NO QUENCH | 212 | 7408 |  |  |  | 1.365 |

Fig. 15.  Test results for Sample 1.

Fig. 16.  Test results for Sample 2. Closed markers denote reaching maximum current without quenching, open markers represent quenches.

Fig. 17.  Test results for Sample 3.

Fig. 18.  Test results for Sample 4.

Fig. 19.  Test results for Sample 5.

Fig. 20.  Test results for Sample 5a. Closed markers represent quenches, open markers denote reaching maximum current without quenching.

Fig. 21.  Test results for Sample 6. Closed markers represent quenches, open markers denote reaching maximum current without quenching.

Fig. 22.  Test results for Sample 7. Open markers represent quenches, closed markers denote reaching maximum current without quenching.

Fig. 23.  Test results for Sample 8.

Fig. 24.  Test results for Sample 8a.

Fig. 25.  Test results for Sample 9.

Fig. 26.  Test results for Sample 10.

Fig. 27.  Test results for Sample 11.

Fig. 28.  Voltage signal pattern for Sample 2/ Test 13. Bottom is a close-up.

Fig. 29.  Voltage signal pattern for Sample 2/ Test 14. Bottom is a close-up.

Fig. 30.  Voltage signal pattern for Sample 2/ Test 17. Bottom is a close-up.

Fig. 31.  Voltage signal pattern for Sample 2/ Test 23. Bottom is a close-up.

Fig. 32.  Voltage signal pattern for Sample 3/ Test 10.

Fig. 33.  Voltage signal pattern for Sample 3/ Test 16. Bottom is a close-up.

Fig. 34.  Voltage signal pattern for Sample 4/ Test 8.

Fig. 35.  Voltage signal pattern for Sample 4/ Test 9.

Fig. 36.  Voltage signal pattern for Sample 5a/ Test 18.

Fig. 37.  Voltage signal pattern for Sample 5a/ Test 22.

Fig. 38.  Voltage signal pattern for Sample 6/ Test 7.

Fig. 39.  Voltage signal pattern for Sample 6/ Test 15.

Fig. 40.  Voltage signal pattern for Sample 6/ Test 23.

Fig. 41.  Voltage signal pattern for Sample 7/ Test 23.

Fig. 42.  Voltage signal pattern for Sample 7/ Test 30.

Fig. 43.  Voltage signal pattern for Sample 8/ Test 1.

Fig. 44.  Voltage signal pattern for Sample 8/ Test 10.

Fig. 45.  Voltage signal pattern for Sample 8a/ Test 11.

Fig. 46.  Voltage signal pattern for Sample 8a/ Test 12.

Fig. 47.  Voltage signal pattern for Sample 9/ Test 17.

Fig. 48.  Voltage signal pattern for Sample 9/ Test 18.

Fig. 49.  Voltage signal pattern for Sample 10/ Test 8.

Fig. 50.  Voltage signal pattern for Sample 10/ Test 14.

Fig. 51.  Voltage signal pattern for Sample 11/ Test 1.

Fig. 52.  Voltage signal pattern for Sample 11/ Test 7.

Fig. 53.  Voltage signal pattern for Sample 11/ Test 15.

REFERENCES

[1]	N. Andreev et al.,	“An Upgraded SC Transformer to Test Rutherford Cables at Self-field”, FNAL TD-04-012.

[2]	D. Turrioni, “A Fast DAQ Solution for Transformer Tests at the SSTF”, FNAL TD-04-011.

[3]	B. Bordini et al., “SR01 Test Summary Report”, FNAL TD-04-035.

[4]	G. Ambrosio et al., “Test of Cables made of 1 mm OST-MJR Strand at BNL”, FNAL TD-04-008.

[5] 	S. Fehers et al., “HFDA-03B Test Summary”, FNAL TD-03-040, Aug. 27, 2003.

[6]	S. Fehers et al., “HFDA-04 Test Summary”, FNAL TD-02-045, Aug. 2, 2002.

[7]	G. Ambrosio et al., “Fabrication and Test of a Racetrack Magnet using Pre-reacted Nb3Sn Cable”, 2002 Applied Superconductivity Conference, IEEE Transactions on Applied Superconductivity, V. 13, No. 2, June 2003, p. 1284.

[8]	G. Ambrosio et al., “Design Modifications, Fabrication and Test of HFDB-03 Racetrack Magnet Wound with Pre-Reacted Nb3Sn Rutherford Cable”, submitted to the Cryogenic Engineering and International Cryogenic Materials Conference, Sept. 22-25, 2003, Alaska, for publication on Advances in Cryogenic Engineering.

# Text boxes

SAMPLE 3

TEST 10

I2 quench = 14,805 A

dt = 0.1 ms

Amplification = 100

I2 quench = 26,600 A

dt = 0.166 ms

Amplification = 100

SAMPLE 2

TEST 13

I2 quench =  20,384 A

dt = 0.166 ms

Amplification = 100

SAMPLE 2

TEST 14

I2 quench = 19,370 A

dt = 0.166 ms

Amplification = 100

SAMPLE 2

TEST 17

I2 quench = 25,627 A

dt = 0.166 ms

Amplification = 100

SAMPLE 2

TEST 23

I2 quench = 15,828 A

dt =  40 (s

Amplification = 100

SAMPLE 3

TEST 16

I2 quench = 10,042 A

dt = 0.05 ms

Amplification = 100

SAMPLE 4

TEST 8

I2 quench = 11,157 A

dt = 0.05 ms

Amplification = 100

SAMPLE 4

TEST 9

SAMPLE 6

TEST 7

I2 quench = 23,899 A

dt = 0.1 ms

Amplification = 100

SAMPLE 6

TEST 15

I2 quench = 26,304 A

dt = 0.066 ms

Amplification = 100

SAMPLE 6

TEST 23

I2 quench = 25,792 A

dt = 0.05 ms

Amplification = 100

I2 quench = 26,870 A

dt = 0.33 ms

Amplification = 100

SAMPLE 7

TEST 23

I2 quench = 27,140 A

dt = 0.33 ms

Amplification = 100

SAMPLE 7

TEST 30

I2 quench = 10,879 A

dt = 0.05ms

Amplification = 100

SAMPLE 8

TEST 1

I2 quench = 16,690 A

dt = 0.05ms

Amplification = 100

SAMPLE 8

TEST 10

I2 quench = 15,645 A

dt = 0.05 ms

Amplification = 10

SAMPLE 9

TEST 17

I2 quench = 15,620 A

dt = 0.05 ms

Amplification = 10

SAMPLE 9

TEST 17

I2 quench = 7,502 A

dt = 0.05ms

Amplification = 100

SAMPLE 10

TEST 8

I2 quench = 7,098 A

dt = 0.05ms

Amplification = 100

SAMPLE 10

TEST 14

I2 quench = 13,300 A

dt = 0.05 ms

Amplification = 10

SAMPLE 8a

TEST 11

I2 quench = 12,965 A

dt = 0.05 ms

Amplification = 10

SAMPLE 8a

TEST 12

I2 quench = 21,730 A

dt = 0.05 ms

Amplification = 10

SAMPLE 5a

TEST 18

I2 quench = 22,405 A

dt = 0.05 ms

Amplification = 10

SAMPLE 5a

TEST 22

I2 quench = 8,255 A

dt = 0.05ms

Amplification = 100

SAMPLE 11

TEST 1

I2 quench = 8,220 A

dt = 0.05ms

Amplification = 100

SAMPLE 11

TEST 14

I2 quench = 7,610 A

dt = 0.05ms

Amplification = 100

SAMPLE 11

TEST 15