| CABLE No. | . L3T-B00909 |
| --- | --- |
| MFG. | 11/10/04 |
| OPERATOR: | N.Liggins & H.Higley |

CABLE LOG SHEET

LBNL-SUPERCON-AFRD

SUPERCONDUCTING MAGNET CABLES

BLD 52

Objective :  Manufacture LHC-HGQ-INNER Cable for FNAL Magnet Production

- STRAND INFORMATION -

| MANUFACTURER : | Teledyne |
| --- | --- |
| BILLET #: | 10 billets. See- Strand Map. |
| SPOOL #: | 15 spools |
| COMPOSITION : | NbTi from SSCL/LBNL Inventory |
| STRAND Dia.. NOMINAL : | 0.808mm | INSP. DIA..: | 0.8069 / 0.812mm See Strand Map |
| Cu/SC RATIO NOMINAL : |  | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : |  | DIRECTION : | Right |
| SHARP BEND TEST : |  |
| LENGTH PER SPOOL : | 830 |

NOTES:  Strand diameters and surface finishes are highly varied.  This is the last of the TWC inventory so we did not have much of a selection to choose from.

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | FNAL_5525-MA-344389A LHC IR QUAD magnet outer cable drawing |
| --- | --- |
| No. of STRANDS: | 37 |
| PITCH DIRECTION: | Left | PITCH LENGTH: | 118mm |
| PLANETARY RATIO: | -.57:1 |
| ROLLER ID #: | P25 & P26 | WIDTH: | 15.210 | ANGLE:: | 1.268 |
| MANDREL ID #: | 20 | WIDTH: | 14.780 | THICKNESS:: | 0.770mm |
| LUBRICATION : | 100% 4-BR 1/5d/pitch |
| STRAND TENSION: | 2.6kg. | TURKS HEAD LOAD "SGM": | -100 kg. |
| Nom. THICKNESS: | 1.465 +/- 0.006mm |
| Nom. WIDTH: | 15.40 +/- 0.025mm |
| Nom. ANGLE: | 1.079 +/- 0.05 deg. |

- FINISHED CABLE -

|  | Meters | ANGLE | WIDTH mm | THICK mm |
| --- | --- | --- | --- | --- |
|  | tot. | avg. | avg. | avg. |
| Ref-Gauge Start |  | 0.0032 | 16.0686 | 1.5125 |
| Ref-Gauge End |  | 0.0040 | 16.0684 | 1.5117 |
| Dif. |  | 0.0008 | 0.0002 | 0.0008 |
| BNL Point Sample | 9 | 1.1048 | 15.3967 | 1.4644 |
| BNL Tail Sample | 9 | 1.1180 | 15.4041 | 1.4656 |
| L3T-B00909 | 754m | 1.0972 | 15.3903 | 1.4628 |

| RESIDUAL TWIST/Mtr.: | < 45 deg./m |
| --- | --- |
| ETCH for FILAMENT DAMAGE: |  |

NOTES:  Mechanical stability is poor, probably due to the strand variability.

| 11-09-2004 Cable RunLHC-3-T-B00909 Unit 0 10:40:23 |  |
| --- | --- |
| LHC-HGQ-INNER CME #2 |  |  |  |
|  | POINT | METERS | kPa | ANGLE | WIDTH | THICK |
| Gage Block Start | 1 | 0 | 34,511 | 0.004 | 16.0687 | 1.5124 |
| Gage Block Start | 2 | 0 | 34,511 | 0.004 | 16.0686 | 1.5126 |
| Gage Block Start | 3 | 0 | 34,536 | 0.003 | 16.0686 | 1.5125 |
| Gage Block Start | 4 | 0 | 34,560 | 0.003 | 16.0686 | 1.5128 |
| Gage Block Start | 5 | 0 | 34,560 | 0.003 | 16.0685 | 1.5127 |
| Gage Block Start | 6 | 0 | 34,516 | 0.003 | 16.0686 | 1.5124 |
| Gage Block Start | 7 | 0 | 34,560 | 0.003 | 16.0686 | 1.5126 |
| Gage Block Start | 8 | 0 | 34,560 | 0.003 | 16.0685 | 1.5124 |
| Gage Block Start | 9 | 0 | 34,560 | 0.003 | 16.0687 | 1.5123 |
| Gage Block Start | 10 | 0 | 34,560 | 0.003 | 16.0684 | 1.5125 |
|  |  |  | 34,543 | 0.0032 | 16.0686 | 1.5125 |
| Gage used at NEEW | 11 | 0 | 34,516 | -0.014 | 15.0055 | 1.5032 |
| Gage used at NEEW | 12 | 0 | 34,560 | -0.013 | 15.0053 | 1.503 |
| Gage used at NEEW | 13 | 0 | 34,560 | -0.013 | 15.0051 | 1.503 |
| Gage used at NEEW | 14 | 0 | 34,560 | -0.013 | 15.0051 | 1.5031 |
|  |  |  | 34,549 | -0.0133 | 15.0053 | 1.5031 |
| Gage Block Check | 15 | 0 | 34,511 | 0.001 | 16.0683 | 1.5125 |
| Gage Block Check | 16 | 0 | 34,511 | 0.002 | 16.0687 | 1.5124 |
| Gage Block Check | 17 | 0 | 34,521 | 0.001 | 16.0685 | 1.5127 |
| Gage Block Check | 18 | 0 | 34,550 | 0.002 | 16.0683 | 1.5125 |
| Gage Block Check | 19 | 0 | 34,560 | 0.002 | 16.0685 | 1.5125 |
|  |  |  | 34,531 | 0.0016 | 16.0685 | 1.5125 |
| Start UP | 20 | 1 | 34,487 | 1.107 | 15.4253 | 1.4881 |
| Start UP | 21 | 1.33 | 34,468 | 1.127 | 15.4096 | 1.4876 |
| Start UP | 22 | 2 | 34,463 | 1.101 | 15.4091 | 1.4853 |
| Start UP | 23 | 8 | 34,463 | 1.1 | 15.3869 | 1.4682 |
| Start UP | 24 | 8.33 | 34,473 | 1.092 | 15.4076 | 1.4671 |
| Start UP | 25 | 8.33 | 34,478 | 1.101 | 15.3929 | 1.4687 |
| Start UP | 26 | 19 | 33,980 | 1.117 | 15.384 | 1.4682 |
| Start UP | 27 | 19.67 | 33,989 | 1.112 | 15.3951 | 1.4689 |
| Start UP | 28 | 20 | 34,560 | 1.125 | 15.3914 | 1.4709 |
| Start UP | 29 | 21.33 | 34,526 | 1.101 | 15.3928 | 1.4674 |
| Start UP | 30 | 38 | 34,526 | -0.001 | 16.0674 | 1.5116 |
|  |  |  | 34,401 | 1.0075 | 15.4602 | 1.4775 |
| Gage Check | 31 | 38 | 34,560 | 0 | 16.0677 | 1.5114 |
| Gage Check | 32 | 38 | 34,560 | 0 | 16.0678 | 1.5114 |
|  |  |  | 34,560 | 0.0000 | 16.0678 | 1.5114 |
| BNL Sample Point END | 33 | 39 | 34,511 | 1.114 | 15.4011 | 1.4671 |
| BNL Sample Point END | 34 | 39.33 | 34,511 | 1.117 | 15.4134 | 1.4651 |
| BNL Sample Point END | 35 | 41.33 | 34,511 | 1.103 | 15.3971 | 1.4632 |
| BNL Sample Point END | 36 | 43.67 | 34,507 | 1.09 | 15.3905 | 1.4634 |
| BNL Sample Point END | 37 | 45 | 34,511 | 1.1 | 15.3816 | 1.4632 |
|  |  | 8m | 34,510 | 1.1048 | 15.3967 | 1.4644 |
| L3T-B00909 Point END | 38 | 50 | 34,511 | 1.095 | 15.3863 | 1.4627 |
| L3T-B00909 | 39 | 55 | 34,511 | 1.093 | 15.3851 | 1.4643 |
| L3T-B00909 | 40 | 60 | 34,511 | 1.086 | 15.3795 | 1.4636 |
| L3T-B00909 | 41 | 65 | 34,511 | 1.089 | 15.388 | 1.4639 |
| L3T-B00909 | 42 | 70 | 34,511 | 1.091 | 15.3852 | 1.4645 |
| L3T-B00909 | 43 | 75 | 34,511 | 1.086 | 15.3851 | 1.4646 |
| L3T-B00909 | 44 | 80 | 34,511 | 1.086 | 15.381 | 1.4641 |
| L3T-B00909 | 45 | 85 | 34,511 | 1.08 | 15.3791 | 1.462 |
| L3T-B00909 | 46 | 90 | 34,511 | 1.088 | 15.3846 | 1.4618 |
| L3T-B00909 | 47 | 95 | 34,511 | 1.088 | 15.3824 | 1.4625 |
| L3T-B00909 | 48 | 100 | 34,511 | 1.087 | 15.3907 | 1.4626 |
| L3T-B00909 | 49 | 105 | 34,511 | 1.083 | 15.3838 | 1.4627 |
| L3T-B00909 | 50 | 110 | 34,511 | 1.085 | 15.3859 | 1.4624 |
| L3T-B00909 | 51 | 115 | 34,511 | 1.078 | 15.3897 | 1.4614 |
| L3T-B00909 | 52 | 120 | 34,511 | 1.079 | 15.382 | 1.4611 |
| L3T-B00909 | 53 | 125 | 34,511 | 1.089 | 15.3853 | 1.4619 |
| L3T-B00909 | 54 | 130 | 34,511 | 1.077 | 15.3849 | 1.4619 |
| L3T-B00909 | 55 | 135 | 34,502 | 1.08 | 15.3905 | 1.4635 |
| L3T-B00909 | 56 | 140 | 34,511 | 1.089 | 15.3816 | 1.4629 |
| L3T-B00909 | 57 | 145 | 34,511 | 1.09 | 15.3835 | 1.4625 |
| L3T-B00909 | 58 | 150 | 34,507 | 1.088 | 15.3945 | 1.4632 |
| L3T-B00909 | 59 | 155 | 34,511 | 1.09 | 15.3855 | 1.4621 |
| L3T-B00909 | 60 | 160 | 34,511 | 1.091 | 15.3874 | 1.4611 |
| L3T-B00909 | 61 | 165 | 34,511 | 1.091 | 15.3818 | 1.4616 |
| L3T-B00909 | 62 | 170 | 34,511 | 1.088 | 15.3887 | 1.4616 |
| L3T-B00909 | 63 | 175 | 34,511 | 1.085 | 15.3852 | 1.4616 |
| L3T-B00909 | 64 | 180 | 34,511 | 1.091 | 15.3862 | 1.4632 |
| L3T-B00909 | 65 | 185 | 34,511 | 1.082 | 15.3824 | 1.4611 |
| L3T-B00909 | 66 | 190 | 34,511 | 1.086 | 15.3811 | 1.4609 |
| L3T-B00909 | 67 | 195 | 34,502 | 1.083 | 15.3821 | 1.461 |
| L3T-B00909 | 68 | 200 | 34,492 | 1.084 | 15.3838 | 1.461 |
| L3T-B00909 | 69 | 205 | 34,511 | 1.09 | 15.3836 | 1.4628 |
| L3T-B00909 | 70 | 210 | 34,511 | 1.091 | 15.388 | 1.4624 |
| L3T-B00909 | 71 | 215 | 34,492 | 1.093 | 15.3961 | 1.462 |
| L3T-B00909 | 72 | 220 | 34,511 | 1.093 | 15.3837 | 1.4616 |
| L3T-B00909 | 73 | 225 | 34,497 | 1.092 | 15.3863 | 1.4617 |
| L3T-B00909 | 74 | 230 | 34,511 | 1.102 | 15.3844 | 1.4611 |
| L3T-B00909 | 75 | 235 | 34,511 | 1.095 | 15.3944 | 1.4626 |
| L3T-B00909 | 76 | 240 | 34,511 | 1.088 | 15.3867 | 1.4619 |
| L3T-B00909 | 77 | 245 | 34,473 | 1.091 | 15.3894 | 1.4623 |
| L3T-B00909 | 78 | 250 | 34,492 | 1.089 | 15.3847 | 1.4622 |
| L3T-B00909 | 79 | 255 | 34,502 | 1.095 | 15.3826 | 1.4617 |
| L3T-B00909 | 80 | 260 | 34,492 | 1.094 | 15.3878 | 1.462 |
| L3T-B00909 | 81 | 265 | 34,492 | 1.085 | 15.386 | 1.4621 |
| L3T-B00909 | 82 | 270 | 34,492 | 1.088 | 15.3886 | 1.4625 |
| L3T-B00909 | 83 | 275 | 34,507 | 1.089 | 15.3853 | 1.4622 |
| L3T-B00909 | 84 | 280 | 34,511 | 1.095 | 15.3865 | 1.4628 |
| L3T-B00909 | 85 | 285 | 34,487 | 1.097 | 15.3907 | 1.4636 |
| L3T-B00909 | 86 | 290 | 34,497 | 1.093 | 15.3892 | 1.4641 |
| L3T-B00909 | 87 | 295 | 34,492 | 1.094 | 15.3873 | 1.4634 |
| L3T-B00909 | 88 | 300 | 34,482 | 1.092 | 15.3896 | 1.4628 |
| L3T-B00909 | 89 | 305 | 34,487 | 1.099 | 15.3886 | 1.4615 |
| L3T-B00909 | 90 | 310 | 34,473 | 1.097 | 15.3918 | 1.4624 |
| L3T-B00909 | 91 | 315 | 34,487 | 1.098 | 15.3867 | 1.4623 |
| L3T-B00909 | 92 | 320 | 34,507 | 1.089 | 15.3843 | 1.462 |
| L3T-B00909 | 93 | 325 | 34,507 | 1.092 | 15.3906 | 1.4616 |
| L3T-B00909 | 94 | 330 | 34,497 | 1.084 | 15.3873 | 1.4619 |
| L3T-B00909 | 95 | 335 | 34,507 | 1.085 | 15.3926 | 1.4624 |
| L3T-B00909 | 96 | 340 | 34,478 | 1.096 | 15.3908 | 1.463 |
| L3T-B00909 | 97 | 345 | 34,482 | 1.086 | 15.3887 | 1.4628 |
| L3T-B00909 | 98 | 350 | 34,468 | 1.091 | 15.3874 | 1.463 |
| L3T-B00909 | 99 | 355 | 34,507 | 1.096 | 15.3811 | 1.4634 |
| L3T-B00909 | 100 | 360 | 34,482 | 1.094 | 15.3961 | 1.4633 |
| L3T-B00909 | 101 | 365 | 34,468 | 1.103 | 15.3963 | 1.4632 |
| L3T-B00909 | 102 | 370 | 34,468 | 1.103 | 15.3889 | 1.4634 |
| L3T-B00909 | 103 | 375 | 34,468 | 1.099 | 15.3887 | 1.4632 |
| L3T-B00909 | 104 | 380 | 34,502 | 1.104 | 15.3919 | 1.4629 |
| L3T-B00909 | 105 | 385 | 34,502 | 1.098 | 15.3889 | 1.4612 |
| L3T-B00909 | 106 | 390 | 34,492 | 1.095 | 15.3891 | 1.4607 |
| L3T-B00909 | 107 | 395 | 34,492 | 1.096 | 15.3875 | 1.4617 |
| L3T-B00909 | 108 | 400 | 34,507 | 1.089 | 15.3804 | 1.4625 |
| L3T-B00909 | 109 | 405 | 34,497 | 1.089 | 15.3852 | 1.4625 |
| L3T-B00909 | 110 | 410 | 34,473 | 1.087 | 15.3891 | 1.4617 |
| L3T-B00909 | 111 | 415 | 34,502 | 1.086 | 15.3889 | 1.4627 |
| L3T-B00909 | 112 | 420 | 34,487 | 1.09 | 15.3945 | 1.4628 |
| L3T-B00909 | 113 | 425 | 34,482 | 1.092 | 15.3867 | 1.4633 |
| L3T-B00909 | 114 | 430 | 34,463 | 1.098 | 15.3901 | 1.4627 |
| L3T-B00909 | 115 | 435 | 34,492 | 1.099 | 15.3896 | 1.4627 |
| L3T-B00909 | 116 | 440 | 34,487 | 1.098 | 15.394 | 1.4641 |
| L3T-B00909 | 117 | 445 | 34,468 | 1.106 | 15.3913 | 1.4628 |
| L3T-B00909 | 118 | 450 | 34,468 | 1.111 | 15.387 | 1.4629 |
| L3T-B00909 | 119 | 455 | 34,468 | 1.103 | 15.3817 | 1.4626 |
| L3T-B00909 | 120 | 460 | 34,468 | 1.094 | 15.3846 | 1.4623 |
| L3T-B00909 | 121 | 465 | 34,478 | 1.098 | 15.3879 | 1.4622 |
| L3T-B00909 | 122 | 470 | 34,482 | 1.096 | 15.3874 | 1.4606 |
| L3T-B00909 | 123 | 475 | 34,468 | 1.092 | 15.3849 | 1.4618 |
| L3T-B00909 | 124 | 480 | 34,478 | 1.085 | 15.3813 | 1.4628 |
| L3T-B00909 | 125 | 485 | 34,473 | 1.091 | 15.3859 | 1.4632 |
| L3T-B00909 | 126 | 490 | 34,482 | 1.095 | 15.3854 | 1.4624 |
| L3T-B00909 | 127 | 495 | 34,482 | 1.092 | 15.3951 | 1.4618 |
| L3T-B00909 | 128 | 500 | 34,502 | 1.09 | 15.3998 | 1.4612 |
| L3T-B00909 | 129 | 505 | 34,473 | 1.095 | 15.395 | 1.4619 |
| L3T-B00909 | 130 | 510 | 34,482 | 1.097 | 15.3914 | 1.4624 |
| L3T-B00909 | 131 | 515 | 34,478 | 1.107 | 15.3853 | 1.4634 |
| L3T-B00909 | 132 | 520 | 34,473 | 1.099 | 15.3952 | 1.4624 |
| L3T-B00909 | 133 | 525 | 34,463 | 1.103 | 15.393 | 1.4631 |
| L3T-B00909 | 134 | 530 | 34,487 | 1.107 | 15.4005 | 1.4628 |
| L3T-B00909 | 135 | 535 | 34,482 | 1.104 | 15.3976 | 1.4627 |
| L3T-B00909 | 136 | 540 | 34,492 | 1.107 | 15.3833 | 1.4626 |
| L3T-B00909 | 137 | 545 | 34,473 | 1.099 | 15.396 | 1.4612 |
| L3T-B00909 | 138 | 550 | 34,468 | 1.089 | 15.3947 | 1.4604 |
| L3T-B00909 | 139 | 555 | 34,497 | 1.1 | 15.3895 | 1.4614 |
| L3T-B00909 | 140 | 560 | 34,468 | 1.095 | 15.3831 | 1.4629 |
| L3T-B00909 | 141 | 565 | 34,473 | 1.102 | 15.3935 | 1.4637 |
| L3T-B00909 | 142 | 570 | 34,492 | 1.098 | 15.3921 | 1.4639 |
| L3T-B00909 | 143 | 575 | 34,492 | 1.095 | 15.3973 | 1.4634 |
| L3T-B00909 | 144 | 580 | 34,468 | 1.099 | 15.3888 | 1.4625 |
| L3T-B00909 | 145 | 585 | 34,468 | 1.1 | 15.3874 | 1.4615 |
| L3T-B00909 | 146 | 590 | 34,482 | 1.108 | 15.3881 | 1.463 |
| L3T-B00909 | 147 | 595 | 34,482 | 1.114 | 15.4076 | 1.4647 |
| L3T-B00909 | 148 | 600 | 34,468 | 1.107 | 15.3979 | 1.4639 |
| L3T-B00909 | 149 | 605 | 34,468 | 1.108 | 15.3967 | 1.4651 |
| L3T-B00909 | 150 | 610 | 34,478 | 1.112 | 15.3969 | 1.4643 |
| L3T-B00909 | 151 | 615 | 34,468 | 1.113 | 15.3972 | 1.4645 |
| L3T-B00909 | 152 | 620 | 34,463 | 1.113 | 15.4017 | 1.4647 |
| L3T-B00909 | 153 | 625 | 34,463 | 1.107 | 15.3941 | 1.464 |
| L3T-B00909 | 154 | 630 | 34,478 | 1.112 | 15.3938 | 1.4633 |
| L3T-B00909 | 155 | 635 | 34,473 | 1.105 | 15.3897 | 1.4634 |
| L3T-B00909 | 156 | 640 | 34,473 | 1.1 | 15.3924 | 1.4631 |
| L3T-B00909 | 157 | 645 | 34,487 | 1.107 | 15.3886 | 1.4648 |
| L3T-B00909 | 158 | 650 | 34,487 | 1.096 | 15.3902 | 1.4643 |
| L3T-B00909 | 159 | 655 | 34,507 | 1.099 | 15.383 | 1.4641 |
| L3T-B00909 | 160 | 660 | 34,473 | 1.102 | 15.3994 | 1.4631 |
| L3T-B00909 | 161 | 665 | 34,468 | 1.1 | 15.3931 | 1.4628 |
| L3T-B00909 | 162 | 670 | 34,478 | 1.104 | 15.3864 | 1.4632 |
| L3T-B00909 | 163 | 675 | 34,482 | 1.11 | 15.3981 | 1.4639 |
| L3T-B00909 | 164 | 680 | 34,468 | 1.108 | 15.3948 | 1.4643 |
| L3T-B00909 | 165 | 685 | 34,473 | 1.113 | 15.4005 | 1.4641 |
| L3T-B00909 | 166 | 690 | 34,463 | 1.113 | 15.3991 | 1.4636 |
| L3T-B00909 | 167 | 695 | 34,473 | 1.114 | 15.3988 | 1.4644 |
| L3T-B00909 | 168 | 700 | 34,468 | 1.116 | 15.4037 | 1.4655 |
| L3T-B00909 | 169 | 705 | 34,473 | 1.116 | 15.3952 | 1.4648 |
| L3T-B00909 | 170 | 710 | 34,487 | 1.114 | 15.398 | 1.465 |
| L3T-B00909 | 171 | 715 | 34,468 | 1.11 | 15.3923 | 1.4645 |
| L3T-B00909 | 172 | 720 | 34,463 | 1.107 | 15.4015 | 1.4628 |
| L3T-B00909 | 173 | 725 | 34,468 | 1.122 | 15.3987 | 1.464 |
| L3T-B00909 | 174 | 730 | 34,463 | 1.11 | 15.4041 | 1.4626 |
| L3T-B00909 | 175 | 735 | 34,463 | 1.114 | 15.3983 | 1.4638 |
| L3T-B00909 | 176 | 740 | 34,487 | 1.113 | 15.3961 | 1.4636 |
| L3T-B00909 | 177 | 745 | 34,463 | 1.106 | 15.3952 | 1.4631 |
| L3T-B00909 | 178 | 750 | 34,463 | 1.118 | 15.4048 | 1.465 |
| L3T-B00909 | 179 | 755 | 34,463 | 1.11 | 15.3987 | 1.464 |
| L3T-B00909 | 180 | 760 | 34,482 | 1.115 | 15.3928 | 1.464 |
| L3T-B00909 | 181 | 765 | 34,463 | 1.112 | 15.4041 | 1.4628 |
| L3T-B00909 | 182 | 770 | 34,468 | 1.11 | 15.4068 | 1.4631 |
| L3T-B00909 | 183 | 775 | 34,463 | 1.117 | 15.4028 | 1.4631 |
| L3T-B00909 | 184 | 780 | 34,463 | 1.114 | 15.3933 | 1.4643 |
|  |  | 754m | 34,488 | 1.0972 | 15.3903 | 1.4628 |
| BNL Sample Tail END | 185 | 785 | 34,463 | 1.112 | 15.4027 | 1.4645 |
| BNL Sample Tail END | 186 | 790 | 34,463 | 1.119 | 15.4083 | 1.466 |
| BNL Sample Tail END | 187 | 795 | 34,463 | 1.123 | 15.4013 | 1.4663 |
|  |  | 9m | 34,463 | 1.1180 | 15.4041 | 1.4656 |
| Gage Block END | 188 | 798.33 | 34,463 | 0.004 | 16.0686 | 1.5117 |
| Gage Block END | 189 | 798.33 | 34,507 | 0.004 | 16.0684 | 1.5114 |
| Gage Block END | 190 | 798.33 | 34,468 | 0.004 | 16.0686 | 1.5115 |
| Gage Block END | 191 | 798.33 | 34,502 | 0.004 | 16.0682 | 1.5119 |
| Gage Block END | 192 | 798.33 | 34,511 | 0.004 | 16.0681 | 1.5118 |
|  |  |  | 34,490 | 0.0040 | 16.0684 | 1.5117 |