MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A05480 | In-Flight Anomaly Number -- | Contractor Report Number S-058 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title FWD OGIVE WELDING UNACCEPTABLE |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A B (X) C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE EXTERNAL TANK | PART# 82601000000 | SER/LOT# LWT-4 | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE FWD OGIVE WELD ASSY | PART# 80912100000-009 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation M - MFG | Prevailing Condtion -- | F / U UC | Fail Mode -- | Cause -- |
| System STRUCTURAL | Defect DE - WLDBRS | Material -- | Work Contact C. VOGEL | Fail Date 07/21/1982 |
| Received at MSFC 09/22/1982 | Date Isolated -- | FMEA Reference 1.1.3 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom -- | Time Cycle -- |
| Effectivity Text LWT5 AND SUBS |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 10/07/1987 | CN RSLV SBMT 04/27/1983 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design J. NICHOLS | Chief Engineer -- | S & MA D. NEWMAN | Project M. PESSIN | Project MGR -- |
| Approval |
| Design J. NICHOLS | Chief Engineer -- | S & MA D. NEWMAN | Project M. PESSIN | Project MGR -- |
| PAC Assignee M. GLASS | PAC Review Complete MG | MSFC Closure Date 06/10/1983 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: (A) LWT FWD OGIVE WELD (0-1) COMPARED TO SAME WELD HWT EXHIBITS SIGNIFICANT INCREASE IN WELD DEFECTSREQ'G REPAIR. THESE DEFECTS ARE CHARACTERIZED BY POROSITY & OXIDE INCLUSIONS. THIS RESULTS IN INCRASED REPAIR TIME WITH SOME REPAIRS REQ'G MULTIPLE HEATS. (B) PEAKING & MISMATCH OVER A MAJOR PORTION OF THE O-1 WELD HAVE OCCURRED ON LWT-5 & FORWARD OGIVES.LWT-6 HAD AVG'D 8.4 DEGS INVERTED PEAKING OVER 80% OF THE AREA BEFORE ANY HEAT REPAIRS WITH A MAX. OF 11 DEGS PEAKING |
| Contractor Investigation/Resolution 4/27/83 CAUSE - A) NO SPECIFIC ITEM COULD BE ISOLATED FOR THE INCREASED WELD DEFECTS SEEN BETWEEN LWT & HWT 0-1 WELDS. LWT-5 WHICH WAS THE WORST IS CONSIDERED AN ISOLATED CASE. THE 0-1 WELD IS PERFORMED THE HORIZONTAL POSITION WHICH WILL MAKE ENTRAPMENT OF DEFECTS MORE LIKELY THAN THE NORMAL VERTICAL ORIENTATION. B) THE SEVERE PEAKING MEASURED ON THE 0-1 WELD ON LWT-6 WAS THE RESULT OF TOOLING (ALSO OBSERVED ON LWT-5 BUT WAS DOCUMENTED AFTER MULTIPLE HEAT REPAIRS). THE ACTIVATION PRESS APPLIED TO THE EX- TERNAL FINGERS MANDREL WAS GREAT ENOUGH TO CAUSE THE GORE PANELS TO FLEX IN THAT AREA WITH THE CHILL BAR OFF-SET FROM THE MANDREL CONTACT LINE. 4/27/83 RESOLUTION - A) WELD DEFECTS SEEN IN THE 0-1 WELD ARE ENTRAPPED BECAUSE OF THE HORIZONTAL WELD POSITION IN WHICH THE WELD IS MADE. THE SPECIFIC SOURCE(S) OF THE DEFECTS IS INDETERMINABLE, HOWEVER THE QUANTITY OF DEFECTS HAVE BEEN REDUCED BY INCORP'D A 4TH WELD PASS & ARE IN THE RANGE OF WHAT WAS REPORTED DURING HWT WELDING. B) PEAKING WAS CAUSED BY HAVING UNCONTROLLED LINE PRESS APPLIED TO THE EXTERNAL FINGERS MANDREL WHICH FLEXED THE FORWARD OGIVE GORE PANELS RADIALLY INWARD. C/A INCORP'D A REGULATING VALVE FOR REDUCED PRESSURES. A CAM ACTIVATED BACK-UP CHILL BAR IS SCHEDULED FOR LWT-16 EFFECTIVITY WHICH WILL PROVIDE ADDITIONAL CONTROL. THIS REGULATOR VALVE CHANGE HAS RESULTED IN CONTROLLING PEAKING TO AN AVG OF 3 DEGS. THE SPEC REQ'S 6.5 DEGS. LWT-5 DISPOSITIONED BY MARS T-54381 LWT-6 REPAIRED PER STD PROCEDURES. LWT-7 & SUBS WILL HAVE INCORP'D C.A FOR PEAKING. LWT-6 & SUBS WILL HAVE ADDITIONAL WELD PASS. LWT-16 & SUBS WILL BE BUILT ON TOOLING WITH CAM ACTUATED MANDREL. 4/28/83 - CLOSURE DISTRIBUTED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A05480 | IFA# -- | Contractor RPT# S-058 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# -- | Asmnt Part Name -- | Asmnt Serial/Lot# -- |
| HCRIT CD -- | FCRIT CD -- | CAUSE CD -- | FAIL MODE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |