## Specifications for RFQ 1-025-RGB.1234

## Title: MEMS Actuator and Sensor Fabrication and Characterization

Description: Design, Fabrication, and Characterization of MEMS Silicon Beam Shear Stress Sensors and Piezoelectric MEMS Actuators

Completion Date: Within 18 Weeks from the date of contract

## Sensors: MEMS Silicon Beam Shear Stress Sensors

Quantity:  Minimum of 20 units of each length (160 total minimum)

Specifications:

- Micro-machined silicon beams electrically insulated from the silicon substrate of 3mm x 5 mm. Sketches of the sensor and specifications are given in Figures 1 and 2, of MS PowerPoint File: “Si-Beams-Diagrams.ppt”

- Dimensions of the sensor beams are shown in the Table I

- The top surface of the silicon beam is in plane with the upper surface of the device

- Beam resistances are equal to or less than 10k Ohms, 1k Ohm preferred.

- Electrical isolation of the beams is achieved by etching the top-level silicon layer surrounding the beam from the Si-SiO2-Si or other substrate structure

- Electrical contact pads are 250 micron square

- The electrical contact pads of the beams are positioned as far away as possible from the beam

- Two (2) electrical contact pads for the top and bottom silicon substrate are required

- Characterization includes measurements of resistance values and average beam dimensions

# Table I

| Die Type | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Length (micron) | 300 | 400 | 500 | 600 | 700 | 400 | 500 | 600 |
| Width (micron) | 1 | 1 | 1 | 1 | 1 | 0.75 | 0.75 | 0.75 |
| ~Thickness (micron) | 0.186 | 0.186 | 0.186 | 0.186 | 0.186 | 0.186 | 0.186 | 0.186 |
| Gap size (micron) | 1.072 | 1.226 | 1.553 | 2.146 | 3.123 | 1.402 | 1.983 | 3.037 |

Actuators: Piezoelectric MEMS Actuators (PZT based)

Quantity:     Total: 66 Minimum

- Pattern A: Minimum 9 units per diaphragm thickness

- Pattern B: Minimum 3 units per diaphragm thickness

- Pattern C: Minimum 3 units per diaphragm thickness

- Pattern D: Minimum 3 units per diaphragm thickness

- Pattern E: Minimum 6 units per diaphragm thickness

- Pattern F: Minimum 9 units per diaphragm thickness

Specifications:

- Four actuating diaphragm sizes are 1mm, 2mm, 2.83mm, and 4mm square for, diaphragms are rigidly fixed at the four edges

- Actuator displacements perpendicular to the diaphragm plane at 40 Volts input are:

  - 20 microns for 1mm square membrane

  - 60 microns for 2 mm square membrane

  - 100 microns for 2.83 mm square membrane

  - 140 microns for 4mm square membrane

- Two (2) different diaphragm thickness are requested for each diaphragm size, they are 0.2 and 5 microns

- Sketches of the actuator dice patterns are shown in the attached MS PowerPoint file “MEMS-Actuator-Diagrams.ppt,” which includes Pattern A through F

- Generalized characterizations of the actuation functions are required:

  - Displacements with respect to diaphragm thickness

  - Displacements with respect to applied voltages