| CABLE No. | . LARP-LR-S3O-B0942R |
| --- | --- |
| MFG. | 4/26/2006 |
| OPERATOR: | H.Higley & N.Liggins |
| Rev: | 7/10/2006 H.H. |

CABLE LOG SHEET

LBNL-SUPERCON-AFRD

SUPERCONDUCTING MAGNET CABLES

BLD 52

Objective : Mfg 1 UL LR Cable for Coils to be wound at BNL.

- STRAND INFORMATION -

| MANUFACTURER : | Oxford |
| --- | --- |
| BILLET #: | 8647 |
| SPOOL #: | 8647-1 , 8647-2 |
| COMPOSITION : | RRP Nb3Sn |
| STRAND Dia.. NOMINAL : | 0.700mm | INSP. DIA..: | 0.7042mm avg. |
| Cu/SC RATIO NOMINAL : |  | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : | 13mm | DIRECTION : | Right |
| SHARP BEND TEST : | na |
| LENGTH PER SPOOL : | 375m x 20spl. |

NOTES:

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | LARP LR per. D. Dietderich 4/25/06 |
| --- | --- |
| No. of STRANDS: | 20 |
| PITCH DIRECTION: | LEFT | PITCH LENGTH: | Set @ 53.9 measured 54.5mm |
| PLANETARY RATIO: | -.57:1 |
| ROLLER ID #: | P35 & 36 | WIDTH: | 7.923mm | ANGLE:: | 0 |
| MANDREL ID #: | 4 | WIDTH: | 6.82mm | THICKNESS:: | 0.40mm |
| LUBRICATION : | 4BR Vanishing lube ~ 1d/pitch |
| STRAND TENSION: | 2.0kg. | TURKS HEAD LOAD "SGM": | -70 lbs. |
| CME Face Load: | 17,500 kPa | CME Edge Load: | 20psiG 10&15psiG checked. |
| Nom. THICKNESS: | 1.276mm +/- 0.010mm ( 1.30mm +/- 0.01 Before Anneal & Resize) |
| Nom. WIDTH: | 7.793mm +/- 0.050mm |

- FINISHED CABLE -

|  | 942 | 942 Annealed | S3O-B0942R |
| --- | --- | --- | --- |
| FINISHED LENGTH: |  |  | 353m -~5m sample = 347.2m |
| Avg. THICKNESS: | 1.306mm | 1.328mm | 1.277mm |
| Avg. WIDTH: | 7.855mm | 7.752mm | 7.828mm |

| RESIDUAL TWIST/Mtr.: | <45 deg/m |
| --- | --- |
| ETCH for FILAMENT DAMAGE: |  |

NOTES: This cable was made the annealed & resized with the edge rolls tight meaning that the width aperture in the turkshead was 7.92mm    Width measurement vs. edge load tests were done.  Samples from the point and tail ends of 942R were cut for metallography.  Also  The measuring machine is having difficulty with angle measurements  The cable seems to fluff up a bit depending on width load used this affects the apparent angle.

Note that the rolls and bearing sets in the turkshead are set for 0.000 deg +/- 0.005.  Edge load studies done after discussions with D.Dietderich and Arup Ghosh about measurement repeatability and loading.

Cable was insulated with FII-282 Spool#1/4 PO# 6806116.  Insulation was cleaned and treated @LBNL 6/15/06

Mfg.1,000ft spool was not long enough so a splice in the insulation is at 46.0m from the hub of the spool.

Final length on spool measured at 347.2m with marked splice 301.2m from the top.

S3O-B0942 Strand Map.

| 04-25-2006 Cable RunSUB-3-O-B0942R Unit 0 14:50:32 |  |  |  |
| --- | --- | --- | --- |
| LBNL SUBSIZED TYPE 3 20STX.7MM CME #2 |  |  |  |
| Annealed Cable @ 206.7c Max. Measure Annealed first 5m Then resize to target dim. |  |
|  |  |  | Edge |  |  |  |  |
| Notes: | POINT | METERS | psiG | kPa | ANGLE | WIDTH | THICK |
| Gage Start | 1 | 0 | 20 | 17,260 | 0.001 | 8.0027 | 1.5068 |
| Gage Start | 2 | 0 | 20 | 17,260 | 0.005 | 8.0033 | 1.5067 |
| Gage Start | 3 | 0 | 20 | 17,260 | 0.005 | 8.0032 | 1.5068 |
| Gage Start | 4 | 0 | 20 | 17,285 | 0.006 | 8.0037 | 1.5068 |
| Gage Start | 5 | 0 | 20 | 17,328 | 0.006 | 8.0036 | 1.5069 |
| Notes: | POINT | METERS | Edge psiG | kPa | ANGLE | WIDTH | THICK |
| 942 Annealed ONLY | 6 | 0 | 20 | 17,260 | -0.061 | 7.7397 | 1.3305 |
| 942 Annealed ONLY | 7 | 0.33 | 20 | 17,260 | -0.263 | 7.7557 | 1.3312 |
| 942 Annealed ONLY | 8 | 0.67 | 20 | 17,260 | -0.138 | 7.7579 | 1.3288 |
| 942 Annealed ONLY | 9 | 1 | 20 | 17,260 | 0.067 | 7.7571 | 1.3263 |
| 942 Annealed ONLY | 10 | 1.67 | 20 | 17,260 | 0.056 | 7.7580 | 1.3243 |
| 942 Annealed ONLY | 11 | 2.67 | 20 | 17,260 | 0.060 | 7.7477 | 1.3276 |
| 942 Annealed ONLY | 12 | 3 | 20 | 17,260 | 0.050 | 7.7524 | 1.3275 |
| 942 Annealed ONLY | 13 | 3.67 | 20 | 17,260 | 0.012 | 7.7510 | 1.3283 |
| 942 Annealed ONLY | 14 | 4.33 | 20 | 17,260 | -0.012 | 7.7514 | 1.3278 |
| 942 Annealed ONLY | 15 | 5 | 20 | 17,260 | -0.013 | 7.7557 | 1.3283 |
| 942 Annealed ONLY AVG= |  |  |  | AVG= | -0.024 | 7.7527 | 1.3281 |
| Gage Check | 16 |  | 20 | 17,260 | -0.010 | 8.0029 | 1.5075 |
| Gage Check | 17 |  | 20 | 17,268 | -0.001 | 8.0032 | 1.5074 |
| Gage Check | 18 |  | 20 | 17,319 | 0.001 | 8.0033 | 1.5073 |
| Gage Check | 19 |  | 20 | 17,328 | 0.002 | 8.0036 | 1.5073 |
| Gage Check | 20 |  | 20 | 17,336 | 0.002 | 8.0035 | 1.5075 |
| Start resize S3O-B0942R | 21 | 0 | 20 | 17,260 | -0.139 | 7.8033 | 1.2899 |
| Start resize S3O-B0942R | 22 | 0.33 | 20 | 17,217 | -0.188 | 7.8270 | 1.2900 |
| Start resize S3O-B0942R | 23 | 0.66 | 20 | 17,192 | -0.259 | 7.8153 | 1.2881 |
| Start resize S3O-B0942R | 24 | 1 | 20 | 17,183 | 0.002 | 7.8188 | 1.2793 |
| Start resize S3O-B0942R Met Sample | 25 | 1.33 | 20 | 17,217 | -0.153 | 7.8350 | 1.2839 |
| kPa Adjust S3O-B0942R | 26 | 0 | 20 | 11,138 | -0.137 | 7.8275 | 1.2879 |
| kPa Adjust S3O-B0942R | 27 | 0 | 20 | 11,138 | -0.154 | 7.8248 | 1.2884 |
| kPa Adjust S3O-B0942R | 28 | 0 | 20 | 11,138 | -0.163 | 7.8233 | 1.2884 |
| kPa Adjust S3O-B0942R | 29 | 0 | 20 | 11,138 | -0.174 | 7.8225 | 1.2885 |
| kPa Adjust S3O-B0942R | 30 | 0 | 20 | 11,138 | -0.177 | 7.8214 | 1.2889 |
| kPa Adjust S3O-B0942R | 31 | 0 | 20 | 15,815 | -0.173 | 7.8203 | 1.2856 |
| kPa Adjust S3O-B0942R | 32 | 0 | 20 | 17,447 | -0.173 | 7.8224 | 1.2848 |
| kPa Adjust S3O-B0942R | 33 | 0 | 20 | 17,464 | -0.172 | 7.8188 | 1.2846 |
| kPa Adjust S3O-B0942R | 34 | 0 | 20 | 17,481 | -0.196 | 7.8198 | 1.2855 |
| kPa Adjust S3O-B0942R | 35 | 0 | 20 | 17,506 | -0.203 | 7.8177 | 1.2856 |
| Edge LOAD TEST S3O-B0942R | 36 | 0 | 15 | 17,515 | -0.187 | 7.8202 | 1.2851 |
| Edge LOAD TEST S3O-B0942R | 37 | 0 | 15 | 17,515 | -0.192 | 7.8220 | 1.2851 |
| Edge LOAD TEST S3O-B0942R | 38 | 0 | 15 | 17,515 | -0.186 | 7.8235 | 1.2853 |
| Edge LOAD TEST S3O-B0942R | 39 | 0 | 15 | 17,515 | -0.186 | 7.8213 | 1.2851 |
| Edge LOAD TEST S3O-B0942R | 40 | 0 | 15 | 17,515 | -0.189 | 7.8218 | 1.2848 |
| Edge LOAD TEST S3O-B0942R | 41 | 0 | 10 | 17,515 | -0.170 | 7.8249 | 1.2844 |
| Edge LOAD TEST S3O-B0942R | 42 | 0 | 10 | 17,515 | -0.170 | 7.8254 | 1.2846 |
| Edge LOAD TEST S3O-B0942R | 43 | 0 | 10 | 17,515 | -0.166 | 7.8261 | 1.2844 |
| Edge LOAD TEST S3O-B0942R | 44 | 0 | 10 | 17,515 | -0.163 | 7.8261 | 1.2843 |
| Edge LOAD TEST S3O-B0942R | 45 | 0 | 10 | 17,515 | -0.165 | 7.8261 | 1.2843 |
| Edge LOAD TEST S3O-B0942R | 46 | 0 | 20 | 17,515 | -0.263 | 7.8140 | 1.2872 |
| Edge LOAD TEST S3O-B0942R | 47 | 0 | 20 | 17,515 | -0.249 | 7.8162 | 1.2866 |
| Edge LOAD TEST S3O-B0942R | 48 | 0 | 20 | 17,515 | -0.244 | 7.8164 | 1.2864 |
| Edge LOAD TEST S3O-B0942R | 49 | 0 | 20 | 17,515 | -0.240 | 7.8163 | 1.2861 |
| Edge LOAD TEST S3O-B0942R | 50 | 0 | 20 | 17,515 | -0.236 | 7.8163 | 1.2862 |
| S3O-B0942R Point End | 51 | 0 | 20 | 17,549 | -0.216 | 7.8179 | 1.2862 |
| S3O-B0942R | 52 | 0.33 | 20 | 17,523 | -0.272 | 7.8173 | 1.2888 |
| S3O-B0942R | 53 | 0.33 | 20 | 17,515 | -0.264 | 7.8381 | 1.2761 |
| S3O-B0942R | 54 | 0.67 | 20 | 17,515 | -0.272 | 7.8443 | 1.2768 |
| S3O-B0942R | 55 | 1.67 | 20 | 17,515 | -0.253 | 7.8408 | 1.2767 |
| S3O-B0942R | 56 | 2.67 | 20 | 17,515 | -0.243 | 7.8512 | 1.2755 |
| S3O-B0942R | 57 | 3.33 | 20 | 17,515 | -0.245 | 7.8535 | 1.2761 |
| S3O-B0942R | 58 | 3.33 | 20 | 17,523 | -0.226 | 7.8448 | 1.2759 |
| S3O-B0942R | 59 | 3.67 | 20 | 17,515 | -0.235 | 7.8316 | 1.2783 |
| S3O-B0942R | 60 | 4 | 20 | 17,515 | -0.230 | 7.8354 | 1.2776 |
| S3O-B0942R | 61 | 5 | 20 | 17,515 | -0.216 | 7.8287 | 1.2744 |
| S3O-B0942R | 62 | 6.67 | 20 | 17,575 | -0.243 | 7.8347 | 1.2752 |
| S3O-B0942R | 63 | 7.67 | 20 | 17,523 | -0.239 | 7.8345 | 1.2736 |
| S3O-B0942R | 64 | 9.67 | 20 | 17,515 | -0.287 | 7.8374 | 1.2740 |
| S3O-B0942R | 65 | 12.67 | 20 | 17,575 | -0.269 | 7.8373 | 1.2747 |
| S3O-B0942R | 66 | 15 | 20 | 17,549 | -0.238 | 7.8323 | 1.2753 |
| S3O-B0942R | 67 | 18.33 | 20 | 17,566 | -0.234 | 7.8419 | 1.2738 |
| S3O-B0942R | 68 | 20.33 | 20 | 17,523 | -0.212 | 7.8351 | 1.2733 |
| S3O-B0942R | 69 | 23.67 | 20 | 17,592 | -0.219 | 7.8356 | 1.2738 |
| S3O-B0942R | 70 | 25 | 20 | 17,600 | -0.214 | 7.8350 | 1.2751 |
| S3O-B0942R | 71 | 25.67 | 20 | 17,566 | -0.210 | 7.8359 | 1.2744 |
| S3O-B0942R | 72 | 26.67 | 20 | 17,557 | -0.210 | 7.8526 | 1.2739 |
| S3O-B0942R | 73 | 28.33 | 20 | 17,583 | -0.205 | 7.8325 | 1.2745 |
| S3O-B0942R | 74 | 30 | 20 | 17,557 | -0.227 | 7.8381 | 1.2796 |
| S3O-B0942R | 75 | 33 | 20 | 17,600 | -0.207 | 7.8323 | 1.2806 |
| S3O-B0942R | 76 | 35 | 20 | 17,600 | -0.213 | 7.8426 | 1.2802 |
| S3O-B0942R | 77 | 37 | 20 | 17,600 | -0.216 | 7.8422 | 1.2808 |
| S3O-B0942R | 78 | 39 | 20 | 17,600 | -0.223 | 7.8288 | 1.2810 |
| S3O-B0942R | 79 | 40.33 | 20 | 17,583 | -0.210 | 7.8401 | 1.2790 |
| S3O-B0942R | 80 | 42.67 | 20 | 17,600 | -0.208 | 7.8245 | 1.2799 |
| S3O-B0942R | 81 | 45.33 | 20 | 17,592 | -0.193 | 7.8442 | 1.2783 |
| S3O-B0942R | 82 | 48 | 20 | 17,600 | -0.244 | 7.8271 | 1.2801 |
| S3O-B0942R | 83 | 51.33 | 20 | 17,600 | -0.238 | 7.8424 | 1.2790 |
| S3O-B0942R | 84 | 53.67 | 20 | 17,592 | -0.231 | 7.8274 | 1.2787 |
| S3O-B0942R | 85 | 55.33 | 20 | 17,557 | -0.225 | 7.8426 | 1.2785 |
| S3O-B0942R | 86 | 57.67 | 20 | 17,600 | -0.226 | 7.8370 | 1.2783 |
| S3O-B0942R | 87 | 59.67 | 20 | 17,600 | -0.232 | 7.8341 | 1.2779 |
| S3O-B0942R | 88 | 62.33 | 20 | 17,600 | -0.230 | 7.8356 | 1.2787 |
| S3O-B0942R | 89 | 64.67 | 20 | 17,592 | -0.225 | 7.8399 | 1.2746 |
| S3O-B0942R | 90 | 66.67 | 20 | 17,583 | -0.268 | 7.8408 | 1.2757 |
| S3O-B0942R | 91 | 69 | 20 | 17,600 | -0.258 | 7.8315 | 1.2775 |
| S3O-B0942R | 92 | 74.33 | 20 | 17,600 | -0.247 | 7.8355 | 1.2771 |
| S3O-B0942R | 93 | 77.33 | 20 | 17,600 | -0.223 | 7.8329 | 1.2755 |
| S3O-B0942R | 94 | 80.33 | 20 | 17,600 | -0.230 | 7.8187 | 1.2762 |
| S3O-B0942R | 95 | 85.33 | 20 | 17,600 | -0.269 | 7.8372 | 1.2780 |
| S3O-B0942R | 96 | 88 | 20 | 17,600 | -0.255 | 7.8215 | 1.2776 |
| S3O-B0942R | 97 | 92.67 | 20 | 17,575 | -0.263 | 7.8258 | 1.2780 |
| S3O-B0942R | 98 | 97.67 | 20 | 17,583 | -0.254 | 7.8355 | 1.2771 |
| S3O-B0942R | 99 | 101.67 | 20 | 17,600 | -0.238 | 7.8242 | 1.2776 |
| S3O-B0942R | 100 | 104.33 | 20 | 17,592 | -0.237 | 7.8224 | 1.2762 |
| S3O-B0942R | 101 | 106.67 | 20 | 17,540 | -0.239 | 7.8370 | 1.2772 |
| S3O-B0942R | 102 | 112.33 | 20 | 17,523 | -0.207 | 7.8393 | 1.2755 |
| S3O-B0942R | 103 | 116.67 | 20 | 17,592 | -0.211 | 7.8224 | 1.2773 |
| S3O-B0942R | 104 | 120 | 20 | 17,583 | -0.220 | 7.8196 | 1.2760 |
| S3O-B0942R | 105 | 123.33 | 20 | 17,549 | -0.251 | 7.8187 | 1.2780 |
| S3O-B0942R | 106 | 128.67 | 20 | 17,566 | -0.258 | 7.8181 | 1.2781 |
| S3O-B0942R | 107 | 134 | 20 | 17,540 | -0.299 | 7.8276 | 1.2786 |
| S3O-B0942R | 108 | 138.33 | 20 | 17,566 | -0.300 | 7.8158 | 1.2785 |
| S3O-B0942R | 109 | 141 | 20 | 17,600 | -0.294 | 7.8257 | 1.2773 |
| S3O-B0942R | 110 | 151.33 | 20 | 17,566 | -0.254 | 7.8201 | 1.2747 |
| S3O-B0942R | 111 | 153.33 | 20 | 17,592 | -0.260 | 7.8204 | 1.2764 |
| S3O-B0942R | 112 | 154.33 | 20 | 17,583 | -0.255 | 7.8128 | 1.2762 |
| S3O-B0942R | 113 | 155 | 20 | 17,600 | -0.255 | 7.8061 | 1.2758 |
| S3O-B0942R | 114 | 155.67 | 20 | 17,592 | -0.240 | 7.8128 | 1.2766 |
| S3O-B0942R | 115 | 156 | 20 | 17,592 | -0.220 | 7.8205 | 1.2741 |
| S3O-B0942R | 116 | 159.67 | 20 | 17,600 | -0.258 | 7.8385 | 1.2740 |
| S3O-B0942R | 117 | 163.33 | 20 | 17,600 | -0.262 | 7.8256 | 1.2773 |
| S3O-B0942R | 118 | 165.67 | 20 | 17,592 | -0.270 | 7.8195 | 1.2755 |
| S3O-B0942R | 119 | 169.67 | 20 | 17,557 | -0.265 | 7.8331 | 1.2737 |
| S3O-B0942R | 120 | 174.67 | 20 | 17,566 | -0.253 | 7.8163 | 1.2770 |
| S3O-B0942R | 121 | 180 | 20 | 17,557 | -0.245 | 7.8250 | 1.2747 |
| S3O-B0942R | 122 | 186 | 20 | 17,592 | -0.253 | 7.8260 | 1.2752 |
| S3O-B0942R | 123 | 188 | 20 | 17,540 | 0.150 | 7.8296 | 1.2764 |
| S3O-B0942R | 124 | 190.67 | 20 | 17,540 | -0.012 | 7.8240 | 1.2722 |
| S3O-B0942R | 125 | 192.67 | 20 | 17,592 | -0.067 | 7.8205 | 1.2718 |
| S3O-B0942R | 126 | 194.67 | 20 | 17,592 | -0.122 | 7.8179 | 1.2743 |
| S3O-B0942R | 127 | 197 | 20 | 17,549 | -0.148 | 7.8160 | 1.2750 |
| S3O-B0942R | 128 | 200 | 20 | 17,575 | -0.177 | 7.8133 | 1.2749 |
| S3O-B0942R | 129 | 203.67 | 20 | 17,592 | -0.233 | 7.8201 | 1.2741 |
| S3O-B0942R | 130 | 205.67 | 20 | 17,600 | -0.228 | 7.8335 | 1.2750 |
| S3O-B0942R | 131 | 210 | 20 | 17,600 | -0.220 | 7.8309 | 1.2749 |
| S3O-B0942R | 132 | 212 | 20 | 17,600 | -0.222 | 7.8255 | 1.2744 |
| S3O-B0942R | 133 | 216 | 20 | 17,600 | -0.236 | 7.8099 | 1.2766 |
| S3O-B0942R | 134 | 220.67 | 20 | 17,566 | -0.243 | 7.8241 | 1.2746 |
| S3O-B0942R | 135 | 224.33 | 20 | 17,583 | -0.232 | 7.8227 | 1.2741 |
| S3O-B0942R | 136 | 228 | 20 | 17,566 | -0.235 | 7.8281 | 1.2745 |
| S3O-B0942R | 137 | 232 | 20 | 17,566 | -0.233 | 7.8157 | 1.2760 |
| S3O-B0942R | 138 | 235.67 | 20 | 17,583 | -0.252 | 7.8249 | 1.2751 |
| S3O-B0942R | 139 | 238.67 | 20 | 17,583 | -0.259 | 7.8256 | 1.2759 |
| S3O-B0942R | 140 | 243 | 20 | 17,600 | -0.274 | 7.8224 | 1.2753 |
| S3O-B0942R | 141 | 245 | 20 | 17,566 | -0.287 | 7.8072 | 1.2777 |
| S3O-B0942R | 142 | 249.33 | 20 | 17,592 | -0.248 | 7.8178 | 1.2763 |
| S3O-B0942R | 143 | 253.33 | 20 | 17,557 | -0.252 | 7.8174 | 1.2758 |
| S3O-B0942R | 144 | 258 | 20 | 17,592 | -0.258 | 7.8187 | 1.2769 |
| S3O-B0942R | 145 | 261.67 | 20 | 17,575 | -0.247 | 7.8233 | 1.2753 |
| S3O-B0942R | 146 | 264.33 | 20 | 17,523 | -0.268 | 7.8272 | 1.2759 |
| S3O-B0942R | 147 | 267 | 20 | 17,532 | -0.268 | 7.8180 | 1.2754 |
| S3O-B0942R | 148 | 271 | 20 | 17,592 | -0.251 | 7.8196 | 1.2759 |
| S3O-B0942R | 149 | 275 | 20 | 17,532 | -0.246 | 7.8154 | 1.2764 |
| S3O-B0942R | 150 | 278.33 | 20 | 17,549 | -0.240 | 7.8203 | 1.2751 |
| S3O-B0942R | 151 | 281.67 | 20 | 17,532 | -0.249 | 7.8209 | 1.2750 |
| S3O-B0942R | 152 | 285 | 20 | 17,540 | -0.276 | 7.8239 | 1.2773 |
| S3O-B0942R | 153 | 290.67 | 20 | 17,549 | -0.253 | 7.8228 | 1.2763 |
| S3O-B0942R | 154 | 294 | 20 | 17,532 | -0.255 | 7.8259 | 1.2753 |
| S3O-B0942R | 155 | 298 | 20 | 17,592 | -0.250 | 7.8362 | 1.2753 |
| S3O-B0942R | 156 | 300.67 | 20 | 17,523 | -0.265 | 7.8381 | 1.2755 |
| S3O-B0942R | 157 | 302.67 | 20 | 17,592 | -0.244 | 7.8170 | 1.2769 |
| S3O-B0942R | 158 | 305.67 | 20 | 17,575 | -0.229 | 7.8310 | 1.2753 |
| S3O-B0942R | 159 | 308 | 20 | 17,549 | -0.236 | 7.8297 | 1.2750 |
| S3O-B0942R | 160 | 311 | 20 | 17,549 | -0.236 | 7.8230 | 1.2757 |
| S3O-B0942R | 161 | 313 | 20 | 17,557 | -0.251 | 7.8306 | 1.2759 |
| S3O-B0942R | 162 | 316 | 20 | 17,575 | -0.247 | 7.8281 | 1.2735 |
| S3O-B0942R | 163 | 318 | 20 | 17,566 | -0.227 | 7.8267 | 1.2748 |
| S3O-B0942R | 164 | 320.67 | 20 | 17,566 | -0.223 | 7.8274 | 1.2745 |
| S3O-B0942R | 165 | 323 | 20 | 17,600 | -0.222 | 7.8290 | 1.2750 |
| S3O-B0942R | 166 | 326 | 20 | 17,583 | -0.216 | 7.8351 | 1.2740 |
| S3O-B0942R | 167 | 328.67 | 20 | 17,592 | -0.228 | 7.8383 | 1.2750 |
| S3O-B0942R | 168 | 331.33 | 20 | 17,600 | -0.233 | 7.8367 | 1.2756 |
| S3O-B0942R | 169 | 336 | 20 | 17,592 | -0.212 | 7.8538 | 1.2740 |
| S3O-B0942R | 170 | 339.67 | 20 | 17,600 | -0.213 | 7.8544 | 1.2736 |
| S3O-B0942R | 171 | 342 | 20 | 17,575 | -0.253 | 7.8502 | 1.2734 |
| S3O-B0942R | 172 | 344.33 | 20 | 17,592 | -0.240 | 7.8458 | 1.2734 |
| S3O-B0942R Tail End Met Sample cut | 173 | 353 | 20 | 17,515 | -0.261 | 7.8160 | 1.2765 |
| S3O-B0942R AVG |  |  |  | AVG | -0.233 | 7.8291 | 1.2762 |
| S3O-B0942R MAX |  |  |  | MAX | 0.150 | 7.8544 | 1.2888 |
| S3O-B0942R MIN |  |  |  | MIN | -0.300 | 7.8061 | 1.2718 |
| S3O-B0942R STDEV |  |  |  | STDEV | 0.050 | 0.0104 | 0.0023 |
| Gage End | 174 | 352 | 20 | 17,600 | 0.000 | 8.0012 | 1.5079 |
| Gage End | 175 | 352 | 20 | 17,600 | 0.002 | 8.0013 | 1.5085 |
| Gage End | 176 | 352 | 20 | 17,609 | 0.003 | 8.0012 | 1.5082 |
| Gage End | 177 | 352 | 20 | 17,634 | 0.002 | 8.0013 | 1.5084 |
| Gage End | 178 | 352 | 20 | 17,617 | 0.003 | 8.0013 | 1.5081 |