SPEC-SHEET RATINGS

From Manufacturers’ Websites

Compiled by Bolko von Roedern

September 2007

| Ranked Module Efficiency (%) | Description of best module | Same module with lowest power rating |
| --- | --- | --- |
| 19.3 (non-stan) | SunPower 315 (SunPower rear-point contacted cells, single crystal FZ) Tcoeff = -0.38 %/C, VOC/cell = 673 mV | Also SunPower 300, efficiency 18.4% |
| 17.2 (non-stan) | Sanyo HIP-215NHE (single crystal CZ Si, HIT (Tcoeff = -0.30 %/C), VOC/cell = 717 mV | Also HIP-205NHE, efficiency 16.4% |
| 15.1 (non-stan) | BP7190 (single crystal laser grooved buried grid cells, CZ-Si, Spain) Tcoeff= -(0.5±0.05) %/C, VOC/cell = 622 mV | Also BP 7170, efficiency 13.5% |
| 14.4 (non-stan) | Advent Solar Advent 240 (emitter wrap thru multi-Si) Tcoeff= -0.52%/C, VOC/cell = 610 mV | Also Advent 210, efficiency 12.6% |
| 14.2 (multi) | Kyocera KC200GHT-2 (cast multi-Si diffused cells) Tcoeff.(only given for Voc, -0.123 V/C), VOC/cell = 609 mV | Only one rating listed, warrant now 80% after 20 years (10/90%, 20/80%) |
| 14.2 (mono) | Solar World AG SW 185 (mono-Si “Shell”) Tcoeff.: VOC= -0.33%/C, VOC/cell = 622 mV | Also SW 160, efficiency 12.3% Power-warranty 12/90%, 25/80% |
| 14.1 (mono) | Sharp NU-185 (mono-Si, diffused) -0.485%/C, VOC/cell = 622 mV | Also Sharp NU-170, efficiency 13.0% |
| 13.9 (multi) | BP 175B ("Solarex" multi-Si diffused Cells) Tcoeff= -(0.5±0.05) %/C, VOC/cell = 614 mV | Also BP 160B, efficiency 12.7% |
| 13.4 (multi) | SunTech STP 260S-24V/b (cast multi-Si diffused cells) VOC/cell = 608 mV | Same module with mono-Si cells is also 260 W |
| 13.4 (multi) | Solar World AG SW 225 (multi-Si) Tcoeff.: VOC= -0.33V/C, VOC/cell = 613 mV | Also SW 200, efficiency 11.9% |
| 13.1 (ribbon) | Evergreen Solar ES 195 (string ribbon Si) Tcoeff= -0.49%/C, VOC/cell = 609 mV | Also ES-180 efficiency 12.0% |
| 12.8 (multi) | Sharp ND-208-U1 (multi-Si, diffused) no Tcoeff given , VOC/cell = 602 mV | Only one rating |
| 11.0 (CIS) | WürthSolar WS11007/80 (CIS) Tcoeff.= -0.36 %/C | Also WS 11007/75, efficiency 10.3% (warranty 20/80%) |
| 10.1 (CdTe) | First Solar FS-272 (CdTe) Tcoeff= -0.25 %/C | Also FS-260, efficiency 8.3 % (25-year warranty) |
| 8.5 (a-Si/nc-Si) | Sharp NA-901-WP (90-W) (amorphous/nanocrystalline Si tandem) | Also Sharp NA-801-Wp Efficiency 7.6% (warranty: 10/90%, 20/80%) |
| 8.1 (CIGS) | GSE Soar GSE 120-W Tcoeff=-0.5%/C | Only one rating, but +/-15% power spec |
| 6.3 (a-Si 1-j) | Mitsubishi Heavy MA100 T2 (single j. a-Si, VHF deposition), Tcoeff.= -0.2 %/C | Only one rating (warranty 20/80% warranty) |
| 6.3 (a-Si 3-j) | Uni-Solar PVL 136 (triple-j. amorphous silicon roofing laminate), Tcoeff = -0.26% | Also as 124 W, eff. 5.7% (20-year warranty) |
| 6.3 (a-Si 1-j) | Kaneka T-SC(EC)-120 (single-j. a-Si) No Tcoeff. given | Only one rating (warranty 25/80%) |
| 5.3 (a-Si/a-Si) | Schott Solar ASI-F 32/12 (same-bandgap double junction a-Si) Tcoeff = - 0.20%/C | Only one rating (only 10-year warranty, link to spec sheet failed) |
| 5.3 (a-Si/a-Si) | EPV EPV-42 (same-bandgap double junction a-Si) Tcoeff = - 0.19%/C | (warranty 25/80%) |