| f | Fermi National Accelerator Laboratory Batavia, IL 60510 |
| --- | --- |
| CMS ME234/2 CATHODE LOWER PANEL FR-4 BAR GLUING TRAVELER |
| Reference Drawing(s) Endcap Muon Chamber ME234/2 Lower Cathode Panel Assembly 5520-ME-368224 |
| Magnet/Device Series: |  |  |
| Budget Code: | Project Code: |
| Released by: | Date: |
| Date Closed: | Scan Pages: |
| Prepared by: B. Jensen, M. Hubbard, L. Lee, P. Isham |
| Title | Signature | Date |
| TD / E&F Process Engineering | Bob Jensen/Designee |  |
| TD / E&F CMS Assembly | Glenn Smith/Designee |  |
| TD / E&F Technological Physicist | Oleg Prokofiev/Designee |  |
| TD / E&F CMS Project Manager | Giorgio Apollinari/Designee |  |

Revision Page

| Revision | Step No. | Revision Description | TRR No. | Date |
| --- | --- | --- | --- | --- |
| None | N/A | Initial Release | N/A | 02/08/00 |
| A | 5.3 5.4 | Added Part number for alignment pins. Added part number for clamps. | 0966 | 05/31/00 |
| B | 3.5 4.0 4.1,5.1 5.3 | Corrected part number for Tape, added part number for Tape Install Machine. Adjusted gluing steps to reflect new hand/syringe gluing procedure. Removed operation of inserting/removing Alignment Pins on Gluing Table. Added label for clarification on Clamp Drawing. | 1011 | 07/24/00 |
| C | 5.4 5.5,5.6 | Added "and transport the Cathode Panel to the Panel Staging Area." Removed the Measurement of the Gap Bar Height. | 1087 | 11/28/00 |
| D | CVRPG 3.11 7.0 | Added magnet device, date closed, scanned pages to the cover sheet, and serial number prefix to the bottom of the cover sheet. Added step 3.11, clamp the gap bars for two hours. Removed step 7.0 and signature line and date. | 1272 | 10/24/01 |

Ensure appropriate memos and specific instructions are placed with the traveler before issuing the sub traveler binder to production.

# 1.0	General Notes

  - White (Lint Free) Gloves (Fermi stock 2250-1800) or Nitrile Gloves (Fermi stock 2250-2040)

or equivalent, shall be worn by all personnel, as required, when handling all product parts after

the parts have been prepared/cleaned.

1.2	All steps that require a sign-off shall include the Technician/Inspectors first initial and full last name.

1.3	No erasures or white out will be permitted to any documentation.  All incorrectly entered data shall

be corrected by placing a single line through the error, initial and date the error before adding the

correct data.

1.4	All Discrepancy Reports issued shall be recorded in the left margin next to the applicable step.

1.5 	All personnel performing steps in this traveler must have documented training for this traveler and

associated operating procedures.

1.6	Personnel shall perform all tasks in accordance with current applicable ES&H guidelines and those

specified within the step.

1.7	Cover the panel/chamber with Mylar when not being serviced or assembled.

1.8	Never hand pass anything over a panel as dropped items may damage the panel.

# 2.0	Parts Kit List

2.1	Attach the completed Parts Kit List for the CMS Cathode Lower (CL) Panel Gluing to this traveler.

Ensure that the serial number on the Parts Kit List matches the serial number of this traveler. Verify

that the Parts Kit received is complete.

Process Engineering/Designee				Date

3.0	Panel Preparation

Completed

3.1	Acquire the Cathode Lower Panel (ME-368224) as per the Panel Serial Number at	

the bottom of this traveler.

3.2	Clean the entire panel (both sides) with Ethyl Alcohol (Fermi Stk. No. #1920-0600)	

and a low-lint wipe (Fermi Stk No. 1660-2500) to remove any dirt, dusts, oils, and

other foreign material on the panel.

3.3	Acquire FR-4 Isolation Strips  (MA-368299 [4ea]) and clean with Ethyl Alcohol	

(Fermi Stk No. 1920-0600) and a low-lint wipe (Fermi Stk No. 1660-2500).

3.4	Acquire the following gap bars; (MA-368292 [1 ea], MA-368293 [1 ea], MA-368294 [1 ea,]	

MA-368295 [1 ea], MA-368296 [1 ea], and MA-368297 [1 ea]) and clean with Ethyl Alcohol

(Fermi Stk. No. #1920-0600) and a low-lint wipe (Fermi Stk No. 1660-2500) to remove any dirt,

dusts, oils, and other foreign material.  Clean out the grooves in the gap bars with cotton swabs

dipped in the ethyl alcohol.

3.5	Load one gap bar into the tape installation machine (368550)(or if preferred, affix gap bar with	

Adhesive tape by hand) and affix 3M Scotch double side adhesive tape (368300) to the back of the

gap bar. Trim both ends to fit. Trim out the holes and trim the tape where there is overlap on the side

of the gap bars. Continue until all gap bars are completed.

Technician(s)						Date

Completed

3.6	Mix glue (Epoxy Adhesive #2216 Parts A&B) in a 50/50 ratio using approximately 30	

grams of each. Allow the glue to sit for at least 30 minutes and no more than 45 minutes.

3.7	When applying the Gap Bar (MB-368293) to the panel, be sure the gas hole in gap bar	

is located on the left side of the Panel Center line.

3.8	Without removing the protective strip, align the gap bars along the panel. Install	

the pins (MA-368941) through the holes in the gap bar and into panel to make sure

the gap bar holes and panel holes align.

3.9	Remove Gap Bars from the panel and remove the adhesive tape protective strip.	

3.10	Apply glue (Epoxy Adhesive #2216 Translucent) with a small brush to all the interfacing	

ends of the gap bars to create a fillet between the Gap Bar and the panel copper. Realign the

gap bars onto the pins. Continue installing gap bars in this way until all gap bars are installed

onto the panel. Ensure all alignment pins are removed from the gap bars once they are

correctly taped in place.

3.11	After gap bars have been taped in place, clamp the gap bars for a minimum of two hours.	

Note(s):

Panels must be glued and clamped the same day the Gap Bars are installed!

During the installation of the gap bars, ensure correct placement of the

gap bars as per the angle cut on the gap bar ends.

During the installation of the gap bars, visually check all four corners to ensure

proper fit of gap bar interfaces.

Ensure the panel is covered with Mylar when the panel is not being serviced

Technician(s)						Date

4.0	Panel Gluing

# Completed

Note(s):

The gluing of the Cathode Panels requires two days. On one day, one Upper and

two Inner Panel sides will be glued. On the following day, one Lower and the other

two sides of the Inner Panels will be glued.

On the day this Lower Cathode Panel is NOT being glued, place it on the Cathode

curing table in the proper order according to the drawing below step 5.3.

4.1	Transport the Cathode Lower Panel with gap bars installed to the Panel	

Gluing Station. Install the Cathode Panel onto the Gluing Station work surface

and pin the panel into position

4.2	Apply a piece of Scotch tape (Fermi Stk. No. #1365-10400) to all the seams of	

the already applied gap bars, to prevent the glue from seeping out of the seams. Put a visible

small mark with a marker on the piece of scotch tape to ensure the tape is removed, once

the epoxy is cured.

4.3	Using a syringe, apply glue (Epoxy Adhesive #2216 Translucent) to the	

isolation strip areas. Install the Isolation Strips onto panel in proper position

over the glue and work the epoxy toward the outer edges of the Isolation Strips.

4.4	Using a syringe, apply glue (Epoxy Adhesive #2216 Translucent) to the inside	

perimeter of the FR-4 Gap Bars.

4.5	Using a syringe, apply glue (Epoxy Adhesive #2216 Translucent) to the outside	

perimeter of the FR-4 Gap Bars.

Technician(s)						Date

5.0	Panel Staging

Completed

5.1	Transport the Cathode Lower Panel with gap bars installed to the Cathode Panel	

Curing Staging Area.

5.2	Set Panel on the Cathode Curing Table. Panel order will be in accordance with the	

drawing. Install technological alignment pins (McMaster-Carr 90139A134).

Note(s):

Panels with fresh epoxy must be positioned so the fresh epoxy is on the top

side of the panel.

Clamping Table #2 is for reference only. Clamping Table #2 shows panel stack up

when doing day two cathode panel gluing.

# The first side glue	The second side glue

Clamping table 1	Clamping table 2

Technician(s)						Date

Completed

5.3	Positioning the Quick Grip Clamp Bars (McMaster-Carr 5039A74) at 6” intervals,	

directly over the Gap Bars, clamp the panels to the table while the epoxy is curing.

Note(s):

Ensure there is even spacing of the clamps all around the panels with clamps at each corner.

17	23

1	40

5.4	Once the epoxy has cured (after 24 hrs) remove alignment pins and clamps from panels,	

and transport the Cathode Panel to the Panel Staging Area.

Technician(s)						Date

6.0	Production Complete

XXX	6.1	Process Engineering verify that the Cathode Lower Panel Traveler (5520-TR-333364) is 					accurate and complete.  This shall include a review of all steps to ensure that all operations have been

completed and signed off.  Ensure that all Discrepancy Reports, Nonconformance Reports, Repair/Rework Forms, Deviation Index and dispositions have been reviewed by the Responsible Authority for conformance before being approved.

Comments:

Process Engineering/Designee				Date

7.0	Proceed to the next major assembly operation as required.