SPECIAL SPECIFICATION

SECTION 09262

GYPSUM SHEATHING

Page

PART 1 - GENERAL

1.01	Related Documents ..............................................................................	2

1.02	References ........................................................................................	2

1.03	Summary .........................................................................................	2

1.04	Definitions .......................................................................................	3

1.05	Submittals ........................................................................................	3

1.06	Quality Assurance ...............................................................................	3

1.07	Delivery, Storage and Handling ...............................................................	3

1.08	Sequencing and Scheduling ....................................................................	3

PART 2 - PRODUCTS

2.01	Gypsum Sheathing Board .....................................................................	4

2.02	Accessory Materials ............................................................................	4

PART 3 - EXECUTION

3.01	Installation ......................................................................................	5

SPECIAL SPECIFICATION

SECTION 09262

GYPSUM SHEATHING

PART 1 - GENERAL

1.01	RELATED DOCUMENTS

A.	Drawings and general provisions of Contract, including General and Supplementary Conditions and Division 1 Specification sections, apply to this section.

1.02	REFERENCES

A.	American Society for Testing and Materials (ASTM)

C 79	Specification for Gypsum Sheathing Board

C 954	Specification for Steel Drill Screws for the Application of Gypsum Board or Metal Plaster Bases to Steel Studs from 0.033 in. (0.84 mm) to 0.112 in. (2.84 mm) in Thickness

C 1002	Specification for Steel Drill Screws for the Application of Gypsum Board or Metal Plaster Bases

1.03	SUMMARY

A.	This Section includes the following applications of gypsum sheathing.

1.	Gypsum sheathing on steel studs in exterior walls (behind exterior finish).

B.	Related Sections:  The following sections contain requirements that relate to this section:

1.	Division 5 Section "Cold-Formed Metal Framing" for steel framing of walls covered with gypsum sheathing.

2.	Division 7 Section "Flashing and Sheet Metal" for flashing applied in conjunction with gypsum sheathing.

3.	Division 7 Section "Joint Sealers" for sealants applied in conjunction with gypsum sheathing.

1.04	DEFINITIONS

A.	Gypsum Board Construction Terminology Standard:  Refer to ASTM C 11 and GA 505 for definitions of terms for gypsum board construction not otherwise defined in this section or other referenced standards.

1.05	SUBMITTALS

A.	Product data for each grade of gypsum sheathing indicated.

B.	Research reports or evaluation reports of model code organization acceptable to authority having jurisdiction which evidence compliance of air infiltration barrier with building code in effect for Project.

1.06	QUALITY ASSURANCE

A.	Single Source Responsibility:  Obtain gypsum sheathing from one source from a single manufacturer.

B.	All materials used shall not contain asbestos fibers or lead.

1.07	DELIVERY, STORAGE AND HANDLING

A.	Deliver gypsum sheathing board and related materials in original packages bearing brand name and identification of manufacturer.

B.	Store gypsum sheathing board so that it is protected against damage from weather, direct sunlight, surface contamination, corrosion, construction traffic, and other causes.  Neatly stack gypsum sheathing boards flat on leveled supports off the ground under protective covering.

C.	Handle gypsum sheathing board to prevent damage to edges, ends, and surfaces.

1.08	SEQUENCING AND SCHEDULING

A.	Sequence installation of gypsum sheathing board with installation of exterior cladding to comply with requirements indicated below:

1.	Do not leave gypsum sheathing board exposed to the weather after application for longer than one month.

a.	Protect cutouts, corners and joints in the sheathing by filling them with a flexible sealant at the time sheathing is applied.

b.	As an alternate to sealant application, cover exposed exterior surface of sheathing with building paper or air infiltration barrier.  Anchor covering with metal lath securely fastened through sheathing to framing.  Apply covering immediately after sheathing is installed.

PART 2 - PRODUCTS

2.01	GYPSUM SHEATHING BOARD

A.	Gypsum Sheathing Board with Water-Resistant Core:  Gypsum sheathing board consisting of noncombustible gypsum core incorporating a water-resistant material, surfaced on face, back and long edges with water-repellent paper; complying with ASTM C 79 and requirements indicated below:

1.	Type:  Regular (not Type X).

2.	Edge and End Configuration:  Square.

3.	Thickness:  5/8 inch.

4.	Size:  4 feet by 8 feet.

B.	Products:  Subject to compliance with requirements, provide one of the following:

1.	Gypsum Sheathing Board with Water-Resistant Core, Regular Type:

"Centex American Gypsum Sheathing"; Centex American Gypsum Co.

"Gyproc Gypsum Sheathing"; Domtar Gypsum Co.

"G-P Gypsum Sheathing"; Georgia-Pacific Corp.

"Gold Bond Gypsum Sheathing"; Gold Bond Building Products Div., National Gypsum Co.

USG Gypsum Sheathing; United States Gypsum Co.

2.02	ACCESSORY MATERIALS

A.	Air Infiltration Barrier:  Refer to "Exterior and Interior Wall Types" on drawings.

B.	Fasteners:  Type S steel drill screws, 1" long, with corrosion-resistant finish in form of cadmium plating or proprietary coating, and as follows:

1.	For attachment of sheathing to light gage steel framing of less than 0.033 of an inch in thickness, provide steel drill screws complying with ASTM C 1002.

2.	For attachment of sheathing to steel framing from 0.033 to 0.112 of an inch in thickness, provide steel drill screws complying with ASTM C 954.

C.	Sealant:  Solvent-release-curing joint sealant compatible with joint substrates formed by gypsum sheathing and other related materials and complying with requirements of Division 7 Section "Joint Sealers."

PART 3 - EXECUTION

3.01	INSTALLATION

A.	General:  Except as otherwise indicated, comply with manufacturer's instructions, GA 252, and the following for the installation of gypsum sheathing.

1.	Cut boards at penetrations, edges and other obstructions of the work; fit tight against abutting work, except provide 3/8 inch setback where non-loadbearing work abuts structural elements at head and jambs.

2.	Coordinate installation of sheathing with installation of flashing and joint sealers so that these combined materials are installed in the sequence and manner which prevents exterior moisture from passing through completed exterior wall assembly to the interior.

3.	Apply fasteners so that screw heads bear tightly against face of gypsum sheathing boards but do not cut into face paper.

4.	Do not bridge building expansion joints with gypsum sheathing; cut and space edges to match spacing of structural support elements.

B.	Vertical Installation:  Install 4-feet wide gypsum sheathing boards vertically with vertical edges centered over flanges of steel studs.  Abut ends and edges of each board with those of adjoining boards.  Screw-attach boards at perimeter and within field of board to each steel stud as follows:

1.	Fasteners spaced approximately 8 inches o.c. and set back 3/8 inch minimum from edges and ends of boards.

C.	Air Infiltration Barrier Application:  Cover gypsum board sheathing with air infiltration barrier as follows:

1.	Cut back air infiltration barrier 1/2 inch on each side of break in supporting members at control joint locations.

2.	Apply asphalt-saturated organic felt horizontally with 2 inch overlap and 6 inch endlap; fasten to sheathing with corrosion-resistant staples.

3.	Apply air infiltration barrier over tops of parapets and down to roof counterflashing with 4 inch lap.

END OF SECTION