Homework Assignment No. --- A.

Superpave Mix Design Calculations

Name:__________________________

Date:___________________________

Project information:

ESAL’s = 1.56 million

Mix is being designed for the top lift (i.e. top 50 mm of the pavement)

Binder and Aggregate information:

Gb = 1.030

Gse = 2.723

Gsb = 2.699

Pba = 0.34

% passing 0.075 mm sieve = 3.0%

Nominal maximum size = 19.0 mm

Use the information in the text book, the equations in the class notes and the information provided above to complete the attached Tables 1,2, and 3 below.  Attach all calculations.

Use the information calculated for Table 3 to construct the six graphs needed for a Superpave mix design.

Identify the appropriate design criteria on each graph.  Select an optimum asphalt content.  Indicate on each graph if your selection meets the criteria.

TABLE 1. Initial Calculations.

| Asphalt Content, % | Sample No. | Sample heights in mm at: |  |  | Volumes, cm3 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Ninitial | Ndesign | Nmax | Ninitial | Ndesign | Nmax |
| 3.5 | 1 | 121.2 | 113.0 | 112.0 |  |  |  |
|  | 2 | 120.1 | 112.5 | 111.5 |  |  |  |
| 4.0 | 1 | 120.4 | 112.6 | 111.6 |  |  |  |
|  | 2 | 120.0 | 112.0 | 111.0 |  |  |  |
| 4.5 | 1 | 120.5 | 112.2 | 111.2 |  |  |  |
|  | 2 | 119.5 | 111.5 | 110.5 |  |  |  |
| 5.0 | 1 | 121.3 | 113.0 | 112.1 |  |  |  |
|  | 2 | 119.9 | 111.9 | 111.0 |  |  |  |

TABLE 2. Correction of Estimated Specific Gravity Values.

| Asphalt Content, % | Mass in mold, g | Estimated Gmb |  |  | Gmb at Nmax | Correction Factor, C |  |  | % Gmm |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Ninitial | Ndesign | Nmax |  | Ninitial | Ndesign | Nmax | Ninitial | Ndesign | Nmax |
| 3.5 | 4765.3 |  |  |  | 2.431 |  |  |  |  |  |  |
|  | 4767.3 |  |  |  | 2.432 |  |  |  |  |  |  |
| 4.0 | 4782.0 |  |  |  | 2.448 |  |  |  |  |  |  |
|  | 4774.2 |  |  |  | 2.450 |  |  |  |  |  |  |
| 4.5 | 4805.3 |  |  |  | 2.469 |  |  |  |  |  |  |
|  | 4789.9 |  |  |  | 2.466 |  |  |  |  |  |  |
| 5.0 | 4836.1 |  |  |  | 2.473 |  |  |  |  |  |  |
|  | 4838.9 |  |  |  | 2.479 |  |  |  |  |  |  |

TABLE 3. Properties at Ndesign.

| Asphalt Content, % | Sample No. | % Effective Asphalt, Pbe | Dust Proportion | Air Voids, % | VMA, % | VFA, % |
| --- | --- | --- | --- | --- | --- | --- |
| 3.5 | 1 |  |  |  |  |  |
|  | 2 |  |  |  |  |  |
| 4.0 | 1 |  |  |  |  |  |
|  | 2 |  |  |  |  |  |
| 4.5 | 1 |  |  |  |  |  |
|  | 2 |  |  |  |  |  |
| 5.0 | 1 |  |  |  |  |  |
|  | 2 |  |  |  |  |  |