WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A10781 | In-Flight Anomaly Number -- | Contractor Report Number S-073 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title SELF-LOCKING HIGH PROFILE NUT HAS LOW TORQUE COEFFICIENT |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT 3 | Sys_Lvl Y | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE HIGH PROFILE NUT | PART# 33L2 | SER/LOT# N/A | MANUFACTURER SPS |
| Test/Operation L - FLD | Prevailing Condtion F - FUNCTIONAL | F / U UC | Fail Mode UC - UNSAT | Cause MAP - MFG-ASY-INST |
| System PROPULSION | Defect CN - CONTAM | Material L - FASTNR | Work Contact C. VOGEL | Fail Date 05/25/1987 |
| Received at MSFC 06/03/1987 | Date Isolated -- | FMEA Reference 2.X.X.X | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text LWTS 16, 20, 21, 22, 24 AND UP |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 01/10/1992 | CN RSLV SBMT 10/13/1987 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design J. WHITE | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| Approval |
| Design -- | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete JE | MSFC Closure Date 11/04/1987 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description HIGH PROFILE, SELF-LOCKING NUTS SUPPLIED BY SPS SHOW TORQUE COEFFICIENTS SIGNIFICANTLY LOWER THAN THE INDUSTRY TYPICAL IN SOME SIZES IN THE 33L2 SERIES. A LOW TORQUE COEFFICIENT RESULTS IN A THAN NORMAL PRELOAD BEING APPLIED TO THE BOLT WHEN THE BOLT IS INSTALLED TO SPECIFIED TORQUE |
| Contractor Investigation/Resolution R/C - THE ENTIRE FLEET AND INVENTORY SHALL BE INSPECTED FOR SUSPECT SPS NUTS. WHERE FOUND, RE- PLACEMENT SHALL BE MADE. INCOMING HARDWARE SHALL BE SUBJECTED TO SAMPLE TESTING AT MAF. AND, COR- RECTIVE ACTION WAS TAKEN AT THE SUPPLIER OF THE DISCREPANT NUTS. THE PROBLEM WITH A LOW TORQUE COEFFICIENT, K, ON THE SPS NUTS WAS DISCOVERED DURING ANALYSIS CON- DUCTED ON BOLT SHANKING BY CAPS S-071 (A10693). BOLT-NUT COMBINATIONS WERE BEING TESTED TO ANALYZE SHANKING AND UNEXPECTED FAILURES WERE SEEN. THE FAILURES WERE ISOLATED TO SPS NUTS AND SUBSEQUENTLY ISOLATED TO ITS CADMIUM PLATING BY PRELIMINARY ANALYSIS TESTS WERE CONDUCTED BY WHICH THE CADMIUM PLATING ON SPS NUTS WERE REMOVED THEN THE NUTS WERE REPLATED BY A DIFFERENT VENDOR. THE REPLATED NUTS HAD NORMAL TORQUE COEFFICIENTS. THE SAME TEST WAS CONDUCTED CONCURRENTLY ON NUTS SUPPLIED BY OTHER VENDORS, VOI-SHAN AND VALLEY TODECO. THE TORQUE COEFFICIENTS (VIO-SHAN AND VALLEY TODECO)WERE IN THE TYPICAL RANGE BEFORE AND AFTER REPLATING. FURTHER ANALYSIS OF THE CAUSE FOR LOW TORQUE COEFFICIENTS DETERMINED THAT THE CAUSE WAS NOT 23 WITH THE CADMIUM PLATE. RATHER, IT WAS A CONTAMINANT OR COATING OF POLYETHELENE GLYCOL ON THE SUR- FACE OF THE NUT (REFERENCE TASK I.C OF THIS CAPS). THE FOLLOWING TASKS HAVE BEEN ASSIGNED IN AN EFFORT TO RESOLVE THE PROBLEM: TASK I FAILURE/PROBLEM INVESTIGATION A. DETERMINE CRITICAL PROBLEM AREAS ENGINEERING SHALL DETERMINE WHICH APPLICATIONS OF SPS NUTS ARE OUTSIDE ACCEPTABLE MARGINS OF SAFETY. ANALYSIS SHALL UTILIZE EMPERICAL DATA OBTAINED ON EACH SIZE 33L2 SPS NUT. CLOSURE STATEMENT THE FOLLOWING LOCATIONS HAVE BEEN IDENTIFIED AS AREAS OF CONCERN IF SPS NUTS WITH CARBOWAX ARE INSTALLED (REFERENCE INTEROFFICE MEMORANDUMS 3521-87-046 AND 3511-87-026): LH2 SIPHON SUPPORT 80924901908 (16) 33L2-5 GH2 PRESSLINE FLANGE 80921021009 (56) 33L2-5 ** LH2 FEEDLINE FLANGE (INTERNAL) 80924901908 (36) 33L2-6 OR 80924901916 ** L02 FEEDLINE FLANGE 80921011009 (252) 33L2-6 ** GH2 VENT VALVE/LINE 80921021309 (12) 33L2-6 L02 FEEDLINE OUTLET 80921111900 (44) 33L2-7 DIAGONAL STRUT FLANGE 80911031780 (10) 33L2-10 THRUST STRUT - END FLANGE 80911071790 (48) 33L2-10 ** ALL 33L2-6 NUTS EXONERATED BY INSPECTION, REFERENCE INTEROFFICE MEMORANDUM 3741-87-108. B. EVALUATION OF TORQUE COEFFICIENTS ENGINEERING SHALL DETERMINE THE TORQUE COEFFICIENT RANGE ON EACH SIZE 33L2 SPS NUT IN STOCK AT MAF VERSUS VOI-SHAN AND VALLEY TODECO NUTS. IDENTIFY THOSE APPLICATIONS THAT HAVE TORQUE COEF- FICIENTS THAT ARE BELOW EXPECTED TYPICALS. CLOSURE STATEMENT TESTS WERE CONDUCTED ON SPS NUTS OF THE FOLLOWING SIZES: 33L2-3, -5, -6, -7, -8, -9, -10, AND -14. TORQUE COEFFICIENTS WERE LOW ON 33L2-3, -5, AND -8 FOR THE SAMPLES TESTED (REFERENCE MAY 4, 1987, PRESENTATION BY D. DEEL "BOLT TORQUE/PRELOAD ASSESSMENT"). C METALURGICAL ANALYSIS CONDUCT A METALURGICAL/CHEMICAL ANALYSIS TO DETERMINE THE DIFFERENCES BETWEEN SPS NUTS VERSUS VOI-SHAN AND VALLEY TODECO. THE ANALYSIS SHALL INCLUDE THE FOLLOWING: O ESCA/AES (SURFACE LAYERS) O STANDARD CHEMICAL (BASE METAL) O STANDARD METALURGICAL (CROSS-SECTION) O FTIR/GC (SURFACE LAYERS) CLOSURE STATEMENT ANALYSIS DETERMINED THAT THERE WAS A CONTAMINATION LAYER OF POLYETHYLENE GLYCOL (CARBOWAX) ON SPS 33L2-3, -5, AND -8 NUTS. NO SUCH CONTAMINATION WAS FOUND ON SAMPLES OF OTHER SIZES SPS OR OTHER VENDOR'S NUTS. REMOVAL OF THE SURFACE CONTAMINATION BY VAPOR DEGREASING PRODUCED AN ACCEPTABLE TORQUE COEFFICIENT (WITHIN TYPICAL RANGE) AS VERIFIED ON SPS 33L2-8 NUTS. SUCH REMOVAL ALSO RESULTED IN A CHANGE IN RUNNING OR LOCKING TORQUE (REFERENCE LAB REPORT NO. 87A207). D. EFFECTS OF TORQUE COEFFICIENT WITH RANGE OF TORQUE COEFFICIENTS FOUND DURING TESTING, DETERMINE THAT ALL FLIGHT INSTALLATIONS MEET DESIGN REQUIREMENTS CLOSURE STATEMENT ENGINEERING REVIEWED THE REQUIREMENTS OF DESIGN AND DETERMINED THAT THE CURRENT FLIGHT INSTAL- LATION METHODS, WITH THE KNOWN RANGE OF TORQUE CO-EFFICIENTS, MEET DESIGN REQUIREMENTS REFERENCE INTEROFFICE MEMORANDUM 3521-87-061. E. VERIFICATION OF USAGE OF SPS NUTS INVESTIGATION HAS ALREADY BEEN MADE INTO USAGE OF ALL 33L2 SERIES NUTS SUPPLIED SPS. PROVIDE RECORDS OF ALL OTHER NUTS SUPPLIED BY SPS. INCLUDE DATE AND QUANTITY. CLOSURE STATEMENT LIST OF ALL NUTS SUPPLIED BY SPS PROVIDED WITH PURCHASE ORDER NUMBER AND QUANTITY. BY SIZE, THE NUTS ARE: 33L1-04, -08, -3, -4, -8, -10, -12; 33L2-3, -5, -5S, -6, -7, -8, -9, -10, -12, -14, -20, -20S; 33L3-06, -08, -3, -4, -5; 33L4-3, -4; 33L8C4; 33L9-08, -3, -4, -5; 33L13-1; 33L14-8, -12; 3315-3. -6; 33L19-9 (REFERENCE INTEROFFICE MEMORANDUM 3760-87-157 WITH AT- TACHMENTS). 6/12/87 STATUS UPDATE- UPGRADED CRIT TO 1 AND A LAUNCH CONSTRAINT FOR 61-M. THIS STATUS UPDATE WAS COORDINATED WITH ________________________________________ MR. G. P. BRIDWELL - ET PROJECT MANAGER ________________________________________ MR. J. NICHOLS - CHIEF ENGINEER 9/4/87 STATUS UPDATE (PRB) - LIFTED LAUNCH CONSTRAINTS WITH THE RATIONALE AS FOLLOWS "INSPECTION AND/OR REPAIR SHALL BE MADE REFERENCE DC&RS S-87-004A, S-87-005A, AND S-87-008." THE ABOVE STATEMENT HAS BEEN APPROVED BY: ______________________________________________ G. P. BRIDWELL - ET PROJECT MANAGER ______________________________________________ J NICHOLS ET CHIEF ENGINEER 10/14/87 - CLOSURE UPDATE - REFERENCE CAPS S-073 REVISION "C". THE FOLLOWING IS A CONTINUATION OF TASK I FAILURE/PROBLEM INVESTIGATION: F. L02 COMPATIBILITY OF POLYETHYLENE GLYCOL 1. EVALUATE THE AFFECT OF THE TANK CLEANING CYCLE AND SUBASSEMBLY CLEANING PER PI 5008. 2. IDENTIFY ALL ADDITIONAL NUTS INSIDE THE L02 TANK OR OTHER AREAS IN CONTACT WITH L02. CLOSURE STATEMENT ALL 33L1 AND 33L2 NUTS INSIDE THE L02 TANK HAVE BEEN IDENTIFIED (REFERENCE INTEROFFICE MEMORAN- DUM FROM J. MCALLISTER TO C VOGEL, DATED JUNE 29, 1987). G. EVALUATE NEW INSPECTION EVALUATE AND DETERMINE THE FEASIBILITY OF DEVELOPING A CONTACT METHOD FOR DETERMINING WHETHER INSTALLED NUTS ARE CONTAMINATED WITH POLYETHYLENE GLYCOL (CARBOWAX). THE METHOD BEING CONSI- DERED SHALL BE CAPABLE OF INSPECTING L02 CLEANED NUTS, AS WELL AS EXTERNAL NUTS THAT ARE NOT COVERED BY TPS. H. REVIEW OF SPS PROCESS 1. EVALUATE SPS PROCESSES TO DETERMINE IF THERE IS ANY RECORD OF APPLICATION OF CARBOWAX ON 33L2 OR 33L1 NUTS. DETERMINE WHAT FORMAL OR INFORMAL CRITERIA GOVERNS ITS APPLICATION AT SPS. DETERMINE WHAT OTHER NUTS MAY ALSO HAVE IT APPLIED DETERMINE WHEN IT OR A SIMILAR PRODUCT WAS FIRST BROUGHT INTO USE AT SPS. CLOSURE STATEMENT NO RECORD IS KEPT OF APPLICATION OF CARBOWAX SPS LISTS "NO LUBRICATION" ON THE BLUEPRINT USED FOR MANUFACTURING AND INSPECTION. NO RECORDS SHOW CARBOWAX APPLIED. NO RECORD REFLECTS WHEN CARBOWAX WAS FIRST BROUGHT INTO USE (REFERENCE INTEROFFICE MEMORANDUM 3760- 87-157, WITH ATTACHMENTS). ITEM CLOSED 2. AN MMC TEAM VISITED SPS ON JUNE 17, 1987, FOR EVALUATION OF NUT FABRICATION PROCESS. DURING THE VISIT, IT WAS DETERMINED THAT THE CARBOWAX WAS APPLIED TO THE 33L2 NUT IN A RANDOM MANNER, AND THE MANUFACTURING PLANNING DID NOT INCLUDE A SPECIFIC EXCLUSION OF CARBOWAX ON THE 33L2 NUTS. THE PLANNING PAPER DID INCLUDE A "NO CARBOWAX STATEMENT" FOR THE 33L1 NUTS. THEREFORE, SPS SHALL REVIEW THEIR HISTORY DATA FILES TO DETERMINE THAT THE PLANNING PAPER HAS NOT CHANGED FOR THE 33L1 AND 33L2 NUTS AND PROVIDE A WRITTEN REPORT. CLOSURE STATEMENT ALL 33L1 PROCESSING SHEETS AND MANUFACTURING DRAWINGS SINCE INITIAL MANUFACTURING RUN STATED "NO CARBOWAX", AND A SPECIFIC BUYOFF POINT EXISTED FOR APPLICATION OF LUBRICANT ON ALL INSPECTION RECORDS. NONE OF THE INSPECTION RECORDS HAD A BUYOFF INDICATING THAT LUBRI- CANT WAS APPLIED. ALSO, EXONERATED ARE 33L2-5S, -20S, AND 33L14 NUTS (REFERENCE INTEROFFICE MEMORANDUM 3741-87-090, AND REPLY TO SCAD-87-145). 3. REVIEW OF SPS PURCHASE ORDER AND RECEIVING RECORDS INDICATES THAT ONLY ONE PURCHASE AND SHIPMENT OF 33L2-6 NUTS WAS EVER MADE. A QUANTITY OF SPS 33L2-6 NUTS STILL EXISTS AT MAF FROM PRODUCTION STORES (CURRENTLY SEQUESTERED). ANALYZE A SAMPLE OF THE 33L2-6 NUTS FOR EVIDENCE OF CARBOWAX. CLOSURE STATEMENT NO EVIDENCE OF CARBOWAX WAS FOUND ON THE 33L2-6 SPS NUTS, FTIR ANALYSIS AND TORQUE TESTS WERE PERFORMED (REFERENCE LAB REPORT #87N293). RELIABILITY ASSURANCE HAS EXONERATED ALL 33L2-6 SPS NUTS BASED UPON THE EVIDENCE THAT NO CARBOWAX WAS EVER APPLIED TO THOSE NUTS (REFERENCE INTEROFFICE MEMORANDUM 3741-87-108). I. REVIEW OF MOD KITS AND HARDWARE SUPPLIED TO VENDORS 1. REVIEW MATERIAL LISTS FOR ALL MOD KITS. MAKE RECORD OF 33L2 AND 33L1 NUT APPLICATIONS SPECIFYING SIZE AND SPECIFIC LOCATION CLOSURE STATEMENT A LIST OF 33L2 AND 33L1 NUTS WITH SPECIFIC MOD KIT ALLOCATION WAS PROVIDED (REFERENCE INTEROFFICE MEMORANDUM 3543-87-024) 2. REVIEW MATERIAL LISTS FOR ALL HARDWARE SUPPLIED TO VENDORS. MAKE RECORD OF 33L2 AND 33L1 NUT APPLICATIONS SPECIFYING SIZE AND SPECIFIC LOCATION. CLOSURE STATEMENT LIST PROVIDED FOR ALL 33L1 AND 33L2 NUTS SHIPPED TO VENDORS. LIST INCLUDES THE FOLLOWING SIZES: 33L1-04, -08, -3, -4, -6; 33L2-3, -6, -8, -20S (REFERENCE DATA SHEET). ITEM CLOSED 3 REVIEW MATERIAL LISTS FOR SHIP LOOSE HARDWARE. MAKE RECORD OF 33L2 AND 33L1 NUT APPLICATIONS SPECIFYING SIZE AND SPECIFIC LOCATION. CLOSURE STATEMENT LIST WAS PROVIDED WITH ALL LOCATIONS WHERE 33L2 NUTS ARE USED IN SHIP LOOSE HARDWARE. 33L1 NUTS WERE EXCLUDED BECAUSE THEY WERE EXONERATED. IT WAS DETERMINED THAT 33L2-5 AND -10 NUTS ARE USED IN THE BIPOD ASSEMBLY KIT, 33L2-4 ARE USED IN THE SRB FAIRING INSTALLATION KIT BUT SPS HAS NEVER SUPPLIED 33L2-4 NUTS (REFERENCE INFORMAL MEMORANDUM FROM J. MCALLISTER TO C. VOGEL, DATED JULY 13, 1987). TASK II CORRECTIVE ACTIONS A. PURGE OF INVENTORY STORES AND PRODUCTION 1. ALL SPS 33L1 AND 33L2 NUTS SHALL BE PURGED FROM INVENTORY AND PRODUCTION STORES. CLOSURE STATEMENT INVENTORY AND PRODUCTION STORES PURGED OF ALL SPS NUTS OF EVERY TYPE AND SIZE (REFERENCE INTEROFFICE MEMORANDUMS 3724-87-078 AND 3762-87-025A). 2. PURGE ALL 33L1 AND 33L2 NUTS FROM PRODUCTION STAGING AREAS AND FROM LOOSE HARDWARE HELD ON THE FLOOR ISSUE A MEMORANDUM STATING THAT ALL 33L1 AND 33L2 NUTS HELD IN UNOFFICIAL AREAS (E.G., TOOL BOXES) SHALL BE TURNED IN TO QUALITY CONTROL. CLOSURE STATEMENT 33L1 AND 33L2 NUTS HAVE BEEN PURGED FROM STAGING AREAS AND A LETTER HAS BEEN DISPERSED BY WHICH LOOSE HARDWARE HELD ON THE FLOOR HAS BEEN PURGED OF ALL SPS 33L1 AND 33L2 NUTS (REF- ERENCE INTEROFFICE MEMORANDUM 3630-87-23). B. SPS NUTS ON PRE-DD250 TANKS AND SUBASSEMBLIES GENERATE A DC&R TO ADDRESS THE POSSIBLE INSTALLATION OF SPS NUTS ON ALL TANKS AND SUBASSEM- BLIES PRE-DD250 THE DC&R SHALL ADDRESS THOSE NUTS SPECIFICALLY IDENTIFIED BY ENGINEERING IN TASK I.A FOR LOW FACTOR OF SAFETY. CLOSURE STATEMENT DC&RS S-87-004 AND S-87-008 HAVE BEEN WRITTEN TO ADDRESS SPS NUTS ON ALL PRE-DD250 TANKS AND SUBASSEMBLIES. C. SPS NUTS ON POST-DD250 TANKS GENERATE A DC&R TO ADDRESS THE POSSIBLE INSTALLATION OF SPS NUTS ON ALL TANKS POST DD250. THE DC&R SHALL ADDRESS THOSE NUTS SPECIFICALLY IDENTIFIED BY ENGINEERING IN TASK I.A FOR LOW FACTOR OF SAFETY. CLOSURE STATEMENT DC&R S-87-005 HAS BEEN WRITTEN TO ADDRESS SPS NUTS ON ALL POST-DD250 TANKS. D. VENDOR IDENTIFICATION ON NUTS EVALUATE IMPOSING THE REQUIREMENT FOR VENDORS TO APPLY THEIR VENDOR IDENTIFICATION TO ALL NUTS. CLOSURE STATEMENT THE QUALITY RECEIVING ACCEPTANCE PLAN HAS BEEN REVISED TO REQUIRE VERIFICATION OF VENDOR ID ON THE NUTS (REFERENCE INTEROFFICE MEMORANDUM 3743-87-097). ITEM CLOSED E. REVISION TO QUALITY RECEIVING ACCEPTANCE PLAN THE RECEIVING ACCEPTANCE PLAN SHALL BE REVISED TO INCLUDE INSPECTION FOR LUBRICATION APPLIED TO NUTS AND BOLTS, IN ANY SERIES THAT SPECIFIES NO LUBRICATION. CLOSURE STATEMENT RAPS (RECEIVING ACCEPTANCE PLAN) HAVE BEEN REVISED TO CHECK FOR THE PRESENCE OF LUBRICATION BY LABORATORY ANALYSIS ON ALL NUTS WHERE "NO LUBRICATION" IS REQUIRED (REFERENCE INTEROFFICE MEMORANDUMS 3743-87-074 AND 3743-87-097). F. INITIATION OF NOTIFYING DOCUMENTS 1. INITIATE A SUPPLIER CORRECTIVE ACTION DIRECTION (SCAD) TO SPS CONCERNING THE PROBLEM WITH POLYETHELYENE GLYCOL (CARBOWAX) APPLIED TO NUTS THAT REQUIRE NO LUBRICATION. CLOSURE STATEMENT SCAD-87-145 WAS ISSUED. ALL 33L2 PROCESSING SHEETS AND MANUFACTURING DRAWINGS HAVE BEEN REVISED TO STATE "NO CARBOWAX". ALL 33L PARTS ARE NOW SUBJECTED TO AN ADDITIONAL SAMPLE TEST TO VERIFY THE NON-PRESENCE OF CARBOWAX. AND, THE MATERIAL HANDLING OF THE NUTS HAVE BEEN IMPROVED WITH A NEW INSPECTION/TEST AREA TO PRECLUDE INCIDENTAL CONTACT WITH CARBOWAX. REFERENCE SCAD 87-145 ITEM CLOSED 2. INITIATE AN ALERT CONCERNING 33L2 SERIES NUTS FROM SPS CLOSURE STATEMENT ALERT NO. MMC-ET-RA07B-26 WAS ISSUED. G. INSPECTION CRITERIA FOR RECEIVING ACCEPTANCE PLAN DEFINE AN INSPECTION CRITERIA FOR THE EVIDENCE OF LUBRICANT APPLIED TO NUTS AND BOLTS, WHERE ENGINEERING REQUIREMENTS SPECIFY NO LUBRICANT. CLOSURE STATEMENT TESTING FOR LUBRICANTS, CARBOWAX, SHALL TAKE PLACE BY ORGANIC CHEMICAL ANALYSIS. REFERENCE INTEROFFICE MEMORANDUM 3772-87-171. ITEM CLOSED H PURGE OF OFF-SITE INVENTORY ALL SPS NUTS, 33L2, SHALL BE PURGED FROM THE INVENTORY OF: 1. MOD KITS AND SHIP LOOSE, FROM OFF-SITE INVENTORY STORES AT KSC, VANDENBURG, AND NSTL. CLOSURE STATEMENT ALL SUSPECT 33L2 NUTS HAVE BEEN SEQUESTERED AT KSC, NSTL AND VANDENBURG, OR TRACKABLE DOCU- MENTATION HAS BEEN WRITTEN. REFERENCE AR NO. M7043-K1, AR NO M7043-M2, AR NO. 7002 AND AR NO. MV7012-MV1. 2. VENDOR KITS CLOSURE STATEMENT ALL 33L2 NUTS IN KITS SUPPLIED TO VENDORS HAVE BEEN PICKED UP BY MMC PERSONNEL. 33L1 NUTS HAVE BEEN EXCLUDED BECAUSE THEY HAVE BEEN EXONERATED (REFERENCE INFORMAL MEMORANDUM FROM T. FARROW TO C. VOGEL, DATED JULY 13, 1987). 3. MODE KITS AND SHIP LOOSE AT MAF: * CLOSURE STATEMENT ALL SUSPECT MOD KITS AND SHIP LOOSE SHALL BE INSPECTED BY DC&R S-87-009. REFERENCE DC&R S-87-009. TASK III CAPS CLOSEOUT SUMMARY * IT WAS DETERMINED, DURING BOLT SHANKING STUDIES, THAT SOME NUTS SUPPLIED BY SPS HAD LOW TORQUE CO-EFFICIENTS. LAB ANALYSIS TRACED THE CAUSE TO LUBRICATION, CARBOWAX, APPLIED TO THE NUTS. IT WAS CONFIRMED THAT SUSPECT NUTS WERE LIMITED TO THOSE PRODUCED BY SPS. ENGINEERING ANALYSIS DETERMINED WHICH SPECIFIC PLACES SUCH NUTS WOULD POSE A CONCERN FOR FACTOR OF SAFETY. ALL LOCA- TIONS THUS IDENTIFIED, AND NOT EXONERATED BY ADEQUATE PURCHASE ORDER TRACEABILTIY, WERE PLACED ON DC&RS FOR INSPECTION/REPLACEMENT IN THE FLEET. CONCURRENTLY, ALL INVENTORY OF NUTS HAS BEEN PURGED OF SUSPECT SPS NUTS. THERE IS TRACKABLE DOCUMENTATION INITIATED FOR INSPECTION OF SUSPECT MOD KITS AND SHIP LOOSE HARDWARE NOT YET ACCESSIBLE FOR INSPECTION. NEW HARDWARE SHALL BE SUB- JECTED TO A REVISED RAP (RECEIVING ACCEPTANCE PLAN) WHICH NOW INCLUDES A SAMPLE INSPECTION FOR EVIDENCE OF LUBRICANT (NO LUBRICATION REQUIRED). CORRECTIVE ACTION WAS ALSO TAKEN AT THE SUPPLIER OF THE DISCREPANT NUTS--IMPROVED DOCUMENTATION, SAMPLE TESTING AND MATERIAL HANDLING. IN SUMMARY, THE ENTIRE FLEET AND INVENTORY SHALL BE INSPECTED FOR SUSPECT SPS NUTS. WHERE FOUND, REPLACEMENT SHALL BE MADE INCOMING HARDWARE SHALL BE SUBJECTED TO SAMPLE TESTING AT MAF. AND, CORRECTIVE ACTION WAS TAKEN AT THE SUPPLIER OF THE DISCREPANT NUTS TASK IV CLEARANCE EFFECTIVITIES LWTS 16, 20, 21, 22, AND 24 THROUGH 46: NO CONSTRAINTS. INSPECTION AND/OR REPAIR SHALL BE MADE (REFERENCE DC&RS S-87-004, S-87-005A, AND S-87-008). LWTS 47 AND UP: NO CONSTRAINTS INVENTORY PURGED OF SUSPECT SPS NUTS |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A10781 | IFA# -- | Contractor RPT# S-073 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 33L2 | Asmnt Part Name HIGH PROFILE NUT | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MAP - MFG-ASY-INST | FAIL MODE MR - TORQUE HI/LO |
| Asmnt FMEA 2.1.13.1 | Asmnt FM 1 | FMEA CSE A | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |