Interpenetrating Networks of Elastomers

Exhibiting 300% Electrically-Induced Area Strain

Soon Mok Ha1, Wei Yuan1, Qibing Pei*1, Ron Pelrine2 and Scott Stanford2

1Department of Materials Science and Engineering, UCLA, Los Angeles, CA, USA 90095;

2SRI International, 333 Ravenswood Avenue, Menlo Park, CA, USA 942025

E-mail : soonmok@ucla.edu, weiyuan@seas.ucla.edu, qpei@seas.ucla.edu, ronald.pelrine@sri.com and scott.stanford@sri.com

Abstract

Mechanical prestrain is generally required for most electroelastomers to obtain high electromechanical strain and high elastic energy density. However, prestrain can cause several serious problems, including a large performance gap between the active materials and packaged actuators, instability at interfaces between the elastomer and prestrain-supporting structure, and stress relaxation. Difunctional and trifunctional liquid additives were introduced into 400% biaxially prestrained acrylic films and subsequently cured to form the second elastomeric network. The goal of this research was to determine the effect of different functional additives and concentrations on the microstructure, the mechanical properties, and the actuation of composite films. In the as-obtained Interpenetrating Polymer Networks (IPN), the additive network can effectively support the prestrain of the acrylic films and as a result, eliminate the external prestrain-supporting structure. However, the large amount of additive used to completely preserve prestrain was found to make the films too stiff, causing damage to IPN composite films. Furthermore, the interpenetrating network formed from a trifunctional monomer is more effective than that formed from the difunctional monomer in supporting the high tension of the VHB network. This high efficiency trifunctional additive leads to the enhancement of the breakdown field, due to less damage on the microstructure. The IPN composite films without external prestrain exhibit electrically-induced strains up to 300% in area, comparable to those of VHB 4910 films under high prestrain conditions.

1. Introduction

In recent studies of large electromechanical strain from electroelastomers, based on acrylic copolymer elastomers (e.g., 3M VHB 4910), it was found that prestrain significantly enhances performance by increasing the dielectric breakdown strength [1-6]. Because an electrically-induced strain is proportional to the square of the applied electric field, the maximum strain is significantly increased as the breakdown field is enhanced. Mechanisms to account for the enhancement of the dielectric breakdown strength have not been well understood; they have been attributed to the increased probability of hot electrons colliding with polymer chains realigned in parallel to the film surfaces. Prestrain is a key factor in transferring electroelastomer performance. Prestrain realigns defects, such as fibrous impurities, non-spherical voids, and gel particles that may be responsible for premature dielectric breakdown.  However, the overall performance of the electroelastomer is observed to substantially decrease when packaged to support the required high prestrain. Disparities in performance between the active material and the packaged actuators are due to the prestrain-supporting structures, which significantly occupy more space and weigh more than the acrylic films themselves [7,8]. In addition, the lifetimes of the actuators are limited due to the stress concentration at the interfaces between the soft polymer film and the rigid supporting structure. The shock tolerance of the actuators is also reduced because of the rigid structural components introduced. The prestrained films exhibit stress relaxation which affects the subsequent actuation [6]. Consequently, it is highly desirable to eliminate mechanical prestrain while retaining its performance benefits.

Recently, we reported interpenetrating polymer networks (IPN) as new electroelastomers that exhibit high actuation performance without mechanical prestrain [9,10]. An IPN is defined as a combination of two or more polymers that form a network, in which at least one polymer is polymerized and/or crosslinked in the immediate presence of the others [11]. In this approach, acrylic elastomers were used as the initial elastomeric network in order to take advantage of the high dielectric breakdown field obtained in highly prestrained acrylic elastomer films. Polymerizable and crosslinkable liquid monomers were introduced into highly-prestrained acrylic films and cured to form the second elastomeric network. When the interpenetrating elastomeric network films were allowed to relax at zero external stress, the acrylic network was observed to contract, compressing the additive network. The resulting free-standing films consist of two networks in balance; one in high tension and the other in high compression. Consequently, the molecular, nanometer, and micrometer-scale alignments may be preserved in the resulting free-standing films. A schematic explanation of this approach is shown in Figure 1.

Figure 1. Schematic illumination of the fabrication process of an IPN electroelastomer film: (a) an acrylic film before processing, (b) after 400 % biaxial prestrain, the film area expands by 24 folds, (c) curable additives are added into the prestrained film and cured, forming an interpenetrating network of a highly crosslinked polymer, (d) after external stress is removed, the interpenetrating network preserves most of the prestrain of the acrylic film

In this study, two functional acrylic monomers, 1,6 hexanediol diacrylate (HDDA) and trimethylolpropane trimethacrylate (TMPTMA), are used to form the interpenetrating network. The density of crosslinks in the interpenetrating network depends on the monomer type and the degree of functionality. At equal weight fractions, TMPTMA, a trifunctional acrylate, has a concentration of crosslinkable double bonds that is 33.68% higher than that of the HDDA, a difunctional acrylate. The network formed from the trifunctional monomer is more effective than that formed from the difunctional monomer in supporting the high tension of the VHB network in the IPN composite films.

2. Experimental

2.1. Materials

An acrylic copolymer elastomer, which is commercially available as a 1 mm-thick adhesive film (3M, VHB 4910), was used as the electroelastomer network. The film is extremely compliant and has a quite uniform surface. In forming an additive network in the acrylic network, a difunctional acrylate monomer or a trifunctional methacrylate monomer was used. The thermally-curable 1,6-hexanediol diacrylate (HDDA), was purchased from Sartomer Co. It has two acrylate functional groups per molecule, a molecular weight of 226 Dalton, and  a viscosity of 9 cps at room temperature. The thermally-curable, trifunctional trimethylolpropane trimethacrylate (TMPTMA) purchased from Sigma Aldrich,  has a molecular weight of 338 Dalton. The chemical structures of the HDDA and TMPTMA are shown in Figure 2. Benzoyl peroxide, was used as a thermally-activated initiator for free-radical polymerization. Benzoyl peroxide is soluble in HDDA and TMPTMA.

(a) 1,6-Hexanediol diacrylate (HDDA) monomer

b) Trimethylolpropane trimethacrylate (TMPTMA) monomer

Figure 2. Chemical structures of difunctional and trifunctional acrylic monomers

2.2. Preparation of IPN in highly prestrained elastomer films.

The fabrication of IPN composite films began with the biaxial stretching of acrylic films. The structures to support the stretched films are made of Mesonite to minimize thermal deformation. The films were stretched to 5 times its original length and width, i.e., 400% biaxial prestrain. The film thickness after the prestrain was 40 μm for VHB 4910. The diacrylate and trimethacrylate monomers were added into the prestrained VHB films. Benzoyl peroxide, a thermal initiator for free-radical polymerization, was also added. The films were then placed in a vacuum oven and heated up to 85 oC to induce the free-radical polymerization of the monomers. Any nonuniform heating or additive degradation gave rise to stress concentration near the edges. Therefore, the edges of the composite films were trimmed to eliminate this problem.

2.3. Analysis of microstructure and FTIR spectroscopy

The microstructure of the IPN formed films was observed by a field emission scanning electron microscope (S4700, Hitatch Inc.). The samples were prepared and attached onto high-density polyethylene. To improve the image quality, the sample surface was coated up to 10 nm with gold by sputtering. FTIR spectroscopy was used to determine the chemical structure change during the thermal curing process. Infrared spectra of IPN electroelastomer films were measured with FTIR spectroscopy (M2200, MIDAC Corporation) in the wavenumber range of 4000-400 cm-1.

2.4. Measurement of mechanical properties

A simple setup was built to measure the biaxial deformation of clamped electroelastomer films under hydraulic load. Acrylic films after thermal polymerization of admixed diacrylate were carefully mounted onto one end of an acrylic tube with an inner diameter of 25.4 mm and a tube length of 1.22 m. Water was added into the tube to provide a hydraulic pressure to biaxially stress the acrylic film [12]. Deflection of the central point in the acrylic film was measured by a non-contacting technique using a CCD camera and image analysis software. Care was taken to prevent delamination of the IPN formed film from the acrylic tube. The deflection was used to calculate the biaxial strain of the acrylic film by the hydraulic pressure. The thickness of the IPN films was measured using a digital thickness gauge (Mitutoyo).

2.5. Actuator fabrication

Diaphragm actuators were fabricated from free-standing composite films. Conductive carbon grease was smeared onto both sides of the film. Thin strips of aluminum foil were used as electrical contacts. Electrically-induced strain was monitored using a CCD camera to capture the changes in diameter and height. Strain in area was computed from geometric relations found between the diameter and height of the bulge. High DC voltages up to 10 kV were supplied from a high voltage power source built in-house. When expanded at a high driving voltage, the IPN films bulged or wrinkled without directional preference. To measure the strain, a small pneumatic pressure was applied to deform the expanding films into a spherical geometry.

3. Results and Discussion

3.1. Preserved prestrain with curable additive

The acrylic copolymers in the 3M VHB films are very soft with a Young’s modulus on the order of 500 kPa. This low modulus is due to the long-chain and branched alkyl groups attached to the acrylate polymer chains. The highly crosslinked polymer of HDDA, with a modulus on the order of 930 MPa [13], is more rigid than the VHBs. However, the flexible hexylene segment between the two acrylate end groups of HDDA allows the polymer to contract or stretch within a certain range. The modulus of poly(TMPTMA) is expected to be higher than that of the poly(HDDA), as the trifunctional TMPTMA results in a higher density of crosslinks. Therefore, the same percentage of preserved prestrain obtained by poly(HDDA) can be accomplished by using a smaller amount of poly(TMPTMA).

In the experiment, various amounts of HDDA and TMPTMA were added separately into a highly prestrained VHB film. Upon curing, an interpenetrating network of poly(HDDA) or poly(TMPTMA) formed in the highly prestrained VHB network. As the IPN composite film was released from the prestrain structure, a contraction occurred in the prestrained VHB network, compressing the poly(HDDA) or poly(TMPTMA) network. The composite film reached a stable geometry when the tension in the VHB network balanced with the compression in the poly(HDDA) or poly(TMPTMA) network. This VHB network remained substantially strained compared to its original geometry. The preservation of the prestrain of the VHB network was measured using the distance between black dots marked on the cured film. The resulting preserved prestrain versus weight percentage of additive is plotted in Figure 3.

Figure 3. Preserved prestrain of VHB 4910 films after being released from prestrain structure. The preserved prestrain is calculated based on the original geometry of the VHB films before prestrain. Preserved prestrains of 0% and 400% correspond to zero and full prestrain preservation, respectively.

As expected, the prestrain preservation is strongly dependent on the amount of additive used. The preserved prestrain increases rapidly above a threshold concentration of additive . This may be explained by the percolation theory [14]. When the amount of additive is increased to a critical value, the polymer forms a crosslinked network of its own. This network effectively supports the prestrain of the preexistent VHB network. The threshold concentrations, the onset of the rapid increase of preserved prestrain, are approximately 14% for HDDA and 8.4% for TMPTMA. The lower threshold concentration of TMPTMA can be attributed to its trifunctionality that facilitates the formation of its 3-dimensional network in the acrylic elastomer.

Figure 4. Scanning electron micrograph (SEM) images of the VHB films for (a) 400% biaxial prestrained VHB 4910 without additive, (b) cured VHB 4910 with 35.94% by weight of poly(HDDA) before releasing, (c) VHB 4910 with 23.38% by weight of poly(TMPTMA) before releasing.

Scanning electron micrographs displayed in Figure 4 showed sub-micron size cracks. These cracks may be due to  the broken additive network, which is less compliant than the VHB network. Figure 4 (b) and (c) compare the VHB-poly(HDDA) and the VHB-poly(TMPTMA) films containing the same molar concentration of crosslinking acrylate or methacrylate functional groups. In an HDDA molecule, the first acrylate group is used for polymerization and the second acrylate is the crosslinkable group that bonds polymer chains together. In TMP-TMA, each molecule contains 2 crosslinkable groups. In Figure 4, the VHB-poly(HDDA) film exhibits a much rougher surface morphology and larger cracks than the VHB-poly(TMPTMA). Consequently, the difunctional HDDA system is more damaged than the trifunctional TMPTMA system containing the same amount of crosslinkable vinyl double bonds. The IPN films with high concentrations of additive appear turbid, indicating that the two networks are chemically independent from each other. For the same concentration of crosslinkable groups, the VHB-poly(HDDA) film is found to be more turbid than the VHB-poly(TMPTMA) film. The turbidity can be attributed to the phase separation of the additive network from the VHB network.  The degree of phase separation is observed to increase proportionally with the turbidity of the IPN film.

3.2. Infrared spectra of IPN films

The curing of the additive and its network formation can be monitored by recording the decrease of IR absorption peaks that are characteristic of the carbon-carbon double bonds in the additive. Figures 5 and 6 show the comparison of FTIR spectra from (a) a 400% biaxial prestrain VHB 4910 without additive, (b) VHB 4910 with additive before curing, and (c) VHB 4910 with additive after curing.  Upon thermal curing, significant changes are observed in the IR spectra of the IPN films. The absorption peak at 810 cm-1 from alkene C-H stretching in the additive, decreases to near disappearance after thermal curing. The other relatively intense absorption peak at 1635 cm-1 (acrylic group. C=C) shown in Figures 5 and 6 (b) also drastically decreases after curing. From these results, it is evident that the HDDA and TMPTMA has polymerized and crosslinked (because they are di- and trifunctional), and that the interpenetrating network of the cured additive has formed in the preexistent VHB network.

Figure 5. FTIR spectra of the VHB films for (a). 400% biaxially prestrained VHB 4910, (b). (a) with 18.3 wt% HDDA, (c). (b) after thermally curing.

Figure 6. FTIR spectra of the VHB films for (a). 400% biaxially prestrained VHB 4910, (b). (a) with 9.7 wt% TMPTMA, (c). (b) after thermally curing

3.3. Mechanical properties of IPN composite films before release

The stress-strain behavior of VHB-poly(HDDA) and VHB-poly(TMPTMA) was measured, assuming little chemical crosslinking occured between the two networks. Results show that the acrylic network remained intact during the formation of the interpenetrating polymer network. Any variation in the stress-strain behavior would occur due to the presence of an additive network. Figure 7 shows the stress-strain response of the cured composite films before the films were released to free-standing. The VHB network is under 400% biaxial prestrain, whereas the additive network is at zero prestrain. There is no experimental data to prove that poly(HDDA) and poly(TMPTMA) aligns itself with the prestrained VHB network.

(a) VHB-poly(HDDA)                  (b) VHB-poly(TMPTMA)

Figure 7. Hydraulic pressure versus stretch ratio curves for prestrained VHB 4910 (a) containing different concentrations of poly(HDDA) and (b) poly (TMPTMA) before being released from prestrain structure. The numbers in the insets are in weight percent of the additive network in the IPN films.

As shown in Figure 7, the stress-strain response is nonlinear for VHB without any additive, but it becomes increasingly linear with higher concentrations of poly(HDDA) and poly(TMPTMA). The non-linearity may be due to a combination of chain uncoiling and bond stretching [15]. At higher stretching ratios, the chemical bonds are stretched very far apart and the VHB network begins to break. With increasing concentrations of additive, the films become stiffer, particularly at high stretch ratios. At small stretch ratios (<1.05), the VHB-poly(HDDA) films in Figure 7 (a) are not much stiffer, or even softer, than the pure VHB films. This is further discussed in the next paragraph.

The theory for large deflection in circular thin plates developed by Timoshenko [16] was used to evaluate the effect of additive on film stiffness. At small stretch ratios, the Young’s modulus E, of a clamped circular plate under a uniform applied pressure P is given by

(1)

where h, ω0, a, and ν are film thickness, deflection at the film center, and radius of plate and Poisson’s ratio, respectively.

Figure 8. Calculated pseudo-Young’s moduli of prestrained VHB 4910 films with or without additive. The VHB films were biaxially prestrained by 400%, admixed with additive and cured. The moduli are calculated based on a stretch ratio of 1.03.

Figure 8 shows the intriguing effects of additive content on the pseudo-Young’s modulus of the prestrained films before release. Note that at zero deflection or at a stretch ratio of 1, the films have built-in tension. The Young’s moduli, which by definition are values at minimal external tension, thus only reflect the stiffness of the films at this condition, and do not correspond to the Young’s moduli of the films. Therefore, we call the calculated values “pseudo-Young’s moduli”. The psuedo-Young’s modulus of VHB 4910 under 400% biaxial prestrain is 18.42 MPa, which increases to 38.76 MPa when the poly(TMPTMA) content is increased to 23.49%. This characteristic effect should result from augmentative proportions of additive network. The additive monomers are polymerized in the presence of the preexistent VHB matrix.  As shown in Figure 8, the psuedo-Young’s modulus of VHB-poly(HDDA)first decreases from 18.42 MPa to 13.3 MPa as the poly(TMPTMA) content is increased from zero to 21.91%. The psuedo-Young’s modulus then continues to increase with  increasing weight percentages of poly(HDDA). The poly(HDDA) content corresponding to the modulus minimum falls near the high end of the percolation transition concentration range shown in Figure 3. The abnormal modulus decrease may be caused by the unreacted and locally polymerized monomers that increase the total film thickness without contributing much to the total elastic modulus [17-19].

3.4. Mechanical behavior of IPN composite films after release

The stress-strain behavior of the IPN composite films after they were released to free-standing were measured. In the free-standing composite films, the VHB network is under tension due to preserved prestrain. Figure 3 shows the additive network  under compression due to the contraction of the films from a 400% prestrain to the preserved prestrain.

(a) VHB-poly(HDDA)                        (b) VHB-poly(TMPTMA)

Figure 9. Hydraulic pressure versus stretch ratio curves for (a) different concentrations of poly(HDDA) and (b) poly (TMPTMA) after being released from prestrain structure. The numbers in the insets are weight percent for poly(1,6-hexanediol diacrylate) in the composite films.

Figure 9 shows the biaxial stretch ratios by the hydraulic pressure of the prestrain preserved, of free-standing composite films. The results of the VHB-poly(HDDA) and VHB-poly(TMPTMA) are similar to those of the unreleased films shown in Figure 7. The VHB-poly(HDDA) films in Figure 9 (a) seem to be considerably softer than the VHB-poly(TMPTMA) films shown in Figure 9 (b) even with respect to equivalent preserved prestrain. These results could be explained by comparing the bridge-length between functional groups (or crosslinks) (see Figure 2). The flexible hexylene segment in poly(HDDA) makes the network more pliable than that of the TMPTMA, which has a much shorter bridge-length. At small stretch ratios, the VHB-poly(HDDA) films appear much softer than the VHB films without poly(HDDA). However, the IPN films are stiffer when film thickness is considered.

Figure 10. Calculated Young’s moduli of IPN films as a function of weight percentage of additive. The VHB films were biaxially prestrained by 400%, admixed with HDDA or TMP-TMA, cured, and released to free-standing. The moduli were calculated based on =1.03.

As shown in Figure 10, the Timoshenko equation for free-standing composite films was used to calculate the Young’s moduli. The Young’s modulus of non-prestrained VHB 4910 is 181.53 kPa.  Although the Young’s moduli of IPN composite films do not theoretically depend on the weight percentage of poly(HDDA) in the range of 18.3-23.6%, experimental data obtained show that the Young’s moduli of VHB-poly(TMPTMA) films increase rather rapidly with an increasing amount of poly(TMPTMA).

3.5. Actuation of IPN films without external prestrain

To accomplish a complete preservation of the original prestrain, a large amount of additive is required. However, according to passive mechanical analysis, the films with a larger amount of additive would require a much higher energy to obtain large strains (stretch ratio greater than 1.2). The electrically-induced strains would thus be diminished. To support this argument, the electrical strains of free-standing IPN composite films with various amounts of additive were measured. The results are displayed in Figure 11. The strains were measured with increasing driving voltage until dielectric breakdown is reached in the film.

(a) VHB-poly(HDDA)                      (b) VHB-poly(TMPTMA)

Figure 11. Electric field induced strain (area expansion) for (a) VHB-poly(HDDA) and (b) VHB-poly(TMPTMA) films containing various concentrations of additive. The films have been released from the prestrain structure and mounted, at minimal external stress, onto a diaphragm structure for the strain measurement.

As expected, the IPN composite films show lower electrically-induced strains with increasing amounts of additive. This is consistent with the increasing film stiffness observed with increasing additive content at large stretch ratios shown in Figure 9. For the VHB-poly(HDDA) shown in Figure 11 (a), the IPN film with 18.33% poly(HDDA) show the highest electrical strain of 233 %, with a breakdown electric field of 300 MV/m. Its preserved prestrain was found to be 275%. The IPN formed film with 35.94% poly(HDDA) is too rigid to obtain high strain. The VHB-poly(TMPTMA) film with 9.7 wt% additive exhibits a preserved strain of 243.75%, with a  maximum electrically-induced strain of 300%. This result deserves further attention. As shown in Figure 9, although the VHB-poly(TMPTMA) film is more rigid than the VHB-poly(HDDA) film with 18.33 wt% of additive, it exhibits a higher electrical strain. It also has a dielectric breakdown strength of 420 MV/m, substantially higher than that of the VHB-poly(HDDA) film. The improved breakdown field in VHB-poly(TMPTMA) film  can be attributed to the more uniform IPN film morphology and the smaller, fewer cracks present in the additive network (compare Figure 4 (b) and (c)). The rather rough surface and submicron-size cracks in the VHB-poly(HDDA) shown in Figure 4 (b), are responsible for the diminished dielectric strength [20]. The electrically induced strain up to 300% in area is comparable to that of the  highly-prestrained, VHB 4910 films. Figure 12 shows the expansion of a diaphragm actuator using free-standing IPN composite films.

VHB-poly(HDDA)

VHB-poly(TMPTMA)

Figure 12. Diaphragm actuators based on IPN composite films. The films are under a constant, small tension maintained by the air pressure in the diaphragm chamber. (a) VHB-poly(HDDA) containing 18.3 wt% HDDA at 0 MV/m, (b) at 300 MV/m, (c) VHB-poly(TMPTMA) film containing 9.7 wt% TMP-TMA at 0 MV/m, (d) at 420 MV/m.

4. Conclusion

High performance interpenetrating polymer networks based on VHB acrylic elastomers, poly(HDDA), and poly(TMPTMA) have been prepared for electroelastomer artificial muscles. The interpenetrating polymer networks are formed in the highly prestrained VHB acrylic elastomer network to effectively support the prestrain of the VHB network. In the free-standing composite films, the VHB network is under tension, balanced by the poly(HDDA) or poly(TMPTMA) network that is in compression. The preserved prestrain of the VHB network can be varied in a wide range depending on the concentration of functional diacrylate or trimethacrylate monomers. Small amounts of additive monomers  are not effective to lock the prestrain, while large amounts can substantially increase the stiffness of the IPN films at large strains. The VHB-poly(HDDA) composite film with 18.3 wt% poly(HDDA) preserves 275% prestrain of the acrylic elastomer and exhibits an electrically-induced strain up to 233% in area expansion, whereas the VHB-poly(TMPTMA) composite film with 9.7 wt% poly(TMPTMA) retains 243.75% prestrain and exhibits a 300% electrical strain. Studies are underway to use such “prestrain-less” electroelastomer films to fabricate new dielectric elastomer actuators without (or minimal) supporting structure/mass and to deliver greater actuator performance.

Acknowledgements

This work was financially supported by the Office of Naval Research, ONR Contract No. N00014-05-C-0005.

References

[1] Bar-Cohen Y ed. 2004 Electroactive Polymer (EAP) Actuator as Artificial Muscles: Reality, Potential, and Challenges Second Edition (Bellingham WA: SPIE Press)

[2] Pelrine R, Kornbluh R and Kofod G 2000 High-Strain Actuator Materials Based on Dielectric Elastomer Advanced Materials 12 1223-1225

[3] Perine R, Kornbluh R, Pei Q and Joseph G 2000 Hight-Speed Electrically Actuated Elastomers with Strain Greater than 100% Science 287 836-839

[4] Meijer K, Rosenthal M and Full R J 2001 Muscle-Like Actuators? A Comparison between Three Electroactive Polyme Proc. SPIE Int. Soc. Opt. Eng. 4329 7-15

[5] Kofod G, Kornbluh R, Pelrine R and Sommer-Larsen P 2001 Actuation Response of Polyacrylate Dielectric Elastomer Proc. SPIE Int. Soc. Opt. Eng. 4329 141-147

[6] Sommer-Larsen P, Kofod G, Shridhar M H, Benslimane M and Gravesen P 2002 Performance of Dielectric Elastomer Actuators and Materials Proc. SPIE Int. Soc. Opt. Eng. 4695 158-166

[7] Kornbluh R, Perine R, Pei Q, Heydt R, Stanford S, Oh S and Eckerle J 2002 Electroelastomer: Application of Dielectric Elastomer Transducers for Actuation, Generation and Smart Structures Proc. SPIE Int. Soc. Opt. Eng. 4698 254-270

[8] Pei Q, Rosenthal M, Stanford S, Prahlad H and Pelrine R 2004 Multiple-Degrees-of-Freedom Electroelastomer Roll Actuators Smart Mater. Struct. 13 N86–N92

[9] Ha S M, Yuan W, Pei Q, Pelrine R and Stanford S 2006 Interpenetrating Polymer Networks for High-Performance Electroelastomer Artificial Muscle Advanced Materials 18 887-891

[10] Ha S M, Yuan W, Pei Q, Pelrine R and Stanford S 2006 New High-Performance Electroelastomer Based on Interpenetrating Polymer Networks Proc. SPIE Int. Soc. Opt. Eng. 6168 616808

[11] Sperling L H 1981 Interpenetrating Polymer Networks and Related Materials (New York: Plenum)

[12] Li Q, Lieh J and Mayer A 2005 Large Deflection of Laminated Circular Plates with Clamped Edge and Uniform Loading J. Process Mechanical Engineering 219 83-88

[13] Manias E, Chen J, Fang N and Zhang X 2001 Polymer Micromechanical Components with Tunable Stiffness Appl. Phys. Lett. 79 1700-1702

[14] Stauffer D and Ahrarony A 19 Introduction to Percolation Theory (New York: Taylor & Francis)

[15] Spering L H 1986 Physical Polymer Science (New York: John Wiley & Sons)

[16] Timoshenko S 1959 Theory of Plates and Shells (New York: McGraw-Hill Book Co.)

[17] Fan J, Hu X and Yue C Y 2001 Interpenetrating Polymer Networks Based On Modified Cyanate Ester Resin Plastics, Rubber and Composites 30 448-454

[18] Sperling L H and Mishra V 1995 The Current Status of Interpenetrating Polymer Networks Polymers for Advanced Technologies 7 197-208

[19] Pierre-Gilles de Gennes 1979 Scaling Concepts in Polymer Physics (New York: Cornell University Press)

[20] Lucas J R 2001 High Voltage Engineering revised edn (Open University of Sri Lanka)

# Text boxes

(b)

(c)

(c)

(a)

(b)

(c)

(a)

(d)

(d)

(a)

(b)