Appendix A

LHC Interaction Region Quadrupole

Cold mass weld coupon tests

Weld Inspections on FNAL Q2a and Q2b Quadrupoles

Agreement with CERN Safety Requirements

The schedule of tests for qualification and for production of Fermilab Q2a and Q2b quadrupoles is consistent with the agreements reached between CERN, Fermilab, and the US LHC Accelerator Project Office on 19 April 2000 (meeting report dated 28 April 2000 issued by M. Bona,).

Three sets of tests are discussed below:

- Table 1 lists the tests that support the qualification of weld materials and weld process.  These tests were proposed by Fermilab in March and finalized in the meeting on 19 April 2000.

- Table 2 lists the tests according to ASME Section IX for qualification and re-qualification of welders (both equipment and personnel).  Welders that are inactive for a period of six months must be re-qualified through the tests listed in Table 2.

- Table 3 lists the tests to be performed on each series production magnet.  These tests support the requirements of ASME Section VIII and Fermilab rules for the operation of pressure vessels.

Qualification of the Weld Materials and Process

The qualification of the weld materials and weld process for the Fermilab Q2a and Q2b magnets takes an approach analogous to that used by Brookhaven National Laboratory (BNL) for the RHIC magnets and accepted by CERN for the BNL beam separation dipoles.  Fermilab provided documents to CERN in March 2000 describing the design and analyzing the operational limits of the weld.  These documents were accepted by CERN as stated in the report of the 19 April 2000 meeting between CERN and Fermilab.

Qualification testing will be performed on a mechanical model.  The weld geometry and weld process are identical to that of prototype and production magnets.  Coupons will be taken from the mechanical model and weld sample tests as described in the Table 1 will be conducted to support qualification of the weld materials and process.

In addition to the tests performed on the mechanical model, one of the prototypes will have strain gauges applied.  The gauges will be applied before welding of the cold mass skin to verify the level of stress obtained after welding.  Since the vertical gap between the two iron halves remains closed, the evolution of stresses during cool-down does not need to be monitored.

#### Table 1 Weld Qualification Tests: The tests are conducted according to standards used by FNAL.  Test standards used by CERN, which are comparable but not necessarily identical, are listed for reference.  Weld samples are taken from the mechanical model.  All tests are conducted at room temperature unless otherwise noted.

| Qualification Tests | CERN Standard (for reference only) | FNAL Standard | Note |
| --- | --- | --- | --- |
| Tests on Mechanical Model |  |  |  |
| Visual inspection | EN 970 (test) ISO 5817 (acpt) | FNAL ES-369730 | 1 |
| Delta ferrite test |  | AWS A 4.2 (test) | 2 |
| Tests on Weld Samples |  |  |  |
| Visual examination (macro-examination) |  | ASME Sec. IX, QW-302.4 (test) ASME Sec. IX, QW-194 (acpt) | 3 |
| Transverse tensile test 300 K, 77 K, and 4.2 K | EN 895 (test) EN10002-1 (acpt) | ASTM E 8M (test) ASME Sec IX, QW-153 (acpt) | 4 |
| Impact test 300 K, 77 K, and 4.2 K 3 required in heat affected zone 3 required in welded metal | EN 875 (test) ISO 148 (test) EN 10045-1 (test) | ASTM E 23-96 (test) ASME Sec. VIII, UG-84 (acpt) | 5 |
| Fracture toughness test 300 K, 77 K, and 4.2 K |  | ASTM E 1737-96 (test) | 6 |
| Radiographic (x-ray) test |  | ASME Sec. IX, QW-302.2 (test) | 7 |

Notes on tests listed in Table 1 – Weld Qualification Tests

- Visual inspection: Each pass of each weld will be visually inspected along its full length.  Fermilab will specify the acceptance in a written engineering specification.

- Delta ferrite test: This test was proposed by Fermilab to support qualification.  AWS A 4.2 is a standard of the American Welding Society.  Delta ferrite measurements are taken of the weld at discrete points along the magnet.  Fermilab will establish a written standard for the spacing between discrete points and the maximum acceptable ferrite number for the GTAW process.

- Visual examination: This test was proposed by Fermilab and required by ASME Sec. IX to check the depth of weld penetration.

- Tensile test: This test was proposed by Fermilab to support qualification.  Uniaxial tensile testing on welds at 300 K, 77 K, and 4 K will be conducted to determine the yield strength and ultimate tensile strength of the weldments.  According to ASME Section IX (QW-153) the weld specimens must have an ultimate strength not less than the minimum specified strength of the base material.  For 304 stainless steel, Table UHA gives a minimum required tensile strength of 550 MPa.

- Impact test: This additional test was included by agreement between CERN and Fermilab.  Charpy V-notch specimens will be impact tested at 300 K, 77 K, and 4.2 K. Three specimens from the weld and three from the heat affected zone will be tested at each temperature. According to UG-84, welded specimens must have a Charpy impact energy not less than the minimum specified impact energy of the base material.  For a minimum tensile strength of 550 MPa, the required average impact energy of three samples is 27 J/cm2 with a minimum impact energy of any one of the specimens of 20 J/cm2.

- Fracture toughness test: This test was proposed by Fermilab to support qualification at cryogenic temperatures.  Notched specimens will be tested at 300 K, 77 K, and 4.2 K to characterize the toughness of the weld material.  From the fracture mechanics analysis submitted to TIS (TD-00-025), we require a weld material with fracture toughness greater than 85 MPa (m.

- Radiographic test: This test was added by Fermilab to further support qualification.  The weld samples that will be taken from the mechanical model will be inspected radiographically.  ASME Section IX will be used as a guide for the test and inspection of the samples.  The radiographic inspector will be asked to identify rounded indications and linear indications (cracks, incomplete fusion, elongated inclusions).  The inspector will be asked to estimate their sizes.

Welder Qualification and Re-qualification

Qualification and re-qualification of the welding equipment and personnel will be according to the requirements of ASME Section IX.  Re-qualification is most often required due to a period of inactivity of six months or more, usually resulting from an interruption in production.  Coupons will be taken from run-offs made during welder qualification (or re-qualification).  Tests as described in the Table 2 will be conducted to support welder qualification or re-qualification.

Table 2 Welder qualification and re-qualification tests.  The tests are conducted according to standards used by FNAL.  Test standards used by CERN, which are comparable but not necessarily identical, are listed for reference.  All tests are done at room temperature.

| Welder Qualification Tests | CERN Standard (for reference only) | FNAL Standard | Note |
| --- | --- | --- | --- |
| Tests on Weld Samples |  |  |  |
| Visual examination |  | ASME Sec. IX, QW -302.4 (test) ASME Sec. IX, QW-194 (acpt) | 1 |
| Bend test | EN 910 (test) ISO 7438 (test) | ASME Sec IX QW-462.3 (b) (test) ASME Sec IX QW-163 (acpt) | 2 |

Notes on tests listed in Table 2 – Welder Qualification Tests

- Visual examination: This test is proposed by Fermilab and required by ASME Sec. IX to check the depth of weld penetration.

- Bend test: This test is required by ASME Section IX to determine the degree of soundness and ductility of weld joints.  ASME requires the bend specimens have no open defects in the weld or heat affected zone exceeding 1/8 in (3.2 mm), measured in any direction on the convex surface of the specimen after bending.

Production Testing

No destructive tests are required for the Q2a and Q2b magnets. The production welds will be tested as indicated in Table 3.

The four run-offs from each production magnet will be saved and archived.  Each run-off will be approximately 150 mm in length along the weld and labeled with the magnet number and location.  The run-offs will become included with the engineering file supplied with each magnet.

Table 3 Production tests on series Q2a and Q2b quadrupoles.  The tests are conducted according to standards and procedures used by FNAL.  Test standards used by CERN, which are comparable but not necessarily identical, are listed for reference.  All tests are conducted at room temperature unless otherwise noted.

| Production Tests | CERN Standard (for reference only) | FNAL Standard | Note |
| --- | --- | --- | --- |
| Tests on Delivered Units |  |  |  |
| Visual inspection | EN 970 (test) ISO 5817 (acpt) | Fermilab ES-369730 | 1 |
| Delta Ferrite Tests |  | AWS A 4.2 (test) | 2 |
| Leak check |  | Fermilab ES-107240 | 3 |
| Pressure test |  | Fermilab ES&H 5034 ASME Sec. VIII , UG-100 | 4 |

Notes on tests listed in Table 3 – Production Tests

- Visual inspection: Each pass of each weld will be inspected along its full length.

- Delta ferrite test: This test was proposed by Fermilab to support qualification and will be conducted on each production unit.  AWS A 4.2 is a standard of the American Welding Society.  Delta ferrite measurements will be taken of the weld at discrete points along the magnet. Fermilab will establish a written standard for the spacing between discrete points and the maximum acceptable ferrite number for the GTAW process.

- Leak check: This test is required by Fermilab.

- Pressure test: This test is required by ASME Section VIII Division 1.  On 1 July 1999 ASME reduced the pneumatic pressure test requirement from 1.25 to 1.1 times design pressure.  Fermilab will continue to pneumatically test each production cold mass to 1.25 design pressure to remain consistent with current FNAL and CERN requirements.

MATERIALS RESEARCH & ENGINEERING, INC.

4820 N. 63rd Street, Suite 102

Boulder, Colorado  80301

(303) 530-9090, (303) 530-9092 FAX

http://www.henge.com/~mre

E-mail: mre@henge.com

Tension tests, charpy impact, AND Fracture Toughness Evaluation of 308L and 316L Weld samples at room temperature, 77k, and 4.2k

(PO: 532752)

FINAL REPORT

Prepared for

## Deepak R. Chichili, Ph.D.

FERMI National Accelerator Laboratory

Technical Division

M/S 316, P.O. Box 500

Batavia, IL  60510

Phone: (630) 840-4710

Fax: (630) 840-8036

December 18, 2000

Prepared by:		___________________________________

John M. Arvidson, Chief

___________________________________

# Michael Goyack, Engineer

___________________________________

Kenneth Blount, Lead Engineer

GENERAL INFORMATION:

Tension, fracture toughness, and Charpy impact specimens were machined from 308L and 316L weld sections provided by FERMI National Laboratory.  Initial inspection of the weld of the 308L panel, shown in Figure 1, confirmed that the weld penetration was satisfactory for machining the requested test specimens.  Inspection of the 316L material revealed similar satisfactory weld penetration.  Periodic examinations during the machining process confirmed the weld penetration depth throughout the panel.

Figure 1. Weld Penetration at the 0-Inch Location of the 308L Panel.

Figures 2 and 3 present the specimen locations for the 308L and 316L panels, respectively.  For the 308L panel, two specimens, COW Charpy #9 and HAZ Charpy #6, were machined from areas to either side of the section that tension specimens 1 through 5 were taken from.  The approximate locations of the FERMI marked sections of A, B, C, and D are indicated.  Three HAZ fracture toughness specimens could not be machined due to the narrow area indicated by the red circle in Figure 1.

Tension tests were carried out on a 20-kip electro-mechanical Instron test frame.  Load and displacement data were recorded by both computer and plotter during each test.  The speed of testing was 0.05 in/min.  During the cryogenic tests, the temperature was controlled with an accuracy of ±2°F using liquid nitrogen (77K) and liquid helium (4K) as the cryogenic media.  A calibrated type-E thermocouple was used to verify the temperature control.  The tension specimen geometry is shown in Figure 4.

Charpy impact tests were performed on a Tinius Olsen impact test machine.  Due to the geometry constraints of the weld section, a 0.194-inch thick impact specimen was employed.  The Charpy impact specimen geometry is shown in Figure 5.

Fracture toughness tests were conducted on weld and heat affected zone specimens.  The specimen geometry, prescribed by ASTM E1820, is shown in Figure 6.  Due to the material constraints, a sub-sized compact tension specimen was machined (W=0.6976-inches).  ASTM recommends testing a specimen with a W of 2.0-inches.  Cryogenic tests were carried out in a cryostat with displacements being measured with cryogenic extensometers.  The temperature was controlled with an accuracy of ±2°F, using liquid nitrogen (77K) and liquid helium (4K) as the cryogenic media.  A calibrated, type-E thermocouple was used to verify the actual temperature and to maintain the temperature control.  Strain extensometers, attached to the specimen at the load line, were used to measure the crack opening displacement (COD).  Fracture toughness tests were performed on a 22-Kip, computer controlled, hydraulic Instron test frame.  Specimen precracking was performed in accordance with ASTM E1820.  Specimens were side-grooved prior to performing the J-test.

The tension specimens for the 308L and 316L weld material are shown in Figures 7 and 8, respectively.  Figure 9 shows all Charpy impact specimens, and Figure 10 shows a representative close-up of one Charpy specimen.  Figure 11 shows representative fracture toughness specimens for both the 308L and 316L weld and HAZ sections.

RESULTS

Tension test results for the 308L weld sections are presented in Table 4, and data for the 316L weld section is in Table 5.  The load versus displacement data for the 308L tension tests appears in Figures 12 through 20.  Similar curves for the 316L tension tests appear in Figures 21 through 23.  The double curves seen in Figures 21 and 22 were the result of the specimens being retested due to load pin failure.  Ultimate tensile strength values were calculated from the minimum cross-sectional area measured before testing.  Specimen T3085 failed in the center key section, but the failure stress for the specimen is based on the minimum area, which was not the center key section.

Ultimate tensile strength values for the 308L specimens did not display a large degree of variability at any of the three test temperatures.  The average UTS value at room temperature was 100.6-ksi.  For the 77K tension tests, the average UTS value was 147.3-ksi, and 150.7-ksi for the 4K tension tests.

The 316L material exhibited a higher amount of variability in the tension test results than was seen in the 308L material. The average UTS value for the material was 154.1-ksi at 4K.  The tension specimen geometry was chosen for conducting the tests within the geometric constraints of the weld section.  A larger grip section is required to accommodate a larger pin diameter, which would eliminate the premature failure of the load pin that occurred during the 316L tests.

Charpy impact data appears in Tables 3 through 5 for the 308L weld material, the 308L heat affected zone material, and the 316L weld material, respectively.  Neither the 308L weld or HAZ material nor the 316 weld material exhibited a large degree of variability in the impact data within individual test temperatures.

Post failure inspection of the fracture toughness samples revealed a normal precrack surface, with no unusual off-angle, out-of-plane behavior.  However, the crack development during the J-testing proved to be difficult in most cases.  The high ductility of the material combined with the subsized specimen geometry resulted in excessive crack blunting during the tests.  Load versus COD data monitored during the J-testing appeared normal, but pop-in events were observed during several of the tests.

Because of the difficulties in achieving stable crack growth during the J-tests, post-test data analysis was performed manually and test results are reported as JQ values only.  J-values presented in this report should be used only as a comparison of each material/location tested.  They should not be used for comparison or analysis outside the scope of this report.  Materials Research and Engineering, Inc. highly recommends that additional tests be performed on standard sized specimens to obtain accurate JIC values.  Results for the J-tests appear in Table 9.  Figure 24 shows the trends of the JQ values as a function of temperature.  The JQ values for each material increased, as expected, as the test temperature was increased.

RECOMMENDATIONS

For the tension and Charpy impact specimens, additional tests must be performed before any opinion can be formed on the precision and accuracy of the data.  Multiple specimens tested at a given temperature help determine the scatter band for a given material.  Three specimens tested per material type and test temperature are adequate for determining the trends in the response of the material with changing temperature, but are not adequate for performing a meaningful statistical analysis. To achieve a better representation of the material, specimens should be chosen from different lots of material and from different locations within each lot.

MRE recommends that additional J-tests be conducted on standard sized fracture toughness samples with a width (W) of 2.0-inches.  Specimens of this geometry are more assured of yielding valid results.  Another important recommendation is the inclusion of additional test specimens (six to ten) at each temperature to obtain statistically meaningful J-value averages.  This will greatly improve the understanding of J-value versus temperature, and will help to quantify the temperature dependence effect of fracture toughness over the entire range of selected test temperatures.

Figure 2.  308L Panel Specimen Locations (dimensions in inches).

Figure 3.  316L Panel Specimen Locations (dimensions in inches).

Figure 4.  Tension Specimen (dimensions in inches).

Figure 5.  Charpy Impact Specimen (dimensions in inches).

Figure 6.  Sub-Sized Compact Tension JIC Specimen (dimensions in inches).

Figure 7.  308L Tension Specimens.

Figure 8.  316L Tension Specimens.

Figure 9.  Charpy Impact Specimens.

Figure 10.  Representative Charpy Impact Specimen.

Figure 11.  Representative Fracture Toughness Specimens.

Table 4.  Tensile Data for 308L Material.

Notes:

- Specimen T3085 failed in the center section of the key.

Table 5.  Tensile Data for 316L Material.

Figure 12.  308L Tension Test at Room Temperature; Specimen #1.

Figure 13.  308L Tension Test at Room Temperature; Specimen #2.

Figure 14.  308L Tension Test at Room Temperature; Specimen #3.

Figure 15.  308L Tension Test at 77K; Specimen #4.

Figure 16.  308L Tension Test at 77K; Specimen #5.

Figure 17.  308L Tension Test at 77K; Specimen #6.

Figure 18.  308L Tension Test at 4K; Specimen #8.

Figure 19.  308L Tension Test at 4K; Specimen #9.

Figure 20.  308L Tension Test at 4K; Specimen #10.

Figure 21.  316L Tension Test at 4K; Specimen #A.

Figure 22.  316L Tension Test at 4K; Specimen #B.

Figure 23.  316L Tension Test at 4K; Specimen #C.

Table 6. Charpy Impact Data for 308L Weld Material.

Table 7. Charpy Impact Data for 308L Heat Affected Zone Material.

Table 8. Charpy Impact Data for 316L Weld Material.

Table 9.  Fracture Toughness Data.

Figure 24.  Fracture Toughness Versus Temperature.