ANALYTICAL RESULTS FOR MINE DUMP SAMPLES AND LEACHATE SOLUTIONS, UPPER ANIMAS RIVER WATERSHED, SAN JUAN COUNTY, COLORADO

by  David L. Fey1, J. Thomas Nash1,

Douglas B. Yager, and George A. Desborough1

# Open-File Report 00-0338

2000

This report is preliminary and has not been reviewed for conformity with U.S. Geological Survey editorial standards and stratigraphic nomenclature.  Any use of trade, product, or firm names is for descriptive purposes only and does not imply endorsement by the U.S. Government.

U.S. DEPARTMENT OF THE INTERIOR

## U.S. GEOLOGICAL SURVEY

1 Denver, Colorado

This report contains text, linked to Excel spreadsheet data files.  The following list provides the names and describes the contents of the files comprising this report.

LIST of FILES

1:  SDCHEMOF.DOC  Text of Open-File Report:  MS-WORD format

2:  SDCHEMOF.PDF  Text of Open-File Report:    Adobe PDF format

3:  SDSITE.xls  Sample localities and descriptions:  EXCEL format

4:  SDGX97.xls  Total-digestion analyses of mineralized rock samples by

ICP-AES: EXCEL format

5:  SDPL97.xls  Analyses of passive leach solutions (1997) by ICP-MS: EXCEL format

6:  SDTL97.xls  Analyses of EPA-1312 (SPLP) solutions by ICP-AES: EXCEL format

7:  SDPL99.xls  Analyses of passive leach solutions (1999) by ICP-MS: EXCEL format

8:  QAQC.xls  Compilation of analytical qc data: EXCEL format

Note: When linking to an Excel file, your web browser will launch Excel, which will automatically open the referenced file.  To return to the text file, use the browser’s “back” button.  This will return you to the first page of the text file.

## Table of Contents

Introduction										1

Sampling Methods									3

Sample Preparation									3

Analytical Methods									3

Discussion of EPA-1312 leach and passive leach results				5

Explanatory notes for Excel files of analytical results				6

References Cited									8

Figure 1.  Map of Upper Animas Watershed study area, with mine-waste site localities plotted, without labels.  Coordinates and descriptions are given in Table 1		2

Table 1.  Sample Identification numbers, list of EXCEL files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions.  This is the same table as contained in the Excel file SDSITE.xls				10

## INTRODUCTION

This report provides analytical results for samples of mine dumps, mill tailings, and some unmined altered rocks.  The analyses are intended to be used to characterize mineralized rocks in the Upper Animas River watershed.  This study represents one component in the U.S. Geological Survey (USGS) program of integrated geological-hydrological-biological-chemical studies underway in the Upper Animas River watershed as part of the Abandoned Mine Lands Initiative (AMLI) to provide Federal land management agencies a scientific rationale for cost-effective restoration of public lands affected by historic mining (Buxton and others, 1997; Nimick and von Guerard, 1998).  Information reported here is part of the mine site, or metal source, component of the project.  Other personnel on the AMLI team are investigating diverse aspects of geology, geochemistry, hydrology, and biology that are pertinent to establishing pre-mining and existing conditions, as well as attainable reclamation goals.

Field studies in the summers of 1997 and 1998 focussed chiefly on historic mines and prospects identified by others as being partly or entirely on public lands administered by the U.S. Bureau of Land Management (BLM) or the USDA-Forest Service (USFS); a limited number of sites on private property were studied for comparison when the owner provided access and permission to sample.  Previous reports (Nash, 1999a; 1999b) presented interim recommendations for establishing priorities or rankings of mine sites for removal or remediation.  These two reports, OFR-99-170 and OFR-99-323, have been included in Nash (2000), a CD-ROM compilation of descriptions and photos of mines, mine waste dumps, mills, and mill tailings and interim interpretations of their significance as sources of acid or metals in the upper Animas River watershed.

Acknowledgements:  Many people with the BLM and USGS have been helpful during this study, in particular Barbara Hite, Stephanie Odell, and Rob Robinson of the BLM, and Daryl Gussey of the USFS.  They have provided helpful information and suggestions.  The friendly advice of the many scientists on the USGS AMLI team has expanded the breadth and depth of our geochemical investigations, but the authors are solely responsible for any errors reported here.

## METHODS OF STUDY

Field and laboratory studies for this investigation utilized methods that were developed for the AMLI program, and efforts have been made to maintain consistency among the scientists working in the Colorado (Animas watershed) and Montana (Boulder River watershed) study areas.  In the Upper Animas study area, sites were first selected for study using information gathered by previous investigators who had made inventories for the BLM (Hite, 1995) or U.S. Forest Service (Lovekin and others, 1997).  Because of the limited amount of field time available in 1997 and 1998, and the large number of potential sites, we focussed on sites that were reasonably accessible, within two miles of major streams, and had waste piles or dumps larger than about 70 cubic yards.  Of the more than 500 sites identified by previous investigators, the majority are smaller than 70

cubic yards, and were considered unlikely to be significant contributors to water quality problems in the watershed (Nash, 1999a; 1999b).  These sites were not sampled and are not included in this study.  Site localities were identified on USGS 1:24,000 topographic

maps and recorded using a standard global position system (GPS) instrument with an estimated accuracy of (100 meters (based on real tests).  Figure 1 shows the upper Animas Basin study area with the localities of mine dumps sampled.  The coordinates and sample names are given in the Excel file SDSITE.xls, and Table 1 of this text.

### Sampling Methods

On-site work included a brief description of the site, rock types, rock alteration and ore mineralogy, a measurement or estimate of size of the dump pile, and the collection of a representative sample of the entire dump or waste pile surface.  Samples of waste-rock from mine dumps were taken from more than 150 inactive mine sites in the upper Animas River study area.  Material was collected from 30 or more subcells, each having an area of about one half square meter, across the top and sides of the dumps to a depth of about 5 cm using four to six randomly selected 50-80 g scoops.  The material was mixed, and a portion passed through a 2-mm sieve to yield about 100 g from each subcell.  The minus-2 mm fraction was saved, as this was deemed to be the most reactive to water in short-term exposures (Desborough and Fey, 1997; Nash, 1999a; 1999b; Smith and others, 2000).  The composite sample, split from the total sieved material, amounted to one to two kg.

Samples with field numbers starting with 97ABS were collected by Fey, those starting with A97W were collected by Desborough, and those starting with NA were collected by Nash.  In the series of samples collected by Nash, the third letter indicates the type of material: D, dump; F, iron flocculate-dominated sample; H, drill hole cuttings; G, smelter slag; R, unmined altered rock; S, soil; and T, mill tailing.  Unless otherwise noted, all dump samples were sieved to minus-2 mm.  Information on the sample sites, their localities, and which sample analyses are contained in which data spreadsheet are in an Excel spreadsheet labeled SDSITE.xls that can be read by most spreadsheet programs.  Not all samples were subjected to the complete suite of analytical chemistry methodology.  This information is also in Table 1 of this text.

#### Sample Preparation

In the laboratory, the composite samples were dried at 40o C, split with a Jones splitter, and recombined several times to achieve thorough mixing.  Splits from the homogenized material were made for:  1) ICP-AES total-digestion analysis, 2) EPA-1312 leach test, 3) passive leach test, and 4) net acid production (NAP) test.  Splits for the EPA-1312 leach and the passive leach did not require further preparation; splits for total-digestion analysis and for NAP measurements were ground in a vertical pulverizer with ceramic plates to minus-200-mesh (75 microns).

### Analytical Methods

Total-digestion ICP-AES analysis for 30 elements

A 0.2 g. portion of minus-200-mesh material was subjected to a mixed-acid total digestion using HCl, HNO3, HCLO4 and HF acids (Briggs, 1996).  The resulting solution was analyzed for 40 elements using inductively coupled-plasma atomic emission spectroscopy (ICP-AES); 30 elements are reported in this report.  This analysis was performed on samples collected in 1997, but not on later samples.  The analytical results are contained in the spreadsheet program SDGX97.xls.

EPA-1312 Leach Method (Synthetic Precipitation Leach Procedure-SPLP)

A 100-g. sample of mine waste was placed in a 2.3L polyethylene bottle.  Two liters of extract solution were added, resulting in a 1:20 sample/extract ratio, with 300 cc of head space.  The SPLP method mandates that an extract solution of pH 4.2 be used on soils from east of the Mississippi River, and solution with pH of 5.0 be used on soils from west of the Mississippi River, and the more acidic pH 4.2 solution be used on mine-waste material.  Because all of these samples were mine waste or altered rock, we used the pH 4.2 extract solution.  The extract solution was made from de-ionized water acidified to a pH of 4.2 with a one percent solution of 60/40 H2SO4/HNO3.  The capped bottles were placed on an end-over-end (tumbling) rotating agitator at 30 rpm for 18 hours.  The leachates were then pressure-filtered through a 142 mm diameter-0.7 micron glass-fiber filter (US-EPA, 1986).  A 100 mL aliquot of filtered solution was acidified with ultra-pure HNO3  for analysis for 25 elements by ICP-AES (Briggs and Fey, 1996) and for sulfate by ICP-AES as sulfur.  Conductivity and pH were determined on the bulk filtered leachate.  This leach and analysis was performed on samples collected in 1997, but not on later samples.  The analytical results for the EPA-1312 (SPLP) leach are contained in the spreadsheet program SDTL97.xls.

Passive Leach Method

A 100-g. sample of mine waste was exposed to 2L of laboratory de-ionized water (pH of 5.0 (0.2) in an open 4L beaker.  Samples were left at rest for one hour, and then gently stirred for five seconds to prevent stratification of the leachate.  The pH of the the leachate of the 1997 samples, and the pH and conductivity of the leachate of the 1999 samples was (were) measured after 24 hours.  A 60 mL aliquot was then filtered through a Gelman 0.45-micron filter using a disposable syringe (Desborough and Fey, 1997), acidified with ultra-pure HNO3, and refrigerated prior to analysis by inductively coupled-plasma-mass spectroscopy (ICP-MS).

Filtered, acidified solutions from the passive leach tests were analyzed by ICP-MS because this method provides information on more than 40 elements of possible interest, with good results to one part per billion (ppb, or microgram per liter), or lower for some elements (Crock and others, 1999).  All of the samples of this study were subjected to the passive leach test.  Samples collected in 1997 and processed in 1998 were analyzed by a commercial laboratory (results contained in spreadsheet file SDPL97.xls).  This file also contains pH but not conductivity measurements of the passive leach solutions.  Samples collected in 1998 and processed in 1999 were analyzed with a similar instrument in the USGS laboratories in Lakewood, Colorado (results contained in spreadsheet file SDPL99.xls).  This file includes pH and conductivity measurements of the passive leach solutions.  Replicate samples and standards were submitted with the leachates to evaluate precision and quality control.

Results of ICP-MS analyses of leachate solutions are best considered semi-quantitative, as is well understood by geochemists who routinely use this method for solutions of highly variable composition.  As demonstrated by Fey and others (1999), data from analyses of leachates are inherently less reproducible than those from total digestion analyses. Our laboratory-produced solutions span a wide range in pH, conductivity, and elemental composition, and one should not expect precision to be constant across five orders of magnitude of concentration.  For base metals such as copper, lead, and zinc, the precision is about (20 percent for solutions whose concentrations resemble typical surface waters; the precision is lower for solutions whose concentrations are 1,000 times or more higher than normal surface waters.  High and very high concentrations are clearly delineated from low concentrations, and the semi-quantitative nature of the results is appropriate for these tests.  The file QAQC.xls included in this report presents data for duplicates, blanks, and standards for the ICP-40 element method, the EPA-1312 method, and the passive leach method.  Further comments are made elsewhere (Nash, 1999a; 1999b).

Net Acid Production (NAP) method

A 1.0-gram sample of pulverized, minus-200-mesh material was digested with a solution of 30 percent hydrogen peroxide to oxidize pyrite, thereby producing sulfuric acid (Lapakko and Lawrence, 1993).  This acidic solution reacted with the bulk of the sample, released additional acidity from water-soluble acid salts (such as iron-sulfates), and reacted with acid-consuming minerals such as carbonates, and some non-carbonates (e.g. biotite, chlorite and epidote).  The solutions were heated for one hour, cooled, and filtered.  The acidic filtrate was then titrated to a pH of 7 with 0.1M NaOH.  A calculated  net acid production (NAP) is expressed in terms of kg-equivalent CaCO3 per metric ton of mine waste.  This NAP is meant to represent the net long-term or total potential of a material to produce acid over an unspecified period of weathering.  This test was applied to samples collected in 1997, and the results are contained in the same spreadsheet file as the EPA-1312 leach analyses, SDTL97.xls.

X-ray diffraction (XRD) studies

X-ray diffraction studies were made to determine major minerals in the minus-2 mm sample material.  Detailed results of the XRD studies are not presented here, but a summary indicates that sulfide minerals are common in these samples:  25 percent of the samples contain pyrite (FeS2), 30 percent contain sphalerite (ZnS), and 30 percent contain galena (PbS).  Calcite (CaCO3), an important acid-buffering phase, was detected by XRD in only three samples.

## DISCUSSION OF EPA-1312 (SPLP) LEACH AND PASSIVE LEACH RESULTS

A comparison between the results of the EPA-1312 leach and the passive leach is reported in Fey and others (2000), which discussed the EPA-1312 leach and the passive leach and their application to the same samples as those from 1997 in this report, plus eighteen mine-waste samples from Montana.  In figure 1 of Fey and others (2000), the pH of the passive leach was plotted versus the pH of the EPA-1312 leach.  The data points cluster quite closely around a diagonal line of 1 to 1 correspondence.  The same is true for many of the trace elements presented in the tables of this report.  We applied both leach procedures to samples collected in 1997 (files SDTL97.xls and SDPL97.xls).  However, we did not apply the EPA-1312 leach to the later samples, because using the passive leach procedure is simpler and faster, yields similar results, and more closely simulates the processes that occur at the surface of waste piles exposed to rainwater and snowmelt runoff.  (Fey and others, 2000).

The relation between the net acid production (NAP) and the sum of dissolved metals As+Cd+Cu+Pb+Zn (in (g/L) from the EPA-1312 leach has also been examined (Fey and others, 2000).  The mine wastes studied can be segregated into groups based on their NAP and summed metals, where samples with NAP greater than 10 kg CaCO3 per ton and the above summed metals greater than 5,000 (g/L would rank as having the greatest potential for causing water quality problems.  The passive leach samples discussed in Fey and others (2000) also exhibit a systematic relationship between summed metals and NAP.  Although the passive leach releases a lower concentration of metals, a similar grouping of the waste samples results.  Here, the group with greatest potential for causing water quality problems (highest rank) have NAP greater than 10 CaCO3 and summed metals greater than 3,000 (g/L.  We did not determine the NAP for the later samples, but did perform the passive leach on all samples in this report, and so some measure of ranking can be achieved by using the 3,000 (g/L value for the sum of the metals As+Cd+Cu+Pb+Zn in the passive leach solutions.  Dissolved iron in the EPA-1312 solutions can also be used to delineate wastes with high potential for water quality degradation.  A value of 1,000 (g/L iron in leach solutions can be used to separate the samples, for reasons also discussed in Fey and others (2000).

## EXPLANATORY NOTES FOR FILES OF ANALYTICAL RESULTS

- In the file SDPL97.xls, the number of figures carried in the spreadsheet tends to exceed the significant figures reported by the analyst.  In most cases, only two figures are significant.  The other spreadsheet files have been formatted to present the correct number of significant figures.

- In all files, additional elements may have been determined but not reported here because the results were either at or below the limit of determination (e.g. Cr and Ti in leachates), or the element is not being used in the geochemical characterization of the watershed.

- Explanations for each specific file are included in notes found at the bottom of each file, below the analytical data.  Especially important are the extra characters attached to some field numbers in the file SDPL99.xls, which indicate that additional or unusual steps were taken in the passive leach of those samples.  Some samples were leached for more than the standard 24 hour period.  Those sample leachates carry extra letters including:  B, 48 hour leach period; C, 72 hours; D, 96 hours; G, 168 hours.  Some solutions were collected using different filtering techniques.  The extra character U indicates the leachate was not filtered prior to analysis, and a V indicates the leachate was filtered through a 0.1 micrometer filter instead of the usual 0.45 micrometer filter.  The extra character Y or X indicates a replicate analysis.  Other letter suffixes (e.g. F, L, P, R, S) refer to sample field attributes, and can be ignored.

- In the file SDSITE.xls, sample locations shown were mostly determined by standard GPS (global positioning satellite), with no subsequent corrections.  Some site locations were determined from USGS 1:24,000 topographic maps where the GPS could not operate.  Field tests show that the GPS is accurate to about ( 100 meters in the San Juan mountains.

References Cited

Briggs, P.H., 1996, Forty elements by inductively coupled plasma-atomic emission spectrometry, in Arbogast, B.F., ed., Analytical methods manual for the Mineral Resource Surveys Program, U.S. Geological Survey Open-File Report 96-525, p. 77-94.

Briggs, P.H., and Fey, D.L., 1996, Twenty-four elements in natural and acid mine waters by inductively coupled plasma-atomic emission spectrometry, in Arbogast, B.F., ed., Analytical methods manual of the Mineral Resource Surveys Program, U.S. Geological Survey Open-File Report 96-525, p. 95-101.

Buxton, H.T., Nimick, D.A., and others, 1997, A science-based, watershed strategy to support effect remediation of abandoned mine lands: Proceedings of the Fourth International Conference on Acid Rock Drainage, Vancouver, B.C., p. 1869-1880.

Crock, J.G., Arbogast, B.F., and Lamothe, P.J., 1999, Laboratory methods for the analysis of environmental samples, in G.S. Plumlee and M.J. Logsdon, eds., The Environmental Geochemistry of Mineral Deposits, part A:  Society of Economic Geologists, Rviews in Economic Geology, vol. 6A, p. 265-287.

Desborough, G.A., and Fey, D.L., 1997, Preliminary characterization of acid-generating potential and toxic metal solubility of some abandoned metal-mining related wastes in the Boulder River headwaters, northern Jefferson County, Montana:  U.S. Geological Survey Open-File Report 97-478, 21 p.

Fey, D.L., Unruh, D.M., and Church, S.E., 1999, Chemical data and lead isotopic composition in stream-sediment samples from the Boulder River watershed, Jefferson County, Montana: U.S. Geological Survey Open-File Report 99-575, 147 p.

Fey, D.L., Desborough, G.A., and Church, S.E.,  2000,  Comparison of two leach procedures applied to metal-mining related wastes in Colorado and Montana and a relative ranking method for mine wastes, in Proceedings of the Fifth International Conference on Acid Rock Drainage, May 20-23, 2000, Denver, Colorado, Society of Mining Engineering, Lakewood, Colo., p. 1477-1487.

Hite, B.J., 1995, Abandoned mine land inventory of BLM Administered land in Upper Animas River watershed, Colorado: U.S. Bureau of Mines, report for Colorado State BLM Office, 15 p. plus appendices; data for 304 sites on diskette.

Lapakko, K., and Lawrence, L.W., 1993, Modification of the net acid production  (NAP) test.  Paper presented at the Seventeenth Annual British Columbia Mine Reclamation Symposium, May 4-7 at Port Hardy, B.C.

Lovekin, J.R., Satre, M.J., Sheriff, W.M., and Sares, M.A., 1997, USFS-Abandoned mine land inventory project final summary report, San Juan National Forest, Columbine Ranger District:  Colorado Geological Survey, 45 p. plus tables.

Nash, J. T., 1999a, Geochemical investigations and interim recommendations for priority abandoned mine sites on U.S.D.A. Forest Service lands, Mineral Creek watershed, San Juan County, Colorado; paper edition: U.S. Geological Survey Open-File Report 99-170, 40 p.

Nash, J.T., 1999b, Geochemical investigations and interim recommendations for priority abandoned mine sites on USBLM lands, Upper Animas River watershed, San Juan County, Colorado; paper edition: U.S. Geological Survey Open-File Report 99-323, 45 p.

Nash, J.T., 2000, Geochemical studies of mines, dumps, and tailings as sources of contamination, Upper Animas River Watershed, Colorado, U.S. Geological Survey Open-File Report 00-104,  CD-ROM

Nimick, D. A., and von Guerard, Paul, 1998, editors, Science for Watershed Decisions on Abandoned Mine Lands: Review of Preliminary Results, Denver, Colorado, February 4-5, 1998:  U.S. Geological Survey Open-File Report 98-297, 70 p.

Smith, K.S., Ramsey, C.A., and Hageman, P.L., 2000, Sampling strategy for the rapid screening of mine-waste dumps on abandoned mine lands, in Proceedings of the Fifth International Conference on Acid Rock Drainage, May 20-23, 2000, Denver, Colorado, Society of Mining Engineering, Lakewood, Colo., p 1456-1462.

U.S. Environmental Protection Agency, 1986, Test Methods for Evaluating Solid Waste, Vol. I and II (SW-846) 3rd Edition, November.  Updates are available through Revision 2B, published April 4, 1995.

Table 1.  Sample Identification numbers, Excel files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions

|  | FILE | FILE | FILE | FILE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SD | SD | SD | SD | Name or | Latitude | Longitude | Size |  |
| Sample ID | GX97 | TL97 | PL97 | PL99 | BLM site # | N (deg) | W (deg) | Est. Tons | Site and/or sample description |
| 97ABS101 | x | x | x |  | B060 | 37.8356 | 107.6858 | >50,000 | Lower level, tan, high clay, low sulfide |
| 97ABS102 | x | x | x |  | B060 | 37.8358 | 107.6864 | >50,000 | Upper level, tan, high clay, med pyrite |
| 97ABS103 | x | x | x |  | -- | 37.8233 | 107.6656 | 100 | Small dump, weakly mineralized volcanics |
| 97ABS104 | x | x | x |  | B160 | 37.8131 | 107.6444 | 5,000 | Gray, weakly altered volcanics, wet by mine drain |
| 97ABS105 | x | x | x |  | B070 | 37.8083 | 107.6650 | 5,000 | Tan and green weakly mineralized volcanics |
| 97ABS106 | x | x | x |  | B248 | 37.8117 | 107.6939 | nd | Red-ocher altered, high pyrite, mixed talus |
| 97ABS107 | x | x | x |  | -- | 37.8672 | 107.6839 | 2,000 | High pyrite waste from shaft, galena-sphalerite |
| 97ABS108 | x | x | x |  | -- | 37.8656 | 107.6811 | 10,000 | High sulfide pyrite-galena-sphalerite from adit |
| 97ABS109 | x | x | x |  | -- | 37.8678 | 107.6750 | 10,000 | Rusty stained low sulfide dump; high flow drainage |
| 97ABS110 | x | x | x |  | -- | 37.7872 | 107.6233 | >50,000 | Dark manganese-stained, oxides, some pyrite-chalcopyrite |
| 97ABS111 | x | x | x |  | -- | 37.7942 | 107.6356 | 2,000 | Oxides of iron-mangangese-copper, low pyrite |
| 97ABS112 | x | x | x |  | Bonner | 37.8431 | 107.7383 | >50,000 | Tan altered volcanics, medium pyrite, some sphalerite |
| 97ABS260 | x | x | x |  | Ferricrete mine | 37.8683 | 107.7269 | 500 | Iron-oxide cemented talus, no sulfides; wet |
| 97ABS261 | x | x | x |  | -- | 37.8672 | 107.7275 | >5,000 | Ocher ferricrete, friable, trenched |
| 97ABS262 | x | x | x |  | -- | 37.8497 | 107.7258 | 2,000 | Brown iron-oxide coated weakly altered volcanics, no pyrite |
| 97ABS263 | x | x | x |  | Imogene | 37.8622 | 107.7292 | 15,000 | Rusty iron-oxide coatings, low pyrite; wet |
| 97ABS264 | x | x | x |  | Silver Crown | 37.8717 | 107.8111 | 20,000 | High sulfide-pyrite-galena-sphalerite, medium clay, wet by mine drain |
| A97W001 | x | x | x |  | Carbon Lake | 37.8977 | 107.7163 | 12,000 | High pyrite-galena-sphalerite, enargite; wet |
| A97W002 | x | x | x |  | Congress | 37.8861 | 107.7023 | 7,000 | High sulfide, high clay, inhomogeneous |
| A97W003 | x | x | x |  | -- | 37.8910 | 107.7066 | 2,500 | High sulfide, high clay dump |
| A97W004 | x | x | x |  | -- | 37.8915 | 107.7102 | <500 | Sulfidic dump from prospect |
| NAD084 | x | x | x |  | -- | 37.9036 | 107.5564 | -- | Private; high pyrite dump, makes yellow sulfates |
| NAD085 | x | x | x |  | B144 | 37.8961 | 107.6144 | 1,000 | High pyrite-galena-sphalerite-chalcopyrite, weathers yellow; high clay |
| NAD086 | x | x | x |  | B152 | 37.8044 | 107.5983 | 20,000 | Sulfidic granitic rocks, galena-sphalerite, is unusual |
| NAD089 | x | x | x |  | -- | 37.8244 | 107.5864 | >100,000 | Private; medium pyrite-galena-sphalerite, ore pile? |
| NAD090 | x | x | x |  | B156 | 37.8658 | 107.5667 | 2,000 | Messy mine drainage makes iron flocculate |
| NAD091 | x | x | x |  | -- | 37.8792 | 107.6728 | 10,000 | Messy mine drainage, much red iron flocculate |
| NAD092 | x | x | x |  | B052 | 37.8914 | 107.6789 | 500 | Only part mine dump, is high sulfide; debris |

Table 1.  Sample Identification numbers, Excel files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions (cont.)

|  | FILE | FILE | FILE | FILE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SD | SD | SD | SD | Name or | Latitude | Longitude | Size |  |
| Sample ID | GX97 | TL97 | PL97 | PL99 | BLM site # | N (deg) | W (deg) | Est. Tons | Site and/or sample description |
| NAD094A | x | x | x |  | -- | 37.8922 | 107.6808 | 10,000 | Lark lower, medium-high sulfide, galena-sphalerite |
| NAD094B | x | x | x |  | B072 | 37.8944 | 107.6806 | 100,000 | Lark upper level, alluvium and high sulfide |
| NAD095 | x | x | x |  | B021 | 37.9014 | 107.6700 | 300 | Very high pyrite, some galena-sphalerite, water in shaft |
| NAD096 | x | x | x |  | B123 | 37.9103 | 107.6306 | 30,000 | Big dump, high pyrite-galena-sphalerite, drain through dump |
| NAD098 | x | x | x |  | B234 | 37.9519 | 107.5833 | 3,000 | Very high sulfide, big vein; water in trenches |
| NAD099 | x | x | x |  | -- | 37.9428 | 107.5344 | 2,000 | Oxidized, high quartz, small dump |
| NAD121 | x | x | x |  | B088 | 37.9336 | 107.5972 | 2,000 | Dump from adit; high clay, medium sulfide |
| NAD123 | x | x | x | x | B213 | 37.9286 | 107.5864 | 1,000 | High clay and black manganese, medium pyrite-sulfide dump, small |
| NAD132 |  |  |  | x | B229 | 37.9264 | 107.5697 | 1,000 | Mostly green-gray altered volcanic rock, background? |
| NAD134 | x | x | x |  | B183 | 37.9428 | 107.5344 | 2,000 | Oxidized, high quartz, small dump |
| NAD137 | x | x | x |  | B184 | 37.9417 | 107.5386 | 7,000 | Yellow sulfate from weathering, high silica |
| NAD142 | x | x | x |  | B182 | 37.9322 | 107.5644 | 6,000 | High quartz-carbonate (tan), low sulfide |
| NAD144 | x | x | x |  | B169 | 37.9400 | 107.5722 | 3,000 | Coarse abundant pyrite-quartz, some mine drainage |
| NAD146 | x | x | x |  | B236 | 37.9494 | 107.5861 | <100 | Abundant pyrite and sulfate, big quartz veins |
| NAD148 | x | x | x |  | -- | 37.9461 | 107.5889 | 8,000 | Stockpile? High pyrite-galena-sphalerite; looks like ore pile |
| NAD149 | x | x | x |  | -- | 37.9483 | 107.5839 | 10,000 | High pyrite-sericite altered volcanics; coarse quartz |
| NAD150 | x | x | x |  | B238 | 37.9450 | 107.5828 | 12,000 | Pyrite-clay rich, some galena-sphalerite; adit on large vein |
| NAD151 | x | x | x | x | B237 | 37.9461 | 107.5789 | 2,000 | Coarse pyrite with clay, big quartz-pyrite vein chunks, small dump |
| NAD155 | x | x | x |  | B234 | 37.9519 | 107.5833 | 3,000 | Very high sulfide, big vein; water in trenches |
| NAD160 | x | x | x |  | B233 | 37.9550 | 107.5783 | 5,000 | High sulfide, coarse pyrite; some mine drainage |
| NAD166 |  |  |  | x | -- | 37.9158 | 107.5642 | <1,000 | Mostly green altered volcanics; background? |
| NAD167 | x | x | x |  | B180 | 37.9147 | 107.5542 | 5,000 | Mixed oxidized sulfide and green altered volcanics |
| NAD172 |  |  |  | x | B120 | 37.9222 | 107.6328 | <100 | Very small but high sulfide |
| NAD175 | x | x | x | x | B123 | 37.9103 | 107.6306 | 30,000 | Big dump, high pyrite-galena-sphalerite, clay, drain through dump |

Table 1.  Sample Identification numbers, Excel files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions (cont.)

|  | FILE | FILE | FILE | FILE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SD | SD | SD | SD | Name or | Latitude | Longitude | Size |  |
| Sample ID | GX97 | TL97 | PL97 | PL99 | BLM site # | N (deg) | W (deg) | Est. Tons | Site and/or sample description |
| NAD177 |  |  |  | x | B010 | 37.9036 | 107.6606 | <100 | Mostly pyrite-sericite altered volcanics; background? |
| NAD181 | x | x | x |  | -- | 37.9069 | 107.6608 | 4,000 | High sulfide dump near lake at pass, clay? |
| NAD184 | x | x | x |  | -- | 37.8981 | 107.6467 | 3,000 | Mixed high pyrite and low pyrite waste; tram |
| NAD187 | x | x | x |  | B006 | 37.9028 | 107.6631 | 500 | Small, pyrite-altered volcanics, any ore? |
| NAD192 | x | x | x |  | B021 | 37.9014 | 107.6700 | 300 | Very high pyrite, some galena-sphalerite, water in shaft |
| NAD196 | x | x | x |  | B103 | 37.8892 | 107.6689 | 800 | Coarse pyrite-quartz veins, steep avalanche path |
| NAD201 | x | x | x |  | B105 | 37.8881 | 107.6650 | 200 | Low sulfide, high iron-oxide on dump, ferricrete |
| NAD204 | x | x | x |  | B072 | 37.8944 | 107.6806 | 100,000 | Lark upper level, alluvium and high sulfide |
| NAD210 | x | x | x |  | -- | 37.8922 | 107.6808 | 10,000 | Lark lower, medium-high sulfide, galena-sphalerite |
| NAD211 | x | x | x | x | -- | 37.8922 | 107.6808 | 10,000 | High pyrite-sphalerite-galena, fresh, few fines; sulfide picks |
| NAD216 | x | x | x |  | -- | 37.8914 | 107.6828 | 100,000 | High sulfide, high clay, weathered?, large |
| NAD218 | x | x | x |  | B052 | 37.8914 | 107.6789 | 500 | Only part mine dump, is high sulfide; debris |
| NAD219 | x | x | x |  | B053 | 37.8931 | 107.6761 | <100 | Small diggings, oxidized sulfides |
| NAD221 | x | x | x |  | B271 | 37.8886 | 107.6789 | 5,000 | Recent mining, low pyrite, slides into creek |
| NAD225 | x | x | x |  | B001 | 37.8792 | 107.6728 | 10,000 | Messy mine drainage, much red iron flocculate |
| NAD227 | x | x | x |  | -- | 37.8792 | 107.6728 | 10,000 | High pyrite part of dump, atypical sample |
| NAD227P |  |  |  | x | -- | 37.8792 | 107.6728 | 10,000 | Sulfidic picks from mostly oxide dump |
| NAD231 | x | x | x |  | B156 | 37.8658 | 107.5667 | 2,000 | Messy mine drainage makes iron flocculate |
| NAD235 | x | x | x |  | B022 | 37.8653 | 107.5381 | 12,000 | Low sulfide gray rocks, wet by mine drainage |
| NAD237 | x | x | x |  | B157 | 37.8672 | 107.5478 | 10,000 | Yellow sulfate colors on high pyrite waste, galena-sphalerite |
| NAD249 | x | x | x |  | B127 | 37.8572 | 107.5742 | 1,500 | Overgrown, variable sulfide, some water |
| NAD252 | x | x | x |  | -- | 37.8231 | 107.5853 | >100,000 | Private; oxide-sulfide-clay mix |
| NAD253 | x | x | x |  | -- | 37.8244 | 107.5864 | >100,000 | Private; medium pyrite-galena-sphalerite, ore pile? |
| NAD254 | x | x | x |  | -- | 37.8244 | 107.5856 | >100,000 | Private; low sulfide, wallrock only? |
| NAD262 | x | x | x |  | Highland Mary | 37.7844 | 107.5839 | >100,000 | Clay-altered volcanics, calcite veins |
| NAD265 | x | x | x |  | -- | 37.7828 | 107.5806 | 10,000 | Altered pre-Cambrian amphibolite, calcite veins |
| NAD286 |  |  |  | x | -- | 37.8061 | 107.5992 | 2,000 | Quartz-sulfide vein, old mine, calcite, -2 mm |

Table 1.  Sample Identification numbers, Excel files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions (cont.)

|  | FILE | FILE | FILE | FILE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SD | SD | SD | SD | Name or | Latitude | Longitude | Size |  |
| Sample ID | GX97 | TL97 | PL97 | PL99 | BLM site # | N (deg) | W (deg) | Est. Tons | Site and/or sample description |
| NAD298 | x | x | x |  | B152 | 37.8044 | 107.5983 | 20,000 | Sulfidic granitic rocks, galena-sphalerite, is unusual |
| NAD300 | x | x | x |  | B248 | 37.8108 | 107.6856 | 5,000 | Highly altered rocks, high pyrite, mixed talus and dump |
| NAD308 | x | x | x |  | B108 | 37.8722 | 107.6719 | 1,500 | Gray volcanics, low pyrite, some iron-oxide, small |
| NAD309 | x | x | x |  | B116 | 37.8722 | 107.6678 | 1,500 | Dump is tan, oxide coatings, pyrite, mine water on dump |
| NAD310 | x | x | x |  | B115 | 37.8728 | 107.6708 | 4,000 | Gray volcanics, low sulfide, no Acid Rock Drainage (ARD) |
| NAD311 | x | x | x |  | B009 | 37.8700 | 107.6747 | 3,000 | Much ocher-red iron flocculate from Acid Mine Drainage (AMD) |
| NAD320 | x | x | x |  | B262 | 37.8594 | 107.6872 | 3,000 | Moderate pyrite, tan clays, AMD on dump |
| NAD323 | x | x | x |  | -- | 37.8603 | 107.6853 | 4,000 | Sulfidic dump with yellow sulfates, high clay |
| NAD327 | x | x | x |  | B114 | 37.8747 | 107.6878 | 8,000 | Low pyrite, low iron-oxide, no ARD |
| NAD339 | x | x | x |  | B144 | 37.8961 | 107.6144 | 1,000 | High pyrite-galena-sphalerite-chalcopyrite, weathers yellow; high clay |
| NAD347 | x | x | x |  | B149 | 37.8919 | 107.6033 | 600 | Mix of sulfidic and green altered volcanics |
| NAD351 | x | x | x |  | -- | 37.8972 | 107.5403 | -- | Klondyke; much black manganese, low iron-oxide, low pyrite |
| NAD352 | x | x | x |  | -- | 37.8992 | 107.5442 | -- | Coarse pyrite-quartz veins, weathers yellow |
| NAD353 | x | x | x |  | -- | 37.9025 | 107.5411 | -- | Coarse pyrite-galena-sphalerite, talus mixed in with dump |
| NAD355 | x | x | x |  | -- | 37.9036 | 107.5564 | -- | Private; high pyrite dump, make yellow sulfates |
| NAD357 | x | x | x |  | -- | 37.9044 | 107.5561 | -- | Private; upper dump like NAD355. |
| NAD361 | x | x | x |  | -- | 37.8103 | 107.6053 | -- | Private; mostly green altered volcanics, some quartz |
| NAD362 | x | x | x |  | -- | 37.8139 | 107.6039 | -- | Private, small; mixed pyrite and yellow sulfates |
| NAD364 | x | x | x |  | B160 | 37.8919 | 107.6033 | 5,000 | Tan dump, high clay, high water flow, no ARD |
| NAD365 | x | x | x |  | -- | 37.8142 | 107.6517 | -- | Stockpile at mill; high pyrite ore (?) |
| NAD380 | x | x | x |  | B318 | 37.9078 | 107.5656 | 10,000 | Recent mining; low sulfide dump |
| NAD381 |  |  |  | x | -- | 37.9331 | 107.6058 | 500 | Stockpile, rich in sphalerite-galena-pyrite |
| NAD387 |  |  |  | x | -- | 37.8969 | 107.5589 | 10,000 | Sulfidic part of dump, chunks? |
| NAD396 | x | x | x |  | B249 | 37.9319 | 107.6056 | 1,000 | Upper dump, moderate pyrite-ocher oxides |
| NAD399 | x | x | x |  | -- | 37.7869 | 107.8003 | >100,000 | Gray siltite, oxide coatings, low sulfide |

Table 1.  Sample Identification numbers, Excel files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions (cont.)

|  | FILE | FILE | FILE | FILE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SD | SD | SD | SD | Name or | Latitude | Longitude | Size |  |
| Sample ID | GX97 | TL97 | PL97 | PL99 | BLM site # | N (deg) | W (deg) | Est. Tons | Site and/or sample description |
| NAD414 | x | x | x |  | -- | 37.8494 | 107.6764 | -- | Private; high pyrite-galena-sphalerite dump, high clay |
| NAD423 | x | x | x |  | -- | 37.8561 | 107.7208 | 500 | Quartz-pyrite-sericite altered rocks, moderate sulfides |
| NAD427 | x | x | x |  | -- | 37.8747 | 107.7325 | 5,000 | Rusty altered rocks, low sulfide?, much mine water |
| NAD501 |  |  |  | x | -- | 37.8653 | 107.7072 | 300 | Yellow, high clay, pyritic dump |
| NAD504 |  |  |  | x | -- | 37.8639 | 107.7169 | 500 | Sulfidic waste from old shaft, bulldozed |
| NAD511 |  |  |  | x | Imogene | 37.8622 | 107.7286 | 10,000 | Gray silicic volcanics, iron-oxide coatings, low pyrite |
| NAD516 |  |  |  | x | Bonner | 37.8431 | 107.7383 | 10,000 | Middle dump, low pyrite, silicic volcanics, iron-oxide |
| NAD517 |  |  |  | x | Bonner | 37.8436 | 107.7383 | 10,000 | Lower dump, low pyrite, high iron-oxide matrix |
| NAD519 |  |  |  | x | West Bonner | 37.8444 | 107.7403 | 7,500 | West of Bonner, low pyrite, high iron-oxide dump |
| NAD520 |  |  |  | x | Paradise | 37.8425 | 107.7644 | 10,000 | Paradise, low pyrite, high iron-oxide and white crust |
| NAD524 |  |  |  | x | Ruby Trust | 37.8458 | 107.7528 | 20,000 | High clay, medium pyrite, iron-oxide coatings on volcanic rocks |
| NAD530 |  |  |  | x | B123 | 37.9103 | 107.6306 | 30,000 | High pyrite-sphalerite-galena; repeat sample |
| NAD555 |  |  |  | x | B116 | 37.8728 | 107.6675 | 1,600 | Tan, low-medium pyrite, iron-oxide coatings |
| NAD557 |  |  |  | x |  | 37.8878 | 107.6842 | 500 | Very high sulfide, fine grained in clay |
| NAD563 |  |  |  | x | N204 | 37.8928 | 107.6811 | 50,000 | Upper Lark, on average is low sulfide with alluvium |
| NAD564 |  |  |  | x | N210 | 37.8925 | 107.6808 | 50,000 | Lower Lark re-sample, medium sulfide, pyrite-sphalerite-galena |
| NAD577 |  |  |  | x | Silver Crown | 37.8717 | 107.7444 | 20,000 | Waste rich in clay and fine pyrite |
| NAD588 |  |  |  | x | Brooklyn | 37.8722 | 107.6972 | 100,000 | Gray dump, high in fine pyrite and clay |
| NAD594 |  |  |  | x | Bullion King | 37.8881 | 107.7422 | 30,000 | Tan color, high clay and iron-oxide, fine pyrite inside |
| NAD601 |  |  |  | x | B152 | 37.8025 | 107.6797 | 20,000 | Granitic rocks, medium pyrite, medium iron-oxide |
| NAD603 |  |  |  | x | Burbank | 37.8189 | 107.7725 | 10,000 | Green altered volcanics, oxide coatings |
| NAD648 |  |  |  | x | Bandora | 37.7867 | 107.8011 | 50,000 | Lower Bandora, tan siltite, iron-oxide coatings, low pyrite |
| NAD650 |  |  |  | x | Bandora | 37.7875 | 107.8019 | 50,000 | Upper dump, tan siltite, has low sulfide |
| NAD696 |  |  |  | x | NAD211 | 37.8925 | 107.6814 | 10,000 | High sulfide dump, coarse, few fines; re-sample |
| NAD726 |  |  |  | x | B234 | 37.9517 | 107.5819 | 3,000 | High pyrite dump, re-sample |
| NAD817 |  |  |  | x | -- | 37.8608 | 107.7163 | >50,000 | High pyrite-sphalerite-galena dump, high clay, recent |
| NAD818 |  |  |  | x | -- | 37.8592 | 107.7013 | 10,000 | High pyrite-sphalerite-galena dump, high clay, recent |

Table 1.  Sample Identification numbers, Excel files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions (cont.)

|  | FILE | FILE | FILE | FILE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SD | SD | SD | SD | Name or | Latitude | Longitude | Size |  |
| Sample ID | GX97 | TL97 | PL97 | PL99 | BLM site # | N (deg) | W (deg) | Est. Tons | Site and/or sample description |
| NAD845 |  |  |  | x | B249 | 37.8525 | 107.5819 | 2,000 | Ocher, mixed sulfide-oxide materials |
| NAD878 |  |  |  | x | B014 | 37.8653 | 107.6806 | 2,000 | From adit, high pyrite-sphalerite-galena dump |
| NAD879 |  |  |  | x | B014 | 37.8650 | 107.6811 | 3,000 | From shaft, very high pyrite, sphalerite-galena |
| NADW520 |  |  |  | x | Paradise | 37.8425 | 107.7644 | 10,000 | Mostly white crust on iron-oxide soil |
| NAF520 |  |  |  | x | Paradise | 37.8425 | 107.7644 | 10,000 | Mostly red and brown fine iron-oxide soil |
| NAF521 |  |  |  | x | Paradise West | 37.8419 | 107.7653 | 5,000 | Fine red iron-oxide soil in matrix |
| NAF687 |  |  |  | x | -- | 37.8783 | 107.6714 |  | Rusty brown iron-oxide from mine drainage |
| NAG299 | x | x | x |  | -- | 37.8078 | 107.6750 | -- | Glassy black smelter slag, ground sand size |
| NAH188 |  |  |  | x | -- | 37.9031 | 107.6669 | na | Drill cuttings, high clay, high pyrite |
| NAH189 |  |  |  | x | -- | 37.9033 | 107.6672 | na | Drill cuttings, high clay, high pyrite |
| NAH558 |  |  |  | x | -- | 37.8886 | 107.6844 | na | Drill cuttings, high clay, high pyrite |
| NAH559 |  |  |  | x | -- | 37.8892 | 107.6847 | na | Drill cuttings, high clay, high pyrite, and oxides |
| NAH560 |  |  |  | x | -- | 37.8894 | 107.6847 | na | Drill cuttings, high pyrite and iron-oxide |
| NAR130 | x | x | x |  | -- | 37.9114 | 107.5967 | -- | Red-black soil along quartz-sulfide vein, -2 mm |
| NAR180 | x | x | x |  | -- | 37.9044 | 107.6633 | -- | Pyrite-jarosite altered volcanic, Red Mtn type, -2 mm |
| NAR190 | x | x | x |  | -- | 37.9031 | 107.6669 | -- | Drill cuttings in red altered volcanics, -2 mm |
| NAR197 |  |  |  | x | -- | 37.8894 | 107.6672 | na | Iron-oxide-pyrite altered volcanic rocks, -2 mm |
| NAR205 |  |  |  | x | -- | 37.8950 | 107.6811 | na | Rusty alluvium at Lark mine |
| NAR207S | x | x | x |  | -- | 37.8983 | 107.6789 | -- | Red soil from pyrite-altered volcanics, -2 mm |
| NAR261 | x | x | x |  | -- | 37.7831 | 107.5839 | -- | Soil from gray clay-carbonate altered volcanics |
| NAR301 | x | x | x |  | -- | 37.8106 | 107.6861 | -- | Red weathered pyrite-altered volcanics, -2 mm |
| NAR366 |  |  |  | x | B218 | 37.9078 | 107.5656 | na | Small dump, mostly gray volcanics |
| NAR391 |  |  |  | x | B288 | 37.7981 | 107.5508 | na | Mostly gray fresh volcanics, low pyrite |
| NAR421 | x | x | x |  | -- | 37.8186 | 107.6983 | -- | Red pyrite-altered volcanics in County pit, -2 mm |
| NAR603 |  |  |  | x | -- | 37.8189 | 107.7719 | na | Green altered volcanic agglomerate |
| NAR691 |  |  |  | x | -- | 37.8992 | 107.6789 | na | Soil in red altered volcanics, from acid sulfate alteration? |

Table 1.  Sample Identification numbers, Excel files containing analytical data, site names, site localities, estimated dump size, and site/sample descriptions (cont.)

|  | FILE | FILE | FILE | FILE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SD | SD | SD | SD | Name or | Latitude | Longitude | Size |  |
| Sample ID | GX97 | TL97 | PL97 | PL99 | BLM site # | N (deg) | W (deg) | Est. Tons | Site and/or sample description |
| NAS638 |  |  |  | x | -- | 37.8983 | 107.6792 | na | Soil in red altered volcanics, from acid sulfate alteration? |
| NAS699F |  |  |  | x | -- | 37.8558 | 107.6775 | na | Schwertmannite (?) ocher crust in Cement Creek |
| NAT088 | x | x | x |  | Highland Mary tails | 37.7886 | 107.5789 | >100,000 | Highland Mary mill tails, light tan, carbonate? |
| NAT230 | x | x | x |  | Kitti-Mack tails | 37.8606 | 107.5706 | >100,000 | Kitti-Mack tails, pale yellow |
| NAT234 | x | x | x |  | Old Kitti-Mack | 37.8622 | 107.5533 | <100 | Old Kitti-Mack millsite, ocher tailings |
| NAT258 | x | x | x |  | Highland Mary tails | 37.7886 | 107.5789 | >100,000 | Highland Mary mill tails, light tan, carbonate? |
| NAT270 | x | x | x |  | Old Hundred | 37.8244 | 107.5864 | 500? | Old Hundred mill tails, ocher |
| NAT287 |  |  |  | x | -- | 37.8061 | 107.5992 | 1,000 | Tails from stamp mill L. Giant |
| NAT378 | x | x | x |  | Vermillion mill | 37.9325 | 107.5961 | <100 | Vermillion mill tails, light gray |
| NAT389 | x | x | x |  | South Howard. Mill? | 37.8325 | 107.6003 | <100 | South Howardsville mill site, rusty tails at mill |
| NAT501 |  |  |  | x | Brooklyn | 37.8581 | 107.7111 | 1,000 | Brooklyn tails, gray, high pyrite |
| NAT525 |  |  |  | x | Ruby Trust | 37.8447 | 107.7519 | <100 | Ruby Trust tails in foundation |
| NAT600 |  |  |  | x | -- | 37.8511 | 107.7264 | <100 | Tailings in burned foundation, pale gray |
| NAT602 |  |  |  | x | Lodore | 37.8022 | 107.6728 | 1,000 | Ocher tailings near Lodore mill |
| NAT622 |  |  |  | x | Lackawanna | 37.8447 | 107.7533 | 30,000 | Gray and ocher tailings, Lackawanna |
| NAT623 |  |  |  | x | -- | 37.8678 | 107.5664 | fluvial | Ocher layer of tailings, upper layer |
| NAT624 |  |  |  | x | -- | 37.8678 | 107.5664 | fluvial | Gray layer of mill tailings, below ocher |
| NAT628 |  |  |  | x | -- | 37.9208 | 107.5597 | fluvial | Ocher tailings on sandbar |
| NAT706 |  |  |  | x | Bagley | 37.9328 | 107.5789 | 10,000 | Bagley tails, ocher, in pond |
| NAT720 |  |  |  | x | -- | 37.8044 | 107.5994 | 1,000 | Below stamp mill, in creek, coarse |
| NAT742 |  |  |  | x | Highland Mary | 37.7883 | 107.5800 | 100,000 | Highland Mary tails, light, calcite? |
| NAT830 |  |  |  | x | Mastodon | 37.9100 | 107.6003 | na | Ocher tailings, reclaimed 1997 |