DEPARTMENT OF HOUSING AND URBAN DEVELOPMENT 	STRUCTURAL ENGINEERING

## Housing - Federal Housing Commissioner 	BULLETIN NO.

# TO: 	DIRECTORS, SINGLE FAMILY HOCs 	ISSUE DATE

# DIRECTORS, MULTIFAMILY HUBs

#### REVIEW DATE

##### SUBJECT: 	1.	 Item Description

- Name and address

of Manufacturer

This Structural Engineering Bulletin (SEB) should be filed with other SEBs and related Bulletins on materials or products as required by prescribed procedures.

1.	General:

This Bulletin sets forth specific requirements under the Technical Suitability of Products Program for determining the eligibility of housing to be constructed under HUD mortgage insurance, or other HUD housing programs.

2.	Scope:

This Bulletin applies only to the structural features of this method of construction.  Final determination of eligibility is made by the appropriate HUD Field Office. Other factors considered will be valuation, location, architectural planning and appeal, mechanical equipment, thermal characteristics, and market acceptance.  Consideration is also necessary to determine whether a specific property will qualify under the specific HUD program, when constructed according to the method outlined in this Bulletin, and where the structure is to be located.

-2-

In geographical areas subject to hurricanes, earthquakes, or other severe conditions affecting dwelling structures, the HUD Field Office or Homeownership Center shall require additional safeguards in proposed designs, when necessary.

3.	Minimum Property Standards (MPS):

Compliance with HUD MPS will be determined by the HUD Field Office or Homeownership Center on the same basis as submissions involving conventional construction, except for the special features described in this Bulletin.

4.	Inspection:

Field compliance inspections covering conventional items of construction and any special features covered in this Bulletin shall be made in accordance with prescribed procedures.

The appropriate HUD Field Office or Homeownership Center shall furnish a copy of a HUD field inspection report to Headquarters, FHA Standards, Office of Manufactured Housing Programs, when there is:

a.	Evidence of noncompliance with portions of the system of construction described in this Bulletin.

b.	Faulty shop fabrication, including significant surface defects.

c.	Damage to shop fabricated items or materials due to improper transportation, storage, handling or assembly.

d.	Unsatisfactory field workmanship or performance of the product or system.

e.	Any significant degradation or deterioration of the product or evidence of lack of durability or performance.

Periodic plant inspections will be made by HUD Field Office, Homeownership Center, State Agency personnel, or a HUD designated representative in accordance with their prescribed procedures.  Factory inspection reports shall be submitted to HUD Headquarters, upon  request.

-3-

5.	Certification:

The manufacturer named in this Bulletin shall furnish the builder with a written certification stating that the product has been manufactured in compliance with the HUD Minimum Property Standards (MPS), except as modified by this Bulletin.  The Builder shall endorse the certification with a statement that the product has been erected in compliance with the HUD MPS except as modified by this Bulletin, and that the manufacturer's certification does not relieve the Builder, in any way, of responsibility under the terms of the Builder's Warranty required by the National Housing Act, or under any provisions applicable to any other housing program.  This certification shall be furnished to the HUD Field Office upon completion of the property.

OUTLINE DESCRIPTION, CATEGORY II CONSTRUCTION

GENERAL:

Shop fabricated foam core sandwich roof, exterior wall, and floor panels are furnished in this method of construction.  Panels consist of oriented strand board (OSB) skins and polystyrene foam cores.  Panels are transported to the building site where they are connected together.

All materials and methods of installation shall be in accordance with HUD Minimum Property Standards (MPS), Use of Materials Bulletins (UM), and Materials Releases (MR), except as may be specifically noted herein. Plumbing, heating and electrical systems are field installed and connected.

This Bulletin is based upon a structural review of the Premier Structural Sandwich Panels, but may be considered applicable to all structurally similar units of this company.  Foundation design and nonstructural items ( such as architectural, plumbing, heating and electrical features ) are not covered by this Bulletin.

SPECIFICATIONS:

Form HUD-92005, "Description of Materials" specifying only the structurally related items (Nos. 1 to 12, 14, 26, and 27), as originally submitted for determination of technical suitability, describes the materials that shall be used in construction of housing units under this system of construction.

DRAWINGS:

The following drawing(s) by Premier Industries, Inc. shall be considered an integral part of this Bulletin:

-4-

Drawing No.		Date	Description

PBS-000			03/19/98	Section

PBS-001			03/19/98	Section

PBS-002			03/19/98	Panel Precautions

PBS-100			03/19/98	Panel Plate Connections

PBS-105			03/19/98	Double Spline Connection

PBS-110			03/19/98	I-Joist Spline Connection

PBS-115			03/19/98	Double 2x Lumber Connection

PBS-120			03/19/98	Top Spline Connection

PBS-125			03/19/98	Panel to Slab/Fnd Connection

PBS-130			03/19/98	Platform Framing w/ Joist Hanger

PBS-135			03/19/98	Platform Framing

PBS-140			03/19/98	Foundation Framing Connection

PBS-141			08/20/99	Foundation Framing Connection

PBS-145			03/19/98	Panel Corner Connection

PBS-150			03/19/98	Angled Panel Corner Connection

PBS-155			03/19/98	Beveled Blk Wall/Roof Connection

PBS-160			03/19/98	Beveled Wall/Roof Connection

PBS-165			03/19/98	Truss Bearing on Wall

PBS-170			03/19/98	Floor Power Blocking

PBS-175			03/19/98	2x Panel Joint Connection

PBS-180			03/19/98	I-Joist Panel Connection

PBS-185			03/19/98	Panel To Steel Member

PBS-190			03/19/98	Roof Valley Connection

PBS-195			03/19/98	Ridge Cap Roof Connection

PBS-200			03/19/98	12:12 Pitch Ridge Connection

PBS-205			03/19/98	Eave Details

PBS-215			03/19/98	Ledger Detail

PBS-220			03/19/98	Parapet Detail

PBS-225			03/19/98	Insul Beam Header

PBS-230			03/19/98	Wall Panel Box Header

PBS-235			03/19/98	Typical Panel Wall

PBS-240			03/19/98	Typical Opening Framing

PBS-245			03/19/98	Post to Concrete Anchorage

PBS-250			03/19/98	Post to Concrete Anchorage

PBS-255			03/19/98	Interior Wall Connection

PBS-275			03/19/98	Roof/Floor Openings

PBS-280			03/19/98	Roof Penetrations

PBS-290			03/19/98	Interior Wall Connection

-5-

The Builder shall submit construction drawing(s) to the HUD Field Office or Homeownership Center with each application under HUD housing programs, which shall include the same or similar structural features as shown on the drawings listed above.  Copies of these listed drawings shall also be furnished to the HUD Field Office or Homeownership Center by the Builder upon request.

SPECIAL  CONSTRUCTION  FEATURES:

General:	Premier Structural Sandwich Panels are factory assembled sandwich panels consisting of expanded polystyrene (EPS) cores with oriented strand board (OSB) facings produced at locations listed in Table 1 of this report.  The panels are used as load bearing wall, roof, and floor components.  Panels are produced in widths ranging from 4 to 8 foot and lengths ranging from 8 to 24 foot.  The panels are manufactured in a Type S, Type I, and Type L panel configuration shown in Figures 1, 2, and 3 of this report.

Type S Panel:  The core for the Type S panel is recessed along the panel sides to receive nominal 4 inch (102 mm) wide OSB spline and recessed on the ends to receive solid sawn dimensional lumber sized to match the core thickness. See Figure 1 of this report.

Type I Panel:  The Type I panel is recessed along the panel side to receive I-joist splines and recessed on the ends to receive nominal 2 inch thickness.  See Figure 2 of this report.

Type L Panel:  The Type L panel is recessed along the panel sides and ends to receive nominal 2 inch thick solid sawn dimensional lumber sized to match the core thickness.  See Figure 3 of this report.

-6-

-7-

-8-

-9-

Materials:

Core:  The core material is EPS foam plastic with a thickness of 3½ to 111/4 inches.  The EPS core has flame spread rating of not more than 75 and a smoked developed rating of not more than 450 when tested in accordance with ASTM E 84 and a density of 0.95 pcf.

Facing:  Panel facing material is 7/16 to 3/4 inch thick Structural 1, Exposure 1 OSB complying with DOC PS-2.

Adhesive:  The adhesive is Structural grade Type II, Class 2 laminating adhesive. (Ashland Adhesive Isoset WD3-A322/CX-47, Ashland Adhesive Isogrip 3030D, Morad Adhesive Mor-Ad M-715/CRL-A, or Morad Adhesive Mor-Ad M640 Series)

Splines:  The splines for the Type S panels are nominal 4 inches wide by 7/16 inch thick OSB material.  The splines for Type I panels are I-joist, sized in depth to match the core thickness.  The splines for Type L panels are nominal 2 inches thick dimensional lumber sized in depth to match the core thickness.

DESIGN  AND  CONSTRUCTION  REQUIREMENTS:

Design Loads:	The method of construction described in this Bulletin is based on the allowable superimposed loads noted in Tables 2 through 11 of this report.  The Builder shall submit structural calculations to the local HUD Office or Homeownership Center  showing that these loads have not been exceeded.

TABLE 1

| LOCATIONS OF PREMIER INDUSTRIES, INC / d.b.a. | LOCATION NUMBERS FOR PRODUCT IDENTIFICATION |
| --- | --- |
| Premier Building Systems 4609 70th Ave. E Fife, Washington 98424 | PB-31 |
| Premier Building Systems 3434 West Papago Street Phoenix, Arizona 85009-6733 | PB-32 |

-10-

TABLE 2

TYPE S PANELS1

MAXIMUM ALLOWABLE TRANSVERSE LOADS(psf)

| PANEL CORE THICKNESS (inches) | DEFLECTION | PANEL SPAN |
| --- | --- | --- |
|  |  | 8 ft | 10 ft | 12 ft | 14 ft | 16 ft | 18 ft | 20 ft | 22 ft | 24 ft |
| 3½2 | L/360 | 40 | 30 | 20 | 15 | 10 | ---- | ---- | ---- | ---- |
|  | L/240 | 60 | 40 | 35 | 25 | 15 | ---- | ---- | ---- | ---- |
|  | L/180 | 60 | 55 | 45 | 35 | 20 | ---- | ---- | ---- | ---- |
| 5½2 | L/360 | 50 | 40 | 30 | 25 | 20 | 15 | 10 | ---- | ---- |
|  | L/240 | 80 | 60 | 35 | 30 | 30 | 20 | 15 | ---- | ---- |
|  | L/180 | 80 | 60 | 45 | 40 | 35 | 30 | 20 | ---- | ---- |
| 71/43 | L/360 | 60 | 60 | 40 | 35 | 25 | 20 | 15 | 15 | 10 |
|  | L/240 | 85 | 75 | 60 | 50 | 40 | 30 | 25 | 20 | 20 |
|  | L/180 | 85 | 75 | 70 | 60 | 50 | 40 | 30 | 25 | 25 |
| 91/44 | L/360 | 80 | 65 | 50 | 40 | 35 | 25 | 20 | 20 | 20 |
|  | L/240 | 85 | 65 | 55 | 50 | 45 | 40 | 35 | 30 | 25 |
|  | L/180 | 85 | 65 | 55 | 50 | 45 | 40 | 40 | 35 | 35 |
| 111/44 | L/360 | 95 | 75 | 50 | 50 | 50 | 40 | 30 | 25 | 20 |
|  | L/240 | 95 | 75 | 60 | 65 | 50 | 45 | 40 | 35 | 30 |
|  | L/180 | 95 | 75 | 60 | 65 | 50 | 45 | 40 | 35 | 35 |

1.	Floor panels shall have a minimum ¾-inch thick top skin or a minimum 7/16-inch thick top skin overlaid with minimum 7/16 inch thick finish flooring perpendicular to the panels.

2.	3½ inch and 5½-inch core panels shall be limited to a maximum span of 12 feet when used in roof applications.

3.	71/4 inch core panels shall be limited to a maximum span of 14 feet when used in roof applications.

4.	91/4-inch and 111/4-inch core panels shall be limited to a maximum span of 16 feet when used in roof applications.

-11-

TABLE 3

TYPE I PANELS1

MAXIMUM ALLOWABLE TRANSVERSE LOADS (psf)

| PANEL CORE THICKNESS (inches) | DEFLECTION | PANEL SPAN (feet) |
| --- | --- | --- |
|  |  | 42 | 8 | 10 | 12 | 14 | 16 | 18 | 20 | 22 | 24 |
| 71/4 | L/360 | 130 | 135 | 95 | 60 | 50 | 40 | 30 | 20 | 20 | 15 |
|  | L/240 | 315 | 150 | 105 | 90 | 70 | 55 | 40 | 30 | 25 | 25 |
|  | L/180 | 320 | 150 | 105 | 90 | 85 | 55 | 50 | 40 | 35 | 30 |
| 91/4 | L/360 | 195 | 165 | 125 | 70 | 65 | 60 | 50 | 35 | 30 | 25 |
|  | L/240 | 320 | 165 | 125 | 105 | 95 | 85 | 70 | 50 | 45 | 35 |
|  | L/180 | 320 | 165 | 125 | 105 | 95 | 85 | 75 | 65 | 55 | 45 |
| 111/4 | L/360 | 260 | 145 | 105 | 85 | 85 | 75 | 60 | 40 | 35 | 30 |
|  | L/240 | 320 | 145 | 105 | 95 | 85 | 75 | 70 | 60 | 55 | 45 |
|  | L/180 | 320 | 145 | 105 | 95 | 85 | 75 | 70 | 60 | 55 | 50 |

1.	Floor panels shall have a minimum 3/4-inch thick top skin or a minimum 7/16-inch thick top skin overlaid with minimum 7/16-inch thick finish flooring perpendicular to the panels.

2.	Panels spanning 4 feet shall be a minimum of 8 feet long spanning a minimum of two 4-foot spans.  No single span conditions shall be permitted.

-12-

TABLE 4

TYPE L PANELS1

MAXIMUM ALLOWABLE TRANSVERSE LOADS (psf)

| PANEL CORE THICKNESS (inches) | DEFLECTION | PANEL SPAN (feet) |
| --- | --- | --- |
|  |  | 42 | 8 | 10 | 12 | 14 | 16 | 18 | 20 | 22 | 24 |
| 3½ | L/360 | 105 | 45 | 35 | 25 | 15 | 10 | ---- | ---- | ---- | ---- |
|  | L/240 | 225 | 70 | 45 | 35 | 25 | 15 | ---- | ---- | ---- | ---- |
|  | L/180 | 300 | 90 | 60 | 45 | 35 | 25 | ---- | ---- | ---- | ---- |
| 5½ | L/360 | 255 | 130 | 55 | 40 | 30 | 25 | 20 | 15 | ---- | ---- |
|  | L/240 | 290 | 180 | 85 | 60 | 50 | 35 | 30 | 20 | ---- | ---- |
|  | L/180 | 290 | 180 | 110 | 80 | 65 | 50 | 40 | 30 | ---- | ---- |
| 71/4 | L/360 | 255 | 170 | 80 | 65 | 55 | 40 | 30 | 25 | ---- | ---- |
|  | L/240 | 290 | 190 | 130 | 100 | 80 | 60 | 50 | 35 | ---- | ---- |
|  | L/180 | 290 | 190 | 135 | 115 | 105 | 80 | 60 | 45 | ---- | ---- |
| 91/4 | L/360 | 285 | 190 | 115 | 100 | 80 | 60 | 45 | 35 | 30 | 30 |
|  | L/240 | 325 | 190 | 145 | 135 | 120 | 90 | 70 | 50 | 45 | 40 |
|  | L/180 | 325 | 190 | 145 | 135 | 120 | 110 | 90 | 70 | 60 | 55 |
| 111/4 | L/360 | 325 | 190 | 165 | 140 | 115 | 90 | 75 | 60 | 45 | 35 |
|  | L/240 | 325 | 190 | 165 | 155 | 130 | 110 | 95 | 85 | 70 | 55 |
|  | L/180 | 325 | 190 | 165 | 155 | 130 | 110 | 95 | 85 | 85 | 70 |

1.	Floor panels shall have a minimum 3/4-inch thick top skin or a minimum 7/16-inch thick top skin overlaid with minimum 7/16-inch thick finish flooring perpendicular to the panels.

2.	Panels spanning 4 feet shall be a minimum of 8 feet long spanning a minimum of two 4-foot spans.  No single span conditions shall be permitted.

-13-

TABLE 5

TYPE S PANELS

MAXIMUM ALLOWABLE AXIAL LOADS (plf)

| PANEL CORE THICKNESS (inches) | PANEL SPAN |
| --- | --- |
|  | 8 ft | 10 ft | 12 ft | 16 ft | 20 ft | 24 ft |
| 3½ | 3500 | 2555 | 2450 | 2120 | ---- | ---- |
| 5½ | 4250 | 4040 | 3375 | 3920 | 2815 | ---- |
| 71/4 | 4915 | 4325 | 4475 | 4195 | 3495 | 3065 |

TABLE 6

TYPE L PANELS

MAXIMUM ALLOWABLE AXIAL LOADS (plf)

| PANEL CORE THICKNESS (inches) | PANEL SPAN |
| --- | --- |
|  | 8 ft | 10 ft | 12 ft | 16 ft | 20 ft | 24 ft |
| 3½ | 4725 | 3905 | 3095 | 2620 | ---- | ---- |
| 5½ | 5850 | 5890 | 4280 | 4310 | 2935 | ---- |
| 71/4 | 6850 | 6110 | 5555 | 5180 | 4835 | 4080 |

-14-

TABLE 7

ALL PREMIER WALL PANELS

MAXIMUM ALLOWABLE POINT LOADS (lbs)

|  | 1½ inch Minimum Bearing Width | 3 inch Minimum Bearing Width |
| --- | --- | --- |
| Standard Detail | 2040 | 2450 |
| Additional Cap Plate1 | 4030 | 4680 |

1.	See Figure 4 of this report.

FIGURE 4

PREMIER CAP PLATE

-15-

TABLE 8

MAXIMUM ALLOWABLE HEADER LOADS WITH NO SPLINES (plf)

| HEADER DEPTH (inches) | DEFLECTION | HEADER SPAN |
| --- | --- | --- |
|  |  | 4 ft | 6 ft | 8 ft | 10 ft |
| 12 | L/360 | 740 | 385 | 230 | 140 |
|  | L/240 | 740 | 385 | 230 | 140 |
|  | L/180 | 740 | 385 | 230 | 140 |
| 18 | L/360 | 795 | 575 | 385 | 310 |
|  | L/240 | 795 | 575 | 385 | 310 |
|  | L/180 | 795 | 575 | 385 | 310 |
| 24 | L/360 | 885 | 630 | 430 | 360 |
|  | L/240 | 885 | 630 | 430 | 360 |
|  | L/180 | 885 | 630 | 430 | 360 |

-16-

TABLE 9

MAXIMUM ALLOWABLE HEADER LOADS WITH SPLINES (plf)

| HEADER DEPTH (inches) | DEFLECTION | HEADER SPAN |
| --- | --- | --- |
|  |  | 4 ft | 6 ft | 8 ft | 10 ft |
| 12 | L/360 | 345 | 245 | 155 | 100 |
|  | L/240 | 450 | 295 | 190 | 125 |
|  | L/180 | 630 | 380 | 235 | 155 |
| 18 | L/360 | 705 | 390 | 255 | 235 |
|  | L/240 | 750 | 480 | 300 | 280 |
|  | L/180 | 750 | 480 | 300 | 280 |
| 24 | L/360 | 700 | 580 | 370 | 350 |
|  | L/240 | 895 | 580 | 370 | 350 |
|  | L/180 | 895 | 580 | 370 | 350 |

TABLE 10

PREMIER WALL PANELS1, 2

MAXIMUM ALLOWABLE SHEAR WALL LOADS

| PANEL TYPE | MINIMUM OSB FACE THICKNESS | ATTACHMENTS3 | SHEAR (plf) |
| --- | --- | --- | --- |
|  |  | 2x Framing | Splines |  |
|  |  | Fasteners | Spacing | Fasteners | Spacing |  |
| L or S | 7/16 inch | 8d nail | 6 inches | 8d nail | 6 inches | 300 |
| S | 7/16 inch | 8d nail | 4 inches | #6 Screw | 4 inches | 6004 |

1.	Framing lumber shall be a minimum of Douglas Fir-Larch having a minimum specific gravity of 0.50.

2.	Minimum panel width shall be four feet.  The maximum panel height-to-width ratio shall be 3½:1.

3.	Nails are box nails.  Screws are #6 x 11/4 inch Type W drywall screws.

4.	Two top plates are required.

-17-

TABLE 11

PREMIER PANELS1

MAXIMUM ALLOWABLE DIAPHRAGM LOADS

| MINIMUM OSB FACE THICKNESS | ATTACHMENTS | SHEAR (plf) |
| --- | --- | --- |
|  | Panel Supports2 | Panel Joints - Top Only3 | Panel Joints - Top & Bottom4 |  |
|  | Fasteners | Spacing | Fasteners | Spacing | Fasteners | Spacing |  |
| 7/16 inch | PBS Screw5 | 12 inches | 8d nail | 3 inches | 8d nail | 6 inches | 425 |
| 7/16 inch | PBS Screw5 | 3 inches | 8d nail | 2 inches | 8d nail | 4 inches | 510 |

1.	The maximum panel height-to-width ratio shall be 4½:1.

2.	See Figure 5 of this report.

3.	See Figure 6 of this report.

4.	See Figure 7 of this report.

5.	Premier Building Systems specially designed “Big Blue” screws.

-18-

Fire Protection and Interior Finish:	The EPS foam core shall have a flame spread rating of not more than 75 and a smoke development rating of not more than 450 when tested in accordance with ASTM E 84.  All interior ceilings and wall surfaces are covered with ½ inch thick gypsum wallboard or other approved 15 minute thermal barrier.  Floor finish shall be a minimum of 5/8 inch blandex or plywood.

Framing of Loadbearing Walls:	Wood-to-wood connections shall be provided between bearing walls and roof/ceiling or floor construction.  Floor covering, including carpeting and vinyl tile, shall not be continued under loadbearing walls.

Roof Construction:	Trussed rafters shall be designed and constructed in accordance with Truss Plate Institute (TPI 1-1995), “National Design Standard for Metal-Plate-Connected Wood Truss Construction”, and the appropriate HUD Truss Connector Bulletin.

MANUFACTURING  PLANT(S):

Premier Panels covered under this Bulletin will be produced in the following plant(s):

Premier Building Systems

4609 70th Ave. E

Fife, Washington  98424

Premier Building Systems

3434 West Papago Street

Phoenix, Arizona  85009-6733

The appropriate HUD Field Office or Homeownership Center in whose jurisdiction the manufacturing plant is located, or HUD designated representative will inspect this (these) plant(s) in accordance with prescribed procedures.

QUALITY CONTROL:

The appropriate HUD Field Office or Homeownership Center in whose jurisdiction the manufacturing plant is located, or the State Agency (in Category III states) shall review and approve plant fabrication procedures and quality control program, to ensure compliance with approved plans and specifications.  The quality control program shall include field erection or supervision by Underwriter’s Laboratories, Inc.

-19-

RECORD  OF  PROPERTIES:

The manufacturer shall provide HUD a list of the first ten properties in which the component or system described in this Bulletin is used.  The list shall include the complete address, or description of location, and approximate date of installation or erection.  Failure of the manufacturer to provide HUD with the above information may result in cancellation of this Bulletin.

NOTICE  OF  CHANGES:

The manufacturer shall inform HUD in advance of changes in production facilities, transportation, field erection procedures, design, or materials used in this product.  Further, the manufacturer must inform HUD of any revision to corporate structure, change of address or change in name or affiliation of the prime manufacturer.  Failure of the manufacturer to notify HUD of any of the above changes may result in cancellation of this Bulletin.

EVALUATION:

This SEB is valid for a period of three years from the date of initial issuance or most recent renewal or revision, whichever is later.  The holder of this SEB shall apply for a renewal or revision 90 days prior to the Review Date printed on this SEB.  Submittals for renewal or revision shall be sent to:

U. S. Department of Housing and Urban Development

Office of Manufactured Housing Programs

451 Seventh Street, SW, Room 9168

Washington, DC 20410-8000

Additionally, the appropriate User Fee shall be sent to:

U. S. Department of Housing and Urban Development

Miscellaneous Income - Technical Suitability of Products Fees

Bank of America

P. O. Box 198762

Atlanta, GA  30384-8762

The holder of this SEB may apply for revision at any time prior to the Review Date.  Minor revisions may be in the form a supplement.

If the Department determines that a proposed renewal or supplement constitutes a revision, the appropriate  User Fee for a revision will need to be submitted in accordance with Code of Federal Regulations 24 CFR 200.934, "User Fee System for the Technical Suitability of Products Program", and current User Fee Schedule.

-20-

CANCELLATION:

Failure to apply for a renewal or revision shall constitute a basis for cancellation of the SEB. HUD will notify the manufacturer that the SEB may be canceled when:

1.	conditions under which the document was issued have changed so as to affect production of, or to compromise the integrity of the accepted material, product, or system,

2.	the manufacturer has changed its organizational form without notifying  HUD, or

3.	the manufacturer has not complied with responsibilities it assumed as a condition of HUD's acceptance.

However, before cancellation, HUD will give the manufacturer a written notice of the specific reasons for cancellation, and the opportunity to present views on why the SEB should not be canceled. No refund of fees will be made on a canceled document.

******************************************************************************

This Structural Engineering Bulletin is issued solely for the captioned firm and is not transferable to any person or successor entity.

******************************************************************************

# Text boxes

Premier Industries, Inc.

17001 Fish Point Road

Prior Lake, MN  44372

Shop Fabricated Foam Core Sandwich Panels Premier Panels

March 1, 2008

March 1, 2005

(Supersedes issue dated

June 4, 2001)

1128 Rev. 1

The technical description, requirements and limitations expressed herein do not constitute an endorsement or approval by the Department of Housing and Urban Development (HUD) of the subject matter, and any statement or representation, however made, indicating approval or endorsement by HUD is unauthorized and false, and will be considered a violation of the United States Criminal Code, 18 U.S.C. 709.

NOTICE: THIS BULLETIN APPLIES TO DWELLING UNITS BUILT UNDER HUD HOUSING PROGRAMS. NON-HUD-INSURED UNITS MAY OR MAY NOT BE IN CONFORMINTY WITH THE REQUIREMENTS OF THE HUD MINIMUM PROPERTY STANDARDS.

Any reproduction of this Bulletin must be in its entirety and any use of all or any part of this Bulletin in sales promotion or advertising is prohibited.