GENERAL AGGREGATE BLENDING PROBLEMS

- Given two aggregates A & B, what combination of the two would you use in a blend to meet specification C?

| Sieve | Percent Finer Than |
| --- | --- |
|  | A | B | Spec |
| 12.5 mm | 100 | 100 | 100 |
| 9.5 mm | 92 | 100 | 95-100 |
| 4.75 mm | 70 | 98 | 75-90 |
| 2.36 mm | 43 | 89 | 60-80 |
| 600 m | 14 | 53 | 20-40 |
| 150 m | 2 | 27 | 10-20 |
| 75 m | 1 | 9 | 4-8 |

Percentage of A is _________________________

Percentage of B is _________________________

The following are the results of gradation tests on three aggregates.  Combine them to the  gradation required.  What is the combined specific gravity?

| Sieve | Percent Passing |
| --- | --- |
|  | Aggregate A | Aggregate B | Aggregate C | Required |
| 25 mm | 100 | 100 | 100 | 100 |
| 19 mm | 92 | 100 | 100 | 95 |
| 9.5 mm | 41 | 100 | 100 | 62 |
| 4.75 mm | 19 | 77 | 96 | 45 |
| 2.36 mm | 7 | 60 | 79 | 32 |
| 600 m | 4 | 42 | 40 |  |
| 300 m | 2 | 36 | 16 | 13 |
| 75 m | 1 | 28 | 3 | 5 |
| Specific Gravity | 2.750 | 2.600 | 2.700 |  |

Percent of A is _________________

Percent of B is _________________

Percent of C is _________________

Combined Specific Gravity is _____________

Given the following data develop a mix design.  You are to develop a 12.5 mm nominal maximum size mix.  Determine the desired blend.

| Sieve | 3/8 Crushed Gravel | No. 67 Limestone | Limestone Screenings | Concrete Sand |
| --- | --- | --- | --- | --- |
| 25 mm | 100 | 100 | 100 | 100 |
| 19 mm | 100 | 98 | 100 | 100 |
| 12.5 mm | 100 | 65 | 100 | 100 |
| 9.5 mm | 88 | 34 | 100 | 100 |
| 4.75 mm | 57 | 6 | 72 | 96 |
| 2.36 mm | 36 | 5 | 42 | 91 |
| 1.18 mm | 23 | 5 | 24 | 78 |
| 0.600 | 15 | 4 | 18 | 51 |
| 0.300 | 10 | 3 | 13 | 16 |
| 0.150 | 6 | 3 | 10 | 3 |
| 0.075 | 3 | 2 | 8 | 1 |
| Percent |  |  |  |  |
| Coarse Aggregate Angularity | 87/78 | 100/100 |  |  |
| Fine Aggregate Angularity |  |  | 45.0 | 45.4 |
| Los Angeles Abrasion | 39 | 24 |  |  |
| Absorption | 0.5 % | 0.4 % | 1.6 | 0.3 |
| Bulk Specific Gravity | 2.620 | 2.722 | 2.721 | 2.639 |
| Sand Equivalent |  |  | 57 | 98 |
| Percent of each sieve | 51 | 26 | 15 | 8 |

.