MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A17753 | In-Flight Anomaly Number -- | Contractor Report Number T-068 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title ET-118 L02 FEEDLINE FOAM DEBOND |
| EICN# -- | ELEMENT ET | Contractor LOCKHEED MARTIN | FSCM# -- | FCRIT 3 |
| HCRIT 1 | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE L02 FEEDLINE | PART# 80971028425-009 | SER/LOT# 162370 | MANUFACTURER LMMSS |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode MSI - INSULATION | Cause MP - MFG-PRC |
| System TPS | Defect DD - DETACH | Material F - INSUL | Work Contact ESMA ALDAHIR | Fail Date 01/29/2002 |
| Received at MSFC 02/12/2002 | Date Isolated 01/29/2002 | FMEA Reference 5.8.1.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom MSI - INSULATION | Time Cycle -- |
| Effectivity Text ETS 93, 94, 112 117 AND SUBSEQUENT |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 08/12/2002 | CN RSLV SBMT 07/26/2002 | Defer Date -- | Add Date 02/12/2002 | R/C Codes 2 - MFG 3 - F/TE -- |
| Assignee |
| Design S. HOLMES | Chief Engineer N. OTTE | S & MA K. LAYNE | Project -- | Project MGR J. SMELSER |
| Approval |
| Design S. HOLMES | Chief Engineer N. OTTE | S & MA A. DANIELS | Project -- | Project MGR T. GREENWOOD |
| PAC Assignee T. WHITE | PAC Review Complete TW | MSFC Closure Date 07/30/2002 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description A 17 INCH LONG - 360 DEGREE CIRCUMFERENTIAL FOAM (BX-250) DEBOND WAS IDENTIFIED ON ET-118'S LO2 F/L SECTION (P/N 80971028425-009 - S/N 00000162370), BETWEEN STATIONS 1129 AND 1377. THE AREA OF DEBOND IS JUST AFT OF THE FEEDLINE'S MOUNTING BRACKET (STA. 1129). A FINAL ASSY. TECHNICIAN, WHO WAS PERFORMING A FOAM CLOSEOUT OPERATION ON THE LO2 FEEDLINE SUPPORT, DISCOVERED THE DISCREPANCY. TECHNICIAN, WHO WAS PERFORMING A FOAM CLOSEOUT OPERATION ON THE LO2 FEEDLINE SUPPORT, DISCOVERED THE DISCREPANCY. |
| Contractor Investigation/Resolution 2/12/2002 - CONTRACTOR SUBMITTED OPENER PROBLEM REPORT AS FOLLOWS: PROBLEM DESCRIPTION ------------------- A 17 INCH LONG - 360 DEGREE CIRCUMFERENTIAL FOAM (BX-250) DEBOND WAS IDENTIFIED ON ET-118'S LO2 F/L SECTION (P/N 80971028425-009 - S/N 00000162370), BETWEEN STATIONS 1129 AND 1377. THE AREA OF DEBOND IS JUST AFT OF THE FEEDLINE'S MOUNTING BRACKET (STA. 1129). A FINAL ASSY. TECHNICIAN, WHO WAS PERFORMING A FOAM CLOSEOUT OPERATION ON THE LO2 FEEDLINE SUPPORT, DISCOVERED THE DISCREPANCY. CRITICALITY: THE FAILURE MODE FOR LOSS OF FOAM IS A CRIT. 1; FMEA ITEM CODE 5.8.1.1. HOWEVER, NO LOSS OF FOAM OCCURRED, THEREFORE THIS IS A DISCRETIONARY CAPS. GENERAL ------- DURING A FOAM CLOSE OUT OPERATION IN FINAL ASSEMBLY, A TECHNICIAN OBSERVED A "BUMP" (A RELATIVELY ABRUPT CONVEXITY ON THE SURFACE) IN THE FOAM JUST AFT OF THE MOUNTING BRACKETS AT STATION 1129. AFTER THE SUSPECT AREA WAS IDENTIFIED, A 4" X 4" SECTION WAS REMOVED VIA N052926, AND A VISUAL INSPECTION WAS PERFORMED. THE REMOVED SECTION WAS NOT BONDED TO THE SUBSTRATE; HOWEVER, A RESIDUE OF FOAM REMAINED ADHERED TO THE SUBSTRATE. CONSEQUENTLY, A FAILURE ANALYSIS INVESTIGATION WAS INITIATED; THE LO2 FEEDLINE WAS REMOVED AND PREPPED FOR EXAMINATION, VIA NCD N023781. AS A RESULT OF THE FAILURE ANALYSIS, IT WAS DEDUCED THAT THE SUSPECT CONDITION WAS A 17-INCH LONG - 360-DEGREE CIRCUMFERENTIAL FOAM (BX-250) DEBOND. TASK I. FAILURE INVESTIGATION --------------------- A. COMPILE LIST OF ALL AFFECTED PARTS (P/NS & S/NS) AND THE ETS THAT THEY WERE INSTALLED ON, USING A SET CRITERIA (LO2 FEEDLINES SPRAYED WITH BX-250). RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/8/2002 CLOSURE STATEMENT ----------------- REFERENCE: ATTACHED SPREADSHEET FOR DETAILS. B. PERFORM NCD SEARCH ON SIMILAR DEBOND ISSUES THAT MAY HAVE OCCURRED PRIOR TO EXISTING ISSUE. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 C. REVIEW BUILD PAPER FOR AFFECTED ETS TO DETERMINE BX-250 SPRAY PROCESS APPLICATION UTILIZED IN THE MANUFACTURING OF THE LO2 FEEDLINES. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 D. REVIEW LAB REPORT OF THE BX-250 MATERIAL UTILIZED TO INSULATE ET-118'S LO2 FEEDLINE. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 E. IDENTIFY AND PERFORM FINGERPRINT TESTING ON RETAINS OF THE BX- 250 MATERIAL UTILIZED TO INSULATE ET-118S NONCONFORMING LO2 FEEDLINE. IN ADDITION, PERFORM SAME FINGERPRINT TESTING ON TWO RANDOMLY SELECTED BX-250 MATERIAL LOTS CURRENTLY WITHIN UPDATED SHELF LIFE AVAILABLE AT MAF. RESPONSIBILITY: D. SPIERS - 4710 / R. LEBOEUF - 4700 ECD: 2/18/2002 F. PERFORM FAILURE ANALYSIS AS DIRECTED PER NCD N023781. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 D. BURAS - 4620 / P. HINKELDEY - 4600 ECD: 2/20/2002 G. INTERVIEW TECHNICIANS IN SOFI SMALL COMPONENT SHOP TO DETERMINE BX-250 SPRAY PROCESS APPLICATION UTILIZED IN THE MANUFACTURING OF LO2 FEEDLINES. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 H. RE-VALIDATE THE APPLICATION OF BX-265 FOAM TO THE LO2 FEEDLINES IDENTIFIED IN "A". RESPONSIBILITY: V. MORALES - 3743 / D. WESTPHAL - 3740 H. GEORGE - 3614 / M. JAVERY - 3600 D. BURAS - 4620 / P. HINKELDEY - 4600 J.E. MOORE - 3673 / J. STANLEY - 3670 ECD: 2/20/2002 I. REVISE MPPS FOR LO2 FEEDLINES TO ADD ONE ADDITIONAL PLUG PULL TEST. ENGINEERING TO PROVIDE LOCATION. RESPONSIBILITY: E. SWEET - 4000 M. RIPOLL - 3614 / M. JAVERY - 3600 V. MORALES - 3743 / D.WESTPHAL - 3743 ECD: 3/15/2002 J. PERFORM PLUG PULL TESTS IN ON ETS 94, 112, 113, 114 AND 118'S LO2 FEEDLINES. IN ADDITION, PERFORM PLUG PULL TESTS ON COMPONENT LO2 FEEDLINES. RESPONSIBILITY: E SWEET - 4000 ECD: 3/15/2002 STATUS OF PLUG PULL TEST RESULTS: O ET-94, WHICH WAS SPRAYED WITH SS-1171 FOAM, MET ENGINEERING REQUIREMENTS, NO CONCERNS. O ET-114, WHICH WAS SPRAYED WITH BX-250 FOAM, MET ENGINEERING REQUIREMENTS ON THREE OF THE FOUR LINES, FOURTH LINE IS PENDING ACCESS. O COMPONENT LO2 FEEDLINES (IN STOCK), WHICH WERE SPRAYED WITH BX- 250 FOAM, MET ENGINEERING REQUIREMENTS ON ONE OF THE THREE LINES. (REFERENCE: N057356, N057357, AND N057358 FOR SPECIFICS) K. IDENTIFY AND TEST POTENTIAL REPAIR METHODS, SOFI AND ADHESIVE MATERIALS FOR NONCONFORMING DEBOND CONDITION AND PROVIDE IN FLIGHT RISK ANALYSIS. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 C. WILLIAMS - 4620 / P. HINKELDEY - 4600 P. KOPFINGER - 4610 / P. HINKELDEY - 4600 ECD: 3/15/2002 L. PERFORM STRESS ANALYSIS ON NONCONFORMING DEBOND CONDITION, USING FLIGHT STRESSES/ENVIRONMENT, AND DETERMINE FLIGHT RISKS. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 ECD: 3/15/2002 M. ASSESS NDE METHODS THAT COULD BE USED TO DETERMINE FLEET HARDWARE ACCEPTABILITY. RESPONSIBILITY: W. USSERY - 4710 / R. LEBOEUF - 4700 C. BOUVIER - 4710 / R. LEBOEUF - 4700 ECD: 3/15/2002 N. DEVELOP FLEET CLEARANCE RATIONALE. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 C. WILLIAMS - 4620 / P. HINKELDEY - 4600 G. COPELAND - 3000 / P. KOPFINGER - 4610 ECD: 3/15/2002 CAUSE ------ PENDING INVESTIGATION TASK II. CORRECTIVE ACTION ------------------ "PENDING INVESTIGATION RESULTS". TASK III. CLEARANCE OF EFFECTIVITIES -------------------------- "PENDING INVESTIGATION RESULTS". TASK IV. CAPS CLOSURE SUMMARY --------------------- "PENDING IDENTIFICATION OF CAUSE(S) 2/25/2002 - REVISION A: PROBLEM -------- A 17 INCH LONG - 360 DEGREE CIRCUMFERENTIAL FOAM (BX-250) DEBOND WAS IDENTIFIED ON ET-118'S LO2 F/L SECTION (P/N 80971028425-009 - S/N 00000162370), BETWEEN STATIONS 1129 AND 1377. THE AREA OF DEBOND IS JUST AFT OF THE FEEDLINE'S MOUNTING BRACKET (STA. 1129). A FINAL ASSY. TECHNICIAN, WHO WAS PERFORMING A FOAM CLOSEOUT OPERATION ON THE LO2 FEEDLINE SUPPORT, DISCOVERED THE DISCREPANCY. CRITICALITY: THE FAILURE MODE FOR LOSS OF FOAM IS A CRIT. 1; FMEA ITEM CODE 5.8.1.1. HOWEVER, NO LOSS OF FOAM OCCURRED, THEREFORE THIS IS A DISCRETIONARY CAPS. REVISION "A": REVISES TASKS I, II, AND III. SEE ASTERISKS (*) FOR CHANGES GENERAL ------- DURING A FOAM CLOSE OUT OPERATION IN FINAL ASSEMBLY, A TECHNICIAN OBSERVED A "BUMP" (A RELATIVELY ABRUPT CONVEXITY ON THE SURFACE) IN THE FOAM JUST AFT OF THE MOUNTING BRACKETS AT STATION 1129. AFTER THE SUSPECT AREA WAS IDENTIFIED, A 4" X 4" SECTION WAS REMOVED VIA N052926, AND A VISUAL INSPECTION WAS PERFORMED. THE REMOVED SECTION WAS NOT BONDED TO THE SUBSTRATE; HOWEVER, A RESIDUE OF FOAM REMAINED ADHERED TO THE SUBSTRATE. CONSEQUENTLY, A FAILURE ANALYSIS INVESTIGATION WAS INITIATED; THE LO2 FEEDLINE WAS REMOVED AND PREPPED FOR EXAMINATION, VIA NCD N023781. AS A RESULT OF THE FAILURE ANALYSIS, IT WAS DEDUCED THAT THE SUSPECT CONDITION WAS A 17-INCH LONG - 360-DEGREE CIRCUMFERENTIAL FOAM (BX-250) DEBOND. TASK I. FAILURE INVESTIGATION --------------------- A. COMPILE LIST OF ALL AFFECTED PARTS (P/NS & S/NS) AND THE ETS THAT THEY WERE INSTALLED ON, USING A SET CRITERIA (LO2 FEEDLINES SPRAYED WITH BX-250). RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/8/2002 CLOSURE STATEMENT ----------------- REFERENCE: ATTACHED EXCEL SPREADSHEET "ACTIONITEM_A_PA" FOR DETAILS. B. PERFORM NCD SEARCH ON SIMILAR DEBOND ISSUES THAT MAY HAVE OCCURRED PRIOR TO EXISTING ISSUE. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 * CLOSURE STATEMENT ----------------- NO PRIOR NONCONFORMANCES FOUND FOR THE AFFECTED HARDWARE IDENTIFIED IN ACTION ITEM "A". C. REVIEW BUILD PAPER FOR AFFECTED ETS TO DETERMINE BX-250 SPRAY PROCESS APPLICATION UTILIZED IN THE MANUFACTURING OF THE LO2 FEEDLINES. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 * CLOSURE STATEMENT ----------------- REVIEWED BUILD PAPER (MPPS) FOR AFFECTED ETS IDENTIFIED IN ACTION ITEM "A", AND THEY CONTAIN INSTRUCTIONS FOR MANUAL SPRAY APPLICATIONS ONLY. D. REVIEW LAB REPORT (PRODUCTION TEST REPORT) OF THE BX-250 MATERIAL UTILIZED TO INSULATE ET-118'S LO2 FEEDLINE. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 * CLOSURE STATEMENT ----------------- LEAD IN AND LEAD OUT PLUG PULL TEST RESULTS FOR ET-118'S SUSPECT LO2 FEEDLINE (P/N 80971028425-009 - S/N 00000162370) MET ENGINEERING REQUIREMENTS. (REFERENCE: ATTACHED LAB JOB NO. 01S0365) E. IDENTIFY AND PERFORM FINGERPRINT TESTING ON RETAINS OF THE BX-250 MATERIAL UTILIZED TO INSULATE ET-118'S NONCONFORMING LO2 FEEDLINE (00G273). IN ADDITION, PERFORM SAME FINGERPRINT TESTING ON TWO RANDOMLY SELECTED BX-250 MATERIAL LOTS CURRENTLY WITHIN UPDATED SHELF LIFE AVAILABLE AT MAF (01G061 SL02 AND 01G129 SL02). RESPONSIBILITY: D. SPIERS - 4710 / R. LEBOEUF - 4700 ECD: 2/18/2002 COMPLETE: 2/11/2002 * CLOSURE STATEMENT ----------------- FINGERPRINT ANALYSIS PERFORMED ON THE B-COMPONENT OF BX-250 RETAINED FROM 00G273 AND TWO OTHER SHELF-LIFE JOBS (01G061 SL02 AND 01G129 SL02) RESULTED IN TOTAL FLAME RETARDANT CONTENT VALUES AND ORIGINAL MAJOR COMPONENT PEAK VALUES CONSISTENT WITH THE CURRENT DATABASE OF FINGERPRINT DATA. THEREFORE, THERE ARE NO CONCERNS WITH THE BX-250 MATERIAL. (REFERENCE: ATTACHED LAB REPORT NO. 02A013 FOR SPECIFICS) F. PERFORM FAILURE ANALYSIS AS DIRECTED PER NCD N023781, AND DETERMINE CAUSE. * RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 D. BURAS - 4620 / P. HINKELDEY - 4600 ECD: 4/2/2002 * STATUS OF FAILURE ANALYSIS RESULTS: ----------------------------------- THE OBJECTIVE OF THE FAILURE ANALYSIS, PERFORMED PER NCD N023781, WAS TO DETERMINE THE CAUSE OF THE FOAM DEBOND DISCREPANCY IDENTIFIED ON ET-118'S LO2 FEEDLINE AT MAF. IT INCLUDED IDENTIFYING THE AREA OF DEBOND, PLUG PULL TESTS, AND KNIT LINE ANALYSIS. DEBOND AREA WAS APPROXIMATELY 17" IN LENGTH AND 3600 AROUND JUST AFT OF THE FEEDLINE'S MOUNTING BRACKET (STA. 1129). PLUG PULLS PERFORMED OUTSIDE OF AREA OF DEBOND WERE ALL FOUND TO BE ABOVE THE ENGINEERING REQUIREMENT OF 35 PSI. IN ADDITION, PLUG PULL TESTS PERFORMED IN THE AREA OF DEBOND PRODUCED FAILING RESULTS (BELOW ENGINEERING REQUIREMENT). KNIT LINE ANALYSIS OF REMOVED FOAM ILLUSTRATED THAT ALL KNIT LINES WERE OF NOMINAL THICKNESS (" 0.375"). THE SUSPECT CONDITION HAS BEEN ISOLATED TO THE AREA AT THE FORWARD END OF THE STRAIGHT FEEDLINE SECTIONS NEAR THE SUPPORT BRACKETS. DUE TO THE SPRAY START-UP PROCESS, THIS AREA HAS A THICKER INITIAL LAYER OF FOAM (" 0.75"). IN ADDITION, EVIDENCE OF DISTORTED FOAM CELLS FROM ADVERSE FLOW OF BLOWING AGENT WAS OBSERVED. (REFERENCE: ATTACHED NCD N023781, AND E-MAIL FROM DAVE BURAS, DATED 2/21/2002) G. INTERVIEW TECHNICIANS IN SOFI SMALL COMPONENT SHOP TO DETERMINE BX- 250 SPRAY PROCESS APPLICATION UTILIZED IN THE MANUFACTURING OF LO2 FEEDLINES. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 * CLOSURE STATEMENT ----------------- INTERVIEWED THE TWO TECHNICIANS WHO SPRAYED THE DISCREPANT LO2 FEED LINE, THEY STATED THAT ALL LO2 FEED LINES SPRAYED WITH BX-250 WERE SPRAYED VIA SEMI-AUTOMATIC SPRAY METHOD WITH THE EXCEPTION OF ONE (80971028425-019--ET-119), WHICH WAS A MANUAL SPRAY. H. DUE TO THE DELINEATION OF BX-250 FOAM, RE-VALIDATE THE APPLICATION OF BX-265 FOAM TO THE LO2 FEEDLINES (80971028425 - 009, - 010, AND - 019S). RESPONSIBILITY: V. MORALES - 3743 / D. WESTPHAL - 3740 H. GEORGE - 3614 / M. JAVERY -3600 D. BURAS - 4620 / P. HINKELDEY - 4600 J.E. MOORE - 3673 / J. STANLEY - 3670 ECD: 2/20/2002 ECD: 4/2/2002 - EXTENSION IS DUE TO SCHEDULE IMPACTS IN FINAL ASSY. (REF. E-MAIL FORM MOORE, J.E., DATED 2/20/2002) I. REVISE MPPS FOR LO2 FEEDLINES TO ADD ONE ADDITIONAL PLUG PULL TEST. ENGINEERING TO PROVIDE LOCATION. RESPONSIBILITY: E. SWEET - 4000 M. RIPOLL - 3614 / M. JAVERY - 3600 V. MORALES - 3743 / D. WESTPHAL - 3743 ECD: 3/15/2002 J. PERFORM PLUG PULL TESTS ON ETS 93, 94, 112 THROUGH 118, AND COMPONENT LO2 FEEDLINES. RESPONSIBILITY: E. SWEET - 4000 ECD: 3/15/2002 * STATUS OF PLUG PULL TEST RESULTS: -------------------------------- O ET-94 - PLUG PULL RESULTS MET ENGINEERING REQUIREMENTS, NO CONCERNS. ET-94'S LO2 FEEDLINES WERE SPRAYED WITH SS-1171. (REFERENCE: N023758 FOR SPECIFICS) O ET-93 - DUE TO ET-94'S SUCCESSFUL PLUG PULL RESULTS, IT WAS CONFIRMED THAT THE DEBOND CONDITION IS ISOLATED TO BX-250 SPRAYED LO2 FEEDLINES. THEREFORE, NO PLUG PULL TESTS WERE REQUIRED, BECAUSE ET- 93'S LO2 FEEDLINES WERE SPRAYED WITH SS-1171. O ET-112 RESULTS FOR THE TWO BX250 FEEDLINES ARE AS FOLLOWS: - PN 80971028425-010 - S/N 1039000; FOUR OF SIX PLUG PULL TESTS MET ENGINEERING REQUIREMENTS. STRESS ANALYSIS WAS PERFORMED TO SHOW BX- 250 FOAM WOULD NOT 'DIVOT' (FS > 2.0) AS A RESULT OF LOW ADHESION STRENGTH TO THE LO2 FEEDLINE. REFERENCE ACTION ITEM "L" FOR DETAILS OF ANALYSIS. (REFERENCE: E-MAIL FROM JEFF PILET DATED 2/18/2002, ET- 112'S FRR CHARTS DATED FEBRUARY 14TH OF 2002). - PN 80971028425-019 - S/N 1044670; ALL 3 PLUG PULLS MET ENGINEERING REQUIREMENTS. (REFERENCE : PR-ET-112-TS-0013) O ET-114, WHICH WAS SPRAYED WITH BX-250 FOAM, MET ENGINEERING REQUIREMENTS ON ALL FOUR LINES. (REFERENCE: PR-ET-114-TS-0007) O COMPONENT LO2 FEEDLINES (IN STOCK), WHICH WERE SPRAYED WITH BX-250 FOAM, MET ENGINEERING REQUIREMENTS ON ONE OF THE THREE LINES. (REFERENCE: NCDS N057356, N057357, AND N057358 FOR SPECIFICS) K. IDENTIFY AND TEST POTENTIAL REPAIR METHODS, SOFI AND ADHESIVE MATERIALS FOR NONCONFORMING DEBOND CONDITION AND PROVIDE IN FLIGHT RISK ANALYSIS. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 C. WILLIAMS - 4620 / P. HINKELDEY - 4600 P. KOPFINGER - 4610 / P. HINKELDEY - 4600 ECD: 3/15/2002 L. PERFORM STRESS ANALYSIS ON NONCONFORMING DEBOND CONDITION, USING FLIGHT STRESSES / ENVIRONMENT, AND DETERMINE FLIGHT RISKS. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 ECD: 3/15/2002 COMPLETE: 2/14/2002 * CLOSURE STATEMENT ----------------- STRESS ANALYSIS WAS PERFORMED TO DEMONSTRATE THAT BX-250 FOAM WOULD NOT 'DIVOT' AS A RESULT OF LOW ADHESION STRENGTH TO THE LO2 FEEDLINE. ANALYSIS WAS BASED ON ET-112'S PLUG PULL VALUES AND THE MINIMUM VALUE EXCEEDING A REALISTIC ESTIMATE OF THE MAXIMUM FOAM CELL 'BURST' PRESSURE IN FLIGHT (12.6 PSI > 4.5 PSI @ -2970F), AT THE FOAM TO SUBSTRATE BONDLINE. ANALYSIS ALSO SHOWED THAT THE FOAM WOULD NOT EXCEED IT'S STRAIN CAPABILITY UNDER 4.5 PSI PRESSURE LOADING. THE HIGH ELASTICITY OF BX-250 ALLOWS THE FOAM TO EXPAND AND INCREASE THE 'DEBONDED' CAVITY VOLUME, AND THEREBY DECREASE THE 'BURST' PRESSURE SUCH THAT THE FINAL CONDITION OF EQUILIBRIUM RESULTS IN A LARGE FS (FS >> 2.0) AGAINST TPS LOSS. (REFERENCE: E-MAIL FROM JEFF PILET DATED 2/21/2002, AND ET-112'S FRR CHARTS DATED FEBRUARY 14TH OF 2002). * M. ASSESS NDE METHODS THAT COULD BE USED TO DETERMINE FLEET HARDWARE ACCEPTANCE. RESPONSIBILITY: W. USSERY/C. BOUVIER - 4710/R. LEBOEUF-4700 ECD: 3/15/2002 CANCELED - PLUG PULL METHOD WILL BE USED N. DEVELOP FLEET CLEARANCE RATIONALE. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 C. WILLIAMS - 4620 / P. HINKELDEY - 4600 P. KOPFINGER - 4610 / P. HINKELDEY - 4600 ECD: 3/15/2002 * STATUS OF FLEET CLEARANCE RATIONALE: ------------------------------------ REFERENCE: ACTION ITEM "J" FOR FLEET CLEARANCE RATIONALE * CAUSE ----- PENDING INVESTIGATION * TASK II. CORRECTIVE ACTION ----------------- THE FOLLOWING CORRECTIVE ACTIONS ARE IN WORK: O SOFI AND ADHESIVE MATERIALS REPAIR METHODS FOR DISCREPANT LINES O VALIDATION OF BX-265 SPRAY PROCESS O MPPS FOR LO2 FEEDLINES TO INCLUDE ADDITIONAL PLUG PULL TEST * TASK III. CLEARANCE OF EFFECTIVITIES -------------------------- O ET-93 - NO FLEET CONCERNS (REFERENCE: ACTION ITEM "J") O ET-94 - NO FLEET CONCERNS (REFERENCE: ACTION ITEM "J") O ET-112 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") O ET-114 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") O ETS 113, 115 THROUGH 117 ARE PENDING PLUG PULL TEST RESULTS. TASK IV. CAPS CLOSURE SUMMARY -------------------- "PENDING IDENTIFICATION OF CAUSE(S) 07/01/2002 - CONTRACTOR SUBMITTED CLOSURE REQUEST AS FOLLOWS: PROBLEM -------- A 17 INCH LONG - 360 DEGREE CIRCUMFERENTIAL FOAM (BX-250) DEBOND WAS IDENTIFIED ON ET-118'S LO2 F/L SECTION (P/N 80971028425-009 - S/N 00000162370), BETWEEN STATIONS 1129 AND 1377. THE AREA OF DEBOND IS JUST AFT OF THE FEEDLINE'S MOUNTING BRACKET (STA. 1129). A FINAL ASSY. TECHNICIAN, WHO WAS PERFORMING A FOAM CLOSEOUT OPERATION ON THE LO2 FEEDLINE SUPPORT, DISCOVERED THE DISCREPANCY. GENERAL ------- DURING A FOAM CLOSE OUT OPERATION IN FINAL ASSEMBLY, A TECHNICIAN OBSERVED A "BUMP" (A RELATIVELY ABRUPT CONVEXITY ON THE SURFACE) IN THE FOAM JUST AFT OF THE MOUNTING BRACKETS AT STATION 1129. AFTER THE SUSPECT AREA WAS IDENTIFIED, A 4" X 4" SECTION WAS REMOVED VIA N052926, AND A VISUAL INSPECTION WAS PERFORMED. THE REMOVED SECTION WAS NOT BONDED TO THE SUBSTRATE; HOWEVER, A RESIDUE OF FOAM REMAINED ADHERED TO THE SUBSTRATE. CONSEQUENTLY, A FAILURE ANALYSIS INVESTIGATION WAS INITIATED; THE LO2 FEEDLINE WAS REMOVED AND PREPPED FOR EXAMINATION, VIA NCD N023781. AS A RESULT OF THE FAILURE ANALYSIS, IT WAS DETERMINED THAT THE SUSPECT CONDITION WAS A 17-INCH LONG - 360-DEGREE CIRCUMFERENTIAL FOAM (BX-250) DEBOND. MADE TASK I. FAILURE INVESTIGATION --------------------- A. COMPILE LIST OF ALL AFFECTED PARTS (P/NS & S/NS) AND THE ETS THAT THEY WERE INSTALLED ON, USING A SET CRITERIA (LO2 FEEDLINES SPRAYED WITH BX-250). RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/8/2002 CLOSURE STATEMENT ----------------- REFERENCE: ATTACHED EXCEL SPREADSHEET "ACTION ITEM_A_PA" FOR DETAILS. DETAILS. B. PERFORM NCD SEARCH ON SIMILAR DEBOND ISSUES THAT MAY HAVE OCCURRED PRIOR TO EXISTING ISSUE. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 CLOSURE STATEMENT ----------------- NO PRIOR NONCONFORMANCES FOR SIMILAR DEBOND ISSUES WERE FOUND FOR THE AFFECTED HARDWARE IDENTIFIED IN ACTION ITEM "A". C. REVIEW BUILD PAPER FOR AFFECTED ETS TO DETERMINE WHAT BX-250 SPRAY APPLICATION PROCESS WAS SPECIFIED IN THE LO2 FEEDLINES MANUFACTURING PROCESS PLANS. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 CLOSURE STATEMENT ----------------- REVIEWED BUILD PAPER (MPPS) FOR AFFECTED ETS IDENTIFIED IN ACTION ITEM "A", AND THEY CONTAIN INSTRUCTIONS FOR MANUAL SPRAY APPLICATIONS ONLY. D. REVIEW LAB REPORT (PRODUCTION TEST REPORT) OF THE BX-250 MATERIAL UTILIZED TO INSULATE ET-118'S LO2 FEEDLINE. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 CLOSURE STATEMENT ----------------- LEAD IN AND LEAD OUT PLUG PULL TEST RESULTS FOR ET-118' SUSPECT LO2 FEEDLINE (P/N 80971028425-009 - S/N 00000162370) MET ENGINEERING REQUIREMENTS. (REFERENCE: ATTACHED LAB JOB NO. 01S0365) E. IDENTIFY AND PERFORM FINGERPRINT TESTING ON RETAINS OF THE BX- 250 MATERIAL UTILIZED TO INSULATE ET-118'S NONCONFORMING LO2 FEEDLINE (00G273). IN ADDITION, PERFORM SAME FINGERPRINT TESTING ON TWO RANDOMLY SELECTED BX-250 MATERIAL LOTS CURRENTLY WITHIN UPDATED SHELF LIFE AVAILABLE AT MAF (01G061 SL02 AND 01G129 SL02). RESPONSIBILITY: D. SPIERS - 4710 / R. LEBOEUF - 4700 ECD: 2/18/2002 COMPLETE: 2/11/2002 CLOSURE STATEMENT ----------------- FINGERPRINT ANALYSIS PERFORMED ON THE B-COMPONENT OF BX-250 RETAINED FROM 00G273 AND TWO OTHER SHELF-LIFE JOBS (01G061 SL02 AND 01G129 SL02) RESULTED IN TOTAL FLAME RETARDANT CONTENT VALUES AND ORIGINAL MAJOR COMPONENT PEAK VALUES CONSISTENT WITH THE CURRENT DATABASE OF FINGERPRINT DATA. THEREFORE, THERE ARE NO CONCERNS WITH THE BX-250 MATERIAL. (REFERENCE: ATTACHED LAB REPORT NO. 02A013 FOR SPECIFICS) F. PERFORM FAILURE ANALYSIS AS DIRECTED PER NCD N023781, AND DETERMINE CAUSE. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 D. BURAS - 4620 / P. HINKELDEY - 4600 ECD: 4/2/2002 ECD: 5/17/2002 - EXTENSION IS DUE TO CONTINUOUS MATERIAL AND PROCESS EVALUATION. COMPLETE: 5/7/2002 * CLOSURE STATEMENT ----------------- THE OBJECTIVE OF THE FAILURE ANALYSIS, PERFORMED PER NCD N023781, WAS TO DETERMINE THE CAUSE OF THE FOAM DEBOND DISCREPANCY IDENTIFIED ON ET- 118'S LO2 FEEDLINE AT MAF. IT INCLUDED IDENTIFYING THE AREA OF DEBOND, PLUG PULL TESTS, AND KNIT LINE ANALYSIS. DEBOND AREA WAS APPROXIMATELY 17"IN LENGTH AND 360 DEGREE AROUND JUST AFT OF THE FEEDLINE'S MOUNTING BRACKET (STA. 1129). PLUG PULLS PERFORMED OUTSIDE OF AREA OF DEBOND WERE ALL FOUND TO BE ABOVE THE ENGINEERING REQUIREMENT OF 35 PSI. IN ADDITION, PLUG PULL TESTS PERFORMED IN THE AREA OF DEBOND PRODUCED FAILING RESULTS (BELOW ENGINEERING REQUIREMENT). KNIT LINE ANALYSIS OF REMOVED FOAM FROM ACCEPTABLE PLUG PULL LOCATIONS INDICATED THAT ALL KNIT LINES WERE OF NOMINAL THICKNESS (~/= 0.375"). THE SUSPECT CONDITION HAS BEEN ISOLATED TO THE AREA AT THE FWD END OF THE STRAIGHT FEEDLINE SECTIONS AFT OF THE SUPPORT BRACKETS. DUE TO THE SPRAY START- UP PROCESS, THE DEBOND AREA HAS A THICKER INITIAL LAYER OF FOAM (~/= 0.75"). IN ADDITION, EVIDENCE OF DISTORTED FOAM CELLS FROM ADVERSE FLOW OF BLOWING AGENT WAS OBSERVED. FURTHERMORE, REGRESSION ANALYSIS OF PLUG PULL AND KNITLINE DATA WAS PERFORMED, AND THE RESULTS ILLUSTRATE A DECREASE IN TENSILE VALUES AND AN INCREASE IN THICKNESS VALUES ACROSS SAMPLES. IN VIEW OF THE RESULTS, IT IS EVIDENT THAT A CHANGE OCCURRED OVER A MEASURABLE PERIOD OF TIME IN THE SPRAY START UP PROCESS. THE PROCESS CHANGE WAS ATTRIBUTED TO, BUT NOT LIMITED TO VARIATION IN THE SPRAY START UP PROCESS. IN CONCLUSION, THE MOST PROBABLE CAUSE OF FOAM DEBOND IS ATTRIBUTED TO PROCESS CREEP. (REFERENCE: ATTACHED NCD N023781, MIKE KELLEY'S STATISTICAL ANALYSIS PRESENTATION, AND E-MAIL FROM DAVE BURAS, DATED 2/21/2002) G. INTERVIEW TECHNICIANS IN SOFI SMALL COMPONENT SHOP TO DETERMINE BX-250 SPRAY PROCESS APPLICATION UTILIZED IN THE MANUFACTURING OF LO2 FEEDLINES. RESPONSIBILITY: E. ALDAHIR - 3741 / D. WESTPHAL - 3740 ECD: 2/20/2002 COMPLETE: 2/19/2002 CLOSURE STATEMENT ----------------- INTERVIEWED THE TWO TECHNICIANS WHO SPRAYED THE DISCREPANT LO2 FEED LINE, THEY STATED THAT ALL LO2 FEED LINES SPRAYED WITH BX-250 WERE SPRAYED VIA SEMI-AUTOMATIC SPRAY METHOD WITH THE EXCEPTION OF ONE (80971028425-019--ET-119), WHICH WAS A MANUAL SPRAY. * H. DUE TO THE PHASE OUT OF BX-250 FOAM, RE-VALIDATE THE APPLICATION OF BX-265 FOAM TO THE LO2 FEEDLINES (80971028425 - 029, - 030, AND - 039S). RESPONSIBILITY: V. MORALES - 3743 / D. WESTPHAL - 3740 H. GEORGE - 3614 / M. JAVERY - 3600 D. BURAS - 4620 / P. HINKELDEY - 4600 J.E. MOORE - 3673 / J. STANLEY - 3670 ECD: 2/20/2002 ECD: 4/2/2002 - EXTENSION IS DUE TO SCHEDULE IMPACTS IN FINAL ASSY. (REF. E-MAIL FORM MOORE, J.E., DATED 2/20/2002) ECD: 5/27/2002 - PENDING COMPLETION OF FIRST SET OF FLIGHT FEEDLINES. COMPLETE: 5/7/2002 CLOSURE STATEMENT ----------------- AS A RESULT OF THE DEBOND DISCREPANCY FOUND ON ET-118'S FEEDLINE, IT WAS DETERMINED THAT A RE-VALIDATION OF THE FEEDLINE SPRAYS USING BX-265 WAS REQUIRED. THE VALIDATION TEAM DECIDED THAT A TWO-SPRAY METHOD WOULD BE THE MOST ROBUST PROCESS. THE VALIDATION WAS PERFORMED BY APPLYING SOFI TO THE SUPPORT RIBS ("EARS") BY THE MANUAL METHOD, WHICH FILLS BETWEEN THE RIBS AND APPLIES RAMPS FORWARD AND AFT OF THE SUPPORT RIBS. A SUBSEQUENT SEMI-AUTOMATIC APPLICATION WAS PERFORMED USING THE ENTEC LATHE IN A SINGLE PASS FROM THE FORWARD END OF THE FEEDLINE TO THE AFT END. THIS ELIMINATED THE NEED TO HOLD THE GUN IN POSITION FOR MULTIPLE REVOLUTIONS OF THE LATHE TO BUILD UP SOFI OVER THE SUPPORT RIBS, THUS REMOVING THE CAUSE OF THE DEBOND DISCREPANCY. A DOE EXPERIMENT WAS PERFORMED TO DETERMINE THE OPTIMUM COMPONENT FLOW RATE, FEEDLINE ROTATION SPEED, AND GUN TRAVEL SPEED SETTINGS (REF. FINAL REPORT 3614-02-007). THE MPP'S HAVE BEEN REVISED TO INCORPORATE ALL VALIDATION REQUIREMENTS AND AN ADDITIONAL PLUG PULL AFT OF THE SUPPORT RIBS (REF. ACTION ITEM I). THIS ADDITIONAL PLUG-PULL REQUIREMENT HAS BEEN INCORPORATED INTO THE ENGINEERING DRAWINGS AT REVISION K FOR THE 80971028425-029, -030, AND -039. (REFERENCE: E-MAIL FROM VINCE MORALES DATED 5/07/2002) *I. REVISE MPPS FOR LO2 FEEDLINES TO ADD ONE ADDITIONAL PLUG PULL TEST. ENGINEERING TO PROVIDE LOCATION. RESPONSIBILITY: E. SWEET - 4000 M. RIPOLL - 3614 / M. JAVERY - 3600 V. MORALES - 3743 / D. WESTPHAL - 3743 ECD: 3/15/2002 ECD: 5/6/2002 - ACTION ITEM "I" IS PENDING COMPLETION OF ACTION ITEM "H". COMPLETE: 5/7/2002 CLOSURE STATEMENT ----------------- THE MPP'S HAVE BEEN REVISED TO INCORPORATE ALL VALIDATION REQUIREMENTS AND AN ADDITIONAL PLUG PULL AFT OF THE SUPPORT RIBS. THIS ADDITIONAL PLUG-PULL REQUIREMENT HAS BEEN INCORPORATED INTO THE ENGINEERING DRAWINGS AT REVISION K FOR THE 80971028425-029, -030, AND -039. (REFERENCE: E-MAIL FROM VINCE MORALES DATED 5/07/2002) J. PERFORM PLUG PULL TESTS ON ETS 93, 94, 112 THROUGH 118, AND COMPONENT LO2 FEEDLINES. RESPONSIBILITY: E. SWEET - 4000 ECD: 3/15/2002 ECD: 4/2/2002 EXTENSION IS DUE TO ET PRIORITY AND LIMITED ACCESS AREAS FOR PLUG PULL TESTING. ECD: 8/1/2002 EXTENSION IS DUE TO LIMITED ACCESS TO ET-116 STATION 1129 AND REPAIR ISSUES ON STATION 1623. COMPLETE: 6/28/2002 * CLOSURE STATEMENTS: ------------------ 0 ET-94 - PLUG PULL RESULTS MET ENGINEERING REQUIREMENTS, NO CONCERNS. ET-94'S LO2 FEEDLINES WERE SPRAYED WITH SS-1171. (REFERENCE: N023758 FOR SPECIFICS) 0 ET-93 - DUE TO ET-94'S SUCCESSFUL PLUG PULL RESULTS, IT WAS CONFIRMED THAT THE DEBOND CONDITION IS ISOLATED TO BX-250 SPRAYED LO2 FEEDLINES. THEREFORE, NO PLUG PULL TESTS WERE REQUIRED, BECAUSE ET- 93'S LO2 FEEDLINES WERE SPRAYED WITH SS-1171. 0 ET-112 RESULTS FOR THE TWO BX250 FEEDLINES ARE AS FOLLOWS (REMAINING TWO LINES SPRAYED WITH SS1171): - P/N 80971028425-010 - S/N 1039000; FOUR OF SIX PLUG PULL TESTS MET ENGINEERING REQUIREMENTS. STRESS ANALYSIS WAS PERFORMED TO SHOW BX-250 FOAM WOULD NOT DIVOT (FS > 2.0) AS A RESULT OF LOW ADHESION STRENGTH TO THE LO2 FEEDLINE, AND THE LINE WAS DISPOSITIONED "USE AS IS". REFERENCE ACTION ITEM "L" FOR DETAILS OF ANALYSIS. (REFERENCE: E-MAIL FROM JEFF PILET DATED 2/18/2002, ET-112'S FRR CHARTS DATED FEBRUARY 14TH OF 2002). - P/N 80971028425-019 - S/N 1044670; ALL 3 PLUG PULLS MET ENGINEERING REQUIREMENTS. (REFERENCE : PR-ET-112-TS-0013) 0 ET-113 RESULTS FOR THE LO2 FEEDLINES ARE AS FOLLOWS: - P/N 80971028425-010 - S/N 1049800, P/N 80971028425-010 - S/N 1049810, AND P/N 80971028425-019 - S/N 1078830; PLUG PULL TESTS ON ALL THREE FEEDLINES MET ENGINEERING REQUIREMENTS REFERENCE: PR-ET-113-TS-0004). - P/N 80971028425-009 - S/N 1049820 @ STA. 1129 THREE OF THE SEVEN PLUG PULL TESTS MET ENGINEERING REQUIREMENTS. THE FAILED PLUG PULL VALUES WERE EVALUATED AND DEEMED ACCEPTABLE BY ENGINEERING, AND AS A RESULT THE FEEDLINE WAS ISPOSITIONED "USE AS IS" (REFERENCE: PR-ET-113-TS-0004). 0 ET-114 - PLUG PULL TESTS ON ALL FOUR FEEDLINES MET ENGINEERING REQUIREMENTS (REFERENCE: PR-ET-114-TS-0007). 0 ET-115 RESULTS FOR THE LO2 FEEDLINES ARE AS FOLLOWS: - P/N 80971028425-010 - S/N 1103270 @ STATION 1377, AND P/N 80971028425-019 - S/N 1125810 @ STATION 1871, PLUG PULL TESTS ON BOTH FEEDLINES MET ENGINEERING REQUIREMENTS. - P/N 80971028425-009 - S/N 1105310 @ STATION 1129 PLUG PULL TESTS DID NOT MEET ENGINEERING REQUIREMENTS; AS A RESULT THE FEEDLINE WAS REPAIRED. - P/N 80971028425-010 - S/N 1103260 @ STATION 1623 THREE OF THE FOUR PLUG PULL TESTS MET ENGINEERING REQUIREMENTS. THE FAILED PLUG PULL VALUES WERE EVALUATED AND DEEMED ACCEPTABLE BY ENGINEERING, AND AS A RESULT THE FEEDLINE WAS ISPOSITIONED "USE AS IS" (REFERENCE: PR-ET-115-TS-0004). 0 ET-116 RESULTS FOR THE LO2 FEEDLINES ARE AS FOLLOWS: - P/N 80971028425-010 - S/N 1123910 @ STATION 1377, AND P/N 80971028425-019 - S/N 1039010 @ STATION 1871, PLUG PULL TESTS ON BOTH FEEDLINES MET ENGINEERING REQUIREMENTS. - P/N 80971028425-010 - S/N 1123900 @ STATION 1623 PLUG PULL TESTS DID NOT MEET ENGINEERING REQUIREMENT, AND AS A RESULT THE FEEDLINE WAS REPAIRED AT KSC PER PR-ET-.116-TS-0001 - P/N 80971028425-009 - S/N 1126790 @ STATION 1129 FIVE OF THE NINE PLUG PULL TESTS MET ENGINEERING REQUIREMENTS. THE FAILED PLUG PULL VALUES WERE EVALUATED AND DEEMED ACCEPTABLE BY ENGINEERING, AND AS A RESULT THE FEEDLINE WAS ISPOSITIONED "USE AS IS" (REFERENCE: PR-ET-116-TS-0001). 0 ET-117 RESULTS FOR THE LO2 FEEDLINES ARE AS FOLLOWS: - P/N 80971028425-009 - S/N 1143180 @ STATION 1129, P/N 80971028425-010 - S/N 1140670 @ STATION 1623, AND P/N 80971028425-019 - S/N 1143940 @ STATION 1871; PLUG PULL TESTS DID NOT MEET ENGINEERING REQUIREMENT, AND AUTHORIZATION PER OPERATIONS DIRECTIVE # 02/OD/0079 TO REMOVE AND REPAIR FOAM ON FEEDLINE IN ACCORDANCE WITH DISPOSITION PROVIDED ON NCD N036015. - P/N 80971028425-010 - S/N 1140660 @ STATION 1377 AUTHORIZATION PER OPERATIONS DIRECTIVE # 02/OD/0079 FOR PLUG PULL REPAIRS AND "USE AS IS" UPON COMPLETION OF PLUG PULL REPAIRS. 0 ET-118 - PLUG PULL TESTS ON ALL FOUR FEEDLINES DID NOT MEET ENGINEERING REQUIREMENTS, AND AS A RESULT WERE REPAIRED PER NCD N055391, NCD N023766, NCD N055390, AND NCD N023767. 0 ET-119 RESULTS FOR THE LO2 FEEDLINES ARE AS FOLLOWS: - P/N 80971028425-009 - S/N 310020, P/N 80971028425-010 - S/N 1171080, AND P/N 80971028425-010 - S/N 1171070; PLUG PULL TESTS DID NOT MEET ENGINEERING REQUIREMENTS, AND AS A RESULT WERE REWORKED PER NCD N057356, NCD N057357, AND NCD N057358. - P/N 80971028425-019 - S/N 1190660 @ STATION 1871 PLUG PULL TESTS MET ENGINEERING REQUIREMENTS. *K. IDENTIFY AND TEST POTENTIAL REPAIR METHODS, SOFI AND ADHESIVE MATERIALS FOR NONCONFORMING DEBOND CONDITION AND PROVIDE IN FLIGHT RISK ANALYSIS. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 C. WILLIAMS - 4620 / P. HINKELDEY - 4600 P. KOPFINGER - 4610 / P. HINKELDEY - 4600 C. JOHNSON - 4620 / P. HINKELDEY - 4600 ECD: 3/15/2002 ECD: 5/10/2002 CLOSURE PENDING CLOSURE OF REPORT. COMPLETE: 5/02/2002 CLOSURE STATEMENT: ------------------ REPAIR METHOD WAS DEVELOPED AND USED TO REPAIR FEEDLINES ON EXTERNAL TANKS. (REFERENCE: ACTION ITEM "J" AND ETTR-MS-02-8) L. PERFORM STRESS ANALYSIS ON NONCONFORMING DEBOND CONDITION, USING FLIGHT STRESSES / ENVIRONMENT, AND DETERMINE FLIGHT RISKS. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 ECD: 3/15/2002 COMPLETE: 2/14/2002 CLOSURE STATEMENT ----------------- STRESS ANALYSIS WAS PERFORMED TO DEMONSTRATE THAT BX-250 FOAM WOULD NOT 'DIVOT' AS A RESULT OF LOW ADHESION STRENGTH TO THE LO2 FEEDLINE. ANALYSIS DEEMED CREDIBLE BASED ON ET-112'S PLUG PULL VALUES OF WHICH FOUR OF THE SIX EXCEEDED THE MATERIAL PROCESSING SPECIFICATION ACCEPTANCE REQUIREMENT OF 35 PSI, AND THE MINIMUM VALUE EXCEEDING A REALISTIC ESTIMATE OF THE MAXIMUM FOAM CELL 'BURST' PRESSURE IN FLIGHT (12.6 PSI > 4.5 PSI @ -2970F) AT THE FOAM TO SUBSTRATE BOND LINE. ANALYSIS ALSO SHOWED THAT THE FOAM WOULD NOT EXCEED ITS STRAIN CAPABILITY UNDER 4.5 PSI PRESSURE LOADING. THE HIGH ELASTICITY OF BX- 250 ALLOWS THE FOAM TO EXPAND AND INCREASE THE 'DEBONDED' CAVITY VOLUME AND THEREBY DECREASE THE 'BURST' PRESSURE SUCH THAT THE FINAL CONDITION OF EQUILIBRIUM RESULTS IN A LARGE FS (FS >> 2.0) AGAINST TPS LOSS (REFERENCE: E-MAIL FROM JEFF PILET DATED 2/21/2002, AND ET-112'S FRR CHARTS DATED FEBRUARY 14TH OF 2002). M. ASSESS NDE METHODS THAT COULD BE USED TO DETERMINE FLEET HARDWARE ACCEPTANCE. RESPONSIBILITY: W. USSERY / C. BOUVIER - 4710 / R. LEBOEUF - 4700 ECD: 3/15/2002 CANCELED - PLUG PULL METHOD WILL BE USED. N. DEVELOP FLEET CLEARANCE RATIONALE. RESPONSIBILITY: J. PILET - 4130 / F. MANTO - 4100 C. WILLIAMS - 4620 / P. HINKELDEY - 4600 P. KOPFINGER - 4610 / P. HINKELDEY - 4600 ECD: 3/15/2002 (REF. ACTION ITEM "J") COMPLETE: 6/28/2002 STATUS OF FLEET CLEARANCE RATIONALE: ------------------------------------- REFERENCE: ACTION ITEM "J" FOR FLEET CLEARANCE RATIONALE. CAUSE THE MOST PROBABLE CAUSE OF THE FOAM DEBOND DISCREPANCY IS PROCESS CREEP. *TASK II. CORRECTIVE ACTION ------------------ THE FOLLOWING CORRECTIVE ACTIONS HAVE BEEN IMPLEMENTED: 0 ENANCEMENT AND REVALIDATION OF BX-265 SPRAY PROCESS 0 DRAWINGS AND MPPS FOR LO2 FEEDLINES TO INCLUDE ADDITIONAL PLUG PULL TEST *TASK III. CLEARANCE OF EFFECTIVITIES -------------------------- 0 ET-93 - NO FLEET CONCERNS (REFERENCE: ACTION ITEM "J") 0 ET-94 - NO FLEET CONCERNS (REFERENCE: ACTION ITEM "J") 0 ET-112 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J" 0 ET-113 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") 0 ET-114 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") 0 ET-115 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") 0 ET-116 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") 0 ET-117 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") 0 ET-118 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") 0 ET-119 - VEHICLE CLEARED (REFERENCE: ACTION ITEM "J") TASK IV. CAPS CLOSURE SUMMARY -------------------- THE MOST PROBABLE CAUSE OF THE FOAM DEBOND DISCREPANCY, IN THE AREA AT THE FORWARD END OF THE STRAIGHT FEEDLINE SECTION NEAR THE SUPPORT BRACKETS, IS PROCESS CREEP. THE PROCESS CREEP IS ATTRIBUTED TO THE VALIDATION OF BX-250 NOT BEING COMPREHENSIVE ENOUGH IN ITS SCOPE. THE DATA REVIEW REVEALED THAT VARIATION IN THE SPRAY START UP PROCESS APPEARS TO BE THE MOST LIKELY CAUSE FOR THE DEBONDS WHICH LED TO THE PROCESS CREEP CONCLUSION. THE SPRAY PROCESS WAS SEMI-AUTOMATIC. AT START UP THE OPERATOR CONTROLLED THE NUMBER OF SPRAY PASSES IN THE SUPPORT BRACKET AREA, AND WHEN PROPER COVERAGE WAS ACHIEVED, THE OPERATOR ENGAGED THE LATHE CARRIAGE (WHERE SPRAY GUN WAS MOUNTED) DRIVE TO ALLOW AUTOMATIC SPRAY OF THE REMAINDER OF THE LINE. IT IS HIGHLY PROBABLE THAT THE THICKNESS OF FOAM GRADUALLY INCREASED OVER TIME IN THE AREA OF DEBOND. THERE IS NO HARD EVIDENCE TO SUPPORT THIS THEORY, OTHER THAN THE FACT THAT THE DEBOND CONDITION ONLY OCCURRED IN THE FIRST 17" AFT OF THE MOUNTING BRACKET, WHICH IS WHERE THE SPRAY GUN REMAINS STATIONARY. THE DEBOND CONDITION WAS NOT FOUND ON THE REMAINDER OF THE FEEDLINE, WHICH IS WHERE THE SPRAY GUN TRAVELS AT A SET SPEED. THE SPRAY PROCESS WAS ESTABLISHED WITH ET-116'S FEEDLINE POSITIONED AT STATION 1871, WHICH WAS SPRAYED ON SEPTEMBER 22ND OF 2000. PLUG PULL TESTS WERE PERFORMED IN THE SUSPECT AREA. THE PLUG PULL TENSILE VALUES MET ENGINEERING REQUIREMENTS WITH NO INDICATION OF A DEBOND CONDITION. DURING THE FAILURE ANALYSIS INVESTIGATION IT WAS OBSERVED THAT THE KNIT LINE THICKNESS OF REMOVED FOAM FROM ACCEPTABLE PLUG PULL LOCATIONS, WHICH WERE OUTSIDE THE AREA OF DEBOND, WERE OF NOMINAL THICKNESS (~ 0.375"). FURTHERMORE, THE AREA OF DEBOND HAD A THICKER INITIAL LAYER OF FOAM (~ 0.75") AND THERE WAS EVIDENCE OF DISTORTED FOAM CELLS FROM ADVERSE FLOW OF BLOWING AGENT. A REGRESSION ANALYSIS OF THE PLUG PULL DATA SHOWED A DECREASE IN TENSILE VALUES ACROSS SAMPLES. IN ADDITION, A REGRESSION ANALYSIS ON KNITLINE THICKNESS DATA SHOWED AN INCREASE IN KNITLINE THICKNESS ACROSS SAMPLES. THE DATA DEMONSTRATES THAT A CHANGE OCCURRED IN THE SPRAY START UP PROCESS OVER A MEASURABLE PERIOD OF TIME. THE THIRD FEEDLINE SPRAYED (9/29/2000), WHICH WAS ET-113'S FEEDLINE, LOCATED AT STATION 1129, WAS THE FIRST FEEDLINE IMPACTED BY THE CHANGE (PROCESS CREEP). PLUG PULL TENSILE TESTS WERE PERFORMED IN THE SUSPECT AREA, AND FOUR OF THE SIX TENSILE VALUES WERE BELOW THE ENGINEERING REQUIREMENT OF 35 PSI (12.7, 24.3, 20.1, AND 19.2 PSI). HOWEVER, STRESS ANALYSIS WAS PERFORMED AND IT SHOWED THAT BX-250 FOAM WOULD NOT DIVOT (FS > 2.0) AS A RESULT OF LOW ADHESION STRENGTH TO THE LO2 FEEDLINE, AND THE LINE WAS DISPOSITIONED "USE AS IS". THE FEEDLINES THAT WERE SPRAYED FROM MARCH 2001 TO JANUARY 2002 WERE MOST SIGNIFICANTLY AFFECTED BY THE CHANGE BECAUSE THEY CONTAINED THE GREATEST NUMBER OF SLICK OFFS AND TENSILE VALUES THAT WERE BELOW THE ENGINEERING REQUIREMENT OF 35 PSI. TO ASCERTAIN THAT IT WASN'T THE MATERIAL THAT WAS THE CONTRIBUTOR TO THE DEBOND CONDITION, THE MDAT TEAM REVIEWED THE MATERIAL DATA ON THE LOTS OF BX-250 MATERIALS USED ON THE FEEDLINES. THE MDAT TEAM CONCLUDED THAT THERE WAS NO EVIDENCE OF A MATERIAL PROBLEM. IN ADDITION, THE LACK OF MATERIAL PROBLEMS ON OTHER HARDWARE SPRAYED WITH THESE LOTS SUPPORTED THEIR CONCLUSION. A BETTER UNDERSTANDING OF PROCESS VARIABLES AND FINAL PRODUCT RESULTS WOULD REQUIRE A COLLECTION OF PROCESS AND PRODUCT DATA. PROCESS DATA PARAMETERS SUCH AS RPM, IPM, FLOW RATE, OR START / STOP SPRAY POSITIONS AND TIMES WERE NOT TRACKED. THEREFORE, THE DATA WAS NOT AVAILABLE FOR ANALYSIS OF WHICH PROCESS PARAMETERS CONTRIBUTED TO THE DEBOND CONDITION. HOWEVER, AS A RESULT OF THE INVESTIGATION, THE PROCESS WAS UPGRADED TO INCLUDE INSTRUMENTATION THAT WILL PROVIDE READOUTS OF PROCESS DATA, LATHE RPM AND CARRIAGE IPM, TO TRACK AND MAINTAIN PROCESS PERFORMANCE. IN ADDITION TO LEAD IN AND LEAD OUT PLUG PULL TENSILE DATA, ADDITIONAL PLUG PULL TESTS WILL BE PERFORMED IN THE AREA AFT OF THE MOUNTING BRACKET. ALSO, THE APPLICATION OF BX-265 FOAM WAS ENHANCED AND REVALIDATED TO MAKE THE PROCESS MORE ROBUST. THE IMPROVEMENTS TO THE PROCESS WILL AID IN THE PREVENTION OF ANY FUTURE DEFECTS OR NONCONFORMANCES THAT ARE DETRIMENTAL TO FOAM PROPERTIES (ENGINEERING REQUIREMENTS). |
| MSFC Response/Concurrence 02/25/2002 - BOARD ACCEPTED INTERIM CLOSURE UNTIL 4/19/2002 PER RATIONALE (E): THERE IS NO OVERALL SAFETY OF FLIGHT CONCERN. 04/23/02 - PROBLEM REPORT REOPENED DUE TO MSFC APPROVED DEFER UNTIL DATE HAS PASSED. 05/23/2002 - BOARD ACCEPTED INTERIM CLOSURE UNTIL 9/1/2002 PER RATIONALE (E): THERE IS NO OVERALL SAFETY OF FLIGHT CONCERN. SIGNATURES ON FILE IN THE PAC. 7/30/02- MSFC APPROVAL CLOSURE. SIGNATURES ARE ON FILE IN THE PAC. |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A17753 | IFA# -- | Contractor RPT# T-068 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80971028425-009 | Asmnt Part Name LO2 FEEDLINE | Asmnt Serial/Lot# 162370 |
| HCRIT CD 1 | FCRIT CD 1 | CAUSE CD MP - MFG-PRC | FAIL MODE MU - MECH TOLRNCE |
| Asmnt FMEA 5.8.1.1 | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |