### ITEM P-153  CONTROLLED LOW-STRENGTH MATERIAL (CLSM)

DESCRIPTION

153.1.1  This item shall consist of furnishing, transporting, and placing  a controlled low-strength material (CLSM) as flowable backfill in trenches or at other locations shown on the plans or as directed by the Engineer.

MATERIALS

153-2.1 MATERIALS

a.  	Portland Cement.  Portland cement shall conform to the requirements of ASTM [     ]  Type [     ].  If for any reason, cement becomes partially set or contains lumps of caked cement, it shall be rejected.  Cement salvaged from discarded or used bags shall not be used.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Engineer shall specify one of the following :	ASTM C 150 - Type I, II.

ASTM C 595 - Type IP, IS, S, I(PM).

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

b.  	Fly Ash.  Fly Ash shall conform to ASTM C 618, Class C or F.

c.  	Fine Aggregate (Sand).  Fine aggregate shall conform to the requirements of ASTM C 33 except for aggregate gradation.  Any aggregate gradation which produces performance characteristics of the CLSM specified herein will be accepted, except as follows.

Sieve Size		Percent Passing by weight

3/4 inch (19.0 mm)			100

No. 200 (0.075 mm)			0 - 12

d.  	Water.  Water used in mixing shall be free of oil, salt, acid, alkali, sugar, vegetable matter, or other substances injurious to the finished product.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

Dyes and other methods of coloring the backfill material may be incorporated if desired.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

MIX DESIGN

153-3.1 PROPORTIONS.  The contractor shall submit, to the Engineer, a mix design including the proportions and source of materials, admixtures, and dry cubic yard (cubic meter) batch weights.  The mix shall contain a minimum of 50 pounds of cement and 250 pounds fly ash per cubic yard (30 kg of cement and 148 kg of fly ash per cubic meter), with the remainder of the volume composed of sand, water, and any approved admixtures.

a.  Compressive Strength.  CLSM shall be designed to achieve a 28-day compressive strength of 100 to 200 psi (690 to 3 680 kPa)when tested in accordance with ASTM C 39.  There should be no significant strength gain after 28 days.  Test specimens shall be made in accordance with ASTM C 31 except that the samples will not be rodded or vibrated and shall be air cured in their molds for the duration of the cure period.

b.  Consistency.  Consistency of the fresh mixture shall be such that the mixture may be placed without segregation.  A desired consistency may be approximated by filling an open-ended three-inch (75 mm) diameter cylinder, six inches (150 mm) high to the top, with the mixture and the cylinder immediately pulled straight up.  The correct consistency of the mixture will produce an approximate eight-inch (205 mm) diameter circular-type spread without segregation.  Adjustments of the proportions of materials should be made to achieve proper solid suspension and flowable characteristics, however the theoretical yield shall be maintained at one cubic yard (cubic meter) for the given batch weights.

CONSTRUCTION METHODS

153-4.1  PLACEMENT.

a.  	Placement.  CLSM may be placed by any reasonable means from a mixing unit into the space to be filled.  Agitation is required during transportation and waiting time.  Placement shall be performed in such a manner that structures or pipes are not displaced from their desired final position and intrusion of CLSM into undesirable areas is avoided.  The material shall be brought up uniformly to the fill line shown on the plans or as directed to the Engineer.  Each placement of CLSM shall be as continuous an operation as possible.  If CLSM is placed in more than one layer,  the base layer shall be free of surface water and loose of foreign material prior to placement of the next layer.

b.  	Limitations of Placement.  CLSM shall not be placed on frozen ground.  Mixing and placing may begin when the air or ground temperature is at least 35 degrees F (2 degrees C) and rising.  At the time of placement, CLSM shall have a temperature of at least 40 degrees F (4 degrees C).  Mixing and placement shall stop when the air temperature is 40 degrees F (4 degrees C) and falling or when the anticipated air or ground temperature will be 35 degrees F (2 degrees C) or less in the 24 hour period following proposed placement.

153-4.2  CURING AND PROTECTION

a.  	Curing.  The air in contact with the CLSM should be maintained at temperatures above freezing for a minimum of 72 hours.  If the CLSM is subjected to temperatures below 32 degrees F (0 degrees C), the material may be rejected by the Engineer if damage to the material is observed.

b.  	Protection.  The CLSM shall not be subject to loads and shall remain undisturbed by construction activities for a period of 48 hours or until a compressive strength of 15 psi (105 kPa) is obtained.  The Contractor shall be responsible for providing evidence to the Engineer that the material has reached the desired strength.  Acceptable evidence shall be based upon compressive tests made in accordance with paragraph 153-3.1a.

MATERIAL ACCEPTANCE

153-5.1  Acceptance.  Acceptance of CLSM delivered and placed as shown on the plans or as directed by the Engineer shall be based upon mix design approval and batch tickets provided by the Contractor to confirm that the delivered material conforms to the mix design.  The Contractor shall verify by additional testing, each 5,000 cubic yards (3,825 cubic meters) of material used.  Verification shall include confirmation of material proportions and tests of compressive strength to confirm that the material meets the original mix design and the requirements of CLSM as defined in this specification.  Adjustments shall be made as necessary to the proportions and materials prior to further production.

METHOD OF MEASUREMENT

153-6.1  Measurement.  Controlled low strength material shall be measured by the number of [cubic yards (cubic meters)] as computed from the neatline plan and section, adjusted for the quantities for any embedments, and as specified, completed, and accepted..

BASIS OF PAYMENT

153-7.1  Payment.  Accepted quantities of controlled low strength material shall be paid for at the contract unit price per [cubic yard (cubic meter)].  Payment shall be full compensation for all materials, equipment, labor, and incidentals required to complete the work as specified.

TESTING REQUIREMENTS

ASTM C 31	Making and Curing Concrete Test Specimens in the Field

ASTM C 39	Compressive Strength of Cylindrical Concrete

MATERIAL REQUIREMENTS

ASTM C 33	Specification for Concrete Aggregates

ASTM C 150	Specification for Portland Cement

ASTM C 618	Specification for Coal Fly Ash and Raw or Calcined Natural Pozzolan for Use as a Mineral Admixture in Concrete

ASTM C 595	Specification for Blended Hydraulic Cements

END OF ITEM P-153

Intentionally Left Blank