$$203.00A

Section 203.—REMOVAL OF STRUCTURES AND OBSTRUCTIONS

Revised 6 May 2005

# INCLUDE THE FOLLOWING FOR BRIDGE CONCRETE REMOVAL

$$203.04A

  - Add the following:

(a)  Concrete Removal by Mechanical Impact Methods.  Furnish equipment that complies with the following:

(1)  Use power-driven hand tools for removal of existing concrete with the following restrictions:

(a)  Do not use jack hammers heavier than 30 pounds (13.6 kilograms).

(b)  Do not operate 30-pound (13.6 kilogram) jack hammers and mechanical chipping tools at an angle in excess of 45 degrees measured from the surface of the slab.

(c)  Do not use chipping hammers heavier than a nominal 15-pound (6.8-kilogram) class to remove concrete from beneath any reinforcing bar.

(2)  Use hand tools (hammers and chisels) for removal of final particles of concrete or to achieve the required depth.

(b)  Reinforcing Steel.  Clean all reinforcing steel that is to remain in place and has been exposed by removal operations.  Remove all rust and corrosive products, including oil, dirt, concrete fragments, laitance, loose scale, and other coating of any character that would destroy or inhibit the bond with the new concrete.

When cleaned reinforcing steel will be exposed for more than 7 calendar days before placing the concrete, protect the steel from corrosion and contamination.  Clean and/or replace all reinforcing steel corroded or contaminated because of the Contractor's failure to protect the steel.

Prevent cutting or damaging reinforcing steel designated to remain in place.  Repair or replace any damaged bars.

INCLUDE THE FOLLOWING, IF APPLICABLE

$$203.05A

203.05(b).  Delete the Subsection and substitute the following:

(b)  Burn.  Burning is prohibited.  Dispose of material according to Subsection 203.05(a).

$$203.05B

203.05(c).  Add the following after the first sentence of the first paragraph:

Bury debris beyond the toes of fills in areas authorized by the CO.

$$203.05C

203.05(c).  Delete the Subsection and substitute the following:

(c)  Bury.  Burying debris is prohibited.  Dispose of material according to Subsection 203.05(a).