96M03/29/06

S204-96M.doc

Use on all projects.

Section 204. - EXCAVATION AND EMBANKMENT

Description

204.02  Definitions.

(c) Embankment material.

(1) Rock.  Delete the text and substitute the following:

Rock is material containing particles that are retained on the 75 mm sieve and having less than 40 percent passing the 4.75 mm sieve or less than 35 percent passing the 2 mm sieve.

Construction Requirements

204.05  Conserved Topsoil.  Delete the first sentence and substitute the following:

Conserve topsoil from the roadway excavation and from embankment foundation areas to the extent and depth determined by the CO.

Use on projects as appropriate.

204.06  Roadway Excavation.

(b) Rock cuts.  Add the following:

When blasting rock, [use/do not use] controlled blasting methods according to Subsection 205.07.

204.11  Compaction.

(b) Earth embankment.  Delete the first paragraph and substitute the following:

Classify the material according to AASHTO M 145.  For material classified A-1 or A-2-4, determine the optimum moisture content and the maximum density according to AASHTO T 180 method D.  For other material classifications, determine the optimum moisture content and the maximum density according to AASHTO T 99 method C

Delete the third paragraph and substitute the following.

Compact material placed in all embankment layers and the material scarified in cut sections to at least 95 percent of the maximum density.  Determine the in place density and moisture content according to AASHTO T-310 or other approved test procedure.

204.14 Disposal of Unsuitable or Excess Material.  Add the following:

Secure environmental clearances according to Subsection 107.10.

Measurement

204.16

(a) Roadway Excavation.

(1) Include the following volumes in roadway excavation:

(e) Delete the text and substitute the following:

Conserved topsoil stripped from cuts.

(h) Delete the text and substitute the following:

Conserved material taken from stockpiles and used in Section 204 work except topsoil measured under Section 624.  Only materials required to be conserved by the CO are eligible for measurement under this item.

(2) Do not include the following in roadway excavation:  Add the following:

(m) Conserved topsoil stripped from fills.

Payment

204.17  Add the following:

Payment for Item 20401 is limited to ten percent of the plan quantity of excavation in the cut until the slope rounding in that cut is completed.