# Appendix 5-D

# Sample Testing Frequency, Acceptance Test and Control Test Summaries

Attachment 1:  Crushed Aggregate Base Course P-209

## Attachment 2:  Plant Mix Bituminous Pavements P-401

Attachment 3:  Concrete Summary P-501

Attachment 4:  Density Tests Summary, P-152, 154, 155, 208, &P-209

Attachment 5:  Density Tests Summary, P-304

Attachment 6:  Test Summary, P-401

Attachment 7:  Gradation Summary, P-154, 208, 209, 304, 402

Attachment 1:  Crushed Aggregate Base Course P-209

| AIRPORT: |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| AIP PROJECT NO: |  |  |  |  |  |
| CRUSHED AGGREGATE BASE COURSE P-209 |  |  |  |  |  |
| Test | Test Procedures | Min. Testing Tolerance | Information Due By | Frequency of | Freq. & Num. of |
|  |  |  |  | Tests Required | Tests Conducted |
| Preliminary Testing: |  |  |  |  |  |
| LA Abrasion | ASTM C 131 | 45% MAX | Before Start of Production | 1 | 1 |
| Sodium Sulfate Soundness | ASTM C 88 | 12% MAX | " | 1 | 1 |
| Plasticity Index | ASTM D 4318 | MAX 25 | " | 1 | 1 |
| Sand Equivalent | ASTM D 2419 | MIN 35 | " | 1 | 1 |
| Gradation | ASTM C 136 & C 117 | See spec & 3% Max/0.2mm | " | 1 | 1 |
| Fractured Faces | (Para 209-2.1) | (Para 209-2.1) | " | 1 | 1 |
| Flat and Elongated | ASTM D 693 | 15% MAX | " | 1 | 1 |
| Placement & Acceptance: |  |  |  |  |  |
| Gradation | ASTM C 136 & C117 | See Spec. 209-2.1 | Day Following Placement | 1 per day | 10 Total |
|  |  | Table 1. |  |  | (1 per day) |
| Laboratory Compaction and | ASTM D 1557 | --------- | Day Following Placement | 1 per lot | 10 |
| opt. moisture content |  |  |  |  |  |
| Sampling locations | ASTM D 3665 | --------- | Prior to placing | 1 per lot when not ex- | 20 (2 per day) |
| In-place moisture | ASTM D 3017 | +1-1/2% opt. | At time of test | ceeding 2400 sq. yds | 20 (2 per day) |
| In-place density | ASTM D 2922 | 100% of Max | At time of test | " |  |
| Surface Tolerance | 16' Straightedge | 3/8" Max | Within 2 days of placement | 2 (one each direction) | 90 locations |
|  |  |  |  | 90 locations |  |
| Thickness Control | Survey (before and after) | 1/2 inch Max. | At end of placement | ------------- | 50' grid |
| Finish Surface | Survey | + 1/2 inch | At end of placement | ------------ | 50' grid |

Attachment 2:  Plant Mix Bituminous Pavements P-401

| AIRPORT: |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| AIP PROJECT NO: |  |  |  |  |  |
| PLANT MIX BITUMINOUS PAVEMENTS P-401 |  |  |  |  |  |
| Test | Test Procedures | Min. Testing Tolerance | Information Due By | Frequency of | Frequency of Tests |
|  |  |  |  | Tests Required | Conducted |
| Preliminary Testing |  |  |  |  |  |
| Review Test Lab Certification | ASTM D 3666 | Paragraph 401-3.5 | Prior to mix design and | …..... | …........ |
| (for QA and mix design) |  |  | acceptance testing |  |  |
| Review of Certified test reports |  |  |  |  |  |
| Course Aggregate: |  |  |  |  |  |
| Percent of wear | ASTM C131 | 40% MAX | Prior to production | 1 | 1 |
| Flat & Elongated | ASTM D4701 | 8% MAX | “ | 1 | 1 |
| Soundness | ASTM C88 | 13% MAX | “ | 1 | 1 |
| Fractured Face | (Refer 401-2.1) | (Refer 401-2.1) | “ | 1 | 1 |
| Fine Aggregate |  |  |  |  |  |
| Liquid Limit | ASTM D423 | 25% MAX | Prior to production | 1 | 1 |
| Plastic Index | ASTM D424 | 6% MAX | “ | 1 | 1 |
| Sand Equivalent | ASTM D2419 | 35% MIN | “ | 1 | 1 |
| Mineral Filler | ASTM D242 | ----------- | “ | 1 | 1 |
| Bituminous Material | ASTM D3381 | ------------- | “ | ----------- | ----------- |
| Review of job mix formula | Marshall MS-2 | (401-3.2) | “ | 1 | 1 |
|  | (Para 401-3.2) |  |  |  |  |
| Test Section: |  |  |  |  |  |
| Random Sampling | ASTM D3665 | ---------- | Prior to sampling | ------------- | ----------- |
| Stability | Para 401-5.1a(2) | MIN 90 PWL | Next following workday | 3 samples | 3 |
| Flow | Para 401-5.1a(2) | “ | “ | “ | 3 |
| Air void | Para 401-5.1a(2) | “ | “ | “ | 3 |
| MAT Cores | Para 401-5.1b(3) & (4) | “ | “ | 3 cores | 3 |
| Joint Cores | Para 401-5.1b(3) & (4) | “ | “ | 3 cores | 3 |
| Gradation | Para 401-6.3b | Para 6.5 a & b | “ | 2 samples | 2 |
| Asphalt Content | Para 401-6.3a | Para 6.5 a & b | “ | 2 samples | 2 |

| P401 (Continued) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Test | Test Procedures | Min. Testing Tolerance | Information Due By | Frequency of | Frequency of |
|  |  |  |  | Tests Required | Tests Conducted |
| Production: |  |  |  |  |  |
| Random Sampling | ASTM D3665 | ------------ | Prior to sampling | ----------- | 10 lots |
| Lab compacted specimens | ASTM D1559 | ---------- | Next following work day | 1 set per sublot | 10 lots, 120 total |
|  |  |  |  | (3 total) |  |
| Stability of flow | ASTM D1559 | Para 401--5.2 | " | 3 per sublot | 120 |
| Air voids | ASTM D3203 | " | " | 3 per sublot | 120 |
| Bulk sps | ASTM D2726 or D1188 | " | " | 3 per sublot | 120 |
| Theor. Max. spg. | ASTM D2041 | " | " | 2 times per lot | 22 |
| Mat & Joint sampling | ASTM D3665 | " | " | 1 per sublot/4 sub | 40 |
|  |  |  |  | lots per lot |  |
| Mat Density | ASTM D2766 or D1188 | " | " | " | 40 |
| Joint Density | " | " | " | " | 40 |
| Thickness | ---------- | Per plan | " | (Using all cores) | 80 |
| Smoothness | (12-foot straight edge) | 15% MAX measures exceed | Prior to acceptance | 50' intervals both | 50' intervals |
|  |  | tolerance |  | directions | trains & longitudual |
| Grade | Survey | Within 1/2" of plan | Prior to acceptance | 50' intervals | 50' intervals |
| QC: Review of QC plan | Para 401-6.2 | ------------- | 5 days prior production | ---------- | -------- |
| Asphalt Content | ASTM D2172 | 401-6.5 a & b | Submit report & chart on | 2 per lot | 24 |
|  |  |  | next following workday |  |  |
| Ash Content | ASTM D2172 | --------- | " | 1st extraction and | 4 |
|  |  |  |  | every 10 extractions |  |
| Gradation | AASHTO T30 | 401-6.5 a & b | " | 2 times per lot | 40 |
| Moisture content of aggregate | ASTM C566 | -------- | " | 1 per lot | 10 |
| Moisture content of mixture | ASTM D1461 | 0.5% MAX | " | 1 per lot | 10 |
| Temperature of: |  |  |  |  |  |
| Dryer | N/A | (Refer to mix) design & temp | " | 4 per lot | 40 |
| Bitumen storage | N/A | Viscosity curve & Para 401-4.6 | " | 4 per lot | 40 |
| Plant mixture | N/A | -4.7> & -4.8 | " | 4 per lot | 40 |
| Mixture at site | N/A | " | " | 4 per lot | 40 |
| Mixing Time | ASTM D2489 | -95% coated particle | Prior to production | 1 | 1 |
| Certification of Q.C. | ----------- | Para 401-6.1 | Prior to testing | 1 | 1 |
| Testing Equipment |  |  |  |  |  |

Attachment 3:  Concrete Summary P-501

| AIRPORTS: |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AIP PROJECT NO: |  |  |  |  |  |  |  |  |  |  |  |  |
| P-501 CONCRETE SUMMARY |  |  |  |  |  |  |  |  |  |  |  |  |
| LOT 1 | CORE THICKNESS (INCHES) |  |  |  |  | FLEXUAL STRENGTH |  |  |  |  |  |  |
|  |  | LOT AVG | PWL | % PAY | 28 DAY | LOT AVG. | PWL | % PAY | TOTAL | LOT | UNIT | TOTAL |
|  |  |  |  |  | SET AVG. |  |  |  | % PAY | QUANTITY | PRICE | PAYMENT |
| Sublot 1 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 2 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 3 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 4 |  |  |  |  |  |  |  |  |  |  |  |  |
| LOT 2 | CORE THICKNESS (INCHES) |  |  |  |  | FLEXUAL STRENGTH |  |  |  |  |  |  |
|  |  | LOT AVG | PWL | % PAY | 28 DAY | LOT AVG. | PWL | % PAY | TOTAL | LOT | UNIT | TOTAL |
|  |  |  |  |  | SET AVG. |  |  |  | % PAY | QUANTITY | PRICE | PAYMENT |
| Sublot 1 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 2 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 3 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 4 |  |  |  |  |  |  |  |  |  |  |  |  |
| LOT 3 | CORE THICKNESS (INCHES) |  |  |  |  | FLEXUAL STRENGTH |  |  |  |  |  |  |
|  |  | LOT AVG | PWL | %PAY | 28 DAY | LOT AVG. | PWL | % PAY | TOTAL | LOT | UNIT | TOTAL |
|  |  |  |  |  | SET AVG. |  |  |  | % PAY | QUANTITY | PRICE | PAYMENT |
| Sublot 1 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 2 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 3 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 4 |  |  |  |  |  |  |  |  |  |  |  |  |
| LOT 4 | CORE THICKNESS (INCHES) |  |  |  |  | FLEXUAL STRENGTH |  |  |  |  |  |  |
|  |  | LOT AVG | PWL | % PAY | 28 DAY | LOT AVG. | PWL | % PAY | TOTAL | LOT | UNIT | TOTAL |
|  |  |  |  |  | SET AVG. |  |  |  | % PAY | QUANTITY | PRICE | PAYMENT |
| Sublot 1 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 2 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 3 |  |  |  |  |  |  |  |  |  |  |  |  |
| Sublot 4 |  |  |  |  |  |  |  |  |  |  |  |  |

Attachment 4:  Density Tests Summary, P-152, 154, 155, 208, &P-209

| AIRPORTS: |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| AIP PROJECT NO: |  |  |  |  |  |  |
| P-152, 154, 155, 208, & P-209 DENSITY TESTS SUMMARY |  |  |  |  |  |  |
| DATE | LOT/SAMPLE NUMBER | * MOISTURE | OPT | MINIMUM | ACTUAL | REMARKS |
|  |  |  |  | Density (%) |  |  |
|  |  | CONTENT (%) | MOISTURE (%) | SPECIFIED | Density (%) |  |
| *For expensive days only (PI > 12) |  |  |  |  |  |  |
| NOTE: Retests must be identified and cross - referenced to original failed test. |  |  |  |  |  |  |

Attachment 5:  Density Tests Summary, P-304

| AIRPORTS: |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AIP PROJECT NO: |  |  |  |  |  |  |  |  |  |  |  |
| P-304 DENSITY TESTS SUMMARY |  |  |  |  |  |  |  |  |  |  |  |
| DATE | NUMBER | DENSITY % |  |  |  | AVERAGE OF | % PAY | LOT | UNIT | TOTAL | REMARKS |
|  |  | sublot 1 | sublot 2 | sublot 3 | sublot 4 | DENSITY |  | QUANTITY | PRICE | PAYMENT |  |
| Attachment 6: Test Summary, P-401 |
| AIRPORT: CITY: STATE: AIP: Page____of____ |  |  |  |  |  |  |  |  |
|  |  | ACCEPTANCE TEST |  | CONTROL TEST |  |  |  |  |
| Unit Price |  | Marshall | MAT | Marshall |  |  |  |  |
| Mix $____/Ton |  | Air | Density | Unit wt | VMA | Stability | Flow | Joint |
| AC $____/____ |  | Voids (%) | (%) | (Pcf) | (%) | (lbs) | (.01 in) | Density (%) |
| Specification |  | ____ - ____ |  |  | ____Min | ____ Blows | ____ - ____ |  |
|  |  |  |  |  |  | ____ Min |  |  |
| DATE: | LOT |  |  |  |  |  |  |  |
| LOT: | AVG |  |  |  |  |  |  |  |
| LOCATION: | STD |  |  |  |  |  |  |  |
| LIFT: | DEV |  |  |  |  |  |  |  |
| % PAY: __________ | QU |  |  |  |  |  |  |  |
| TONS MIX: _______ | QL |  |  |  |  |  |  |  |
| TON AC: _________ |  |  |  |  |  |  |  |  |
| TOTAL PAY: $_____ | PWL |  |  |  |  |  |  |  |
| DATE: | LOT |  |  |  |  |  |  |  |
| LOT: | AVG |  |  |  |  |  |  |  |
| LOCATION: | STD |  |  |  |  |  |  |  |
| LIFT: | DEV |  |  |  |  |  |  |  |
| % PAY: __________ | QU |  |  |  |  |  |  |  |
| TONS MIX: _______ | QL |  |  |  |  |  |  |  |
| TON AC: _________ |  |  |  |  |  |  |  |  |
| TOTAL PAY: $_____ | PWL |  |  |  |  |  |  |  |
| DATE: | LOT |  |  |  |  |  |  |  |
| LOT: | AVG |  |  |  |  |  |  |  |
| LOCATION: | STD |  |  |  |  |  |  |  |
| LIFT: | DEV |  |  |  |  |  |  |  |
| % PAY: __________ | QU |  |  |  |  |  |  |  |
| TONS MIX: _______ | QL |  |  |  |  |  |  |  |
| TON AC: _________ |  |  |  |  |  |  |  |  |
| TOTAL PAY: $_____ | PWL |  |  |  |  |  |  |  |

Attachment 7:  Gradation Summary, P-154, 208, 209, 304, 402

| AIRPORT: |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| AIP PROJECT NO: |  |  |  |  |  |  |
| P-154, 208, 209, 304, 402 GRADATION SUMMARY |  |  |  |  |  |  |
| SIEVE | GRADATIONS |  |  |  | SPECIFIED | REMARKS |
| SIZE | SAMPLE #1 | SAMPLE #2 | SAMPLE #3 | SAMPLE #4 | GRADATION |  |
| *Note: Include % fractured face test for P-209 and P-402 |  |  |  |  |  |  |
| Retest must be identified and cross-referenced to original field test. |  |  |  |  |  |  |