| CABLE No. | . F5O-B00891 a,b,c,d |
| --- | --- |
| MFG. | 2/18/2004 |
| OPERATOR: | H.Higley, |
|  | D.Dietderich, R.Yamada |
| Rev. | 2/24/2004 |

CABLE LOG SHEET

LBNL-SUPERCON-AFRD

SUPERCONDUCTING MAGNET CABLES

BLD 52

Objective : Manufacture cable to FNAL Cos-(  modified specifications per. A. Zloben and Ryuji Yamada.

- STRAND INFORMATION -

| MANUFACTURER : | OXFORD |
| --- | --- |
| BILLET #: | 7054, 7060, 6813 |
| SPOOL #: | See strand map.F5O-B00891-892_stmp.xls |
| COMPOSITION : | Nb3Sn |
| STRAND Dia.. NOMINAL : | 0.700 | INSP. DIA..: | 0.7029 |
| Cu/SC RATIO NOMINAL : |  | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : |  | DIRECTION : | Right |
| SHARP BEND TEST : |  |
| LENGTH PER SPOOL : | 355m |

NOTES:

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | Prototype FNAL Cos-0 modified specifications per. A. Zloben and Ryuji Yamada. |
| --- | --- |
| No. of STRANDS: | 39 |
| PITCH DIRECTION: | Left | PITCH LENGTH: | 111mm |
| PLANETARY RATIO: | -0.57:1 (54t,13t) |
| ROLLER ID #: | P27 & 28 | WIDTH: | 14.299mm | ANGLE:: | (A=0.982) & (B--= 1.052) |
| MANDREL ID #: | 21 | WIDTH: | 13.62mm | THICKNESS:: | 0.47mm |
| LUBRICATION : | 4-BR vanishing lube+ @ 1to2 drop/pitch |
| STRAND TENSION: | 4.25 lb. | TURKS HEAD LOAD "SGM": | -140lbs. |
|  | Stage 1 | Stage 2 |
| Nom. THICKNESS: | 1.280 | 1.200 |
| Nom. WIDTH: | 14.36 | 14.36 |
| Nom. ANGLE: | 0.982 | 0.982 |

- FINISHED CABLE -

|  | Startup | Stage 1 | Restart | Stage 2 |
| --- | --- | --- | --- | --- |
|  | 891-A | 891-B | 891-C | 891-D |
| FINISHED LENGTH: | 5m | 8m | 5.5m | 79.7m |
| Avg. THICKNESS: | 1.2650 | 1.2794 | 1.2220 | 1.2044 |
| Avg. WIDTH: | 14.369 | 14.355 | 14.340 | 14.342 |
| Avg. ANGLE: | 0.895 | 0.996 | .966 | .947 |
| RESID. TWIST/Mtr.: | 180 under | 180 under | 100 under | 90 under |
| Photos : | 891-A photos | 891-B photos | none | 891-D photos |

NOTES:  Cabling went well.  The pinch point seemed a bit sensitive to crossovers at .050in. from pinch point.  Ran mandrel at 0.025in from pinch point.  Rolls were re-ground between 891-A & 891-B to increase keystone angle.  Cable 891-D run at 20 rpm.

| 02-17-2004 Cable RunFNL-5-O-B00891 Unit 0 09:55:35 |  |
| --- | --- |
| FNAL COS-0 39ST X 0.7MM X .982d CME #2 |  |  |
|  |  |  |  |  |  | Mid |  |
| Sample | POINT | METERS | kPa | ANGLE | WIDTH | THICK | Date |
| Gage | 1 | 0 | 17,089 | 0.017 | 13.9925 | 1.5024 | 2/17/2004 |
| Gage | 2 | 0 | 17,079 | 0.017 | 13.9924 | 1.5025 | 2/17/2004 |
| Gage | 3 | 0 | 17,073 | 0.016 | 13.9925 | 1.5024 | 2/17/2004 |
| Gage | 4 | 0 | 17,079 | 0.016 | 13.9924 | 1.5024 | 2/17/2004 |
| Gage | 5 | 0 | 17,111 | 0.016 | 13.9924 | 1.5024 | 2/17/2004 |
| Gage | 6 | 0 | 17,128 | 0.016 | 13.9928 | 1.5022 | 2/17/2004 |
| Gage | 7 | 0 | 17,128 | 0.016 | 13.9928 | 1.5024 | 2/17/2004 |
| Gage | 8 | 0 | 17,128 | 0.017 | 13.9926 | 1.5023 | 2/17/2004 |
| Gage | 9 | 0 | 17,128 | 0.016 | 13.9925 | 1.5024 | 2/17/2004 |
| Gage | 10 | 0 | 17,128 | 0.016 | 13.9927 | 1.5020 | 2/17/2004 |
|  |  | avg.= | 17,107 | 0.016 | 13.9926 | 1.5023 |  |
| 891-A LBL | 11 | 0 | 17,073 | 0.903 | 14.3711 | 1.2627 | 2/17/2004 |
| 891-A LBL | 12 | 0 | 17,073 | 0.905 | 14.3662 | 1.2612 | 2/17/2004 |
| 891-A LBL | 13 | 1 | 17,073 | 0.877 | 14.3923 | 1.2695 | 2/17/2004 |
| 891-A LBL | 14 | 2.33 | 17,073 | 0.899 | 14.3644 | 1.2656 | 2/17/2004 |
| 891-A LBL | 15 | 3.33 | 17,073 | 0.892 | 14.3641 | 1.2659 | 2/17/2004 |
| 891-A LBL | 16 | 4.33 | 17,073 | 0.894 | 14.3572 | 1.2649 | 2/17/2004 |
| 891-A SEM-LBL | 17 | 5 | 17,073 | 0.897 | 14.3662 | 1.2655 | 2/17/2004 |
| 891-A SEM-FNAL |  | 17,073 | 0.895 | 14.3688 | 1.2650 |  |
| Regrind roll angle & restart cable. |  |  |  |  |  |
| Gage | 18 | 5 | 17,062 | 0.017 | 13.9927 | 1.5021 | 2/18/2004 |
| Gage | 19 | 5 | 17,073 | 0.017 | 13.9928 | 1.5020 | 2/18/2004 |
| Gage | 20 | 5 | 17,073 | 0.018 | 13.9925 | 1.5022 | 2/18/2004 |
| Gage | 21 | 5 | 17,073 | 0.018 | 13.9924 | 1.5021 | 2/18/2004 |
| Gage | 22 | 5 | 17,073 | 0.018 | 13.9924 | 1.5023 | 2/18/2004 |
| Gage | 23 | 5 | 17,068 | 0.017 | 13.9925 | 1.5023 | 2/18/2004 |
| Gage | 24 | 5 | 17,073 | 0.017 | 13.9926 | 1.5023 | 2/18/2004 |
| Gage | 25 | 5 | 17,073 | 0.018 | 13.9929 | 1.5024 | 2/18/2004 |
|  |  | avg.= | 17,071 | 0.018 | 13.9926 | 1.5022 |  |
| Cable at nominal size (Stage 1 ) |  |  |  |  |  |
| 891-B -FNAL | 26 | 5.67 | 17,019 | 0.987 | 14.3658 | 1.2765 | 2/18/2004 |
| 891-B -FNAL | 27 | 6 | 16,997 | 0.998 | 14.3623 | 1.2791 | 2/18/2004 |
| 891-B -FNAL | 28 | 6.33 | 17,019 | 0.994 | 14.3546 | 1.2772 | 2/18/2004 |
| 891-B -FNAL | 29 | 6.67 | 17,019 | 1.006 | 14.3505 | 1.2785 | 2/18/2004 |
| 891-B -FNAL | 30 | 7.33 | 17,013 | 1.013 | 14.3531 | 1.2809 | 2/18/2004 |
| 891-B -FNAL | 31 | 8 | 17,019 | 1.003 | 14.3555 | 1.2813 | 2/18/2004 |
| 891-B -LBL 1.5M | 32 | 8 | 17,019 | 0.970 | 14.3411 | 1.2821 | 2/18/2004 |
|  |  |  | 17,015 | 0.996 | 14.3547 | 1.2794 |  |
| Ryugi Yamada/FNAL arrives at LBNL |  |  |  |  |
| Gage | 33 | 8 | 16,964 | 0.017 | 13.9922 | 1.5022 | 2/18/2004 |
| Gage | 34 | 8 | 16,964 | 0.017 | 13.9925 | 1.5023 | 2/18/2004 |
| Gage | 35 | 8 | 16,986 | 0.017 | 13.9925 | 1.5019 | 2/18/2004 |
| Gage | 36 | 8 | 16,964 | 0.017 | 13.9926 | 1.5021 | 2/18/2004 |
| Gage | 37 | 8 | 16,964 | 0.017 | 13.9926 | 1.5020 | 2/18/2004 |
|  |  | avg.= | 16,968 | 0.017 | 13.9925 | 1.5021 |  |
| New target mid thickness 1.200mm "Yamada / Zlobin" |  |  |  |
| Reduce thickness and measure. |  |  |  |  |  |
| 891-C FNAL | 38 | 17.33 | 16,959 | 0.967 | 14.3507 | 1.2228 | 2/18/2004 |
| 891-C FNAL | 39 | 17.67 | 16,959 | 0.979 | 14.3435 | 1.2217 | 2/18/2004 |
| 891-C FNAL | 40 | 17.67 | 16,964 | 0.964 | 14.3396 | 1.2225 | 2/18/2004 |
| 891-C FNAL | 41 | 18 | 16,964 | 0.959 | 14.3431 | 1.2224 | 2/18/2004 |
| 891-C FNAL | 42 | 19 | 16,964 | 0.962 | 14.3422 | 1.2222 | 2/18/2004 |
| 891-C FNAL | 43 | 19.67 | 16,964 | 0.957 | 14.3395 | 1.2229 | 2/18/2004 |
| 891-C FNAL | 44 | 20.67 | 16,964 | 0.971 | 14.3413 | 1.2226 | 2/18/2004 |
| 891-C FNAL | 45 | 21.33 | 16,964 | 0.957 | 14.3397 | 1.2223 | 2/18/2004 |
| 891-C FNAL | 46 | 22.33 | 16,964 | 0.968 | 14.3360 | 1.2206 | 2/18/2004 |
| 891-C FNAL | 47 | 22.67 | 16,964 | 0.967 | 14.3332 | 1.2212 | 2/18/2004 |
| 891-C FNAL | 48 | 23 | 16,964 | 0.972 | 14.3352 | 1.2211 | 2/18/2004 |
|  |  |  | 16,963 | 0.966 | 14.3404 | 1.2220 |  |
| 891-C still connected at hub of spool to 891-D |  |  |  |  |
| Reduce thickness |  |  |  |  |  |  |
| 891-D FNAL | 49 | 23.33 | 16,964 | 0.943 | 14.3332 | 1.2055 | 2/18/2004 |
| 891-D FNAL | 50 | 23.67 | 16,964 | 0.936 | 14.3334 | 1.2066 | 2/18/2004 |
| 891-D FNAL | 51 | 25 | 16,964 | 0.948 | 14.3367 | 1.2067 | 2/18/2004 |
| 891-D FNAL | 52 | 26 | 16,964 | 0.957 | 14.3356 | 1.2067 | 2/18/2004 |
| 891-D FNAL | 53 | 27 | 16,964 | 0.956 | 14.3374 | 1.2065 | 2/18/2004 |
| 891-D FNAL | 54 | 28 | 16,964 | 0.957 | 14.3342 | 1.2063 | 2/18/2004 |
| 891-D FNAL | 55 | 29 | 16,964 | 0.956 | 14.3355 | 1.2059 | 2/18/2004 |
| 891-D FNAL | 56 | 30 | 16,964 | 0.955 | 14.3353 | 1.2056 | 2/18/2004 |
| 891-D FNAL | 57 | 31 | 16,964 | 0.951 | 14.3339 | 1.2051 | 2/18/2004 |
| 891-D FNAL | 58 | 32 | 16,964 | 0.950 | 14.3381 | 1.2059 | 2/18/2004 |
| 891-D FNAL | 59 | 33 | 16,964 | 0.950 | 14.3323 | 1.2055 | 2/18/2004 |
| 891-D FNAL | 60 | 34 | 16,964 | 0.951 | 14.3338 | 1.2045 | 2/18/2004 |
| 891-D FNAL | 61 | 35 | 16,964 | 0.948 | 14.3363 | 1.2049 | 2/18/2004 |
| 891-D FNAL | 62 | 36 | 16,964 | 0.945 | 14.3322 | 1.2026 | 2/18/2004 |
| 891-D FNAL | 63 | 37 | 16,964 | 0.943 | 14.3316 | 1.2023 | 2/18/2004 |
| 891-D FNAL | 64 | 38 | 16,964 | 0.944 | 14.3332 | 1.2027 | 2/18/2004 |
| 891-D FNAL | 65 | 39 | 16,964 | 0.946 | 14.3327 | 1.2032 | 2/18/2004 |
| 891-D FNAL | 66 | 40 | 16,964 | 0.950 | 14.3394 | 1.2046 | 2/18/2004 |
| 891-D FNAL | 67 | 41 | 16,970 | 0.952 | 14.3396 | 1.2049 | 2/18/2004 |
| 891-D FNAL | 68 | 42 | 16,964 | 0.951 | 14.3402 | 1.2045 | 2/18/2004 |
| 891-D FNAL | 69 | 43 | 16,964 | 0.949 | 14.3427 | 1.2054 | 2/18/2004 |
| 891-D FNAL | 70 | 44 | 16,964 | 0.948 | 14.3387 | 1.2050 | 2/18/2004 |
| 891-D FNAL | 71 | 45 | 16,964 | 0.941 | 14.3423 | 1.2045 | 2/18/2004 |
| 891-D FNAL | 72 | 46 | 16,964 | 0.940 | 14.3378 | 1.2049 | 2/18/2004 |
| 891-D FNAL | 73 | 47 | 16,970 | 0.948 | 14.3385 | 1.2046 | 2/18/2004 |
| 891-D FNAL | 74 | 48 | 16,964 | 0.939 | 14.3430 | 1.2047 | 2/18/2004 |
| 891-D FNAL | 75 | 49 | 16,964 | 0.944 | 14.3425 | 1.2053 | 2/18/2004 |
| 891-D FNAL | 76 | 50 | 16,964 | 0.946 | 14.3430 | 1.2046 | 2/18/2004 |
| 891-D FNAL | 77 | 51 | 16,970 | 0.946 | 14.3432 | 1.2050 | 2/18/2004 |
| 891-D FNAL | 78 | 52 | 16,964 | 0.948 | 14.3430 | 1.2046 | 2/18/2004 |
| 891-D FNAL | 79 | 53 | 16,964 | 0.947 | 14.3449 | 1.2043 | 2/18/2004 |
| 891-D FNAL | 80 | 54 | 16,964 | 0.943 | 14.3445 | 1.2046 | 2/18/2004 |
| 891-D FNAL | 81 | 55 | 16,964 | 0.945 | 14.3439 | 1.2041 | 2/18/2004 |
| 891-D FNAL | 82 | 56 | 16,964 | 0.946 | 14.3449 | 1.2045 | 2/18/2004 |
| 891-D FNAL | 83 | 57 | 16,970 | 0.946 | 14.3431 | 1.2045 | 2/18/2004 |
| 891-D FNAL | 84 | 58 | 16,964 | 0.951 | 14.3417 | 1.2043 | 2/18/2004 |
| 891-D FNAL | 85 | 59 | 16,970 | 0.950 | 14.3465 | 1.2054 | 2/18/2004 |
| 891-D FNAL | 86 | 60 | 16,970 | 0.952 | 14.3401 | 1.2050 | 2/18/2004 |
| 891-D FNAL | 87 | 61 | 16,964 | 0.950 | 14.3458 | 1.2050 | 2/18/2004 |
| 891-D FNAL | 88 | 62 | 16,964 | 0.943 | 14.3448 | 1.2048 | 2/18/2004 |
| 891-D FNAL | 89 | 63 | 16,964 | 0.948 | 14.3437 | 1.2046 | 2/18/2004 |
| 891-D FNAL | 90 | 64 | 16,964 | 0.941 | 14.3475 | 1.2048 | 2/18/2004 |
| 891-D FNAL | 91 | 65 | 16,970 | 0.935 | 14.3404 | 1.2049 | 2/18/2004 |
| 891-D FNAL | 92 | 66 | 16,964 | 0.940 | 14.3434 | 1.2040 | 2/18/2004 |
| 891-D FNAL | 93 | 67 | 16,964 | 0.940 | 14.3457 | 1.2038 | 2/18/2004 |
| 891-D FNAL | 94 | 68 | 16,970 | 0.945 | 14.3440 | 1.2038 | 2/18/2004 |
| 891-D FNAL | 95 | 69 | 16,964 | 0.946 | 14.3459 | 1.2037 | 2/18/2004 |
| 891-D FNAL | 96 | 70 | 16,975 | 0.942 | 14.3443 | 1.2040 | 2/18/2004 |
| 891-D FNAL | 97 | 71 | 16,970 | 0.942 | 14.3421 | 1.2038 | 2/18/2004 |
| 891-D FNAL | 98 | 72 | 16,970 | 0.942 | 14.3466 | 1.2037 | 2/18/2004 |
| 891-D FNAL | 99 | 73 | 16,975 | 0.941 | 14.3444 | 1.2038 | 2/18/2004 |
| 891-D FNAL | 100 | 74 | 16,964 | 0.946 | 14.3442 | 1.2034 | 2/18/2004 |
| 891-D FNAL | 101 | 75 | 16,986 | 0.949 | 14.3461 | 1.2038 | 2/18/2004 |
| 891-D FNAL | 102 | 76 | 16,964 | 0.954 | 14.3425 | 1.2038 | 2/18/2004 |
| 891-D FNAL | 103 | 77 | 16,975 | 0.954 | 14.3450 | 1.2037 | 2/18/2004 |
| 891-D FNAL | 104 | 78 | 16,981 | 0.953 | 14.3454 | 1.2043 | 2/18/2004 |
| 891-D FNAL | 105 | 79 | 16,986 | 0.952 | 14.3421 | 1.2045 | 2/18/2004 |
| 891-D FNAL | 106 | 80 | 16,975 | 0.946 | 14.3456 | 1.2047 | 2/18/2004 |
| 891-D FNAL | 107 | 81 | 16,981 | 0.943 | 14.3446 | 1.2048 | 2/18/2004 |
| 891-D FNAL | 108 | 82 | 16,970 | 0.942 | 14.3439 | 1.2042 | 2/18/2004 |
| 891-D FNAL | 109 | 83 | 16,975 | 0.939 | 14.3461 | 1.2041 | 2/18/2004 |
| 891-D FNAL | 110 | 84 | 16,964 | 0.943 | 14.3436 | 1.2037 | 2/18/2004 |
| 891-D FNAL | 111 | 85 | 16,970 | 0.948 | 14.3466 | 1.2035 | 2/18/2004 |
| 891-D FNAL | 112 | 86 | 16,964 | 0.948 | 14.3451 | 1.2035 | 2/18/2004 |
| 891-D FNAL | 113 | 87 | 16,986 | 0.947 | 14.3444 | 1.2033 | 2/18/2004 |
| 891-D FNAL | 114 | 88 | 16,975 | 0.947 | 14.3468 | 1.2037 | 2/18/2004 |
| 891-D FNAL | 115 | 89 | 16,981 | 0.944 | 14.3433 | 1.2039 | 2/18/2004 |
| 891-D FNAL | 116 | 90 | 16,970 | 0.944 | 14.3462 | 1.2044 | 2/18/2004 |
| 891-D FNAL | 117 | 91 | 16,975 | 0.940 | 14.3464 | 1.2044 | 2/18/2004 |
| 891-D FNAL | 118 | 92 | 16,975 | 0.947 | 14.3437 | 1.2041 | 2/18/2004 |
| 891-D FNAL | 119 | 93 | 16,981 | 0.946 | 14.3452 | 1.2041 | 2/18/2004 |
| 891-D FNAL | 120 | 94 | 16,975 | 0.954 | 14.3444 | 1.2033 | 2/18/2004 |
| 891-D FNAL | 121 | 95 | 16,986 | 0.954 | 14.3434 | 1.2031 | 2/18/2004 |
| 891-D FNAL | 122 | 96 | 16,964 | 0.950 | 14.3469 | 1.2040 | 2/18/2004 |
| 891-D FNAL | 123 | 97 | 16,964 | 0.951 | 14.3417 | 1.2036 | 2/18/2004 |
| 891-D FNAL | 124 | 98 | 16,964 | 0.947 | 14.3449 | 1.2037 | 2/18/2004 |
| 891-D FNAL | 125 | 99 | 16,970 | 0.944 | 14.3455 | 1.2041 | 2/18/2004 |
| 891-D FNAL | 126 | 100 | 16,970 | 0.940 | 14.3422 | 1.2043 | 2/18/2004 |
| 891-D FNAL | 127 | 101 | 17,008 | 0.942 | 14.3469 | 1.2041 | 2/18/2004 |
| 891-D FNAL | 128 | 102 | 17,003 | 0.949 | 14.3507 | 1.2042 | 2/18/2004 |
| 891-D FNAL | 129 | 103 | 17,003 | 0.950 | 14.3482 | 1.2026 | 2/18/2004 |
| 891-D LBNL 1.9m |  | 79.67 | 16,970 | 0.947 | 14.3420 | 1.2044 |  |
| Gage | 130 | 104.33 | 17,019 | 0.019 | 13.9914 | 1.5019 | 2/18/2004 |
| Gage | 131 | 104.33 | 17,024 | 0.019 | 13.9927 | 1.5020 | 2/18/2004 |
| Gage | 132 | 104.33 | 17,051 | 0.019 | 13.9927 | 1.5020 | 2/18/2004 |
| Gage | 133 | 104.33 | 17,073 | 0.019 | 13.9928 | 1.5022 | 2/18/2004 |
| Gage | 134 | 104.33 | 17,068 | 0.019 | 13.9927 | 1.5019 | 2/18/2004 |
|  |  | avg.= | 17047 | 0.019 | 13.9925 | 1.5020 |  |