Project Number:   AW 2226

Contract Number:   TW-0681 Date:  May 5, 1995

SPECIAL SPECIFICATION

SECTION 07411

MANUFACTURED METAL ROOF PANELS

Page

PART 1- GENERAL

1.01	Description of Work	2

1.02	References	2

1.03	System Description	3

1.04	Submittals	3

1.05	Quality Assurance	3

1.06	Warranty	3

PART 2-  PRODUCTS

2.01	Materials	4

2.02	Roof System	4

2.03	Finishes	5

PART 3- EXECUTION

3.01	Examination	5

3.02	Installation	6

3.03	Cleaning and Protection	6

SPECIAL SPECIFICATION

SECTION 07411

MANUFACTURED METAL ROOF PANELS

PART 1 - GENERAL

1.01	DESCRIPTION OF WORK

A.	This Section includes a manufactured metal roofing system:

a.	Manufactured metal roof panels.

b.	Installation accessories.

B.	Related Sections:  Refer to the following sections for related work.

1.	Division 5, Sections “Structural Steel,” “Metal Decking” and “Cold-Formed Metal Framing”

2.	Division 7, Section “Manufactured Metal Wall Panels”

3.	Division 7, Section “Flashing and Sheet Metal” for sheet metal, closures, flashing and trim, sheet metal gutters and downspouts.

1.02	REFERENCES

A.	American Society for Testing and Materials (ASTM)

A792	Standard Specification for Steel Sheet, 55% Aluminum-Zinc Alloy-Coated by the Hot-Dip Process, General Requirements

D226	Standard Specification for Asphalt-Saturated Organic Felt Used in Roofing and Waterproofing

D4601	Standard Specification for Asphalt-Coated Glass Fiber Base Sheet Used in Roofing

B.	Underwriters Laboratories, Inc. (UL)

Roofing Materials and Systems Directory

580	Tests for Uplift Resistance of Roof Assemblies;  Underwriters Laboratories, Inc.

1.03	SYSTEM DESCRIPTION

A.	Environmental Requirements:  Provide for expansion and contraction of system components due to ambient temperature and solar heat gain.  Accommodate movement due to temperature change without buckling, undue stress on structural elements, reduction of performance, or other damaging effects.

Anticipated ambient temperature range:  Minus 5 to plus 140 degrees F (minus 21 to plus 60 degrees C).

B.	Wind Uplift:  Provide metal roof panel systems which have been tested in accordance with UL 580 and listed in the UL “Roofing Materials and Systems Directory” for the following rating:   Class 60 minimum.

1.04	SUBMITTALS

A.	Product Data:  Manufacturer’s written technical information, including performance data, details, and installation recommendations, which demonstrate that metal panel assembly components comply with Contract documents.

B.	Shop Drawings:  Drawings which show arrangement and orientation of panels, roof accessories as well as details of panel joints, corners, custom profiles, supporting devices, and closure trim and flashing.  Show panel system in relation to adjacent construction.

C.	Samples for Selection of Coated Finishes:  Coating manufacturer’s full range of color selection data.

D.	Provide certification that products used are asbestos-free and lead paint-free.

E.	Warranty:  Submit specimen copy of manufacturer’s warranty covering weathertightness and finish.

1.05	QUALITY ASSURANCE

A.	Manufacturer Qualifications:  A company with a minimum of 5 years successful experience in the design, fabrication, and installation of metal panel systems comparable in size and nature to those required for this project.

B.	Field Measurements:  Measure in-place construction on which panel system will be installed if possible, before fabrication of panels.  If not feasible, fabricate material to allow in-field trimming of panels to assure proper fit.

Coordinate field measurements and shop drawings with shop fabrication to minimize field adjustments, splicing, and mechanical joints.

1.06	WARRANTY

Provide manufacturer’s standard minimum 15 year warranty for roof weathertightness and standard 20 year warranty on finish.

PART 2 - PRODUCTS

2.01	MATERIALS

“Galvalume” Sheet:  ASTM A792;  Steel sheet, coated with zinc-aluminum alloy.

2.02	ROOF SYSTEM

A.	Manufacturer:  Products of the following manufacturers, provided they comply with requirements of the Contract documents and are compatible with adjacent materials, will be among those considered acceptable:

Architectural Panels, Inc.

Butler

Copper Sales, Inc.

Merchant & Evans, Inc.

Varco Pruden Roof Systems

B.	System Type:  Standing seam system consisting of roof panels with concealed attachment clips in panel;  clips to rigid substrate.

1.	Seam type:  Factory-formed, field-clinched.

2.	Fabricate panels from “Galvalume” sheet steel, minimum 24 gage (0.607 mm).

3.	Exterior Finish:  “Galvalume.”

4.	Interior (underside) Finish:  Mill finish.

5.	Panel Width (nominal coverage): 24 inches (610 mm)

6.	Panel Profile:  Manufacturer’s standard.

C.	Underlayment:  Unperforated asphalt-saturated felt;  ASTM D226, Type II or ASTM D4601, Type II.

D.	Concealed Panel Clips

1.	Fabricate from galvanized steel.

2.	Provide roof system manufacturer’s standard type clips to suit project requirements, including but to limited to the following:

a.	Live loads.

b.	Thermal movement; accommodate expansion and contraction without introducing stress into roof system.

c.	Slope of roof.

d.	Special conditions at transitions, penetrations, and terminations.

E.	Fasteners

1.	Threaded Fasteners:  Provide manufacturer’s standard corrosion-resistant fasteners of size and type required for intended application.

2.	Rivets:  Noncorrosive metal, compatible with metals to be fastened.

F.	Accessories

1.	Flexible Closures:  Closed-cell neoprene rubber, formed to fit panel profile with 5 to 10 percent compression when secured in place.

2.	Sheet Metal Closures, Flashing and Trim:  Fabricate from same type of sheet metal used for panel system, but with Fluoropolymer finish.

3.	Flexible Sheet Flashing:  Comply with requirements of Contract documents.

4.	Concealed Sealants and Gaskets:  Manufacturer’s standard.

5.	Exposed Joint Sealant:  Comply with requirements of Contract documents.

2.03	FINISHES

A.	Mill Finish:  All roof panels;  As-fabricated, welds cleaned and dressed, exposed welds ground smooth.  Remove oil, grease, dirt, and weld spatter from finished units.

B.	Flouropolymer Finish:  At all exposed sheet metal closures, flashings and trim.

1.	Pretreatment:  Etch and conversion coating, each followed by water rinse.

2.	Primer:  Modified epoxy primer, minimum 0.2 mils (0.00508 mm) thick;  bake to cure.

3.	Finish Coat:  70 percent “Kynar 500” or “Hylar 5000” resin finish coat, minimum 0.8 mils (0.02032 mm) thick;  bake to cure.

Color:  Selected from submittals from manufacturer’s standard colors.

4.	Protection films provide strippable plastic film.

PART 3 - EXECUTION

3.01	EXAMINATION

A.	Verify that substrate or structural system to receive work of this section is complete, properly sized, and is laid out correctly in plan and elevations.

B.	Correct unacceptable substrate installations before start of metal panel erection.

C.	Coordinate work with other adjacent elements of building envelope to ensure watertight construction.

3.02	INSTALLATION

A.	General:  Install manufactured metal panels in accordance with panel manufacturer’s recommended practices.

1.	Fasten panels to structure as necessary to comply with performance criteria, allowing for expansion and contraction due to temperature variations and building movement.

2.	Install gaskets, sealants, closures, and trim as the work progresses to ensure airtight and watertight performance of the completed installation.

B.	Roof System Installation

1.	Underlayment:  Install only when recommended by roof manufacturer to isolate dissimilar materials or to comply with design, code, or warranty criteria for the proposed assembly.

2.	Roof Panel Installation:  Install roof panels using concealed clips in panel joints.

Use of exposed fasteners is not permitted unless specifically approved by the Sandia Delegated Representative (SDR).

3.	Field Seaming:  Close seams using powered seaming tool of size and type recommended by panel fabricator.  Inspect and clean tool regularly to avoid damage to prefinished surfaces.

3.03	CLEANING AND PROTECTION

A.	Remove protective coverings from prefinished metal surfaces after each panel is installed.

B.	Touch up or refinish marred or abraded surfaces.  Replace damaged units and units which cannot be refinished to the architect’s satisfaction.

C.	Clean finished surfaces using techniques and materials recommended by panel manufacturer.  Protect cleaned surfaces until project completion.

END OF SECTION