96E01/04/08

S702-96E.doc

Use on projects as appropriate.

Section 702. - ASPHALT MATERIAL

702.01  Asphalt Binder.  Delete the Subsection and add the following:

702.01  Asphalt Binder.  Conform to AASHTO M 20, M 226, or M 320, Table 1.  Conform to Subsection 702.04.

In AASHTO M 320, Table 1 replace footnote g with the following:

g  If the creep stiffness is below 300MPa, the direct tension test is not required.  If the creep stiffness is between 300 and 600 MPa, the direct tension failure strain requirement shall be used in lieu of the creep stiffness requirement.  The m-value requirement must be satisfied in both cases.

When an Open Graded Friction Course is specified, use the following:

702.01  Asphalt Cement.  Add the following:

Asphalt cement for the open-graded asphalt friction course will be viscosity Grade AC-20 (P or R) conforming to Table 702-2 and subsection 702.04.  Add the rubber additive at the refinery.

Table 702-2

Open-Graded Friction Course Asphalt Cement

| Property | AASHTO Test No. | Minimum | Maximum |
| --- | --- | --- | --- |
| Tests on Original Material |
| Penetration, 77ºF, 100 g, 5 sec | T 49 | 50 | --- |
| Viscosity @ 140ºF, Poises | T 202 (1) | 1600 | 2400 |
| Viscosity @ 275ºF, cSt | T 201 | 325 | --- |
| Flash Point, ºF, COC | T 48 | 450 | --- |
| Ductility @ 39.2ºF (5 cm/min.) cm | T 51 (2) | 50 | --- |
| Synthetic Rubber, residual wt. |  | 2.0 % | --- |
| Toughness, inch-pounds | ASTM D 5801 | 110 | --- |
| Tenacity, inch-pounds | ASTM D 5801 | 75 | --- |
| Test on Residue |
| Viscosity @ 140ºF, Poises | T 202 (1) | --- | 8000 |
| Ductility @ 39.2ºF (5 cm/min.) cm | T 51 (2) | 25 | --- |

(1) Use an Asphalt Institute viscometer to determine viscosity @ 140ºF.  Heat the asphalt up to 325ºF prior to pouring if desired.

(2) Trimming the ductility specimen prior to testing is waived.

When a PBA grade asphalt binder is specified with Section 401, use the following:

702.01  Asphalt Cement.  Delete the text and substitute the following:

Conform to Table 702-3 and subsection 702.04.

Table 702-3

Performance Based Asphalt Binder

| Property | AASHTO Test No. | Performance Based Asphalt Grade |
| --- | --- | --- |
|  |  | PBA-1 | PBA-4 | PBA-6a | PBA-6b | PBA-7 |
| Tests On Original Asphalt Binder Material |
| Flash point, COC, min. (1) (°F) | T 48 | 450 |
| Absolute viscosity at 140°F, min. (Pa·s x 10-1) | T 202 | 800 | 2800 | 2000 (2) | 2000 (2) | 2000 (2) |
| Kinematic viscosity at 275°F, max. (m2/s x 10-6) | T 201 | --- | --- | 2000 | 2000 | 2000 |
| Solubility in Trichloroethylene, min. (%) | T 44 | 99.0 | 99.0 | Report (3) | Report (3) | Report (3) |
| Tests On Aged Residue Asphalt Binder Material (4) |
| Mass loss after RTFO, max. (%) | T 240 | Report (3) | Report (3) | 0.60 (5) | 0.60 (5) | 0.60 (5) |
| Penetration at 77°F (dmm) | T 49 | 25 | 20 | --- | --- | --- |
| Ductility at 77°F, 5cm.min., min. (cm) | T 51 | 75 | 50 | 60 | 60 | 75 |
| Absolute viscosity at 140°F (Pa·s x 10-1) | T 202 | 2500-5000 (6) | 14000 max. | 5000 min. (2) | 5000 min. (2) | 3000 min. (2) |
| Kinematic viscosity at 275°F, min. (m2/s x 10-6) | T 201 | 275 | 350 | 275 | 275 | 275 |
| Absolute viscosity ratio at 140°F RTFO vis/Orig vis , max. |  | 4.0 | 4.0 | 4.0 | 4.0 | 4.0 |
| Tests On Pressure Aging Vessel Residue Asphalt Binder Material (7) |
| PAV test temperature | R 28 | 90°C | 100°C | 100°C | 100°C | 110°C |
| Stiffness, 300.0 Mpa, max.And M-value, 0.30 min. at test temp | T 313 | -6°C | -6°C | -24°C | -30°C | -6°C |

(1) Actual results of the test shall be part of the certified copy of test results and when PBA-6a, 6b, or 7 is used an additional statement verifying an acceptable flash point shall be included with the Certificate of Compliance.

(2) The Absolute Viscosity at 140ºF of PBA-6a, 6b, and 7 will be determined a 1 sec-1 using ASTM Designation D 4957 with Asphalt Institute Vacuum Capillary Viscometers.  Sample preparation and viscometer charging temperature shall be 300 ± 10°F.

(3) Where “Report” is indicated, there is no requirement.  However the actual test result shall be part of the certified copy of test results, or shall be furnished with the Certificate of Compliance.

(4) “Aged Residue Asphalt Binder Material” means the asphaltic residue obtained using the Rolling Thin Film Oven Test (RTFO Test), AASHTO Test Method T 240.

(5) Actual results of the test shall be part of the certified copy of test results and when PBA-6a, 6b, or 7 is used an additional statement verifying an acceptable mass loss shall be included with the Certificate of Compliance.

(6) Where actual limits (2500-5000) are indicated, the actual test results shall be part of the certified copy of test results, or shall be furnished with the Certificated of Compliance.

(7) “Pressure Aging Vessel Residue Asphalt Binder Material” means the asphaltic residue obtained using the Accelerated Aging of Asphalt Binder Using a Pressure Aging Vessel Test (PAV Test), AASHTO Test Method R 28.

Use on all projects when a Prime coat is specified.

702.03  Emulsified Asphalt.  Add the following:

(e) Other emulsified asphalts.  Other emulsified asphalts not covered by items (a) through (d) will conform to the following:

(1) Saybolt furol viscosity at 122(F, AASHTO T 59	15 – 150 sec

(2) Settlement, AASHTO T 59	1% max.

(3) Residue by distillation, AASHTO T 59	65% min.

(4) Oil Distillate by volume, AASHTO T 59	25% max.

(5) Solubility in trichloroethylene, AASHTO T 44	97.5 % min.

Use on all projects with asphalt material.

702.04  Application Temperatures.  Delete Table 702-1, and substitute the following:

Table 702-1

Application Temperatures - Range ºF

| Type and Grade Of Asphalt Material | Temperature Ranges Minimum - Maximum |
| --- | --- |
|  | Spraying Temperatures | Mixing Temperatures(1) |
| Cub-back asphalt- MC-30 RC or MC-70 RC or MC-250 RC or MC-800 RC or MC-3000 | 85 - (2) 120 - (2) 165 - (2) 200 - (2) 230 - (2) | --- --- 135 - 175(3) 165 - 210(3) 180 – 240(3) |
| Emulsified asphalt- RS-1 RS-2 MS-1 MS-2, MS-2h HFMS-1, 2, 2h, 2s SS-1, 1h, CSS-1, 1h CRS-1 CRS-2 CMS-2, CMS-2h | 70 - 140 125 - 185 70 - 160 - 70 - 160 70 - 160(4) 125 - 185 140 - 185 100 - 160 | --- --- 70 - 160 70 - 160 50 - 160 70 - 160 --- --- 120 – 140 |
| Asphalt binder- All grades | 365 max. | 365 max. |

(1) Temperatures of mix immediately after discharge.

(2) The maximum temperature at which fogging or foaming does not occur.

(3) Temperature may be above flash point.  Take precautions to prevent fire or explosion.

(4) For fog seals and tack coats.

Include subsection 702.05(d) when dampproofing of masonary surfaces is specified.

702.05  Material for Dampproofing and Waterproofing Concrete and Masonry Surfaces.

(d) Mortar Delete the text and substitute the following:

Conform to Subsection 712.05(b).

Include subsection 702.08(c) when there is a pay item for 40105C Antistrip additive type 3.

702.08  Antistrip Additive.

(c) Type 3  Delete the text and substitute the following:

Furnish lime conforming to AASHTO M 303.

When a cold asphalt mix is specified, include the following.

702.10  Cold Asphalt Mix.  Delete the text and substitute the following:

Conform to ASTM D 4215.

Do not use an aggregate that strips.  For patching mixes, use an asphalt grade and mix that remains pliable and workable at 14ºF.

When waterproof deck membranes on bridges are required, include Section 559 and the following:

Add the following:

702.11  Granulated Rubber for Waterproofing.

Granulated rubber shall conform to the following:

(a) Free from fabric, wire, or other contaminating materials except that up to 4.0% of calcium carbonate may be included to prevent particles from sticking together.

(b) With one of the following gradations as the Contractor elects:

(1) When only ground, fully vulcanized tired rubber is used, at least 95% shall pass the No. 16 sieve and not more than 10% shall pass the No. 25 sieve.

(2) If powdered, reclaimed devulcanized rubber is used, approximately 40% shall be added to 60% ground fully vulcanized tire rubber and the total blend shall meet the following gradation:

| Sieve Size Passing | Percentage (by weight) |
| --- | --- |
| No. 8 | 100 |
| No. 30 | 60-80 |
| No. 50 | 15-40 |
| No. 100 | 0-15 |

(c) With a certification from the supplier for each shipment of ground rubber that the material was tested and that it meets the specified material requirements, calcium carbonate content and gradation.