In Situ Biological Treatment of Hexavalent Chromium at the Selma Pressure Treating Superfund Site.

Daniel P. Leigh, David Cacciatore, Larry Hudson, (Shaw E&I, Concord, CA)

Tarek Ladaa (Shaw Environmental, Knoxville, TN)

Charnjit Bhullar (USEPA Region IX, San Francisco, CA.)

# Waleed Shaheen (US Army Corp of Engineers, Omaha, NE )

Soil and groundwater at many sites, including wood pressure treating facilities, have been affected by discharges of hexavalent chromium (Cr6+). At many Cr6+ contamination sites, plume migration is controlled by pump and treat (P&T) systems. Although potentially effective for plume control, P&T systems are generally ineffective as a stand-alone technology for complete site remediation. Therefore, new treatment techniques are being developed for remediation of Cr6+. An innovative technique for treatment of Cr6+ is being evaluated at the Selma Pressure Treating Superfund Site (Selma) located in Selma, California.

Soil and groundwater at Selma have been affected by historical discharges of Cr6+. A pilot test was conducted in 2004 and 2005 in an approximately 25-foot thick treatment zone in a 40,000 square foot portion of the unconfined aquifer. Cr6+ has been detected in the groundwater in this area at concentrations in excess 80,000 µg/L. Groundwater at the site is presently aerobic and sulfate concentration are in the range of 100 mg/L.

Bench tests were conducted to evaluate potential substrates for degradation of the Cr6+. The bench tests demonstrated each substrate was effective at degrading the Cr6+. During the tests Cr6+ was converted to Cr3+ prior to nitrate reduction, indicating that establishment of highly reducing conditions are not required for degradation of the contaminant. Arsenic was not mobilized during the bench tests. In addition, conversion of Cr3+ back to Cr6+ upon return to oxidizing conditions did not occur.

Previous treatment of groundwater conducted by high pressure injection required the application of excessive amounts of substrate to assure adequate distribution. The excessive amount of substrate resulted in the establishment of substantially more reducing conditions than necessary for the reduction of the Cr6+. These conditions resulted in the mobilization of manganese, iron and the production of methane.

In order to more adequately control the distribution of substrate, minimize establishment of excessively reducing conditions and to provide a mechanism for distribution of substrate into deeper portions of the aquifer not reachable by direct push technologies a groundwater recirculation system was designed, installed and operated. The recirculation system distributed substrate throughout the treatment area by extraction of groundwater from radially arranged extraction wells and injection of water into centrally located injection wells. Substrate was delivered to the recirculation system by regularly timed pulsed injections. Prior to implementation of the full-scale system field tests were conducted to determine the optimal amount of substrate required for the reduction of Cr6+. During full-scale system operation, the amount of substrate was controlled to provide only sufficient substrate to reduce the Cr6+ and thereby minimize the establishment of excessively reducing conditions.

In Situ Biological Treatment of Hexavalent Chromium at the Selma Pressure Treating Superfund Site.

Corresponding Author

Daniel Leigh P.G., R.G., C.HG. Shaw Environmental & Infrastructure, Inc. 4005 Port Chicago Highway Concord, CA 94520 Telephone925.288.2193 E-mail: Daniel.Leigh@shawgrp.com Fax: 925.288.0888

Co-Authors

Larry Hudson Shaw Environmental & Infrastructure, Inc. Telephone: 925.288.2193 4005 Port Chicago Highway E-mail: Larry.Hudson@shawgrp.com Concord, CA 94520 Fax: 925.288.0888

David Cacciatore Shaw Environmental & Infrastructure, Inc. 925.288.2037 4005 Port Chicago Highway E-mail:cleet.carlton@shawgrp.com Concord, CA 94520 Fax: 925.288.0888

Tarek Ladaa Shaw Environmental & Infrastructure, Inc. (865)690-3211 312 Directors Drive E-mail: tarek.ladaa@shawgrp.com Knoxville, TN Fax: (865) 690-3626

Charnjit Bhullar US Environmental Protection Agency Region 9 (SFD 7-1) Telephone: 415.972.3960 75 Hawthorne St. E-mail: Bhullar.charnjit@epamail.epa.gov San Francisco, CA 94105 Fax: 415.947.3526

Waleed Shaheen P.E. U.S. Army Corps of Engineers Telephone: (402)293-2517 P.O.Box 13287 E-mail: waleed.w.shaheen@nwo02.usace.army.mil Offutt AFB, NE 68113 Fax: (402)291-8177