96M03/29/06

S305-96M.doc

When aggregate-topsoil course is required, include the following:

Section 305. - AGGREGATE-TOPSOIL COURSE

305.04  Mixing, Placing, and Compacting.  Delete the third paragraph and substitute the following:

Uniformly compact the mixture so that it does not exhibit heaving, pumping, rutting, or shearing.  After compaction, dry seed the surface again at a rate of 85 kilograms per hectare.

305.05 Acceptance.  Delete the second paragraph and substitute the following:

Construction of aggregate-topsoil course will be evaluated under Subsection 106.02.

Table 305-1 Sampling and Testing.  Delete Table 305-1 and substitute following:

Table 305-1

Sampling and Testing

| Material or Product | Property or Characteristic | Test Methods or Specifications | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Aggregate for aggregate-topsoil | Gradation | AASHTO T 27 and AASHTO T 11 | 1 for each 1500 t | Source of material or stockpile |